Optimization of Ni-MOF Electrodes: Influence of Ni to Organic Linker Ratio and investigation of the process underlying superior capacitance

Tanya Dagar1, Rajkamal Arya2, M.N Singh3, A. K. Sinha2*

1Department of Chemistry, School of Advanced Engineering, UPES, Dehradun, Uttarakhand-248007, India

2Department of Physics, School of Advanced Engineering, UPES, Dehradun, Uttarakhand-248007, India

3Synchrotron Utilization Division, Raja Ramanna Center for Advanced Technology, Indore, Madhya Pradesh 452013, India

Corresponding author: anilksinha11@gmail.com

Figure S1: XRD plot of S-1 and S-3 with varying Ni: Organic linker ration

Figure S1: XRD plot of S-1 and S-3 with varying Ni: Organic linker ration

Figure S2: FTIR spectra of samples S-1 and S-3 with Ni-Organic linker ratios samples

Figure S2: FTIR spectra of samples S-1 and S-3 with Ni-Organic linker ratios samples

Figure S3: (a-c) CV of S-1, S-2 and S-3samples, (d) Log-Log plot of Scan rate vs peak current, (e) specific capacitance v/s scan rate

(e)

(e)

(d)

(d)

(c)

(c)

(b))

(b))

(a)

(a)

Table S1: Specific capacitance of Ni-MOF(Ni-Ratio) samples at various scan rates.

| Scan rate (mV/s) | Specific Capacitance (F/g) S-2 (0.9g) | Specific Capacitance (F/g) S-1(0.8g) | Specific Capacitance (F/g) S-3(1g) |
| --- | --- | --- | --- |
| 1 | 2054 | 1901 | 438 |
| 2 | 1704 | 1689 | 324 |
| 5 | 990 | 1807 | 327 |
| 10 | 800 | 1089 | 248 |
| 20 | 634 | 776 | 176 |
| 30 | 533 | 637 | 141 |
| 40 | 465 | 553 | 119 |
| 60 | 371 | 445 | 91 |
| 80 | 311 | 381 | 77 |
| 100 | 267 | 340 | 67 |

Figure S4: Galvanostatic charge and discharge (GCD) Profile (a-c) S-1, S-2 and S-3 at various current densities respectively (d) plot of specific capacitance v/s current density of all samples

Figure S4: Galvanostatic charge and discharge (GCD) Profile (a-c) S-1, S-2 and S-3 at various current densities respectively (d) plot of specific capacitance v/s current density of all samples

(d)

(d)

(c)

(c)

(a)

(a)

(b)

(b)

Table S2: GCD data of S-1,2 and 3 samples at Various current densities

| Current density (I) (A/g) | Cs (F/g) S-2 | Cs (F/g) S-1 | Cs (F/g) S-3 |
| --- | --- | --- | --- |
| 0.5 | 924 | 1186 | - |
| 1 | 735 | 838 | 96 |
| 2 | 630 | 632 | 24 |
| 3 | - | - | 16 |
| 5 | 513 | 380 | 10 |
| 10 | 500 | 240 | - |

Figure S5: Nyquist plots of all three samples. (Inset: Fitted Equivalent Electrical circuit diagram

Figure S5: Nyquist plots of all three samples. (Inset: Fitted Equivalent Electrical circuit diagram

Table S3: EIS Fitting Parameters of Ni-MOF based all samples with various Ni ratios:

| Samples | Ni amount (g) | Rs (Ω) | Rct (Ω) | CPE - R(Ω) | Warburg (Wo) (Ω) |
| --- | --- | --- | --- | --- | --- |
| S-2 | 0.9 | 0.36 | 0.52 | T- 0.00962 P- 0.24 | R- 3.0 T- 0.0331 P- 0.52 |
| S-1 | 0.8 | 0.37 | 0.58 | T- 0.0082 P- 0.3529 | R-12.5 T- 4.22 P- 0.45 |
| S-3 | 1.0 | 1.3 | 26.35 | T- 20.18 P- 0.021 | R- 44.7 T- 6.423 P- 0.368 |