A Ultrasonic Accelerated Three-Component Condensation by KCC-1 with a Fibrous: a High mechanical stability Silica Nanospheres as a good catalysis for ultrasonic irradiation

Hourieh Sadat Oboudatian, Javad Safaei Ghomi*

Department of Organic Chemistry, Faculty of Chemistry, University of Kashan, Kashan, 51167, I. R. Iran

*Corresponding Author Tel.: +98 31 55912385; fax: +98 31 55552935; *E-mail: safaei@kashanu.ac.ir

Table of Content

| S.No | Content | Page Numbers |
| --- | --- | --- |
| 1 | Characterization data | S2-S8 |
| 2 | References | S9 |
| 3 | Spectral data of the new compounds | S10-21 |

Characterization data

Physical and spectroscopic data of all products

2-(4-nitrobenzylidene)malononitrile (Ι)

96%, yellow solid, 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 8.11-8.13 (d, J = 8.8 Hz, 2H, Haromatic), 8.42-8.44 (d, J =8.8 Hz, 2H, Haromatic), 8.71 (s, 1H, Hvinyl).

3,9-diamino-1,7-diphenyl-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4a)

89%, yellow solid, m.p. = 295-300 °C, IR (KBr) ν (cm-1): 3416 (NH2), 3284 (NH2), 3183, 3027, 2193(CN), 1648 (NH2 bending), 1597, 1496, 1453, 1386, 1281, 1186, 1080 (C-O), 740, 700; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 4.89 (s, 2H, CH), 7.15 (br.s, 4H, NH2), 7.20-7.33 (m, 12H, Haromatic) 7.86-7.89 (dd, J =8 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 40.31, 56.20, 116.79, 118.97, 119.04, 120.32, 122.47, 126.97, 127.07, 127.58, 127.62, 128.72, 142.94, 145.50, 159.99. Anal. calcd for C30H20N4O2, % C, 76.91; H, 4.30; N, 11.96; Found, %: C, 76.59; H, 4.28; N, 11.98.

3,9-diamino-1,7-bis(4-chlorophenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4b)

96%, yellow solid, m.p = 310-320 °C (decomp.), IR (KBr) ν (cm-1): 3463 (NH2), 3325 (NH2), 3193,  2196(CN), 1662 (NH2 bending), 1596, 1490, 1386, 1280, 1186, 1083 (C-O), 888, 799, 755; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 4.95 (s, 2H, CH), 7.20 (br.s, 4H, NH2), 7.23-7.27 (m, 6H, Haromatic), 7.35-7.39 (m, 4H, Haromatic), 7.86-7.88 (d, J = 8.8 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 38.37, 59.00, 115.36, 117.82, 120.66, 121.49, 124.92, 126.96, 127.17, 129.92, 132.07, 139.71, 143.64, 145.26, 160.34. Anal. calcd for C30H18Cl2N4O2, % C, 67.05; H, 3.38; N, 10.43; Found, %: C, 67.00; H, 3.34; N, 9.89.

3,9-diamino-1,7-bis(2,4-dichlorophenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4c)

94%, yellow solid, m.p. =320-325 °C (decomp.), IR (KBr) ν (cm-1): 3462 (NH2), 3325 (NH2), 3190,  2204(CN), 1670 (NH2 bending), 1596, 1489, 1390, 1283, 1180, 1083 (C-O), 867, 793, 758; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 5.40 (s, 2H, CHbenzyl), 7.09-7.12 (d, J =8.8 Hz, 2H, Haromatic), 7.25-7.29 (m, 6H, Haromatic and NH2), 7.37-7.41 (m, 2H, Haromatic), 7.63 (s, 2H, Haromatic), 7.86-7.88 (dd, J =10.8 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 35.57, 57.24, 116.06, 119.96, 121.76, 123.89, 125.92, 127.96, 129.67, 132.62, 133.47, 138.91, 141.00, 143.66, 159.84. Anal. calcd for C30H16Cl4N4O2, % C, 59.43; H, 2.66; N, 9.24; Found, %: C, 59.13; H, 2.57; N, 9.15.

3,9-diamino-1,7-bis(3-chlorophenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4d):

92%, Yellow solid, m.p = 310-315 °C (decomp.), IR (KBr) ν (cm-1): 3439 (NH2), 3327 (NH2), 3198,  2195(CN), 1649 (NH2 bending), 1595, 1474, 1385, 1280, 1187, 1080 (C-O), 893, 753; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 4.97 (s, 2H, CHbenzyl), 7.17-7.35 (m, 10H, Haromatic), 7.24 (br.s, 4H, NH2), 7.88-7.90 (dd, J =8.4 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 37.77, 54.34, 117.06, 119.82, 122.56, 123.69, 126.42, 128.16, 129.27, 132.62, 133.07, 140.91, 141.00, 143.26, 160.14. Anal. calcd for C30H18Cl2N4O2, % C, 67.05; H, 3.38; N, 10.43; Found, %: C, 66.13; H, 2.97; N, 10.45.

3,9-diamino-1,7-bis(4-bromophenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4e)

93%, Yellow solid, m.p =300-310 °C (decomp.), IR (KBr) ν (cm-1): 3460 (NH2), 3325 (NH2), 3194,  2195(CN), 1660 (NH2 bending), 1595, 1486, 1386, 1281, 1186, 1078 (C-O), 888, 795; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 4.93 (s, 2H, CHbenzyl), 7.17-7.21 (m, 6H, Haromatic), 7.22 (br.s, 4H, NH2), 7.49-7.52 (m, 4H, Haromatic), 7.86-7.88 (dd, J =8.4 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 40.10, 55.65, 116.90, 118.44, 118.50, 120.11, 120.18, 122.53, 127.02, 129.91, 129.94, 131.63, 142.95, 144.87, 159.95. Anal. calcd for C30H18Br2N4O2, % C, 57.53; H, 2.90; N, 8.95; Found, %: C, 57.13; H, 2.67; N, 9.00.

3,9-diamino-1,7-bis(3-hydroxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4f)

90%, Yellow solid, m.p. >300 °C (decomp.), IR (KBr) ν (cm-1): 3444 (NH2), 3301 (NH2,OH), 2192(CN), 1652 (NH2 bending), 1596, 1455, 1386, 1280, 1246, 1187, 1081 (C-O), 886, 761; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 4.78 (s, 2H, CHbenzyl), 6.67-6.69 (m, 4H, Haromatic), 7.07-7.10 (m, 4H, Haromatic), 7.13 (br.s, 4H, NH2), 7.22-7.24 (m, 2H, Haromatic), 7.86-7.88 (dd, J=8.4 Hz, 2H, Haromatic), 9.35 (s, 2H, OH). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 45.63, 55.15, 115.55, 116.42, 119.32, 120.62, 122.25, 126.54, 127.91, 129.17, 131.38, 142.97, 146.44, 154.46, 160.57. Anal. calcd for C30H20N4O4, % C, 71.99; H, 4.03; N, 11.19; Found, %: C, 70.86; H, 3.98; N, 10.85.

3,9-diamino-1,7-bis(4-hydroxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4g)

87%, Yellow solid, m.p. >300 °C (decomp.), IR (KBr) ν (cm-1): 3422 (NH2), 3323 (NH2,OH), 2923, 2180(CN), 1655 (NH2 bending), 1595, 1511, 1389, 1255, 1184, 1085 (C-O), 759; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 4.75 (s, 2H, CHbenzyl), 6.67-6.69 (d, J = 8 Hz, 4H, Haromatic), 7.00-7.02 (d, J = 8 Hz, 4H, Haromatic), 7.06 (br.s, 4H, NH2), 7.17-7.20 (d, J = 8.8 Hz, 2H, Haromatic), 7.83-7.85 (d, J =8.4 Hz, 2H, Haromatic), 9.34 (s, 2H, OH). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 40.46, 55.04, 109.29, 111.23, 116.72, 118.52, 120.21, 124.06, 124.30, 127.45, 128.99, 142.85, 146.44, 153.29, 160.35. Anal. calcd for C30H20N4O4, % C, 71.99; H, 4.03; N, 11.19; Found, %: C, 71.26; H, 3.97; N, 11.37.

3,9-diamino-1,7-bis(2-hydroxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4h)

85%, Yellow solid, m.p. >300 °C (decomp.), IR (KBr) ν (cm-1): 3467 (NH2), 3332 (NH2 ,OH), 3196,  2192(CN), 1650 (NH2 bending), 1595, 1461, 1383, 1280, 1187, 1080 (C-O), 889, 799; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 5.11 (s, 2H, CHbenzyl), 6.91-6.93 (d, J=7.2 Hz, 2H, Haromatic), 6.98-7.01 (d, J=8.8 Hz, 2H, Haromatic), 7.27 (s, 4H, NH2), 7.39-7.43 (dd, J=8 Hz, 2H, Haromatic), 7.66-7.68 (d, J=8.4 Hz, 2H, Haromatic), 7.77-7.80 (d, J=8.8 Hz, 2H, Haromatic), 8.18-8.20 (d, J=8.4 Hz, 2H, Haromatic), 10.30 (s, 2H, OH). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 40.41, 56.23, 111.97, 118.19, 119.77, 120.63, 124.18, 124.63, 127.18, 138.25, 142.44, 147.75, 148.69, 153.24, 160.07. Anal. calcd for C30H20N4O4, % C, 71.99; H, 4.03; N, 11.19; Found, %: C, 71.96; H, 4.43; N, 11.54.

3,9-diamino-1,7-bis(4-isopropylphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4i)

82%, Yellow solid, m.p = 315-320 °C (decomp.), IR (KBr) ν (cm-1): 3492 (NH2), 3379 (NH2), 2198(CN), 1651 (NH2 bending), 1596, 1455, 1386, 1272, 1232, 1187, 1086 (C-O), 755; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 1.148 (s, 6H, CH3), 1.161 (s, 6H, CH3), 2.82 (m, 2H, CH)  4.84 (s, 2H, CHbenzyl), 7.12 (br.s, 4H, NH2), 7.13-7.27 (m, 10H, Haromatic), 7.85-7.88 (dd, J = 8.4 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 23.82, 33.00, 40.37, 56.28, 116.73, 119.13, 119.21, 120.45, 122.43, 126.63, 127.12, 127.38, 127.44, 142.93, 143.04, 146.96, 160.02. Anal. calcd for C36H32N4O2, % C, 78.24; H, 5.84; N, 10.14; Found, %: C, 77.86; H, 5.53; N, 10.44.

3,9-diamino-1,7-bis(4-methylphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4j)

85%, Yellow solid, m.p =310-320 °C (decomp.), IR (KBr) ν (cm-1): 3454 (NH2), 3325 (NH2), 3202, 2922, 2196(CN), 1659 (NH2 bending), 1596, 1500, 1388, 1282, 1238, 1187, 1084 (C-O), 854, 763; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 2.07 (s, 6H, CH3), 5.40 (s, 2H, CHbenzyl), 7.09-7.13 (m, 2H, Haromatic), 7.22-7.29 (m, 8H, Haromatic  and NH2), 7.37-7.40 (m, 2H, Haromatic), 7.61-7.63 (dd, J=8 Hz, 2H, Haromatic), 7.86-7.88 (dd, J = 8.8 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 39.17, 40.02, 55.28, 117.15, 118.08, 120.04, 122.08, 122.22, 122.66, 127.03, 130.53, 134.62, 143.08, 147.55, 147.95, 160.20. Anal. calcd for C32H24N4O2, % C, 77.40; H 4.87; N, 11.28.  Found, %: C, 75.86; H, 4.03; N, 11.14.

3,9-diamino-1,7-bis(3-nitrophenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4k)

87%, Yellow solid, m.p >300 °C (decomp.), IR (KBr) ν (cm-1): 3439 (NH2), 3327 (NH2), 3198,  2195(CN), 1649 (NH2 bending), 1595, 1474, 1385, 1280, 1187, 1080 (C-O), 893, 753; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 5.20 (s, 2H, CHbenzyl), 7.32 (m, 8H, Haromatic and NH2), 7.62-7.71 (m, 4H, Haromatic), 7.90-7.92 (m, 2H, Haromatic), 8.12 (br.s, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 39.43, 57.26, 116.71, 120.61, 124.62, 124.95, 125.21, 125.67, 127.52, 129.53, 137.61, 143.19, 146.57, 147.55, 160.10. Anal. calcd for C30H18N6O6, % C, 64.52; H, 3.25; N, 15.05.  Found, %: C, 62.95; H, 2.85; N, 14.50.

3,9-diamino-1,7-bis(4-nitrophenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8 dicarbonitrile (4l)

94%, Yellow solid, m.p. >300  °C (decomp.), IR (KBr) ν (cm-1): 3441 (NH2), 3336 (NH2), 3196, 2190(CN), 1655 (NH2 bending), 1597, 1527, 1387, 1350, 1281, 1187, 1082 (C-O), 800, 728; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 5.21 (s, 2H, CHbenzyl), 7.28-7.30 (m, 4H, Haromatic), 7.34 (br.s, 4H, NH2), 7.60-7.73 (m, 6H, Haromatic), 7.90-7.92 (d, J =8 Hz, 2H, Haromatic), 8.12 (br.s, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 40.03, 55.26, 117.16, 118.11, 120.02, 122.05, 122.21, 122.67, 127.02, 130.53, 134.61, 143.09, 147.57, 147.95, 160.20. Anal. calcd for C30H18N6O6, % C, 64.52; H, 3.25; N, 15.05.  Found, %: C, 63.45; H, 3.05; N, 15.45.

3,9-diamino-1,7-bis(4-methoxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4m)

87%, Yellow solid, m.p =300-305 °C (decomp.), IR (KBr) ν (cm-1): 3456 (NH2), 3330 (NH2), 3191,  2195(CN), 1659 (NH2 bending), 1596, 1388, 1282, 1187, 1084 (C-O), 817; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 3.70 (s, 6H, CH3O), 4.83 (s, 2H, CHbenzyl), 6.85-6.87 (d, J = 8.4, 4H, Haromatic), 7.09 (br.s, 4H, NH2), 7.12-7.15 (d, J = 8.4, 4H, Haromatic), 7.18-7.20 (d, J =8 Hz, 2H, Haromatic), 7.84-7.86 (d, J=8.8 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 38.95, 55.73, 60.27, 112.53, 113.95, 117.66, 120.82, 121.89, 122.46, 126.78, 127.80, 129.33, 143.05, 146.09, 158.43, 160.26. Anal. calcd for C32H24N4O4, % C, 72.72; H, 4.58; N, 10.60.  Found, %: C, 72.68; H, 4.51; N, 10.62.

3,9-diamino-1,7-bis(2,3-dimethoxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4n)

83%, Yellow solid, m.p >300 °C (decomp.), IR (KBr) ν (cm-1): 3430 (NH2), 3315 (NH2), 2195 (CN), 1654 (NH2 bending), 1599, 1477, 1386, 1284, 1077 (C-O), 766; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 3.55 (s, 6H, CH3O), 3.73 (s, 6H, CH3O), 5.06 (s, 2H, CHbenzyl), 6.62-6.64 (d, J=8 Hz, 2H, Haromatic), 6.87-6.89 (d, J=8 Hz, 2H, Haromatic), 6.94-6.98 (dd, J=8, 2H, Haromatic), 7.07 (br.s, 4H, NH2), 7.11-7.13 (d, J=8.4 Hz, 2H, Haromatic), 7.81-7.83 (d, J=8.4 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 35.55, 55.53, 60.19, 60.27, 111.63, 116.55, 118.76, 120.52, 121.09, 122.36, 124.18, 126.70, 138.33, 143.05, 146.09, 146.21, 152.43, 160.16. Anal. calcd for C34H28N4O6, % C, 69.38; H, 4.79; N, 9.52.  Found, %: C, 67.45; H, 3.95; N, 9.61.

3,9-diamino-1,7-bis(3,4-dimethoxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4o)

85%, Yellow solid, m.p >300 °C (decomp.), IR (KBr) ν (cm-1): 3447 (NH2), 3385 (NH2), 3.202, 2189(CN), 1660 (NH2 bending), 1601, 1512, 1389, 1270, 1195, 1140, 1081 (C-O), 1020, 802, 766; 1H NMR (DMSO-d6, 400 MHz) δ (ppm): 3.68 (s, 6H, CH3O), 3.69 (s, 6H, CH3O), 4.80 (s, 2H, CHbenzyl), 6.70-6.72 (d, J=8, 2H, Haromatic), 7.01-7.06 (m, 6H, Haromatic and NH2), 7.38-7.40 (dd, 2H, Haromatic), 7.63-7.65 (d, J = 8 Hz, 2H, Haromatic), 7.74-7.77 (d, J = 8.4 Hz, 2H, Haromatic). 13C NMR (DMSO-d6, 400 MHz) δ (ppm): 37.55, 55.83, 60.19, 61.27, 116.63, 117.75, 119.66, 119.92, 120.96, 122.76, 125.18, 138.73, 143.55, 146.89, 147.21, 156.43, 160.16. Anal. calcd for C34H28N4O6, % C, 69.38; H, 4.79; N, 9.52.  Found, %: C, 68.85; H, 4.15; N, 9.50.

References

- A.M. Shestopalov, Yu.M. Emelianova, V.N. Nesterov, One_step synthesis of substituted 2-amino-4H-chromenes and 2-amino-4H-benzo[f]chromenes. Molecular and crystal structure of 2-amino-3-cyano-6-hydroxy-4-phenyl-4H-benzo[f]chromene. Russ. Chem. Bull. 51 (2002) 2238-2243. https://doi.org/10.1023/A:1022135402451

- M. Hosseini-sarvari, S. Shafiee-haghighi, Multi-component synthesis of 2-amino-4H-chromenes catalysed by nano ZnO in water, Collect. Czech. Chem. Commun. 76 (2011) 1285–1298. https://doi.org/10.1135/cccc2011050.

- X. Wang, D. Shi, H. Yu, G. Wang, S. Tu, Synthesis of 2-Aminochromene Derivatives Catalyzed by KF/Al2O3, Synth. Commun. 34 (2004) 509–514. https://doi.org/10.1081/SCC-120027291.

Spectral data of the new compounds

3,9-diamino-1,7-bis(3-chlorophenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4d):

3,9-diamino-1,7-bis(3-hydroxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4f)

3,9-diamino-1,7-bis(4-hydroxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4g)

3,9-diamino-1,7-bis(2-hydroxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4h)

3,9-diamino-1,7-bis(4-isopropylphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4i)

3,9-diamino-1,7-bis(4-methylphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4j)

3,9-diamino-1,7-bis(4-nitrophenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8 dicarbonitrile (4l)

3,9-diamino-1,7-bis(2,3-dimethoxyphenyl)-1,7-dihydrochromeno[8,7-h]chromene-2,8-dicarbonitrile (4n)