Supporting Information

Valorization of phosphate–potassium ore tailings via microwave-assisted calcination: a novel multifunctional soil conditioner for fertility enhancement and contamination remediation

Shiwei Leia, Shida Lia, Chuan Guanb, Xiaojun Yangb, Baoxin Lic, Hexi Tangb, Changjun Chenc, Wei Zhangb, Cheng Lib, Yuting Guob, Ping Jiangb, Yang Tangb,*, Zhenhua Fengb,*, Hongguan Xiea,*

a College of Ecology and Environment, Chengdu University of Technology, Chengdu, Sichuan 610059, China.

b Sichuan Experimental Testing and Research Center of Natural Resources (Sichuan Nuclear Emergency Technical Support Center), Chengdu, Sichuan 610081, China.

c Sichuan Institute of Nuclear Geological Survey, Chengdu, Sichuan 610061, China.

* Corresponding authors: E-mail: Tyoung94_SCETRCNR@163.com (Y.T.); fengshanzhong86@163.com (Z.F.); Xiehongguan@hotmail.com (H.X).

Table of Contents

Section S1. Preparation of soil conditioner by conventional calcination	3

Section S2. Determination of available potassium and activation Rate	4

Section S3. Determination of total cadmium in Soil	5

Section S4. Determination of bioavailable cadmium in soil	6

Section S5. Determination of soil nutrient indicators	7

Section S6. Tables and Figures	8

Section S1. Preparation of soil conditioner by conventional calcination

Firstly, phosphorus-potassium ore tailings, limestone, and dolomite were mixed at a mass ratio of 1:1:1, which were then added into an agate mortar to be ground for 15 min until fully mixed and ground to −200 mesh. Subsequently, 15 g of the mixed mineral sample (phosphorus-potassium ore tailings, dolomite, and limestone) was loaded into a corundum crucible. Afterwards, the mixed mineral sample was calcined at 900oC for different holding time in a conventional box-type resistance muffle furnace, which was heated to the target temperature at a steady heating rate and maintained at a constant temperature throughout the whole calcination process. Finally, the calcined solids were naturally cooled to room temperature, followed by regrinding to −200 mesh to obtain conventional calcinated conditioner.

Section S2. Determination of available potassium and activation rate

The available potassium content of the calcined products was extracted with neutral 1 mol·L⁻¹ ammonium acetate solution, in accordance with the Chinese agricultural industry standard NY/T 889-2004.

Briefly, 2.000 g of the sample was weighed into a 250 mL conical flask, and 100 mL of 1 mol·L⁻¹ NH4OAc solution was added. The mixture was oscillated at 25 ± 1oC and 180 r·min⁻¹ for 30 min, then filtered through dry quantitative filter paper. The filtrate was diluted appropriately with ultra-pure water, and the available potassium concentration was determined by ICP-OES.

Section S3. Determination of total cadmium in soil

0.2000 g of air-dried soil sample (sieved through a 100-mesh nylon sieve) was weighed into a PTFE digestion tube, with 6 mL HNO3, 3 mL HF, and 1 mL HClO4 added sequentially. The digestion procedure was consistent with Section S2. After digestion, the solution was evaporated to near dryness, acidified, fixed to a 25 mL volumetric flask, filtered through a 0.45 μm filter membrane, and the total Cd concentration was determined by ICP-OES.

Section S4. Determination of bioavailable cadmium in soil

The bioavailable (DTPA-extractable) Cd in soil was extracted using diethylenetriaminepentaacetic acid (DTPA) solution, in accordance with GB/T 23739-2009.

Briefly, 10.00 g of air-dried soil sample (sieved through a 2 mm nylon sieve) was weighed into a 50 mL centrifuge tube, and 20 mL of DTPA extractant (pH 7.30 ± 0.05, containing 0.005 mol·L-1 DTPA, 0.01 mol·L-1 CaCl2, and 0.1 mol·L-1 triethanolamine) was added. The mixture was oscillated at 25 ± 1oC and 180 r·min-1 for 2 h, then centrifuged at 4000 r·min-1 for 10 min. The supernatant was filtered through a 0.45 μm filter membrane, and the DTPA-extractable Cd concentration was determined by ICP-OES.

Section S5. Determination of soil nutrient indicators

Available phosphorus: Extracted with 0.5 mol·L-1 NaHCO3 solution (pH 8.5), in accordance with NY/T 1121.7-2014; the P concentration in the extract was determined by ICP-OES.

Readily available potassium: Extracted with 1 mol·L-1 neutral NH4OAc solution, consistent with Section S1.2.2; K concentration determined by ICP-OES.

Slowly available potassium: Extracted with 1 mol·L-1 boiling HNO3 solution, in accordance with NY/T 889-2004; K concentration determined by ICP-OES.

Available silicon: Extracted with 0.025 mol·L-1 citric acid solution, in accordance with NY/T 1121.15-2006; Si concentration determined by ICP-OES.

Exchangeable calcium and magnesium: Extracted with 1 mol·L-1 neutral NH4OAc solution, in accordance with NY/T 1121.13-2006; Ca and Mg concentrations determined by ICP-OES.

Soil organic matter: Determined by potassium dichromate oxidation-external heating method, in accordance with NY/T 1121.6-2006; the organic carbon content was quantified by titration with ferrous sulfate standard solution, and converted to soil organic matter content with the conversion factor of 1.724.

Cation exchange capacity (CEC): Extracted with 1 mol·L⁻¹ neutral NH4OAc solution, in accordance with NY/T 1121.5-2021; the total concentration of exchangeable base cations (K+, Na+, Ca2+, Mg2+) in the extract was determined by ICP-OES, and the soil cation exchange capacity was calculated by combining with exchangeable acidity data.

Section S6. Tables and Figures

Table S1. XRF detection data of main components in Phosphorus-Potassium Mine Tailings (wt. %).

| MgO | P2O5 | K2O | SiO2 | CaO | Cu | PbO | As2O3 | Hg | CdO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 2.01% | 7.16% | 8.71% | 45.13% | 32.98% | < | < | < | < | < |

Table S2. XRF detection data of main components in dolomite (wt. %).

| MgO | P2O5 | K2O | SiO2 | CaO | CuO | PbO | As2O3 | HgO | CdO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 15.19% | 0.0124% | 0.0549% | 1.28% | 26.79% | < | < | < | < | < |

Table S3. XRF detection data of main components in limeston (wt. %).

| MgO | P2O5 | K2O | SiO2 | CaO | CuO | PbO | As2O3 | HgO | CdO |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 0.758% | 0.0034% | 0.0054% | 0.0527% | 44.22% | < | < | < | < | < |

Table S4. Basic physicochemical properties of the tested soil.

| Indicator | Value | Unit |
| --- | --- | --- |
| pH | 6.55 | — |
| Readily Available potassium (K) | 136 | mg kg-1 |
| Exchangeable calcium (Ca) | 13.7 | cmol(+) kg-1 |
| Exchangeable magnesium (Mg) | 2.95 | cmol(+) kg-1 |
| Available phosphorus (P) | 47.1 | mg kg-1 |
| Total cadmium (Cd) | 1.76 | mg kg-1 |
| Available cadmium (Cd) | 0.677 | mg kg-1 |
| Organic matter | 26.4 | g kg-1 |
| Cation exchange capacity(CEC) | 13.71 | cmol(+) kg-1 |

Table S5. Phase powder diffraction file (PDF) code.

| Phase | Code |
| --- | --- |
| Ca5(PO4)3F | 00-015-0876 |
| CaCO3 | 00-005-0586 |
| CaMg(CO3)2 | 00-011-0078 |
| KAlSi3O8 | 00-010-0353 |
| MgO | 00-004-0829 |
| Ca2MgSi2O7 | 00-011-0129 |
| Ca2SiO4 | 00-001-1029 |
| CaAl2Si2O8 | 00-001-0572 |
| K2CO3 | 00-016-0820 |

Fig. S1. Content of the available elements (P, K, Si, Ca, and Mg) in the soil conditioners prepared by microwave-assisted calcination at different temperatures (700, 800, 900, 1000, and 1100oC) for 1 h.

Fig. S2. Activation rate of the available elements (P, K, Si, Ca, and Mg) in the soil conditioners prepared by microwave-assisted calcination at different temperatures (700, 800, 900, 1000, and 1100oC) for 1 h.

Fig. S3. Content of the available elements (P, K, Si, Ca, and Mg) in the soil conditioners prepared by microwave-assisted calcination at 900oC for different holding times (0.5, 1, 1.5, 2, and 2.5 h).

Fig. S4. Activation rate of the available elements (P, K, Si, Ca, and Mg) in the soil conditioners prepared by microwave-assisted calcination at 900oC for different holding times (0.5, 1, 1.5, 2, and 2.5 h).

Fig. S5. Spearman correlation heatmap between soil physicochemical properties and dominant microbial genera in Cd-contaminated soil, * indicates significant difference at p < 0.05. ** indicates extremely significant difference at p < 0.01.

Fig. S6. Effects of PPMC application on the α-diversity indices of soil bacterial and fungal communities in Cd-contaminated farmland soil. (a) Chao1 index of soil bacterial community; (b) Shannon index of soil bacterial community; (c) Chao1 index of soil fungal community; (d) Shannon index of soil fungal community. * indicates significant difference at p < 0.05, ** indicates extremely significant difference at p < 0.01 (independent-samples t-test).