Supplementary Information

Polarization Effects on Interfacial Migration Between Molten Fe–Tramp Elements (Cu, Sn, Ni, Cr) and Molten Oxide Containing FeS

Masahiro Ambiru1,+, Shungo Natsui2,*, Akihisa Ito2,+, Miho Hayasaka2,+, and Hiroshi Nogami2,+

1Graduate School of Engineering, Tohoku University, Katahira 2−1−1, Aoba−ku, Sendai, Miyagi 980−8577, Japan

2Institute of Multidisciplinary Research for Advanced Materials, Tohoku University, Katahira 2−1−1, Aoba−ku, Sendai, Miyagi 980−8577, Japan

*natsui@tohoku.ac.jp

+these authors contributed equally to this work

Supplemental Note 1: Current–time curves

Fig. S1 |  Time variations of current during constant−potential electrolysis. Current–time curves for experiments #2, #4, and #6 are shown as representative results of constant−potential electrolysis.

Supplemental Note 2: Formal Standard Formation Potentials for Oxidation and Sulfidation (1873 K)

This supplemental table summarizes formal standard electrode potentials (E°) at T = 1873 K for oxide and sulfide formation reactions of Fe, Cu, Sn, Ni, and Cr. The standard Gibbs energy change is expressed as:

∆G°T=A+BTlogT+CT [J/mol]				(S1)

E°T=∆G°nF[V], F=96485 [C/mol]				(S2)

Here, ΔG°(T) denotes the standard Gibbs energy change normalized to 1 mol of the compound produced (e.g., divide by 2 for reactions producing 2 mol of oxide/sulfide), n is the number of electrons associated with forming 1 mol of the compound (e.g., n = 2 for MO with M2+; n = 2 for Cu2O and Cu2S; n = 6 for Cr2O3; n = 4 for Ni3S2).

Table S1 | Estimated standard electrode potentials for oxidation and sulfidation (1873 K).

A. Oxide systems (O2 basis)

| Formation reaction | ΔG° at 1873 K [kJ] | ΔG° per mol compound [kJ/mol] | n | E° [V] |
| --- | --- | --- | --- | --- |
| 4Cu(l) + O2(g) = 2Cu2O(l) | –79.802 | –39.901 | 2 | –0.2068 |
| 2Sn(l) + O2(g) = 2SnO(g) | –174.917 | –87.458 | 2 | –0.4532 |
| 2Ni(l) + O2(g) = 2NiO(s) | –149.004 | –74.502 | 2 | –0.3861 |
| 2Fe(l) + O2(g) = 2FeO(l) | –295.767 | –147.883 | 2 | –0.7664 |
| 4/3Cr(s) + O2(g) = 2/3Cr2O3(s) | –436.490 | –654.735 | 6 | –1.1310 |

B. Sulfide systems (S2 basis)

| Formation reaction | ΔG° at 1873 K [kJ] | ΔG° per mol compound [kJ/mol] | n | E° [V] |
| --- | --- | --- | --- | --- |
| 4Cu(l) + S2(g) = 2Cu2S(l) | –142.424 | –71.212 | 2 | –0.3690 |
| 2Sn(l) + S2(g) = 2SnS(g) | –122.675 | –61.338 | 2 | –0.3179 |
| 3Ni(l) + S2(g) = Ni3S2(l) | –116.081 | –116.081 | 4 | –0.3008 |
| 2Fe(l) + S2(g) = 2FeS(l) | –110.248 | –55.124 | 2 | –0.2857 |
| Cr(s) + 1/2 S2(g) = CrS(s) | –96.723 | –96.723 | 2 | –0.5012 |

References

Knacke O, Kubaschewski O, Hesselmann K. Thermochemical Properties of Inorganic Substances. 2nd ed. Berlin: Springer−Verlag; 1991.

Oikawa K, Mitsui H, Ohtani H, Ishida K. Thermodynamic calculations of phase equilibria in the Fe–Cr–S system. ISIJ Int. 2000;40:182–190.

Supplemental Note 3: Thermodynamic interpretation using Wagner interaction parameters

Activities of dilute solutes in molten iron were discussed using Wagner’s first–order interaction parameter formalism:

lnγi=jεijwj						(S3)

Here, γi is the activity coefficient of solute i in molten Fe, εij is the interaction parameter (wt% basis), and wj is the solute concentration (wt%). On the grounds that insufficient data was found, the Cu–Ni interaction was set to zero (εCu,Ni = 0). Table S2 lists the interaction parameters εij used for the five–component subspace: Cu, Sn, Ni, Cr, S. Temperature–dependent terms were evaluated at 1873 K.

Table S2 | Estimated interaction parameters εij (wt% basis).

| i / j | Cu | Sn | Ni | Cr | S |
| --- | --- | --- | --- | --- | --- |
| Cu | –5.4 | –0.013 | 0 | 3.9 | –2.4 |
| Sn | –0.024 | 0.0017 | –6.8 | 0.015 | –0.028 |
| Ni | 0 | –6.8 | 0.0007 | 0 | –0.1 |
| Cr | 4.1 | 0.009 | 0 | 0.005 | –22 |
| S | –2.3 | –0.0044 | –0.1 | –22 | –5.7 |

Contribution analysis of lnγi

Using the composition in metal (wt%): Cu = 0.5, Sn = 0.2, Ni = 0.2, Cr = 0.2, S = 0.286, Eq. (S3) was evaluated and decomposed into individual contributions εij·wj. Each contribution in Table S3 is reported in natural log units (ln).

Table S3 | Estimated activity coefficient of solute i in molten Fe.

| i | Cu contrib. | Sn contrib. | Ni contrib. | Cr contrib. | S contrib. | ln γi | γi |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Cu | –2.700 | –0.003 | 0.000 | 0.780 | –0.686 | –2.609 | 0.0736 |
| Sn | –0.012 | 0.000 | –1.360 | 0.003 | –0.008 | –1.377 | 0.252 |
| Ni | 0.000 | –1.360 | 0.000 | 0.000 | –0.029 | –1.388 | 0.250 |
| Cr | 2.050 | 0.002 | 0.000 | 0.001 | –6.292 | –4.239 | 0.0144 |
| S | –1.150 | –0.001 | –0.020 | –4.400 | –1.630 | –7.201 | 0.000746 |

In the absence of applied potential, transfer from metal to slag is considered by chemical equilibrium involving sulfide formation/partitioning: i(in Fe) + S(in Fe) ⇌ iS(in slag)

Table S3 shows that sulfur in the metal has a very small activity coefficient (lnγS = –7.201, γS ≈ 7.46×10–4), dominated by the strong negative contribution of Cr (εS,Cr·wCr = –4.400) and the sulfur self–term (εS,S·wS = –1.630). Under such low effective sulfur activity in the metal, removal is not determined by γi alone; it is strongly influenced by the stability (low activity) of iS species in the slag (i.e., the slag–side ‘capacity’ for each sulfide). Thus, Sn and Cr can still be preferentially removed if the slag stabilizes SnS and CrS (or related sulfide/oxide species) more strongly than Ni sulfide under the present slag chemistry.

Notes on applied potential (1 V) and interfacial effects

When a potential is applied across the metal–slag interface, the final metal compositions differ from those at 0 V. This suggests additional electrochemical/interfacial effects beyond bulk chemical equilibrium, such as electric–double–layer formation and electrocapillarity that can modify interfacial adsorption and the effective reaction area.

References

Hino, M. & Ito, K. (eds) Thermodynamic Data for Steelmaking (Tohoku University Press, 2010).

Ueda, S. Measurements and theoretical predictions of thermodynamic properties of trace elements in molten iron. PhD thesis, The University of Tokyo. https://doi.org/10.15083/0002002001 (2019).