Table 1 - Physicochemical and surface characterization results

| % Chamotte | Contact angle (°) | Density (g/cm³) | Water absorption (%) |
| --- | --- | --- | --- |
| 0,0% | 68,5 | 1,207 | 1,56 |
| 0,5% | 57,8 | 1,216 | 1,48 |
| 1,0% | 51,2 | 1,220 | 1,47 |
| 1,5% | 54,6 | 1,242 | 1,51 |
| 2,0% | 60,3 | 1,257 | 1,54 |

Table 2- Analysis of variance (ANOVA) of the properties of Chamotte-reinforced composites a) Stress – Flexural; b) Strain – Flexural; c) Stress – Tensile; d) Strain – Tensile; e) Stress – Compression; f) Strain – Compression; g) Impact Izod test; h) Shore hardness A

| - Stress – Flexure |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Source | Sum of Squares | Degrees of Freedom | Mean Squares | F (Calculated) | p-Value | F Critical |
| Between Groups | 12 863 | 4 | 3 215,8 | ≈ 296,4 | < 0,001 | 2,87 |
| Within Groups | 217 | 20 | 10,85 | — | — | — |
| Total | 13 080 | 24 | — | — | — | — |
| - Strain – Flexure |  |  |  |  |  |  |
| Source | Sum of Squares | Degrees of Freedom | Mean Squares | F (Calculated) | p-Value | F Critical |
| Between Groups | 3,61 | 4 | 0,902 | ≈ 11,1 | < 0,001 | 2,87 |
| Within Groups | 1,63 | 20 | 0,081 | — | — | — |
| Total | 5,24 | 24 | — | — | — | — |
| - Stress – Tension |  |  |  |  |  |  |
| Source | Sum of Squares | Degrees of Freedom | Mean Squares | F (Calculated) | p-Value | F Critical |
| Between Groups | 117,62 | 4 | 29,41 | 5,08 | < 0,001 | 2,87 |
| Within Groups | 173,81 | 30 | 5,79 | — | — | — |
| Total | 291,43 | 34 | — | — | — | — |
| - Strain – Tension |  |  |  |  |  |  |
| Source | Sum of Squares | Degrees of Freedom | Mean Squares | F (Calculated) | p-Value | F Critical |
| Between Groups | 6,38 | 4 | 1,59 | 6,72 | < 0,001 | 2,87 |
| Within Groups | 4,73 | 20 | 0,24 | — | — | — |
| Total | 11,11 | 24 | — | — | — | — |
| - Stress – Compression |  |  |  |  |  |  |
| Source | Sum of Squares | Degrees of Freedom | Mean Squares | F (Calculated) | p-Value | F Critical |
| Between Groups | 3244,5 | 4 | 811,1 | 29,4 | < 0,001 | 2,87 |
| Within Groups | 829,0 | 30 | 27,6 | — | — | — |
| Total | 4073,5 | 34 | — | — | — | — |
| - Strain – Compression |  |  |  |  |  |  |
| Source | Sum of Squares | Degrees of Freedom | Mean Squares | F (Calculated) | p-Value | F Critical |
| Between Groups | 30,19 | 4 | 7,55 | 2,78 | 0,056 | 2,87 |
| Within Groups | 54,31 | 20 | 2,72 | — | — | — |
| Total | 84,50 | 24 | — | — | — | — |
| - Izod test |  |  |  |  |  |  |
| Source | Sum of Squares | Degrees of Freedom | Mean Squares | F (Calculated) | p-Value | F Critical |
| Between Groups | 0,48 | 4 | 0,12 | 0,37 | 0,83 | 2,87 |
| Within Groups | 6,50 | 20 | 0,33 | — | — | — |
| Total | 6,98 | 24 | — | — | — | — |
| - Shore D Hardness |  |  |  |  |  |  |
| Source | Sum of Squares | Degrees of Freedom | Mean Squares | F (Calculated) | p-Value | F Critical |
| Between Groups | 70,6 | 4 | 17,65 | 57,3 | < 0,0001 | 2,87 |
| Within Groups | 6,16 | 20 | 0,31 | — | — | — |
| Total | 76,76 | 24 | — | — | — | — |

Table 3- Results with Tukey’s Post Hoc Test

| Amount of chamote (%) |  | 0,0 | 0,5 | 1,0 | 1,5 | 2,0 |
| --- | --- | --- | --- | --- | --- | --- |
| Com- pression | Strain (MPa) | 106,6±5,4a | 99,5±5,0b | 86,7± 4,0c | 83,9±3,2c | 81,9±7,6c |
|  | Stress (%) | 41,70±1,20 | 40,72±1,13 | 39,60±1,67 | 39,83±1,76 | 38,27±1,98 |
| Flexural | Strain (MPa) | 95,7±2,7c | 105,4±2,4b | 123,9±2,6a | 80,2±2,8d | 53,1±4,7e |
|  | Stress (%) | 0,83±0,20c | 0,92±0,43c | 1,08± 0,25bc | 1,95±0,31a | 1,28±0,26b |
| Tensile | Strain (MPa) | 20,0±1,9b | 22,1±1,3ab | 24,5± 3,7a | 21,1±1,6b | 19,4 ± 2,7b |
|  | Stress (%) | 3,4±0,76a | 2,5±0,34b | 2,5±0,52b | 2,21±0,21bc | 1,65 ± 0,28c |
| Impact Izod (J) |  | 1,7±0,6 | 1,9±0,6 | 2,0 ± 0,5 | 1,7±0,6 | 1,6 ± 0,3 |
| Hardness Shore A |  | 78,0±0,89a | 79,8±0,43b | 80,2 ± 0,30c | 81,0±0,56c | 83,2 ± 0,40d |

Table 4-  Dimensional deviation and warpage behavior of the SLA resin reinforced with chamotte

| Chamotte (%) | Dimensional deviation (%) | Warpage (mm) | Dimensional accuracy (%) |
| --- | --- | --- | --- |
| 0.0 | 2.84 ± 0.12 | 2.31 ± 0.15 | 94.3 ± 1.2 |
| 0.5 | 2.21 ± 0.10 | 1.86 ± 0.11 | 95.8 ± 1.0 |
| 1.0 | 1.74 ± 0.08 | 1.42 ± 0.09 | 97.4 ± 0.8 |
| 1.5 | 1.93 ± 0.11 | 1.57 ± 0.12 | 96.7 ± 0.9 |
| 2.0 | 2.17 ± 0.14 | 1.79 ± 0.13 | 95.9 ± 1.1 |

Table 5 – Directional shrinkage behavior of the SLA resin reinforced with chamotte

| Chamotte (%) | X-axis shrinkage (%) |  | Y-axis shrinkage (%) | Z-axis shrinkage (%) |
| --- | --- | --- | --- | --- |
| 0.0 | 2.42 ± 0.11 |  | 2.58 ± 0.13 | 3.12 ± 0.16 |
| 0.5 | 2.03 ± 0.10 |  | 2.11 ± 0.12 | 2.71 ± 0.14 |
| 1.0 | 1.68 ± 0.08 |  | 1.73 ± 0.09 | 2.21 ± 0.12 |
| 1.5 | 1.82 ± 0.10 |  | 1.89 ± 0.11 | 2.39 ± 0.13 |
| 2.0 | 2.05 ± 0.12 |  | 2.12 ± 0.13 | 2.63 ± 0.15 |