Supplementary Information:

Highly efficient and reusable energy-absorbing metamaterials exploiting soft rate-dependent frictional interfaces

Jinyou Li1, Zhe Chen1, Qunyang Li*1, Lihua Jin†2, and Zhihua Zhao‡1

1School of Aerospace Engineering, Tsinghua University, Beijing 100084, PRC

2Department of Mechanical and Aerospace Engineering, University of California, Los Angeles, CA 90095, USA

Table of Contents

Supplementary Figure 1: Fabrication process of the reinforced elastomer.	2

Supplementary Figure 2: Periodic stiff porous frame of the reinforced elastomer modified from Schwarz primitive minimal surface.	3

Supplementary Figure 3: Measurements of rate-dependent μ between the steel and silicone elastomer.	4

Supplementary Figure 4: FEM model for calculating the nonlinear N-F relationship of a quarter column.	6

Supplementary Figure 5: Tested mechanical properties of the silicone elastomer and the corresponding Ogden material model.	7

Supplementary Figure 6: Energy-absorbing capacity per life versus reusability.	8

Supplementary References	9

Supplementary Figures

Supplementary Figure 1: Fabrication process of the reinforced elastomer. a Components required for manufacturing the reinforced elastomer, including a stiff porous frame and four molds. The stiff frame, outer mold, top mold, and bottom mold are 3D printed through FDM technology (Hori Z300 3D printer) with PLA filaments (eSUN poly lactic acid). Rod molds are commercial 304 stainless steel rods of diameter 1.8 mm. b Assemble molds and stiff frame together. c Inject liquid silicone elastomer into the assembled outer mold by a syringe, in which the silicone elastomer consists of two liquid constituents and they are mixed in ratio 1:1. d Push the top mold and the stiff frame downward until the top mold encloses the outer mold, and leave the assembly at room temperature for 6 hours to cure the silicone elastomer. e Remove the molds to get the reinforced elastomer, in which the cured silicone elastomer interweaves with the stiff porous frame.

Supplementary Figure 2: Periodic stiff porous frame of the reinforced elastomer modified from Schwarz primitive minimal surface. a A cubic unit with a smooth surface modified from Schwarz’ P surface [1]. The yellow patch with six red edges is a 1/8 portion of the surface, and each edge is a quarter circle. b Surface in (a) split the cube into two domains: inner and outer; and the outer domain is a filled solid. c 3×3×3 array structure of the cubic cell in (b). d A cubic unit with a surface modified from (a) by enlarging circles on the faces of the cube. e A cubic cell obtained by filling the outer domain in (d) as a solid. f 3×3×3 array structure of the cubic cell in (e). g A hexagonal unit with the surface modified from (d) by changing the top and bottom faces from square to hexagon. This modification allows a cell to have more neighbors in the horizontal plane. h A hexagonal cell obtained by filling the outer domain in (g) as a solid. i Seven-column array structure of the hexagonal cell in (h). It is design of the stiff porous frame in the reinforced elastomer.

Supplementary Figure 3: Measurements of rate-dependent μ between the steel and silicone elastomer. a The specimen of the silicone elastomer layer, with thickness t. b FEM model to determine the applied force Fz that can maintain the nominal normal stress to be about 0.53 MPa. c Schematic diagram of the measurement of  using a Tribometer (Rtec MFT-V). d Experimental results of the relationship between  and the sliding speed v, measured by specimens with thickness 0.4 mm and 1.3 mm. e Raw data from the tests for the specimens with thickness 0.4 mm and 1.3 mm, respectively.

We use a Tribometer (Rtec MFT-V) to measure the frictional coefficient  between the steel and silicone elastomer. As shown in Supplementary Fig. 3c, a steel sphere is mounted on the clamp of the machine, and pressed with Fz on the silicone elastomer layer. The steel sphere is a commercial one with diameter 6.35 mm to match the machine, and the silicone layer is cured from liquid form on a steel base with diameter 6.25 cm. We make two elastomer discs with thickness 0.4 mm and 1.3 mm, because the thickness of the elastomer surrounding a single rod varies along the rod in the proposed metamaterials. Since depends on normal stress, Fz is applied to maintain the nominal normal stress, defined as Fz divide the contact area An, to be about 0.53 MPa. In the experiments, the silicone elastomer layer is driven to rotate at a set speed, while the steel sphere is fixed. Lateral force and normal force are recorded. Calculating their ratio gives . Results in Supplementary Fig. 3d indicate that increases with the speed from 57 to 1885 mm/min, covering that in the compression experiments on steel rods within the speed limit of the MTS testing machine (500 mm/min).

Supplementary Figure 4: FEM model for calculating the nonlinear N-F relationship of a quarter column. a FEM model of a quarter column of the metamaterial. The red dashed lines in the bottom inlet represent symmetry boundary conditions. b A cell of (a) to illustrate the model in detail. Stiff frame (yellow), silicone elastomer (grey) and steel rod (black) are all meshed with eight-node hexahedral elements. The interface between the frame and elastomer is set as contact, in which the frictional coefficient is set as 1. The interface nodes of the elastomer and rod are merged together. The constitutive behavior of the silicone elastomer is obtained from Supplementary Fig. 5. Normal force N is calculated as an integration of normal stress n over the rod surface. c Numerical simulations are processed in two quasi-static steps. In step 1, the temperature T in the rod is raised until rod diameter increases from 1.8 mm to 2.0 mm to build up prestress in the rod and elastomer. In step 2, the rod is forced to move downward by displacement u, which increases gradually from 0 to 1.5 mm. The reaction force F is computed. d Calculated nonlinear N-F relationship in step 2. At the beginning of step 2, the average normal stress σn is about 0.53 MPa, which is used to test the rate-dependent frictional coefficient between steel and the silicone elastomer in Supplementary Fig. 3.

Supplementary Figure 5: Tested mechanical properties of the silicone elastomer and the corresponding Ogden material model. a-b Stress-strain curve of the silicone elastomer specimen under uniaxial tensile and compression test, and the corresponding theoretical curve of Ogden material model with parameters in the main context or the next paragraph.

Here, we adopted the third order Ogden material model [2] to formulate the hyperelastic behavior of the elastomer. Its strain energy potential density is

W=i=132μiαi2λ1αi+λ2αi+λ3αi-3

where λ1, λ2 and λ3 are principle stretches, and αi and μi, i = 1, 2, 3, are material parameters determined by fitting the experimental data of tensile and compression test. Due to elastomer’s Mullins effect, the tensile stress-strain curves change significantly between the first and the subsequent tests. Since our metamaterials are for repeated usage, the second tensile curve and the averaged compression curve were adopted as the stress-strain curves for fitting Ogden model. The fitted material parameters are:

α1=3.248, α2=13.706, α3=-3.490,

μ1=0.322 MPa,  μ2=7.949×10-5 MPa,  μ3=6.667×10-2 MPa.

Supplementary Figure 6: Energy-absorbing capacity per life versus reusability. The numbers n of repeated cycles tested in the references are used for the calculation, and the references are listed in the main text.

Supplementary References

- Shin, J. et al. Finite element analysis of Schwarz P surface pore geometries for tissue-engineered scaffolds. Math. Probl. Eng. 2012, 694194 (2012).

- Bergstrom, J. S. Mechanics of Solid Polymers: Theory and Computational Modeling (William Andrew, San Diego, 2015).

* corresponding author, qunyang@tsinghua.edu.cn

† corresponding author, lihuajin@seas.ucla.edu

‡ corresponding author, zhaozh@tsinghua.edu.cn