Supporting Information

TEXT-II

Sustainable Utilization of Biomass-Derived Biochar for Asphalt Modification: Multiscale Experimental and Theoretical Insights

Meili Liua, Shaocheng Shenb, Kun Wangb,c, Fuwu Zhangb, Xianming Shia,*

a Civil and Architectural Engineering, University of Miami, Coral Gables, Florida 33146, USA

b Department of Chemistry, University of Miami, Coral Gables, Florida 33146, USA

c Department of Physics, University of Miami, Coral Gables, Florida 33146, USA

*: Corresponding authors

E-mail address: xxs784@miami.edu

Table SS 1-24. Local minima and maxima on the Electrostatic potentials (ESP) surface of 12 asphalt molecules and WS-biochar doped Asphalt systems. All the ESP calculations are performed at the level of B3LYP/6-31G (d, p). Yellow and cyan spheres denote the surface local maxima and minima of the ESP values.

Table of Contents

Table SS 1. Benzobisbenzothiophene of local minima and maxima on the Electrostatic potentials	S4

Table SS 2. Trimethylbenzene of local minima and maxima on the Electrostatic potentials (ESP) surface	S6

Table SS 3. Thiophene of local minima and maxima on the Electrostatic potentials (ESP) surface	S9

Table SS 4. Pyridinohopane of local minima and maxima on the Electrostatic potentials (ESP) surface	S12

Table SS 5. Quinolinohopane of local minima and maxima on the Electrostatic potentials (ESP) surface	S17

Table SS 6. DOCHN of local minima and maxima on the Electrostatic potentials (ESP) surface	S20

Table SS 7. PHPN of local minima and maxima on the Electrostatic potentials (ESP) surface	S23

Table SS 8. Squalane of local minima and maxima on the Electrostatic potentials (ESP) surface	S26

Table SS 9. Hopane of local minima and maxima on the Electrostatic potentials (ESP) surface	S30

Table SS 10. Phenol of local minima and maxima on the Electrostatic potentials (ESP) surface	S33

Table SS 11. Pyrrole of local minima and maxima on the Electrostatic potentials (ESP) surfaces	S37

Table SS 12. Thioisorenieratane of local minima and maxima on the Electrostatic potentials (ESP) surface	S42

Table SS 13. Benzobisbenzothiophene with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S46

Table SS 14. Trimethylbenzene with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S50

Table SS 15. Thiophene with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S55

Table SS 16. Pyridinohopane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S61

Table SS 17. Quinolinohopane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S66

Table SS 18. DOCHN with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S71

Table SS 19. PHPN with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S76

Table SS 20. Squalane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S80

Table SS 21. Hopane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S86

Table SS 22. Phenol with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S92

Table SS 23. Pyrrole with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S97

Table SS 24. Thioisorenieratane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface	S104

Table SS 1. Benzobisbenzothiophene of local minima and maxima on the Electrostatic potentials

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1      -8.044  -0.176   0.017  1.00 15.02          C

HETATM    2  C   MOL A   1      -6.312  -3.627  -0.027  1.00 14.62          C

HETATM    3  C   MOL A   1      -6.029   2.983   0.024  1.00 15.71          C

HETATM    4  C   MOL A   1      -4.360   3.009   0.037  1.00 14.21          C

HETATM    5  C   MOL A   1      -4.062  -0.334  -1.740  1.00-11.03          C

HETATM    6  C   MOL A   1      -4.044  -0.327   1.744  1.00-11.03          C

HETATM    7  C   MOL A   1      -2.134   0.551   1.789  1.00 -4.70          C

HETATM    8  C   MOL A   1      -2.149   0.613  -1.792  1.00 -4.70          C

HETATM    9  C   MOL A   1      -1.538  -3.535   0.019  1.00 19.83          C

HETATM   10  C   MOL A   1      -0.511   3.404   0.016  1.00 15.11          C

HETATM   11  C   MOL A   1      -0.002  -0.012  -1.720  1.00 -8.98          C

HETATM   12  C   MOL A   1       0.017   0.002   1.721  1.00 -8.98          C

HETATM   13  C   MOL A   1       0.492  -3.408  -0.034  1.00 15.10          C

HETATM   14  C   MOL A   1       1.556   3.528   0.018  1.00 19.83          C

HETATM   15  C   MOL A   1       2.152  -0.561   1.789  1.00 -4.68          C

HETATM   16  C   MOL A   1       2.144  -0.565  -1.789  1.00 -4.69          C

HETATM   17  C   MOL A   1       4.052   0.308  -1.745  1.00-11.04          C

HETATM   18  C   MOL A   1       4.035   0.350   1.744  1.00-11.03          C

HETATM   19  C   MOL A   1       4.382  -3.009  -0.033  1.00 14.18          C

HETATM   20  C   MOL A   1       6.036  -2.979   0.019  1.00 15.71          C

HETATM   21  C   MOL A   1       6.341   3.607   0.029  1.00 14.62          C

HETATM   22  C   MOL A   1       8.043   0.166  -0.030  1.00 15.02          C

HETATM    1  O   MOL A   1      -4.615  -0.889  -1.892  1.00-12.76          O

HETATM    2  O   MOL A   1      -4.619  -0.923   1.900  1.00-12.76          O

HETATM    3  O   MOL A   1      -2.385   2.527  -2.199  1.00-14.29          O

HETATM    4  O   MOL A   1      -2.364   2.541   2.197  1.00-14.29          O

HETATM    5  O   MOL A   1      -0.150   0.872  -1.948  1.00-10.96          O

HETATM    6  O   MOL A   1      -0.152   0.863   1.946  1.00-10.96          O

HETATM    7  O   MOL A   1       0.159  -0.879  -1.949  1.00-10.95          O

HETATM    8  O   MOL A   1       0.152  -0.815   1.937  1.00-10.95          O

HETATM    9  O   MOL A   1       2.381  -2.559  -2.193  1.00-14.29          O

HETATM   10  O   MOL A   1       2.399  -2.537   2.197  1.00-14.29          O

HETATM   11  O   MOL A   1       4.590   0.937  -1.899  1.00-12.76          O

HETATM   12  O   MOL A   1       4.608   0.943   1.904  1.00-12.76          O

END

Table SS 2. Trimethylbenzene of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -12.402  -1.490   1.426  1.00  6.47          C

HETATM    2  C   MOL A   1     -11.501   1.965  -0.471  1.00  6.08          C

HETATM    3  C   MOL A   1     -11.191  -1.602  -2.441  1.00  6.45          C

HETATM    4  C   MOL A   1     -10.853  -0.988   3.161  1.00  6.59          C

HETATM    5  C   MOL A   1      -9.753   2.524   1.435  1.00  6.32          C

HETATM    6  C   MOL A   1      -9.139   2.411  -1.202  1.00  4.93          C

HETATM    7  C   MOL A   1      -9.004  -1.245  -2.984  1.00  5.62          C

HETATM    8  C   MOL A   1      -8.903  -2.978   0.465  1.00  5.10          C

HETATM    9  C   MOL A   1      -7.159   1.918   2.166  1.00  4.52          C

HETATM   10  C   MOL A   1      -7.036  -0.295   2.511  1.00  7.10          C

HETATM   11  C   MOL A   1      -6.619  -2.033   0.982  1.00  6.02          C

HETATM   12  C   MOL A   1      -6.438   2.980  -1.671  1.00  5.03          C

HETATM   13  C   MOL A   1      -5.903  -0.853  -2.730  1.00  6.20          C

HETATM   14  C   MOL A   1      -5.889   2.553   3.123  1.00  6.61          C

HETATM   15  C   MOL A   1      -4.833  -1.301  -2.144  1.00  5.95          C

HETATM   16  C   MOL A   1      -4.769  -1.006   1.987  1.00  5.62          C

HETATM   17  C   MOL A   1      -4.373   4.155  -0.318  1.00  6.30          C

HETATM   18  C   MOL A   1      -4.002   2.650  -2.273  1.00  5.33          C

HETATM   19  C   MOL A   1      -2.729  -2.069  -2.749  1.00  5.63          C

HETATM   20  C   MOL A   1      -2.390  -1.701   1.091  1.00  7.41          C

HETATM   21  C   MOL A   1      -2.135  -2.407   0.621  1.00  7.51          C

HETATM   22  C   MOL A   1      -2.084   2.014   2.045  1.00  7.59          C

HETATM   23  C   MOL A   1      -1.662   1.896  -3.189  1.00  5.27          C

HETATM   24  C   MOL A   1      -1.330   2.108   0.814  1.00  7.01          C

HETATM   25  C   MOL A   1      -0.322  -2.110  -4.220  1.00  5.97          C

HETATM   26  C   MOL A   1       0.368   1.832  -3.666  1.00  5.60          C

HETATM   27  C   MOL A   1       0.463  -3.698  -2.157  1.00  6.12          C

HETATM   28  C   MOL A   1       0.601  -0.218   2.354  1.00  9.76          C

HETATM   29  C   MOL A   1       0.846   1.061   0.378  1.00  7.46          C

HETATM   30  C   MOL A   1       1.201  -1.227   3.478  1.00 11.02          C

HETATM   31  C   MOL A   1       1.201   1.315   1.116  1.00  9.55          C

HETATM   32  C   MOL A   1       1.493  -3.859   2.711  1.00 11.40          C

HETATM   33  C   MOL A   1       1.970   3.365   1.021  1.00  8.72          C

HETATM   34  C   MOL A   1       2.628  -3.532  -1.501  1.00  5.87          C

HETATM   35  C   MOL A   1       2.868  -1.398  -2.699  1.00  2.22          C

HETATM   36  C   MOL A   1       3.651   2.045   3.905  1.00  9.52          C

HETATM   37  C   MOL A   1       3.655  -4.863  -0.246  1.00  7.13          C

HETATM   38  C   MOL A   1       4.360   3.135   3.729  1.00  8.82          C

HETATM   39  C   MOL A   1       4.891  -1.486   4.156  1.00  6.91          C

HETATM   40  C   MOL A   1       5.208  -3.547   3.453  1.00  6.80          C

HETATM   41  C   MOL A   1       5.456   5.426   0.475  1.00  7.87          C

HETATM   42  C   MOL A   1       6.004  -3.485  -1.448  1.00 -0.11          C

HETATM   43  C   MOL A   1       6.919   4.584  -0.713  1.00  6.96          C

HETATM   44  C   MOL A   1       7.286  -0.830  -3.669  1.00  5.34          C

HETATM   45  C   MOL A   1       7.511   0.505  -4.066  1.00  6.41          C

HETATM   46  C   MOL A   1       8.397   3.841  -1.910  1.00  6.90          C

HETATM   47  C   MOL A   1       9.274  -1.633  -0.567  1.00  4.28          C

HETATM   48  C   MOL A   1       9.965   0.190  -1.215  1.00  5.85          C

HETATM    1  O   MOL A   1     -12.752  -0.207  -0.824  1.00 -2.38          O

HETATM    2  O   MOL A   1     -11.763   0.651   1.215  1.00 -2.03          O

HETATM    3  O   MOL A   1     -11.159   0.825   1.795  1.00 -1.96          O

HETATM    4  O   MOL A   1     -10.851   0.545  -2.040  1.00 -2.11          O

HETATM    5  O   MOL A   1     -10.003   0.667  -2.151  1.00 -1.98          O

HETATM    6  O   MOL A   1      -9.909   1.777  -0.078  1.00  2.42          O

HETATM    7  O   MOL A   1      -9.626   1.058   3.236  1.00 -1.87          O

HETATM    8  O   MOL A   1      -6.671   3.062   0.471  1.00 -2.04          O

HETATM    9  O   MOL A   1      -6.531  -2.065  -1.140  1.00 -0.67          O

HETATM   10  O   MOL A   1      -6.035   3.358   0.943  1.00 -2.04          O

HETATM   11  O   MOL A   1      -5.016   2.806  -1.123  1.00  2.41          O

HETATM   12  O   MOL A   1      -4.238   3.914   2.035  1.00 -2.00          O

HETATM   13  O   MOL A   1      -3.765   0.469  -2.830  1.00 -1.74          O

HETATM   14  O   MOL A   1      -3.148   0.311   1.694  1.00  0.87          O

HETATM   15  O   MOL A   1      -2.569  -0.056  -3.534  1.00 -1.91          O

HETATM   16  O   MOL A   1      -1.964  -0.190  -3.710  1.00 -1.94          O

HETATM   17  O   MOL A   1      -1.932   0.343   1.552  1.00  0.76          O

HETATM   18  O   MOL A   1      -1.356  -3.220  -1.362  1.00 -0.07          O

HETATM   19  O   MOL A   1      -0.638   1.701  -1.596  1.00  1.72          O

HETATM   20  O   MOL A   1      -0.248  -2.190   2.047  1.00  2.82          O

HETATM   21  O   MOL A   1       2.263   0.812  -2.874  1.00 -4.34          O

HETATM   22  O   MOL A   1       3.241  -1.161   4.356  1.00  2.69          O

HETATM   23  O   MOL A   1       4.566  -2.120  -1.243  1.00-17.40          O

HETATM   24  O   MOL A   1       4.737   1.616  -1.608  1.00-20.64          O

HETATM   25  O   MOL A   1       6.194  -2.574   1.019  1.00-25.87          O

HETATM   26  O   MOL A   1       7.087   1.301   1.293  1.00-21.37          O

HETATM   27  O   MOL A   1       9.466   1.812  -2.872  1.00 -1.66          O

END

Table SS 3. Thiophene of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -12.402  -1.490   1.426  1.00  6.47          C

HETATM    2  C   MOL A   1     -11.501   1.965  -0.471  1.00  6.08          C

HETATM    3  C   MOL A   1     -11.191  -1.602  -2.441  1.00  6.45          C

HETATM    4  C   MOL A   1     -10.853  -0.988   3.161  1.00  6.59          C

HETATM    5  C   MOL A   1      -9.753   2.524   1.435  1.00  6.32          C

HETATM    6  C   MOL A   1      -9.139   2.411  -1.202  1.00  4.93          C

HETATM    7  C   MOL A   1      -9.004  -1.245  -2.984  1.00  5.62          C

HETATM    8  C   MOL A   1      -8.903  -2.978   0.465  1.00  5.10          C

HETATM    9  C   MOL A   1      -7.159   1.918   2.166  1.00  4.52          C

HETATM   10  C   MOL A   1      -7.036  -0.295   2.511  1.00  7.10          C

HETATM   11  C   MOL A   1      -6.619  -2.033   0.982  1.00  6.02          C

HETATM   12  C   MOL A   1      -6.438   2.980  -1.671  1.00  5.03          C

HETATM   13  C   MOL A   1      -5.903  -0.853  -2.730  1.00  6.20          C

HETATM   14  C   MOL A   1      -5.889   2.553   3.123  1.00  6.61          C

HETATM   15  C   MOL A   1      -4.833  -1.301  -2.144  1.00  5.95          C

HETATM   16  C   MOL A   1      -4.769  -1.006   1.987  1.00  5.62          C

HETATM   17  C   MOL A   1      -4.373   4.155  -0.318  1.00  6.30          C

HETATM   18  C   MOL A   1      -4.002   2.650  -2.273  1.00  5.33          C

HETATM   19  C   MOL A   1      -2.729  -2.069  -2.749  1.00  5.63          C

HETATM   20  C   MOL A   1      -2.390  -1.701   1.091  1.00  7.41          C

HETATM   21  C   MOL A   1      -2.135  -2.407   0.621  1.00  7.51          C

HETATM   22  C   MOL A   1      -2.084   2.014   2.045  1.00  7.59          C

HETATM   23  C   MOL A   1      -1.662   1.896  -3.189  1.00  5.27          C

HETATM   24  C   MOL A   1      -1.330   2.108   0.814  1.00  7.01          C

HETATM   25  C   MOL A   1      -0.322  -2.110  -4.220  1.00  5.97          C

HETATM   26  C   MOL A   1       0.368   1.832  -3.666  1.00  5.60          C

HETATM   27  C   MOL A   1       0.463  -3.698  -2.157  1.00  6.12          C

HETATM   28  C   MOL A   1       0.601  -0.218   2.354  1.00  9.76          C

HETATM   29  C   MOL A   1       0.846   1.061   0.378  1.00  7.46          C

HETATM   30  C   MOL A   1       1.201  -1.227   3.478  1.00 11.02          C

HETATM   31  C   MOL A   1       1.201   1.315   1.116  1.00  9.55          C

HETATM   32  C   MOL A   1       1.493  -3.859   2.711  1.00 11.40          C

HETATM   33  C   MOL A   1       1.970   3.365   1.021  1.00  8.72          C

HETATM   34  C   MOL A   1       2.628  -3.532  -1.501  1.00  5.87          C

HETATM   35  C   MOL A   1       2.868  -1.398  -2.699  1.00  2.22          C

HETATM   36  C   MOL A   1       3.651   2.045   3.905  1.00  9.52          C

HETATM   37  C   MOL A   1       3.655  -4.863  -0.246  1.00  7.13          C

HETATM   38  C   MOL A   1       4.360   3.135   3.729  1.00  8.82          C

HETATM   39  C   MOL A   1       4.891  -1.486   4.156  1.00  6.91          C

HETATM   40  C   MOL A   1       5.208  -3.547   3.453  1.00  6.80          C

HETATM   41  C   MOL A   1       5.456   5.426   0.475  1.00  7.87          C

HETATM   42  C   MOL A   1       6.004  -3.485  -1.448  1.00 -0.11          C

HETATM   43  C   MOL A   1       6.919   4.584  -0.713  1.00  6.96          C

HETATM   44  C   MOL A   1       7.286  -0.830  -3.669  1.00  5.34          C

HETATM   45  C   MOL A   1       7.511   0.505  -4.066  1.00  6.41          C

HETATM   46  C   MOL A   1       8.397   3.841  -1.910  1.00  6.90          C

HETATM   47  C   MOL A   1       9.274  -1.633  -0.567  1.00  4.28          C

HETATM   48  C   MOL A   1       9.965   0.190  -1.215  1.00  5.85          C

HETATM    1  O   MOL A   1     -12.752  -0.207  -0.824  1.00 -2.38          O

HETATM    2  O   MOL A   1     -11.763   0.651   1.215  1.00 -2.03          O

HETATM    3  O   MOL A   1     -11.159   0.825   1.795  1.00 -1.96          O

HETATM    4  O   MOL A   1     -10.851   0.545  -2.040  1.00 -2.11          O

HETATM    5  O   MOL A   1     -10.003   0.667  -2.151  1.00 -1.98          O

HETATM    6  O   MOL A   1      -9.909   1.777  -0.078  1.00  2.42          O

HETATM    7  O   MOL A   1      -9.626   1.058   3.236  1.00 -1.87          O

HETATM    8  O   MOL A   1      -6.671   3.062   0.471  1.00 -2.04          O

HETATM    9  O   MOL A   1      -6.531  -2.065  -1.140  1.00 -0.67          O

HETATM   10  O   MOL A   1      -6.035   3.358   0.943  1.00 -2.04          O

HETATM   11  O   MOL A   1      -5.016   2.806  -1.123  1.00  2.41          O

HETATM   12  O   MOL A   1      -4.238   3.914   2.035  1.00 -2.00          O

HETATM   13  O   MOL A   1      -3.765   0.469  -2.830  1.00 -1.74          O

HETATM   14  O   MOL A   1      -3.148   0.311   1.694  1.00  0.87          O

HETATM   15  O   MOL A   1      -2.569  -0.056  -3.534  1.00 -1.91          O

HETATM   16  O   MOL A   1      -1.964  -0.190  -3.710  1.00 -1.94          O

HETATM   17  O   MOL A   1      -1.932   0.343   1.552  1.00  0.76          O

HETATM   18  O   MOL A   1      -1.356  -3.220  -1.362  1.00 -0.07          O

HETATM   19  O   MOL A   1      -0.638   1.701  -1.596  1.00  1.72          O

HETATM   20  O   MOL A   1      -0.248  -2.190   2.047  1.00  2.82          O

HETATM   21  O   MOL A   1       2.263   0.812  -2.874  1.00 -4.34          O

HETATM   22  O   MOL A   1       3.241  -1.161   4.356  1.00  2.69          O

HETATM   23  O   MOL A   1       4.566  -2.120  -1.243  1.00-17.40          O

HETATM   24  O   MOL A   1       4.737   1.616  -1.608  1.00-20.64          O

HETATM   25  O   MOL A   1       6.194  -2.574   1.019  1.00-25.87          O

HETATM   26  O   MOL A   1       7.087   1.301   1.293  1.00-21.37          O

HETATM   27  O   MOL A   1       9.466   1.812  -2.872  1.00 -1.66          O

END

Table SS 4. Pyridinohopane of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -18.297  -3.900   0.958  1.00 -0.58          C

HETATM    2  C   MOL A   1     -16.866  -0.404   0.791  1.00 -0.33          C

HETATM    3  C   MOL A   1     -15.612  -2.553   3.247  1.00 -0.35          C

HETATM    4  C   MOL A   1     -15.434  -0.568   2.375  1.00 -0.27          C

HETATM    5  C   MOL A   1     -13.034  -0.565  -1.330  1.00 -1.55          C

HETATM    6  C   MOL A   1     -12.496  -4.378  -2.547  1.00 -0.96          C

HETATM    7  C   MOL A   1     -12.024   1.376   2.494  1.00 -0.31          C

HETATM    8  C   MOL A   1     -11.804  -2.709   1.149  1.00 -1.57          C

HETATM    9  C   MOL A   1     -11.282  -0.565  -2.199  1.00 -1.26          C

HETATM   10  C   MOL A   1     -10.044  -2.695   0.224  1.00 -1.27          C

HETATM   11  C   MOL A   1      -9.637   3.557   3.645  1.00 -0.62          C

HETATM   12  C   MOL A   1      -9.396   0.777  -1.973  1.00 -1.61          C

HETATM   13  C   MOL A   1      -8.860   2.761  -0.426  1.00 -1.65          C

HETATM   14  C   MOL A   1      -8.028  -1.359   0.341  1.00 -1.58          C

HETATM   15  C   MOL A   1      -7.759  -2.721  -3.670  1.00 -0.73          C

HETATM   16  C   MOL A   1      -7.536   0.387   1.706  1.00 -1.80          C

HETATM   17  C   MOL A   1      -7.191   1.986  -2.072  1.00 -1.58          C

HETATM   18  C   MOL A   1      -6.547   5.890  -0.401  1.00 -0.93          C

HETATM   19  C   MOL A   1      -6.464  -2.777  -0.325  1.00 -0.06          C

HETATM   20  C   MOL A   1      -5.661   1.590   1.690  1.00 -1.80          C

HETATM   21  C   MOL A   1      -5.090   0.006  -5.690  1.00 -0.90          C

HETATM   22  C   MOL A   1      -4.897   3.007  -2.265  1.00 -1.61          C

HETATM   23  C   MOL A   1      -4.886   6.251   3.539  1.00 -0.74          C

HETATM   24  C   MOL A   1      -4.611   2.372   1.853  1.00 -1.85          C

HETATM   25  C   MOL A   1      -4.022   0.863   0.277  1.00 -1.94          C

HETATM   26  C   MOL A   1      -2.984  -2.404  -4.797  1.00 -1.08          C

HETATM   27  C   MOL A   1      -2.815   2.293  -3.494  1.00 -1.80          C

HETATM   28  C   MOL A   1      -2.570   4.112  -1.970  1.00 -1.70          C

HETATM   29  C   MOL A   1      -2.225   0.264  -0.718  1.00 -2.24          C

HETATM   30  C   MOL A   1      -2.139   1.737   0.515  1.00 -2.12          C

HETATM   31  C   MOL A   1      -1.773   3.182   2.056  1.00 -2.04          C

HETATM   32  C   MOL A   1      -1.328  -1.475  -4.724  1.00 -0.99          C

HETATM   33  C   MOL A   1      -1.204  -2.375   2.631  1.00 -2.00          C

HETATM   34  C   MOL A   1      -0.769   0.705  -0.519  1.00 -2.38          C

HETATM   35  C   MOL A   1      -0.669   3.004  -3.250  1.00 -1.68          C

HETATM   36  C   MOL A   1      -0.510   7.139   4.046  1.00  0.92          C

HETATM   37  C   MOL A   1      -0.118  -3.582  -0.560  1.00 -2.09          C

HETATM   38  C   MOL A   1       0.073   0.657   4.711  1.00 -1.98          C

HETATM   39  C   MOL A   1       0.604  -5.009   2.543  1.00 -1.90          C

HETATM   40  C   MOL A   1       1.469  -3.185   5.789  1.00 -1.70          C

HETATM   41  C   MOL A   1       1.639  -6.264   0.404  1.00 -1.76          C

HETATM   42  C   MOL A   1       2.169  -6.150   3.878  1.00 -1.60          C

HETATM   43  C   MOL A   1       2.263   0.575   7.011  1.00 -1.66          C

HETATM   44  C   MOL A   1       2.198   2.206   5.073  1.00 -1.97          C

HETATM   45  C   MOL A   1       2.954   5.461   1.014  1.00 -1.56          C

HETATM   46  C   MOL A   1       3.149   2.938  -3.400  1.00 -1.81          C

HETATM   47  C   MOL A   1       3.300  -2.777   6.739  1.00 -1.68          C

HETATM   48  C   MOL A   1       3.392  -7.457   1.433  1.00 -1.52          C

HETATM   49  C   MOL A   1       3.464  -5.164  -3.018  1.00 -1.64          C

HETATM   50  C   MOL A   1       4.074  -6.847  -2.079  1.00 -1.54          C

HETATM   51  C   MOL A   1       5.005  -4.304   5.460  1.00 -1.60          C

HETATM   52  C   MOL A   1       5.460   1.030   4.135  1.00 -2.24          C

HETATM   53  C   MOL A   1       5.742  -0.172   6.018  1.00 -1.75          C

HETATM   54  C   MOL A   1       5.898  -4.016   4.880  1.00 -1.65          C

HETATM   55  C   MOL A   1       6.667   1.298  -4.252  1.00 -1.67          C

HETATM   56  C   MOL A   1       6.788  -6.342   2.307  1.00 -1.58          C

HETATM   57  C   MOL A   1       6.803  -2.933  -3.951  1.00 -1.62          C

HETATM   58  C   MOL A   1       6.849  -6.685   0.463  1.00 -1.52          C

HETATM   59  C   MOL A   1       6.822  -6.088  -2.193  1.00 -1.56          C

HETATM   60  C   MOL A   1       8.199   4.191  -2.705  1.00 -1.50          C

HETATM   61  C   MOL A   1       8.761  -3.585   2.848  1.00 -1.65          C

HETATM   62  C   MOL A   1       9.032  -2.212   2.726  1.00 -1.70          C

HETATM   63  C   MOL A   1       9.193  -5.220  -1.732  1.00 -1.50          C

HETATM   64  C   MOL A   1      10.122  -2.232  -3.220  1.00 -1.78          C

HETATM   65  C   MOL A   1      10.315   3.994  -2.306  1.00 -1.26          C

HETATM   66  C   MOL A   1      10.620  -3.904   0.167  1.00 -1.60          C

HETATM   67  C   MOL A   1      12.307   4.081  -1.470  1.00 -1.22          C

HETATM   68  C   MOL A   1      12.846   1.363  -4.098  1.00 -1.32          C

HETATM   69  C   MOL A   1      14.726   2.690   1.505  1.00 -1.13          C

HETATM   70  C   MOL A   1      14.796   3.944  -2.231  1.00 -1.07          C

HETATM   71  C   MOL A   1      15.916  -1.008   0.094  1.00 -1.13          C

HETATM   72  C   MOL A   1      16.039   0.510  -3.453  1.00 -1.04          C

HETATM   73  C   MOL A   1      17.041   4.215  -0.944  1.00 -0.86          C

HETATM   74  C   MOL A   1      18.137   1.516   1.583  1.00 -0.83          C

HETATM   75  C   MOL A   1      18.222   0.706  -2.148  1.00 -0.84          C

HETATM    1  O   MOL A   1     -15.947  -5.412  -1.599  1.00 -2.66          O

HETATM    2  O   MOL A   1     -13.649  -1.200  -1.867  1.00 -1.63          O

HETATM    3  O   MOL A   1     -13.386   0.070  -0.825  1.00 -1.64          O

HETATM    4  O   MOL A   1     -12.239  -3.582   0.893  1.00 -1.65          O

HETATM    5  O   MOL A   1     -11.994  -2.312   1.853  1.00 -1.66          O

HETATM    6  O   MOL A   1     -10.271  -3.582  -2.704  1.00 -2.08          O

HETATM    7  O   MOL A   1      -9.580   3.086   0.039  1.00 -1.76          O

HETATM    8  O   MOL A   1      -9.222   2.051  -1.266  1.00 -1.73          O

HETATM    9  O   MOL A   1      -8.849   0.423  -2.941  1.00 -1.77          O

HETATM   10  O   MOL A   1      -7.976   0.516   2.457  1.00 -1.90          O

HETATM   11  O   MOL A   1      -6.591   1.578  -3.064  1.00 -1.77          O

HETATM   12  O   MOL A   1      -6.309   0.591   1.504  1.00 -1.89          O

HETATM   13  O   MOL A   1      -5.882   3.007  -2.196  1.00 -1.68          O

HETATM   14  O   MOL A   1      -5.767   2.925   3.242  1.00 -2.44          O

HETATM   15  O   MOL A   1      -3.624   2.530  -3.365  1.00 -1.84          O

HETATM   16  O   MOL A   1      -3.537   3.097   2.761  1.00 -2.21          O

HETATM   17  O   MOL A   1      -3.452  -2.386  -1.274  1.00 -3.10          O

HETATM   18  O   MOL A   1      -2.272   3.245  -3.204  1.00 -1.86          O

HETATM   19  O   MOL A   1      -2.224   1.774  -4.290  1.00 -1.91          O

HETATM   20  O   MOL A   1      -1.934   6.673   0.469  1.00 -1.91          O

HETATM   21  O   MOL A   1      -1.509  -0.724  -1.316  1.00 -2.50          O

HETATM   22  O   MOL A   1      -1.533   3.561   2.855  1.00 -2.20          O

HETATM   23  O   MOL A   1      -1.182  -0.597  -1.306  1.00 -2.50          O

HETATM   24  O   MOL A   1       0.236  -3.069   3.489  1.00 -2.25          O

HETATM   25  O   MOL A   1       0.905  -0.422   5.600  1.00 -2.17          O

HETATM   26  O   MOL A   1       1.160   5.166  -1.517  1.00 -2.18          O

HETATM   27  O   MOL A   1       1.320  -0.085  -1.113  1.00 -4.48          O

HETATM   28  O   MOL A   1       1.470   1.010   4.966  1.00 -2.17          O

HETATM   29  O   MOL A   1       1.644   4.920   2.868  1.00 -2.60          O

HETATM   30  O   MOL A   1       1.903  -5.291   1.822  1.00 -2.05          O

HETATM   31  O   MOL A   1       2.660  -4.727   5.677  1.00 -1.94          O

HETATM   32  O   MOL A   1       4.538  -5.407   3.779  1.00 -2.01          O

HETATM   33  O   MOL A   1       4.787   1.737  -1.943  1.00 -3.16          O

HETATM   34  O   MOL A   1       4.956  -7.639  -0.244  1.00 -1.84          O

HETATM   35  O   MOL A   1       5.053  -6.420   2.134  1.00 -1.89          O

HETATM   36  O   MOL A   1       5.018  -2.153   5.145  1.00 -2.13          O

HETATM   37  O   MOL A   1       5.425   1.020   1.494  1.00 -4.37          O

HETATM   38  O   MOL A   1       5.839  -6.759  -1.276  1.00 -1.84          O

HETATM   39  O   MOL A   1       7.310  -4.542   3.475  1.00 -1.91          O

HETATM   40  O   MOL A   1       7.420  -4.556  -3.034  1.00 -1.97          O

HETATM   41  O   MOL A   1       7.666  -5.250  -1.431  1.00 -1.78          O

HETATM   42  O   MOL A   1       8.693  -4.029   0.869  1.00 -1.95          O

HETATM   43  O   MOL A   1       9.643   0.126  -2.714  1.00 -2.49          O

HETATM   44  O   MOL A   1      11.960  -1.111   0.714  1.00 -3.42          O

HETATM   45  O   MOL A   1      16.171   2.958   0.979  1.00 -1.25          O

HETATM   46  O   MOL A   1      17.066  -0.089  -0.045  1.00 -1.25          O

HETATM   47  O   MOL A   1      18.563   2.478  -0.625  1.00 -1.18          O

END

Table SS 5. Quinolinohopane of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.837   0.662   0.218  1.00  6.64          C

HETATM    2  C   MOL A   1     -12.088   4.273  -0.256  1.00  6.59          C

HETATM    3  C   MOL A   1     -11.622   2.245   3.218  1.00  6.87          C

HETATM    4  C   MOL A   1     -10.748   1.056  -2.256  1.00  5.94          C

HETATM    5  C   MOL A   1     -10.246  -0.975   1.014  1.00  6.89          C

HETATM    6  C   MOL A   1      -9.689   4.425  -0.494  1.00  5.85          C

HETATM    7  C   MOL A   1      -9.446  -1.387   0.153  1.00  7.55          C

HETATM    8  C   MOL A   1      -8.882   2.265   2.949  1.00  6.73          C

HETATM    9  C   MOL A   1      -8.697   1.055  -2.408  1.00  5.33          C

HETATM   10  C   MOL A   1      -8.529  -1.167  -2.330  1.00  9.87          C

HETATM   11  C   MOL A   1      -6.986   0.762   2.847  1.00  8.91          C

HETATM   12  C   MOL A   1      -6.391   3.278   0.607  1.00  4.98          C

HETATM   13  C   MOL A   1      -5.780  -2.396  -3.949  1.00  3.90          C

HETATM   14  C   MOL A   1      -5.169   1.005   2.785  1.00 12.22          C

HETATM   15  C   MOL A   1      -4.062  -0.526   3.788  1.00 11.10          C

HETATM   16  C   MOL A   1      -3.436   2.610   2.108  1.00 11.12          C

HETATM   17  C   MOL A   1      -2.170  -4.260   0.393  1.00 -0.55          C

HETATM   18  C   MOL A   1      -0.355   1.187   3.127  1.00 12.16          C

HETATM   19  C   MOL A   1       0.119  -4.123  -2.803  1.00  4.37          C

HETATM   20  C   MOL A   1       0.411  -3.084   2.998  1.00 10.83          C

HETATM   21  C   MOL A   1       0.607  -0.302  -3.338  1.00  6.60          C

HETATM   22  C   MOL A   1       0.994   1.264  -0.662  1.00  8.88          C

HETATM   23  C   MOL A   1       0.974   3.274  -1.069  1.00  7.14          C

HETATM   24  C   MOL A   1       1.416  -5.218  -0.817  1.00  7.03          C

HETATM   25  C   MOL A   1       1.443  -1.365  -3.871  1.00  5.97          C

HETATM   26  C   MOL A   1       1.563   1.460   0.535  1.00  8.38          C

HETATM   27  C   MOL A   1       2.215   3.537  -3.181  1.00  6.39          C

HETATM   28  C   MOL A   1       2.840  -5.126   0.383  1.00  7.31          C

HETATM   29  C   MOL A   1       2.840   3.195   2.376  1.00  8.82          C

HETATM   30  C   MOL A   1       2.925   1.466  -2.939  1.00  6.54          C

HETATM   31  C   MOL A   1       2.977  -0.536   3.922  1.00  8.50          C

HETATM   32  C   MOL A   1       3.086   1.691   2.292  1.00  7.46          C

HETATM   33  C   MOL A   1       3.384   6.524   0.058  1.00  6.87          C

HETATM   34  C   MOL A   1       3.848  -4.189  -1.624  1.00  8.28          C

HETATM   35  C   MOL A   1       4.413  -2.836   3.694  1.00  8.54          C

HETATM   36  C   MOL A   1       4.810   6.441  -1.768  1.00  6.43          C

HETATM   37  C   MOL A   1       5.076   0.838  -3.800  1.00  7.74          C

HETATM   38  C   MOL A   1       5.201  -4.338   2.251  1.00  7.00          C

HETATM   39  C   MOL A   1       5.286   6.045   1.086  1.00  6.13          C

HETATM   40  C   MOL A   1       6.248   3.269  -3.460  1.00  5.89          C

HETATM   41  C   MOL A   1       6.629   0.813   4.077  1.00  6.22          C

HETATM   42  C   MOL A   1       7.420  -2.517  -0.507  1.00  7.69          C

HETATM   43  C   MOL A   1       7.462   3.543  -1.605  1.00  8.04          C

HETATM   44  C   MOL A   1       7.620  -1.701   1.426  1.00  6.27          C

HETATM   45  C   MOL A   1       7.881   3.274   2.504  1.00  6.86          C

HETATM   46  C   MOL A   1       8.127  -0.370  -1.141  1.00  7.42          C

HETATM   47  C   MOL A   1       8.209   0.416   0.766  1.00  5.57          C

HETATM    1  O   MOL A   1     -13.429   2.889   1.413  1.00 -1.90          O

HETATM    2  O   MOL A   1     -11.327  -0.290  -0.686  1.00 -0.44          O

HETATM    3  O   MOL A   1     -11.288   3.766   1.655  1.00 -1.52          O

HETATM    4  O   MOL A   1     -10.181   3.672   1.569  1.00 -1.19          O

HETATM    5  O   MOL A   1      -9.768   0.760   2.070  1.00  2.13          O

HETATM    6  O   MOL A   1      -9.536   0.662   1.991  1.00  2.12          O

HETATM    7  O   MOL A   1      -5.655  -2.822  -0.498  1.00-17.87          O

HETATM    8  O   MOL A   1      -5.199   0.625  -2.320  1.00-17.80          O

HETATM    9  O   MOL A   1      -2.779  -2.582  -3.563  1.00-40.34          O

HETATM   10  O   MOL A   1      -2.551   1.067   3.808  1.00  4.11          O

HETATM   11  O   MOL A   1       0.685  -0.610   3.712  1.00  4.00          O

HETATM   12  O   MOL A   1       1.436   5.296   0.000  1.00 -1.36          O

HETATM   13  O   MOL A   1       1.565   5.385  -0.534  1.00 -1.38          O

HETATM   14  O   MOL A   1       1.517   5.377  -0.383  1.00 -1.37          O

HETATM   15  O   MOL A   1       1.922   0.265  -3.074  1.00  1.14          O

HETATM   16  O   MOL A   1       1.949   2.088  -1.137  1.00  2.72          O

HETATM   17  O   MOL A   1       2.263   1.054   2.666  1.00  4.51          O

HETATM   18  O   MOL A   1       2.231   5.218  -1.416  1.00 -1.61          O

HETATM   19  O   MOL A   1       2.383   5.199  -1.510  1.00 -1.61          O

HETATM   20  O   MOL A   1       2.502  -4.695   2.721  1.00 -0.78          O

HETATM   21  O   MOL A   1       2.910   5.438  -2.233  1.00 -1.84          O

HETATM   22  O   MOL A   1       3.006   5.499  -2.474  1.00 -1.85          O

HETATM   23  O   MOL A   1       3.347   2.189   1.887  1.00  6.66          O

HETATM   24  O   MOL A   1       4.172   5.028  -3.695  1.00 -2.12          O

HETATM   25  O   MOL A   1       4.653   1.443   3.762  1.00  0.20          O

HETATM   26  O   MOL A   1       4.905  -1.401  -3.738  1.00 -0.56          O

HETATM   27  O   MOL A   1       5.072  -1.381  -3.648  1.00 -0.55          O

HETATM   28  O   MOL A   1       5.905   3.071   3.353  1.00 -0.40          O

HETATM   29  O   MOL A   1       5.920   3.270   3.311  1.00 -0.40          O

HETATM   30  O   MOL A   1       6.010  -4.630  -0.086  1.00 -1.18          O

HETATM   31  O   MOL A   1       6.394  -2.195   3.120  1.00  0.02          O

HETATM   32  O   MOL A   1       6.492   5.433  -0.490  1.00 -0.41          O

HETATM   33  O   MOL A   1       7.285  -0.606   0.536  1.00  3.65          O

HETATM   34  O   MOL A   1       7.518   0.918  -3.077  1.00 -1.22          O

END

Table SS 6. DOCHN of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -10.108  -5.291  -1.272  1.00  5.37          C

HETATM    2  C   MOL A   1      -9.157  -4.246   2.458  1.00  6.37          C

HETATM    3  C   MOL A   1      -9.000  -8.059   1.173  1.00  6.39          C

HETATM    4  C   MOL A   1      -8.458  -2.376   0.917  1.00  5.41          C

HETATM    5  C   MOL A   1      -7.370  -3.331  -2.919  1.00  5.42          C

HETATM    6  C   MOL A   1      -6.448  -6.935  -1.739  1.00  5.44          C

HETATM    7  C   MOL A   1      -6.288  -0.822   1.040  1.00  5.97          C

HETATM    8  C   MOL A   1      -5.647  -6.027   2.178  1.00  6.73          C

HETATM    9  C   MOL A   1      -5.312  -4.512   2.234  1.00  6.05          C

HETATM   10  C   MOL A   1      -5.302  -1.975  -2.820  1.00  5.70          C

HETATM   11  C   MOL A   1      -4.422  -5.476  -1.575  1.00  5.67          C

HETATM   12  C   MOL A   1      -4.326   0.751   0.946  1.00  7.34          C

HETATM   13  C   MOL A   1      -3.948   4.065   0.929  1.00 10.43          C

HETATM   14  C   MOL A   1      -4.017   6.367   1.002  1.00 10.53          C

HETATM   15  C   MOL A   1      -3.925   1.934  -0.177  1.00  8.27          C

HETATM   16  C   MOL A   1      -3.324  -2.852   2.407  1.00  6.23          C

HETATM   17  C   MOL A   1      -3.214  -0.528  -2.707  1.00  6.15          C

HETATM   18  C   MOL A   1      -2.278  -3.966  -1.410  1.00  6.26          C

HETATM   19  C   MOL A   1      -2.244   9.934   0.604  1.00 10.20          C

HETATM   20  C   MOL A   1      -1.802   0.968   2.751  1.00  7.31          C

HETATM   21  C   MOL A   1      -1.322  -1.178   2.590  1.00  6.88          C

HETATM   22  C   MOL A   1      -0.782   0.326  -2.748  1.00  5.54          C

HETATM   23  C   MOL A   1      -0.661   6.283  -1.668  1.00-16.12          C

HETATM   24  C   MOL A   1      -0.577   4.413  -1.663  1.00-15.42          C

HETATM   25  C   MOL A   1      -0.508  -2.896  -0.976  1.00  6.67          C

HETATM   26  C   MOL A   1       0.116   6.215   1.814  1.00-16.12          C

HETATM   27  C   MOL A   1       0.182   4.378   1.716  1.00-15.41          C

HETATM   28  C   MOL A   1       0.569  -2.865   0.756  1.00  6.68          C

HETATM   29  C   MOL A   1       0.605   0.273   2.622  1.00  5.54          C

HETATM   30  C   MOL A   1       1.253  -0.981  -2.770  1.00  6.88          C

HETATM   31  C   MOL A   1       1.435  10.088  -0.270  1.00 10.20          C

HETATM   32  C   MOL A   1       1.587   1.196  -2.844  1.00  7.31          C

HETATM   33  C   MOL A   1       2.471  -3.834   1.160  1.00  6.28          C

HETATM   34  C   MOL A   1       3.100  -0.423   2.550  1.00  6.16          C

HETATM   35  C   MOL A   1       3.429  -2.537  -2.653  1.00  6.20          C

HETATM   36  C   MOL A   1       3.471   6.706  -0.801  1.00 10.54          C

HETATM   37  C   MOL A   1       3.541   4.397  -0.886  1.00 10.43          C

HETATM   38  C   MOL A   1       3.659   2.232   0.119  1.00  8.27          C

HETATM   39  C   MOL A   1       4.138   1.088  -1.063  1.00  7.35          C

HETATM   40  C   MOL A   1       4.722  -5.217   1.236  1.00  5.73          C

HETATM   41  C   MOL A   1       5.268  -1.650   2.597  1.00  5.75          C

HETATM   42  C   MOL A   1       5.649  -3.881  -2.587  1.00  5.72          C

HETATM   43  C   MOL A   1       6.202  -0.339  -1.221  1.00  6.03          C

HETATM   44  C   MOL A   1       6.858  -6.569   1.244  1.00  5.52          C

HETATM   45  C   MOL A   1       7.528  -3.040   2.668  1.00  5.45          C

HETATM   46  C   MOL A   1       7.789  -5.231  -2.513  1.00  5.52          C

HETATM   47  C   MOL A   1       8.423  -1.692  -1.142  1.00  5.51          C

HETATM   48  C   MOL A   1       9.764  -4.362   2.710  1.00  6.26          C

HETATM   49  C   MOL A   1      10.501  -7.015  -0.232  1.00  6.30          C

HETATM   50  C   MOL A   1      10.662  -3.076  -1.057  1.00  6.27          C

HETATM    1  O   MOL A   1      -9.734  -6.178   1.876  1.00 -1.74          O

HETATM    2  O   MOL A   1      -8.565  -6.690  -1.733  1.00 -1.60          O

HETATM    3  O   MOL A   1      -8.167  -6.496   2.879  1.00 -2.10          O

HETATM    4  O   MOL A   1      -7.695  -2.086  -1.142  1.00 -1.89          O

HETATM    5  O   MOL A   1      -6.962  -7.643   1.557  1.00 -1.57          O

HETATM    6  O   MOL A   1      -7.038  -7.610   1.799  1.00 -1.56          O

HETATM    7  O   MOL A   1      -6.882  -7.628   1.309  1.00 -1.58          O

HETATM    8  O   MOL A   1      -6.769  -1.575  -1.108  1.00 -1.74          O

HETATM    9  O   MOL A   1      -4.027  -4.825   0.524  1.00 -1.31          O

HETATM   10  O   MOL A   1      -3.323  -4.293   0.598  1.00 -1.23          O

HETATM   11  O   MOL A   1      -1.311   4.152  -1.678  1.00-16.55          O

HETATM   12  O   MOL A   1      -1.187   7.117  -1.657  1.00-18.30          O

HETATM   13  O   MOL A   1      -0.433  -1.085  -1.830  1.00  2.64          O

HETATM   14  O   MOL A   1      -0.382   4.215   2.016  1.00-16.26          O

HETATM   15  O   MOL A   1      -0.303   7.152  -1.860  1.00-18.28          O

HETATM   16  O   MOL A   1      -0.289   7.079   2.040  1.00-18.28          O

HETATM   17  O   MOL A   1      -0.068   4.295  -1.941  1.00-16.26          O

HETATM   18  O   MOL A   1       0.435  -1.099   1.664  1.00  2.65          O

HETATM   19  O   MOL A   1       0.598   7.077   1.833  1.00-18.30          O

HETATM   20  O   MOL A   1       0.902   4.145   1.723  1.00-16.55          O

HETATM   21  O   MOL A   1       2.823   2.336  -1.698  1.00  2.29          O

HETATM   22  O   MOL A   1       3.534  -4.031  -0.887  1.00 -1.33          O

HETATM   23  O   MOL A   1       4.748  -5.026  -0.942  1.00 -1.65          O

HETATM   24  O   MOL A   1       5.483  -5.342  -0.860  1.00 -1.73          O

HETATM   25  O   MOL A   1       6.519  -5.945  -0.833  1.00 -1.72          O

HETATM   26  O   MOL A   1       6.677  -6.137  -0.861  1.00 -1.72          O

HETATM   27  O   MOL A   1       6.680  -1.023   0.915  1.00 -1.69          O

HETATM   28  O   MOL A   1       8.814  -2.296   0.990  1.00 -2.04          O

HETATM   29  O   MOL A   1       9.779  -2.937   0.995  1.00 -2.16          O

HETATM   30  O   MOL A   1      11.367  -4.753   0.756  1.00 -2.36          O

END

Table SS 7. PHPN of local minima and maxima on the Electrostatic potentials (ESP) surface

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -12.592  -1.781   0.073  1.00  7.37          C

HETATM    2  C   MOL A   1     -10.881   1.489   1.411  1.00  8.38          C

HETATM    3  C   MOL A   1     -10.682   1.260  -2.030  1.00  9.45          C

HETATM    4  C   MOL A   1     -10.391   2.636   1.499  1.00  9.13          C

HETATM    5  C   MOL A   1      -9.551  -2.373   2.335  1.00  7.54          C

HETATM    6  C   MOL A   1      -9.232  -3.350  -1.044  1.00  5.22          C

HETATM    7  C   MOL A   1      -7.911   4.169  -1.435  1.00  9.42          C

HETATM    8  C   MOL A   1      -7.663  -3.167   1.704  1.00  9.53          C

HETATM    9  C   MOL A   1      -6.765  -0.471  -1.439  1.00-16.67          C

HETATM   10  C   MOL A   1      -6.514   0.883   1.740  1.00-16.83          C

HETATM   11  C   MOL A   1      -5.999   3.700  -1.396  1.00  9.74          C

HETATM   12  C   MOL A   1      -5.255  -3.740   1.654  1.00  9.27          C

HETATM   13  C   MOL A   1      -4.780  -0.875  -1.449  1.00-16.90          C

HETATM   14  C   MOL A   1      -4.508   0.419   1.770  1.00-17.01          C

HETATM   15  C   MOL A   1      -3.657   3.180  -1.431  1.00 10.31          C

HETATM   16  C   MOL A   1      -3.027  -4.516   0.546  1.00  7.51          C

HETATM   17  C   MOL A   1      -1.526  -2.220   3.147  1.00  6.83          C

HETATM   18  C   MOL A   1      -1.138   0.161  -2.893  1.00  5.58          C

HETATM   19  C   MOL A   1      -1.129   2.465   2.197  1.00  4.27          C

HETATM   20  C   MOL A   1      -0.957  -2.354  -2.385  1.00  5.57          C

HETATM   21  C   MOL A   1      -0.329  -0.073   2.683  1.00  5.06          C

HETATM   22  C   MOL A   1       0.094   1.930  -3.152  1.00  5.78          C

HETATM   23  C   MOL A   1       0.619   4.675  -0.090  1.00  5.84          C

HETATM   24  C   MOL A   1       0.783  -3.548   0.717  1.00  7.89          C

HETATM   25  C   MOL A   1       0.878  -0.538  -2.769  1.00  5.59          C

HETATM   26  C   MOL A   1       1.167   1.749   2.427  1.00  5.18          C

HETATM   27  C   MOL A   1       1.575  -3.414  -0.009  1.00  7.95          C

HETATM   28  C   MOL A   1       1.956  -0.635   2.816  1.00  6.53          C

HETATM   29  C   MOL A   1       2.454   1.358  -3.023  1.00  5.01          C

HETATM   30  C   MOL A   1       2.947   4.159   0.006  1.00  5.43          C

HETATM   31  C   MOL A   1       3.310  -1.694  -2.344  1.00  5.66          C

HETATM   32  C   MOL A   1       3.466  -3.759  -0.015  1.00  7.74          C

HETATM   33  C   MOL A   1       3.810   1.125   2.542  1.00  6.18          C

HETATM   34  C   MOL A   1       4.339  -3.170  -2.482  1.00 10.63          C

HETATM   35  C   MOL A   1       4.542  -0.851   2.883  1.00  8.06          C

HETATM   36  C   MOL A   1       5.488   2.157  -0.783  1.00  0.85          C

HETATM   37  C   MOL A   1       6.349   0.244   2.850  1.00 10.27          C

HETATM   38  C   MOL A   1       7.054   2.712   1.346  1.00  5.31          C

HETATM   39  C   MOL A   1       7.947  -2.821  -4.026  1.00 10.45          C

HETATM   40  C   MOL A   1       8.570   0.247   3.257  1.00  7.92          C

HETATM   41  C   MOL A   1       9.757   2.293   3.692  1.00  7.56          C

HETATM   42  C   MOL A   1       9.908   1.998  -1.821  1.00  5.18          C

HETATM   43  C   MOL A   1      10.144   4.914   0.623  1.00  7.14          C

HETATM   44  C   MOL A   1      10.689  -0.869  -2.006  1.00 10.40          C

HETATM   45  C   MOL A   1      11.371  -0.532   0.073  1.00  7.86          C

HETATM   46  C   MOL A   1      12.428   1.596   0.692  1.00  7.52          C

HETATM    1  O   MOL A   1     -10.014   3.835  -0.474  1.00  1.11          O

HETATM    2  O   MOL A   1      -7.142  -1.016  -1.344  1.00-17.56          O

HETATM    3  O   MOL A   1      -6.916   0.086  -1.835  1.00-17.77          O

HETATM    4  O   MOL A   1      -6.929   0.482   2.131  1.00-17.83          O

HETATM    5  O   MOL A   1      -6.611   1.590   1.633  1.00-17.85          O

HETATM    6  O   MOL A   1      -4.669  -1.562  -1.327  1.00-17.88          O

HETATM    7  O   MOL A   1      -4.440  -0.546  -1.752  1.00-17.49          O

HETATM    8  O   MOL A   1      -4.382  -0.077   2.129  1.00-17.80          O

HETATM    9  O   MOL A   1      -4.061   1.038   1.651  1.00-18.07          O

HETATM   10  O   MOL A   1      -2.604  -3.629   2.228  1.00  1.08          O

HETATM   11  O   MOL A   1      -0.559  -3.644  -0.884  1.00  0.28          O

HETATM   12  O   MOL A   1      -0.418   1.431   1.953  1.00  2.23          O

HETATM   13  O   MOL A   1       0.015   0.740  -2.517  1.00  3.36          O

HETATM   14  O   MOL A   1       0.791   0.329   2.142  1.00  3.39          O

HETATM   15  O   MOL A   1       1.260   1.039  -2.473  1.00  3.01          O

HETATM   16  O   MOL A   1       2.295  -2.414   1.740  1.00  0.42          O

HETATM   17  O   MOL A   1       2.307   0.811   2.072  1.00  2.85          O

HETATM   18  O   MOL A   1       2.434   0.160  -2.341  1.00  2.43          O

HETATM   19  O   MOL A   1       3.724   2.866  -1.798  1.00 -2.34          O

HETATM   20  O   MOL A   1       6.812   0.148  -1.920  1.00-17.53          O

HETATM   21  O   MOL A   1       7.759  -3.008  -0.195  1.00-18.20          O

HETATM   22  O   MOL A   1      11.543   3.541   2.200  1.00 -1.28          O

END

Table SS 8. Squalane of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -15.523   0.077   1.146  1.00  5.91          C

HETATM    2  C   MOL A   1     -15.328  -2.167   1.382  1.00  5.83          C

HETATM    3  C   MOL A   1     -13.809   0.101  -2.550  1.00  5.63          C

HETATM    4  C   MOL A   1     -13.620  -2.543  -2.269  1.00  5.49          C

HETATM    5  C   MOL A   1     -12.450   2.533   0.261  1.00  6.08          C

HETATM    6  C   MOL A   1     -11.922  -0.623   2.767  1.00  4.57          C

HETATM    7  C   MOL A   1     -11.725  -4.044   0.987  1.00  5.82          C

HETATM    8  C   MOL A   1     -11.600  -1.054  -2.825  1.00  4.44          C

HETATM    9  C   MOL A   1     -11.358   2.455  -0.955  1.00  5.37          C

HETATM   10  C   MOL A   1     -10.283  -3.008   0.520  1.00  3.81          C

HETATM   11  C   MOL A   1     -10.049   0.719   2.336  1.00  5.09          C

HETATM   12  C   MOL A   1      -9.966  -1.589   2.179  1.00  6.21          C

HETATM   13  C   MOL A   1      -8.798  -1.284  -2.677  1.00  4.22          C

HETATM   14  C   MOL A   1      -8.321   2.589  -1.643  1.00  5.01          C

HETATM   15  C   MOL A   1      -7.929  -3.220  -0.880  1.00  5.77          C

HETATM   16  C   MOL A   1      -7.690   1.703   1.980  1.00  4.28          C

HETATM   17  C   MOL A   1      -6.304  -1.794  -2.232  1.00  4.51          C

HETATM   18  C   MOL A   1      -6.308   2.326  -1.555  1.00  4.74          C

HETATM   19  C   MOL A   1      -5.993  -2.056   2.340  1.00  6.57          C

HETATM   20  C   MOL A   1      -5.230   1.713   2.090  1.00  4.90          C

HETATM   21  C   MOL A   1      -5.046  -2.152   1.711  1.00  6.29          C

HETATM   22  C   MOL A   1      -4.167  -1.983   2.407  1.00  6.56          C

HETATM   23  C   MOL A   1      -3.919   2.403  -1.534  1.00  4.76          C

HETATM   24  C   MOL A   1      -3.559  -1.679  -2.123  1.00  4.51          C

HETATM   25  C   MOL A   1      -2.790   1.939   2.136  1.00  4.29          C

HETATM   26  C   MOL A   1      -1.938  -2.907  -0.725  1.00  5.77          C

HETATM   27  C   MOL A   1      -1.951   2.781  -1.548  1.00  4.85          C

HETATM   28  C   MOL A   1      -0.868  -1.127  -2.208  1.00  4.59          C

HETATM   29  C   MOL A   1      -0.470   2.524   2.081  1.00  4.84          C

HETATM   30  C   MOL A   1      -0.157  -1.294   2.405  1.00  6.11          C

HETATM   31  C   MOL A   1       0.425   3.532  -1.793  1.00  5.53          C

HETATM   32  C   MOL A   1       0.817  -1.186   1.448  1.00  5.49          C

HETATM   33  C   MOL A   1       1.203   3.800  -2.517  1.00  6.15          C

HETATM   34  C   MOL A   1       1.543  -0.236  -2.424  1.00  4.78          C

HETATM   35  C   MOL A   1       2.086   3.397   1.906  1.00  4.71          C

HETATM   36  C   MOL A   1       3.134   5.173   0.608  1.00  5.67          C

HETATM   37  C   MOL A   1       3.710  -0.610   1.461  1.00  5.79          C

HETATM   38  C   MOL A   1       3.895   0.616  -2.682  1.00  4.25          C

HETATM   39  C   MOL A   1       4.617   3.398   2.167  1.00  4.61          C

HETATM   40  C   MOL A   1       5.258   4.198  -2.733  1.00  6.06          C

HETATM   41  C   MOL A   1       5.893  -0.339  -1.910  1.00  4.88          C

HETATM   42  C   MOL A   1       6.380   1.666   3.371  1.00  4.46          C

HETATM   43  C   MOL A   1       6.418   3.369  -1.555  1.00  4.87          C

HETATM   44  C   MOL A   1       6.455   4.445   0.750  1.00  4.18          C

HETATM   45  C   MOL A   1       7.212  -1.791   1.343  1.00  5.44          C

HETATM   46  C   MOL A   1       7.408  -2.229   0.356  1.00  5.87          C

HETATM   47  C   MOL A   1       7.472  -3.027  -0.850  1.00  6.39          C

HETATM   48  C   MOL A   1       7.727   1.503  -2.031  1.00  4.52          C

HETATM   49  C   MOL A   1       8.852   2.701   3.368  1.00  5.33          C

HETATM   50  C   MOL A   1       9.249  -0.164  -2.560  1.00  5.08          C

HETATM   51  C   MOL A   1       9.569  -0.006   3.082  1.00  4.38          C

HETATM   52  C   MOL A   1       9.859  -4.536   1.919  1.00  5.85          C

HETATM   53  C   MOL A   1      10.201  -5.851  -1.934  1.00  6.07          C

HETATM   54  C   MOL A   1      10.117   3.805  -0.358  1.00  5.66          C

HETATM   55  C   MOL A   1      10.669  -2.138  -3.146  1.00  4.54          C

HETATM   56  C   MOL A   1      10.746  -2.306   2.498  1.00  4.72          C

HETATM   57  C   MOL A   1      11.284   1.891  -0.128  1.00  4.61          C

HETATM   58  C   MOL A   1      12.469  -5.413  -2.049  1.00  5.97          C

HETATM   59  C   MOL A   1      12.474  -4.133   1.825  1.00  5.62          C

HETATM   60  C   MOL A   1      12.610  -0.100  -0.452  1.00  4.80          C

HETATM   61  C   MOL A   1      13.932  -1.745  -1.147  1.00  5.98          C

HETATM    1  O   MOL A   1     -14.959  -0.786  -0.830  1.00 -2.74          O

HETATM    2  O   MOL A   1     -14.873  -1.581  -0.739  1.00 -2.72          O

HETATM    3  O   MOL A   1     -14.729   1.505  -0.756  1.00 -2.75          O

HETATM    4  O   MOL A   1     -14.061  -3.895  -0.165  1.00 -2.94          O

HETATM    5  O   MOL A   1     -14.030   1.568   1.345  1.00 -2.03          O

HETATM    6  O   MOL A   1     -12.892  -1.180  -2.005  1.00  1.85          O

HETATM    7  O   MOL A   1     -11.837  -3.101  -1.079  1.00 -2.75          O

HETATM    8  O   MOL A   1     -11.181  -2.660  -1.352  1.00 -2.72          O

HETATM    9  O   MOL A   1     -10.388   2.188   0.821  1.00 -1.48          O

HETATM   10  O   MOL A   1      -8.008  -3.221   1.541  1.00 -2.38          O

HETATM   11  O   MOL A   1      -8.004  -1.281   2.867  1.00 -1.54          O

HETATM   12  O   MOL A   1      -7.743  -1.642  -1.615  1.00  1.54          O

HETATM   13  O   MOL A   1      -7.713   0.550  -2.470  1.00 -2.69          O

HETATM   14  O   MOL A   1      -6.689   0.328  -2.557  1.00 -2.83          O

HETATM   15  O   MOL A   1      -6.262   1.870   0.345  1.00  0.52          O

HETATM   16  O   MOL A   1      -5.485   0.312  -2.384  1.00 -2.96          O

HETATM   17  O   MOL A   1      -5.062  -0.328   2.398  1.00 -1.08          O

HETATM   18  O   MOL A   1      -4.504   0.389  -2.351  1.00 -2.96          O

HETATM   19  O   MOL A   1      -4.034   1.975   0.417  1.00  0.51          O

HETATM   20  O   MOL A   1      -3.227   0.487  -2.399  1.00 -2.85          O

HETATM   21  O   MOL A   1      -2.258  -1.400  -1.453  1.00  1.74          O

HETATM   22  O   MOL A   1      -2.279  -0.889   3.042  1.00 -1.95          O

HETATM   23  O   MOL A   1      -2.125   0.706  -2.353  1.00 -2.80          O

HETATM   24  O   MOL A   1      -1.871  -2.930   1.789  1.00 -2.60          O

HETATM   25  O   MOL A   1      -1.639   2.414   0.413  1.00  0.54          O

HETATM   26  O   MOL A   1      -1.179   0.986  -2.507  1.00 -2.73          O

HETATM   27  O   MOL A   1      -1.004   1.026  -2.472  1.00 -2.74          O

HETATM   28  O   MOL A   1       1.857   1.191   2.034  1.00 -2.34          O

HETATM   29  O   MOL A   1       3.124   5.394  -1.871  1.00 -2.77          O

HETATM   30  O   MOL A   1       3.275   3.564  -3.313  1.00 -2.07          O

HETATM   31  O   MOL A   1       3.453   3.660   1.151  1.00  1.81          O

HETATM   32  O   MOL A   1       4.434  -0.838  -0.482  1.00 -1.62          O

HETATM   33  O   MOL A   1       4.731   5.001  -0.747  1.00 -2.33          O

HETATM   34  O   MOL A   1       5.426   1.725  -1.908  1.00  0.82          O

HETATM   35  O   MOL A   1       5.584   1.645  -1.829  1.00  0.82          O

HETATM   36  O   MOL A   1       5.822   1.566  -1.747  1.00  0.82          O

HETATM   37  O   MOL A   1       7.172  -0.163   2.969  1.00 -1.94          O

HETATM   38  O   MOL A   1       7.754  -1.025  -1.370  1.00 -1.28          O

HETATM   39  O   MOL A   1       8.616  -5.378  -0.036  1.00 -2.55          O

HETATM   40  O   MOL A   1       8.557   4.554   1.656  1.00 -3.11          O

HETATM   41  O   MOL A   1       8.659  -4.376  -2.120  1.00 -1.85          O

HETATM   42  O   MOL A   1       9.791   1.217  -1.205  1.00  0.62          O

HETATM   43  O   MOL A   1      10.181   2.850   1.693  1.00 -2.86          O

HETATM   44  O   MOL A   1      10.943  -5.403   0.176  1.00 -2.55          O

HETATM   45  O   MOL A   1      11.064  -3.495   1.550  1.00  2.13          O

HETATM   46  O   MOL A   1      11.045  -0.482  -1.582  1.00  0.63          O

HETATM   47  O   MOL A   1      11.114   0.622   1.686  1.00 -2.93          O

HETATM   48  O   MOL A   1      11.583  -0.436   1.541  1.00 -2.85          O

HETATM   49  O   MOL A   1      11.730  -5.290   0.112  1.00 -2.56          O

HETATM   50  O   MOL A   1      13.006  -2.228   0.866  1.00 -2.64          O

HETATM   51  O   MOL A   1      13.960  -4.251  -0.244  1.00 -2.82          O

END

Table SS 9. Hopane of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1      -9.734   1.875   1.604  1.00  5.18          C

HETATM    2  C   MOL A   1      -9.642   0.695  -1.168  1.00  4.79          C

HETATM    3  C   MOL A   1      -9.601   2.659  -0.396  1.00  5.65          C

HETATM    4  C   MOL A   1      -7.959  -2.619  -2.195  1.00  5.23          C

HETATM    5  C   MOL A   1      -7.703  -1.395   2.156  1.00  6.46          C

HETATM    6  C   MOL A   1      -7.169  -0.163   3.505  1.00  4.38          C

HETATM    7  C   MOL A   1      -6.487   1.909  -2.885  1.00  6.59          C

HETATM    8  C   MOL A   1      -6.262   3.750   2.468  1.00  5.58          C

HETATM    9  C   MOL A   1      -5.946  -3.563   0.409  1.00  4.47          C

HETATM   10  C   MOL A   1      -5.932   4.489   0.171  1.00  6.68          C

HETATM   11  C   MOL A   1      -4.730   0.373  -2.984  1.00  7.41          C

HETATM   12  C   MOL A   1      -4.263  -3.373   2.321  1.00  6.70          C

HETATM   13  C   MOL A   1      -4.295   0.436   3.738  1.00  5.51          C

HETATM   14  C   MOL A   1      -4.194   2.264   2.390  1.00  3.89          C

HETATM   15  C   MOL A   1      -2.196   2.909   1.842  1.00  7.03          C

HETATM   16  C   MOL A   1      -1.944  -2.710  -2.196  1.00  7.48          C

HETATM   17  C   MOL A   1      -1.890   3.059  -2.362  1.00  4.49          C

HETATM   18  C   MOL A   1      -1.028  -0.829   3.312  1.00  6.94          C

HETATM   19  C   MOL A   1      -0.733   0.876  -3.480  1.00  7.28          C

HETATM   20  C   MOL A   1      -0.511  -4.532   0.665  1.00  4.39          C

HETATM   21  C   MOL A   1      -0.304   3.602  -0.387  1.00  4.48          C

HETATM   22  C   MOL A   1       0.102  -1.841   3.303  1.00  6.15          C

HETATM   23  C   MOL A   1       0.616  -3.431  -2.411  1.00  5.53          C

HETATM   24  C   MOL A   1       0.856  -1.265  -3.122  1.00  4.30          C

HETATM   25  C   MOL A   1       1.540  -4.564   1.378  1.00  5.15          C

HETATM   26  C   MOL A   1       1.946   1.479   2.002  1.00  7.86          C

HETATM   27  C   MOL A   1       2.941   2.543  -2.410  1.00  6.01          C

HETATM   28  C   MOL A   1       3.191  -1.546  -3.809  1.00  4.08          C

HETATM   29  C   MOL A   1       4.083  -2.251   1.924  1.00  6.58          C

HETATM   30  C   MOL A   1       4.204  -4.182  -2.298  1.00  5.43          C

HETATM   31  C   MOL A   1       4.309   2.664   0.489  1.00  4.03          C

HETATM   32  C   MOL A   1       4.805  -0.334  -4.426  1.00  5.28          C

HETATM   33  C   MOL A   1       6.202   0.986   3.261  1.00  4.28          C

HETATM   34  C   MOL A   1       6.446  -2.087  -1.492  1.00  3.58          C

HETATM   35  C   MOL A   1       6.751  -2.365   1.037  1.00  4.55          C

HETATM   36  C   MOL A   1       6.928   3.250   0.028  1.00  4.54          C

HETATM   37  C   MOL A   1       7.121   1.824  -2.369  1.00  3.58          C

HETATM   38  C   MOL A   1       7.898  -0.162  -2.019  1.00  4.74          C

HETATM   39  C   MOL A   1       8.530   1.739   3.216  1.00  4.62          C

HETATM   40  C   MOL A   1       9.309   3.824   0.077  1.00  4.80          C

HETATM   41  C   MOL A   1       9.395  -1.705   1.127  1.00  4.66          C

HETATM   42  C   MOL A   1      10.163   0.403  -2.010  1.00  4.88          C

HETATM   43  C   MOL A   1      11.035   2.341   3.236  1.00  5.71          C

HETATM   44  C   MOL A   1      11.932  -1.068   1.207  1.00  5.72          C

HETATM   45  C   MOL A   1      13.038   2.505  -0.226  1.00  5.81          C

HETATM    1  O   MOL A   1      -9.344  -0.353   0.597  1.00 -1.90          O

HETATM    2  O   MOL A   1      -8.222   3.396   1.610  1.00 -2.96          O

HETATM    3  O   MOL A   1      -8.074   2.252   3.391  1.00 -3.17          O

HETATM    4  O   MOL A   1      -7.817   3.852  -1.649  1.00 -2.64          O

HETATM    5  O   MOL A   1      -7.494  -0.737  -3.059  1.00 -1.56          O

HETATM    6  O   MOL A   1      -5.284  -1.700   3.742  1.00 -2.44          O

HETATM    7  O   MOL A   1      -4.909  -3.224  -1.342  1.00 -1.90          O

HETATM    8  O   MOL A   1      -4.503   2.904  -2.374  1.00 -1.43          O

HETATM    9  O   MOL A   1      -4.322   3.150   0.825  1.00  1.46          O

HETATM   10  O   MOL A   1      -3.987  -3.528   0.153  1.00 -2.01          O

HETATM   11  O   MOL A   1      -3.160   1.389   2.071  1.00  1.70          O

HETATM   12  O   MOL A   1      -2.559  -0.791  -3.759  1.00 -1.77          O

HETATM   13  O   MOL A   1      -2.218   3.656  -0.424  1.00 -1.39          O

HETATM   14  O   MOL A   1      -0.993  -3.528   2.347  1.00 -1.63          O

HETATM   15  O   MOL A   1      -0.432   1.643   3.215  1.00 -2.46          O

HETATM   16  O   MOL A   1       0.018   2.742  -2.210  1.00 -1.26          O

HETATM   17  O   MOL A   1       0.809  -0.044   3.100  1.00 -2.53          O

HETATM   18  O   MOL A   1       2.236  -0.833   3.410  1.00 -2.55          O

HETATM   19  O   MOL A   1       2.232   2.879  -0.469  1.00 -1.36          O

HETATM   20  O   MOL A   1       3.001  -4.518  -0.305  1.00 -2.45          O

HETATM   21  O   MOL A   1       4.032   1.155   1.918  1.00 -1.74          O

HETATM   22  O   MOL A   1       4.706  -2.307  -2.418  1.00 -0.13          O

HETATM   23  O   MOL A   1       5.326   1.997  -3.559  1.00 -3.38          O

HETATM   24  O   MOL A   1       7.332  -0.741   2.486  1.00 -2.93          O

HETATM   25  O   MOL A   1       7.330  -1.232  -0.465  1.00  0.32          O

HETATM   26  O   MOL A   1       8.278  -0.432   2.583  1.00 -2.87          O

HETATM   27  O   MOL A   1       8.754   2.699   1.556  1.00  0.37          O

HETATM   28  O   MOL A   1       9.186   2.267  -1.461  1.00 -2.36          O

HETATM   29  O   MOL A   1       9.507  -0.155   2.671  1.00 -2.83          O

HETATM   30  O   MOL A   1      10.041  -0.569  -0.293  1.00  0.47          O

HETATM   31  O   MOL A   1      10.695   0.203   2.589  1.00 -2.81          O

HETATM   32  O   MOL A   1      12.909   1.170   1.946  1.00 -2.85          O

END

Table SS 10. Phenol of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -11.056  -2.123   1.402  1.00  8.43          C

HETATM    2  C   MOL A   1     -10.090  -4.343   1.013  1.00  9.02          C

HETATM    3  C   MOL A   1      -8.820   2.561  -0.000  1.00  8.05          C

HETATM    4  C   MOL A   1      -8.587  -0.378  -1.381  1.00  8.99          C

HETATM    5  C   MOL A   1      -8.596   1.102   2.203  1.00  8.64          C

HETATM    6  C   MOL A   1      -8.233  -2.649   3.797  1.00  6.51          C

HETATM    7  C   MOL A   1      -7.627   0.589  -0.971  1.00  8.82          C

HETATM    8  C   MOL A   1      -7.477   4.383  -3.371  1.00  7.21          C

HETATM    9  C   MOL A   1      -7.454   1.380   1.418  1.00  8.26          C

HETATM   10  C   MOL A   1      -7.064  -3.070  -1.676  1.00 10.41          C

HETATM   11  C   MOL A   1      -6.873   0.660   2.606  1.00  6.25          C

HETATM   12  C   MOL A   1      -6.045   5.481   0.294  1.00  7.87          C

HETATM   13  C   MOL A   1      -5.843  -4.579   0.561  1.00 15.66          C

HETATM   14  C   MOL A   1      -4.626  -5.376  -0.343  1.00 50.00          C

HETATM   15  C   MOL A   1      -4.226   3.991   1.168  1.00  8.62          C

HETATM   16  C   MOL A   1      -3.938   3.948  -1.980  1.00  4.57          C

HETATM   17  C   MOL A   1      -3.116  -0.220   1.784  1.00-15.87          C

HETATM   18  C   MOL A   1      -3.095   0.107  -1.673  1.00-15.93          C

HETATM   19  C   MOL A   1      -2.304   4.030   0.657  1.00 13.43          C

HETATM   20  C   MOL A   1      -2.223  -2.197   1.575  1.00-14.89          C

HETATM   21  C   MOL A   1      -2.229  -1.882  -1.847  1.00-14.77          C

HETATM   22  C   MOL A   1      -1.431   6.283  -0.364  1.00  6.98          C

HETATM   23  C   MOL A   1      -0.847   5.423   1.495  1.00  8.16          C

HETATM   24  C   MOL A   1      -0.694   0.045  -1.650  1.00-11.34          C

HETATM   25  C   MOL A   1      -0.600  -0.451   1.691  1.00-11.41          C

HETATM   26  C   MOL A   1      -0.257   3.428  -2.727  1.00 -0.78          C

HETATM   27  C   MOL A   1       0.152   7.893   0.942  1.00  7.01          C

HETATM   28  C   MOL A   1       0.896   1.952  -1.409  1.00-15.18          C

HETATM   29  C   MOL A   1       0.951   1.296   1.973  1.00-15.86          C

HETATM   30  C   MOL A   1       1.093  -4.363  -0.653  1.00 12.03          C

HETATM   31  C   MOL A   1       1.260   6.692  -3.501  1.00  5.79          C

HETATM   32  C   MOL A   1       1.729   0.019  -1.784  1.00-15.39          C

HETATM   33  C   MOL A   1       1.904  -0.601   1.646  1.00-15.25          C

HETATM   34  C   MOL A   1       2.703   8.048  -2.239  1.00  6.76          C

HETATM   35  C   MOL A   1       3.448   4.905   2.008  1.00  7.70          C

HETATM   36  C   MOL A   1       3.887   4.428  -1.009  1.00  5.15          C

HETATM   37  C   MOL A   1       3.996   6.629   1.366  1.00  7.51          C

HETATM   38  C   MOL A   1       4.218  -4.236   0.939  1.00  5.76          C

HETATM   39  C   MOL A   1       4.268  -5.376  -4.384  1.00  6.22          C

HETATM   40  C   MOL A   1       4.208  -1.559  -3.900  1.00  3.71          C

HETATM   41  C   MOL A   1       4.372   3.364   0.627  1.00 10.77          C

HETATM   42  C   MOL A   1       4.925  -5.775  -0.397  1.00  6.80          C

HETATM   43  C   MOL A   1       5.411  -1.721   2.638  1.00  4.20          C

HETATM   44  C   MOL A   1       5.475   1.851  -1.715  1.00  6.88          C

HETATM   45  C   MOL A   1       6.015  -0.491  -2.792  1.00  5.79          C

HETATM   46  C   MOL A   1       6.753   1.940   2.056  1.00  6.49          C

HETATM   47  C   MOL A   1       7.168  -3.362  -2.540  1.00  7.25          C

HETATM   48  C   MOL A   1       7.342  -3.309  -0.569  1.00  7.55          C

HETATM   49  C   MOL A   1       7.446  -1.807   3.301  1.00  5.62          C

HETATM   50  C   MOL A   1       7.624   0.824  -1.750  1.00  6.34          C

HETATM   51  C   MOL A   1       8.015  -2.951  -0.529  1.00  7.26          C

HETATM   52  C   MOL A   1       9.200   1.603   2.734  1.00  5.88          C

HETATM   53  C   MOL A   1       9.840  -2.118   3.919  1.00  6.40          C

HETATM   54  C   MOL A   1      10.144   0.494  -1.072  1.00  5.95          C

HETATM   55  C   MOL A   1      10.698  -3.180   0.115  1.00  6.70          C

HETATM   56  C   MOL A   1      12.709  -0.119   1.905  1.00  6.54          C

HETATM    1  O   MOL A   1     -10.401   0.144   0.820  1.00 -0.09          O

HETATM    2  O   MOL A   1     -10.443   0.142   1.032  1.00 -0.07          O

HETATM    3  O   MOL A   1     -10.362   0.105   0.581  1.00 -0.09          O

HETATM    4  O   MOL A   1      -9.427  -2.899  -0.559  1.00  1.03          O

HETATM    5  O   MOL A   1      -8.252  -4.803   1.965  1.00  1.49          O

HETATM    6  O   MOL A   1      -8.172   5.024  -1.121  1.00 -1.02          O

HETATM    7  O   MOL A   1      -6.763   5.559  -1.767  1.00 -0.69          O

HETATM    8  O   MOL A   1      -6.446   5.474  -1.847  1.00 -0.69          O

HETATM    9  O   MOL A   1      -2.980  -1.959  -2.039  1.00-16.09          O

HETATM   10  O   MOL A   1      -2.901  -2.257   1.771  1.00-16.06          O

HETATM   11  O   MOL A   1      -2.696   0.585   2.061  1.00-17.79          O

HETATM   12  O   MOL A   1      -2.637   0.972  -1.785  1.00-17.85          O

HETATM   13  O   MOL A   1      -1.338  -2.185  -2.137  1.00-16.90          O

HETATM   14  O   MOL A   1      -1.278  -6.069  -0.242  1.00-26.17          O

HETATM   15  O   MOL A   1      -1.213  -2.523   1.781  1.00-17.40          O

HETATM   16  O   MOL A   1       0.175   1.551   2.236  1.00-17.44          O

HETATM   17  O   MOL A   1       0.146   1.846  -1.616  1.00-16.08          O

HETATM   18  O   MOL A   1       1.113  -0.845  -2.147  1.00-17.60          O

HETATM   19  O   MOL A   1       1.101   0.339   2.037  1.00-16.51          O

HETATM   20  O   MOL A   1       1.043   0.820  -1.839  1.00-16.33          O

HETATM   21  O   MOL A   1       1.188   4.300  -3.139  1.00 -4.50          O

HETATM   22  O   MOL A   1       1.338   1.766   2.191  1.00-16.90          O

HETATM   23  O   MOL A   1       1.381  -1.466   1.688  1.00-17.09          O

HETATM   24  O   MOL A   1       1.538   2.105  -1.569  1.00-16.12          O

HETATM   25  O   MOL A   1       2.335   8.713   0.082  1.00 -1.71          O

HETATM   26  O   MOL A   1       4.290  -6.165  -2.391  1.00 -1.59          O

HETATM   27  O   MOL A   1       5.713  -3.864  -4.103  1.00 -1.40          O

HETATM   28  O   MOL A   1       5.826  -5.814  -2.678  1.00 -1.81          O

HETATM   29  O   MOL A   1       6.024  -4.416  -3.972  1.00 -1.34          O

HETATM   30  O   MOL A   1       6.409   0.225  -1.839  1.00  4.24          O

HETATM   31  O   MOL A   1       7.062  -0.019   2.641  1.00  1.89          O

HETATM   32  O   MOL A   1       7.187  -1.659  -1.760  1.00  0.74          O

HETATM   33  O   MOL A   1       8.225   1.609   0.285  1.00 -0.88          O

HETATM   34  O   MOL A   1       9.779  -3.144   2.054  1.00 -1.67          O

HETATM   35  O   MOL A   1       9.824   1.656   0.701  1.00 -1.20          O

HETATM   36  O   MOL A   1      10.065   1.609   0.779  1.00 -1.20          O

HETATM   37  O   MOL A   1      11.834  -2.515   2.373  1.00 -2.11          O

END

Table SS 11. Pyrrole of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.079  -2.868  -0.276  1.00  7.11          C

HETATM    2  C   MOL A   1     -11.670  -5.498   2.587  1.00  7.72          C

HETATM    3  C   MOL A   1     -11.020  -6.190  -1.215  1.00  7.32          C

HETATM    4  C   MOL A   1     -10.795  -6.374   2.512  1.00  7.81          C

HETATM    5  C   MOL A   1     -10.187   6.882  -0.293  1.00  6.85          C

HETATM    6  C   MOL A   1      -9.990  -1.758   2.189  1.00  6.15          C

HETATM    7  C   MOL A   1      -9.540  -2.484  -1.738  1.00  6.38          C

HETATM    8  C   MOL A   1      -8.872   8.938   0.047  1.00  6.67          C

HETATM    9  C   MOL A   1      -8.808  -3.198   3.850  1.00  6.87          C

HETATM   10  C   MOL A   1      -8.426  -6.222  -0.924  1.00  6.62          C

HETATM   11  C   MOL A   1      -8.422   3.212   0.351  1.00  7.55          C

HETATM   12  C   MOL A   1      -7.989   6.416   2.689  1.00  4.90          C

HETATM   13  C   MOL A   1      -7.847  -2.325  -1.528  1.00  6.07          C

HETATM   14  C   MOL A   1      -7.703  -1.702   2.227  1.00  6.07          C

HETATM   15  C   MOL A   1      -7.360   5.229  -2.794  1.00  7.01          C

HETATM   16  C   MOL A   1      -7.190   2.850  -0.198  1.00  7.42          C

HETATM   17  C   MOL A   1      -7.016  -0.826  -0.219  1.00  9.19          C

HETATM   18  C   MOL A   1      -6.756   3.206   1.064  1.00  5.69          C

HETATM   19  C   MOL A   1      -6.622  -6.294   2.644  1.00  9.19          C

HETATM   20  C   MOL A   1      -6.594   4.102  -2.425  1.00  6.80          C

HETATM   21  C   MOL A   1      -6.018  -6.350  -0.810  1.00  9.33          C

HETATM   22  C   MOL A   1      -6.016   1.322   2.016  1.00  4.63          C

HETATM   23  C   MOL A   1      -5.858  -5.738   2.686  1.00  9.41          C

HETATM   24  C   MOL A   1      -5.865   7.600  -2.426  1.00  6.69          C

HETATM   25  C   MOL A   1      -5.442   1.658  -3.262  1.00  3.98          C

HETATM   26  C   MOL A   1      -5.013  -6.935  -0.864  1.00  9.71          C

HETATM   27  C   MOL A   1      -4.989   8.713   1.233  1.00  6.49          C

HETATM   28  C   MOL A   1      -4.844  -6.059   2.745  1.00  8.89          C

HETATM   29  C   MOL A   1      -4.499   6.912   1.958  1.00  3.93          C

HETATM   30  C   MOL A   1      -4.187   7.302  -1.694  1.00  6.74          C

HETATM   31  C   MOL A   1      -3.543  -8.902  -0.728  1.00  9.49          C

HETATM   32  C   MOL A   1      -3.352  -2.413   1.751  1.00-18.47          C

HETATM   33  C   MOL A   1      -3.251  -8.120   3.253  1.00  8.14          C

HETATM   34  C   MOL A   1      -2.934   7.395  -0.576  1.00  8.04          C

HETATM   35  C   MOL A   1      -2.762   3.558   1.327  1.00-18.71          C

HETATM   36  C   MOL A   1      -2.688  -0.889  -2.013  1.00-15.72          C

HETATM   37  C   MOL A   1      -2.280  -0.722   1.415  1.00-17.88          C

HETATM   38  C   MOL A   1      -1.787   7.438   1.548  1.00  4.46          C

HETATM   39  C   MOL A   1      -1.512   1.402   1.457  1.00-15.18          C

HETATM   40  C   MOL A   1      -1.193   1.482  -1.953  1.00-15.30          C

HETATM   41  C   MOL A   1      -0.949  -6.118  -1.513  1.00 16.03          C

HETATM   42  C   MOL A   1      -0.672  -5.699   2.540  1.00  3.75          C

HETATM   43  C   MOL A   1      -0.336   9.786  -0.443  1.00  6.40          C

HETATM   44  C   MOL A   1      -0.056  -0.244  -2.157  1.00-16.49          C

HETATM   45  C   MOL A   1      -0.009  -1.144   1.197  1.00-16.55          C

HETATM   46  C   MOL A   1       0.064  -8.841   0.822  1.00  8.58          C

HETATM   47  C   MOL A   1       0.122  -6.413  -3.254  1.00 46.45          C

HETATM   48  C   MOL A   1       0.312   4.887   3.125  1.00  3.20          C

HETATM   49  C   MOL A   1       0.845   0.977   1.786  1.00-18.32          C

HETATM   50  C   MOL A   1       1.258  -3.366   0.332  1.00-16.18          C

HETATM   51  C   MOL A   1       1.420  -1.849  -2.763  1.00-17.99          C

HETATM   52  C   MOL A   1       1.501   1.877  -1.483  1.00-18.54          C

HETATM   53  C   MOL A   1       1.542   5.485  -1.993  1.00  2.55          C

HETATM   54  C   MOL A   1       1.779   7.136  -2.579  1.00  5.68          C

HETATM   55  C   MOL A   1       2.228  -1.133   1.315  1.00-18.47          C

HETATM   56  C   MOL A   1       2.244   7.054   1.003  1.00  6.58          C

HETATM   57  C   MOL A   1       2.464   1.548   4.298  1.00  0.81          C

HETATM   58  C   MOL A   1       2.543   0.007  -1.914  1.00-18.88          C

HETATM   59  C   MOL A   1       3.026   5.695   0.917  1.00  8.03          C

HETATM   60  C   MOL A   1       3.496   5.056  -0.991  1.00  3.78          C

HETATM   61  C   MOL A   1       4.292   6.092   1.946  1.00  5.97          C

HETATM   62  C   MOL A   1       5.309   6.168  -1.742  1.00  5.50          C

HETATM   63  C   MOL A   1       5.546   3.544   3.902  1.00  5.09          C

HETATM   64  C   MOL A   1       5.782  -4.017   0.193  1.00  4.53          C

HETATM   65  C   MOL A   1       5.905   1.268   0.847  1.00  4.77          C

HETATM   66  C   MOL A   1       6.025  -4.233  -1.792  1.00 10.77          C

HETATM   67  C   MOL A   1       6.282  -0.334   2.354  1.00  4.72          C

HETATM   68  C   MOL A   1       6.677   1.253  -0.988  1.00  5.48          C

HETATM   69  C   MOL A   1       7.018   3.170   2.690  1.00  5.07          C

HETATM   70  C   MOL A   1       7.484  -3.992   0.948  1.00  5.37          C

HETATM   71  C   MOL A   1       7.787   2.920  -1.147  1.00  5.91          C

HETATM   72  C   MOL A   1       7.964  -2.308  -2.628  1.00  5.66          C

HETATM   73  C   MOL A   1       8.245   6.324   0.985  1.00  5.91          C

HETATM   74  C   MOL A   1       8.594  -0.307   2.693  1.00  5.53          C

HETATM   75  C   MOL A   1       8.986   1.117  -0.963  1.00  5.33          C

HETATM   76  C   MOL A   1       9.474   0.558   2.764  1.00  6.13          C

HETATM   77  C   MOL A   1      10.087  -3.906   1.473  1.00  4.90          C

HETATM   78  C   MOL A   1      10.382  -2.332  -2.291  1.00  5.18          C

HETATM   79  C   MOL A   1      11.443  -2.861   3.295  1.00  5.72          C

HETATM   80  C   MOL A   1      11.494   1.051  -0.833  1.00  4.35          C

HETATM   81  C   MOL A   1      12.447  -2.363  -2.300  1.00  5.13          C

HETATM   82  C   MOL A   1      12.718  -3.963   1.419  1.00  4.84          C

HETATM   83  C   MOL A   1      13.574   0.452   2.737  1.00  6.22          C

HETATM   84  C   MOL A   1      13.990   1.040  -0.960  1.00  5.89          C

HETATM   85  C   MOL A   1      14.518  -0.507   2.652  1.00  6.38          C

HETATM   86  C   MOL A   1      15.888  -2.492  -0.602  1.00  6.07          C

HETATM    1  O   MOL A   1     -12.888  -5.294   0.183  1.00 -1.38          O

HETATM    2  O   MOL A   1     -12.738  -3.715   1.666  1.00 -0.82          O

HETATM    3  O   MOL A   1     -10.237  -1.577   0.059  1.00 -0.58          O

HETATM    4  O   MOL A   1      -9.524   4.818  -1.548  1.00 -1.64          O

HETATM    5  O   MOL A   1      -8.904  -5.616   4.009  1.00 -1.15          O

HETATM    6  O   MOL A   1      -8.825  -2.599   2.385  1.00  3.87          O

HETATM    7  O   MOL A   1      -8.650   6.885  -1.863  1.00 -1.45          O

HETATM    8  O   MOL A   1      -8.003   7.921  -1.702  1.00 -1.55          O

HETATM    9  O   MOL A   1      -6.798   0.710   0.852  1.00  1.55          O

HETATM   10  O   MOL A   1      -6.498   2.205  -2.257  1.00  0.70          O

HETATM   11  O   MOL A   1      -6.474   9.454  -0.674  1.00 -2.03          O

HETATM   12  O   MOL A   1      -4.428  -2.774  -1.758  1.00-16.83          O

HETATM   13  O   MOL A   1      -3.770  -2.227   1.903  1.00-18.87          O

HETATM   14  O   MOL A   1      -3.337  -1.534  -2.114  1.00-16.43          O

HETATM   15  O   MOL A   1      -2.696   4.104   1.436  1.00-19.18          O

HETATM   16  O   MOL A   1      -2.537   3.136   1.512  1.00-18.92          O

HETATM   17  O   MOL A   1      -2.449  -2.318   1.798  1.00-19.48          O

HETATM   18  O   MOL A   1      -2.397   0.056   1.588  1.00-18.88          O

HETATM   19  O   MOL A   1      -2.234   3.941  -2.204  1.00-19.23          O

HETATM   20  O   MOL A   1      -1.816   2.998  -2.174  1.00-19.12          O

HETATM   21  O   MOL A   1      -1.797  -9.469   2.129  1.00 -0.12          O

HETATM   22  O   MOL A   1      -1.324  -0.321  -2.390  1.00-18.78          O

HETATM   23  O   MOL A   1      -1.285  -0.934   1.511  1.00-19.79          O

HETATM   24  O   MOL A   1      -1.066  -8.059   2.702  1.00 -0.35          O

HETATM   25  O   MOL A   1      -0.159  -5.661   0.529  1.00 -1.13          O

HETATM   26  O   MOL A   1      -0.061   0.942   1.806  1.00-19.49          O

HETATM   27  O   MOL A   1       0.230   6.954   2.098  1.00 -1.45          O

HETATM   28  O   MOL A   1       0.486  -1.445  -2.805  1.00-19.78          O

HETATM   29  O   MOL A   1       1.420  -0.347   1.768  1.00-19.77          O

HETATM   30  O   MOL A   1       1.731  -2.045   1.193  1.00-19.67          O

HETATM   31  O   MOL A   1       1.848  -0.658  -2.463  1.00-20.47          O

HETATM   32  O   MOL A   1       2.940  -1.135   1.585  1.00-20.00          O

HETATM   33  O   MOL A   1       3.019  -4.701   0.034  1.00-18.14          O

HETATM   34  O   MOL A   1       3.239   0.373  -1.906  1.00-20.21          O

HETATM   35  O   MOL A   1       5.829   3.958  -1.755  1.00 -3.57          O

HETATM   36  O   MOL A   1       6.235   5.097   2.700  1.00 -1.43          O

HETATM   37  O   MOL A   1       7.464   5.215  -1.838  1.00 -2.94          O

HETATM   38  O   MOL A   1       8.184   0.780   0.998  1.00 -1.38          O

HETATM   39  O   MOL A   1       8.647  -0.583  -1.719  1.00  1.17          O

HETATM   40  O   MOL A   1       8.808  -0.661  -1.715  1.00  1.17          O

HETATM   41  O   MOL A   1      10.565  -0.571  -1.458  1.00  0.85          O

HETATM   42  O   MOL A   1      10.964  -3.579  -0.508  1.00 -2.23          O

HETATM   43  O   MOL A   1      11.452  -3.160   1.707  1.00  2.05          O

HETATM   44  O   MOL A   1      11.445  -0.411   3.945  1.00 -2.76          O

HETATM   45  O   MOL A   1      11.530   1.191   2.831  1.00 -2.00          O

HETATM   46  O   MOL A   1      11.495   1.297   2.255  1.00 -2.03          O

HETATM   47  O   MOL A   1      11.531   1.284   2.458  1.00 -2.03          O

HETATM   48  O   MOL A   1      11.903  -3.596  -0.520  1.00 -2.21          O

HETATM   49  O   MOL A   1      15.358  -2.167   1.425  1.00 -1.96          O

HETATM   50  O   MOL A   1      15.730  -0.176   0.364  1.00 -2.59          O

END

Table SS 12. Thioisorenieratane of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is kcal/mol

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -12.939  -1.229  -0.609  1.00  8.46          C

HETATM    2  C   MOL A   1     -12.352  -2.921  -0.795  1.00  8.29          C

HETATM    3  C   MOL A   1     -12.234   2.793   0.260  1.00  8.51          C

HETATM    4  C   MOL A   1     -11.222   4.115   0.549  1.00  8.54          C

HETATM    5  C   MOL A   1      -8.913  -4.104   1.128  1.00  7.93          C

HETATM    6  C   MOL A   1      -8.602  -3.325  -2.556  1.00  8.27          C

HETATM    7  C   MOL A   1      -7.919   3.425   2.863  1.00  8.58          C

HETATM    8  C   MOL A   1      -7.487  -3.538   1.512  1.00  7.76          C

HETATM    9  C   MOL A   1      -7.423  -3.004  -2.220  1.00  8.36          C

HETATM   10  C   MOL A   1      -7.386   4.253  -0.687  1.00  8.99          C

HETATM   11  C   MOL A   1      -6.682   3.147   2.106  1.00  7.89          C

HETATM   12  C   MOL A   1      -6.380   4.903  -1.377  1.00  7.78          C

HETATM   13  C   MOL A   1      -5.329  -0.894   1.519  1.00  7.28          C

HETATM   14  C   MOL A   1      -4.782  -1.015  -0.709  1.00  7.64          C

HETATM   15  C   MOL A   1      -4.575   3.427   1.723  1.00  7.36          C

HETATM   16  C   MOL A   1      -4.381   2.332  -3.860  1.00  5.94          C

HETATM   17  C   MOL A   1      -3.954  -1.125  -0.783  1.00  6.34          C

HETATM   18  C   MOL A   1      -3.776   0.462  -2.722  1.00  4.16          C

HETATM   19  C   MOL A   1      -2.967   2.118   2.743  1.00 11.67          C

HETATM   20  C   MOL A   1      -2.300   4.567  -1.164  1.00  7.07          C

HETATM   21  C   MOL A   1      -1.707   3.193  -0.234  1.00  5.67          C

HETATM   22  C   MOL A   1      -1.096  -3.507  -1.418  1.00  5.84          C

HETATM   23  C   MOL A   1      -0.493  -0.112  -1.009  1.00-15.16          C

HETATM   24  C   MOL A   1      -0.239  -5.507  -0.293  1.00  8.82          C

HETATM   25  C   MOL A   1       0.014  -5.782  -0.645  1.00  8.82          C

HETATM   26  C   MOL A   1       0.223   0.274   4.558  1.00  8.43          C

HETATM   27  C   MOL A   1       0.890   2.765   1.678  1.00  8.03          C

HETATM   28  C   MOL A   1       1.002  -3.274  -2.728  1.00  8.29          C

HETATM   29  C   MOL A   1       2.291  -3.535   2.736  1.00  6.82          C

HETATM   30  C   MOL A   1       2.298  -0.840   2.339  1.00 10.74          C

HETATM   31  C   MOL A   1       2.490  -5.942   2.517  1.00  7.32          C

HETATM   32  C   MOL A   1       2.442   3.208  -1.407  1.00  8.23          C

HETATM   33  C   MOL A   1       2.889  -4.115  -2.797  1.00  6.93          C

HETATM   34  C   MOL A   1       3.303   2.722  -2.847  1.00  8.57          C

HETATM   35  C   MOL A   1       3.837  -0.962   0.244  1.00  7.92          C

HETATM   36  C   MOL A   1       3.939  -7.403  -0.984  1.00  7.98          C

HETATM   37  C   MOL A   1       4.032   6.714  -0.064  1.00  8.84          C

HETATM   38  C   MOL A   1       4.428  -4.097   2.647  1.00  6.69          C

HETATM   39  C   MOL A   1       4.850   4.928  -3.641  1.00  8.12          C

HETATM   40  C   MOL A   1       5.111  -3.083  -2.877  1.00  7.21          C

HETATM   41  C   MOL A   1       5.196  -0.478  -2.058  1.00  8.70          C

HETATM   42  C   MOL A   1       5.170   6.688   1.201  1.00  8.93          C

HETATM   43  C   MOL A   1       5.527  -6.284  -0.717  1.00  6.95          C

HETATM   44  C   MOL A   1       6.789  -2.840   2.538  1.00  6.43          C

HETATM   45  C   MOL A   1       6.955   2.016  -4.173  1.00  8.68          C

HETATM   46  C   MOL A   1       7.103  -1.809  -3.008  1.00  6.65          C

HETATM   47  C   MOL A   1       7.601   0.346  -3.150  1.00  7.53          C

HETATM   48  C   MOL A   1       7.681  -5.119  -0.768  1.00  6.70          C

HETATM   49  C   MOL A   1       8.347   4.933   3.260  1.00  8.86          C

HETATM   50  C   MOL A   1       8.608  -0.169   2.471  1.00  9.02          C

HETATM   51  C   MOL A   1       9.374  -1.947   2.191  1.00  7.70          C

HETATM   52  C   MOL A   1       9.455   3.631   3.542  1.00  8.82          C

HETATM   53  C   MOL A   1       9.578  -4.343  -1.178  1.00  7.66          C

HETATM   54  C   MOL A   1      10.269   0.571  -0.399  1.00  8.27          C

HETATM   55  C   MOL A   1      10.492  -0.310  -1.108  1.00  8.19          C

HETATM   56  C   MOL A   1      10.973   1.749   0.249  1.00  8.71          C

HETATM    1  O   MOL A   1     -10.471  -4.467  -0.766  1.00 -0.17          O

HETATM    2  O   MOL A   1     -10.117  -0.142   1.824  1.00-20.32          O

HETATM    3  O   MOL A   1      -9.714   0.671  -1.785  1.00-20.31          O

HETATM    4  O   MOL A   1      -9.241   4.782   1.515  1.00  0.48          O

HETATM    5  O   MOL A   1      -9.139   4.821   1.398  1.00  0.48          O

HETATM    6  O   MOL A   1      -9.043   4.862   1.237  1.00  0.48          O

HETATM    7  O   MOL A   1      -9.011   4.923   0.959  1.00  0.48          O

HETATM    8  O   MOL A   1      -5.697  -2.917  -0.085  1.00 -1.39          O

HETATM    9  O   MOL A   1      -3.999   4.545  -3.124  1.00 -1.81          O

HETATM   10  O   MOL A   1      -3.831   4.462  -3.151  1.00 -1.82          O

HETATM   11  O   MOL A   1      -2.732   2.891  -2.604  1.00 -1.95          O

HETATM   12  O   MOL A   1      -2.602  -3.075   1.281  1.00-16.33          O

HETATM   13  O   MOL A   1      -1.790  -1.757   2.313  1.00-17.57          O

HETATM   14  O   MOL A   1      -1.137  -0.521  -2.059  1.00-15.93          O

HETATM   15  O   MOL A   1      -1.067  -2.285   2.238  1.00-17.77          O

HETATM   16  O   MOL A   1      -0.410  -4.258  -1.649  1.00  3.09          O

HETATM   17  O   MOL A   1      -0.022   2.334   3.668  1.00  1.17          O

HETATM   18  O   MOL A   1       0.294  -0.045  -0.630  1.00-17.24          O

HETATM   19  O   MOL A   1       1.906  -7.490   0.646  1.00 -1.00          O

HETATM   20  O   MOL A   1       3.361  -2.377   1.645  1.00  2.26          O

HETATM   21  O   MOL A   1       3.396   5.902  -2.200  1.00  0.39          O

HETATM   22  O   MOL A   1       3.592   6.053  -2.241  1.00  0.39          O

HETATM   23  O   MOL A   1       4.052  -1.805  -1.623  1.00  1.21          O

HETATM   24  O   MOL A   1       4.583   1.069  -3.555  1.00  0.74          O

HETATM   25  O   MOL A   1       5.201  -4.669  -1.745  1.00  3.06          O

HETATM   26  O   MOL A   1       5.536   2.801   1.607  1.00-19.75          O

HETATM   27  O   MOL A   1       5.839  -5.207   1.276  1.00 -0.71          O

HETATM   28  O   MOL A   1       7.041  -4.588   1.294  1.00 -0.86          O

HETATM   29  O   MOL A   1       7.265  -3.568  -1.855  1.00  2.72          O

HETATM   30  O   MOL A   1       7.303  -4.504   1.311  1.00 -0.84          O

HETATM   31  O   MOL A   1       7.844  -1.952   1.858  1.00  4.21          O

HETATM   32  O   MOL A   1       7.903   4.622  -0.618  1.00-19.97          O

HETATM   33  O   MOL A   1       9.106  -3.793   0.897  1.00 -0.82          O

HETATM   34  O   MOL A   1      10.525   1.614   2.628  1.00  0.56          O

HETATM   35  O   MOL A   1      10.790  -2.659   0.263  1.00 -1.07          O

END

Table SS 13. Benzobisbenzothiophene with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.752  -3.006  -1.396  1.00 -0.70          C

HETATM    2  C   MOL A   1     -11.181  -5.607  -0.819  1.00 -0.47          C

HETATM    3  C   MOL A   1     -10.724  -3.479  -3.619  1.00 -0.49          C

HETATM    4  C   MOL A   1      -9.732  -5.114  -2.465  1.00 -0.43          C

HETATM    5  C   MOL A   1      -8.787   0.201   1.800  1.00 -1.13          C

HETATM    6  C   MOL A   1      -7.905   7.575   0.290  1.00 -0.70          C

HETATM    7  C   MOL A   1      -7.365  -1.571  -1.669  1.00 -1.78          C

HETATM    8  C   MOL A   1      -6.705   4.446   1.554  1.00 -0.85          C

HETATM    9  C   MOL A   1      -6.045  -2.841   1.924  1.00 -1.45          C

HETATM   10  C   MOL A   1      -5.861  -5.528  -2.407  1.00 -0.48          C

HETATM   11  C   MOL A   1      -5.789  10.014  -1.370  1.00 -0.69          C

HETATM   12  C   MOL A   1      -5.702  -0.773  -0.829  1.00 -1.51          C

HETATM   13  C   MOL A   1      -4.462   5.963  -1.733  1.00 -2.10          C

HETATM   14  C   MOL A   1      -3.809  -3.358   1.831  1.00 -1.80          C

HETATM   15  C   MOL A   1      -3.769   7.358   1.355  1.00 -2.07          C

HETATM   16  C   MOL A   1      -3.652   0.632   3.131  1.00 -0.93          C

HETATM   17  C   MOL A   1      -3.266  -1.175  -0.775  1.00 -1.82          C

HETATM   18  C   MOL A   1      -2.819   4.657  -1.584  1.00 -1.97          C

HETATM   19  C   MOL A   1      -2.775  -6.731  -3.288  1.00 -0.78          C

HETATM   20  C   MOL A   1      -2.459  -5.143   0.601  1.00 -1.84          C

HETATM   21  C   MOL A   1      -2.361   0.749  -0.423  1.00 -0.30          C

HETATM   22  C   MOL A   1      -2.104  -2.725  -1.860  1.00 -2.01          C

HETATM   23  C   MOL A   1      -2.102   6.167   1.593  1.00 -1.95          C

HETATM   24  C   MOL A   1      -1.904   9.303  -1.939  1.00 -0.75          C

HETATM   25  C   MOL A   1      -1.330  -3.556   2.063  1.00 -1.77          C

HETATM   26  C   MOL A   1      -0.919   3.588   1.903  1.00 -2.07          C

HETATM   27  C   MOL A   1      -0.696   4.733  -2.064  1.00 -2.32          C

HETATM   28  C   MOL A   1      -0.312  -0.455   5.300  1.00 -1.01          C

HETATM   29  C   MOL A   1       0.081  -3.116  -1.738  1.00 -1.99          C

HETATM   30  C   MOL A   1       0.034   6.142   1.030  1.00 -2.29          C

HETATM   31  C   MOL A   1       0.857   2.042  -0.390  1.00 -2.04          C

HETATM   32  C   MOL A   1       0.859   2.442   4.059  1.00 -1.23          C

HETATM   33  C   MOL A   1       0.910  -7.092   0.918  1.00 -1.06          C

HETATM   34  C   MOL A   1       1.196   2.636   1.402  1.00 -1.81          C

HETATM   35  C   MOL A   1       1.198  -3.556   2.347  1.00 -1.78          C

HETATM   36  C   MOL A   1       1.255  -1.571  -0.461  1.00 -2.12          C

HETATM   37  C   MOL A   1       1.355  -3.471  -1.851  1.00 -2.02          C

HETATM   38  C   MOL A   1       1.519   4.701  -2.653  1.00 -2.30          C

HETATM   39  C   MOL A   1       2.261   6.165   0.558  1.00 -2.26          C

HETATM   40  C   MOL A   1       2.542   2.197   4.132  1.00 -1.15          C

HETATM   41  C   MOL A   1       2.616  -0.128   0.433  1.00 -2.30          C

HETATM   42  C   MOL A   1       2.694  -7.218  -3.003  1.00 -0.85          C

HETATM   43  C   MOL A   1       2.782  -1.807   3.463  1.00 -1.93          C

HETATM   44  C   MOL A   1       3.321  -1.651  -0.618  1.00 -2.26          C

HETATM   45  C   MOL A   1       3.778  -3.669   2.155  1.00 -1.85          C

HETATM   46  C   MOL A   1       4.114   0.095   0.254  1.00 -2.36          C

HETATM   47  C   MOL A   1       4.211  -3.074  -2.020  1.00 -2.18          C

HETATM   48  C   MOL A   1       4.413   7.047  -2.336  1.00 -1.47          C

HETATM   49  C   MOL A   1       5.119  -1.730   3.178  1.00 -1.82          C

HETATM   50  C   MOL A   1       5.749   6.796  -2.574  1.00 -1.44          C

HETATM   51  C   MOL A   1       7.002  -6.382  -3.495  1.00  0.84          C

HETATM   52  C   MOL A   1       8.566   0.092   3.127  1.00 -1.99          C

HETATM   53  C   MOL A   1       9.447  -3.077  -0.827  1.00 -1.69          C

HETATM    1  O   MOL A   1     -12.211  -0.309   0.832  1.00 -2.80          O

HETATM    2  O   MOL A   1     -11.435   0.005   1.121  1.00 -2.80          O

HETATM    3  O   MOL A   1      -8.484  -3.243   1.568  1.00 -1.81          O

HETATM    4  O   MOL A   1      -7.982  -0.824  -1.463  1.00 -1.86          O

HETATM    5  O   MOL A   1      -7.661  -4.392   0.760  1.00 -1.81          O

HETATM    6  O   MOL A   1      -7.212  -2.052  -2.239  1.00 -1.86          O

HETATM    7  O   MOL A   1      -6.289   0.535   1.755  1.00 -2.29          O

HETATM    8  O   MOL A   1      -4.911   5.580  -1.609  1.00 -2.13          O

HETATM    9  O   MOL A   1      -4.562   6.406  -2.058  1.00 -2.13          O

HETATM   10  O   MOL A   1      -4.202   7.255   1.638  1.00 -2.10          O

HETATM   11  O   MOL A   1      -3.772   7.911   1.236  1.00 -2.10          O

HETATM   12  O   MOL A   1      -3.491  -2.603   2.780  1.00 -1.96          O

HETATM   13  O   MOL A   1      -3.257   3.032  -1.226  1.00 -2.27          O

HETATM   14  O   MOL A   1      -3.166  -4.512   1.328  1.00 -1.92          O

HETATM   15  O   MOL A   1      -3.028  -5.699   0.256  1.00 -1.94          O

HETATM   16  O   MOL A   1      -2.506  -3.126  -2.574  1.00 -2.11          O

HETATM   17  O   MOL A   1      -2.131   4.388   2.825  1.00 -2.33          O

HETATM   18  O   MOL A   1      -1.250   2.673   2.226  1.00 -2.64          O

HETATM   19  O   MOL A   1      -1.088  -2.759   2.981  1.00 -1.95          O

HETATM   20  O   MOL A   1      -1.047  -2.365  -1.652  1.00 -2.09          O

HETATM   21  O   MOL A   1       0.303   3.634  -2.052  1.00 -2.45          O

HETATM   22  O   MOL A   1       0.478  -4.508  -3.082  1.00 -2.60          O

HETATM   23  O   MOL A   1       0.513   0.889   0.283  1.00 -2.84          O

HETATM   24  O   MOL A   1       0.855   5.373   1.433  1.00 -2.39          O

HETATM   25  O   MOL A   1       2.161  -2.507   3.322  1.00 -1.98          O

HETATM   26  O   MOL A   1       2.202   5.645  -3.721  1.00 -2.54          O

HETATM   27  O   MOL A   1       2.548  -3.784  -2.656  1.00 -2.35          O

HETATM   28  O   MOL A   1       3.103  -1.084   4.108  1.00 -2.03          O

HETATM   29  O   MOL A   1       3.173   7.477   0.203  1.00 -2.51          O

HETATM   30  O   MOL A   1       3.322   0.644   0.499  1.00 -2.38          O

HETATM   31  O   MOL A   1       3.668  -2.603   3.252  1.00 -1.99          O

HETATM   32  O   MOL A   1       4.605  -3.397  -2.733  1.00 -2.31          O

HETATM   33  O   MOL A   1       5.433  -6.062   0.045  1.00 -2.03          O

HETATM   34  O   MOL A   1       6.280   1.680   1.232  1.00 -4.41          O

HETATM   35  O   MOL A   1       7.782  -3.076   1.711  1.00 -2.32          O

HETATM   36  O   MOL A   1       8.083  -3.340  -2.660  1.00 -2.68          O

HETATM   37  O   MOL A   1       8.285   2.397  -1.673  1.00 -4.87          O

HETATM   38  O   MOL A   1       8.903  -1.714   2.185  1.00 -2.35          O

END

Table SS 14. Trimethylbenzene with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.967   1.782   0.152  1.00 -1.57          C

HETATM    2  C   MOL A   1     -13.246  -1.779  -0.088  1.00 -1.61          C

HETATM    3  C   MOL A   1     -12.771   0.526  -3.025  1.00 -1.73          C

HETATM    4  C   MOL A   1     -12.237   1.878   2.695  1.00 -1.63          C

HETATM    5  C   MOL A   1     -11.807   3.690   0.462  1.00 -1.86          C

HETATM    6  C   MOL A   1     -11.717  -1.667   2.250  1.00 -1.66          C

HETATM    7  C   MOL A   1     -11.109   2.512  -2.790  1.00 -2.04          C

HETATM    8  C   MOL A   1      -9.422   5.516   0.383  1.00 -1.87          C

HETATM    9  C   MOL A   1      -9.000   0.748   2.993  1.00 -1.93          C

HETATM   10  C   MOL A   1      -8.997   4.404  -2.994  1.00 -2.05          C

HETATM   11  C   MOL A   1      -8.585   2.497   2.208  1.00 -2.09          C

HETATM   12  C   MOL A   1      -7.317  -3.210   2.216  1.00 -1.65          C

HETATM   13  C   MOL A   1      -7.315   6.847   1.006  1.00 -1.61          C

HETATM   14  C   MOL A   1      -7.048   6.627  -2.687  1.00 -1.71          C

HETATM   15  C   MOL A   1      -6.771  -4.278  -2.743  1.00 -1.96          C

HETATM   16  C   MOL A   1      -6.184   3.786   1.737  1.00 -2.07          C

HETATM   17  C   MOL A   1      -6.032   4.502  -3.670  1.00 -2.15          C

HETATM   18  C   MOL A   1      -4.466  -2.664   6.159  1.00  0.85          C

HETATM   19  C   MOL A   1      -4.098   6.190  -0.371  1.00 -1.74          C

HETATM   20  C   MOL A   1      -3.344   3.690  -4.268  1.00 -2.14          C

HETATM   21  C   MOL A   1      -3.105   3.115   3.281  1.00 -1.49          C

HETATM   22  C   MOL A   1      -3.070  -5.005  -1.823  1.00 -1.77          C

HETATM   23  C   MOL A   1      -2.295  -1.517   2.296  1.00 -2.12          C

HETATM   24  C   MOL A   1      -2.273   0.554   4.114  1.00 -1.52          C

HETATM   25  C   MOL A   1      -2.012  -0.845  -4.632  1.00 -2.04          C

HETATM   26  C   MOL A   1      -1.518  -1.591   0.462  1.00 -2.32          C

HETATM   27  C   MOL A   1      -1.440  -5.123   0.224  1.00 -1.79          C

HETATM   28  C   MOL A   1      -1.434  -2.815  -5.723  1.00 -1.10          C

HETATM   29  C   MOL A   1      -1.353   2.813  -5.163  1.00 -1.91          C

HETATM   30  C   MOL A   1      -1.359   6.665   2.510  1.00 -1.22          C

HETATM   31  C   MOL A   1      -1.403   6.804  -1.328  1.00 -1.37          C

HETATM   32  C   MOL A   1      -0.724   8.045   2.180  1.00 -1.11          C

HETATM   33  C   MOL A   1      -0.663  -4.831  -2.163  1.00 -1.88          C

HETATM   34  C   MOL A   1      -0.501   4.073   4.821  1.00 -1.32          C

HETATM   35  C   MOL A   1      -0.004  -2.893   6.027  1.00 -0.85          C

HETATM   36  C   MOL A   1       0.267   1.823   5.463  1.00 -1.35          C

HETATM   37  C   MOL A   1       0.402  -2.328  -6.100  1.00 -1.19          C

HETATM   38  C   MOL A   1       0.387  -1.267  -0.031  1.00 -2.10          C

HETATM   39  C   MOL A   1       0.668   1.431  -2.511  1.00 -2.24          C

HETATM   40  C   MOL A   1       1.028  -0.741   1.903  1.00 -1.97          C

HETATM   41  C   MOL A   1       1.183  -4.645  -0.330  1.00 -1.71          C

HETATM   42  C   MOL A   1       1.335  -0.108   0.069  1.00 -1.97          C

HETATM   43  C   MOL A   1       1.578  -0.965   1.746  1.00 -1.99          C

HETATM   44  C   MOL A   1       1.622   8.894  -0.728  1.00 -1.06          C

HETATM   45  C   MOL A   1       2.056  -5.518   3.321  1.00 -1.02          C

HETATM   46  C   MOL A   1       2.144  -4.785  -4.763  1.00 -1.00          C

HETATM   47  C   MOL A   1       3.310   0.830  -2.324  1.00 -0.30          C

HETATM   48  C   MOL A   1       3.464   0.872   0.105  1.00 -1.77          C

HETATM   49  C   MOL A   1       3.545  -3.874  -0.415  1.00 -1.70          C

HETATM   50  C   MOL A   1       3.641   8.055  -0.568  1.00 -1.10          C

HETATM   51  C   MOL A   1       4.662   0.181  -0.732  1.00 -1.79          C

HETATM   52  C   MOL A   1       4.634   2.341   3.995  1.00 -1.37          C

HETATM   53  C   MOL A   1       4.832  -3.415   1.574  1.00 -1.77          C

HETATM   54  C   MOL A   1       4.991  -1.623  -4.615  1.00 -0.87          C

HETATM   55  C   MOL A   1       5.133  -1.271   5.185  1.00 -0.78          C

HETATM   56  C   MOL A   1       5.648   7.371  -0.474  1.00 -1.05          C

HETATM   57  C   MOL A   1       5.888  -3.028  -0.711  1.00 -1.73          C

HETATM   58  C   MOL A   1       6.261   3.680  -1.153  1.00 -1.26          C

HETATM   59  C   MOL A   1       6.425   2.979   1.259  1.00 -1.33          C

HETATM   60  C   MOL A   1       6.635   5.103   2.361  1.00 -1.09          C

HETATM   61  C   MOL A   1       6.817   0.956  -1.381  1.00 -1.44          C

HETATM   62  C   MOL A   1       7.947  -0.580   3.345  1.00 -0.45          C

HETATM   63  C   MOL A   1       7.986  -2.294  -1.450  1.00 -1.38          C

HETATM   64  C   MOL A   1       8.469   1.524  -0.416  1.00 -1.72          C

HETATM   65  C   MOL A   1       9.843   0.206  -4.049  1.00 -1.08          C

HETATM   66  C   MOL A   1      11.579   0.594   2.605  1.00 -0.39          C

HETATM   67  C   MOL A   1      12.053   2.634   1.960  1.00 -0.47          C

HETATM   68  C   MOL A   1      13.174  -0.663   1.808  1.00 -0.43          C

HETATM   69  C   MOL A   1      15.101   1.885  -0.157  1.00 -0.67          C

HETATM    1  O   MOL A   1     -12.760   0.069   1.336  1.00 -2.08          O

HETATM    2  O   MOL A   1     -12.184   2.341   0.780  1.00 -2.04          O

HETATM    3  O   MOL A   1     -11.993   2.580  -1.441  1.00 -2.26          O

HETATM    4  O   MOL A   1     -10.260   3.939  -1.447  1.00 -2.39          O

HETATM    5  O   MOL A   1     -10.006   2.673   1.501  1.00 -2.34          O

HETATM    6  O   MOL A   1      -9.688   3.378   1.178  1.00 -2.34          O

HETATM    7  O   MOL A   1      -8.694   5.404  -1.713  1.00 -2.26          O

HETATM    8  O   MOL A   1      -8.125  -0.285   0.275  1.00 -4.05          O

HETATM    9  O   MOL A   1      -8.009   3.726   1.293  1.00 -2.32          O

HETATM   10  O   MOL A   1      -6.915   0.400  -2.749  1.00 -4.66          O

HETATM   11  O   MOL A   1      -6.774   0.356  -2.745  1.00 -4.66          O

HETATM   12  O   MOL A   1      -6.507  -3.597   3.652  1.00 -2.55          O

HETATM   13  O   MOL A   1      -6.139   0.801  -0.284  1.00 -4.36          O

HETATM   14  O   MOL A   1      -5.963  -1.735   3.382  1.00 -2.64          O

HETATM   15  O   MOL A   1      -5.555  -5.026   0.551  1.00 -2.28          O

HETATM   16  O   MOL A   1      -4.637   3.286   0.741  1.00 -2.47          O

HETATM   17  O   MOL A   1      -4.375  -1.115  -2.676  1.00 -4.49          O

HETATM   18  O   MOL A   1      -4.350   4.271  -2.633  1.00 -2.49          O

HETATM   19  O   MOL A   1      -2.973   3.998  -2.398  1.00 -2.43          O

HETATM   20  O   MOL A   1      -2.777  -5.106   3.646  1.00 -2.00          O

HETATM   21  O   MOL A   1      -2.690  -1.206   3.021  1.00 -2.24          O

HETATM   22  O   MOL A   1      -1.518   1.851   4.394  1.00 -1.70          O

HETATM   23  O   MOL A   1      -1.428  -5.345  -1.355  1.00 -1.95          O

HETATM   24  O   MOL A   1      -1.105  -4.941  -3.097  1.00 -1.99          O

HETATM   25  O   MOL A   1      -0.848  -1.118   2.640  1.00 -2.29          O

HETATM   26  O   MOL A   1      -0.042   2.467  -3.205  1.00 -2.39          O

HETATM   27  O   MOL A   1       0.093  -5.010  -1.663  1.00 -1.93          O

HETATM   28  O   MOL A   1       0.466  -0.516  -2.552  1.00 -2.98          O

HETATM   29  O   MOL A   1       0.851   0.270  -4.490  1.00 -3.21          O

HETATM   30  O   MOL A   1       1.742  -0.836   4.111  1.00 -2.60          O

HETATM   31  O   MOL A   1       2.126  -4.656  -0.016  1.00 -1.79          O

HETATM   32  O   MOL A   1       2.154   4.416  -0.868  1.00 -2.60          O

HETATM   33  O   MOL A   1       2.377   1.144   2.790  1.00 -2.94          O

HETATM   34  O   MOL A   1       2.627   5.767   2.469  1.00 -2.46          O

HETATM   35  O   MOL A   1       3.165  -4.202  -1.539  1.00 -1.89          O

HETATM   36  O   MOL A   1       3.483   0.165   2.430  1.00 -2.25          O

HETATM   37  O   MOL A   1       5.130   0.751   1.001  1.00 -2.05          O

HETATM   38  O   MOL A   1       5.467  -3.410  -1.857  1.00 -1.89          O

HETATM   39  O   MOL A   1       5.469  -3.454   0.543  1.00 -1.85          O

HETATM   40  O   MOL A   1       5.532  -3.317   2.204  1.00 -1.87          O

HETATM   41  O   MOL A   1       6.857   4.087   0.523  1.00 -1.47          O

HETATM   42  O   MOL A   1       7.438  -0.206  -4.004  1.00 -2.22          O

HETATM   43  O   MOL A   1       8.471   1.684   0.457  1.00 -1.81          O

HETATM   44  O   MOL A   1       9.041   1.951  -1.123  1.00 -1.80          O

HETATM   45  O   MOL A   1       9.755  -1.944   0.305  1.00 -1.75          O

HETATM   46  O   MOL A   1      10.377  -1.724  -1.209  1.00 -1.75          O

HETATM   47  O   MOL A   1      13.260   1.393  -3.432  1.00 -2.75          O

END

Table SS 15. Thiophene with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.430  -4.669  -2.699  1.00 -0.67          C

HETATM    2  C   MOL A   1     -13.071   7.559   0.182  1.00 -0.59          C

HETATM    3  C   MOL A   1     -10.969   4.281   0.636  1.00 -0.73          C

HETATM    4  C   MOL A   1     -10.955   7.341   3.223  1.00 -0.70          C

HETATM    5  C   MOL A   1     -10.627  -2.656  -4.119  1.00 -0.46          C

HETATM    6  C   MOL A   1     -10.491  -6.101  -4.523  1.00 -0.42          C

HETATM    7  C   MOL A   1     -10.148   6.935  -2.356  1.00 -0.67          C

HETATM    8  C   MOL A   1      -9.933   9.846   0.401  1.00 -0.68          C

HETATM    9  C   MOL A   1      -9.348  -4.335  -4.827  1.00 -0.38          C

HETATM   10  C   MOL A   1      -8.925   6.097  -2.135  1.00 -0.80          C

HETATM   11  C   MOL A   1      -8.733   0.598   3.684  1.00 -0.99          C

HETATM   12  C   MOL A   1      -8.733  -1.728   0.802  1.00 -1.27          C

HETATM   13  C   MOL A   1      -8.662   4.528   1.671  1.00 -0.84          C

HETATM   14  C   MOL A   1      -8.574  -5.122   1.949  1.00 -1.07          C

HETATM   15  C   MOL A   1      -7.954   9.521  -0.871  1.00 -0.76          C

HETATM   16  C   MOL A   1      -7.548   1.615   0.800  1.00 -1.13          C

HETATM   17  C   MOL A   1      -7.484   8.346   2.828  1.00 -0.83          C

HETATM   18  C   MOL A   1      -7.429   4.259  -1.487  1.00 -0.95          C

HETATM   19  C   MOL A   1      -7.214   1.989   3.813  1.00 -1.00          C

HETATM   20  C   MOL A   1      -7.225   3.316   1.561  1.00 -0.88          C

HETATM   21  C   MOL A   1      -6.946  -1.688  -0.562  1.00 -1.40          C

HETATM   22  C   MOL A   1      -6.567   5.912  -3.314  1.00 -0.92          C

HETATM   23  C   MOL A   1      -6.270  -2.360   4.300  1.00 -1.17          C

HETATM   24  C   MOL A   1      -6.080   9.464  -2.043  1.00 -0.80          C

HETATM   25  C   MOL A   1      -5.856   8.686  -4.267  1.00 -0.77          C

HETATM   26  C   MOL A   1      -5.732   8.559   1.406  1.00 -0.97          C

HETATM   27  C   MOL A   1      -5.569  -6.428  -0.472  1.00 -1.37          C

HETATM   28  C   MOL A   1      -5.474  -4.108  -4.995  1.00 -0.44          C

HETATM   29  C   MOL A   1      -4.857  -0.934   4.425  1.00 -1.27          C

HETATM   30  C   MOL A   1      -4.427   5.433  -4.347  1.00 -1.05          C

HETATM   31  C   MOL A   1      -4.033   0.027  -0.835  1.00 -1.65          C

HETATM   32  C   MOL A   1      -3.487  -5.294   3.276  1.00 -0.84          C

HETATM   33  C   MOL A   1      -3.479   1.696   0.029  1.00 -2.19          C

HETATM   34  C   MOL A   1      -3.457  -2.363   2.030  1.00 -1.30          C

HETATM   35  C   MOL A   1      -3.256  -6.295  -0.846  1.00 -1.73          C

HETATM   36  C   MOL A   1      -3.238  -2.895  -0.374  1.00 -1.87          C

HETATM   37  C   MOL A   1      -3.262   3.665   2.863  1.00 -2.18          C

HETATM   38  C   MOL A   1      -3.187   9.208  -0.630  1.00 -0.96          C

HETATM   39  C   MOL A   1      -2.798  10.297  -2.572  1.00 -0.80          C

HETATM   40  C   MOL A   1      -2.487  -2.287   1.425  1.00 -0.69          C

HETATM   41  C   MOL A   1      -2.462   8.182  -5.889  1.00 -0.81          C

HETATM   42  C   MOL A   1      -2.318  -3.474  -6.297  1.00 -0.77          C

HETATM   43  C   MOL A   1      -2.052  -2.584  -2.124  1.00 -2.03          C

HETATM   44  C   MOL A   1      -1.842  -5.939  -2.944  1.00 -1.78          C

HETATM   45  C   MOL A   1      -1.827   0.374   0.682  1.00 -2.18          C

HETATM   46  C   MOL A   1      -1.691   2.393   3.701  1.00 -2.16          C

HETATM   47  C   MOL A   1      -1.253   2.358  -0.509  1.00 -2.16          C

HETATM   48  C   MOL A   1      -1.105   4.237   2.315  1.00 -2.11          C

HETATM   49  C   MOL A   1      -0.717  -6.255  -0.786  1.00 -1.70          C

HETATM   50  C   MOL A   1      -0.526   7.035  -1.658  1.00 -0.89          C

HETATM   51  C   MOL A   1      -0.314  -0.623   4.070  1.00 -1.72          C

HETATM   52  C   MOL A   1       0.234  -7.368   3.597  1.00 -0.97          C

HETATM   53  C   MOL A   1       0.251  -2.582  -2.282  1.00 -1.99          C

HETATM   54  C   MOL A   1       0.297   0.882   0.312  1.00 -2.53          C

HETATM   55  C   MOL A   1       0.856  -4.665   5.529  1.00 -1.13          C

HETATM   56  C   MOL A   1       1.013   2.633  -0.891  1.00 -2.47          C

HETATM   57  C   MOL A   1       1.128  -1.093   4.409  1.00 -1.68          C

HETATM   58  C   MOL A   1       1.348  -2.479  -2.470  1.00 -2.03          C

HETATM   59  C   MOL A   1       1.356  -2.760  -0.230  1.00 -2.12          C

HETATM   60  C   MOL A   1       1.359   0.340   5.797  1.00 -1.83          C

HETATM   61  C   MOL A   1       1.410   4.505   1.956  1.00 -2.40          C

HETATM   62  C   MOL A   1       1.350   6.529  -3.325  1.00 -1.15          C

HETATM   63  C   MOL A   1       1.758  -6.156  -0.537  1.00 -1.70          C

HETATM   64  C   MOL A   1       1.824  -6.689  -4.238  1.00 -1.04          C

HETATM   65  C   MOL A   1       1.838   8.288  -0.541  1.00 -1.17          C

HETATM   66  C   MOL A   1       2.627  -4.504   5.480  1.00 -1.02          C

HETATM   67  C   MOL A   1       2.697  -2.552   1.502  1.00 -2.26          C

HETATM   68  C   MOL A   1       2.641  -1.868   1.925  1.00 -2.24          C

HETATM   69  C   MOL A   1       3.017  -2.997  -6.257  1.00 -0.90          C

HETATM   70  C   MOL A   1       3.257  -6.015   1.677  1.00 -1.85          C

HETATM   71  C   MOL A   1       3.332  -2.357  -0.147  1.00 -2.19          C

HETATM   72  C   MOL A   1       3.553  -0.384  -0.419  1.00 -2.19          C

HETATM   73  C   MOL A   1       3.560   3.029   4.127  1.00 -2.03          C

HETATM   74  C   MOL A   1       3.641  -1.096   8.012  1.00 -1.49          C

HETATM   75  C   MOL A   1       4.112  -2.066   1.512  1.00 -2.18          C

HETATM   76  C   MOL A   1       4.207  -1.645  -1.894  1.00 -2.19          C

HETATM   77  C   MOL A   1       4.399  -5.618  -0.547  1.00 -1.77          C

HETATM   78  C   MOL A   1       4.532   1.699   6.206  1.00 -1.92          C

HETATM   79  C   MOL A   1       4.869   7.587  -2.611  1.00 -1.18          C

HETATM   80  C   MOL A   1       5.550  -5.287   1.841  1.00 -1.71          C

HETATM   81  C   MOL A   1       5.743  -2.493   5.991  1.00 -1.92          C

HETATM   82  C   MOL A   1       5.889   1.218  -2.033  1.00 -2.21          C

HETATM   83  C   MOL A   1       7.051  -1.100  -5.409  1.00  0.67          C

HETATM   84  C   MOL A   1       7.719   6.000  -0.213  1.00 -1.83          C

HETATM   85  C   MOL A   1       8.050  -2.760   4.012  1.00 -2.11          C

HETATM   86  C   MOL A   1       8.029   6.521  -2.924  1.00 -1.49          C

HETATM   87  C   MOL A   1       8.257   2.637  -4.590  1.00 -1.65          C

HETATM   88  C   MOL A   1       9.206  -2.245  -1.222  1.00 -2.27          C

HETATM   89  C   MOL A   1      10.004   3.985  -4.834  1.00 -1.47          C

HETATM   90  C   MOL A   1      10.097  -2.904   1.679  1.00 -1.93          C

HETATM   91  C   MOL A   1      10.220   5.941   0.162  1.00 -1.72          C

HETATM   92  C   MOL A   1      10.958   1.291  -3.085  1.00 -1.85          C

HETATM   93  C   MOL A   1      11.017   7.370  -4.675  1.00 -1.14          C

HETATM   94  C   MOL A   1      11.263   7.635  -0.950  1.00 -1.28          C

HETATM   95  C   MOL A   1      12.223   3.373  -1.796  1.00 -1.71          C

HETATM   96  C   MOL A   1      13.287   5.019  -2.990  1.00 -1.26          C

HETATM    1  O   MOL A   1     -12.182   5.719   1.120  1.00 -1.00          O

HETATM    2  O   MOL A   1     -11.959  -5.049   0.882  1.00 -2.75          O

HETATM    3  O   MOL A   1     -11.352   8.148  -1.182  1.00 -0.97          O

HETATM    4  O   MOL A   1      -9.685   5.202  -0.919  1.00 -1.07          O

HETATM    5  O   MOL A   1      -9.697   8.883   2.364  1.00 -0.99          O

HETATM    6  O   MOL A   1      -8.026  -2.773  -0.709  1.00 -1.76          O

HETATM    7  O   MOL A   1      -7.942  -6.654  -1.106  1.00 -1.73          O

HETATM    8  O   MOL A   1      -7.131  -2.573  -2.106  1.00 -1.79          O

HETATM    9  O   MOL A   1      -7.075  -6.426  -2.536  1.00 -1.74          O

HETATM   10  O   MOL A   1      -7.123   6.143   2.491  1.00 -1.18          O

HETATM   11  O   MOL A   1      -7.098   7.541  -2.564  1.00 -1.13          O

HETATM   12  O   MOL A   1      -6.837  -0.540   4.452  1.00 -1.43          O

HETATM   13  O   MOL A   1      -6.183  -4.511   2.307  1.00 -2.22          O

HETATM   14  O   MOL A   1      -4.605   9.897  -3.289  1.00 -1.09          O

HETATM   15  O   MOL A   1      -4.117   1.859  -0.224  1.00 -2.23          O

HETATM   16  O   MOL A   1      -4.206   9.227  -1.816  1.00 -1.07          O

HETATM   17  O   MOL A   1      -3.826   3.500   3.172  1.00 -2.22          O

HETATM   18  O   MOL A   1      -2.871  -6.668   0.243  1.00 -1.88          O

HETATM   19  O   MOL A   1      -2.558   3.081   3.468  1.00 -2.26          O

HETATM   20  O   MOL A   1      -2.474  -6.350  -2.059  1.00 -1.86          O

HETATM   21  O   MOL A   1      -2.374  -6.004  -3.636  1.00 -1.88          O

HETATM   22  O   MOL A   1      -2.395  -2.208  -2.860  1.00 -2.14          O

HETATM   23  O   MOL A   1      -2.084   3.631  -1.618  1.00 -2.30          O

HETATM   24  O   MOL A   1      -1.928   5.807   1.642  1.00 -2.25          O

HETATM   25  O   MOL A   1      -1.735   1.059   5.026  1.00 -2.39          O

HETATM   26  O   MOL A   1      -1.620   8.743  -3.821  1.00 -1.19          O

HETATM   27  O   MOL A   1      -0.963  -2.444  -1.589  1.00 -2.13          O

HETATM   28  O   MOL A   1      -0.709  -2.283   4.375  1.00 -3.04          O

HETATM   29  O   MOL A   1      -0.502  -6.608   0.397  1.00 -1.88          O

HETATM   30  O   MOL A   1      -0.240  -5.776   4.899  1.00 -1.27          O

HETATM   31  O   MOL A   1       0.526  -2.211   2.529  1.00 -3.11          O

HETATM   32  O   MOL A   1       0.627  -2.057  -4.122  1.00 -2.61          O

HETATM   33  O   MOL A   1       0.872   2.281   3.859  1.00 -2.53          O

HETATM   34  O   MOL A   1       0.933  -6.439  -1.030  1.00 -1.78          O

HETATM   35  O   MOL A   1       1.129  -2.496  -1.088  1.00 -2.24          O

HETATM   36  O   MOL A   1       1.095   5.093   1.808  1.00 -2.45          O

HETATM   37  O   MOL A   1       1.174  -0.152   0.792  1.00 -2.71          O

HETATM   38  O   MOL A   1       1.254   3.578   2.927  1.00 -2.48          O

HETATM   39  O   MOL A   1       1.985  -0.933   6.041  1.00 -1.97          O

HETATM   40  O   MOL A   1       2.618  -6.376   0.980  1.00 -1.91          O

HETATM   41  O   MOL A   1       2.618  -1.686  -3.024  1.00 -2.41          O

HETATM   42  O   MOL A   1       3.094  -2.091  -1.069  1.00 -2.29          O

HETATM   43  O   MOL A   1       3.508  -6.142   2.651  1.00 -1.94          O

HETATM   44  O   MOL A   1       3.559   2.553  -1.522  1.00 -2.72          O

HETATM   45  O   MOL A   1       4.104  -6.127   0.794  1.00 -1.92          O

HETATM   46  O   MOL A   1       4.364  -1.049  -2.704  1.00 -2.39          O

HETATM   47  O   MOL A   1       4.978   4.059   1.796  1.00 -2.80          O

HETATM   48  O   MOL A   1       5.778  -1.840   3.389  1.00 -3.12          O

HETATM   49  O   MOL A   1       5.753  -0.498   1.421  1.00 -3.42          O

HETATM   50  O   MOL A   1       6.176  -4.446  -3.726  1.00 -2.07          O

HETATM   51  O   MOL A   1       6.740   1.922  -2.615  1.00 -2.35          O

HETATM   52  O   MOL A   1       7.036   0.249  -0.481  1.00 -3.78          O

HETATM   53  O   MOL A   1       7.362   5.778  -1.500  1.00 -1.91          O

HETATM   54  O   MOL A   1       7.980   4.047  -3.441  1.00 -1.99          O

HETATM   55  O   MOL A   1       8.271  -3.795  -1.093  1.00 -2.33          O

HETATM   56  O   MOL A   1       8.340   1.846   1.917  1.00 -4.58          O

HETATM   57  O   MOL A   1       8.494  -0.695  -2.372  1.00 -3.12          O

HETATM   58  O   MOL A   1       8.630   5.780  -0.713  1.00 -1.95          O

HETATM   59  O   MOL A   1       8.684  -3.361   2.821  1.00 -2.26          O

HETATM   60  O   MOL A   1      10.091   0.260  -0.157  1.00 -4.31          O

HETATM   61  O   MOL A   1      10.198   2.303  -3.722  1.00 -2.05          O

HETATM   62  O   MOL A   1      10.647   2.645  -3.093  1.00 -2.05          O       END

Table SS 16. Pyridinohopane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -18.297  -3.900   0.958  1.00 -0.58          C

HETATM    2  C   MOL A   1     -16.866  -0.404   0.791  1.00 -0.33          C

HETATM    3  C   MOL A   1     -15.612  -2.553   3.247  1.00 -0.35          C

HETATM    4  C   MOL A   1     -15.434  -0.568   2.375  1.00 -0.27          C

HETATM    5  C   MOL A   1     -13.034  -0.565  -1.330  1.00 -1.55          C

HETATM    6  C   MOL A   1     -12.496  -4.378  -2.547  1.00 -0.96          C

HETATM    7  C   MOL A   1     -12.024   1.376   2.494  1.00 -0.31          C

HETATM    8  C   MOL A   1     -11.804  -2.709   1.149  1.00 -1.57          C

HETATM    9  C   MOL A   1     -11.282  -0.565  -2.199  1.00 -1.26          C

HETATM   10  C   MOL A   1     -10.044  -2.695   0.224  1.00 -1.27          C

HETATM   11  C   MOL A   1      -9.637   3.557   3.645  1.00 -0.62          C

HETATM   12  C   MOL A   1      -9.396   0.777  -1.973  1.00 -1.61          C

HETATM   13  C   MOL A   1      -8.860   2.761  -0.426  1.00 -1.65          C

HETATM   14  C   MOL A   1      -8.028  -1.359   0.341  1.00 -1.58          C

HETATM   15  C   MOL A   1      -7.759  -2.721  -3.670  1.00 -0.73          C

HETATM   16  C   MOL A   1      -7.536   0.387   1.706  1.00 -1.80          C

HETATM   17  C   MOL A   1      -7.191   1.986  -2.072  1.00 -1.58          C

HETATM   18  C   MOL A   1      -6.547   5.890  -0.401  1.00 -0.93          C

HETATM   19  C   MOL A   1      -6.464  -2.777  -0.325  1.00 -0.06          C

HETATM   20  C   MOL A   1      -5.661   1.590   1.690  1.00 -1.80          C

HETATM   21  C   MOL A   1      -5.090   0.006  -5.690  1.00 -0.90          C

HETATM   22  C   MOL A   1      -4.897   3.007  -2.265  1.00 -1.61          C

HETATM   23  C   MOL A   1      -4.886   6.251   3.539  1.00 -0.74          C

HETATM   24  C   MOL A   1      -4.611   2.372   1.853  1.00 -1.85          C

HETATM   25  C   MOL A   1      -4.022   0.863   0.277  1.00 -1.94          C

HETATM   26  C   MOL A   1      -2.984  -2.404  -4.797  1.00 -1.08          C

HETATM   27  C   MOL A   1      -2.815   2.293  -3.494  1.00 -1.80          C

HETATM   28  C   MOL A   1      -2.570   4.112  -1.970  1.00 -1.70          C

HETATM   29  C   MOL A   1      -2.225   0.264  -0.718  1.00 -2.24          C

HETATM   30  C   MOL A   1      -2.139   1.737   0.515  1.00 -2.12          C

HETATM   31  C   MOL A   1      -1.773   3.182   2.056  1.00 -2.04          C

HETATM   32  C   MOL A   1      -1.328  -1.475  -4.724  1.00 -0.99          C

HETATM   33  C   MOL A   1      -1.204  -2.375   2.631  1.00 -2.00          C

HETATM   34  C   MOL A   1      -0.769   0.705  -0.519  1.00 -2.38          C

HETATM   35  C   MOL A   1      -0.669   3.004  -3.250  1.00 -1.68          C

HETATM   36  C   MOL A   1      -0.510   7.139   4.046  1.00  0.92          C

HETATM   37  C   MOL A   1      -0.118  -3.582  -0.560  1.00 -2.09          C

HETATM   38  C   MOL A   1       0.073   0.657   4.711  1.00 -1.98          C

HETATM   39  C   MOL A   1       0.604  -5.009   2.543  1.00 -1.90          C

HETATM   40  C   MOL A   1       1.469  -3.185   5.789  1.00 -1.70          C

HETATM   41  C   MOL A   1       1.639  -6.264   0.404  1.00 -1.76          C

HETATM   42  C   MOL A   1       2.169  -6.150   3.878  1.00 -1.60          C

HETATM   43  C   MOL A   1       2.263   0.575   7.011  1.00 -1.66          C

HETATM   44  C   MOL A   1       2.198   2.206   5.073  1.00 -1.97          C

HETATM   45  C   MOL A   1       2.954   5.461   1.014  1.00 -1.56          C

HETATM   46  C   MOL A   1       3.149   2.938  -3.400  1.00 -1.81          C

HETATM   47  C   MOL A   1       3.300  -2.777   6.739  1.00 -1.68          C

HETATM   48  C   MOL A   1       3.392  -7.457   1.433  1.00 -1.52          C

HETATM   49  C   MOL A   1       3.464  -5.164  -3.018  1.00 -1.64          C

HETATM   50  C   MOL A   1       4.074  -6.847  -2.079  1.00 -1.54          C

HETATM   51  C   MOL A   1       5.005  -4.304   5.460  1.00 -1.60          C

HETATM   52  C   MOL A   1       5.460   1.030   4.135  1.00 -2.24          C

HETATM   53  C   MOL A   1       5.742  -0.172   6.018  1.00 -1.75          C

HETATM   54  C   MOL A   1       5.898  -4.016   4.880  1.00 -1.65          C

HETATM   55  C   MOL A   1       6.667   1.298  -4.252  1.00 -1.67          C

HETATM   56  C   MOL A   1       6.788  -6.342   2.307  1.00 -1.58          C

HETATM   57  C   MOL A   1       6.803  -2.933  -3.951  1.00 -1.62          C

HETATM   58  C   MOL A   1       6.849  -6.685   0.463  1.00 -1.52          C

HETATM   59  C   MOL A   1       6.822  -6.088  -2.193  1.00 -1.56          C

HETATM   60  C   MOL A   1       8.199   4.191  -2.705  1.00 -1.50          C

HETATM   61  C   MOL A   1       8.761  -3.585   2.848  1.00 -1.65          C

HETATM   62  C   MOL A   1       9.032  -2.212   2.726  1.00 -1.70          C

HETATM   63  C   MOL A   1       9.193  -5.220  -1.732  1.00 -1.50          C

HETATM   64  C   MOL A   1      10.122  -2.232  -3.220  1.00 -1.78          C

HETATM   65  C   MOL A   1      10.315   3.994  -2.306  1.00 -1.26          C

HETATM   66  C   MOL A   1      10.620  -3.904   0.167  1.00 -1.60          C

HETATM   67  C   MOL A   1      12.307   4.081  -1.470  1.00 -1.22          C

HETATM   68  C   MOL A   1      12.846   1.363  -4.098  1.00 -1.32          C

HETATM   69  C   MOL A   1      14.726   2.690   1.505  1.00 -1.13          C

HETATM   70  C   MOL A   1      14.796   3.944  -2.231  1.00 -1.07          C

HETATM   71  C   MOL A   1      15.916  -1.008   0.094  1.00 -1.13          C

HETATM   72  C   MOL A   1      16.039   0.510  -3.453  1.00 -1.04          C

HETATM   73  C   MOL A   1      17.041   4.215  -0.944  1.00 -0.86          C

HETATM   74  C   MOL A   1      18.137   1.516   1.583  1.00 -0.83          C

HETATM   75  C   MOL A   1      18.222   0.706  -2.148  1.00 -0.84          C

HETATM    1  O   MOL A   1     -15.947  -5.412  -1.599  1.00 -2.66          O

HETATM    2  O   MOL A   1     -13.649  -1.200  -1.867  1.00 -1.63          O

HETATM    3  O   MOL A   1     -13.386   0.070  -0.825  1.00 -1.64          O

HETATM    4  O   MOL A   1     -12.239  -3.582   0.893  1.00 -1.65          O

HETATM    5  O   MOL A   1     -11.994  -2.312   1.853  1.00 -1.66          O

HETATM    6  O   MOL A   1     -10.271  -3.582  -2.704  1.00 -2.08          O

HETATM    7  O   MOL A   1      -9.580   3.086   0.039  1.00 -1.76          O

HETATM    8  O   MOL A   1      -9.222   2.051  -1.266  1.00 -1.73          O

HETATM    9  O   MOL A   1      -8.849   0.423  -2.941  1.00 -1.77          O

HETATM   10  O   MOL A   1      -7.976   0.516   2.457  1.00 -1.90          O

HETATM   11  O   MOL A   1      -6.591   1.578  -3.064  1.00 -1.77          O

HETATM   12  O   MOL A   1      -6.309   0.591   1.504  1.00 -1.89          O

HETATM   13  O   MOL A   1      -5.882   3.007  -2.196  1.00 -1.68          O

HETATM   14  O   MOL A   1      -5.767   2.925   3.242  1.00 -2.44          O

HETATM   15  O   MOL A   1      -3.624   2.530  -3.365  1.00 -1.84          O

HETATM   16  O   MOL A   1      -3.537   3.097   2.761  1.00 -2.21          O

HETATM   17  O   MOL A   1      -3.452  -2.386  -1.274  1.00 -3.10          O

HETATM   18  O   MOL A   1      -2.272   3.245  -3.204  1.00 -1.86          O

HETATM   19  O   MOL A   1      -2.224   1.774  -4.290  1.00 -1.91          O

HETATM   20  O   MOL A   1      -1.934   6.673   0.469  1.00 -1.91          O

HETATM   21  O   MOL A   1      -1.509  -0.724  -1.316  1.00 -2.50          O

HETATM   22  O   MOL A   1      -1.533   3.561   2.855  1.00 -2.20          O

HETATM   23  O   MOL A   1      -1.182  -0.597  -1.306  1.00 -2.50          O

HETATM   24  O   MOL A   1       0.236  -3.069   3.489  1.00 -2.25          O

HETATM   25  O   MOL A   1       0.905  -0.422   5.600  1.00 -2.17          O

HETATM   26  O   MOL A   1       1.160   5.166  -1.517  1.00 -2.18          O

HETATM   27  O   MOL A   1       1.320  -0.085  -1.113  1.00 -4.48          O

HETATM   28  O   MOL A   1       1.470   1.010   4.966  1.00 -2.17          O

HETATM   29  O   MOL A   1       1.644   4.920   2.868  1.00 -2.60          O

HETATM   30  O   MOL A   1       1.903  -5.291   1.822  1.00 -2.05          O

HETATM   31  O   MOL A   1       2.660  -4.727   5.677  1.00 -1.94          O

HETATM   32  O   MOL A   1       4.538  -5.407   3.779  1.00 -2.01          O

HETATM   33  O   MOL A   1       4.787   1.737  -1.943  1.00 -3.16          O

HETATM   34  O   MOL A   1       4.956  -7.639  -0.244  1.00 -1.84          O

HETATM   35  O   MOL A   1       5.053  -6.420   2.134  1.00 -1.89          O

HETATM   36  O   MOL A   1       5.018  -2.153   5.145  1.00 -2.13          O

HETATM   37  O   MOL A   1       5.425   1.020   1.494  1.00 -4.37          O

HETATM   38  O   MOL A   1       5.839  -6.759  -1.276  1.00 -1.84          O

HETATM   39  O   MOL A   1       7.310  -4.542   3.475  1.00 -1.91          O

HETATM   40  O   MOL A   1       7.420  -4.556  -3.034  1.00 -1.97          O

HETATM   41  O   MOL A   1       7.666  -5.250  -1.431  1.00 -1.78          O

HETATM   42  O   MOL A   1       8.693  -4.029   0.869  1.00 -1.95          O

HETATM   43  O   MOL A   1       9.643   0.126  -2.714  1.00 -2.49          O

HETATM   44  O   MOL A   1      11.960  -1.111   0.714  1.00 -3.42          O

HETATM   45  O   MOL A   1      16.171   2.958   0.979  1.00 -1.25          O

HETATM   46  O   MOL A   1      17.066  -0.089  -0.045  1.00 -1.25          O

HETATM   47  O   MOL A   1      18.563   2.478  -0.625  1.00 -1.18          O

END

Table SS 17. Quinolinohopane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.614  -1.427  -2.204  1.00 -0.70          C

HETATM    2  C   MOL A   1     -13.572   3.382   0.877  1.00 -0.93          C

HETATM    3  C   MOL A   1     -11.828   2.557  -2.505  1.00 -0.92          C

HETATM    4  C   MOL A   1     -11.422  -4.197  -3.211  1.00 -0.45          C

HETATM    5  C   MOL A   1     -10.351  -0.983  -4.090  1.00 -0.47          C

HETATM    6  C   MOL A   1     -10.323   2.858   2.966  1.00 -1.10          C

HETATM    7  C   MOL A   1     -10.243   5.233   0.115  1.00 -0.96          C

HETATM    8  C   MOL A   1      -9.701  -3.023  -4.124  1.00 -0.41          C

HETATM    9  C   MOL A   1      -9.119   2.470  -2.571  1.00 -1.01          C

HETATM   10  C   MOL A   1      -9.119   5.632   0.825  1.00 -0.93          C

HETATM   11  C   MOL A   1      -8.957  -1.815   2.593  1.00 -1.11          C

HETATM   12  C   MOL A   1      -8.487   0.406   1.238  1.00 -1.54          C

HETATM   13  C   MOL A   1      -8.105   3.008   2.804  1.00 -1.16          C

HETATM   14  C   MOL A   1      -8.068  -4.495  -0.266  1.00 -1.70          C

HETATM   15  C   MOL A   1      -7.940   5.169   3.228  1.00 -0.85          C

HETATM   16  C   MOL A   1      -7.317   4.123  -2.448  1.00 -0.91          C

HETATM   17  C   MOL A   1      -7.080  -1.224  -1.074  1.00 -1.77          C

HETATM   18  C   MOL A   1      -6.557  -4.652   0.911  1.00 -1.44          C

HETATM   19  C   MOL A   1      -6.337   1.909  -1.214  1.00 -1.29          C

HETATM   20  C   MOL A   1      -6.032  -4.088  -4.132  1.00 -0.47          C

HETATM   21  C   MOL A   1      -5.544  -1.424   0.198  1.00 -1.49          C

HETATM   22  C   MOL A   1      -5.316   3.812  -2.582  1.00 -0.83          C

HETATM   23  C   MOL A   1      -5.122   6.071   4.598  1.00 -1.10          C

HETATM   24  C   MOL A   1      -4.226  -5.321   0.671  1.00 -1.80          C

HETATM   25  C   MOL A   1      -4.204   3.254   1.551  1.00 -2.13          C

HETATM   26  C   MOL A   1      -4.221   5.397  -3.388  1.00 -0.83          C

HETATM   27  C   MOL A   1      -4.090  -3.094   4.165  1.00 -0.96          C

HETATM   28  C   MOL A   1      -3.666   2.194  -2.509  1.00 -1.01          C

HETATM   29  C   MOL A   1      -3.336  -2.067   0.051  1.00 -1.82          C

HETATM   30  C   MOL A   1      -2.818  -6.071  -1.372  1.00 -1.85          C

HETATM   31  C   MOL A   1      -2.826  -4.826  -5.409  1.00 -0.79          C

HETATM   32  C   MOL A   1      -2.539  -0.914   1.704  1.00 -0.35          C

HETATM   33  C   MOL A   1      -2.194  -2.669  -1.709  1.00 -2.03          C

HETATM   34  C   MOL A   1      -2.119   3.603   1.408  1.00 -1.95          C

HETATM   35  C   MOL A   1      -1.752  -5.884   0.827  1.00 -1.78          C

HETATM   36  C   MOL A   1      -1.731   8.647   0.281  1.00 -1.35          C

HETATM   37  C   MOL A   1      -0.793   4.111  -3.733  1.00 -0.99          C

HETATM   38  C   MOL A   1      -0.778  -5.697   5.364  1.00 -1.04          C

HETATM   39  C   MOL A   1       0.002  -3.252  -1.788  1.00 -2.00          C

HETATM   40  C   MOL A   1       0.377  -2.705   6.272  1.00 -1.21          C

HETATM   41  C   MOL A   1       0.350   3.526   1.307  1.00 -1.48          C

HETATM   42  C   MOL A   1       0.564  -8.005  -2.258  1.00 -1.07          C

HETATM   43  C   MOL A   1       0.505   7.956  -2.554  1.00 -0.99          C

HETATM   44  C   MOL A   1       0.638   2.932   0.680  1.00 -1.49          C

HETATM   45  C   MOL A   1       0.572   7.867   3.226  1.00 -1.23          C

HETATM   46  C   MOL A   1       0.795  -6.269   1.105  1.00 -1.79          C

HETATM   47  C   MOL A   1       0.939  -3.435  -1.955  1.00 -2.05          C

HETATM   48  C   MOL A   1       0.886   1.200  -0.437  1.00 -1.83          C

HETATM   49  C   MOL A   1       1.020  -2.958   0.189  1.00 -2.19          C

HETATM   50  C   MOL A   1       1.150   4.326   3.451  1.00 -1.44          C

HETATM   51  C   MOL A   1       1.657   9.366   1.381  1.00 -1.09          C

HETATM   52  C   MOL A   1       2.065   5.381   3.647  1.00 -1.44          C

HETATM   53  C   MOL A   1       2.201  -2.783   6.196  1.00 -1.11          C

HETATM   54  C   MOL A   1       2.232   0.545   1.620  1.00 -2.24          C

HETATM   55  C   MOL A   1       2.382  -5.713   3.133  1.00 -1.94          C

HETATM   56  C   MOL A   1       2.363  -2.494   1.784  1.00 -2.43          C

HETATM   57  C   MOL A   1       2.462  -5.495  -5.323  1.00 -0.91          C

HETATM   58  C   MOL A   1       2.398   1.518  -3.443  1.00 -1.69          C

HETATM   59  C   MOL A   1       2.546   5.560  -4.239  1.00 -1.24          C

HETATM   60  C   MOL A   1       2.602  -1.991  -2.360  1.00 -2.11          C

HETATM   61  C   MOL A   1       3.091  -2.944   0.193  1.00 -2.34          C

HETATM   62  C   MOL A   1       3.159   8.255   1.538  1.00 -1.25          C

HETATM   63  C   MOL A   1       3.236   9.439  -0.218  1.00 -1.14          C

HETATM   64  C   MOL A   1       3.494  -6.298   0.974  1.00 -1.85          C

HETATM   65  C   MOL A   1       3.848  -3.057  -1.690  1.00 -2.27          C

HETATM   66  C   MOL A   1       3.811  -2.141   1.943  1.00 -2.48          C

HETATM   67  C   MOL A   1       3.873   1.743  -4.258  1.00 -1.76          C

HETATM   68  C   MOL A   1       4.332   8.007  -3.614  1.00 -1.16          C

HETATM   69  C   MOL A   1       4.372   8.182   1.547  1.00 -1.25          C

HETATM   70  C   MOL A   1       4.780  -5.398   3.145  1.00 -1.81          C

HETATM   71  C   MOL A   1       5.063  -1.194  -3.406  1.00 -2.09          C

HETATM   72  C   MOL A   1       5.483   8.905  -1.954  1.00 -1.21          C

HETATM   73  C   MOL A   1       5.985  -5.793   0.941  1.00 -2.13          C

HETATM   74  C   MOL A   1       6.176   4.203  -5.070  1.00 -1.47          C

HETATM   75  C   MOL A   1       6.755  -4.359  -5.034  1.00  0.69          C

HETATM   76  C   MOL A   1       7.383   1.417  -4.276  1.00 -1.82          C

HETATM   77  C   MOL A   1       7.583   6.336  -2.432  1.00 -1.46          C

HETATM   78  C   MOL A   1       7.801   7.002  -0.030  1.00 -1.40          C

HETATM   79  C   MOL A   1       7.974  -3.332   4.279  1.00 -2.18          C

HETATM   80  C   MOL A   1       8.983  -3.959  -0.675  1.00 -2.08          C

HETATM   81  C   MOL A   1       9.933  -3.733   1.709  1.00 -1.93          C

HETATM    1  O   MOL A   1     -12.223   3.927  -0.756  1.00 -1.29          O

HETATM    2  O   MOL A   1     -11.261  -0.944   1.796  1.00 -2.74          O

HETATM    3  O   MOL A   1     -10.919   4.129   1.863  1.00 -1.31          O

HETATM    4  O   MOL A   1     -10.554   0.243  -0.831  1.00 -1.70          O

HETATM    5  O   MOL A   1      -9.305   3.939  -1.153  1.00 -1.25          O

HETATM    6  O   MOL A   1      -8.865  -4.331   0.213  1.00 -1.77          O

HETATM    7  O   MOL A   1      -8.095  -4.840  -1.074  1.00 -1.79          O

HETATM    8  O   MOL A   1      -7.691  -0.703  -0.592  1.00 -1.84          O

HETATM    9  O   MOL A   1      -6.931  -1.270  -1.884  1.00 -1.85          O

HETATM   10  O   MOL A   1      -6.421  -1.894   2.897  1.00 -2.29          O

HETATM   11  O   MOL A   1      -5.225   6.853   1.149  1.00 -2.07          O

HETATM   12  O   MOL A   1      -4.688   2.951   1.214  1.00 -2.17          O

HETATM   13  O   MOL A   1      -4.602   3.259   2.420  1.00 -2.23          O

HETATM   14  O   MOL A   1      -3.988  -5.400   1.862  1.00 -1.97          O

HETATM   15  O   MOL A   1      -3.589  -5.982  -0.526  1.00 -1.93          O

HETATM   16  O   MOL A   1      -3.423  -6.208  -2.032  1.00 -1.95          O

HETATM   17  O   MOL A   1      -2.559   6.799  -0.367  1.00 -1.86          O

HETATM   18  O   MOL A   1      -2.431  -2.510  -2.568  1.00 -2.12          O

HETATM   19  O   MOL A   1      -2.050   6.045   4.024  1.00 -3.13          O

HETATM   20  O   MOL A   1      -1.967   3.208   0.752  1.00 -2.01          O

HETATM   21  O   MOL A   1      -1.564  -5.920   1.963  1.00 -1.97          O

HETATM   22  O   MOL A   1      -0.254  -6.464   0.831  1.00 -1.87          O

HETATM   23  O   MOL A   1       0.264  -1.014   3.147  1.00 -3.29          O

HETATM   24  O   MOL A   1       0.426  -3.462  -3.676  1.00 -2.61          O

HETATM   25  O   MOL A   1       1.580   9.194  -0.761  1.00 -1.48          O

HETATM   26  O   MOL A   1       1.685  -6.157   2.578  1.00 -2.00          O

HETATM   27  O   MOL A   1       2.393  -3.160  -2.732  1.00 -2.42          O

HETATM   28  O   MOL A   1       2.320   0.948   1.000  1.00 -2.27          O

HETATM   29  O   MOL A   1       2.621  -5.515   4.125  1.00 -2.04          O

HETATM   30  O   MOL A   1       2.545   6.988  -3.614  1.00 -1.44          O

HETATM   31  O   MOL A   1       2.747   8.575   0.719  1.00 -1.30          O

HETATM   32  O   MOL A   1       3.024   9.223  -2.416  1.00 -1.46          O

HETATM   33  O   MOL A   1       3.136  -6.229   2.498  1.00 -2.00          O

HETATM   34  O   MOL A   1       3.173   2.240  -2.911  1.00 -1.85          O

HETATM   35  O   MOL A   1       3.788  -0.640  -3.093  1.00 -2.29          O

HETATM   36  O   MOL A   1       4.446  -2.751  -2.491  1.00 -2.46          O

HETATM   37  O   MOL A   1       5.302  -6.618  -2.264  1.00 -2.10          O

HETATM   38  O   MOL A   1       5.598  -1.783   3.432  1.00 -3.59          O

HETATM   39  O   MOL A   1       6.284   7.164  -2.887  1.00 -1.63          O

HETATM   40  O   MOL A   1       6.510   0.001   3.846  1.00 -4.59          O

HETATM   41  O   MOL A   1       6.943   7.366  -1.709  1.00 -1.64          O

HETATM   42  O   MOL A   1       7.383  -5.598   0.196  1.00 -2.35          O

HETATM   43  O   MOL A   1       7.611  -2.619  -2.271  1.00 -3.19          O

HETATM   44  O   MOL A   1       8.240  -4.234   3.054  1.00 -2.34          O

HETATM   45  O   MOL A   1       8.430   0.880   1.159  1.00 -4.75          O

END

Table SS 18. DOCHN with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.904   2.464   1.074  1.00 -1.70          C

HETATM    2  C   MOL A   1     -13.439   0.954  -2.339  1.00 -1.79          C

HETATM    3  C   MOL A   1     -12.580  -0.956   0.675  1.00 -1.93          C

HETATM    4  C   MOL A   1     -11.868   4.160  -1.157  1.00 -1.89          C

HETATM    5  C   MOL A   1     -11.400   3.945   2.773  1.00 -1.84          C

HETATM    6  C   MOL A   1     -11.222   0.397   2.820  1.00 -2.02          C

HETATM    7  C   MOL A   1      -9.327   4.673  -0.045  1.00 -2.18          C

HETATM    8  C   MOL A   1      -8.603   3.902   3.699  1.00 -2.01          C

HETATM    9  C   MOL A   1      -8.284   0.413   3.447  1.00 -2.22          C

HETATM   10  C   MOL A   1      -7.511  -4.458  -1.877  1.00 -1.66          C

HETATM   11  C   MOL A   1      -6.873  -0.569  -5.136  1.00 -1.96          C

HETATM   12  C   MOL A   1      -6.318   4.899   0.904  1.00 -2.15          C

HETATM   13  C   MOL A   1      -5.604   3.787   4.362  1.00 -1.86          C

HETATM   14  C   MOL A   1      -4.721  -7.704   0.435  1.00  0.84          C

HETATM   15  C   MOL A   1      -3.907   4.784   1.165  1.00 -1.90          C

HETATM   16  C   MOL A   1      -3.673  -1.808   6.319  1.00 -1.16          C

HETATM   17  C   MOL A   1      -3.117  -1.427  -4.942  1.00 -1.80          C

HETATM   18  C   MOL A   1      -3.015  -2.962   7.884  1.00 -0.95          C

HETATM   19  C   MOL A   1      -2.917   4.187   4.462  1.00 -1.61          C

HETATM   20  C   MOL A   1      -2.781  -1.201   2.494  1.00 -1.88          C

HETATM   21  C   MOL A   1      -2.645  -3.633  -0.017  1.00 -2.15          C

HETATM   22  C   MOL A   1      -2.523   4.352  -0.689  1.00 -1.85          C

HETATM   23  C   MOL A   1      -1.859  -1.894  -0.910  1.00 -2.22          C

HETATM   24  C   MOL A   1      -1.775   5.789   2.755  1.00 -1.48          C

HETATM   25  C   MOL A   1      -1.609  -3.306  -4.056  1.00 -1.82          C

HETATM   26  C   MOL A   1      -1.536   3.034  -4.701  1.00 -1.06          C

HETATM   27  C   MOL A   1      -1.384  -0.090  -1.554  1.00 -2.32          C

HETATM   28  C   MOL A   1      -1.162   5.144  -2.366  1.00 -1.53          C

HETATM   29  C   MOL A   1      -0.834  -1.060  -4.848  1.00 -1.91          C

HETATM   30  C   MOL A   1      -0.614   7.339   0.953  1.00 -1.37          C

HETATM   31  C   MOL A   1      -0.524   0.453   8.177  1.00 -2.14          C

HETATM   32  C   MOL A   1      -0.494   4.702   4.570  1.00 -1.32          C

HETATM   33  C   MOL A   1      -0.212  -7.578   0.431  1.00 -0.85          C

HETATM   34  C   MOL A   1      -0.139  -3.582   9.999  1.00 -0.78          C

HETATM   35  C   MOL A   1       0.181   6.412  -3.886  1.00 -1.24          C

HETATM   36  C   MOL A   1       0.205  -1.352  -0.744  1.00 -2.07          C

HETATM   37  C   MOL A   1       0.279  -3.417   0.198  1.00 -2.00          C

HETATM   38  C   MOL A   1       0.310   3.641  -4.322  1.00 -1.11          C

HETATM   39  C   MOL A   1       0.674  -1.953   5.972  1.00 -2.23          C

HETATM   40  C   MOL A   1       0.766   8.886  -0.750  1.00 -1.18          C

HETATM   41  C   MOL A   1       0.945  -2.630  -3.856  1.00 -1.74          C

HETATM   42  C   MOL A   1       1.471  -2.867   0.356  1.00 -1.97          C

HETATM   43  C   MOL A   1       1.482   7.856  -5.359  1.00 -1.02          C

HETATM   44  C   MOL A   1       1.667   4.417   2.535  1.00 -1.37          C

HETATM   45  C   MOL A   1       1.869  -6.261  -3.053  1.00 -1.03          C

HETATM   46  C   MOL A   1       1.866   2.691   2.972  1.00 -1.30          C

HETATM   47  C   MOL A   1       2.023   1.276  -5.966  1.00 -0.96          C

HETATM   48  C   MOL A   1       2.103  10.345  -2.286  1.00 -0.98          C

HETATM   49  C   MOL A   1       2.545   2.285   5.331  1.00 -1.04          C

HETATM   50  C   MOL A   1       2.928   6.292   1.017  1.00 -1.29          C

HETATM   51  C   MOL A   1       3.042  -1.680   9.687  1.00 -0.77          C

HETATM   52  C   MOL A   1       3.305   1.827   0.052  1.00 -0.13          C

HETATM   53  C   MOL A   1       3.325  -2.233  -3.221  1.00 -1.72          C

HETATM   54  C   MOL A   1       3.531  -2.039   0.862  1.00 -1.98          C

HETATM   55  C   MOL A   1       3.507   1.017   7.083  1.00 -0.90          C

HETATM   56  C   MOL A   1       3.780   5.318  -3.774  1.00 -1.16          C

HETATM   57  C   MOL A   1       4.175  10.384  -5.427  1.00 -0.81          C

HETATM   58  C   MOL A   1       4.348   7.868  -0.589  1.00 -1.10          C

HETATM   59  C   MOL A   1       4.469  -0.094   0.251  1.00 -1.73          C

HETATM   60  C   MOL A   1       4.643  -3.792  -1.922  1.00 -1.79          C

HETATM   61  C   MOL A   1       4.811   2.544  -3.070  1.00 -0.81          C

HETATM   62  C   MOL A   1       4.881  -6.093   1.621  1.00 -0.77          C

HETATM   63  C   MOL A   1       5.198   6.684  -5.179  1.00 -0.93          C

HETATM   64  C   MOL A   1       5.711  -1.598  -2.586  1.00 -1.75          C

HETATM   65  C   MOL A   1       5.767   9.284  -2.102  1.00 -0.90          C

HETATM   66  C   MOL A   1       6.645   0.736   0.700  1.00 -1.41          C

HETATM   67  C   MOL A   1       7.736  -4.138   1.464  1.00 -0.45          C

HETATM   68  C   MOL A   1       7.834  -0.634  -2.247  1.00 -1.39          C

HETATM   69  C   MOL A   1       8.296   0.159   1.624  1.00 -1.71          C

HETATM   70  C   MOL A   1       9.659   2.797  -1.157  1.00 -1.07          C

HETATM   71  C   MOL A   1      11.352  -3.026   2.139  1.00 -0.39          C

HETATM   72  C   MOL A   1      11.866  -1.479   3.724  1.00 -0.45          C

HETATM   73  C   MOL A   1      12.966  -2.884   0.745  1.00 -0.43          C

HETATM   74  C   MOL A   1      14.920   0.018   2.074  1.00 -0.67          C

HETATM    1  O   MOL A   1     -13.452   0.468  -0.203  1.00 -2.20          O

HETATM    2  O   MOL A   1     -12.156   0.575   1.492  1.00 -2.23          O

HETATM    3  O   MOL A   1      -9.526   1.816   3.249  1.00 -2.48          O

HETATM    4  O   MOL A   1      -8.044   4.275   1.302  1.00 -2.50          O

HETATM    5  O   MOL A   1      -7.459   0.129   0.314  1.00 -4.54          O

HETATM    6  O   MOL A   1      -7.350   1.891   3.752  1.00 -2.46          O

HETATM    7  O   MOL A   1      -7.263   1.736  -1.236  1.00 -4.56          O

HETATM    8  O   MOL A   1      -6.311  -4.805   0.001  1.00 -2.66          O

HETATM    9  O   MOL A   1      -5.582  -3.631  -4.143  1.00 -2.30          O

HETATM   10  O   MOL A   1      -5.415  -0.235   0.374  1.00 -4.45          O

HETATM   11  O   MOL A   1      -4.764   1.140  -2.030  1.00 -4.67          O

HETATM   12  O   MOL A   1      -3.136   4.940   0.907  1.00 -1.97          O

HETATM   13  O   MOL A   1      -2.914  -4.249   0.637  1.00 -2.30          O

HETATM   14  O   MOL A   1      -2.840  -6.367  -2.698  1.00 -2.01          O

HETATM   15  O   MOL A   1      -2.080   1.529   6.470  1.00 -2.29          O

HETATM   16  O   MOL A   1      -1.628  -2.032  -4.926  1.00 -1.97          O

HETATM   17  O   MOL A   1      -1.240  -0.335  -5.375  1.00 -2.01          O

HETATM   18  O   MOL A   1      -0.908  -4.138   0.748  1.00 -2.35          O

HETATM   19  O   MOL A   1      -0.825  -1.128   3.998  1.00 -2.42          O

HETATM   20  O   MOL A   1      -0.739   0.019   8.715  1.00 -2.19          O

HETATM   21  O   MOL A   1      -0.271   5.477   2.183  1.00 -1.66          O

HETATM   22  O   MOL A   1      -0.139  -1.604  -4.758  1.00 -1.95          O

HETATM   23  O   MOL A   1      -0.121   0.304   8.687  1.00 -2.19          O

HETATM   24  O   MOL A   1       0.188  -0.447   3.860  1.00 -2.41          O

HETATM   25  O   MOL A   1       0.291  -2.128  -0.179  1.00 -2.19          O

HETATM   26  O   MOL A   1       0.254   1.732  -1.172  1.00 -2.97          O

HETATM   27  O   MOL A   1       0.436  -2.566   6.264  1.00 -2.28          O

HETATM   28  O   MOL A   1       1.229  -4.553   1.345  1.00 -2.62          O

HETATM   29  O   MOL A   1       1.326  -2.040   6.179  1.00 -2.28          O

HETATM   30  O   MOL A   1       1.960  -2.844  -3.744  1.00 -1.81          O

HETATM   31  O   MOL A   1       2.009   3.400  -0.137  1.00 -1.93          O

HETATM   32  O   MOL A   1       2.411  -2.010   0.633  1.00 -2.07          O

HETATM   33  O   MOL A   1       2.500   3.640  -2.504  1.00 -2.27          O

HETATM   34  O   MOL A   1       2.979  -1.356  -4.010  1.00 -1.90          O

HETATM   35  O   MOL A   1       3.595   8.049  -5.640  1.00 -1.23          O

HETATM   36  O   MOL A   1       3.849  -2.593   1.578  1.00 -2.10          O

HETATM   37  O   MOL A   1       4.156  10.294  -3.068  1.00 -1.20          O

HETATM   38  O   MOL A   1       5.271  -2.960  -2.378  1.00 -1.87          O

HETATM   39  O   MOL A   1       5.295  -0.773  -3.428  1.00 -1.90          O

HETATM   40  O   MOL A   1       5.345  -4.300  -1.572  1.00 -1.90          O

HETATM   41  O   MOL A   1       7.357   2.562  -1.633  1.00 -2.20          O

HETATM   42  O   MOL A   1       7.409   2.505  -1.792  1.00 -2.20          O

HETATM   43  O   MOL A   1       8.299  -0.569   2.173  1.00 -1.80          O

HETATM   44  O   MOL A   1       8.854   0.939   1.697  1.00 -1.78          O

HETATM   45  O   MOL A   1       9.568  -2.068  -1.145  1.00 -1.76          O

HETATM   46  O   MOL A   1      10.159  -0.685  -1.594  1.00 -1.75          O

HETATM   47  O   MOL A   1      13.122   2.731   0.185  1.00 -2.75          O

END

Table SS 19. PHPN with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -12.178   0.674   4.888  1.00 -2.00          C

HETATM    2  C   MOL A   1     -11.609  -2.243   3.862  1.00 -2.06          C

HETATM    3  C   MOL A   1     -10.748  -4.319   4.503  1.00 -1.66          C

HETATM    4  C   MOL A   1      -9.473   2.896   5.292  1.00 -2.06          C

HETATM    5  C   MOL A   1      -8.791  -0.686   5.898  1.00 -2.22          C

HETATM    6  C   MOL A   1      -8.393  -6.825   3.862  1.00 -1.46          C

HETATM    7  C   MOL A   1      -8.202   0.529  -4.143  1.00 -1.65          C

HETATM    8  C   MOL A   1      -8.141   4.643  -1.059  1.00 -1.96          C

HETATM    9  C   MOL A   1      -5.445  -6.384   1.722  1.00 -1.55          C

HETATM   10  C   MOL A   1      -5.118  -2.181  -1.536  1.00 -2.27          C

HETATM   11  C   MOL A   1      -4.887  -2.208  -6.471  1.00  0.84          C

HETATM   12  C   MOL A   1      -4.805  -5.014  -0.713  1.00 -1.72          C

HETATM   13  C   MOL A   1      -4.408   4.527  -1.615  1.00 -1.79          C

HETATM   14  C   MOL A   1      -3.376  -4.513   2.575  1.00 -1.84          C

HETATM   15  C   MOL A   1      -3.210   5.603   2.915  1.00 -1.05          C

HETATM   16  C   MOL A   1      -3.200  -0.663  -2.477  1.00 -2.09          C

HETATM   17  C   MOL A   1      -2.833   1.042   4.153  1.00 -2.01          C

HETATM   18  C   MOL A   1      -2.755   0.718  -0.900  1.00 -2.15          C

HETATM   19  C   MOL A   1      -2.663   3.445  -3.043  1.00 -1.82          C

HETATM   20  C   MOL A   1      -2.500   1.782   0.693  1.00 -2.29          C

HETATM   21  C   MOL A   1      -2.261  -2.494   4.508  1.00 -1.76          C

HETATM   22  C   MOL A   1      -2.184   4.802  -1.058  1.00 -1.90          C

HETATM   23  C   MOL A   1      -1.871  -4.488  -2.330  1.00 -1.39          C

HETATM   24  C   MOL A   1      -1.431   5.554   3.743  1.00 -1.13          C

HETATM   25  C   MOL A   1      -0.903  -4.232   2.588  1.00 -1.58          C

HETATM   26  C   MOL A   1      -0.753   0.905  -0.258  1.00 -2.01          C

HETATM   27  C   MOL A   1      -0.590  -0.765  -1.682  1.00 -1.91          C

HETATM   28  C   MOL A   1      -0.449  -1.636  -6.067  1.00 -0.83          C

HETATM   29  C   MOL A   1      -0.446  -0.451  -1.936  1.00 -1.94          C

HETATM   30  C   MOL A   1      -0.210   3.766  -2.168  1.00 -1.72          C

HETATM   31  C   MOL A   1      -0.026  -5.885   0.529  1.00 -1.35          C

HETATM   32  C   MOL A   1       0.180  -2.185   4.456  1.00 -1.51          C

HETATM   33  C   MOL A   1       0.209   6.865   1.176  1.00 -0.96          C

HETATM   34  C   MOL A   1       0.428  -3.220  -3.690  1.00 -1.54          C

HETATM   35  C   MOL A   1       0.724  -0.610  -0.829  1.00 -1.92          C

HETATM   36  C   MOL A   1       0.837  -3.922   3.002  1.00 -1.40          C

HETATM   37  C   MOL A   1       0.835  -0.276  -1.294  1.00 -1.95          C

HETATM   38  C   MOL A   1       1.064   2.247  -5.494  1.00 -1.04          C

HETATM   39  C   MOL A   1       1.367  -5.527  -3.139  1.00 -1.08          C

HETATM   40  C   MOL A   1       2.112   3.635  -1.535  1.00 -1.69          C

HETATM   41  C   MOL A   1       2.267   1.389   3.154  1.00 -0.17          C

HETATM   42  C   MOL A   1       3.301   4.811   3.154  1.00 -0.79          C

HETATM   43  C   MOL A   1       3.773  -4.868  -3.593  1.00 -0.86          C

HETATM   44  C   MOL A   1       3.751  -1.509   3.269  1.00 -1.04          C

HETATM   45  C   MOL A   1       3.729   2.221  -2.726  1.00 -1.78          C

HETATM   46  C   MOL A   1       4.484   3.602  -0.737  1.00 -1.73          C

HETATM   47  C   MOL A   1       4.525  -1.630  -4.234  1.00 -0.87          C

HETATM   48  C   MOL A   1       5.669  -4.813   0.622  1.00 -2.00          C

HETATM   49  C   MOL A   1       5.861   1.178   2.304  1.00 -1.39          C

HETATM   50  C   MOL A   1       6.053  -1.745   3.429  1.00 -0.94          C

HETATM   51  C   MOL A   1       6.133  -4.968  -3.545  1.00 -0.71          C

HETATM   52  C   MOL A   1       6.491   3.872   0.235  1.00 -1.38          C

HETATM   53  C   MOL A   1       7.418  -7.345  -1.774  1.00 -0.79          C

HETATM   54  C   MOL A   1       7.561  -0.315  -2.364  1.00 -0.58          C

HETATM   55  C   MOL A   1       7.658   0.508   2.042  1.00 -1.70          C

HETATM   56  C   MOL A   1       7.953  -2.033   3.671  1.00 -0.88          C

HETATM   57  C   MOL A   1       8.293   3.212  -0.141  1.00 -1.66          C

HETATM   58  C   MOL A   1       8.366  -4.331  -3.767  1.00 -0.69          C

HETATM   59  C   MOL A   1       8.378   4.004   3.860  1.00 -1.04          C

HETATM   60  C   MOL A   1       9.795  -4.795   1.718  1.00 -0.68          C

HETATM   61  C   MOL A   1      10.135  -1.543   0.142  1.00 -0.64          C

HETATM   62  C   MOL A   1      10.319  -2.596  -0.907  1.00 -0.63          C

HETATM   63  C   MOL A   1      10.963  -6.171  -1.932  1.00 -0.60          C

HETATM   64  C   MOL A   1      11.001  -0.197  -0.900  1.00 -0.36          C

HETATM   65  C   MOL A   1      11.684  -1.189   0.839  1.00 -0.42          C

HETATM   66  C   MOL A   1      12.274   1.556  -1.201  1.00 -0.41          C

HETATM   67  C   MOL A   1      14.290   1.289   1.922  1.00 -0.65          C

HETATM    1  O   MOL A   1     -11.126   0.852   0.070  1.00 -4.51          O

HETATM    2  O   MOL A   1     -10.404  -0.800   4.851  1.00 -2.52          O

HETATM    3  O   MOL A   1      -9.632   0.684   5.548  1.00 -2.51          O

HETATM    4  O   MOL A   1      -6.961  -2.348   3.618  1.00 -3.28          O

HETATM    5  O   MOL A   1      -6.815  -1.323  -3.917  1.00 -2.68          O

HETATM    6  O   MOL A   1      -6.488   3.053  -3.714  1.00 -2.29          O

HETATM    7  O   MOL A   1      -6.089   1.938   1.552  1.00 -4.64          O

HETATM    8  O   MOL A   1      -5.757   0.232  -0.150  1.00 -4.22          O

HETATM    9  O   MOL A   1      -4.421  -4.745   1.239  1.00 -1.99          O

HETATM   10  O   MOL A   1      -3.522  -1.449  -2.969  1.00 -2.26          O

HETATM   11  O   MOL A   1      -3.466   1.364  -5.742  1.00 -2.00          O

HETATM   12  O   MOL A   1      -2.897   4.563  -2.010  1.00 -1.96          O

HETATM   13  O   MOL A   1      -2.695   5.480  -0.458  1.00 -2.00          O

HETATM   14  O   MOL A   1      -1.462  -1.317  -2.710  1.00 -2.26          O

HETATM   15  O   MOL A   1      -1.516   4.720  -1.422  1.00 -1.94          O

HETATM   16  O   MOL A   1      -0.948   2.324   3.386  1.00 -3.08          O

HETATM   17  O   MOL A   1       0.196  -1.074  -2.215  1.00 -2.20          O

HETATM   18  O   MOL A   1       0.438  -0.193  -1.054  1.00 -1.98          O

HETATM   19  O   MOL A   1       0.682   3.708  -2.408  1.00 -1.79          O

HETATM   20  O   MOL A   1       1.007  -1.074  -1.743  1.00 -2.22          O

HETATM   21  O   MOL A   1       1.640  -1.760  -3.888  1.00 -2.40          O

HETATM   22  O   MOL A   1       1.556   4.491  -0.973  1.00 -1.88          O

HETATM   23  O   MOL A   1       3.062  -4.948   0.206  1.00 -2.15          O

HETATM   24  O   MOL A   1       3.080  -4.532   1.028  1.00 -2.15          O

HETATM   25  O   MOL A   1       3.292  -0.835  -0.423  1.00 -2.53          O

HETATM   26  O   MOL A   1       3.848   4.482  -0.220  1.00 -1.88          O

HETATM   27  O   MOL A   1       4.165   2.974  -2.049  1.00 -1.86          O

HETATM   28  O   MOL A   1       4.465   1.827  -3.202  1.00 -1.89          O

HETATM   29  O   MOL A   1       5.197  -1.868  -2.057  1.00 -1.84          O

HETATM   30  O   MOL A   1       5.509  -4.647   1.330  1.00 -2.04          O

HETATM   31  O   MOL A   1       6.046   4.079   3.428  1.00 -2.17          O

HETATM   32  O   MOL A   1       8.300   0.602   2.598  1.00 -1.75          O

HETATM   33  O   MOL A   1       8.454   2.825  -0.897  1.00 -1.74          O

HETATM   34  O   MOL A   1       8.867  -6.832  -2.451  1.00 -1.01          O

HETATM   35  O   MOL A   1       8.932   3.780   0.444  1.00 -1.73          O

HETATM   36  O   MOL A   1      12.047   3.392   4.112  1.00 -2.73          O

END

Table SS 20. Squalane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.884   4.507  -1.501  1.00 -1.97          C

HETATM    2  C   MOL A   1     -13.683   2.746  -3.904  1.00 -1.95          C

HETATM    3  C   MOL A   1     -11.673   6.841  -2.858  1.00 -1.87          C

HETATM    4  C   MOL A   1     -11.515   5.008  -5.398  1.00 -1.87          C

HETATM    5  C   MOL A   1     -10.945   5.788   0.406  1.00 -2.11          C

HETATM    6  C   MOL A   1     -10.485   1.617  -5.329  1.00 -2.10          C

HETATM    7  C   MOL A   1     -10.284  -3.002  -0.516  1.00 -2.01          C

HETATM    8  C   MOL A   1      -9.732  -0.741   3.968  1.00 -1.67          C

HETATM    9  C   MOL A   1      -9.072   6.060   0.071  1.00 -2.21          C

HETATM   10  C   MOL A   1      -9.052   6.087  -3.889  1.00 -2.13          C

HETATM   11  C   MOL A   1      -8.408   2.828  -4.528  1.00 -2.46          C

HETATM   12  C   MOL A   1      -6.633  -3.956  -0.159  1.00 -1.84          C

HETATM   13  C   MOL A   1      -6.332   5.871  -3.414  1.00 -2.08          C

HETATM   14  C   MOL A   1      -6.135   6.235   0.143  1.00 -2.01          C

HETATM   15  C   MOL A   1      -6.100  -0.094   7.247  1.00  0.83          C

HETATM   16  C   MOL A   1      -5.799   3.149  -4.732  1.00 -2.13          C

HETATM   17  C   MOL A   1      -5.401  -3.043  -4.684  1.00 -1.13          C

HETATM   18  C   MOL A   1      -4.768  -3.995   1.588  1.00 -1.86          C

HETATM   19  C   MOL A   1      -4.539  -0.042   2.932  1.00 -2.19          C

HETATM   20  C   MOL A   1      -4.434  -4.371  -0.860  1.00 -1.96          C

HETATM   21  C   MOL A   1      -4.191  -0.634   0.971  1.00 -2.29          C

HETATM   22  C   MOL A   1      -4.067  -0.922  -1.039  1.00 -2.42          C

HETATM   23  C   MOL A   1      -3.913   5.648   0.197  1.00 -1.85          C

HETATM   24  C   MOL A   1      -3.656   4.974  -3.457  1.00 -1.88          C

HETATM   25  C   MOL A   1      -3.564  -3.032  -5.455  1.00 -1.21          C

HETATM   26  C   MOL A   1      -2.565   1.872  -3.124  1.00 -2.08          C

HETATM   27  C   MOL A   1      -2.291  -4.291   0.570  1.00 -1.78          C

HETATM   28  C   MOL A   1      -2.288  -0.876   0.174  1.00 -2.13          C

HETATM   29  C   MOL A   1      -2.207  -5.556  -3.795  1.00 -1.03          C

HETATM   30  C   MOL A   1      -2.213   0.225  -1.183  1.00 -2.18          C

HETATM   31  C   MOL A   1      -1.850  -1.177   6.469  1.00 -0.86          C

HETATM   32  C   MOL A   1      -1.775   5.127   0.913  1.00 -1.59          C

HETATM   33  C   MOL A   1      -1.685  -0.523   2.375  1.00 -2.00          C

HETATM   34  C   MOL A   1      -0.946  -4.689   4.127  1.00 -1.06          C

HETATM   35  C   MOL A   1      -0.958   4.657  -2.822  1.00 -1.59          C

HETATM   36  C   MOL A   1      -0.561  -0.529   1.653  1.00 -1.97          C

HETATM   37  C   MOL A   1       0.012   4.848   1.858  1.00 -1.38          C

HETATM   38  C   MOL A   1       0.154  -4.198  -0.062  1.00 -1.75          C

HETATM   39  C   MOL A   1       0.630   2.752  -3.544  1.00 -1.43          C

HETATM   40  C   MOL A   1       0.793  -0.262  -3.331  1.00 -0.41          C

HETATM   41  C   MOL A   1       1.247  -3.239  -4.801  1.00 -0.88          C

HETATM   42  C   MOL A   1       1.463  -0.384   0.674  1.00 -2.02          C

HETATM   43  C   MOL A   1       1.503   4.736  -1.717  1.00 -1.36          C

HETATM   44  C   MOL A   1       1.850  -3.728   1.587  1.00 -1.81          C

HETATM   45  C   MOL A   1       2.071  -0.724  -1.419  1.00 -1.76          C

HETATM   46  C   MOL A   1       2.449  -4.086  -0.797  1.00 -1.77          C

HETATM   47  C   MOL A   1       2.701   5.686   3.496  1.00 -0.97          C

HETATM   48  C   MOL A   1       3.011   1.625  -1.225  1.00 -1.42          C

HETATM   49  C   MOL A   1       3.281  -1.044   4.556  1.00 -0.76          C

HETATM   50  C   MOL A   1       3.737   1.005   3.674  1.00 -1.11          C

HETATM   51  C   MOL A   1       3.806   4.978  -0.235  1.00 -1.15          C

HETATM   52  C   MOL A   1       4.052   2.358   5.476  1.00 -0.90          C

HETATM   53  C   MOL A   1       4.219  -0.707  -2.531  1.00 -1.43          C

HETATM   54  C   MOL A   1       4.503  -4.108  -1.985  1.00 -1.42          C

HETATM   55  C   MOL A   1       5.275   1.205  -0.197  1.00 -1.20          C

HETATM   56  C   MOL A   1       5.799  -1.527   2.235  1.00 -0.47          C

HETATM   57  C   MOL A   1       5.792   0.378   3.973  1.00 -0.86          C

HETATM   58  C   MOL A   1       5.964   5.146   1.039  1.00 -0.97          C

HETATM   59  C   MOL A   1       6.095  -0.444  -1.911  1.00 -1.72          C

HETATM   60  C   MOL A   1       6.301  -3.916  -1.417  1.00 -1.70          C

HETATM   61  C   MOL A   1       6.333   5.368   4.675  1.00 -0.78          C

HETATM   62  C   MOL A   1       6.391  -2.759  -5.319  1.00 -1.09          C

HETATM   63  C   MOL A   1       7.377   1.813   5.427  1.00 -0.77          C

HETATM   64  C   MOL A   1       7.600  -1.013   2.698  1.00 -0.71          C

HETATM   65  C   MOL A   1       7.720   3.963   4.062  1.00 -0.81          C

HETATM   66  C   MOL A   1       7.932   4.021   0.318  1.00 -0.86          C

HETATM   67  C   MOL A   1       9.347   4.395   2.534  1.00 -0.74          C

HETATM   68  C   MOL A   1       9.452  -1.766   0.720  1.00 -0.44          C

HETATM   69  C   MOL A   1       9.628   3.086  -1.899  1.00 -0.73          C

HETATM   70  C   MOL A   1       9.977  -0.848   4.358  1.00 -0.63          C

HETATM   71  C   MOL A   1      10.138  -0.037  -0.251  1.00 -0.54          C

HETATM   72  C   MOL A   1      10.144   0.525  -0.567  1.00 -0.65          C

HETATM   73  C   MOL A   1      10.458  -3.360   0.126  1.00 -0.45          C

HETATM   74  C   MOL A   1      11.023  -0.828   1.581  1.00 -0.64          C

HETATM   75  C   MOL A   1      11.064   2.866   5.274  1.00 -0.59          C

HETATM   76  C   MOL A   1      11.130   4.767   0.970  1.00 -0.65          C

HETATM   77  C   MOL A   1      12.494   0.010  -2.540  1.00 -0.73          C

HETATM   78  C   MOL A   1      12.537  -1.931  -2.620  1.00 -0.67          C

HETATM   79  C   MOL A   1      12.551   2.525   3.501  1.00 -0.62          C

HETATM   80  C   MOL A   1      12.707  -0.487  -0.309  1.00 -0.65          C

HETATM   81  C   MOL A   1      12.829   5.172  -0.723  1.00 -0.63          C

HETATM   82  C   MOL A   1      12.867   3.717  -4.277  1.00 -0.62          C

HETATM   83  C   MOL A   1      14.231   2.621   1.694  1.00 -0.59          C

HETATM   84  C   MOL A   1      14.767   0.051  -1.987  1.00 -0.59          C

HETATM   85  C   MOL A   1      15.071   3.770  -3.561  1.00 -0.54          C

HETATM   86  C   MOL A   1      15.855   3.145   0.229  1.00 -0.50          C

HETATM    1  O   MOL A   1     -12.707   4.739  -3.335  1.00 -2.40          O

HETATM    2  O   MOL A   1     -10.811   2.577   0.389  1.00 -4.63          O

HETATM    3  O   MOL A   1     -10.478   5.526  -3.798  1.00 -2.35          O

HETATM    4  O   MOL A   1      -9.520   5.926  -1.743  1.00 -2.58          O

HETATM    5  O   MOL A   1      -9.303   1.317  -2.006  1.00 -4.59          O

HETATM    6  O   MOL A   1      -9.301   3.780  -4.618  1.00 -2.60          O

HETATM    7  O   MOL A   1      -8.689  -1.065   5.297  1.00 -2.56          O

HETATM    8  O   MOL A   1      -8.721  -0.889   5.327  1.00 -2.56          O

HETATM    9  O   MOL A   1      -8.539  -3.163   2.420  1.00 -2.33          O

HETATM   10  O   MOL A   1      -7.980   0.608   4.566  1.00 -2.68          O

HETATM   11  O   MOL A   1      -7.532  -0.242  -1.724  1.00 -4.63          O

HETATM   12  O   MOL A   1      -7.415   4.022  -3.838  1.00 -2.66          O

HETATM   13  O   MOL A   1      -6.642   0.552  -0.458  1.00 -4.56          O

HETATM   14  O   MOL A   1      -5.306  -3.178   5.016  1.00 -2.04          O

HETATM   15  O   MOL A   1      -5.338   5.824  -1.832  1.00 -2.38          O

HETATM   16  O   MOL A   1      -5.099  -4.494   0.152  1.00 -2.01          O

HETATM   17  O   MOL A   1      -5.022  -4.585  -1.667  1.00 -2.06          O

HETATM   18  O   MOL A   1      -4.680   0.467   3.651  1.00 -2.33          O

HETATM   19  O   MOL A   1      -3.702  -4.596  -0.460  1.00 -2.00          O

HETATM   20  O   MOL A   1      -2.714   0.114   3.327  1.00 -2.34          O

HETATM   21  O   MOL A   1      -2.545  -0.308  -3.633  1.00 -3.22          O

HETATM   22  O   MOL A   1      -0.551  -4.631  -0.951  1.00 -1.94          O

HETATM   23  O   MOL A   1      -0.424   0.020   3.565  1.00 -2.58          O

HETATM   24  O   MOL A   1      -0.164   3.863  -2.422  1.00 -1.69          O

HETATM   25  O   MOL A   1       0.226  -0.355   0.552  1.00 -2.08          O

HETATM   26  O   MOL A   1       1.564   1.795  -2.157  1.00 -1.73          O

HETATM   27  O   MOL A   1       1.823  -4.551  -1.746  1.00 -1.93          O

HETATM   28  O   MOL A   1       2.231  -4.126   0.564  1.00 -1.89          O

HETATM   29  O   MOL A   1       2.240  -0.632  -2.046  1.00 -1.80          O

HETATM   30  O   MOL A   1       2.169   0.053   1.062  1.00 -2.13          O

HETATM   31  O   MOL A   1       2.601  -3.700   2.137  1.00 -1.91          O

HETATM   32  O   MOL A   1       4.036  -2.649  -4.855  1.00 -2.23          O

HETATM   33  O   MOL A   1       5.753   3.149   5.043  1.00 -1.18          O

HETATM   34  O   MOL A   1       6.169   2.514  -0.359  1.00 -1.32          O

HETATM   35  O   MOL A   1       6.415  -0.128  -1.199  1.00 -1.80          O

HETATM   36  O   MOL A   1       6.581  -3.920  -0.640  1.00 -1.77          O

HETATM   37  O   MOL A   1       6.671  -0.333  -2.771  1.00 -1.80          O

HETATM   38  O   MOL A   1       6.886  -4.178  -2.151  1.00 -1.77          O

HETATM   39  O   MOL A   1       7.284   0.572   3.889  1.00 -1.01          O

HETATM   40  O   MOL A   1       7.697  -1.059   1.353  1.00 -0.85          O

HETATM   41  O   MOL A   1       7.945   0.137   4.533  1.00 -1.03          O

HETATM   42  O   MOL A   1       8.830   3.178   5.090  1.00 -1.00          O

HETATM   43  O   MOL A   1       9.284  -2.550  -5.634  1.00 -2.76          O

HETATM   44  O   MOL A   1       9.262  -0.607   1.662  1.00 -0.91          O

HETATM   45  O   MOL A   1       9.399   3.387   0.117  1.00 -1.02          O

HETATM   46  O   MOL A   1      10.003  -2.486  -5.467  1.00 -2.77          O

HETATM   47  O   MOL A   1      10.631   1.482  -3.572  1.00 -1.20          O

HETATM   48  O   MOL A   1      10.884   0.242   0.189  1.00 -0.77          O

HETATM   49  O   MOL A   1      11.266   0.808   4.247  1.00 -0.97          O

HETATM   50  O   MOL A   1      12.578   0.650   2.205  1.00 -0.96          O

HETATM   51  O   MOL A   1      12.974   0.370  -1.747  1.00 -0.79          O

HETATM   52  O   MOL A   1      14.131   0.833   0.389  1.00 -0.93          O

HETATM   53  O   MOL A   1      15.060   4.303  -1.466  1.00 -0.86          O

END

Table SS 21. Hopane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -15.924   2.260  -2.823  1.00 -0.64          C

HETATM    2  C   MOL A   1     -14.191  -1.044  -3.096  1.00 -0.40          C

HETATM    3  C   MOL A   1     -12.741   1.695  -4.730  1.00 -0.42          C

HETATM    4  C   MOL A   1     -12.405  -0.430  -4.240  1.00 -0.35          C

HETATM    5  C   MOL A   1     -11.167   2.320   1.937  1.00 -1.07          C

HETATM    6  C   MOL A   1     -10.870  -1.098  -0.124  1.00 -1.64          C

HETATM    7  C   MOL A   1      -9.464   1.640  -1.788  1.00 -1.69          C

HETATM    8  C   MOL A   1      -9.368  -1.201   1.033  1.00 -1.35          C

HETATM    9  C   MOL A   1      -9.096   4.716  -0.758  1.00 -1.27          C

HETATM   10  C   MOL A   1      -8.872  -2.049  -3.941  1.00 -0.39          C

HETATM   11  C   MOL A   1      -7.906   1.532  -0.512  1.00 -1.46          C

HETATM   12  C   MOL A   1      -7.427   6.177   2.300  1.00 -1.18          C

HETATM   13  C   MOL A   1      -7.308  -2.317   0.990  1.00 -1.70          C

HETATM   14  C   MOL A   1      -7.251   2.486   2.533  1.00 -1.48          C

HETATM   15  C   MOL A   1      -6.357   0.422   3.927  1.00 -0.84          C

HETATM   16  C   MOL A   1      -6.188  -3.816  -0.694  1.00 -1.74          C

HETATM   17  C   MOL A   1      -6.063   2.576  -1.848  1.00 -1.45          C

HETATM   18  C   MOL A   1      -5.976  -3.684  -4.956  1.00 -0.71          C

HETATM   19  C   MOL A   1      -5.932   6.270  -1.312  1.00 -1.24          C

HETATM   20  C   MOL A   1      -5.835   0.349  -0.594  1.00 -1.83          C

HETATM   21  C   MOL A   1      -5.054  -3.312   1.396  1.00 -1.65          C

HETATM   22  C   MOL A   1      -4.831   6.180   2.254  1.00 -1.32          C

HETATM   23  C   MOL A   1      -4.734  -0.929  -1.940  1.00 -1.90          C

HETATM   24  C   MOL A   1      -4.126  -2.151   5.673  1.00 -0.88          C

HETATM   25  C   MOL A   1      -3.539  -6.642  -0.913  1.00 -1.00          C

HETATM   26  C   MOL A   1      -3.535   6.078  -1.299  1.00 -1.32          C

HETATM   27  C   MOL A   1      -3.245   4.781  -2.595  1.00 -1.39          C

HETATM   28  C   MOL A   1      -2.754  -4.208   1.863  1.00 -1.65          C

HETATM   29  C   MOL A   1      -2.792  -1.928  -1.709  1.00 -1.85          C

HETATM   30  C   MOL A   1      -2.188   0.881   1.032  1.00 -0.11          C

HETATM   31  C   MOL A   1      -2.117   6.256   2.164  1.00 -1.35          C

HETATM   32  C   MOL A   1      -1.993   0.597   5.868  1.00 -1.00          C

HETATM   33  C   MOL A   1      -1.705  -2.504  -1.794  1.00 -1.90          C

HETATM   34  C   MOL A   1      -1.393   7.090  -0.200  1.00 -1.38          C

HETATM   35  C   MOL A   1      -1.071  -5.749  -4.400  1.00 -0.84          C

HETATM   36  C   MOL A   1      -1.053  -3.603   3.768  1.00 -1.80          C

HETATM   37  C   MOL A   1      -0.351  -0.112   6.012  1.00 -0.90          C

HETATM   38  C   MOL A   1      -0.378   6.421  -3.693  1.00 -1.25          C

HETATM   39  C   MOL A   1      -0.216  -5.003   1.943  1.00 -1.74          C

HETATM   40  C   MOL A   1      -0.140   2.637  -3.467  1.00 -1.48          C

HETATM   41  C   MOL A   1       0.273  -1.959   0.310  1.00 -2.04          C

HETATM   42  C   MOL A   1       0.282   5.746   2.574  1.00 -1.42          C

HETATM   43  C   MOL A   1       0.568   1.364   0.113  1.00 -1.74          C

HETATM   44  C   MOL A   1       0.919   1.460   0.918  1.00 -1.74          C

HETATM   45  C   MOL A   1       1.067  -2.911  -1.470  1.00 -2.11          C

HETATM   46  C   MOL A   1       1.225  -4.058   3.848  1.00 -1.68          C

HETATM   47  C   MOL A   1       1.311   6.860  -2.574  1.00 -1.41          C

HETATM   48  C   MOL A   1       1.469  -1.233   1.792  1.00 -1.99          C

HETATM   49  C   MOL A   1       1.478   8.458   0.129  1.00 -1.27          C

HETATM   50  C   MOL A   1       2.661   0.275  -3.132  1.00 -1.97          C

HETATM   51  C   MOL A   1       3.141   5.678  -2.431  1.00 -1.60          C

HETATM   52  C   MOL A   1       3.381  -5.998  -4.073  1.00  0.74          C

HETATM   53  C   MOL A   1       3.621   3.213   3.709  1.00 -1.87          C

HETATM   54  C   MOL A   1       3.630   6.398   3.062  1.00 -1.49          C

HETATM   55  C   MOL A   1       4.068   3.359  -3.882  1.00 -1.69          C

HETATM   56  C   MOL A   1       4.389   7.086  -0.667  1.00 -1.48          C

HETATM   57  C   MOL A   1       4.654  -2.898   4.819  1.00 -2.15          C

HETATM   58  C   MOL A   1       4.749   3.297  -4.138  1.00 -1.68          C

HETATM   59  C   MOL A   1       4.887   0.511  -4.154  1.00 -2.01          C

HETATM   60  C   MOL A   1       5.506  -5.357   0.283  1.00 -2.15          C

HETATM   61  C   MOL A   1       5.685   5.770   2.290  1.00 -1.74          C

HETATM   62  C   MOL A   1       6.229  -5.051   2.977  1.00 -1.84          C

HETATM   63  C   MOL A   1       6.564   5.293  -1.692  1.00 -1.70          C

HETATM   64  C   MOL A   1       7.441  -1.858  -3.921  1.00 -2.03          C

HETATM   65  C   MOL A   1       7.479   5.146  -0.637  1.00 -1.83          C

HETATM   66  C   MOL A   1       8.367   2.809  -3.684  1.00 -1.80          C

HETATM   67  C   MOL A   1       8.505   3.673   2.565  1.00 -1.97          C

HETATM   68  C   MOL A   1       8.657  -3.312  -3.620  1.00 -1.83          C

HETATM   69  C   MOL A   1       8.877   4.232  -2.233  1.00 -1.87          C

HETATM   70  C   MOL A   1       9.227   3.034   2.484  1.00 -2.01          C

HETATM   71  C   MOL A   1       9.493  -4.005  -0.826  1.00 -2.17          C

HETATM   72  C   MOL A   1       9.877  -0.054  -4.845  1.00 -1.65          C

HETATM   73  C   MOL A   1       9.867   1.688  -4.267  1.00 -1.69          C

HETATM   74  C   MOL A   1      10.892   3.673   0.503  1.00 -1.82          C

HETATM   75  C   MOL A   1      11.139  -1.167   1.620  1.00 -2.07          C

HETATM   76  C   MOL A   1      12.062  -2.474  -3.376  1.00 -1.57          C

HETATM   77  C   MOL A   1      12.383  -2.911  -0.836  1.00 -1.70          C

HETATM   78  C   MOL A   1      12.403   0.653   0.562  1.00 -1.78          C

HETATM   79  C   MOL A   1      12.388   3.269  -2.191  1.00 -1.53          C

HETATM   80  C   MOL A   1      12.973  -0.228  -2.776  1.00 -1.60          C

HETATM    1  O   MOL A   1     -14.245   3.354   0.510  1.00 -2.73          O

HETATM    2  O   MOL A   1     -13.608   3.291   0.914  1.00 -2.73          O

HETATM    3  O   MOL A   1     -11.650  -0.650   0.355  1.00 -1.71          O

HETATM    4  O   MOL A   1     -11.008  -1.645  -0.829  1.00 -1.72          O

HETATM    5  O   MOL A   1      -9.863   2.424  -1.300  1.00 -1.78          O

HETATM    6  O   MOL A   1      -9.342   1.355  -2.588  1.00 -1.77          O

HETATM    7  O   MOL A   1      -8.858   1.749   2.407  1.00 -2.22          O

HETATM    8  O   MOL A   1      -8.390   2.407   0.252  1.00 -1.91          O

HETATM    9  O   MOL A   1      -8.217   2.330   0.205  1.00 -1.90          O

HETATM   10  O   MOL A   1      -7.893   5.977   0.198  1.00 -1.55          O

HETATM   11  O   MOL A   1      -7.024  -2.109   2.186  1.00 -1.84          O

HETATM   12  O   MOL A   1      -6.883  -3.336   0.110  1.00 -1.82          O

HETATM   13  O   MOL A   1      -6.801  -4.045  -1.391  1.00 -1.84          O

HETATM   14  O   MOL A   1      -5.101  -0.839  -2.735  1.00 -2.01          O

HETATM   15  O   MOL A   1      -4.921   1.436   1.273  1.00 -2.46          O

HETATM   16  O   MOL A   1      -4.822  -3.106   2.489  1.00 -1.82          O

HETATM   17  O   MOL A   1      -4.495   3.913  -1.638  1.00 -1.69          O

HETATM   18  O   MOL A   1      -3.990  -0.904  -1.550  1.00 -1.95          O

HETATM   19  O   MOL A   1      -3.857   2.546   3.513  1.00 -2.83          O

HETATM   20  O   MOL A   1      -3.696  -4.340   1.467  1.00 -1.74          O

HETATM   21  O   MOL A   1      -3.303   5.974   0.748  1.00 -1.57          O

HETATM   22  O   MOL A   1      -2.505   6.097   0.355  1.00 -1.58          O

HETATM   23  O   MOL A   1      -2.469  -2.796  -3.534  1.00 -2.51          O

HETATM   24  O   MOL A   1      -1.950   6.191  -2.118  1.00 -1.62          O

HETATM   25  O   MOL A   1      -1.796  -3.954   3.306  1.00 -1.85          O

HETATM   26  O   MOL A   1      -1.773   2.730  -2.016  1.00 -1.79          O

HETATM   27  O   MOL A   1      -0.726  -3.276   4.721  1.00 -1.90          O

HETATM   28  O   MOL A   1      -0.329  -2.879  -2.582  1.00 -2.28          O

HETATM   29  O   MOL A   1      -0.046   7.013   0.994  1.00 -1.67          O

HETATM   30  O   MOL A   1       0.194   2.017   0.995  1.00 -1.87          O

HETATM   31  O   MOL A   1       0.352   7.114  -0.915  1.00 -1.61          O

HETATM   32  O   MOL A   1       0.542  -0.181   2.609  1.00 -2.14          O

HETATM   33  O   MOL A   1       1.307  -6.805  -0.989  1.00 -2.03          O

HETATM   34  O   MOL A   1       1.384   4.391  -2.780  1.00 -1.82          O

HETATM   35  O   MOL A   1       1.693  -3.085  -2.348  1.00 -2.32          O

HETATM   36  O   MOL A   1       2.587   3.677  -3.193  1.00 -1.84          O

HETATM   37  O   MOL A   1       2.808   6.839  -0.983  1.00 -1.64          O

HETATM   38  O   MOL A   1       3.274  -1.010   3.680  1.00 -3.13          O

HETATM   39  O   MOL A   1       3.685  -5.925   1.230  1.00 -2.29          O

HETATM   40  O   MOL A   1       4.059   1.208  -3.652  1.00 -2.16          O

HETATM   41  O   MOL A   1       4.897   4.391  -2.561  1.00 -2.03          O

HETATM   42  O   MOL A   1       4.987  -4.095  -1.767  1.00 -3.18          O

HETATM   43  O   MOL A   1       6.301  -2.601  -1.238  1.00 -4.35          O

HETATM   44  O   MOL A   1       6.296   5.240   0.346  1.00 -2.06          O

HETATM   45  O   MOL A   1       6.441   0.019   3.730  1.00 -4.44          O

HETATM   46  O   MOL A   1       6.465   1.296  -3.929  1.00 -2.30          O

HETATM   47  O   MOL A   1       6.537  -0.057  -4.101  1.00 -2.32          O

HETATM   48  O   MOL A   1       6.951   4.159  -3.616  1.00 -2.05          O

HETATM   49  O   MOL A   1       7.890  -1.705   1.146  1.00 -4.12          O

HETATM   50  O   MOL A   1       8.907   3.989   0.820  1.00 -2.28          O

HETATM   51  O   MOL A   1      10.041  -3.462  -1.706  1.00 -2.26          O

HETATM   52  O   MOL A   1      11.181   0.297  -3.581  1.00 -1.99          O

HETATM   53  O   MOL A   1      11.809  -1.312   0.699  1.00 -2.18          O

HETATM   54  O   MOL A   1      12.616   1.360  -1.002  1.00 -1.96          O

END

Table SS 22. Phenol with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -13.343   3.396   2.702  1.00 -1.58          C

HETATM    2  C   MOL A   1     -11.831   5.026  -0.272  1.00 -1.71          C

HETATM    3  C   MOL A   1     -11.222   6.246   3.129  1.00 -1.56          C

HETATM    4  C   MOL A   1     -10.043   2.964   4.527  1.00 -1.91          C

HETATM    5  C   MOL A   1      -8.947   5.026  -0.499  1.00 -2.08          C

HETATM    6  C   MOL A   1      -8.875  -4.267   0.071  1.00 -1.68          C

HETATM    7  C   MOL A   1      -8.452   5.986   2.867  1.00 -1.91          C

HETATM    8  C   MOL A   1      -8.376  -1.084  -3.806  1.00 -1.96          C

HETATM    9  C   MOL A   1      -7.970   4.242  -3.323  1.00 -1.91          C

HETATM   10  C   MOL A   1      -7.460   5.423  -1.062  1.00 -2.01          C

HETATM   11  C   MOL A   1      -7.129   2.743   4.250  1.00 -2.14          C

HETATM   12  C   MOL A   1      -6.170  -7.357   2.755  1.00  0.82          C

HETATM   13  C   MOL A   1      -5.613   5.563   2.377  1.00 -2.08          C

HETATM   14  C   MOL A   1      -5.621   6.812  -3.251  1.00 -1.52          C

HETATM   15  C   MOL A   1      -5.205   4.073  -5.632  1.00 -1.51          C

HETATM   16  C   MOL A   1      -4.645  -2.514  -3.886  1.00 -1.88          C

HETATM   17  C   MOL A   1      -4.487   6.540  -1.029  1.00 -1.74          C

HETATM   18  C   MOL A   1      -4.093   0.185   4.051  1.00 -1.69          C

HETATM   19  C   MOL A   1      -3.775  -3.784   1.274  1.00 -2.19          C

HETATM   20  C   MOL A   1      -3.781  -2.510   6.286  1.00 -1.35          C

HETATM   21  C   MOL A   1      -3.766  -0.914  -0.785  1.00 -2.67          C

HETATM   22  C   MOL A   1      -3.223  -0.289   5.964  1.00 -1.46          C

HETATM   23  C   MOL A   1      -3.127  -4.339  -2.853  1.00 -1.89          C

HETATM   24  C   MOL A   1      -2.925  -2.368  -0.013  1.00 -2.35          C

HETATM   25  C   MOL A   1      -2.575   1.687  -4.741  1.00 -1.26          C

HETATM   26  C   MOL A   1      -2.365  -0.858  -0.963  1.00 -2.59          C

HETATM   27  C   MOL A   1      -2.258  -5.280   4.457  1.00 -1.37          C

HETATM   28  C   MOL A   1      -2.249  -2.422  -4.099  1.00 -2.01          C

HETATM   29  C   MOL A   1      -2.172   1.724  -0.441  1.00 -2.98          C

HETATM   30  C   MOL A   1      -1.757  -7.799   2.305  1.00 -0.87          C

HETATM   31  C   MOL A   1      -1.721   5.912  -2.305  1.00 -1.29          C

HETATM   32  C   MOL A   1      -1.395  -3.717   1.157  1.00 -2.15          C

HETATM   33  C   MOL A   1      -1.224   2.977   3.344  1.00 -2.56          C

HETATM   34  C   MOL A   1      -0.904  -2.092  -0.129  1.00 -2.25          C

HETATM   35  C   MOL A   1      -0.764   2.021  -4.690  1.00 -1.39          C

HETATM   36  C   MOL A   1      -0.522  -3.984  -2.974  1.00 -1.81          C

HETATM   37  C   MOL A   1      -0.193  -3.064   6.596  1.00 -1.25          C

HETATM   38  C   MOL A   1       0.091  -7.444  -1.603  1.00 -1.07          C

HETATM   39  C   MOL A   1       0.176   4.360   1.957  1.00 -2.28          C

HETATM   40  C   MOL A   1       0.554  -0.469   5.762  1.00 -1.33          C

HETATM   41  C   MOL A   1       0.673  -0.687  -5.871  1.00 -1.12          C

HETATM   42  C   MOL A   1       1.081  -1.159   1.443  1.00 -1.99          C

HETATM   43  C   MOL A   1       1.528  -2.201   4.599  1.00 -1.42          C

HETATM   44  C   MOL A   1       1.526   5.788   0.607  1.00 -2.31          C

HETATM   45  C   MOL A   1       1.955  -3.695  -2.675  1.00 -1.78          C

HETATM   46  C   MOL A   1       2.414   0.583   3.971  1.00 -1.11          C

HETATM   47  C   MOL A   1       2.678  -2.905   1.303  1.00 -2.05          C

HETATM   48  C   MOL A   1       2.781   0.644  -0.345  1.00 -0.71          C

HETATM   49  C   MOL A   1       3.209  -5.184  -1.237  1.00 -1.83          C

HETATM   50  C   MOL A   1       3.606  -6.845   2.623  1.00 -0.77          C

HETATM   51  C   MOL A   1       3.747  -1.278   0.288  1.00 -1.86          C

HETATM   52  C   MOL A   1       3.708   7.105  -3.077  1.00  0.71          C

HETATM   53  C   MOL A   1       3.936   0.768  -3.569  1.00 -0.97          C

HETATM   54  C   MOL A   1       4.414  -3.280  -2.429  1.00 -1.79          C

HETATM   55  C   MOL A   1       4.485   1.459   4.777  1.00 -1.14          C

HETATM   56  C   MOL A   1       5.047   7.494  -1.895  1.00 -0.67          C

HETATM   57  C   MOL A   1       6.241  -0.200   5.024  1.00 -1.06          C

HETATM   58  C   MOL A   1       6.314   5.352   3.272  1.00 -1.09          C

HETATM   59  C   MOL A   1       6.560  -2.583  -2.514  1.00 -1.42          C

HETATM   60  C   MOL A   1       6.626  -5.367   1.754  1.00 -0.46          C

HETATM   61  C   MOL A   1       6.786   4.874  -2.692  1.00 -0.92          C

HETATM   62  C   MOL A   1       6.902   3.718   2.924  1.00 -1.08          C

HETATM   63  C   MOL A   1       7.331   2.726   0.638  1.00 -1.16          C

HETATM   64  C   MOL A   1       7.418   8.280   1.750  1.00 -0.91          C

HETATM   65  C   MOL A   1       7.892  -1.669   2.861  1.00 -1.39          C

HETATM   66  C   MOL A   1       8.207  -3.247  -1.754  1.00 -1.69          C

HETATM   67  C   MOL A   1       8.235   3.290  -0.609  1.00 -1.07          C

HETATM   68  C   MOL A   1       8.283   4.785   3.327  1.00 -0.91          C

HETATM   69  C   MOL A   1       8.542   1.938   3.028  1.00 -1.08          C

HETATM   70  C   MOL A   1       8.986   0.739  -2.255  1.00 -1.08          C

HETATM   71  C   MOL A   1       9.131   7.851  -1.363  1.00 -0.77          C

HETATM   72  C   MOL A   1      10.246   6.608   0.541  1.00 -0.82          C

HETATM   73  C   MOL A   1      10.443  -4.651   1.760  1.00 -0.40          C

HETATM   74  C   MOL A   1      11.305  -2.991   2.977  1.00 -0.47          C

HETATM   75  C   MOL A   1      11.862  -4.976   0.163  1.00 -0.44          C

HETATM   76  C   MOL A   1      14.244  -2.196   0.799  1.00 -0.68          C

HETATM    1  O   MOL A   1     -10.552  -0.140   0.538  1.00 -4.47          O

HETATM    2  O   MOL A   1      -9.409   5.580   0.957  1.00 -2.30          O

HETATM    3  O   MOL A   1      -9.106   1.832  -0.400  1.00 -4.44          O

HETATM    4  O   MOL A   1      -9.015   0.243   1.790  1.00 -4.51          O

HETATM    5  O   MOL A   1      -8.443  -2.909  -2.773  1.00 -2.32          O

HETATM    6  O   MOL A   1      -8.143  -5.691   0.558  1.00 -2.57          O

HETATM    7  O   MOL A   1      -8.199  -5.594   0.730  1.00 -2.57          O

HETATM    8  O   MOL A   1      -7.507  -4.451   1.896  1.00 -2.67          O

HETATM    9  O   MOL A   1      -7.101  -4.167  -2.451  1.00 -2.34          O

HETATM   10  O   MOL A   1      -7.118   5.250   0.952  1.00 -2.43          O

HETATM   11  O   MOL A   1      -7.031   5.306  -1.939  1.00 -2.13          O

HETATM   12  O   MOL A   1      -6.867   4.239   3.182  1.00 -2.42          O

HETATM   13  O   MOL A   1      -5.174   0.611  -1.267  1.00 -4.56          O

HETATM   14  O   MOL A   1      -4.576  -6.885  -0.794  1.00 -2.05          O

HETATM   15  O   MOL A   1      -4.156   5.274  -4.040  1.00 -1.89          O

HETATM   16  O   MOL A   1      -4.118   5.731  -2.301  1.00 -1.88          O

HETATM   17  O   MOL A   1      -4.007  -4.173   1.994  1.00 -2.32          O

HETATM   18  O   MOL A   1      -3.000  -3.155  -3.993  1.00 -2.05          O

HETATM   19  O   MOL A   1      -2.914   4.622   1.661  1.00 -2.69          O

HETATM   20  O   MOL A   1      -2.597  -1.649  -4.767  1.00 -2.11          O

HETATM   21  O   MOL A   1      -2.180  -4.251   1.914  1.00 -2.34          O

HETATM   22  O   MOL A   1      -2.077   3.074   3.449  1.00 -2.60          O

HETATM   23  O   MOL A   1      -1.777  -1.393   6.215  1.00 -1.69          O

HETATM   24  O   MOL A   1      -1.563  -2.841  -4.051  1.00 -2.05          O

HETATM   25  O   MOL A   1      -0.680  -2.645   0.667  1.00 -2.36          O

HETATM   26  O   MOL A   1      -0.445   1.386  -1.028  1.00 -3.71          O

HETATM   27  O   MOL A   1       0.282   5.991   0.645  1.00 -2.43          O

HETATM   28  O   MOL A   1       0.335  -5.299   2.598  1.00 -2.58          O

HETATM   29  O   MOL A   1       0.345   6.691  -3.731  1.00 -2.64          O

HETATM   30  O   MOL A   1       0.358  -1.956   5.165  1.00 -1.55          O

HETATM   31  O   MOL A   1       0.988  -2.752   1.274  1.00 -2.23          O

HETATM   32  O   MOL A   1       1.536  -2.923  -3.597  1.00 -1.99          O

HETATM   33  O   MOL A   1       1.959   4.098   2.791  1.00 -2.42          O

HETATM   34  O   MOL A   1       1.939   5.974   0.633  1.00 -2.33          O

HETATM   35  O   MOL A   1       2.794  -3.334   1.981  1.00 -2.13          O

HETATM   36  O   MOL A   1       3.604  -4.438  -2.071  1.00 -1.91          O

HETATM   37  O   MOL A   1       3.823  -5.696  -0.903  1.00 -1.93          O

HETATM   38  O   MOL A   1       3.850   1.797  -0.298  1.00 -2.11          O

HETATM   39  O   MOL A   1       3.884  -2.555  -3.370  1.00 -1.96          O

HETATM   40  O   MOL A   1       4.003  -0.249  -0.032  1.00 -1.96          O

HETATM   41  O   MOL A   1       6.524   0.739  -2.411  1.00 -2.25          O

HETATM   42  O   MOL A   1       6.680   1.766   4.017  1.00 -1.43          O

HETATM   43  O   MOL A   1       6.705   4.393   2.786  1.00 -1.14          O

HETATM   44  O   MOL A   1       7.159   8.480  -0.511  1.00 -1.13          O

HETATM   45  O   MOL A   1       8.109  -2.204   2.193  1.00 -1.66          O

HETATM   46  O   MOL A   1       8.314  -4.012  -1.395  1.00 -1.77          O

HETATM   47  O   MOL A   1       8.525  -0.294   0.875  1.00 -1.82          O

HETATM   48  O   MOL A   1       9.004  -2.791  -2.178  1.00 -1.77          O

HETATM   49  O   MOL A   1       9.162   3.570   1.415  1.00 -1.35          O

HETATM   50  O   MOL A   1      12.504   0.436  -1.337  1.00 -2.77          O

END

Table SS 23. Pyrrole with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -11.156   6.785   1.945  1.00 -1.79          C

HETATM    2  C   MOL A   1     -10.720   6.075   5.576  1.00 -1.63          C

HETATM    3  C   MOL A   1      -9.844   7.116   0.491  1.00 -1.89          C

HETATM    4  C   MOL A   1      -9.791  -6.898   1.183  1.00 -1.03          C

HETATM    5  C   MOL A   1      -9.685  -2.106  -0.934  1.00 -1.59          C

HETATM    6  C   MOL A   1      -9.611   2.668  -2.380  1.00 -2.02          C

HETATM    7  C   MOL A   1      -8.639   8.466   3.905  1.00 -1.60          C

HETATM    8  C   MOL A   1      -8.620  -8.992   1.451  1.00 -0.87          C

HETATM    9  C   MOL A   1      -7.621  -5.123   3.890  1.00 -1.23          C

HETATM   10  C   MOL A   1      -7.155   5.433   5.398  1.00 -1.95          C

HETATM   11  C   MOL A   1      -6.898  -6.067  -2.051  1.00  0.62          C

HETATM   12  C   MOL A   1      -6.913   6.067  -1.181  1.00 -1.96          C

HETATM   13  C   MOL A   1      -6.438  -7.428   4.274  1.00 -1.01          C

HETATM   14  C   MOL A   1      -6.436   7.641   2.305  1.00 -1.89          C

HETATM   15  C   MOL A   1      -6.322   2.036  -4.095  1.00 -1.78          C

HETATM   16  C   MOL A   1      -5.115  -2.144   4.611  1.00 -1.78          C

HETATM   17  C   MOL A   1      -5.013   5.241   4.019  1.00 -2.07          C

HETATM   18  C   MOL A   1      -4.880  -9.132   1.077  1.00 -0.90          C

HETATM   19  C   MOL A   1      -4.854  -0.049  -4.863  1.00 -1.81          C

HETATM   20  C   MOL A   1      -4.742   1.245  -1.000  1.00 -2.54          C

HETATM   21  C   MOL A   1      -4.586  -2.171  -1.242  1.00 -2.20          C

HETATM   22  C   MOL A   1      -4.540  -7.140   3.738  1.00 -1.12          C

HETATM   23  C   MOL A   1      -4.432  -7.245  -0.291  1.00 -1.11          C

HETATM   24  C   MOL A   1      -4.431  -1.932  -0.700  1.00 -2.19          C

HETATM   25  C   MOL A   1      -3.963   2.341  -4.753  1.00 -1.91          C

HETATM   26  C   MOL A   1      -3.904  -0.279  -1.540  1.00 -2.30          C

HETATM   27  C   MOL A   1      -3.825   5.803  -2.382  1.00 -1.05          C

HETATM   28  C   MOL A   1      -3.184   1.541  -1.442  1.00 -2.44          C

HETATM   29  C   MOL A   1      -3.081   7.368   2.484  1.00 -1.42          C

HETATM   30  C   MOL A   1      -2.837  -7.478   2.562  1.00 -1.06          C

HETATM   31  C   MOL A   1      -2.767  -5.904  -3.558  1.00 -0.93          C

HETATM   32  C   MOL A   1      -2.562  -7.429   4.355  1.00 -1.11          C

HETATM   33  C   MOL A   1      -2.453   4.717  -1.253  1.00 -1.73          C

HETATM   34  C   MOL A   1      -2.181   0.514  -5.273  1.00 -1.75          C

HETATM   35  C   MOL A   1      -2.136   6.162  -2.448  1.00 -1.13          C

HETATM   36  C   MOL A   1      -1.919   8.134  -1.780  1.00 -1.16          C

HETATM   37  C   MOL A   1      -1.973   9.174   2.153  1.00 -1.14          C

HETATM   38  C   MOL A   1      -1.808  -2.966  -6.640  1.00 -1.08          C

HETATM   39  C   MOL A   1      -1.838   0.197  -1.849  1.00 -2.18          C

HETATM   40  C   MOL A   1      -1.501  -2.184  -2.134  1.00 -2.16          C

HETATM   41  C   MOL A   1      -1.371  -7.913   0.700  1.00 -1.12          C

HETATM   42  C   MOL A   1      -1.180   4.872  -5.534  1.00 -1.01          C

HETATM   43  C   MOL A   1      -1.076   1.976  -0.849  1.00 -0.92          C

HETATM   44  C   MOL A   1      -0.798  -1.711   0.392  1.00 -2.50          C

HETATM   45  C   MOL A   1      -0.855  -1.702   3.815  1.00 -2.38          C

HETATM   46  C   MOL A   1      -0.544  -1.863  -2.140  1.00 -2.13          C

HETATM   47  C   MOL A   1      -0.438 -10.007   3.138  1.00 -0.87          C

HETATM   48  C   MOL A   1      -0.004   6.069   3.100  1.00 -1.01          C

HETATM   49  C   MOL A   1       0.246   0.201  -1.891  1.00 -2.14          C

HETATM   50  C   MOL A   1       0.321   0.673  -5.271  1.00 -1.76          C

HETATM   51  C   MOL A   1       0.426  -0.019   4.089  1.00 -2.39          C

HETATM   52  C   MOL A   1       0.797   6.274   5.072  1.00  0.50          C

HETATM   53  C   MOL A   1       1.201  -5.735  -0.618  1.00 -1.34          C

HETATM   54  C   MOL A   1       1.181   8.766   0.554  1.00 -1.14          C

HETATM   55  C   MOL A   1       1.264   4.935  -4.279  1.00 -1.03          C

HETATM   56  C   MOL A   1       1.461  -7.488   5.275  1.00 -0.97          C

HETATM   57  C   MOL A   1       1.583  -1.474   0.311  1.00 -2.54          C

HETATM   58  C   MOL A   1       1.667  -1.471  -1.982  1.00 -2.21          C

HETATM   59  C   MOL A   1       1.749  -1.328  -5.423  1.00 -1.83          C

HETATM   60  C   MOL A   1       1.856  -2.161   3.694  1.00 -2.38          C

HETATM   61  C   MOL A   1       2.103   3.011   1.674  1.00 -2.48          C

HETATM   62  C   MOL A   1       2.238   4.580  -3.473  1.00 -1.05          C

HETATM   63  C   MOL A   1       2.312  -7.815   1.675  1.00 -0.98          C

HETATM   64  C   MOL A   1       2.543  -5.162  -3.844  1.00 -0.82          C

HETATM   65  C   MOL A   1       2.763   0.428  -1.767  1.00 -2.18          C

HETATM   66  C   MOL A   1       2.862   0.990  -5.147  1.00 -1.80          C

HETATM   67  C   MOL A   1       2.956  -0.326   4.134  1.00 -2.37          C

HETATM   68  C   MOL A   1       3.002   0.673   0.846  1.00 -2.53          C

HETATM   69  C   MOL A   1       3.256  -6.229   1.676  1.00 -1.01          C

HETATM   70  C   MOL A   1       3.972  -5.441   3.903  1.00 -1.15          C

HETATM   71  C   MOL A   1       4.116   6.859   5.709  1.00 -0.42          C

HETATM   72  C   MOL A   1       5.068  -6.949   0.952  1.00 -0.93          C

HETATM   73  C   MOL A   1       5.071   1.619  -5.013  1.00 -1.45          C

HETATM   74  C   MOL A   1       5.089   1.072  -1.582  1.00 -1.65          C

HETATM   75  C   MOL A   1       5.556  -6.640   4.860  1.00 -0.88          C

HETATM   76  C   MOL A   1       5.545  -3.320  -4.047  1.00 -0.50          C

HETATM   77  C   MOL A   1       6.194  -4.443  -1.141  1.00 -1.00          C

HETATM   78  C   MOL A   1       6.582   3.687   4.367  1.00 -0.92          C

HETATM   79  C   MOL A   1       6.647  -2.190   3.089  1.00 -1.12          C

HETATM   80  C   MOL A   1       6.636   1.988   5.008  1.00 -1.10          C

HETATM   81  C   MOL A   1       6.841   0.117  -1.715  1.00 -1.80          C

HETATM   82  C   MOL A   1       6.751   0.752  -5.149  1.00 -1.71          C

HETATM   83  C   MOL A   1       7.390  -1.622   3.426  1.00 -1.06          C

HETATM   84  C   MOL A   1       7.723   3.955  -2.913  1.00 -1.13          C

HETATM   85  C   MOL A   1       7.737  -4.293   0.324  1.00 -0.96          C

HETATM   86  C   MOL A   1       8.116   3.632   1.530  1.00 -1.19          C

HETATM   87  C   MOL A   1       8.217  -3.655   4.252  1.00 -0.89          C

HETATM   88  C   MOL A   1       8.538  -7.027   2.468  1.00 -0.77          C

HETATM   89  C   MOL A   1       8.795   1.860   4.763  1.00 -0.99          C

HETATM   90  C   MOL A   1       9.290  -2.664  -3.962  1.00 -0.43          C

HETATM   91  C   MOL A   1       9.912  -1.465   3.180  1.00 -0.95          C

HETATM   92  C   MOL A   1      10.410  -2.326  -2.286  1.00 -0.49          C

HETATM   93  C   MOL A   1      10.423  -1.539  -5.681  1.00 -0.49          C

HETATM   94  C   MOL A   1      10.713   3.679   0.956  1.00 -1.17          C

HETATM   95  C   MOL A   1      11.242   2.148   4.214  1.00 -0.91          C

HETATM   96  C   MOL A   1      12.556  -1.155   3.030  1.00 -0.88          C

HETATM   97  C   MOL A   1      13.095   0.037  -3.727  1.00 -0.71          C

HETATM   98  C   MOL A   1      13.282   2.512   4.005  1.00 -0.81          C

HETATM   99  C   MOL A   1      13.579   3.689   0.409  1.00 -0.97          C

HETATM  100  C   MOL A   1      14.072  -0.824  -0.704  1.00 -0.76          C

HETATM  101  C   MOL A   1      14.945  -0.882   3.103  1.00 -0.68          C

HETATM  102  C   MOL A   1      15.124  -0.002  -0.668  1.00 -0.70          C

HETATM  103  C   MOL A   1      16.443   2.505   2.076  1.00 -0.65          C

HETATM    1  O   MOL A   1      -9.071  -3.541  -2.072  1.00 -2.53          O

HETATM    2  O   MOL A   1      -8.637  -0.352  -3.403  1.00 -2.30          O

HETATM    3  O   MOL A   1      -8.403   7.259   1.677  1.00 -2.27          O

HETATM    4  O   MOL A   1      -8.014  -3.335   1.873  1.00 -1.93          O

HETATM    5  O   MOL A   1      -7.936   1.632   2.705  1.00 -4.91          O

HETATM    6  O   MOL A   1      -7.636  -2.983  -0.261  1.00 -2.42          O

HETATM    7  O   MOL A   1      -7.499   7.062   0.483  1.00 -2.31          O

HETATM    8  O   MOL A   1      -6.988  -0.607   0.719  1.00 -3.99          O

HETATM    9  O   MOL A   1      -6.989   2.823  -0.230  1.00 -3.60          O

HETATM   10  O   MOL A   1      -6.792  -9.090   0.514  1.00 -1.20          O

HETATM   11  O   MOL A   1      -6.251   5.997   3.661  1.00 -2.27          O

HETATM   12  O   MOL A   1      -6.067  -3.455  -4.555  1.00 -2.03          O

HETATM   13  O   MOL A   1      -5.862   0.198  -0.156  1.00 -3.78          O

HETATM   14  O   MOL A   1      -5.218  -7.469  -0.039  1.00 -1.16          O

HETATM   15  O   MOL A   1      -4.890  -7.884   2.893  1.00 -1.30          O

HETATM   16  O   MOL A   1      -4.725   1.565  -5.039  1.00 -1.97          O

HETATM   17  O   MOL A   1      -4.530  -3.617  -5.076  1.00 -1.92          O

HETATM   18  O   MOL A   1      -4.423   3.309  -4.650  1.00 -2.01          O

HETATM   19  O   MOL A   1      -3.418   2.249  -0.652  1.00 -2.90          O

HETATM   20  O   MOL A   1      -3.295   1.864  -5.196  1.00 -1.96          O

HETATM   21  O   MOL A   1      -3.117  -0.995  -1.585  1.00 -2.39          O

HETATM   22  O   MOL A   1      -2.713  -3.096  -1.540  1.00 -2.57          O

HETATM   23  O   MOL A   1      -2.282  -2.965   0.189  1.00 -2.69          O

HETATM   24  O   MOL A   1      -2.081  -8.541   3.407  1.00 -1.29          O

HETATM   25  O   MOL A   1      -2.075  -2.826   4.032  1.00 -2.51          O

HETATM   26  O   MOL A   1      -1.981  -0.454  -0.023  1.00 -2.73          O

HETATM   27  O   MOL A   1      -1.494  -0.905  -1.804  1.00 -2.38          O

HETATM   28  O   MOL A   1      -1.329   0.213  -5.605  1.00 -1.83          O

HETATM   29  O   MOL A   1      -1.425   4.403  -0.788  1.00 -2.14          O

HETATM   30  O   MOL A   1      -0.696  -3.604  -2.026  1.00 -2.73          O

HETATM   31  O   MOL A   1      -0.072   1.709  -5.385  1.00 -1.92          O

HETATM   32  O   MOL A   1      -0.083   8.053   2.147  1.00 -1.44          O

HETATM   33  O   MOL A   1       0.418  -1.375   0.190  1.00 -2.63          O

HETATM   34  O   MOL A   1       0.485   1.156   4.702  1.00 -2.49          O

HETATM   35  O   MOL A   1       0.630  -1.553   4.122  1.00 -2.47          O

HETATM   36  O   MOL A   1       0.862  -0.841  -1.762  1.00 -2.35          O

HETATM   37  O   MOL A   1       1.309  -8.737   3.756  1.00 -1.25          O

HETATM   38  O   MOL A   1       1.496  -0.366  -1.684  1.00 -2.35          O

HETATM   39  O   MOL A   1       1.626   0.074   4.452  1.00 -2.46          O

HETATM   40  O   MOL A   1       1.773   3.463  -0.684  1.00 -3.21          O

HETATM   41  O   MOL A   1       1.931  -2.168  -1.789  1.00 -2.29          O

HETATM   42  O   MOL A   1       2.004  -0.106   0.346  1.00 -2.62          O

HETATM   43  O   MOL A   1       2.125  -0.208  -5.582  1.00 -1.92          O

HETATM   44  O   MOL A   1       2.226   1.711   0.876  1.00 -2.64          O

HETATM   45  O   MOL A   1       2.293  -2.032  -5.648  1.00 -1.92          O

HETATM   46  O   MOL A   1       2.367   2.015  -5.259  1.00 -1.95          O

HETATM   47  O   MOL A   1       3.416  -0.660   4.165  1.00 -2.40          O

HETATM   48  O   MOL A   1       3.537   0.556   0.642  1.00 -2.58          O

HETATM   49  O   MOL A   1       4.108  -5.763   2.704  1.00 -1.21          O

HETATM   50  O   MOL A   1       5.097   3.558  -1.950  1.00 -2.40          O

HETATM   51  O   MOL A   1       5.789  -5.283  -0.085  1.00 -1.24          O

HETATM   52  O   MOL A   1       6.223  -7.236   2.957  1.00 -1.17          O

HETATM   53  O   MOL A   1       6.840  -0.041  -5.450  1.00 -1.79          O

HETATM   54  O   MOL A   1       7.151   0.915  -1.332  1.00 -1.86          O

HETATM   55  O   MOL A   1       7.401   1.401  -5.211  1.00 -1.77          O

HETATM   56  O   MOL A   1       7.624  -1.072   1.278  1.00 -1.41          O

HETATM   57  O   MOL A   1       7.867   3.212   3.178  1.00 -1.36          O

HETATM   58  O   MOL A   1       8.508  -4.639   2.459  1.00 -1.19          O

HETATM   59  O   MOL A   1       9.117   3.100   2.830  1.00 -1.36          O

HETATM   60  O   MOL A   1      10.282   3.570  -2.494  1.00 -2.77          O

HETATM   61  O   MOL A   1      12.190  -1.629   0.685  1.00 -1.17          O

HETATM   62  O   MOL A   1      14.999   1.282   3.417  1.00 -1.02          O

HETATM   63  O   MOL A   1      16.217   0.038   1.288  1.00 -1.02          O

END

Table SS 24. Thioisorenieratane with WS-biochar of local minima and maxima on the Electrostatic potentials (ESP) surface.

REMARK   Unit of B-factor field (i.e. ESP) is eV

REMARK   Carbon: Surface maximum    Oxygen: surface minimum

HETATM    1  C   MOL A   1     -10.146   3.032  -3.243  1.00 -1.93          C

HETATM    2  C   MOL A   1      -9.850   0.434  -2.326  1.00 -2.21          C

HETATM    3  C   MOL A   1      -9.186  -3.634   4.933  1.00 -1.24          C

HETATM    4  C   MOL A   1      -8.754  -4.084  -0.674  1.00  0.66          C

HETATM    5  C   MOL A   1      -8.453   1.215   5.505  1.00 -2.00          C

HETATM    6  C   MOL A   1      -7.650   5.019  -3.373  1.00 -2.18          C

HETATM    7  C   MOL A   1      -7.300  -0.573   6.653  1.00 -1.49          C

HETATM    8  C   MOL A   1      -7.119  -3.787   8.008  1.00 -1.09          C

HETATM    9  C   MOL A   1      -6.883  -2.950   1.051  1.00 -1.64          C

HETATM   10  C   MOL A   1      -5.768  -4.029   0.413  1.00 -1.46          C

HETATM   11  C   MOL A   1      -5.766   2.639   5.022  1.00 -2.15          C

HETATM   12  C   MOL A   1      -5.479  -5.022   7.884  1.00 -1.05          C

HETATM   13  C   MOL A   1      -5.190  -1.236  -0.766  1.00 -2.21          C

HETATM   14  C   MOL A   1      -5.094   2.258  -4.873  1.00 -1.77          C

HETATM   15  C   MOL A   1      -4.764  -5.815  -1.562  1.00 -0.93          C

HETATM   16  C   MOL A   1      -4.424  -0.303  -4.775  1.00 -1.82          C

HETATM   17  C   MOL A   1      -4.402   1.135  -0.213  1.00 -2.36          C

HETATM   18  C   MOL A   1      -4.306   2.180  -1.459  1.00 -2.17          C

HETATM   19  C   MOL A   1      -3.929   6.772  -1.009  1.00 -1.99          C

HETATM   20  C   MOL A   1      -3.855   0.258  -1.415  1.00 -2.21          C

HETATM   21  C   MOL A   1      -3.832   4.870   3.837  1.00 -2.02          C

HETATM   22  C   MOL A   1      -3.331  -0.493   1.752  1.00 -1.88          C

HETATM   23  C   MOL A   1      -2.879   1.705  -1.616  1.00 -2.27          C

HETATM   24  C   MOL A   1      -2.805   1.619  -5.121  1.00 -1.90          C

HETATM   25  C   MOL A   1      -2.675  -6.337   1.201  1.00 -1.25          C

HETATM   26  C   MOL A   1      -2.621   7.044   2.486  1.00 -1.68          C

HETATM   27  C   MOL A   1      -2.404  -4.571  -4.956  1.00 -1.07          C

HETATM   28  C   MOL A   1      -2.428  -2.282  -0.942  1.00 -2.04          C

HETATM   29  C   MOL A   1      -2.387  -6.295   6.090  1.00 -1.04          C

HETATM   30  C   MOL A   1      -1.947  -0.224  -1.409  1.00 -2.12          C

HETATM   31  C   MOL A   1      -1.767  -0.817  -4.784  1.00 -1.75          C

HETATM   32  C   MOL A   1      -1.728   4.778   4.034  1.00 -1.68          C

HETATM   33  C   MOL A   1      -1.708   5.419  -3.773  1.00 -1.03          C

HETATM   34  C   MOL A   1      -1.291  -2.332  -0.821  1.00 -1.99          C

HETATM   35  C   MOL A   1      -1.155  -6.402   4.466  1.00 -1.06          C

HETATM   36  C   MOL A   1      -1.163   1.688   0.255  1.00 -2.11          C

HETATM   37  C   MOL A   1      -0.831  -2.720  -0.416  1.00 -2.01          C

HETATM   38  C   MOL A   1      -0.904   2.409   5.193  1.00 -1.29          C

HETATM   39  C   MOL A   1      -0.889   6.151  -0.597  1.00 -1.60          C

HETATM   40  C   MOL A   1      -0.348  -3.307   2.729  1.00 -1.41          C

HETATM   41  C   MOL A   1       0.110   5.073  -3.714  1.00 -1.13          C

HETATM   42  C   MOL A   1       0.109   5.873   0.574  1.00 -1.55          C

HETATM   43  C   MOL A   1       0.458  -6.858  -0.750  1.00 -0.80          C

HETATM   44  C   MOL A   1       0.610  -1.566  -4.345  1.00 -1.75          C

HETATM   45  C   MOL A   1       0.757   2.706  -6.038  1.00 -0.99          C

HETATM   46  C   MOL A   1       0.844  -2.670  -0.360  1.00 -2.03          C

HETATM   47  C   MOL A   1       1.169  -3.839  -3.598  1.00 -1.83          C

HETATM   48  C   MOL A   1       1.154  -0.611   5.900  1.00 -1.14          C

HETATM   49  C   MOL A   1       1.225   2.945   7.134  1.00 -1.05          C

HETATM   50  C   MOL A   1       1.988   0.699  -0.372  1.00 -0.84          C

HETATM   51  C   MOL A   1       2.599  -1.138  -0.580  1.00 -1.85          C

HETATM   52  C   MOL A   1       3.078  -2.105  -3.838  1.00 -1.78          C

HETATM   53  C   MOL A   1       3.773  -1.088   4.355  1.00 -1.19          C

HETATM   54  C   MOL A   1       3.873  -6.241  -0.843  1.00 -0.48          C

HETATM   55  C   MOL A   1       3.932   2.007  -3.191  1.00 -0.87          C

HETATM   56  C   MOL A   1       4.384   1.286   5.886  1.00 -0.89          C

HETATM   57  C   MOL A   1       4.725  -2.755   4.346  1.00 -1.05          C

HETATM   58  C   MOL A   1       4.884  -1.289  -0.175  1.00 -1.42          C

HETATM   59  C   MOL A   1       4.954   1.845   5.420  1.00 -0.91          C

HETATM   60  C   MOL A   1       5.110  -1.334   0.392  1.00 -1.45          C

HETATM   61  C   MOL A   1       5.109   2.288   0.702  1.00 -1.14          C

HETATM   62  C   MOL A   1       5.378  -2.166  -3.513  1.00 -1.42          C

HETATM   63  C   MOL A   1       6.075   3.780   2.578  1.00 -1.04          C

HETATM   64  C   MOL A   1       6.551  -3.565  -3.031  1.00 -1.70          C

HETATM   65  C   MOL A   1       6.793   0.342   5.106  1.00 -0.99          C

HETATM   66  C   MOL A   1       6.829   3.754  -2.396  1.00 -0.93          C

HETATM   67  C   MOL A   1       7.050   6.165   0.362  1.00 -0.89          C

HETATM   68  C   MOL A   1       7.662  -6.850  -0.292  1.00 -0.42          C

HETATM   69  C   MOL A   1       7.674   3.998  -3.383  1.00 -0.86          C

HETATM   70  C   MOL A   1       8.139   6.811  -0.886  1.00 -0.80          C

HETATM   71  C   MOL A   1       8.283  -2.442   3.270  1.00 -0.98          C

HETATM   72  C   MOL A   1       8.442  -0.247  -2.038  1.00 -1.22          C

HETATM   73  C   MOL A   1       8.708  -6.159   1.531  1.00 -0.48          C

HETATM   74  C   MOL A   1       8.816   1.433   4.592  1.00 -0.89          C

HETATM   75  C   MOL A   1       9.155  -6.970  -1.815  1.00 -0.46          C

HETATM   76  C   MOL A   1       9.310  -1.096   3.118  1.00 -0.93          C

HETATM   77  C   MOL A   1      10.189   1.765   5.006  1.00 -0.77          C

HETATM   78  C   MOL A   1      11.314   5.420  -2.713  1.00 -0.70          C

HETATM   79  C   MOL A   1      12.106  -5.609   0.027  1.00 -0.70          C

HETATM   80  C   MOL A   1      12.605   4.251  -1.721  1.00 -0.71          C

HETATM   81  C   MOL A   1      12.956   0.572   2.709  1.00 -0.77          C

HETATM   82  C   MOL A   1      13.486   1.792   1.154  1.00 -0.75          C

HETATM    1  O   MOL A   1      -8.996  -0.748  -0.278  1.00 -3.26          O

HETATM    2  O   MOL A   1      -8.848   3.635   1.573  1.00 -4.82          O

HETATM    3  O   MOL A   1      -8.432   0.121  -3.857  1.00 -2.35          O

HETATM    4  O   MOL A   1      -8.288   3.754  -3.861  1.00 -2.32          O

HETATM    5  O   MOL A   1      -7.053   1.452   0.088  1.00 -3.68          O

HETATM    6  O   MOL A   1      -6.881  -2.873  -3.823  1.00 -2.08          O

HETATM    7  O   MOL A   1      -5.769  -1.648  -0.220  1.00 -2.36          O

HETATM    8  O   MOL A   1      -5.555  -5.178   3.835  1.00 -2.48          O

HETATM    9  O   MOL A   1      -5.516   4.210  -1.731  1.00 -3.34          O

HETATM   10  O   MOL A   1      -4.756   1.531   4.038  1.00 -2.42          O

HETATM   11  O   MOL A   1      -4.444   2.760   3.835  1.00 -2.41          O

HETATM   12  O   MOL A   1      -3.847  -2.200   4.867  1.00 -2.63          O

HETATM   13  O   MOL A   1      -3.869   0.967  -5.328  1.00 -1.96          O

HETATM   14  O   MOL A   1      -3.733  -2.244  -0.496  1.00 -2.37          O

HETATM   15  O   MOL A   1      -3.523   1.207   0.735  1.00 -2.47          O

HETATM   16  O   MOL A   1      -3.462   1.209  -1.422  1.00 -2.30          O

HETATM   17  O   MOL A   1      -2.809   2.568  -5.363  1.00 -1.99          O

HETATM   18  O   MOL A   1      -2.335   0.741  -5.287  1.00 -1.95          O

HETATM   19  O   MOL A   1      -2.242  -4.415  -0.262  1.00 -2.54          O

HETATM   20  O   MOL A   1      -2.022  -1.048  -1.045  1.00 -2.23          O

HETATM   21  O   MOL A   1      -1.625  -4.343   1.057  1.00 -1.77          O

HETATM   22  O   MOL A   1      -1.378   5.827   1.938  1.00 -1.97          O

HETATM   23  O   MOL A   1      -0.928  -1.492  -4.844  1.00 -1.84          O

HETATM   24  O   MOL A   1      -0.648   1.873  -1.152  1.00 -2.79          O

HETATM   25  O   MOL A   1       0.045  -1.799  -0.530  1.00 -2.11          O

HETATM   26  O   MOL A   1       0.192   0.881   2.165  1.00 -2.53          O

HETATM   27  O   MOL A   1       0.652  -0.460  -4.854  1.00 -1.93          O

HETATM   28  O   MOL A   1       1.082  -3.288   0.115  1.00 -2.12          O

HETATM   29  O   MOL A   1       1.140   4.050  -1.170  1.00 -2.95          O

HETATM   30  O   MOL A   1       1.172   4.550   3.443  1.00 -2.40          O

HETATM   31  O   MOL A   1       1.566  -4.662  -3.468  1.00 -1.93          O

HETATM   32  O   MOL A   1       2.130  -3.219  -3.914  1.00 -1.90          O

HETATM   33  O   MOL A   1       2.512   5.037   1.938  1.00 -2.28          O

HETATM   34  O   MOL A   1       2.702  -0.572  -0.530  1.00 -1.90          O

HETATM   35  O   MOL A   1       2.994  -0.998  -4.400  1.00 -1.93          O

HETATM   36  O   MOL A   1       4.174  -1.955   1.857  1.00 -1.64          O

HETATM   37  O   MOL A   1       5.026  -0.857   4.446  1.00 -1.25          O

HETATM   38  O   MOL A   1       5.152   3.912  -0.183  1.00 -1.48          O

HETATM   39  O   MOL A   1       6.007  -3.699   0.834  1.00 -1.81          O

HETATM   40  O   MOL A   1       6.300   0.624  -2.125  1.00 -2.25          O

HETATM   41  O   MOL A   1       6.377  -4.427  -3.013  1.00 -1.79          O

HETATM   42  O   MOL A   1       6.590  -2.478   4.351  1.00 -1.32          O

HETATM   43  O   MOL A   1       6.853  -0.533  -0.167  1.00 -1.71          O

HETATM   44  O   MOL A   1       7.416  -2.282   0.725  1.00 -1.81          O

HETATM   45  O   MOL A   1       7.562  -3.238  -3.183  1.00 -1.78          O

HETATM   46  O   MOL A   1      10.187   1.100  -0.486  1.00 -2.28          O

HETATM   47  O   MOL A   1      10.424   4.207   1.608  1.00 -2.04          O

HETATM   48  O   MOL A   1      10.664  -1.195  -1.093  1.00 -2.90          O

END