SUPPORTING INFORMATION

PH Controlled the Supramolecular Assemblies of Two Guanosine Monophosphate Cadmium Metal Coordination Complexes: Structure and Chirality

Muhammad Javed Iqbal, Zhongkui Li, Maroof Ahmad Khan, Wajid Hussain, Muhammad Sohail Riaz, Rizwan Shoukat, Khalid Talha, Hui Li*

Key Laboratory of cluster Science of Ministry of education, School of Chemistry and Chemical Engineering, Beijing Institute of Technology, Beijing 100081, P. R. China.

Analytical and Testing Centre, Beijing Institute of Technology, Beijing 10081, P. R. China

CONTENT:

- Selected Bond Lengths for Complex 1…….……………………………………….…. 3

- Selected Bond Lengths for Complex 2…….……………………………………….…. 4

- Selected Bond Angles for Complex 1……………………………………………..…... 5

- Selected Bond Angles for Complex 2……………………………………………..…... 6

- Selected Hydrogen Bonds for Complex 1…………………………………………..… 8

- Selected Hydrogen Bonds for Complex 2…………………………………………..… 9

- Molecular structure of complexes (1) with metal-metal distances………………..…10

- Structures of complexes (1-2) with parallel distances between bases and BPe……..10

- 2D structures of complexes 1-2 with primary and secondary ligands ……………...11

- 3D Supramolecular framework of complexes 2...…………………………………….11

- Angles between Sugar ring and Guanine base of complexes 1...…………..………...12

- Angles between Sugar ring and Guanine base of complexes 1……………...….........14

- Angles between Sugar ring and Guanine base of complexes 2…...……………….....15

- UV Visible Spectra of GMP, Complex 1 and Complex 2………………………….…16

- Infrared Spectra of GMP, Complex 1 and Complex 2…………………………….…17

- Infrared Spectra of GMP, BPe, Complex 1 and Complex 2………..…………….… 17

- X-ray powder diffraction of complexes 1 and 2………………………………….….. 18

Table S1: Selected Bond Lengths for Complex 1 [GMP-Cd-bpe (1)]

| Atom-Atom | Length/Å | Atom-Atom | Length/Å |
| --- | --- | --- | --- |
| Cd1-O1 | 2.231(8) | N4-C10 | 1.315(17) |
| Cd1-O3 | 2.301(9) | N4-C18 | 1.361(12) |
| Cd1-O4 | 2.355(8) | C3-C19 | 1.40(2) |
| Cd1-O7 | 2.299(9) | C4-C7 | 1.391(16) |
| Cd1-N31 | 2.364(10) | C4-C11 | 1.375(16) |
| Cd1-N4 | 2.312(10) | N5-C6 | 1.432(13) |
| P1-O1 | 1.520(8) | N5-C11 | 1.368(12) |
| P1-O9 | 1.589(8) | N6-C16 | 1.353(15) |
| P1-O10 | 1.500(8) | C5-C10 | 1.375(14) |
| P1-O13 | 1.497(9) | C5-C14 | 1.351(19) |
| O2-C1 | 1.415(11) | C6-C9 | 1.538(15) |
| N1-C11 | 1.360(13) | O14-C9 | 1.395(12) |
| N1-C16 | 1.309(16) | C7-N7 | 1.404(14) |
| O5-C6 | 1.394(13) | C8-C20 | 1.526(13) |
| O5-C20 | 1.449(11) | C12-C13 | 1.384(15) |
| N2-C2 | 1.280(12) | C13-C15 | 1.36(2) |
| N2-C4 | 1.419(15) | C14-C17 | 1.372(14) |
| O9-C8 | 1.400(11) | C14-C22 | 1.548(18) |
| N3-C3 | 1.325(15) | C15-C19 | 1.366(16) |
| N3-C12 | 1.338(16) | C15-C21 | 1.525(19) |
| C1-C9 | 1.518(14) | N7-C16 | 1.347(15) |
| C1-C20 | 1.507(13) | C17-C18 | 1.394(14) |
| C2-N5 | 1.373(12) | C21-C22 | 1.253(19) |
| O11-C7 | 1.232(13) |  |  |

| Table S2: Selected Bond lengths for Complex 2 (GMP-Cd). |  |  |  |  |
| --- | --- | --- | --- | --- |
| Atom-Atom | Length/Å |  | Atom-Atom | Length/Å |
| Cd1-O4 | 2.304(4) |  | N6-C6 | 1.409(7) |
| Cd1-O7 | 2.304(4) |  | N2-C1 | 1.373(7) |
| Cd1-O10 | 2.273(4) |  | N2-C3 | 1.347(7) |
| Cd1-N6 | 2.294(5) | N2-C7 |  | 1.491(7) |
| Cd1-O13 | 2.368(5) |  | O12-C5 | 1.411(6) |
| Cd1-O14 | 2.253(5) |  | N3-C4 | 1.350(8) |
| P1-O3 | 1.519(4) |  | C1-N4 | 1.356(7) |
| P1-O5 | 1.617(4) |  | C1-C6 | 1.388(7) |
| P1-O17 | 1.521(4) |  | C2-C9 | 1.514(7) |
| P1-O15 | 1.515(4) |  | N4-C4 | 1.325(7) |
| O1-C10 | 1.244(6) |  | N5-C4 | 1.377(7) |
| O5-C2 | 1.441(7) |  | N5-C10 | 1.397(8) |
| O8-C8 | 1.419(6) |  | C5-C8 | 1.517(8) |
| O9-C7 | 1.417(7) |  | C5-C9 | 1.525(8) |
| O9-C9 | 1.451(7) |  | C6-C10 | 1.411(9) |
| N6-C3 | 1.317(7) | C7-C8 |  | 1.511(9) |

Table S3: Selected bond Angles for Complex 1 [GMP-Cd-bpe (1)]

| Atom-Atom-Atom | Angle/˚ | Atom-Atom-Atom | Angle/˚ |
| --- | --- | --- | --- |
| O1-Cd1-O3 | 101.8(3) | C11-C4-C7 | 120.7(11) |
| O1-Cd1-O4 | 167.7(3) | C2-N5-C6 | 127.8(8) |
| O1-Cd1-O7 | 86.0(3) | C11-N5-C2 | 105.0(8) |
| O1-Cd1-N31 | 87.5(3) | C11-N5-C6 | 127.1(8) |
| O1-Cd1-N4 | 98.5(3) | C14-C5-C10 | 120.1(13) |
| O3-Cd1-O4 | 87.5(3) | O5-C6-N5 | 110.0(9) |
| O3-Cd1-N31 | 84.1(4) | O5-C6-C9 | 107.4(8) |
| O3-Cd1-N4 | 86.2(3) | N5-C6-C9 | 115.1(8) |
| O4-Cd1-N31 | 85.5(3) | O11-C7-C4 | 129.4(11) |
| O7-Cd1-O3 | 171.2(4) | O11-C7-N7 | 119.5(9) |
| O7-Cd1-O4 | 85.3(3) | C4-C7-N7 | 111.1(10) |
| O7-Cd1-N31 | 100.4(4) | O9-C8-C20 | 110.0(8) |
| O7-Cd1-N4 | 88.7(3) | C1-C9-C6 | 101.6(8) |
| N4-Cd1-O4 | 90.0(3) | O14-C9-C1 | 110.0(8) |
| N4-Cd1-N31 | 169.5(4) | O14-C9-C6 | 111.7(8) |
| O1-P1-O9 | 103.2(4) | N4-C10-C5 | 123.9(13) |
| O10-P1-O1 | 111.9(5) | N1-C11-C4 | 126.6(10) |
| O10-P1-O9 | 108.2(5) | N1-C11-N5 | 125.9(9) |
| O13-P1-O1 | 113.5(5) | N5-C11-C4 | 107.5(9) |
| O13-P1-O9 | 108.1(5) | N3-C12-C13 | 120.0(12) |
| O13-P1-O10 | 111.4(6) | C15-C13-C12 | 120.8(13) |
| P1-O1-Cd1 | 136.0(5) | C5-C14-C17 | 118.1(10) |
| C16-N1-C11 | 111.7(10) | C5-C14-C22 | 114.1(11) |
| C6-O5-C20 | 109.7(8) | C17-C14-C22 | 127.6(12) |
| C2-N2-C4 | 104.7(9) | C13-C15-C19 | 119.6(15) |
| C8-O9-P1 | 123.1(7) | C13-C15-C21 | 129.5(13) |
| C3-N3-Cd12 | 119.4(9) | C19-C15-C21 | 110.9(15) |
| C3-N3-C12 | 119.0(11) | C16-N7-C7 | 124.1(10) |
| C12-N3-Cd12 | 121.0(8) | N1-C16-N6 | 119.3(11) |
| O2-C1-C9 | 115.1(8) | N1-C16-N7 | 125.7(11) |
| O2-C1-C20 | 111.1(8) | N7-C16-N6 | 114.9(10) |
| C20-C1-C9 | 101.5(7) | C14-C17-C18 | 118.9(10) |
| N2-C2-N5 | 114.5(8) | N4-C18-C17 | 122.5(10) |
| C10-N4-Cd1 | 125.2(8) | C15-C19-C3 | 116.9(16) |
| C10-N4-C18 | 116.0(10) | O5-C20-C1 | 104.4(7) |
| C18-N4-Cd1 | 118.6(7) | O5-C20-C8 | 107.8(8) |
| N3-C3-C19 | 123.7(13) | C1-C20-C8 | 115.2(7) |
| C7-C4-N2 | 131.0(12) | C22-C21-C15 | 121.8(14) |
| C11-C4-N2 | 108.3(10) | C21-C22-C14 | 119.0(14) |

| Table S4: Selected Bond Angles for Complex (GMP-Cd). |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Atom-Atom-Atom | Angle/˚ |  | Atom-Atom-Atom |  |  | Angle/˚ |
| O4-Cd1-O13 | 88.61(17) |  | N2-C1-C6 |  |  | 105.3(5) |
| O7-Cd1-O4 | 92.52(15) |  | N4-C1-N2 |  |  | 126.6(5) |
| O7-Cd1-O13 | 166.46(16) |  | N4-C1-C6 |  |  | 128.1(5) |
| O10-Cd1-O4 | 86.14(16) |  | O5-C2-C9 |  |  | 108.8(4) |
| O10-Cd1-O7 | 95.39(18) |  | C4-N4-C1 |  |  | 112.0(4) |
| O10-Cd1-N6 | 87.49(17) |  | C4-N5-C10 |  |  | 124.4(5) |
| O10-Cd1-O13 | 98.14(18) |  | N6-C3-N2 |  |  | 112.8(5) |
| N6-Cd1-O4 | 173.58(16) |  | N3-C4-N5 |  |  | 115.4(5) |
| N6-Cd1-O7 | 88.90(16) |  | N4-C4-N3 |  |  | 120.4(5) |
| N6-Cd1-O13 | 91.47(17) |  | N4-C4-N5 |  |  | 124.2(5) |
| O14-Cd1-O4 | 93.7(2) |  | O12-C5-C8 |  |  | 111.5(4) |
| O14-Cd1-O7 | 87.72(19) |  | O12-C5-C9 |  |  | 114.3(4) |
| O14-Cd1-O10 | 176.9(2) |  | C8-C5-C9 |  |  | 103.2(5) |
| O14-Cd1-N6 | 92.6(2) |  | N6-C6-C10 |  |  | 131.5(5) |
| O14-Cd1-O13 | 78.74(19) |  | C1-C6-N6 |  |  | 109.4(5) |
| O3-P1-O5 | 102.2(2) |  | C1-C6-C10 |  |  | 118.9(5) |
| O3-P1-O17 | 113.9(2) |  | O9-C7-N2 |  |  | 106.7(5) |
| O17-P1-O5 | 107.2(3) |  | O9-C7-C8 |  |  | 108.4(5) |
| O15-P1-O3 | 113.0(2) |  | N2-C7-C8 |  |  | 113.3(5) |
| O15-P1-O5 | 108.7(2) |  | O8-C8-C5 |  |  | 112.7(4) |
| O15-P1-O17 | 111.3(2) |  | O8-C8-C7 |  |  | 110.4(5) |
| C2-O5-P1 | 118.9(4) |  | C7-C8-C5 |  |  | 101.9(4) |
| C7-O9-C9 | 109.7(4) |  | O9-C9-C2 |  |  | 108.5(4) |
| C3-N6-Cd1 | 119.6(4) |  | O9-C9-C5 |  |  | 103.5(4) |
| C3-N6-C6 | 104.5(4) |  | C2-C9-C5 |  |  | 116.5(5) |
| C6-N6-Cd1 | 135.9(4) |  | O1-C10-N5 |  |  | 119.2(6) |
| C1-N2-C7 | 124.7(4) |  | O1-C10-C6 |  |  | 128.5(7) |
| C3-N2-C1 | 108.0(4) |  | N5-C10-C6 |  |  | 112.2(5) |
| C3-N2-C7 | 126.9(5) |  |  |  |  |  |

| Table S 5: Selected hydrogen Bonds for Complex 1 [GMP-Cd-bpe (1)] |  |  |  |  |
| --- | --- | --- | --- | --- |
| D-H--A | d(D-H)/Å | d(H-A)/Å | d(D-A)/Å | D-H-A/° |
| O6-H6C--N2 | 0.85 | 2.00 | 2.726(11) | 142.8 |
| O6-H6D--O3 | 0.85 | 1.91 | 2.739(13) | 165.2 |
| O7-H7A--O10 | 0.94 | 1.79 | 2.657(12) | 153.0 |
| O7-H7B--O81 | 0.94 | 1.77 | 2.696(13) | 166.7 |
| O12-H12A--O13 | 0.85 | 1.79 | 2.639(14) | 177.2 |
| O14-H14--O42 | 0.82 | 2.09 | 2.747(11) | 137.5 |
| O17-H17A--O8 | 0.85 | 1.99 | 2.680(14) | 138.2 |
| N7-H7--O123 | 0.86 | 1.91 | 2.761(15) | 172.5 |
| O18-H18B--O12 | 0.85 | 2.29 | 2.84(3) | 122.8 |

| Table S 6: Selected Hydrogen Bonds for Complex (GMP-Cd). |  |  |  |  |
| --- | --- | --- | --- | --- |
| D-H-A | d(D-H)/Å | d(H-A)/Å | d(D-A)/Å | D-H-A/° |
| O4-H4A-O171 | 0.85 | 1.93 | 2.748(6) | 159.1 |
| O7-H7A-O152 | 0.85 | 1.80 | 2.609(6) | 156.4 |
| O7-H7B-O3 | 0.85 | 1.92 | 2.747(6) | 164.1 |
| O10-H10A-O123 | 0.85 | 1.96 | 2.733(6) | 150.8 |
| O10-H10B-O1 | 0.85 | 1.91 | 2.737(8) | 163.7 |
| O11-H11A-O34 | 0.85 | 2.05 | 2.829(7) | 152.6 |
| O11-H11B-O2 | 0.85 | 1.91 | 2.737(8) | 165.0 |
| O12-H12-O115 | 0.82 | 1.76 | 2.567(8) | 167.7 |
| O13-H13A-O16 | 0.86 | 1.95 | 2.751(9) | 155.2 |
| O13-H13B-O151 | 0.86 | 2.02 | 2.807(6) | 151.7 |
| O14-H14A-O17 | 0.85 | 1.85 | 2.633(6) | 153.4 |
| O14-H14B-O151 | 0.85 | 1.91 | 2.651(6) | 145.2 |

Fig. S1. The coordination molecular structure with  distances between bpe-bpe, bpe-Guanine base and Guanine base-Guanibe base (a)the distance between bpe-bpe and bpe-Guanine bases of different layers are 3.623Å, 3.347Å and 6.23Å  in Complex 1,(b) distance between Guanine bases of two parallel layers are 3.482 Å and 3.388 Å in complex 2 (c) plane through the sugar  motif (Blue color) and Gunine base (Yellow) showing the Angle between Gunine base ring and sugar motif is 67.939(155)o in Complex 1, (d) Angle between Sugar motif (Blue Plan) and Guanine base ring (Yellow Plan) is 79.506(377)o in complex 2.

Fig. S2. The metal coordinated molecular structure showing distances and orientations of Nucleotide bases and Auxiliary ligand (a) the distance between Cd-Cd in complex 1 is 13.997Å, (b) 2D layers of complex 1 showing the orientation of Guanine bases (c) showing the 2D layers a- view of Complex 2, like a top view of butterfly  (d) 2D structure showing side view of butterfly in c-view of complex 2

Fig. S3: (a) Showinth the coordination environment and orientation of guanine base with pyridine rings of bpe (b-d) 3D Supramolecular framework of complexes with Hydrogen bonding and pi-pi interactions (Bpe-Bpe, Bpe-Adenine, Adenine-Adenine bases) among different layers in a, b, c- view of Complex 1 (GMP-Cd-Bpe)

Fig. S4: (a) Showing the coordination environment and orientation of guanine base with pyridine rings of bpe (b-d) 3D Supramolecular framework of complexes with Hydrogen bonding and pi-pi interactions (Guanine-Guanine bases) among different layers in a, b, c- view of Complex 2 (GMP-Cd)

Fig. S5: In Complex 1 (a) Showing the coordination environment and orientation of guanine base with pyridine rings of bpe (b) Coordination environment and bond lengths between Cd and other Coordinated atoms are Cd1-O1=2.231(8)Å, Cd1-O3=2.301(9)Å, Cd1-O4=2.355(8)Å, Cd1-O7=2.299(9)Å, Cd1-N31=2.364(10)Å, Cd1-N4=2.312(10)Å, (c) Phosphate group coordinated with metal showing the bond lengths are P1-O1=1.520(8)Å, P1-O9=1.589(8)Å, P1-O10=1.500(8)Å, P1-O13=1.497(9)Å and bond angles are O1-Cd1-O3=101.8(3)o, O1-Cd1-O4=167.7(3)o, O1-Cd1-O7=86.0(3)o, O1-Cd1-N31=87.5(3)o, O1-Cd1-N4=98.5(3)o, O3-Cd1-O4=87.5(3)o, O3-Cd1-N31=84.1(4)o, O3-Cd1-N4=86.2(3)o, O4-Cd1-N31=85.5(3)o, O7-Cd1-O3=171.2(4)o, O7-Cd1-O4=90.0(3)o, O7-Cd1-N31=100.4(4)o, O7-Cd1-N4=88.7(3)o, N4-Cd1-O4=90.0(3)o, N4-Cd1-N31=169.5(4)o, (d) Sugar motif  showing the twist or orientation of carbon out of plane (green through C9, C20,O5, C6) the distance of C1 from plane is 0.5931 Å

Figure S6:  Complex 2 Showing  (a) the coordination environment and orientation of guanine base with Cd (II) (b) bond lengths and Angles between Cd and other Coordinated atoms are Cd1-O4=2.304(4)Å, Cd1-O7=2.304(4)Å, Cd1-O10=2.273(4)Å, Cd1-O13=2.368(5)Å, Cd1-O14=2.253(5)Å, Cd1-N6=2.294(5)Å (c) Phosphate group coordinated with metal showing the bond lengths are P1-O3=1.519(4)Å, P1-O5=1.617(4)Å, P1-O17=1.521(4)Å, P1-O15=1.515(4)Å  and bond angles are O10-Cd1-O13=98.14(18)o, N6-Cd1-O4=173.58(16)o, N6-Cd1-O7=88.90(16)o, N6-Cd1-O13=91.47(17)o, O14-Cd1-O4=93.7(2)o, O14-Cd1-O7=87.72(19)o, O14-Cd1-O7=87.72(19)o, O14-Cd1-O10=176.9(2)o, O14-Cd1-N6=92.6(2)o, O14-Cd1-O13=78.74(19)o, (d) Sugar motif  showing the twist or orientation of carbon (C5) out of plane (Green through C7, C9,O9, C8)  the distance from plane is 0.5546 Å

Figure S7: UV-Vis spectra of complex 1(blue), Complex 2(Red) ans GMP ligand (black) with concentration 1.0 x10-5 M/L. The GMP ligand and complexes shows λmax at 253nm, 254nm, 260nm respectively.The peak at 190nm is due to sugar motif of GMP ligand.

Fig. S10: The Infrared spectrumof complexes were measured in range of 4000-500 cm-1 and 2000-500 cm-1 for comparison between GMP Ligand and Complexes. (a) IR spectra of GMP (Black), GMP-Cd-bpe (Complex 1) (red). (b) IR spectra of GMP (Black), GMP-Cd-bpe (Complex 1) (red) and bpe (blue). (c) IR spectra of bpe (blue) ans GMP-Cd (Complex 2) (red).    (d) IR spectra of GMP (Black), GMP-Cd (Complex 2) (red).  The IR peaks of complexes are well matched with IR spectra of GMP ligand which proves that GMP ligand is coordinated with Cdmium metal for construction of GMP Coordination polymer.

Fig. S12: A pure phase of single crystals of complexes 1-2 waqs measured by X-ray powder diffraction (PXRD). Experimental PXRD patterns of complexes shows the contrast between the investigational value and Simulated for complex 1 (GMP-Cd-bpe) (a) and Complex 2 (GMP-Cd) (b)