Supplimentary material

Images of various pants and animal species involve in this paper.

Energy dispersive X-ray spectroscopy

| Element | Weight% | Atomic% |
| --- | --- | --- |
| C K | 60.36 | 66.98 |
| O K | 39.64 | 33.02 |
| Totals | 100.00 |  |

| Element | Weight% | Atomic% |
| --- | --- | --- |
| C K | 75.84 | 80.70 |
| O K | 24.16 | 19.30 |
| Totals | 100.00 |  |

E-DAX analysis				EDS analysis of rGO prepared

of graphene oxide				by reduction with E coli

| Element | Weight% | Atomic% |
| --- | --- | --- |
| C K | 63.09 | 69.48 |
| O K | 36.91 | 30.52 |
| Totals | 100.00 |  |

EDS analysis of rGO prepared by reduction using Fruit extract