SUPPLEMENTARY INFORMATION

Evaluating the host potential of 9,9’-bifluorenyl-9,9’-diol for anisole and the three methylanisole isomers, and its behaviour in mixed guest solutions

Benita Barton,* Jaime-lee Groenewaldt,* and Eric C. Hosten

Department of Chemistry, Nelson Mandela University, PO Box 77000, Port Elizabeth, 6031, South Africa. Email: benita.barton@mandela.ac.za; s224525069@mandela.ac.za

(a) 	(b)

(c)	(d)

(e)

Figure S1 1H-NMR spectra of (a) 2(H)·ANI, (b) H·2MA, (c) H·3MA, (d) 3(H)·2(4MA1), and (e) H·4MA2 from single-solvent host crystallization experiments.

(a) 										(b)

(c)

Figure S2 Relevant data for H equimolar guest competition of ANI:2MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

(a)  										(b)

(c)

Figure S3 Relevant data for H equimolar guest competition of ANI:3MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

(a) 										(b)

(c) 										(d)

Figure S4 Relevant data for H equimolar guest competition of ANI:4MA (a) GC trace, (b) GC trace of its duplicate, (c) GC trace of its triplicate, and (d) 1H-NMR spectra.

(a) 										(b)

(c)

Figure S5 Relevant data for H equimolar guest competition of 2MA:3MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

(a)					 					(b)

(c)

Figure S6 Relevant data for H equimolar guest competition of 2MA:4MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

- (b)

(c)

Figure S7 Relevant data for H equimolar guest competition of 3MA:4MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

- (b)

(c)

Figure S8 Relevant data for H equimolar guest competition of ANI:2MA:3MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

- (b)

(c)

Figure S9 Relevant data for H equimolar guest competition of ANI:2MA:4MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

(a) 										(b)

(c)

Figure S10 Relevant data for H equimolar guest competition of ANI:3MA:4MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

(a)    										(b)

(c)

Figure S11 Relevant data for H equimolar guest competition of 2MA:3MA:4MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

(a)  										(b)

(c)

Figure S12 Relevant data for H equimolar guest competition of ANI:2MA:3MA:4MA (a) GC trace, (b) GC trace of its duplicate, and (c) 1H-NMR spectra.

(a)   										(b)

(c)  										(d)

Figure S13 GC traces for H binary mixtures of ANI and 2MA (a) 20:80, (b) 40:60, (c) 60:40, and (d) 80:20.

(a)  										(b)

(c)  										(d)

Figure S14 GC traces for H binary mixtures of ANI and 3MA (a) 20:80, (b) 40:60, (c) 60:40, and (d) 80:20.

(a)  										(b)

(c)  										(d)

Figure S15 GC traces for H binary mixtures of ANI and 4MA (a) 20:80, (b) 40:60, (c) 60:40, and (d) 80:20.

(a)  										(b)

(c)  										(d)

Figure S16 GC traces for H binary mixtures of 2MA and 3MA (a) 20:80, (b) 40:60, (c) 60:40, and (d) 80:20.

(a)  										(b)

(c)  										(d)

Figure S17 GC traces for H binary mixtures of 2MA and 4MA (a) 20:80, (b) 40:60, (c) 60:40, and (d) 80:20.

(a)  										(b)

(c)    										(d)

Figure S18 GC traces for H binary mixtures of 3MA and 4MA (a) 20:80, (b) 40:60, (c) 60:40, and (d) 80:20.

(a)    										(b)

(c) 										(d)

(e)  										(f)

Figure S19 Selectivity profiles for H when crystallized from the (a) 2MA/ANI, (b) 3MA/ANI, (c) 4MA/ANI, (d) 3MA/2MA, (e) 4MA/2MA and (f) 4MA/3MA binary guest solutions. The straight diagonal lines have been inserted to denote a host compound that exhibits no selectivity whatsoever.

Table S1 Calculated K values for H in binary mixtures of ANI and the MAs.

| Guest (the first listed in each pair) percentage in the original solution | K values (in favour of) |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
|  | 2MA/ANI | 3MA/ANI | 4MA/ANI | 3MA/2MA | 4MA/2MA | 4MA/3MA |
| 20 | 1.1 (ANI) | 1.2 (ANI) | 1.2 (4MA) | 1.9 (2MA) | 2.6 (2MA) | 3.3 (3MA) |
| 40 | 1.3 (2MA) | 1.2 (3MA) | 3.9 (4MA) | 1.2 (2MA) | 1.2 (4MA) | 1.2 (3MA) |
| 50 | 1.5 (2MA) | 1.2 (3MA) | 2.2 (4MA) | 1.4 (3MA) | 2.4 (4MA) | 1.3 (4MA) |
| 60 | 1.4 (2MA) | 2.2 (3MA) | 8.5 (4MA) | 1.3 (3MA) | 5.6 (4MA) | 1.1 (4MA) |
| 80 | 1.1 (2MA) | 3.0 (3MA) | 5.2 (4MA) | 1.5 (3MA) | 5.9 (4MA) | 0.9 (4MA) |

(a)

(b)

(c)

(d)

(e)

Figure S20 ORTEP diagrams for the complexes formed (a) H·0.778(ANI), (b) H·0.778(2MA), (c) H·0.667(3MA), (d) H·0.667(4MA1) and (e) H·0.75(4MA2).

Table S2 Crystallographic data before and after the SQUEEZE routine for the complexes of H with ANI, 2MA, 3MA and 4MA.

| Guest | ANI | ANI SQ | 2MA | 2MA SQ | 3MA1 | 3MA2 | 3MA SQ | 4MA1 | 4MA1 SQ | 4MA2 | 4MA2 SQ |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Comment |  |  |  |  | (Initially) | (Refined) |  |  |  |  |  |
| Space group | R-3 | R-3 | R-3 | R-3 | P-1 | P-1 | P-1 | P-1 | P-1 | P-1 | P-1 |
| a | 31.8624 | 31.8624 | 32.0983 | 32.0983 | 18.6966 | 12.1377 | 12.138 | 12.215 | 12.215 | 10.227 | 10.2266 |
| b | 31.8624 | 31.8624 | 32.0983 | 32.0983 | 18.9785 | 18.4488 | 18.449 | 18.389 | 18.3885 | 12.692 | 12.6915 |
| c | 12.1461 | 12.1461 | 12.1248 | 12.1248 | 24.1663 | 18.7002 | 18.7 | 18.552 | 18.5519 | 19.322 | 19.3221 |
| α | 90 | 90 | 90 | 90 | 101.404 | 115.101 | 115.1 | 115.85 | 115.854 | 84.939 | 84.9386 |
| β | 90 | 90 | 90 | 90 | 103.102 | 101.188 | 101.19 | 101.14 | 101.141 | 83.883 | 83.8825 |
| γ | 120 | 120 | 120 | 120 | 116.657 | 102.425 | 102.43 | 100.54 | 100.542 | 77.579 | 77.5793 |
| Platon ratio H | 1 | 1 | 2 | 1 | 12 | 1 | 1 | 3 | 1 | 4 | 1 |
| Platon ratio G | 0.727 | 0 | 0.667 | 0 | 7 | 0.522 | 0 | 2 | 0 | 3 | 0 |
| ratio H:G | 1.38 | #N/A | 3 | #N/A | 1.71 | 1.92 | #N/A | 1.5 | #N/A | 1.33 | #N/A |
| z | 18 | 18 | 9 | 18 | 1 | 6 | 6 | 2 | 6 | 1 | 4 |
| e- (H) | 190 | 190 | 190 | 190 | 190 | 190 | 190 | 190 | 190 | 190 | 190 |
| e- (G) | 58 | 58 | 66 | 66 | 66 | 66 | 66 | 66 | 66 | 66 | 66 |
| F(OOO) | 4179 | 3420 | 3816 | 3420 | 2742 | 1347 | 1140 | 1404 | 1140 | 958 | 760 |
| Calc tot e- | 4178.99 | 3420 | 3816.2 | 3420 | 2742 | 1346.712 | 1140 | 1404 | 1140 | 958 | 760 |
| Rint | 0.046 | 0.046 | 0.151 | 0.151 | 0.065 | 0.053 | 0.053 | 0.094 | 0.094 | 0.063 | 0.063 |
| R | 0.0997 | 0.0619 | 0.1447 | 0.0768 | 0.0903 | 0.0879 | 0.0708 | 0.1501 | 0.1339 | 0.0485 | 0.0547 |
| wR2 | 0.305 | 0.149 | 0.3999 | 0.1731 | 0.238 | 0.23 | 0.1856 | 0.3659 | 0.3313 | 0.1075 | 0.1364 |
| S | 1.11 | 1.08 | 1.67 | 1.05 | 1.09 | 1.13 | 1.13 | 1.24 | 1.17 | 1.13 | 1.1 |
| e- void/cell | #N/A | 811 | #N/A | 892 | #N/A | #N/A | 250 | #N/A | 291 | #N/A | 201 |
| Num G | #N/A | 13.983 | #N/A | 13.515 | #N/A | #N/A | 3.788 | #N/A | 4.409 | #N/A | 3.045 |
| round (Num G) | #N/A | 14 | #N/A | 14 | #N/A | #N/A | 4 | #N/A | 4 | #N/A | 3 |
| ratio H:G | #N/A | 1.29 | #N/A | 1.29 | #N/A | #N/A | 1.5 | #N/A | 1.5 | #N/A | 1.33 |

(a)

(b)

Figure S21 Calculated powder X-ray diffraction (PXRD) patterns for the complexes of H with (a) ANI and (b) 2MA, illustrating the close similarity between the two.

(a)

(b)

Figure S22 Calculated powder X-ray diffraction (PXRD) patterns for the complexes of H with (a) 3MA and (b) 4MA1, illustrating their isostructurality.