Supporting information

Molecular Weight Effects on the Physicochemical and Functional Behavior of Pectin from Pomelo Peel Waste

Li-Fang Zhu1·Zhigang Gao2 · John J. Wang3 · Weng Qi Biao4 · Ming-Wei Chang5* · Xiaojing Li2*

1 College of Tourism and Leisure Management, Fujian Business University, Fuzhou 350012, China
2 College of Environment & Safety Engineering, Fuzhou University, Fuzhou, 350108,
China
3 School of Resources and Safety Engineering, Chongqing University, Chongqing, 401331, China
4 Fujian Provincial Key Laboratory of Eel Breeding and Processing, Fuzhou, 350108,
China
5 Nanotechnology and Integrated Bioengineering Centre, University of Ulster, Belfast BT15 1AP, UK
* Corresponding author

Table S1. The effects of ultrasound duration and enzyme dosage on DE

| Treatment |  | Degree of esterification (DE, %) |
| --- | --- | --- |
| Ultrasonic duration | 30 s | 83.42 |
|  | 15 min | 84.37 |
|  | 30 min | 83.26 |
|  | 45 min | 2.34 |
| Enzyme dosages /U | 5000 | 91.8 |
|  | 10000 | 93.19 |
|  | 20000 | 84.48 |
|  | 30000 | 65.0 |

Table S2. Swelling properties of the HMP and LMP

| Time (min) | Swelling ratio (%) |  |
| --- | --- | --- |
|  | HMP | LMP |
| 0 | 0 | 0 |
| 15 | 59.1 | 33 |
| 30 | 87 | 47.5 |
| 45 | 115.8 | 67.3 |
| 60 | 137.5 | 83 |
| 90 | 159.3 | 102 |
| 120 | 181.1 | 118.4 |
| 180 | 209.1 | 142.4 |
| 240 | 227.4 | 167.2 |
| 360 | 250.9 | 193.4 |
| 480 | 267.6 | 212.4 |
| 600 | 284.4 | 226 |
| 720 | 297.1 | 238.7 |
| 840 | 300.4 | 248.3 |
| 1020 | 304.5 | 252 |
| 1200 | 305.3 | 253.4 |
| 1440 | 305.8 | 253.8 |

Figure S1. Effects of extraction parameters on pectin yield: (a) temperature; (b) solid-to-liquid ratio; (c) extraction time; (d) pH.

Figure S2. Molecular weight determination of pectin extracted under different ultrasonic durations and enzyme dosages: (a1) 15 min, (a2) 30 min, (a3) 45 min; (b1) 10,000 U, (b2) 20,000 U, (b3) 30,000 U.

Figure S3. FTIR spectra of pectin extracted by UAE (a) and enzymatic treatment (b).

Figure S4. XPS survey spectra of HMP and LMP.

Figure S5. Ion chromatograms of mixed monosaccharide standards (a), HMP (b), and LMP (c).