Supplementary Material

Antibacterial cotton fabric prepared by a “grafting to” strategy using a QAC copolymer

Pei Wang1·JieHao Qu2·Lujie Wang1·Junzhao Geng1·FeiYa Fu1·Xiangdong Liu*1

1 School of Materials Science and Engineering, Zhejiang Sci-Tech University, Xiasha Higher Education Zone, Hangzhou 310018, People’s Republic of China

2 Zhejiang Huashuaite New Material Technology Co., Ltd., No. 188, East Yongqing Road, Shendang, Haiyan, Jiaxing, Zhejiang 314311, People’s Republic of China.

*Corresponding authors: Xiangdong Liu, liuxd@zstu.edu.cn

Other materials

Escherichia coli (E. coli, LWCC1003) and Staphylococcus aureus (S. aureus, LWCC1002) were obtained by Luwei Technology. Co., Ltd (Shanghai, China). Cell counting kit-8 (CCK-8) was purchased from Dojindo (Japan). Mouse embryonic fibroblast cells (NIH/3T3) and the Annexin V-FITC Apoptosis Detection Kit were produced by BD Biosciences (San Diego, USA). Glutaraldehyde aqueous (50%), PBS solution and ethanol (50%, 70%, 90%, 100%) were obtained from Shanghai McLean Biochemical Co., Ltd.

Antimicrobial durability test

Laundering durability was evaluated by monitoring the antimicrobial ability of the modified cotton fabric sample periodically after repeated stringent washing cycles. The cotton fabrics (5.00 cm × 5.00 cm) were washed with 50.0 mL of aqueous solution of sodium dodecane sulfonate (2.00 wt%) in a beaker (diameter, 50 mm), stirring (300 rpm, magnetic stirrer) at 25 °C for 10 min, rinsed with deionized water (25 °C, 10.0 mL × 3 times), and dried at 100 °C for 1h. The antimicrobial function of the laundered samples was evaluated using the antimicrobial test described above.

Water vapor permeability test

Water vapor permeability was evaluated using the ASTM E-96 (open cup test) method. A shallow dish containing deionized water was tightly covered using a test cotton fabric (5.00 cm × 5.00 cm). The weight loss of the test assembly over 24 h was measured and the vapor transmission rate (g/m2/d) was calculated as water vapor permeability. Water absorptivity was measured using the difference in weight of the cotton sample after immersing in plenty of deionized water and hanging out for another 10 min. These measurements were repeated for three times to get the average values.

where T is the water vapor permeability (g/m2/d), which means the lost weight on per square meter 24 h. m0 and ma are the water weight before and after 24 h, respectively, r is the inside radius of the cup.

Water absorptivity

Water absorptivity was measured using the difference in weight of the cotton sample after immersing in plenty of deionized water and hanging out for another 10 min. These measurements were repeated for three times to get the average values. The formula for calculating the water absorbability is as follows:

The 𝑤% refers to the water absorbability of cotton fabric. The 𝑤0 and 𝑤𝑎 represent the weight of cotton fabric before soaking and after hanging

Flexibility test

Flexibility was determined by the flat loop method (IS 7016 Part 11). Fabric samples were cut from warp and weft directions (40 mm × 160 mm). A loop was made and placed on a horizontal plane. The height of the loop was measured as an index of the flexibility of the fabric. The lower the height of the loop, the greater is the flexibility.

Fig. S1. Synthesis of poly(DMC-co-MA), for PD10M1, PD50M1 and PD100M1 copolymers, the monomer ratios of DMC/MA are 10:1, 50:1 and 100:1, respectively.

Fig. S2. Linear relationship of absorbance at 460 nm versus methyl orange concentration.

Table S1 Mole ratio of DMC and MA units calculated from the 1H-NMR spectra.

| sample | integral area |  |  | mole ratio a |
| --- | --- | --- | --- | --- |
|  | a | e, f | g |  |
| PD10M1 | 1.233 | 1.092 | 1.000 | 13.4 |
| PD50M1 | 1.440 | 1.027 | 1.000 | 53.3 |
| PD100M1 | 1.593 | 1.017 | 1.000 | 93.7 |

a The DMC/MA unit ratios in the poly(DMC-co-MA)s were calculated by the integral values of the NMR peaks (Figure 2, a, e, f and g) by {a/[(e, f)-g)]}.

Table S2. The elemental contents of the coatings on the fabric surfaces that measured by XPS techniques.

| Sample | Atomic composition (%) |  |  |  |
| --- | --- | --- | --- | --- |
|  | C1s | O1s | N1s | Cl2s |
| original cotton | 59.62 | 40.38 | - | - |
| PD100M1 | 63.19 | 34.01 | 2.21 | 0.59 |

Table S3 Poly(DMC-co-MA) copolymers that grafted on the cotton fabrics

| Sample | MODa (mmol/L) | PMFb (g/kg) |
| --- | --- | --- |
| original cotton PD10M1-CMC-Cotton | 0 17.4 × 10-4 | 0 0.237 |
| PD50M1-CMC-Cotton | 28.9 × 10-4 | 0.394 |
| PD100M1-CMC-Cotton | 42.4 × 10-4 | 0.579 |

a Decrease in methyl orange concentration : MOD (mmol/L)

b Estimated poly(DMC-co-MA) moieties that grafted on the fabrics : PMF (g/kg)