Aluminum-modified silica achieves efficient removal of low fluoride wastewater by inducing crystallization

Supplementary information

Shida Zhang ab, Zhen Qi ab, Fengke Dou c, Weijie Zhong c, Yingqiang Li ab, Zheyu Wang ab, Cui Zhen Sun, Feiyong Chen a, Xue Shen a*, Rupeng Liu a*

a Institute of Resources and Environment Innovation, Shandong Jianzhu University, Jinan 250101, P.R. China

b School of Municipal and Environmental Engineering, Shandong Jianzhu University, Jinan 250101, P.R. China

c Shandong Coal Field Geological Survey and Research Institute, Jinan 250101, P.R. China

* Corresponding author

Xue Shen, E-mail: shenxue20@sdjzu.edu.cn; Tel: +86-17862922336;

Rupeng Liu, E-mail: liurupeng@sdjzu.edu.cn; Tel: +86-13305310386.

Fig. S1. The schematic diagram of the production route of Al@SiO2.

Fig. S2. EDS spectrum diagram of quartz sand (A), SiO2 (B), and Al@SiO2 (C).

Table S1. Orthogonal experimental factor level setting.

|  | A | B | C | D |
| --- | --- | --- | --- | --- |
| Factor level | Dosage (g/L) | P: F | Ca/ F | Time (min) |
| 1 | 2.4 | 7 | 12 | 80 |
| 2 | 2 | 5 | 10 | 60 |
| 3 | 1.6 | 3 | 8 | 40 |

Table S2. Orthogonal experimental design scheme and results.

| Number | A | B | C | D | Removal (%) |  |
| --- | --- | --- | --- | --- | --- | --- |
| 1 | 1.6 | 3 | 10 | 60 |  | 74.32 |
| 2 | 2.4 | 3 | 10 | 60 |  | 81.32 |
| 3 | 1.6 | 7 | 10 | 60 |  | 77.55 |
| 4 | 2.4 | 7 | 10 | 60 |  | 81.77 |
| 5 | 2 | 5 | 8 | 40 |  | 80.15 |
| 6 | 2 | 5 | 12 | 40 |  | 82.78 |
| 7 | 2 | 5 | 8 | 80 |  | 80.45 |
| 8 | 2 | 5 | 12 | 80 |  | 84.55 |
| 9 | 1.6 | 5 | 10 | 40 |  | 73.24 |
| 10 | 2.4 | 5 | 10 | 40 |  | 79.46 |
| 11 | 1.6 | 5 | 10 | 80 |  | 76.24 |
| 12 | 2.4 | 5 | 10 | 80 |  | 82.93 |
| 13 | 2 | 3 | 8 | 60 |  | 78.74 |
| 14 | 2 | 7 | 8 | 60 |  | 82.44 |
| 15 | 2 | 3 | 12 | 60 |  | 84.47 |
| 16 | 2 | 7 | 12 | 60 |  | 84.35 |
| 17 | 1.6 | 5 | 8 | 60 |  | 73.48 |
| 18 | 2.4 | 5 | 8 | 60 |  | 82.72 |
| 19 | 1.6 | 5 | 12 | 60 |  | 80.23 |
| 20 | 2.4 | 5 | 12 | 60 |  | 82.85 |
| 21 | 2 | 3 | 10 | 40 |  | 78.23 |
| 22 | 2 | 7 | 10 | 40 |  | 79.11 |
| 23 | 2 | 3 | 10 | 80 |  | 79.13 |
| 24 | 2 | 7 | 10 | 80 |  | 83.92 |
| 25 | 2 | 5 | 10 | 60 |  | 86.67 |
| 26 | 2 | 5 | 10 | 60 |  | 85.98 |
| 27 | 2 | 5 | 10 | 60 |  | 86.63 |
| 28 | 2 | 5 | 10 | 60 |  | 85.89 |

Table S3. Analysis of variance results.

| Source | Sum of Squares | df | Mean Square | F-value | p-value | Significant |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Model | 387.66 | 14 | 27.69 | 70.15 | <0.0001 | Significant |
| A-dosage | 107.94 | 1 | 107.94 | 273.18 | < 0.0001 |  |
| B-P:F | 13.93 | 1 | 13.93 | 35.26 | < 0.0001 |  |
| C-Ca:F | 37.63 | 1 | 37.63 | 95.24 | < 0.0001 |  |
| D-time | 16.92 | 1 | 16.92 | 42.83 | < 0.0001 |  |
| AB | 1.93 | 1 | 1.93 | 4.89 | 0.0455 |  |
| AC | 10.96 | 1 | 10.96 | 27.73 | 0.0002 |  |
| AD | 0.0552 | 1 | 0.0552 | 0.1398 | 0.7145 |  |
| BC | 3.65 | 1 | 3.65 | 9.23 | 0.0095 |  |
| BD | 3.82 | 1 | 3.82 | 9.67 | 0.0083 |  |
| CD | 0.5402 | 1 | 0.5402 | 1.37 | 0.2633 |  |
| A² | 154.05 | 1 | 154.05 | 389.88 | < 0.0001 |  |
| B² | 42.52 | 1 | 42.52 | 107.61 | < 0.0001 |  |
| C² | 8.35 | 1 | 8.35 | 21.13 | 0.0005 |  |
| D² | 65.62 | 1 | 65.62 | 166.08 | < 0.0001 |  |
| Residual | 5.14 | 13 | 0.3951 |  |  |  |
| Lack of Fit | 4.62 | 10 | 0.4621 | 2.69 | 0.2251 | Not significant |
| Pure Error | 5.14 | 13 | 0.3951 |  |  |  |
| Cor Total | 392.69 | 27 |  |  |  |  |

Fig. S3. EDS spectrum diagram of Al@SiO2 after reaction.

Fig. S4. The full spectrum of the XPS scan before the reaction.