Highlights

1. Five nucleating agents for SAT supercooling suppression were systematically compared.

2. 4.0 wt.% Na₄P₂O₇·10H₂O reduces SAT supercooling to 2.7 °C.

3. 1.0 wt.% nano-α-Al₂O₃ gives 4.2 °C supercooling, +60% κ, 3.6% latent loss.

4. Non-monotonic relationship between nucleator concentration and supercooling suppression due to nanoparticle agglomeration.

5. SAT with 1.0 wt.% nano-α-Al₂O₃ excels for low-to-medium thermal storage applications.