Table S1. Proximate analysis of Rhizoclonium hookeri biochar.

| Components | Amount (%) |
| --- | --- |
| Moisture content | 6.4 |
| Volatile content | 44.80 |
| Ash content | 46.17 |
| Fixed carbon content | 2.63 |
| % Yield | 69 |

Table S2. Calibration data for MG dye

| S.NO | Concentration (mg/ml) | Absorbance (a.u) |
| --- | --- | --- |
| 1 | 10 | 0.168 |
| 2 | 20 | 0.319 |
| 3 | 30 | 0.479 |
| 4 | 40 | 0.642 |
| 5 | 50 | 0.805 |
| 6 | 60 | 0.945 |
| 7 | 70 | 1.099 |

Figure S1. Calibration curve illustrates the relationship between the absorbance of MG and its concentration.

Table S3. Elemental composition of Rhizoclonium hookeri biochar.

| Element | %Weight | Atomic % | Elements | % Weight | Atomic |
| --- | --- | --- | --- | --- | --- |
| C | 31.92 | 43.29 | Cl | 0.23 | 0.10 |
| O | 43.83 | 44.63 | K | 3.58 | 1.49 |
| Mg | 1.40 | 0.94 | Ca | 2.90 | 1.18 |
| Al | 3.23 | 1.95 | Fe | 2.24 | 0.65 |
| Si | 8.41 | 4.88 | Cu | 1.05 | 0.27 |
| S | 1.23 | 0.62 | Total | 100.00 | 100.00 |

Table S4. Parameters extracted from pseudo-first-order and pseudo-second-order kinetic model.

| Pseudo-first-order kinetics |  |  |  |  | Pseudo-second-order kinetics |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| qe (mg g-1) experimental | qe (mg g-1) calculated | R² | RMSE | K1 (1/min) |  | qe (mg g-1) calculated | qe (mg g-1) experimental | R² | K2 | RMSE |  |
| 29.9 | 62.5 | 0.931 | 0.553 | 0.0566 |  | 29.04 | 34.01 mg | 0.9996 | 0.00128 | 0.080 |  |

PSEUDO 2ND ORDER KINETICS

Figure S2. Test plots of Pseudo-first- and Pseudo-Second-Order models for MG dye adsorption on Rhizoclonium hookeri biochar.

Table S5. Parameters extracted from intraparticle diffusion model.

| Intraparticle diffusion model | Kid | C(intercept) | R2 |
| --- | --- | --- | --- |
| qt = kid t1/2 + C | 0.0681 | 3.05 | 0.9624 |

Figure S3 Test Plot of t vs t^1/2 for Intra-particle Diffusion Model

Figure S4. Langmuir isotherm for MG adsorption on biochar.

Table S6. Langmuir and Freundlich constant for the adsorption of MG.

| Langmuir constant |  |  |  |  | Freundlich constant |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| qmax (mg g-1) | KL | R2 | RMSE | X2 |  | RL | Kf | 1/n | R2 | RMSE | X2 |
| 35.46 | 0.0286 | 0.997 | 0.060 | 0.695 |  | 0.33 | 0.412 | 2.39 | 0.95 | 2.56 | 1.48 |

Figure S.7   Freundlich isotherm for MG adsorption on Rhizoclonium hookeri biochar.