Supporting Information

Functionalized porous nanoscale Fe3O4 particles supported biochar from peanut shell for Pb(II) ions removal from wastewater of wetland park

Xiaojun Jin1, 2, Renrong Liu1, Huifang Wang1, Li Han1, Muqing Qiu1*, Baowei Hu1

1 School of Life Science, Shaoxing University, Shaoxing, 312000, P.R. China

2 Tongchuang Engineering Design Co. LTD., Shaoxing , 312000, P.R. China

*Corresponding author: Muqing Qiu, qiumuqing@usx.edu.cn

Characterization of sorbents

SEM (JEOL 6500F, Japan) and TEM (Tecnai G2 20, Netherlands) was used to observe the surface morphology and structure of adsorbents. The surface area and pore size of adsorbents were determined by the NOVA 4200e Surface area and Pore size analyzer (Quantachrome, FL, USA) at a relative pressure of 0.95 following the multipoint N2-BET adsorption method. The surface functional groups of adsorbents in the wave number range of 500-4000 cm-1 were recorded on a Nexus 670 FT-IR spectrometer (Thermo Nicolet, Madison). The crystalline structures of the adsorbents were conducted in a D/Max-IIIA Powder X-ray Diffractomer (Rigaku Corp., Japan). XPS (X-ray photoelectron spectrometer, Krato AXIS Ultra DLD, Japan) and the model Axis-HS (Kratos Analytical) were used to determine the surface of adsorbents.

Calculation of removal rate and uptake capacity

The removal rate ((%)) and the adsorption capacity ((mg/g)) were calculated according to the following Eq.1-2.

(1)

(2)

Where (mg/L) and (mg/L) were initial concentration and equilibrium concentration, respectively. (L) was the solution volume and (g) was the weight of adsorbent.

Adsorption experiments

The effect of pH

50 mg adsorbent and 50 mL 100 mg/L Pb(II) ions in solution with different pH (2.0, 4.0, 6.0, 8.0, 10.0 and 12.0) were charged into a series of flasks, respectively.  The mixture was shaken at 200 rpm and 25 °C for 8 h.

The effect of initial concentration

50 mg adsorbent and 50 mL initial concentration of Pb(II) ions in solution with a different initial concentration (50, 100, 150, 200, 300, 400 and 500 mg/L) were charged into a series of flasks, respectively. The mixture was shaken at pH6.0, 200 rpm and 25 °C for 8 h.

The effect of contact time

50 mg adsorbent and 50 mL 100 mg/L Pb(II) ions in solution were charged into a series of flasks, respectively. The mixture was shaken at pH 6.0, 200 rpm and 25 °C for different time (10, 20, 30, 60, 90, 120, 180, 240, 300, 360 and 420 min).

The effect of temperature

50 mg adsorbent and 50 mL 100 mg/L Pb(II) ions in solution were charged into a series of flasks, respectively. The mixture was shaken at pH 6.0 and 200 rpm for 8 h. Temperature is 25, 35 and 45°C, respectively.

Recycle experiment

50 mg adsorbent and 50 mL 100 mg/L Pb(II) ions in solution were charged into a series of flasks, respectively. The mixture was shaken at pH 6.0, 200 rpm and 25 °C for 8 h.

Pseudo first-order and pseudo second-order kinetic

In order to describe the adsorption mechanism, the adsorption kinetics is described by the pseudo first-order and pseudo second-order kinetic models. The Eq.3-4 represent the linear forms of pseudo first-order (Hummers ＆ Offeman 1958) and pseudo second-order kinetic models (Lagergren 1898).

(3)

(4)

Where, (mg/g) and  (mg/g) are adsorption capacity of NO3- and PO43- ions solution by Mg/Ca@PS at adsorption time  and adsorption equilibrium respectively.  (min-1) and  (min-1) are the adsorption rate constant.

Langmuir isotherm model and Freundlich isotherm model

In order to investigate adsorption process, the experimental data of N and P uptake onto Mg/Ca@PS are analyzed using Langmuir isotherm model (Langmuir 1918) and Freundlich isotherm model (Freundlich 1906). Langmuir isotherm model expresses monolayer adsorption. The adsorbate arrives at the unevenly surface of the adsorbent from the liquid phase. They can be expressed in Eq.5-6. They are following as:

(5)

Where, (mg/g) is concentration of adsorbed NO3- and PO43- ions at equilibrium. (mg/g) is the maximum uptake capacity of N and P. (mg/L) is concentration of N and P at equilibrium and (L/mg) is constant.

(6)

Where, (mg/g) is the amount of adsorbed NO3- and PO43- ions per unit mass of the adsorbent at equilibrium. (mg/L) is concentration of NO3- and PO43- ions at equilibrium.  and  are constant.

Calculation of thermodynamic parameters

In order to explore further mechanism of U(VI) uptake, thermodynamic parameters are evaluated to determine the spontaneity of the reaction. They are Gibbs free energy ((kJ/mol)), enthalpy ((kJ/mol)) and entropy ((J/mol/K)) respectively. They are associated with the adsorption can be calculated using the following Eq.7-9:

(7)

(8)

(9)

Where,  is the solution temperature (K),  is the adsorption equilibrium constant,  is the gas constant (8.314 J.mol-1.K-1),  is the amount of adsorbate adsorbed per unit mass of adsorbate at equilibrium (mg/g) and  is the equilibrium concentration of the adsorbate (mg/L).  and  are calculated from the slope and the intercept respectively.

Table 1 Comparison of adsorption capacity of Pb2+ ions by different adsorbents

| Adsorbent | (mg/g) | Ref. |
| --- | --- | --- |
| M-Lignin-PEI CP-Fe-Mn L1@MNP MCW-2 Fe3O4-GS Magnetic-biochar Fe3O4-CS-L CS-S-Fe-Mn PS-Fe3O4 | 96.60 49.64 111.23 41.19 27.95 64.13 128.63 147.76 188.68 | Zhang et al. 2019 Maneechakr ＆ Mongkollertlop, 2020 Zhou et al. 2021 Edathil et al. 2018 Guo et al. 2014 Li et al. 2019 Guo et al. 2017 Maneechakr ＆ Karnjanakom 2021 This work |

Table 2 Thermodynamic parameters of Pb2+ ions in solution removal by PS-Fe3O4 composites

| (kJ/mol) |  |  | (kJ/mol) | (J/mol/K) |
| --- | --- | --- | --- | --- |
| 298 (K) | 308 (K) | 318 (K) |  |  |
| -7.04 | -8.27 | -10.28 | 41.13 | 161.25 |

References

Freundlich H.M.F. 1906. Uber die adsorption in lasungen. J. Phys. Chem., 57, 385-470.

Hummers W.S., Offeman R.E. 1958. Preparation of graphitic oxide. J. Am. Chem. Soc., 80, 1339-1339.

Lagergren S. 1898. Zur theorie der sogenannten adsorption geloster stoffe. Pseudo-second order model for sorption processes. Handlingar, 24, 1-39.

Langmuir I. 1918. The adsorption of gases on plane surface of glass, mica and platinum. J. Am. Chem. Soc., 40, 1361-1403.