Supporting Information for

Development of a self-reporting electrochemical sensor utilizing CoNiFe-PBA for detection of BPA in food Samples

Zitong Yang , Jingyu Deng, Yili Zhang, Wenkai Qi, Yuxia Zhang*

Key Laboratory of Hunan Province for Advanced Carbon-based Functional Materials, School of Chemistry and Chemical Engineering, Hunan Institute of Science and Technology, Yueyang 414006, China

*Corresponding Author

Email: zyxia2010@126.com (Y.Z)

Fig. S1 .CV (A) and DPV (B) measurements of bare GCE (b) and RGO/GCE (c) in 0.1 M KCl solution containing 2.5. mM [Fe(CN)6]3-/4-

Fig. S2. Linear calibration curve of absorbance versus BPA concentration.

Fig. S3. MIP/CoNiFe-PBA/RGO/GCE repeatability (A) and reproducibility(B).

Table. S1. Recovery experiment results of MIP/CoNiFe-PBA/RGO/GCE in actual samples

| Actual samples | Add (nM) | Found (nM) | Recovery (%) | RSD (%, N=3) |
| --- | --- | --- | --- | --- |
| Lake water | 25 | 25.56 | 102.24 | 3.40 |
|  | 250 | 245.49 | 98.20 | 2.16 |
|  | 500 | 487.42 | 97.48 | 1.48 |
| Tap water | 25 | 25.96 | 103.84 | 3.92 |
|  | 250 | 244.50 | 97.8 | 1.82 |
|  | 500 | 486.57 | 97.31 | 2.15 |
| Mineral water | 25 | 24.21 | 96.84 | 3.68 |
|  | 250 | 247.61 | 99.04 | 1.10 |
|  | 500 | 516.37 | 103.27 | 2.36 |
| AD Calcium Milk | 25 | 24.6 | 98.4 | 4.27 |
|  | 250 | 257.41 | 102.96 | 1.78 |
|  | 500 | 485.89 | 97.18 | 2.27 |
| Pure milk | 25 | 24.6 | 98.4 | 4.31 |
|  | 250 | 257.16 | 102.86 | 1.31 |
|  | 500 | 485.89 | 97.18 | 1.73 |

| Actual samples | Add (nM) | Found (nM) | Recovery (%) | RSD (%, N=3) |
| --- | --- | --- | --- | --- |
| Paperboard carton | 25 | 26.16 | 104.64 | 5.37 |
|  | 250 | 256.99 | 102.80 | 1.81 |
|  | 500 | 512.43 | 102.49 | 2.27 |
| Plastic bottle | 25 | 25.72 | 102.88 | 4.17 |
|  | 250 | 258.27 | 103.31 | 0.52 |
|  | 500 | 515.37 | 103.07 | 1.61 |

Recovery experiment results of MIP/CoNiFe-PBA/RGO/GCE in actual samples (Continued Table. S1.)

| Soy sauce | 25 | 25.26 | 101.04 | 4.08 |
| --- | --- | --- | --- | --- |
|  | 250 | 244.32 | 97.73 | 1.30 |
|  | 500 | 505.45 | 101.09 | 2.02 |
| Juice | 25 | 24.66 | 98.64 | 2.40 |
|  | 250 | 256.27 | 102.5 | 1.15 |
|  | 500 | 486.57 | 97.31 | 2.23 |
| Can coating | 25 | 26.21 | 104.84 | 4.77 |
|  | 250 | 262.43 | 104.97 | 1.81 |
|  | 500 | 512.48 | 102.50 | 1.95 |

Table. S2. Spiked recovery test data for HPLC analysis of BPA in actual samples

| Actual samples | Add (nM) | Found (nM) | Recovery (%) | RSD (%, N=3) |
| --- | --- | --- | --- | --- |
| Lake water | 250 | 256.04 | 102.42 | 1.95 |
| Mineral water |  | 252.37 | 100.9 | 1.74 |
| Tap water |  | 254.13 | 101.65 | 2.45 |
| AD Calcium Milk |  | 256.04 | 102.42 | 1.27 |
| Pure milk |  | 260.79 | 104.32 | 1.04 |
| Soy sauce |  | 254.79 | 101.92 | 2.19 |
| Juice |  | 259.70 | 103.88 | 1.58 |
| Can coating |  | 264.05 | 105.62 | 0.97 |
| Paperboard carton |  | 262.43 | 104.97 | 1.44 |
| Plastic bottle |  | 264.11 | 105.64 | 1.72 |