Supplementary Information

Efficient ethylene purification by a robust ethane-trapping porous organic cage

Kongzhao Su1,2,4, Wenjing Wang1,4, Shunfu Du1,3, Chunqing Ji1,2 & Daqiang Yuan1,2,*

1State Key Laboratory of Structure Chemistry, Fujian Institute of Research on the Structure of Matter, Chinese Academy of Sciences, Fuzhou, 350002 Fujian, China

2University of the Chinese Academy of Sciences, Beijing, 100049, China

3College of Chemistry, Fuzhou University, Fuzhou, 350116, China

4These authors contributed equally

Corresponding author. E-mail address: ydq@fjirsm.ac.cn (D.Q. Yuan).

Supplementary Fig. 1 Keto–enol tautomerization within CPOC-1.

Supplementary Fig. 2 1HNMR of CPOC-1 (CDCl3, 400 MHz, 298 K).

Supplementary Fig. 3 FT-IR spectra of CPOC-1.

Supplementary Fig. 4 1HNMR of CPOC-1 after storing in air for half a year (CDCl3, 400 MHz, 298 K).

Supplementary Fig. 5 TGA curve of CPOC-1.

Supplementary Fig. 6 PXRD pattern of CPOC-1.

Supplementary Fig. 7 C2H6 adsorption/desorption isotherm of CPOC-301 at 273, 283 and 293 K.

Supplementary Fig. 8 C2H4 adsorption/desorption isotherm of CPOC-301 at 273, 283 and 293 K.

Supplementary Fig. 9 (a) Virial equation fitting of the C2H6 adsorption isotherm of CPOC-301 at 273, 283 and 293 K. (b) Relevant fitting parameters for C2H6.

Supplementary Fig. 10 (a) Virial equation fitting of the C2H4 adsorption isotherm of CPOC-301 at 273, 283 and 293 K. (b) Relevant fitting parameters for C2H4.

Supplementary Fig. 11 Selectivity of CPOC-301 predicted by the IAST method for an equimolar C2H6/C2H4 mixture at 293 K.

Supplementary Fig. 12 Dual-site Langmuir-Freundlich fitting of the C2H6 adsorption isotherm of CPOC-301 at 293 K. (b) Relevant fitting parameters for C2H6.

Supplementary Fig. 13 Dual-site Langmuir-Freundlich fitting of the C2H4 adsorption isotherm of CPOC-301 at 293 K. (b) Relevant fitting parameters for C2H4.

Supplementary Fig. 14 1HNMR of CPOC-301 after breakthrough experiments (CDCl3, 400 MHz, 298 K).

Supplementary Fig. 15 PXRD of CPOC-301 after breakthrough experiments.

Supplementary Fig. 16 (a) Virial equation fitting of the C2H2 adsorption isotherm of CPOC-301 at 273, 283 and 293 K. (b) Relevant fitting parameters for C2H2.