Supplementary Material

Selective fragmentation of polyphthalamide via induced foaming assisted ball milling for multi-component recovery from LEDs

Mingfei Xing1*, Ping Xu1, Yun Zhao1, Shuofei Fu1, Mingshi Wang1, Li Zhao1, Fayang Guo1, Fengcheng Jiang1

1Institute of Resource and Environment, Henan Polytechnic University, Jiaozuo, China

Supplementary Material Content：

7 pages (including the cover page),

6 Figures,

3 Tables.

Elemental composition of waste LED

The metal lead frame was digested using a microwave digestion system (Anton Paar Microwave PRO) with 1.5 mL of nitric acid and 4.5 mL of hydrochloric acid at 170 °C and 40 bar for 30 min. The digested solution was subsequently evaporated to near dryness, diluted, and analyzed for elemental composition using ICP-OES (Avio 500).

Table. S1. Elemental composition of the metal lead frame

| element | Ag | Al | Cu | Fe | Ni | Zn |
| --- | --- | --- | --- | --- | --- | --- |
| Content (%) | 0.015±0.002 | 0.021±0.0001 | 65.50±0.85 | 0.011±0.001 | 0.39±0.02 | 34.07±0.31 |

Experimental design

Table. S2. Subcritical water experimental parameters

|  | Temperature (℃) | Holding time(min) | Liquid to solid ratio | Pressure（MPa） |
| --- | --- | --- | --- | --- |
| 1 | 255 | 20 | 40：1 | 3.7 |
| 2 | 270 | 20 | 40：1 | 4.6 |
| 3 | 285 | 20 | 40：1 | 5.5 |
| 4 | 300 | 20 | 40：1 | 6.4 |
| 5 | 315 | 20 | 40：1 | 9.3 |
| 6 | 285 | 25 | 40：1 | 5.5 |
| 7 | 285 | 15 | 40：1 | 5.5 |
| 8 | 285 | 10 | 40：1 | 5.5 |
| 9 | 285 | 5 | 40：1 | 5.5 |
| 10 | 255 | 10 | 40：1 | 3.7 |
| 11 | 270 | 10 | 40：1 | 4.6 |
| 12 | 300 | 10 | 40：1 | 6.4 |
| 13 | 315 | 10 | 40：1 | 9.3 |
| 14 | 285 | 10 | 20：1 | 4.6 |
| 15 | 285 | 10 | 10：1 | 4.6 |
| 16 | 285 | 10 | 5：1 | 4.6 |
| 17 | 285 | 10 | 1：1 | 4.6 |

EDS spectrum of virgin PPA cross-section

Fig. S1. EDS spectrum of virgin PPA cross-section

From Fig. S1, the presence of Ti in PPA indicates the incorporation of titanium dioxide, which serves as a whitening agent in the plastic. The detection of Si and Mg elements can be attributed to the additives contained in the PPA material.

FTIR spectra of PPA obtained at different SubCW treatment temperatures.

Fig. S2. FTIR spectra of PPA obtained at different SubCW treatment temperatures.

Analysis of oil-phase products after subcritical water treatment

The oil-phase products obtained from LEDs after subcritical water treatment were analyzed using gas chromatography–mass spectrometry (GC–MS, Agilent 7890A/5975C, USA). A DB-5 capillary column (60 m × 0.25 mm × 0.25 μm) was employed. The oven temperature program was set as follows: initial temperature of 50 °C (held for 5 min), ramped at 10 °C/min to 280 °C, and maintained for 20 min.

Table. S3. GC–MS results of the oil-phase products obtained at different temperatures.

| Components | Chemical formulas | Area (%) (255℃) | Area (%) (270℃) | Area (%) (285℃) | Area (%) (300℃) | Area (%) (315℃) |
| --- | --- | --- | --- | --- | --- | --- |
| Benzoic acid | C7H6O2 |  |  |  |  | 28.11 |
| 2,4-Di-tert-butylphenol | C₁₄H₂₂O | 3.74 | 6.39 | 2.12 | 5.73 |  |
| Tributyl phosphate | C₁₂H₂₇O₄P | 1.73 | 0.95 |  |  | 1.41 |
| 2,4-bis(1-methyl-1-phenylethyl) | C24H26O | 4.00 |  |  | 4.17 |  |
| n-Hexadecanoic acid | C16H32O2 | 32.73 | 34.08 | 16.58 | 14.1 | 16.24 |
| Bicyclo[3.3.1]nona-2,6-diene | C14H11N |  |  |  | 5.87 |  |
| Eicosyl isobutyl ether | C24H50O | 1.19 |  |  |  |  |
| Tetrazolo[1,5-a]pyrimidine, 5,7-dimethyl | C6H7N5 |  |  |  | 12.70 |  |
| Oleic Acid | C18H34O2 | 8.10 | 4.69 | 12.13 | 11.6 | 15.78 |
| 9-Octadecenoic acid, (E)- | C18H34O2 |  |  | 30.07 |  |  |
| Octadecanoic acid | C18H36O2 | 25.82 | 24.64 | 17.14 | 12.58 | 13.79 |
| N-Acrylonitryl-2,2-dimethylaziridine | C4H9N |  |  |  | 17.26 |  |
| Ethyl hexadecyl ether | C18H38O | 2.13 |  |  |  |  |
| 9-Octadecenamide | C18H35N |  |  |  | 4.08 |  |
| 2,4,6-Trimethylbenzoic acid | C10H12O2 |  |  | 1.23 |  |  |
| (9E,11E)-Octadecadienoic acid | C18H32O2 | 1.99 | 7.54 | 8.73 | 1.59 | 2.69 |
| 10E,12Z-Octadecadienoic acid | C18H32O2 | 1.79 | 1.14 |  |  |  |

Proposed degradation mechanism of PPA plastic in subcritical water

The removal of PPA from waste LEDs is a key step toward the complete recovery of all components. Therefore, based on bond energy theory and GC–MS analysis, the possible degradation pathways of organic compounds in PPA under subcritical water conditions were investigated. The proposed degradation pathways of organics in PPA are illustrated in Fig. S3.

Fig. S3. Proposed bond cleavage and decomposition pathways of PPA and additives in SubCW.

Thermal performance analysis of virgin and recycled PPA

Fig. S4. TG–DTG curves (a, b) and DSC curves (c, d) of the virgin and recovered PPA.

SEM micrographs of the recycled products

Fig. S5. SEM images of recovered products: PPA powder (a), silver wire(b), LED chip (c), and phosphor (d).

Glass fiber analysis in virgin and recycled PPA

To compare the morphology of glass fiber bundles in virgin and recycled PPA, 0.1g of each sample was accurately weighed and digested in 5mL of concentrated nitric acid using microwave-assisted digestion at 200°C for 30min. This treatment effectively removed the organic polymer matrix and exposed the embedded glass fibers. After digestion, the residues were thoroughly washed and dried, followed by microscopic examination to evaluate and compare the morphology of the glass fiber bundles.

Fig. S6. Glass fibers in virgin PPA (a) and recycled PPA (b).