Supplementary Information

Coupled Ionic–Electronic Transport Governs Energy Conversion in Hydrogel Salinity-Gradient Batteries

Chun-Hao Huang, 1‡ Chia-Fu Chang, 1‡ Bing-Xuan Zhong, 1‡ Phok-Jin Yang,2 Ying-Huang Lai,3 Yi-Qi Yeh,2 Chia-Hsin Wang,2 Lo-Yueh Chang,2 Ying-Rui Lu,2 U-Ser Jeng,2 Chien-Lung Wang,1* Wei-Tsung Chuang, 2*

1 Department of Chemistry, National Taiwan University, No. 1, Sec. 4, Roosevelt Road, Taipei 10617, Taiwan

2 National Synchrotron Radiation Research Center, 101 Hsin-Ann Road, Hsinchu 300092, Taiwan

3 Department of Chemistry, Tunghai University, No. 1727, Sec. 4, Taiwan Boulevard, Taichung 40704, Taiwan

‡These authors contributed equally.

Correspondence.

Chien-Lung Wang (kclwang@ntu.edu.tw),

Wei-Tsung Chuang (weitsung@nsrrc.org.tw)

Supplementary Figure 1. SAXS profiles of NxEy@H70%-LiCl hydrogels fitted using the Ornstein–Zernike (O–Z) and Guinier models for different monomer ratios (x : y): (a) 9 : 1, (b) 7 : 3, (c) 5 : 5, (d) 3 : 7, (e) 1 : 9.

Supplementary Figure 2. SAXS profiles of N7E3@Hw%-LiCl hydrogels fitted using the Ornstein–Zernike (O–Z) and Guinier models for different water contents (w %): (a) 70 %, (b) 68 %, (c) 62 %, (d) 58 %.

Supplementary Figure 3. Photographs of N7E3@Hw% hydrogels with different water contents. At w = 80 %, the sample exhibits a soft, sol-like state.

Supplementary Figure 4. SAXS profiles of N7E3@Hw%-LiCl hydrogels fitted using the Ornstein–Zernike (O–Z) and Guinier models for different alkali metal cations (ACl) (a) LiCl (b) NaCl (c) KCl (d) CsCl.

Supplementary Figure 5. Representative voltage–time profiles of HSGB devices under different structural and ionic conditions: (a) NxEy@H70%-LiCl hydrogels with different monomer ratios (x : y); (b) N7E3@Hw%-LiCl hydrogels with different water contents (w %); (c) N7E3@H70%-LiX hydrogels showing the effect of halide anions (X⁻= Cl⁻, Br⁻, I⁻); (d) N7E3@H70%-ACl hydrogels illustrating the influence of alkali-metal cations (A⁺= Li⁺, Na⁺, K⁺, Cs⁺).

Supplementary Figure 6. Representative current–voltage (I–V) curves and power density plots for paper-based N7E3@H70% HSGB devices with different electrodes: (a) carbon paper (CP), (b) K4[Fe(CN)6]/K3[Fe(CN)6]/CP, (c) PEDOT:PSS/CP, (d) K4[Fe(CN)6]/K3[Fe(CN)6]/PEDOT:PSS/CP.

Supplementary Figure 7. Cyclic voltammograms recorded at different scan rates of (a) 10 mV/s and (b) 0.5 mV/s, with the peak-to-peak separation (ΔEp) indicated in the figures.

Supplementary Figure 8. Solubility assessment of N7E3@H70% hydrogels in water, tetrahydrofuran (THF), N,N-dimethylformamide (DMF), dimethyl sulfoxide (DMSO), chloroform, and dichloromethane (DCM).

Supplementary Figure 9. Raman spectra of PEGMA monomer, NIPAM monomer, and N7E3@H70% hydrogel, confirming the successful synthesis of the PNIPAM–PEGMA-based bottlebrush polymer hydrogels.

Supplementary Figure 10. (a) Equivalent circuit of the HSGB device; (b) photographs of the assembled HSGB components and the complete device; and (c) photographs of the assembled components and complete paper-based HSGB device.

Supplementary Table 1. Calculation of free-water fraction by DSC

- Monomer ratio (x : y)

| Sample | ∆Hm(mJ/mg) | Wt(mg)a | Wf(mg)b | Wnf(mg)ac | Free-water content (%)b | Bound-water content (%)d |
| --- | --- | --- | --- | --- | --- | --- |
| Pure water | 311.02 | 4.90 | 4.90 | 0 | 100 | 0 |
| N9E1@H70% | 259.28 | 1.79 | 1.49 | 0.30 | 83 | 17 |
| N7E3@H70% | 130.14 | 2.16 | 0.90 | 1.26 | 42 | 58 |
| N5E5@H70% | 95.22 | 4.01 | 1.22 | 2.78 | 31 | 69 |
| N3E7@H70% | 89.49 | 2.45 | 0.70 | 1.75 | 28 | 72 |
| N1E9@H70% | 91.73 | 2.89 | 0.85 | 2.04 | 29 | 71 |

- Water content (w%)

| Sample | ∆Hm(mJ/mg) | Wt(mg)a | Wf(mg)b | Wnf(mg)ac | Free-water content (%)b | Bound-water content (%)d |
| --- | --- | --- | --- | --- | --- | --- |
| Pure water | 311.02 | 4.90 | 4.90 | 0 | 100 | 0 |
| N7E3@H80% | 189.72 | 1.90 | 0.61 | 1.29 | 61 | 39 |
| N7E3@H70% | 130.14 | 2.16 | 0.90 | 1.26 | 42 | 58 |
| N7E3@H60% | 49.85 | 1.76 | 0.28 | 1.48 | 16 | 84 |
| N7E3@H50% | 0 | 0.85 | 0 | 0.85 | 0 | 100 |

(c) Anionic effect (LiX)

| Sample | ∆Hm(mJ/mg) | Wt(mg)a | Wf(mg)b | Wnf(mg)ac | Free-water content (%)b | Bound-water content (%)d |
| --- | --- | --- | --- | --- | --- | --- |
| Pure water | 311.02 | 4.90 | 4.90 | 0 | 100 | 0 |
| N7E3@H70%-LiCl | 130.14 | 2.16 | 0.90 | 1.26 | 42 | 58 |
| N7E3@H70%-LiBr | 112.32 | 2.98 | 1.08 | 1.90 | 36 | 64 |
| N7E3@H70%-LiI | 73.49 | 3.55 | 0.84 | 2.71 | 24 | 76 |

(d) Cationic effect (ACl)

| Sample | ∆Hm(mJ/mg) | Wt(mg)a | Wf(mg)b | Wnf(mg)ac | Free-water content (%)b | Bound-water content (%)d |
| --- | --- | --- | --- | --- | --- | --- |
| Pure water | 311.02 | 4.90 | 4.90 | 0 | 100 | 0 |
| N7E3@H70%-CsCl | 197.34 | 2.79 | 1.77 | 1.02 | 64 | 36 |
| N7E3@H70%-KCl | 186.78 | 2.21 | 1.33 | 0.88 | 60 | 40 |
| N7E3@H70%-NaCl | 179.62 | 2.93 | 1.58 | 1.35 | 53 | 47 |
| N7E3@H70%-LiCl | 130.14 | 2.16 | 0.90 | 1.26 | 42 | 58 |

aWt=Wgel×w%

bFree water content (%)= WfWt=∆Hm,gel/∆Hm,water

cWb=Wt-Wf

dBound water content (%)= WbWt

Wgel= gel weight

Wt= total water weight

Wf = free-water weight

Wnf = nonfree-water weight

Wb= bound-water weight

∆Hm,gel= melting enthalpy of gels

∆Hm,water= melting enthalpy of water

Supplementary Table 2. Hydration enthalpies of representative ions, as reported in reference 38.

| Cations | ∆Hhyd (kJ/mol) | Anions | ∆Hhyd (kJ/mol) |
| --- | --- | --- | --- |
| Li+ | －531.4 | Cl－ | －351.5 |
| Na+ | －422.6 | Br－ | －318.0 |
| K+ | －338.9 | I－ | －280.3 |
| Cs+ | －280.3 |  |  |

Supplementary Table 3. Summary of electrochemical performance parameters for the paper-based HSGB devices with different electrodes (carbon paper (CP), K4[Fe(CN)6]/K3[Fe(CN)6]/CP, PEDOT:PSS/CP, K4[Fe(CN)6]/K3[Fe(CN)6]/PEDOT:PSS/CP).

| Electrode | VOC (mV) | ISC (mA) | Pmaxa (x10-3 mW) | Dmaxa (mW/m2) | Dmaxb (mW/m2) |
| --- | --- | --- | --- | --- | --- |
| Carbon Paper (CP) | 106 ± 4.5 | 0.143 ± 0.007 | 2.69 ± 0.04 | 34.2 ± 0.5 | 48.0 ± 2.1 |
| K4[Fe(CN)6]/K3[Fe(CN)6]/CP | 37 ± 5.6 | 0.58 ± 0.04 | 5.4 ± 0.5 | 69±6 | 68 ± 5.6 |
| PEDOT:PSS/CP | 289 ± 44 | 0.38 ± 0.03 | 35.9 ± 2.1 | 457±27 | 347 ± 35 |
| K4[Fe(CN)6]/K3[Fe(CN)6]/PEDOT:PSS/CP | 149 ± 3.9 | 4.51 ± 0.45 | 161 ± 12 | 2050 ± 150 | 2129 ± 178 |

ᵃ The experimental maximum power (Pmax​) and maximum power density (Dmax) were determined from the peak of the power–voltage (P–V) curve, as shown in Figure S6, where P = I × V. The power density was calculated by dividing Pmax by the device’s active area.

ᵇ The theoretical maximum power density was calculated using a simplified linear resistor model (assuming constant internal resistance) according to the equation: Dmax​=(Voc×Isc​)/(4×A).