C4C5 - As(V) 200 mM

| Peak No. | Wavenumber (cm⁻¹) | Probable Functional Group | Vibration Type |
| --- | --- | --- | --- |
| 3908–3571 | 3908, 3889, 3873, 3857, 3843, 3825, 3806, 3786, 3772, 3737, 3715, 3694, 3680, 3659, 3635, 3571 | Free O–H (alcohol/phenol), structural hydroxyl | O–H stretching |
| 3269 | 3269.07 | Hydrogen-bonded O–H / possibly N–H | Broad O–H stretching |
| 2899 | 2899.77 | Aliphatic C–H | C–H stretching (CH₂/CH₃) |
| 2161 | 2161.23 | C≡C (alkyne) / weak C≡N region | Triple bond stretching |
| 1637 | 1637.80 | C=C (alkene) / Amide I / adsorbed water | C=C stretching |
| 1427 | 1427.86 | CH₂ bending / Aromatic ring | Bending vibration |
| 1334 | 1334.39 | C–N / Phenolic O–H bend | Stretching |
| 1314 | 1314.80 | C–N stretching | Stretching |
| 1279 | 1279.81 | C–O (phenol/alcohol/ether) | C–O stretching |
| 1204 | 1204.48 | C–O / C–N | Stretching |
| 1160 | 1160.42 | C–O–C (ether) | Asymmetric stretch |
| 1109 | 1109.90 | C–O (alcohol/ether) | Stretching |
| 1055 | 1055.11 | C–O (primary alcohol) | Stretching |
| 1031 | 1031.56 | C–O / Si–O (if inorganic present) | Stretching |
| 999 | 999.82 | =C–H bending (alkene) | Out-of-plane bend |
| 660 | 660.13 | C–Cl / Aromatic C–H | Stretching |
| 554 | 554.91 | C–Br / Metal–O | Stretching |
| 515 | 515.92 | Metal–O / C–Br | Stretching |
| 434 | 434.23 | Metal–O vibration | Bending/Stretching |

C2C5 - As(V) 200 mM

| Peak No. | Wavenumber (cm⁻¹) | Probable Functional Group | Type of Vibration |
| --- | --- | --- | --- |
| 3934–3574 | 3934, 3911, 3892, 3876, 3861, 3845, 3828, 3809, 3787, 3718, 3697, 3682, 3661, 3637, 3574 | Free –OH (alcohol/phenol), structural hydroxyl | O–H stretching |
| 3269 | 3269.08 | Hydrogen-bonded –OH / N–H | Broad O–H stretching |
| 2899 | 2899.50 | Aliphatic –CH₂ / –CH₃ | C–H stretching |
| 2161 | 2161.55 | C≡C (alkyne) / possible C≡N | Triple bond stretching |
| 1634 | 1634.49 | C=C (alkene) / Amide I / adsorbed water | Stretching |
| 1427 | 1427.82 | CH₂ bending / Aromatic ring | Bending |
| 1334 | 1334.44 | C–N (amine) / Phenolic O–H bend | Stretching |
| 1314 | 1314.83 | C–N stretching | Stretching |
| 1279 | 1279.94 | C–O (phenol/alcohol/ether) | Stretching |
| 1204 | 1204.58 | C–O / C–N | Stretching |
| 1160 | 1160.13 | C–O–C (ether linkage) | Asymmetric stretch |
| 1109 | 1109.84 | C–O (secondary alcohol) | Stretching |
| 1054 | 1054.70 | C–O (primary alcohol) | Stretching |
| 1031 | 1031.29 | C–O / Si–O (if inorganic matrix present) | Stretching |
| 660 | 660.28 | C–Cl / Aromatic C–H (out-of-plane) | Stretching |
| 555 | 555.14 | C–Br / Metal–O | Stretching |
| 516 | 516.12 | Metal–O / C–Br | Stretching |
| 434 | 434.42 | Metal–O vibration | Bending/Stretching |

C2C4 - As(V) 200 mM

| Peak No. | Wavenumber (cm⁻¹) | Probable Functional Group | Type of Vibration |
| --- | --- | --- | --- |
| 3908–3572 | 3908, 3889, 3873, 3857, 3843, 3825, 3806, 3786, 3772, 3737, 3715, 3695, 3680, 3660, 3636, 3572 | Free hydroxyl (–OH), structural –OH | O–H stretching |
| 2161 | 2161.00 | C≡C (alkyne) / possible C≡N | Triple bond stretching |
| 1313 | 1313.91 | C–N (amine) / phenolic O–H bend | Stretching |
| 1160 | 1160.52 | C–O–C (ether linkage) | Asymmetric stretch |
| 1109 | 1109.52 | C–O (secondary alcohol) | Stretching |
| 1054 | 1054.15 | C–O (primary alcohol) | Stretching |
| 1030 | 1030.28 | C–O / Si–O (if inorganic matrix present) | Stretching |
| 662 | 662.17 | Aromatic C–H (out-of-plane) / C–Cl | Bending/Stretching |
| 556 | 556.35 | C–Br / Metal–O | Stretching |
| 516 | 516.41 | Metal–O / C–Br | Stretching |
| 434 | 434.95 | Metal–O vibration | Bending/Stretching |

C2C4 - As(III) 5 mM

| Peak No. | Wavenumber (cm⁻¹) | Probable Functional Group | Type of Vibration |
| --- | --- | --- | --- |
| 1 | 3286.79 | Hydrogen-bonded –OH / –NH | O–H / N–H stretching |
| 2 | 2899.53 | Aliphatic –CH₂ / –CH₃ | C–H stretching |
| 3 | 1644.16 | C=O (amide I) / C=C / adsorbed water | Stretching |
| 4 | 1540.23 | Amide II (N–H bend + C–N stretch) | Bending/Stretching |
| 5 | 1314.28 | C–N (amine) / Phenolic O–H | Stretching |
| 6 | 1160.97 | C–O–C (ether linkage) | Asymmetric stretching |
| 7 | 1109.55 | C–O (secondary alcohol) | Stretching |
| 8 | 1054.45 | C–O (primary alcohol) | Stretching |
| 9 | 1030.80 | C–O / possible As–O interaction | Stretching |
| 10 | 661.88 | C–Cl / aromatic C–H (out-of-plane) | Bending |
| 11 | 556.71 | Metal–O / As–O | Stretching |
| 12 | 435.08 | Metal–O / As–O | Bending/Stretching |

C4C5 - As(III) 5 mM

| Peak No. | Wavenumber (cm⁻¹) | Probable Functional Group | Type of Vibration |
| --- | --- | --- | --- |
| 1 | 3335.76 | Hydrogen-bonded –OH / –NH | O–H / N–H stretching |
| 2 | 2900.76 | Aliphatic –CH₂ / –CH₃ | C–H stretching |
| 3 | 1643.28 | C=O (Amide I) / C=C / bound water | Stretching |
| 4 | 1547.02 | Amide II (N–H bend + C–N stretch) | Bending/Stretching |
| 5 | 1427.64 | CH₂ bending / Aromatic ring vibration | Bending |
| 6 | 1369.97 | CH₃ bending / Phenolic O–H | Bending |
| 7 | 1334.32 | C–N (amine) | Stretching |
| 8 | 1314.64 | C–N / Phenolic group | Stretching |
| 9 | 1204.95 | C–O (alcohol/phenol) | Stretching |
| 10 | 1160.63 | C–O–C (ether linkage) | Asymmetric stretching |
| 11 | 1109.70 | C–O (secondary alcohol) | Stretching |
| 12 | 1054.48 | C–O (primary alcohol) | Stretching |
| 13 | 1031.09 | C–O / possible As–O interaction | Stretching |
| 14 | 999.93 | =C–H bending (alkene) | Out-of-plane bending |
| 15 | 896.40 | C–H bending (aromatic) | Out-of-plane bending |
| 16 | 661.51 | C–Cl / aromatic C–H | Bending |
| 17 | 556.18 | As–O / Metal–O | Stretching |
| 18 | 517.71 | As–O / Metal–O | Stretching |
| 19 | 434.95 | Metal–O / As–O | Bending |

C2C5 - As(III) 5 mM

| Peak No. | Wavenumber (cm⁻¹) | Probable Functional Group | Type of Vibration |
| --- | --- | --- | --- |
| 1 | 3335.88 | Hydrogen-bonded –OH / –NH | O–H / N–H stretching |
| 2 | 2902.02 | Aliphatic –CH₂ / –CH₃ | C–H stretching |
| 3 | 2161.21 | C≡C (alkyne) / possible C≡N | Triple bond stretching |
| 4 | 1635.23 | C=O (Amide I) / C=C / adsorbed water | Stretching |
| 5 | 1427.95 | CH₂ bending / aromatic ring vibration | Bending |
| 6 | 1369.99 | CH₃ bending / phenolic O–H | Bending |
| 7 | 1334.64 | C–N (amine) | Stretching |
| 8 | 1315.06 | C–N / phenolic group | Stretching |
| 9 | 1280.07 | C–O (phenol/alcohol) | Stretching |
| 10 | 1204.93 | C–O (alcohol/ether) | Stretching |
| 11 | 1160.42 | C–O–C (ether linkage) | Asymmetric stretching |
| 12 | 1109.96 | C–O (secondary alcohol) | Stretching |
| 13 | 1055.32 | C–O (primary alcohol) | Stretching |
| 14 | 1031.75 | C–O / possible As–O interaction | Stretching |
| 15 | 660.15 | Aromatic C–H (out-of-plane) / C–Cl | Bending |
| 16 | 555.48 | As–O / Metal–O | Stretching |
| 17 | 517.07 | As–O / Metal–O | Stretching |
| 18 | 434.65 | Metal–O / As–O | Bending/Stretching |

Comparison

| Functional Region (cm⁻¹) | Functional group | As(V) C4C5 | As(V) C2C5 | As(V) C2C4 | As(III) C2C4 | As(III) C4C5 | As(III) C2C5 | Interpretation |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| 3900–3570 | Free –OH (alcohol/phenol) | ✓ | ✓ | ✓ | — | — | — | Structural hydroxyl groups prominent in As(V) samples |
| 3335–3286 | H-bonded –OH / –NH | 3269 | 3269 | — | 3286 | 3335 | 3335 | Shift toward lower region in As(III) indicates stronger H-bonding |
| ~2900 | Aliphatic C–H stretching | 2899 | 2899 | — | 2899 | 2900 | 2902 | Organic backbone preserved in all treated samples |
| ~2161 | C≡C / C≡N | 2161 | 2161 | 2161 | — | — | 2161 | Minor contribution; not central to adsorption |
| 1645–1634 | Amide I (C=O) / C=C | 1637 | 1634 | — | 1644 | 1643 | 1635 | Stronger in As(III) → protein involvement |
| 1547–1540 | Amide II (N–H bend) | — | — | — | 1540 | 1547 | — | Present only in As(III) samples |
| ~1427 | CH₂ bending | 1427 | 1427 | — | — | 1427 | 1427 | Slight persistence after adsorption |
| 1369–1313 | C–N stretching | 1334–1314 | 1334–1314 | 1313 | 1314 | 1334–1314 | 1334–1315 | Amino groups involved in metal binding |
| 1280–1204 | Phenolic C–O | 1279–1204 | 1279–1204 | — | — | 1204 | 1280–1204 | Minor shifts indicate coordination |
| 1160–1030 | C–O / C–O–C | 1160–1031 | 1160–1031 | 1160–1030 | 1160–1030 | 1160–1031 | 1160–1031 | Significant region for arsenic interaction |
| 999–896 | Aromatic C–H | 999 | — | — | — | 999, 896 | — | Aromatic contribution in selected samples |
| ~660 | C–Cl / aromatic C–H | 660 | 660 | 662 | 661 | 661 | 660 | Stable aromatic/halide vibrations |
| 560–430 | As–O / Metal–O | 554–434 | 555–434 | 556–434 | 556–435 | 556–434 | 555–434 | Direct evidence of arsenic coordination |