Table 1. Water quality analysis of Yang 101 well block platforms

| Parameter | Yang 101H56 | Yang 101H37 | Yang 101H41 |
| --- | --- | --- | --- |
| Total dissolved solids (mg/L) | 32,133.43 | 24,070.50 | 14,271.13 |
| pH | 7.02 | 7.33 | 6.88 |
| Sodium (mg/L) | 11,751.83 | 8,874.00 | 5,224.25 |
| Calcium (mg/L) | 254.14 | 273.50 | 101.67 |
| Magnesium (mg/L) | 22.28 | 32.50 | 7.30 |
| Barium (mg/L) | 667.29 | 342.33 | 226.49 |
| Strontium (mg/L) | 144.75 | 104.00 | 59.25 |
| Lithium (mg/L) | 53.89 | 31.30 | 26.01 |
| Chloride (mg/L) | 18,463.50 | 13,832.17 | 8,113.92 |
| Sulfate (mg/L) | 1.55 | 11.21 | 1.63 |
| Bicarbonate (mg/L) | 769.14 | 678.00 | 478.88 |
| Iodine (mg/L) | 32.95 | 9.95 | 8.63 |
| Bromine (mg/L) | 110.14 | 82.05 | 49.14 |
| Boron (mg/L) | 76.19 | 27.32 | 33.94 |
| Relative density | 1.02 | 1.02 | 1.01 |

Table 2. Resource potential assessment for Yang 101H56 platform

| Well ID | Li content (mg/L) | Daily water (m³) | Li2CO₃ (kg/d) |
| --- | --- | --- | --- |
| Yang 101H56-1 | 49 | 13.25 | 3.46 |
| Yang 101H56-2 | 44 | 62.92 | 14.93 |
| Yang 101H56-3 | 65 | 113.81 | 34.60 |
| Total (H56) | - | 189.98 | 52.99 |

Table 3. Comparative evaluation of lithium adsorbents

| Parameter | Aluminum-based | Titanium-based | Manganese-based |
| --- | --- | --- | --- |
| Applicable pH range | Neutral | Neutral to weak alkaline | Neutral to weak alkaline |
| Adsorption capacity | ~3 mg/g | 5-6 mg/g | 5-6 mg/g |
| Dissolution loss | ≤0.005% | Low | High (~50%) |
| Initial filling (ton Li) | 1 ton | 3 tons | 3 tons |
| Adsorbent price | 60,000 CNY/ton | 300-500k CNY/ton | 250-300k CNY/ton |
| Annual replenishment | <5% of total | 5-10 tons | 5-15 tons |
| Eluate Li concentration | >500 mg/L | >500 mg/L | >500 mg/L |
| Li recovery rate | ~87% | 70-80% | ~70% |

Table 4. Ion concentrations at different process stages

| Process Stage | Li (g/L) | Mg (g/L) | Ca (g/L) | Na (g/L) |
| --- | --- | --- | --- | --- |
| Raw feed | 0.065 | 0.032 | 0.254 | 11.75 |
| RO concentrate | 3.38 | 0.17 | 0.28 | 5.20 |
| NF permeate | 3.55 | 0.03 | 0.06 | 4.80 |
| HP-RO concentrate | 9.70 | 0.07 | 0.15 | 3.50 |
| Resin product | 9.68 | <0.001 | <0.001 | 2.80 |

Table 5. Comparison with conventional lithium extraction processes

| Parameter | This study | Conventional process | Improvement |
| --- | --- | --- | --- |
| Li recovery rate | 87% | 70-75% | +12-17% |
| Daily production | 30.1 kg | ~10 kg | +200% |
| Energy consumption | Baseline | 2x baseline | -50% |
| Operators required | 6 | 20+ | -70% |
| Product purity | >99.5% | 98-99% | +0.5-1.5% |