- Supporting Information

Built-in electric field-boosted attomolar Pb²⁺ sensing on carboxylated black phosphorene

Fan Yang1, 2, 8, Xixi Yuan3, 8, Jiaqi Zhu1, 2, Yuanyuan Pan4, Zhongjun Li5, Jianqing Li4, Yanqi Ge6, Leiming Wu1, 2, *, Yuanjiang Xiang7, *, Han Zhang6, *, Jun Yang 1, 2, *, Yuwen Qin 1, 2

1Institute of Advanced Photonics Technology, School of Information Engineering, Guangdong University of Technology, Guangzhou, China

2Key Laboratory of Photonic Technology for Integrated Sensing and Communication（Guangdong University of Technology）, Ministry of Education of China, Guangzhou, China

3School of Computer Science and Technology, Guangdong University of Technology, Guangzhou, China

4School of Computer Science and Engineering, Macau University of Science and Technology, Macau, China

5Institute of Systems Engineering, Macau University of Science and Technology, Macau, China

6State Key Laboratory of Radio Frequency Heterogeneous Integration, College of Physics and Optoelectronic Engineering, Shenzhen University,

Shenzhen, China

7College of Electrical and Electronic Engineering, Wenzhou University, Wenzhou, China

8These authors contributed equally: Fan Yang, XixiYuan

*Corresponding Author: leiming_wu@gdut.edu.cn; xiangyuanjiang@126.com; hzhang@szu.edu.cn; yangj@gdut.edu.cn

Fig. S1 Experimental refractive-index calibration of bare-Au SPR and SPR+BP-COOH. (a) Angle-scanned reflectance curves of bare-Au SPR measured in sensing media with refractive indices nₛ = 1.3320, 1.3385, 1.3435, 1.3472 and 1.3530. (b) Angle-scanned reflectance curves of the 13 nm SPR+BP-COOH structure measured in sensing media with refractive indices nₛ = 1.3320, 1.3385, 1.3435, 1.3472 and 1.3530. (c) Resonance angle as a function of refractive index for bare-Au SPR and the 13 nm SPR+BP-COOH structure, together with linear fitting curves.

Fig. S2 Repeatability test of Pb²⁺ sensing performed on the same 13 nm SPR+BP-COOH structure. (a) Angle-scanned reflectance curves of the same 13 nm SPR+BP-COOH structure measured for Pb²⁺ concentrations of 0, 10⁻²⁰, 10⁻¹⁹, 10⁻¹⁸, 10⁻¹⁷, 10⁻¹⁶ and 10⁻¹⁵ M. (b) Resonance-angle shift Δθ as a function of Pb²⁺ concentration for the same 13 nm SPR+BP-COOH structure, together with the nonlinear fitting curve.

Fig. S3 Pb²⁺ sensing results obtained from an SPR+BP-COOH structure with a thickness of approximately 11 nm. (a) Angle-scanned reflectance curves of the 11 nm SPR+BP-COOH structure measured for Pb²⁺ concentrations of 0, 10⁻²⁰, 10⁻¹⁹, 10⁻¹⁸, 10⁻¹⁷, 10⁻¹⁶ and 10⁻¹⁵ M. (b) Resonance-angle shift Δθ as a function of Pb²⁺ concentration for the 11 nm SPR+BP-COOH structure, together with the nonlinear fitting curve. (c) AFM image of the 11 nm BP-COOH functional layer. (d) Height profile extracted from the AFM image in c, showing a thickness of approximately 11 nm.

Fig. S4 Angle-scanned reflectance curves and resonance-angle fitting results for Pb²⁺ detection by bare-Au SPR. (a) Angle-scanned reflectance curves of bare-Au SPR measured for Pb²⁺ concentrations of 0, 10⁻⁶, 10⁻⁵, 10⁻⁴, 10⁻³ and 10⁻² M. (b) Resonance-angle shift Δθ as a function of Pb²⁺ concentration for bare-Au SPR, together with the nonlinear fitting curve.

Fig. S5 Angle-scanned reflectance curves and resonance-angle fitting results for Cd²⁺ detection by SPR+BP-COOH. (a) Angle-scanned reflectance curves of SPR+BP-COOH measured for Cd²⁺ concentrations of 0, 10⁻¹³, 10⁻¹², 10⁻¹¹, 10⁻¹⁰ and 10⁻⁹ M. (b) Resonance-angle shift Δθ as a function of Cd²⁺ concentration, together with the nonlinear fitting curve.

Fig. S6 Angle-scanned reflectance curves and resonance-angle fitting results for Cu²⁺ detection by SPR+BP-COOH. (a) Angle-scanned reflectance curves of SPR+BP-COOH measured for Cu²⁺ concentrations of 0, 10⁻¹³, 10⁻¹², 10⁻¹¹, 10⁻¹⁰ and 10⁻⁹ M. (b) Resonance-angle shift Δθ as a function of Cu²⁺ concentration, together with the nonlinear fitting curve.

Fig. S7 Angle-scanned reflectance curves and resonance-angle fitting results for Zn²⁺ detection by SPR+BP-COOH. (a) Angle-scanned reflectance curves of SPR+BP-COOH measured for Zn²⁺ concentrations of 0, 10⁻¹², 10⁻¹¹, 10⁻¹⁰, 10⁻⁹ and 10⁻⁸ M. (b) Resonance-angle shift Δθ as a function of Zn²⁺ concentration, together with the nonlinear fitting curve.

Fig. S8 Angle-scanned reflectance curves and resonance-angle fitting results for Ni²⁺ detection by SPR+BP-COOH. (a) Angle-scanned reflectance curves of SPR+BP-COOH measured for Ni²⁺ concentrations of 0, 10⁻¹⁰, 10⁻⁹, 10⁻⁸, 10⁻⁷ and 10⁻⁶ M. (b) Resonance-angle shift Δθ as a function of Ni²⁺ concentration, together with the nonlinear fitting curve.

Fig. S9 Angle-scanned reflectance curves and resonance-angle fitting results for Ca²⁺ detection by SPR+BP-COOH. (a) Angle-scanned reflectance curves of SPR+BP-COOH measured for Ca²⁺ concentrations of 0, 10⁻⁹, 10⁻⁸, 10⁻⁷, 10⁻⁶ and 10⁻⁵ M. (b) Resonance-angle shift Δθ as a function of Ca²⁺ concentration, together with the nonlinear fitting curve.

Fig. S10 Angle-scanned reflectance curves and resonance-angle fitting results for Mg²⁺ detection by SPR+BP-COOH. (a) Angle-scanned reflectance curves of SPR+BP-COOH measured for Mg²⁺ concentrations of 0, 10⁻⁸, 10⁻⁷, 10⁻⁶, 10⁻⁵ and 10⁻⁴ M. (b) Resonance-angle shift Δθ as a function of Mg²⁺ concentration, together with the nonlinear fitting curve.

Fig. S11 Repeated measurements of the same pure-water sample on SPR+BP-COOH at 2 min intervals. Angle-scanned reflectance curves recorded at 0, 2, 4, 6, 8, 10, 12, 14, 16, 18, 20, 22, 24 and 26 min after deposition of the BP-COOH functional layer.