Supplementary information

Potential for tracking acrylamide residues in dialyzed melanoidin macromolecules via mid-infrared profiling

Ghassan Faisal Mohsin[a] (dr.ghassan.f.m@uomisan.edu.iq), Andrea Isabel Hornemann[b] (andrea.hornemann@gmx.de), Franz-Josef Schmitt*[c] (franz-josef.schmitt@physik.uni-halle.de)

a Ministry of Education, General Directorate of Vocational Education, Department of Vocational Education in Maysan, Maysan 62001, Iraq

b Projektträger Jülich, Lützowstraße 109, 10785 Berlin

c Martin-Luther-Universität Halle-Wittenberg, Institut für Physik, von-Danckelmann-Platz 3, 06120 Halle, Germany

*Corresponding author: Franz-Josef Schmitt

franz-josef.schmitt@physik.uni-halle.de

Phone:  +49 30 314 23511

Telefax: +49 30 31478600

Ghassan Faisal Mohsin: ORCID ID: https://orcid.org/0000-0002-2648-386X 
Franz-Josef Schmitt: ORCID ID: https://orcid.org/0000-0001-9058-5804

Andrea Hornemann: ORCID ID: https://orcid.org/0000-0002-0945-1508

Supplementary data

Fig.  S-1 Melanoidin polymers' second derivative characteristics in the 1800–1000 cm-1 spectral range

Table S-1 Fundamental functional groups of pure Asn, Acryl, and different melanoidin specimens. (§: melanoidins prepared in a solvent-free phase, ¶: in aqueous phase at pH 5 and 8) (+: present, ˗: absent)

| Vibrational modes | Wavenumber (cm-1) | Asn | Acryl | §Glc-Asn and Fru-Asn | ¶Glc-Asn and Fru-Asn | §Mal-Asn | ¶Mal-Asn | References |
| --- | --- | --- | --- | --- | --- | --- | --- | --- |
| υO-H | 3420-3410 | ˗ | ˗ | + | + | + | + | [31, 38] |
| υN-H2/Amide A+B | 3352-3187 | + | + | + overlap with υOH | + overlap with υOH | + overlap with υOH | + overlap with υOH | [42, 46] |
| υC-H (CH3+CH2) | 2925-2188 | + | + | + | + | + | + | [38, 42] |
| υC=O of the Amadori product | 1734-1714 | ˗ | ˗ | + | + | + overlap | + | [31, 56] |
| amide I (mainly attributed to the amide C=O stretch), υC=C, υC=N and δNH2 | 1667–1615 | + | + | + | + Only a single band at 1640 cm-1 | + Only a single band at 1642 cm-1 | + Only a single band at 1642 cm-1 | [33, 41, 74] |
| Amide II | 1580-1530 | + | ˗ | ˗ | ˗ | ˗ | ˗ | [31, 38, 41] |
| Amide II and δCH3 | 1480-1409 | + | + | + | + | + | + |  |
| Amide III and δC-H | 1350–1215 | + | + | + | + | + | + | [38, 41] |
| I. υC-N of Asn and Acryl II. υC–O/C–C/C–O–H and δC–O–C of reducing sugars in the melanoidin skeleton | 1201–1050 | + | + | + | + | + | + | [38, 51] |
| δC-H | 986-960 | ˗ | + | ˗ | ˗ | ˗ | ˗ | [33, 46] |