S1 MPs in the original road surface sediments from three different functional areas

S2 MPs types in original road surface sediments from different functional areas

S3 Variation characteristics of MPs degradation with humidity in road surface sediments under UV irradiation (a) and high temperature exposure (b)

S4 Degradation kinetic rate constant of MPs and their corresponding mass change determination parameters in road surface sediments

Table 1 Traffic area (site 1)

| Condition | Pseudo-first-order kinetic constant （1/h） R2 |  | Pseudo-second-order kinetic constant 1/（g·h） R2 |  |
| --- | --- | --- | --- | --- |
|  | k1 （1/h） | R2 | k2 1/（g·h） | R2 |
| UV irradiation at 30 W/m2 | 0.1008±0.0064 | 0.9722 | 7.3103±0.4119 | 0.9783 |
| High temperature at 65 ℃ | 0.1148±0.0056 | 0.9838 | 8.7165±0.3971 | 0.9857 |
| The combined action at 65 ℃+30 W/m2 | 0.1407±0.0040 | 0.9944 | 10.9586±0.4414 | 0.9888 |

Table 2 Cultural and educational area (site 2)

| Condition | Pseudo-first-order kinetic constant （1/h） R2 |  | Pseudo-second-order kinetic constant 1/（g·h） R2 |  |
| --- | --- | --- | --- | --- |
|  | k1 （1/h） | R2 | k2 1/（g·h） | R2 |
| UV irradiation at 30 W/m2 | 0.0368±0.0029 | 0.9588 | 0.9249±0.0682 | 0.9634 |
| High temperature at 65 ℃ | 0.1182±0.0088 | 0.9629 | 3.5820±0.2092 | 0.9767 |
| The combined action at 65 ℃+30 W/m2 | 0.1811±0.0248 | 0.8843 | 6.2244±0.6703 | 0.9249 |

Table 3 Commercial area (site 3)

| Condition | Pseudo-first-order kinetic constant （1/h） R2 |  | Pseudo-second-order kinetic constant 1/（g·h） R2 |  |
| --- | --- | --- | --- | --- |
|  | k1 （1/h） | R2 | k2 1/（g·h） | R2 |
| UV irradiation at 30 W/m2 | 0.0523±0.0037 | 0.9670 | 1.3451±0.0879 | 0.9710 |
| High temperature at 65 ℃ | 0.1220±0.0114 | 0.9421 | 3.6310±0.2563 | 0.9663 |
| The combined action at 65 ℃+30 W/m2 | 0.2441±0.0304 | 0.9019 | 9.4673±0.8180 | 0.9503 |

S5 Pearson correlation coefficients of MPs quantity reduction rate with their degradation efficiency under UV irradiation and high temperature exposure (n = 18)

|  | <100 μm | 100-200 μm | 200-300 μm | 300-400 μm | 400-500 μm |
| --- | --- | --- | --- | --- | --- |
| UV irradiation | -0.237 (0.848) | 0.449 (0.704) | 0.932 (0.236) | -0.218 (0.860) | 0.668 (0.535) |
| High temperature exposure | -0.997* (0.046) | -0.807* (0.402) | -0.202 (0.871) | -0.999* (0.033) | -0.623 (0.571) |

Note: * means significantly correlated at the 0.05 level.

S6 the corresponding between fluorescent substances and fluorescent regions (EX/EM)

| Fluorescent substances | EX excitation wavelength/nm | EM emission wavelength/nm |
| --- | --- | --- |
|  | λEX (nm) | λEM (nm) |
| Fulvic acid-like components | 240-290 | 370-440 |
| Humic acid-like components | 350-440 | 430-510 |
| Protein-like components | 250-280 | 300-380 |

S7 Pearson correlation coefficients between reduction rate of protein-like components fluorescence intensity and MPs degradation efficiency (n = 36)

|  | Fulvic acid-like components | Humic acid-like components | Protein-like components |
| --- | --- | --- | --- |
| MPs degradation | -0.018 (0.973) | -0.290 (0.577) | 0.484 (0.331) |