Supplementary Information

Protecting benzylic C–H bonds by deuteration doubles the operational lifetime of 
deep blue Ir-phenylimidazole dopants in phosphorescent OLEDs

Hye Jin Bae1, Jong Soo Kim1, Alexander Yakubovich2, Jinhoon Jeong4,5, Sangho Park1, Jun Chwae1, Satoko Ishibe1, Won-Joon Son3, Yongsik Jung1, Sunghan Kim1, Hyeonho Choi1,*, and Mu-Hyun Baik4,5,*

1Samsung Advanced Institute of Technology (SAIT), Samsung Electronics Co., Ltd., 130 Samsung-ro, Suwon, 16678, Republic of Korea

2Samsung R&D Institute Russia (SRR), Samsung Electronics Co., Ltd., 12 Dvintsev Street, Moscow 127018, Russia

3Data and Information Technology (DIT) Center, Samsung Electronics Co., Ltd., Hwaseong, 18448, Republic of Korea

4Department of Chemistry, Korea Advanced Institute of Science and Technology (KAIST), Daejeon 34141, Republic of Korea

5Center for Catalytic Hydrocarbon Functionalizations, Institute for Basic Science (IBS), Daejeon 34141, Republic of Korea

E-mail: hono.choi@samsung.com; mbaik2805@kaist.ac.kr

Experimental procedure

The bis(1,5-cyclooctadiene)iridium(I) tetrafluoroborate was purchased from Colonial Metals Inc. The starting materials based phenylimidazole ligands 2-bromo-1-(4-(tert-butyl)-2,6-dimethylphenyl)-1H-imidazole, 2-bromo-1-(4-(tert-butyl)-2,6-dimethylphenyl)-1H-imidazole(d), 2-bromo-1-mesityl-1H-imidazole, 2-bromo-1-mesityl-1H-imidazole(d), 2-bromo-1-(2,6-diisopropylphenyl)-1H-imidazole, 2-bromo-1-(2,6-diisopropylphenyl)-1H-imidazole(d), 2-methyl-5-(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)benzonitrile, 2-methyl-5-(4,4,5,5-tetramethyl-1,3,2-dioxaborolan-2-yl)benzonitrile(d) were purchased from HANCHAM. All other Chemicals were purchased from Commercial sources (Sigma-Aldrich Co., Tokyo Chemical Industry Co.) and used without further purification. NMR spectra were recorded on a Bruker ASCEND 500 at 500 MHz for 1H and 13C using deuterated solvent CD2Cl2. Elemental analyses were performed on a PE 2400 Series Ⅱ (PerkinElmer) by the Environmental Analysis Laboratory at Samsung Advanced Institute of Technology. The MLADI-TOF mass spectra were obtained using a Bruker Ultraflex III TOF/TOF 200 spectrometer. The Ultraviolet–Visible (UV-Vis) absorption spectra and phosphorescence PL spectra were recorded on a Varian model UV-Vis-NIR spectrophotometer 5000 and a HITACHI F7000 spectrometer. Thermogravimetric analysis (TGA) was done by a TA Discovery instrument under nitrogen at a heating rate of 10oC min1. Emission lifetimes were measured on Fluo time 300. The cyclic voltammetry (CV) were performed in nitrogen-purged DMF with a three-electrode cell configuration composed a carbon working electrode, a platinum wire counter electrode, and a saturated Ag/AgCl as a reference electrode. Ferrocene was used as the standard reference. Purity & Mass of the dopants was examined by performing Liquid Chromatograph Mass Spectrometer-Ion Trap-Time of Flight (LCMS-IT-TOF) analyses. The LCMS-IT-TOF consisted of LC-30A Nexera SR system instrument (Shimadzu) connected to a hybrid mass spectrometer IT-TOF equipped with an electrospray ionization source. FT-IR spectra were measured on a Varian 670infrared spectrophotometer.

Synthesis

General procedure : synsthesis of tris(1-(4-(tert-butyl)-2,6-dimethylphenyl)-2-(3-cyanophenyl)-1H-imidazole)iridium(Ⅲ) (Ir1) as a representative.

3-(1-(4-(tert-butyl)-2, 6-dimethylphenyl)-1H-imidazol-2-yl)benzonitrile (Ir1L) (6.0 g, 18.21 mmol)  and Ir(COD)2BF4 (2.27 g, 4.55 mmol) were added into NMP (1-methyl-2-pyrrolidinone) (60 mL) at room temperature under N2. The reaction solution was stirred at 180 oC for 4 hours. After cooling to room temperature, water was added to quench the reaction and the aqueous layer was extracted with CH2Cl2 (3  30 mL). The organic layer was dried over MgSO4. The crude product was purified by column chromatography (eluent: dichloromethane: n-hexane = 9:1) to afford a yellow solid (1.7 g, 32%). 1H NMR (500 MHz, CD2Cl2): δ (ppm) 7.33 (s, 3H), 7.32 (s, 3H), 6.93 (d, J = 1.4 Hz, 3H), 6.80, 6.81 (ABq, JAB =7.3 Hz, 6H), 6.76 (d, J = 1.4 Hz, 3H), 6.25 (s, 3H), 2.10 (s, 9H), 1.85 (s, 9H), 1.40 (s, 27H); 13C NMR (126 MHz, CD2Cl2): 169.2, 154.9, 154.2, 138.1, 137.8, 135.9, 135.3, 133.2, 131.3, 126.8, 126.7, 126.5, 124.3, 121.8, 121.4, 102.6, 31.6, 18.2, 17.9; MALDI-TOF/MS: 1177.42 [(M + H)+]. Anal. Calcd. for C66H66IrN9 : C, 67.32; H, 5.65; N, 10.71. Found : C, 66.8; H, 5.7; N, 10.8

Synthesis of tris(1-mesityl-2-(3-cyanophenyl)-1H-imidazole)iridium(Ⅲ) (Ir2). The compound was prepared in the same procedure as of Ir1 (1.5 g, 25%). 1H NMR (500 MHz, CD2Cl2): δ (ppm) 7.13 (br. s, 3H), 7.12 (br. s, 3H), 6.87 (d, J = 1.5 Hz, 3H), 6.80, 6.82 (ABq, JAB =7.6 Hz, 6H), 6.73 (d, J = 1.4 Hz, 3H), 6.40 (br. s, 3H), 2.43 (s, 9H), 2.05 (s, 9H), 1.81 (s, 9H); 13C NMR (126 MHz, CD2Cl2): 169.4, 154.7, 140.6, 138.2, 137.8, 136.2, 135.6, 133.2, 131.4, 130.4, 130.3, 126.5, 124.1, 122.1, 121.5, 102.5, 21.5, 17.9, 17.7; MALDI-TOF/MS: 1051.32 [(M + H)+]. Anal. Calcd. for C45H29N5 : C, 65.12; H, 4.60; N, 11.99. Found : C, 65.1; H, 4.6; N, 12.2

Synthesis of tris(1-mesityl-2-(3-cyano-4-methylphenyl)-1H-imidazole)iridium(Ⅲ) (Ir3). The compound was prepared in the same procedure as of Ir1 (0.6 g, 18%). 1H NMR (500 MHz, CD2Cl2): δ (ppm) 7.14 (s, 3H), 7.11 (s, 3H), 1 6.71 (d, J = 1.4 Hz, 3H), 6.66 (s, 3H), 6.36 (s, 3H), 2.43 (s, 9H), 2.17 (s, 9H), 2.08 (s, 9H), 1.80 (s, 9H); 13C NMR (126 MHz, CD2Cl2): 169.5, 154.9, 140.9, 140.7, 139.2, 136.1, 135.6, 135.5, 133.4, 130.3, 130.2, 126.5, 124.3, 121.5, 120.8, 103.1, 21.5, 20.5, 18.0, 17.6; MALDI-TOF/MS: 1093.41 [(M + H)+]. Anal. Calcd. for C45H29N5 : C, 65.91; H, 4.98; N, 11.53. Found : C, 65.4; H, 4.9; N, 11.5

Synthesis of tris(1-(2,6-diisopropylphenyl)-2-(3-cyanophenyl)-1H-imidazole)iridium(Ⅲ) (Ir4). The compound was prepared in the same procedure as of Ir1 (1.1 g, 25%). 1H NMR (500 MHz, CD2Cl2): δ (ppm) 7.63 (t, J = 7.6 Hz, 3H), 7.43 (dd, J = 7.8, 1.2 Hz, 3H), 7.41 (dd, J = 7.8, 1.2 Hz, 3H), 6.98 (d, J = 1.4 Hz, 3H), 6.81 (dd, J = 7.9, 1.8 Hz, 3H), 6.80 (d, J = 1.5 Hz, 3H), 6.75 (d, J = 7.9 Hz, 3H), 6.27 (d, J = 1.8 Hz, 3H), 2.60 (septet, J = 6.8 Hz, 3H), 2.16 (septet, J = 6.8 Hz, 3H), 1.23 (d, J = 6.9 Hz, 9H), 1.01 (d, J = 6.8 Hz, 9H), 0.95 (d, J = 6.8 Hz, 9H), 0.95 (d, J = 6.9 Hz, 9H); 13C NMR (126 MHz, CD2Cl2): 169.2, 156.1, 146.8, 146.2, 138.3, 137.5, 133.1, 131.6, 131.2, 126.2, 125.6, 125.3, 125.2, 123.5, 121.2, 102.2, 29.2, 28.8, 24.8, 24.6, 23.5, 23.4; MALDI-TOF/MS: 1177.42 [(M + H)+]. Anal. Calcd. for C66H66IrN9 : C, 67.32; H, 5.65; N, 10.71. Found : C, 67.0; H, 5.6; N, 10.8

Synthesis of tris(1-(4-(tert-butyl)-2,6-dimethylphenyl)-2-(3-cyanophenyl)-1H-imidazole)iridium(Ⅲ)-d24 (Ir1D). The compound was prepared in the same procedure as of Ir1 (1.3 g, 29%). 1H NMR (500 MHz, CD2Cl2): δ (ppm) 7.35 (d, J = 2.3 Hz, 3H), 7.33 (d, J = 2.2 Hz, 3H), 6.95 (s, 0.6H), 6.82, 6.82 (ABq, JAB =7.1 Hz, 6H), 6.78 (d, J = 1.4 Hz, 1H), 6.27 (s, 2.5H), 2.08-2.10 (m, 0.8H), 1.83-1.86 (m, 0.8H), 1.42 (s, 27H); 13C NMR (126 MHz, CD2Cl2): 169.2, 154.8, 154.8, 154.1, 138.1, 137.8, 137.7, 135.8, 135.7, 135.2, 135.2, 133.3, 131.2, 126.8, 126.7, 126.5, 126.4, 124.3, 121.9, 121.7, 121.4, 102.6, 102.5, 35.2, 31.6, 17.1-17.9 (m).; MALDI-TOF/MS: 1199.53 [(M + H)+].

Synthesis of tris(1-mesityl-2-(3-cyanophenyl)-1H-imidazole)iridium(Ⅲ)-d33 (Ir2D). The compound was prepared in the same procedure as of Ir1 (1.7 g, 27%). 1H NMR (500 MHz, CD2Cl2): δ (ppm) 7.13 (d, J = 1.9 Hz, 3H), 7.11 (d, J = 1.9 Hz, 3H), 6.88 (s, 0.7H), 6.81, 6.83 (ABq, JAB =7.5 Hz, 6H), 6.73 (s, 0.8H), 6.40 (s, 2.6H), 2.40-2.43 (m, 1.2H), 2.03-2.06 (m, 1.1H), 1.78-1.81 (m, 1.1H); 13C NMR (126 MHz, CD2Cl2): 169.3, 154.7, 154.7, 140.8, 140.7, 138.2, 137.8, 136.0, 135.5, 135.5, 133.3, 131.4, 130.4, 130.3, 126.3, 124.1, 122.0, 121.5, 102.5, 20.6-21.2 (m), 16.8-17.6 (m); MALDI-TOF/MS: 1079.51 [(M + H)+]. Anal. Calcd. for C45H29N5 : C, 84.48; H, 4.57; N, 10.95. Found : C, 84.4; H, 4.6; N, 11.0

Synthesis of tris(1-mesityl-2-(3-cyano-4-methylphenyl)-1H-imidazole)iridium(Ⅲ)-d42 (Ir3D). The compound was prepared in the same procedure as of Ir1 (0.7 g, 26%). 1H NMR (500 MHz, CD2Cl2): δ (ppm) 7.14 (d, J = 2 Hz, 3H), 7.11 (d, J = 2Hz, 3H), 6.83 (s, 0.6H), 6.71 (s, 0.8H), 6.6 (s, 3H), 6.36 (s, 2.2H), 2.38-2.42 (m, 0.7H), 2.13-2.15 (m, 0.9H), 2.03-2.05 (m, 0.7H), 1.78-1.80 (m, 0.7H); 13C NMR (126 MHz, CD2Cl2): 169.5, 154.9(, 154.9), 140.7, 140.6, 139.2, 136.0, 135.5, 135.4, 133.4, 130.2, 126.3, 124.2, 121.4, 120.9, 103.1(, 103.1), 20.6-21.0 (m), 19.5-20.1 (m), 16.6-17.4 (m); MALDI-TOF/MS: 1128.64 [(M + H)+].

Synthesis of tris(1-(2,6-diisopropylphenyl)-2-(3-cyanophenyl)-1H-imidazole)iridium(Ⅲ)-d51 (Ir4D). The compound was prepared in the same procedure as of Ir1 (0.8 g, 22%). 1H NMR (500 MHz, CD2Cl2): δ (ppm) 7.63 (t, J = 7.8 Hz, 0.8H), 7.4-7.42(br. d, 6H), 6.98 (s, 0.4H), 6.81 (dd, J = 7.9, 1.6 Hz, 3H), 6.80 (s, 1.3H), 6.76 (d, J = 7.9 Hz, 3H), 6.27 (d, J = 1.1 Hz, 2.9H), 2.57-2.63 (m, 0.5H), 2.13-2.19 (m, 0.5H), 1.19-1.24 (m, 4.7H), 0.97-1.02 (m, 4.7H), 0.90-0.95 (m, 9.2H); 13C NMR (126 MHz, CD2Cl2): 169.2, 156.1, 156.1, 146.8, 146.2, 138.3, 137.6, 133.1, 131.6, 131.2, 126.1, 125.6, 125.5, 125.3, 125.2, 125.2, 123.5, 123.3, 121.2, 102.2, 28.5-28.8 (m), 24.7, 24.0-24.6 (m), 22.7-23.4 (m); MALDI-TOF/MS: 1207.59 [(M + H)+].

Figure S1. 1H (top) and 13C (bottom) spectrum of Ir1.

Figure S2. 1H (top) and 13C (bottom) spectrum of Ir1D.

Figure S3. 1H (top) and 13C (bottom) spectrum of Ir2.

Figure S4. 1H (top) and 13C (bottom) spectrum of Ir2D.

Figure S5. 1H (top) and 13C (bottom) spectrum of Ir3.

Figure S6. 1H (top) and 13C (bottom) spectrum of Ir3D.

Figure S7. 1H (top) and 13C (bottom) spectrum of Ir4.

Figure S8. 1H (top) and 13C (bottom) spectrum of Ir4D.

Figure S9. MALDI-TOF spectra (a) Ir1–1D, (b) Ir2–2D and (c) Ir3–3D, (d) Ir4–4D.

Figure S10. CV spectra of (a) Ir1–1D, (b) Ir2–2D and (c) Ir3–3D, (d) Ir4–4D.

Figure S11. TGA curves of Ir1–4 and Ir1D–4D.

Figure S12. Device performances. (a) J-V-L characteristics, (b) normalized voltage rise during operational life time for each Ir complexes doped OLED devices.

Figure S13. Summarized (a) EQE and (b) life time variation in accordance with substitution of deuteration for Ir complexes doped OLED devices.

Computational Details

The free energy in solution phase G(sol) has been calculated as follows:

G(sol) = G(gas) + G(solv)

G(gas) = H(gas) + TS(gas)

H(gas) = E(SCF) + ZPE

∆E(SCF) = ∑E(SCF) for products – ∑E(SCF) for reactants

∆G(sol)  = ∑G(sol) for products – ∑G(sol) for reactants

G(gas) is the free energy in has phase; G(solv) is the free energy of solvation as computed using the continuum solvation model; H(gas) is the enthalpy in gas phase; T is the temperature; S(gas) is the entropy in gas phase; E(SCF) is the self-consistent field energy; ZPE is the zero-point energy.

Table S1. Computed energy components for DFT-optimized structures

|  | E(SCF)/(eV) cc-pVTZ(-f) /LACV3P | ZPE/(kcal/mol) LACVP** | S(gas)/(cal/(mol*K)) LACVP** | G(solv)/(kcal/mol) LACVP** |
| --- | --- | --- | --- | --- |
| 1 | –20343.446 | 162.80 | 74.03 | –25.22 |
| 2 | –85707.905 | 737.42 | 330.84 | –15.12 |
| 2(D) | –85707.905 | 735.38 | 331.53 | –15.12 |
| TS | –106050.795 | 898.71 | 390.10 | –32.40 |
| TS(D) | –106050.795 | 897.41 | 390.40 | –32.40 |
| 3 | –106050.885 | 900.66 | 395.22 | –32.93 |
| Energies for BDE calculations in eV |  |  |  |  |
| H (doublet) | –13.634 |  |  |  |
| Ir1_1 (doublet) | –85691.631 |  |  |  |
| Ir1_2 (doublet) | –85691.577 |  |  |  |
| Ir1_3 (doublet) | –85692.947 |  |  |  |
| Ir1_4 (doublet) | –85692.037 |  |  |  |
| Ir1_5 (doublet) | –85692.059 |  |  |  |
| Ir1_6 (doublet) | –85692.087 |  |  |  |
| Ir1_7 (doublet) | –85692.012 |  |  |  |
| Ir1_8 (doublet) | –85692.410 |  |  |  |
| Ir2_T1 (triplet) | –76088.433 |  |  |  |
| Ir2_1 (doublet) | –76072.213 |  |  |  |
| Ir2_2 (doublet) | –76072.109 |  |  |  |
| Ir2_3 (doublet) | –76073.472 |  |  |  |
| Ir2_4 (doublet) | –76072.487 |  |  |  |
| Ir2_5 (doublet) | –76072.524 |  |  |  |
| Ir2_6 (doublet) | –76072.610 |  |  |  |
| Ir2_7 (doublet) | –76072.541 |  |  |  |
| Ir2_9 (doublet) | –76073.486 |  |  |  |
| Ir3_T1 (triplet) | –79295.384 |  |  |  |
| Ir3_1 (doublet) | –79279.175 |  |  |  |
| Ir3_2 (doublet) | –79279.103 |  |  |  |
| Ir3_3 (doublet) | –79280.448 |  |  |  |
| Ir3_4 (doublet) | –79279.491 |  |  |  |
| Ir3_5 (doublet) | –79279.528 |  |  |  |
| Ir3_6 (doublet) | –79279.590 |  |  |  |
| Ir3_9 (doublet) | –79280.461 |  |  |  |
| Ir3_10 (doublet) | –79280.499 |  |  |  |
| Ir4_T1 (triplet) | –85707.718 |  |  |  |
| Ir4_1 (doublet) | –85691.466 |  |  |  |
| Ir4_2 (doublet) | –85691.393 |  |  |  |
| Ir4_3 (doublet) | –85692.857 |  |  |  |
| Ir4_4 (doublet) | –85691.808 |  |  |  |
| Ir4_5 (doublet) | –85691.785 |  |  |  |
| Ir4_6 (doublet) | –85691.862 |  |  |  |
| Ir4_7 (doublet) | –85691.813 |  |  |  |
| Ir4_11 (doublet) | –85692.232 |  |  |  |
| Ir4_12 (doublet) | –85691.801 |  |  |  |

In 2(D) and TS(D), a benzyl hydrogen participating in the H-abstraction reaction is deuterated.

In the denotation of “IrX_N” in BDE calculations, “X” means the number of iridium dopants and “N” indicates the position of the homolytically dissociated hydrogen. The “IrX_T1” means that T1 state of the IrX. (Ir1_T1 is same with 2)

Figure S14. HOMO/LUMO of Ir1–4 in the ground state S0. (Isodensity value = 0.03 a.u.)

Table S2. Results on calculated HOMO/LUMO energy levels in the ground S0 state and spin density on Ir atom in T1 state are summarized

|  | Ir1 | Ir2 | Ir3 | Ir4 |
| --- | --- | --- | --- | --- |
| HOMO (eV) | –5.637 | –5.608 | –5.500 | –5.749 |
| LUMO (eV) | –1.376 | –1.318 | –1.200 | –1.456 |
| Spin density on Ir | 0.237 | 0.247 | 0.223 | 0.252 |

Figure S15. Before and after isothermal LC-MASS spectra and proposed mass assignments for the unknow impurities of (a) Ir1–1D, (b) Ir2–2D and (c) Ir3–3D, (d) Ir4–4D.

Figure S16 shows FT-IR spectra of hydrogenated Ir1–4 and deuterated Ir1D–4D. The C–H stretching frequencies of Ir1–4 observed at 2900~3100 cm–1. The C–D stretching frequencies of Ir1D–4D is expected to be observed ~2200 cm–1, but it is difficult to observe because it overlaps with the strong peak of C≡N stretching frequencies. It can be seen that the decrease of the C–H stretching frequencies of 2900~3100 cm–1 in the FT-IR spectra of Ir1D–4D is by deuterium. However, in the case of Ir1D, the decrease is small due to tert-butyl.

Figure S16. FT-IR spectra of (a) Ir1–1D, (b) Ir2–2D and (c) Ir3–3D, (d) Ir4–4D.

Table S3. Cartesian Coordinates of the Optimized Geometries.

===============================

1

===============================

N    0.356528401  -0.389536440  -1.581056595

C   -0.668675959  -0.949274600  -0.833167493

C    1.071210623   0.498947352  -0.792095900

C   -0.621479988  -0.412419051   0.475054681

C   -1.588756561  -1.928524494  -1.213107347

C    0.498195767   0.519132197   0.501561344

C   -1.538528919  -0.836333156   1.415877461

C    1.031366587   1.350123405   1.466490507

C    2.140494347   1.320366740  -1.155686975

C    2.129797697   2.156340361   1.122376919

H    0.613747299   1.391080976   2.467304945

C    2.668715000   2.144319296  -0.166363344

H    2.560772657   2.811313152   1.872912765

H    3.504695654   2.793314695  -0.403861821

H    2.534049511   1.325999260  -2.166089773

C   -2.510235071  -2.335701466  -0.252892882

H   -1.576356292  -2.364601135  -2.205845833

C   -2.491088629  -1.797173977   1.035790086

H   -3.247006416  -3.089770079  -0.507885456

H   -3.219970226  -2.136705875   1.764822721

H   -1.526674628  -0.447126925   2.428846598

C    0.629726768  -0.679009080  -2.933946133

C    1.930548668  -1.026706457  -3.313785315

C   -0.406485140  -0.610811532  -3.871703386

C    2.188075542  -1.310631633  -4.647626877

C   -0.129231930  -0.891337514  -5.202200413

C    1.163277268  -1.242144585  -5.591007233

H    2.710818768  -1.108828425  -2.563815594

H   -1.399450779  -0.302467853  -3.560292482

H    3.188973188  -1.600581765  -4.950587273

H   -0.920823932  -0.821835458  -5.941245079

H    1.372754931  -1.462651730  -6.633022308

===============================

2

===============================

N    0.382426322   1.730975151   0.083303362

C    1.245456696   1.366599798  -0.903022826

C   -0.834913611   1.141653657  -0.186380833

C   -0.673157215   0.429720998  -1.342504978

N    0.614191532   0.576922894  -1.767126679

H   -1.387192965  -0.161848232  -1.895321012

H   -1.683547497   1.292811155   0.462707311

C    2.630158663   1.722813129  -1.159859776

C    3.110867739   1.247260213  -2.416969299

C    3.440290213   2.450688839  -0.291518092

C    4.446203232   1.537948728  -2.738697767

C    4.760928631   2.725360870  -0.656235099

C    5.262277126   2.262719393  -1.882075548

H    3.071633577   2.811905861   0.661387086

H    4.837284565   1.207725763  -3.697125196

H    6.289891243   2.485965014  -2.155670643

C    5.572411537   3.487922430   0.234531403

N    6.203833103   4.115416050   0.982130408

C    0.649061441   2.664237022   1.129218817

C    0.537304163   4.031002045   0.843138993

C    1.103466511   2.192346573   2.360157490

C    0.934418201   4.927399635   1.829145193

C    1.490143299   3.134057045   3.316535711

C    1.438693047   4.506260395   3.065757990

H    0.875670791   5.989755630   1.606338978

H    1.870161057   2.767768145   4.264626980

N    4.082390785  -3.224612236  -3.397081614

C    3.555623293  -2.027040243  -3.878609419

C    3.481399298  -3.483652592  -2.185261488

N    2.619292974  -1.580114841  -2.957756996

C    2.591960430  -2.453613520  -1.939552188

H    3.723814011  -4.366947174  -1.614498496

H    1.950098276  -2.307460785  -1.082579255

C    3.824515820  -1.262246728  -4.993485928

C    3.013142347  -0.007733144  -5.077074051

C    4.761624813  -1.570016980  -6.038736343

C    3.172823668   0.785413802  -6.205718994

C    4.851968765  -0.734139502  -7.121045589

H    5.394727230  -2.446995258  -5.985911369

C    4.055539131   0.458037853  -7.240204811

H    2.598702908   1.705300689  -6.281453133

H    4.171967983   1.090515733  -8.113182068

N    6.526322842  -1.348067999  -8.998061180

C    5.776085854  -1.067607164  -8.155143738

C    6.352540493  -3.944290400  -3.857202530

C    4.984726906  -4.051060200  -4.118529320

C    4.489868164  -4.833796024  -5.170836926

C    7.235927105  -4.613271236  -4.706882477

C    5.408745766  -5.480107307  -5.990216255

C    6.791309357  -5.359654427  -5.800007343

H    8.299304962  -4.500027657  -4.522196293

H    5.029433727  -6.060792446  -6.827375412

Ir    1.779985070   0.247550741  -3.537452221

C   -0.396883965   0.284430563  -5.469264984

N   -1.204455018  -0.342764437  -6.366117954

C   -1.069874883  -1.702538133  -6.169927597

N    0.223626196  -0.626621783  -4.724359035

C   -0.177966326  -1.860538125  -5.145759106

H   -1.613003016  -2.409362555  -6.778090477

H    0.202465221  -2.764155626  -4.693566799

C    0.938287973   1.912115932  -4.307790279

C   -0.113377087   1.691204548  -5.244799614

C   -0.793154478   2.743412971  -5.852689266

C    1.257051468   3.248566389  -4.019842625

C   -0.437000543   4.057558060  -5.541724205

H   -1.590775490   2.569935560  -6.565590858

C    0.590134382   4.307443619  -4.620412827

H    2.066631556   3.461164474  -3.327205181

H    0.862210631   5.334377289  -4.391679764

C   -1.129299641   5.125840187  -6.184889793

N   -1.706260085   5.977371693  -6.726367474

C   -1.893941164   0.284268439  -7.448314190

C   -1.160892963   0.605140924  -8.593731880

C   -3.238208771   0.642755687  -7.297362804

C   -1.801699042   1.342530727  -9.591697693

C   -3.830470324   1.374145746  -8.322524071

C   -3.126637220   1.761548042  -9.470959663

H   -1.224006295   1.612232447 -10.469798088

H   -4.867172718   1.677732587  -8.200149536

C   -5.055202007   1.934579492 -11.063625336

C   -3.811284065   2.650441647 -10.512215614

C   -4.231837749   3.966126680  -9.832551003

C   -2.887532473   2.987922192 -11.686231613

H   -5.563915253   2.572610617 -11.795164108

H   -4.781305790   0.997821569 -11.560792923

H   -5.774791241   1.698114753 -10.273671150

H   -4.701699257   4.634485722 -10.563179016

H   -4.953655243   3.795301914  -9.027629852

H   -3.369339228   4.483981133  -9.399869919

H   -1.996806860   3.533898592 -11.357748032

H   -2.566127539   2.089221478 -12.224305153

H   -3.420166492   3.626159191 -12.398819923

C    1.955088973   5.549930573   4.057752132

C    0.814428329   6.508205414   4.436066151

C    2.496491909   4.912178040   5.339717388

C    3.096674919   6.338856697   3.390422583

H   -0.006078423   5.968665123   4.921309948

H    1.178763866   7.272376060   5.131824493

H    0.406142116   7.024001122   3.561451197

H    2.853259087   5.695906162   6.015851021

H    1.724167228   4.344354153   5.870554924

H    3.340887070   4.245373726   5.135000706

H    3.506176472   7.075222969   4.091376305

H    3.909473419   5.674318790   3.078458071

H    2.752500772   6.881019592   2.504148483

C    7.746129036  -5.994100571  -6.812350273

C    7.451496601  -5.405279160  -8.204054832

C    7.530487537  -7.515699387  -6.837197781

C    9.214489937  -5.717124462  -6.476281643

H    7.570001125  -4.316586018  -8.210407257

H    8.139636040  -5.828086376  -8.944959641

H    6.432200909  -5.628739357  -8.534049988

H    6.502710819  -7.777105331  -7.107913017

H    8.196662903  -7.979607105  -7.573388100

H    7.743556023  -7.957937717  -5.858027935

H    9.495387077  -6.129708290  -5.500935078

H    9.857382774  -6.183539391  -7.229843616

H    9.433191299  -4.643908024  -6.475710392

C   -3.983657360   0.300903589  -6.038566113

H   -5.014808655   0.659550667  -6.084817886

H   -4.003363609  -0.779886544  -5.861407757

H   -3.504108429   0.758664846  -5.165248871

C    0.284359515   0.215950802  -8.716929436

H    0.903648496   0.746019304  -7.984531403

H    0.432251513  -0.853048563  -8.530422211

H    0.668198466   0.446869582  -9.713387489

C    3.014647961  -4.889290810  -5.446552277

H    2.783886671  -5.650699139  -6.195648670

H    2.445003510  -5.112919807  -4.538188457

H    2.656216383  -3.922275543  -5.821998119

C    6.847455502  -3.059338570  -2.748518229

H    6.460085392  -3.373774290  -1.773269057

H    7.939035892  -3.065185308  -2.699477673

H    6.516523361  -2.025022507  -2.899959803

C    1.243405342   0.717528343   2.609097004

H    1.577733517   0.523025692   3.630904913

H    0.297802359   0.188397765   2.449851274

H    1.975893021   0.276095122   1.922667265

C    0.067870073   4.496396065  -0.505461872

H    0.777518630   4.210677147  -1.290449142

H   -0.892922401   4.045992851  -0.776954889

H   -0.043879937   5.583070755  -0.527979732

===============================

TS

===============================

N   -0.085820697   1.772907257   0.318870783

C    0.753162563   1.305253148  -0.642168164

C   -1.308073044   1.166121244   0.140848085

C   -1.176903725   0.336562097  -0.940203786

N    0.102780998   0.427083760  -1.403340816

H   -1.907048941  -0.302765906  -1.413000584

H   -2.139597893   1.382491469   0.793951273

C    2.116906643   1.664627433  -0.990006089

C    2.574334145   1.053690791  -2.194538593

C    2.937001705   2.520784378  -0.256398261

C    3.880757570   1.344945788  -2.616600752

C    4.230607033   2.783443451  -0.710516989

C    4.702133179   2.194941759  -1.892329216

H    2.600037575   2.988934994   0.659654140

H    4.248076439   0.913838565  -3.542448759

H    5.707958698   2.418606758  -2.235837936

C    5.059516907   3.661847830   0.048263408

N    5.719358921   4.376928806   0.682570577

C    0.288599074   2.685810089   1.351995587

C    0.158453748   4.060492039   1.117234230

C    0.924655497   2.177124023   2.484559774

C    0.729507327   4.925409317   2.045055389

C    1.478719473   3.088432074   3.385352373

C    1.426099420   4.466933727   3.172142267

H    0.659281433   5.993665218   1.856833339

H    1.995935082   2.693424702   4.253710270

N    3.776639938  -3.446246386  -2.535044432

C    3.165579081  -2.328782320  -3.116860390

C    3.247608423  -3.556963682  -1.243929267

N    2.216212988  -1.831215143  -2.238616467

C    2.315599680  -2.550601006  -1.101463079

H    3.579528570  -4.320497990  -0.556924880

H    1.712851644  -2.320776463  -0.233109459

C    3.441648960  -1.669388056  -4.306052208

C    2.527111053  -0.569010913  -4.592571735

C    4.459909439  -2.010793924  -5.237390995

C    2.639910460   0.062622547  -5.828826904

C    4.501317978  -1.353535891  -6.454402447

H    5.214168072  -2.753590345  -5.011543751

C    3.592416525  -0.320584983  -6.775114536

H    1.985374212   0.897490978  -6.057745934

H    3.665854216   0.180325747  -7.734724045

N    6.297546387  -2.142685652  -8.142317772

C    5.493541718  -1.763362527  -7.394541740

C    5.705948830  -4.857663155  -3.036815405

C    4.414733887  -4.412730694  -3.323028088

C    3.749644995  -4.861464024  -4.520070553

C    6.362226963  -5.643644333  -3.994168520

C    4.488254070  -5.604775429  -5.467590332

C    5.796087742  -5.999529362  -5.238453865

H    7.380998611  -5.945112705  -3.772868156

H    3.982927322  -5.883367538  -6.389096737

Ir    1.265312433  -0.168386325  -3.097399235

C   -0.818766654  -0.623342872  -5.077145100

N   -1.534724712  -1.452296734  -5.881649017

C   -1.402023673  -2.732168674  -5.386329651

N   -0.240918189  -1.336556792  -4.110843182

C   -0.594606400  -2.644503355  -4.287362099

H   -1.893910527  -3.567516804  -5.860265255

H   -0.278894633  -3.417930126  -3.606947899

C    0.338101685   1.277178884  -4.156111240

C   -0.602509379   0.811773479  -5.118593216

C   -1.262927771   1.688918114  -5.975112915

C    0.538376629   2.661213875  -4.064303875

C   -1.006449699   3.057225704  -5.878164291

H   -1.965101480   1.336295485  -6.721161366

C   -0.116484068   3.545230150  -4.911563396

H    1.255357742   3.048387051  -3.345907211

H    0.066831298   4.614002705  -4.847027779

C   -1.666139007   3.940457582  -6.784318447

N   -2.212338209   4.631843567  -7.541121006

C   -2.151829004  -1.096525550  -7.121987343

C   -1.346562028  -1.065185189  -8.262894630

C   -3.495272160  -0.705838203  -7.143845558

C   -1.913315296  -0.590056241  -9.446344376

C   -4.010869980  -0.239241153  -8.349664688

C   -3.234019041  -0.146386355  -9.512840271

H   -1.281155944  -0.546100914 -10.326558113

H   -5.046425343   0.090966426  -8.368864059

C    6.398603916  -4.441157341  -1.773661494

H    6.207586288  -3.384944201  -1.557413578

H    6.040853024  -5.018279076  -0.911799192

H    7.478029251  -4.591213226  -1.847273707

C    2.350678921  -4.721440315  -4.679496765

H    1.812962174  -3.978664160  -4.095231533

H    1.925160050  -4.949090481  -5.657188892

C    0.096687451  -1.475895286  -8.202374458

H    0.685377717  -0.778860331  -7.595568657

H    0.216922432  -2.462956667  -7.743875027

H    0.537540078  -1.506218195  -9.201542854

C   -4.316424370  -0.714879453  -5.886157990

H   -5.363084316  -0.486794949  -6.100377560

H   -4.272531033  -1.684860229  -5.379436970

H   -3.947005510   0.035683502  -5.176303387

C    1.095809340   0.696156263   2.671842337

H    1.863010883   0.307079643   1.989567876

H    1.411394715   0.466925085   3.692309141

H    0.169456691   0.149878681   2.466832399

C   -0.498428464   4.567328453  -0.135753065

H    0.052209575   4.243310452  -1.027489424

H   -1.520841599   4.188775063  -0.240521371

H   -0.538148999   5.659037113  -0.142576441

C    6.551463127  -6.781229973  -6.311855316

C   -3.834562540   0.468741775 -10.778995514

C    2.130887032   5.474358082   4.082888603

C    1.098524213   6.461235046   4.651988506

H    0.344478458   5.940167904   5.251486301

H    1.596185684   7.195744991   5.294441700

H    0.578911424   7.012446404   3.862030506

C    2.850081205   4.794958591   5.251760960

H    3.340563774   5.553979397   5.869075298

H    2.154773712   4.245412827   5.896100998

H    3.626520634   4.104787350   4.904322624

C    3.175875902   6.237658024   3.248284817

H    3.706897736   6.957492352   3.880670547

H    3.915832996   5.558029652   2.812053680

H    2.713259459   6.797400475   2.429300070

C    5.818926334  -8.111974716  -6.558798790

H    4.794832706  -7.951550961  -6.914330482

H    6.342654228  -8.698714256  -7.320924759

H    5.774322033  -8.712327003  -5.642209530

C    7.991274834  -7.089631081  -5.895376682

H    8.032490730  -7.712994576  -4.994995594

H    8.495623589  -7.638965607  -6.696093082

H    8.565061569  -6.174513340  -5.714142799

C    6.579239845  -5.954681873  -7.609282970

H    7.068857193  -4.986857891  -7.460864067

H    7.126240730  -6.498272419  -8.386981964

H    5.573070526  -5.755124092  -7.991344452

C   -5.063986301  -0.345631272 -11.213606834

H   -5.512580395   0.100717649 -12.107888222

H   -4.787012577  -1.378474593 -11.451399803

H   -5.834335804  -0.372889161 -10.436479568

C   -4.253688812   1.916966081 -10.466700554

H   -4.659918785   2.392732382 -11.366283417

H   -5.025526047   1.961230040  -9.691857338

H   -3.401668072   2.512257814 -10.121510506

C   -2.835478783   0.494957238 -11.939204216

H   -1.952216625   1.098142982 -11.702587128

H   -2.506093025  -0.512053549 -12.219060898

H   -3.309328794   0.941788495 -12.819122314

N    1.311250091  -6.889817715  -3.452469826

C    0.902754962  -7.698767185  -4.601595402

C    0.078298137  -6.296811581  -2.954820156

C   -0.462763608  -7.520529747  -4.837955475

C    1.732918382  -8.462146759  -5.400692940

C   -0.984793961  -6.639548779  -3.794420719

C   -1.042326093  -8.151330948  -5.936532497

C   -2.250501633  -6.122807980  -3.519835234

C   -0.039665252  -5.453701973  -1.865047455

C   -2.401881218  -5.280151844  -2.419381618

H   -3.101271391  -6.370810032  -4.147943020

C   -1.315213084  -4.949791908  -1.602190137

H   -3.382522106  -4.869585514  -2.193205833

H   -1.460708857  -4.282334805  -0.756967783

H    0.821008742  -5.186274529  -1.256695151

C    1.133496881  -9.089910507  -6.494253159

H    2.790650368  -8.579389572  -5.183591843

C   -0.231515586  -8.933600426  -6.756480694

H    1.739089608  -9.709292412  -7.150196552

H   -0.668264866  -9.433676720  -7.616714001

H   -2.101125956  -8.037630081  -6.150225163

C    2.165624380  -7.561182499  -2.470625877

C    1.578868389  -8.196897507  -1.380348921

C    3.539136648  -7.599061489  -2.680105925

C    2.393916845  -8.861250877  -0.470866114

C    4.342787266  -8.266541481  -1.758868694

C    3.775203466  -8.892066002  -0.653829277

H    0.501960874  -8.172722816  -1.242970824

H    3.986113787  -7.126180172  -3.546709538

H    1.944080591  -9.360030174   0.382549435

H    5.417553425  -8.290535927  -1.915752053

H    4.406046867  -9.409996033   0.063084245

H    1.886065125  -5.958974361  -3.931412220

===============================

3

===============================

N   -0.189317346   1.737607479   0.174521893

C    0.649717093   1.151519418  -0.718785465

C   -1.451911569   1.236367583  -0.049749441

C   -1.342193127   0.348694593  -1.085458040

N   -0.036467481   0.298938543  -1.477502584

H   -2.103937149  -0.244431660  -1.568261862

H   -2.293810606   1.559755087   0.542994022

C    2.063652277   1.342764497  -0.985823452

C    2.517321110   0.684166431  -2.166521311

C    2.935207605   2.072779417  -0.181029573

C    3.884407520   0.766839504  -2.471203804

C    4.284389973   2.150172472  -0.531286776

C    4.759850979   1.489063382  -1.673389196

H    2.590302706   2.586876154   0.707756758

H    4.255321026   0.287216127  -3.372534275

H    5.812073708   1.563470364  -1.932765126

C    5.158306122   2.921204567   0.291298777

N    5.845124245   3.558546543   0.977761269

C    0.163361996   2.784331083   1.083863735

C    0.130660653   4.106152534   0.622652113

C    0.626312017   2.447936773   2.356493711

C    0.627878189   5.091711044   1.468225121

C    1.113040924   3.476604700   3.165935040

C    1.151008487   4.803771019   2.734696627

H    0.630145788   6.116460800   1.107194185

H    1.496063948   3.213156939   4.146514416

N    3.234474897  -3.812986135  -2.994391680

C    2.710613966  -2.634652615  -3.499849081

C    2.725642204  -3.979362488  -1.710437298

N    1.848888636  -2.114212036  -2.566989899

C    1.890410423  -2.911949635  -1.475633502

H    3.027751923  -4.804384232  -1.082567215

H    1.325265527  -2.681236506  -0.583828449

C    3.001319408  -1.921111584  -4.667679310

C    2.268323660  -0.660276473  -4.778478146

C    3.898696661  -2.304875612  -5.697240353

C    2.453648806   0.101706296  -5.934019089

C    4.031338215  -1.504321694  -6.816181660

H    4.491731167  -3.206537485  -5.630088806

C    3.308067799  -0.292475402  -6.959812164

H    1.936330318   1.051284790  -6.024512291

H    3.448662281   0.317859054  -7.845027924

N    5.662529469  -2.329947710  -8.647545815

C    4.930557251  -1.941487074  -7.833010197

C    5.365177631  -4.831991196  -3.554077625

C    3.994674683  -4.715269566  -3.769447327

C    3.357433796  -5.394070625  -4.859215736

C    6.118798256  -5.609167576  -4.448029995

C    4.172978401  -6.179183483  -5.713594913

C    5.554240704  -6.255936623  -5.559333801

H    7.190357208  -5.656937122  -4.287399769

H    3.687378407  -6.679449558  -6.547076225

Ir    1.096354008  -0.264728576  -3.220225573

C   -1.103344321  -0.200842395  -5.111969471

N   -1.956633329  -0.828600943  -5.960907459

C   -1.936833143  -2.172713757  -5.656734467

N   -0.556609392  -1.099402547  -4.292954445

C   -1.059210539  -2.325745344  -4.619888306

H   -2.539937973  -2.876776695  -6.209224701

H   -0.771678984  -3.219590187  -4.087212563

C    0.365416914   1.405359030  -4.086718082

C   -0.700727284   1.191133738  -5.004963398

C   -1.280253649   2.246883869  -5.705715656

C    0.812806904   2.720227957  -3.908003807

C   -0.804369867   3.542895317  -5.500976563

H   -2.087901831   2.088836432  -6.410304070

C    0.244489744   3.779193640  -4.602528095

H    1.647750378   2.912782431  -3.240678072

H    0.613618612   4.792021275  -4.467686176

C   -1.388109207   4.612377167  -6.242815971

N   -1.876226068   5.463101864  -6.864826679

C   -2.577402592  -0.218872651  -7.096234798

C   -1.805840254  -0.056139924  -8.249306679

C   -3.865935326   0.312788725  -6.974495411

C   -2.344621420   0.705899954  -9.287514687

C   -4.354669094   1.063695431  -8.038883209

C   -3.599638224   1.307481647  -9.194872856

H   -1.736747622   0.853223562 -10.173509598

H   -5.343138218   1.505075455  -7.941842556

C    6.020496368  -4.092329025  -2.424081087

H    5.695641518  -3.046870232  -2.403209925

H    5.751530170  -4.523549080  -1.451377511

H    7.108559608  -4.116594315  -2.515398264

C    1.972962022  -5.276206493  -5.105369568

H    1.338363647  -4.632058144  -4.509697437

H    1.525875688  -5.794374466  -5.946689606

C   -0.416903764  -0.621095240  -8.340662956

H    0.276090026  -0.083532348  -7.682751656

H   -0.383015335  -1.672768593  -8.037197113

H   -0.032788984  -0.547785044  -9.360708237

C   -4.649149418   0.144790292  -5.703469276

H   -5.657948017   0.550042808  -5.809969902

H   -4.732651234  -0.907816172  -5.413158417

H   -4.161756516   0.669688940  -4.872650146

C    0.679637313   1.014439225   2.801224470

H    1.406994462   0.447838098   2.206442118

H    0.974326849   0.941829085   3.850505114

H   -0.288884401   0.518840432   2.681823254

C   -0.366181612   4.432814598  -0.756338239

H    0.298141092   4.021151543  -1.524526477

H   -1.359036803   4.010538101  -0.943373144

H   -0.422732681   5.513713360  -0.905088127

C    6.400103092  -6.967072964  -6.618107796

C   -4.151526451   2.240345955  -10.274665833

C    1.788568020   5.924816132   3.557433605

C    0.765396059   7.048927307   3.787157536

H   -0.103053167   6.682889938   4.345001221

H    1.223216057   7.859515667   4.364524364

H    0.405549198   7.477614880   2.846856117

C    2.282407522   5.433116436   4.919876099

H    2.726336956   6.268009186   5.471172333

H    1.463653564   5.034031391   5.528578758

H    3.053145885   4.661308765   4.819395542

C    2.994972467   6.470501900   2.771157265

H    3.489795208   7.263119221   3.343244791

H    3.730094671   5.682260513   2.575294971

H    2.694308043   6.894536018   1.807882190

C    6.000166893  -8.447513580  -6.692456722

H    4.936100483  -8.577908516  -6.912672520

H    6.568779469  -8.949892044  -7.481764793

H    6.213931084  -8.957987785  -5.746480942

C    7.899143696  -6.881489754  -6.316206932

H    8.155456543  -7.363342285  -5.365647793

H    8.459229469  -7.394715786  -7.103613853

H    8.250083923  -5.844424248  -6.288650513

C    6.137163639  -6.293795586  -7.978407860

H    6.371394157  -5.224533081  -7.950774670

H    6.758362293  -6.758296967  -8.751690865

H    5.092790127  -6.396223545  -8.289839745

C   -5.484304905   1.685640812 -10.803881645

H   -5.893798828   2.358087301 -11.565614700

H   -5.346988201   0.699199975 -11.259573936

H   -6.233054638   1.589911819 -10.011337280

C   -4.377064228   3.628969431  -9.650004387

H   -4.750688553   4.325162888 -10.408978462

H   -5.112308502   3.597773075  -8.839952469

H   -3.447808027   4.039059162  -9.240559578

C   -3.188076496   2.392585039 -11.454405785

H   -2.227044582   2.816106319 -11.143426895

H   -3.003565788   1.435831666 -11.955224037

H   -3.620974779   3.072803259 -12.194774628

N    2.215890884  -7.546505451  -2.958695650

C    2.411444902  -8.715381622  -3.853715658

C    0.761115491  -7.288716793  -3.008442879

C    1.188427329  -9.059988022  -4.432929039

C    3.611307383  -9.334054947  -4.117582798

C    0.165373877  -8.166927338  -3.916458845

C    1.171363950 -10.119614601  -5.343282223

C   -1.205656528  -8.031816483  -4.159269333

C    0.095555559  -6.300217152  -2.319433212

C   -1.906338692  -7.037298203  -3.483707905

H   -1.712045908  -8.688170433  -4.858893871

C   -1.276932240  -6.183355331  -2.571812153

H   -2.972044468  -6.926038265  -3.663188934

H   -1.854511142  -5.428972244  -2.046772003

H    0.611731470  -5.633478642  -1.635140657

C    3.574126720 -10.392148972  -5.031615734

H    4.535197735  -9.023391724  -3.640988588

C    2.367179871 -10.771900177  -5.628308296

H    4.490259647 -10.918470383  -5.277703762

H    2.363677502 -11.598591805  -6.332671165

H    0.245359764 -10.429286003  -5.816460609

C    2.810826302  -7.703571796  -1.624422669

C    2.071166039  -8.296948433  -0.610557914

C    4.130517483  -7.309895992  -1.443769693

C    2.674794197  -8.479555130   0.629083216

C    4.719884872  -7.500382423  -0.197024554

C    3.994017124  -8.083708763   0.837981939

H    1.044767857  -8.603772163  -0.782776117

H    4.690507889  -6.862107754  -2.259603977

H    2.109074116  -8.938434601   1.434261441

H    5.750220299  -7.194848537  -0.041155387

H    4.456062794  -8.229728699   1.809621930

H    2.658603907  -6.739420891  -3.444473982

Table S4. Vibrational Frequencies (in cm–1) of the Optimized Geometries

===============================

1

===============================

65.32    72.06    78.72   110.46   146.91   195.94

243.99   275.75   283.42   321.29   405.20   413.87

426.50   430.85   440.25   493.07   503.31   556.98

601.85   610.69   621.53   637.57   644.33   707.81

717.05   726.22   760.26   762.94   774.19   782.58

791.95   861.70   890.28   905.48   932.34   958.94

963.19   976.50   977.41   996.82  1003.19  1012.11

1013.61  1019.65  1029.13  1054.56  1060.34  1062.55

1075.70  1128.08  1133.74  1172.41  1199.55  1202.62

1202.98  1222.64  1233.26  1256.05  1306.33  1334.60

1348.47  1360.23  1388.48  1400.18  1445.66  1479.55

1486.88  1501.47  1521.28  1530.72  1542.32  1625.42

1640.91  1643.03  1655.01  1657.03  1691.58  3228.55

3233.31  3233.83  3234.07  3239.34  3242.66  3243.41

3246.84  3249.61  3249.78  3252.93  3258.02  3258.27

===============================

2

===============================

12.00    14.09    17.00    17.94    19.73    21.25

24.79    25.45    27.49    31.32    31.93    34.62

39.26    42.28    44.39    50.49    51.37    51.86

77.03    79.38    79.93    82.69    87.81    89.34

91.38    98.54   100.78   104.63   112.65   114.29

116.14   119.94   127.82   128.61   128.75   132.74

138.67   142.97   145.25   153.78   156.50   159.01

159.72   165.40   169.86   184.70   187.05   188.42

200.60   211.18   214.39   232.42   236.55   237.84

241.12   243.77   244.39   246.38   247.10   248.60

252.37   256.28   263.45   271.43   271.91   272.09

281.06   288.97   290.14   290.35   290.89   293.37

296.61   302.03   308.29   316.53   319.21   320.57

324.46   328.39   330.97   334.21   354.84   355.20

355.73   359.89   360.54   376.49   379.04   382.02

383.39   383.58   384.16   405.68   421.68   422.15

422.96   427.67   429.01   429.72   442.86   450.37

451.13   457.47   467.70   472.89   489.12   490.80

508.49   524.00   525.20   526.15   526.28   528.92

541.82   542.96   543.42   547.96   550.43   552.66

554.51   572.70   573.53   574.69   575.43   577.09

592.95   596.83   599.14   602.86   603.02   613.51

621.51   622.91   630.94   633.35   656.58   662.12

662.62   665.75   673.06   673.92   678.22   690.86

704.43   705.44   705.96   728.56   735.08   735.33

753.21   755.86   762.93   763.97   764.52   795.31

798.93   818.72   819.82   820.89   843.53   854.31

854.38   857.21   857.56   860.14   861.62   863.65

866.42   899.72   900.27   901.44   908.72   909.23

910.71   914.05   922.94   926.58   932.98   941.59

943.04   944.01   951.37   951.47   951.97   959.21

960.21   961.40   967.22   967.67   968.53   970.59

972.22   975.32   978.64   978.91   979.95   984.80

994.65   999.01  1007.90  1010.37  1024.90  1025.28

1025.83  1051.51  1053.50  1053.70  1055.05  1055.14

1055.43  1056.03  1057.47  1057.59  1058.67  1059.36

1061.07  1062.50  1063.06  1064.94  1068.02  1070.38

1070.76  1087.79  1101.97  1107.75  1119.53  1120.57

1137.05  1158.10  1167.11  1173.22  1173.93  1181.47

1182.00  1188.56  1190.11  1192.26  1228.84  1229.99

1231.97  1246.72  1246.80  1246.99  1248.89  1249.65

1250.95  1252.58  1266.87  1268.35  1274.40  1275.48

1276.89  1293.64  1295.34  1295.45  1308.67  1312.43

1313.15  1337.16  1338.60  1341.43  1348.61  1354.90

1356.25  1368.40  1370.67  1371.69  1376.03  1379.55

1383.92  1397.43  1407.93  1408.41  1408.67  1411.00

1411.31  1411.46  1411.89  1413.96  1416.41  1420.18

1420.59  1420.91  1426.38  1426.87  1427.31  1440.54

1441.51  1442.84  1443.05  1443.42  1454.88  1466.03

1467.13  1467.21  1474.73  1475.18  1483.42  1489.07

1489.17  1489.44  1489.56  1489.92  1490.02  1490.17

1490.20  1490.39  1490.58  1491.21  1492.83  1492.89

1493.43  1496.50  1496.81  1497.03  1497.41  1508.44

1508.94  1509.61  1515.13  1515.43  1515.52  1518.65

1518.75  1519.01  1524.93  1531.97  1532.39  1533.61

1538.49  1539.54  1553.65  1554.26  1560.34  1563.95

1566.38  1583.75  1593.24  1594.26  1600.01  1602.50

1645.84  1660.77  1665.02  1667.22  1672.41  1675.61

1683.49  1683.86  1685.61  2361.28  2371.57  2372.41

3055.55  3056.36  3056.37  3056.81  3057.84  3057.94

3058.01  3061.86  3061.92  3062.36  3062.69  3062.78

3062.85  3067.05  3068.63  3126.23  3131.18  3131.40

3131.62  3137.13  3138.83  3140.34  3140.61  3140.68

3141.75  3141.92  3142.06  3144.32  3144.38  3144.94

3147.51  3147.62  3147.73  3150.26  3150.83  3151.04

3153.41  3153.43  3154.58  3164.27  3166.25  3166.29

3167.73  3168.38  3169.56  3205.83  3207.05  3207.84

3208.57  3210.36  3212.06  3226.51  3227.79  3230.38

3231.34  3232.15  3242.91  3252.05  3252.58  3258.08

3291.55  3301.05  3302.27  3317.12  3323.60  3324.30

===============================

2(D)

===============================

12.05    14.13    17.23    17.98    19.80    21.50

24.70    25.21    27.88    31.31    31.87    34.92

39.11    42.27    44.34    50.14    51.38    51.83

76.56    79.42    79.91    82.73    86.66    89.19

91.15    98.65   100.77   104.65   112.67   114.15

116.40   119.21   122.50   127.78   128.59   130.83

134.29   140.70   145.22   151.04   153.99   156.63

159.04   164.99   169.74   183.48   187.02   188.40

200.45   211.28   214.42   231.84   236.51   237.74

240.87   243.64   244.11   245.59   246.93   248.47

252.30   256.00   263.26   268.26   271.73   271.93

280.38   288.88   290.09   290.21   290.88   293.21

296.03   301.91   308.17   314.09   319.21   320.56

324.34   328.28   330.79   333.83   354.79   355.11

355.76   359.92   360.51   376.47   378.72   381.24

383.36   383.51   384.15   404.09   421.26   422.07

422.23   427.67   428.65   429.60   439.43   449.78

451.11   456.50   467.56   472.60   489.07   490.69

507.02   517.28   524.03   525.18   526.29   528.90

539.99   542.94   543.40   547.47   549.72   552.69

554.50   571.09   572.92   573.62   575.42   577.10

592.55   596.77   599.12   601.73   602.88   610.44

621.16   622.77   630.94   633.33   656.57   662.09

662.66   664.37   673.09   673.95   678.37   691.27

702.51   704.71   705.52   727.35   734.99   735.16

752.81   755.51   757.22   763.96   764.43   795.35

798.88   817.66   819.81   820.87   842.39   854.03

854.18   856.93   859.26   860.10   861.68   863.52

865.65   866.57   900.20   901.40   901.62   909.15

910.63   910.74   918.75   922.87   926.40   933.12

941.57   942.86   944.01   951.36   951.39   951.99

959.47   960.21   961.41   967.15   967.66   968.52

970.50   972.21   975.26   978.90   979.96   985.94

992.69   994.62   998.91  1007.87  1010.36  1015.09

1025.26  1025.85  1051.82  1053.40  1053.73  1054.29

1055.13  1055.41  1056.01  1057.58  1057.85  1058.65

1058.86  1061.03  1061.97  1062.56  1063.03  1070.36

1070.77  1087.18  1101.98  1107.81  1119.48  1120.45

1134.49  1157.92  1166.52  1173.18  1173.87  1181.45

1181.92  1187.26  1189.99  1192.23  1228.05  1229.91

1231.86  1246.72  1246.79  1246.97  1248.53  1249.64

1250.93  1252.10  1266.63  1267.57  1268.33  1275.31

1276.78  1283.86  1295.30  1295.40  1303.10  1309.63

1312.47  1313.11  1326.94  1337.61  1338.77  1341.46

1354.61  1356.06  1357.70  1368.41  1370.74  1372.42

1377.55  1379.57  1383.92  1400.40  1408.13  1408.41

1408.65  1410.99  1411.33  1411.45  1411.86  1413.96

1416.85  1420.22  1420.95  1425.65  1426.30  1426.95

1440.54  1441.47  1442.81  1443.03  1443.38  1457.01

1465.82  1466.02  1467.14  1474.59  1474.91  1475.22

1489.03  1489.13  1489.55  1489.93  1489.98  1490.09

1490.25  1490.43  1490.60  1491.20  1492.66  1492.78

1492.87  1493.36  1496.50  1496.82  1496.98  1502.25

1508.42  1509.00  1515.09  1515.43  1515.47  1518.60

1518.74  1518.96  1522.42  1531.96  1532.35  1533.48

1538.42  1539.56  1553.70  1554.21  1559.26  1563.88

1566.30  1584.30  1593.17  1594.21  1599.99  1602.54

1640.12  1660.64  1665.02  1667.19  1672.42  1675.50

1683.00  1683.49  1685.63  2281.44  2359.84  2371.62

2372.42  3056.37  3056.38  3056.81  3057.84  3057.95

3058.02  3061.88  3061.89  3062.35  3062.70  3062.78

3062.86  3067.03  3068.62  3079.43  3131.20  3131.43

3131.59  3137.11  3138.81  3140.36  3140.61  3140.69

3141.75  3141.93  3142.06  3144.33  3144.38  3144.94

3147.52  3147.62  3147.73  3150.27  3150.83  3151.05

3153.42  3153.44  3154.57  3156.03  3166.26  3166.30

3167.71  3168.38  3169.56  3205.85  3207.06  3207.82

3208.61  3210.39  3212.01  3226.54  3227.76  3230.38

3231.36  3232.15  3242.72  3252.06  3252.55  3258.16

3291.56  3301.07  3302.32  3317.14  3323.61  3324.31

===============================

TS

===============================

–669.85     9.57    14.12    16.98    19.13    19.62

21.20    22.42    26.97    27.62    30.24    32.23

35.33    36.20    36.91    38.35    40.99    43.28

45.10    45.92    51.52    51.75    58.15    61.19

68.22    77.14    78.99    80.20    82.01    87.46

89.83    94.25    96.92    98.59   101.03   103.75

111.95   113.26   115.35   120.03   120.65   124.77

129.78   134.25   136.19   137.83   143.62   147.66

149.52   154.11   159.85   161.92   165.74   167.21

171.66   187.25   189.05   192.37   201.63   206.63

211.22   217.09   227.29   233.58   236.60   238.32

240.49   243.01   244.55   245.84   247.53   249.91

251.23   257.26   262.64   269.17   269.28   271.88

273.66   285.16   287.97   289.11   291.32   294.05

295.08   298.93   301.68   308.00   308.49   318.60

319.37   320.11   323.03   323.52   326.21   330.15

340.84   353.84   355.13   357.86   359.48   362.79

373.47   378.21   378.69   381.52   382.69   384.29

397.97   419.36   421.17   422.20   423.68   425.39

426.06   428.48   432.29   435.77   443.05   446.72

448.91   451.65   459.52   463.33   466.93   467.89

483.36   485.94   493.04   495.56   508.59   523.37

524.99   525.87   528.93   529.68   538.28   541.25

542.20   543.62   548.56   551.23   554.18   556.46

569.53   573.04   573.56   574.48   576.92   581.11

594.17   596.00   598.21   603.50   611.65   612.27

620.11   621.93   623.48   625.22   626.32   630.16

632.62   634.98   640.92   646.64   654.40   658.80

663.51   664.60   672.39   674.39   687.99   695.17

696.78   705.28   717.91   730.71   739.97   742.66

743.33   748.48   756.88   759.68   760.79   761.69

762.27   764.72   774.87   778.78   792.77   796.50

797.74   800.51   817.02   819.51   820.36   844.16

847.04   855.06   856.22   860.00   861.59   862.40

864.47   866.14   868.17   869.10   888.42   891.96

895.36   899.98   903.17   904.75   913.60   913.65

916.14   923.85   927.51   930.45   931.48   939.73

942.14   944.43   949.22   951.32   951.55   952.39

957.72   958.56   960.36   961.02   964.14   967.68

968.53   969.02   969.42   971.00   972.38   977.15

979.03   979.53   996.27   998.55   998.74   999.20

1000.66  1006.16  1010.45  1012.77  1014.26  1017.06

1020.74  1024.22  1024.94  1026.25  1026.89  1050.74

1052.51  1054.46  1054.50  1054.57  1054.69  1055.68

1056.59  1057.10  1057.48  1058.61  1059.87  1060.15

1062.88  1063.34  1064.08  1065.09  1067.23  1069.74

1070.21  1092.09  1099.96  1102.22  1107.08  1116.13

1119.64  1127.50  1135.99  1148.29  1155.13  1165.69

1172.90  1173.95  1175.16  1181.65  1185.28  1187.62

1195.05  1195.81  1197.64  1199.62  1206.32  1213.47

1217.29  1220.68  1228.18  1230.54  1234.17  1244.05

1246.24  1246.58  1248.67  1249.24  1250.15  1252.33

1266.10  1267.28  1267.32  1275.65  1276.39  1277.65

1284.34  1294.78  1296.13  1296.21  1308.36  1312.34

1314.94  1316.98  1336.43  1339.64  1341.49  1346.59

1352.25  1354.46  1355.67  1367.75  1370.83  1372.76

1378.78  1379.93  1382.12  1383.45  1390.09  1391.26

1396.15  1406.28  1407.82  1409.57  1409.90  1411.03

1412.11  1412.71  1413.08  1418.19  1420.87  1421.55

1422.50  1426.83  1427.37  1430.60  1433.58  1436.75

1439.64  1439.81  1444.15  1444.53  1444.87  1446.65

1459.60  1465.58  1466.32  1473.24  1473.83  1476.64

1487.13  1488.75  1488.84  1489.50  1490.25  1490.37

1490.61  1490.71  1490.89  1491.08  1492.03  1492.85

1493.82  1494.64  1496.22  1496.30  1497.81  1505.57

1506.37  1508.00  1508.08  1510.90  1513.62  1515.66

1516.14  1517.22  1519.44  1519.64  1519.74  1523.21

1527.22  1530.53  1531.79  1532.30  1533.14  1538.63

1540.92  1543.42  1546.62  1546.83  1553.88  1560.91

1564.87  1571.75  1591.20  1593.08  1594.54  1600.28

1604.01  1607.04  1635.51  1666.11  1666.19  1667.86

1670.37  1670.68  1675.28  1678.03  1679.08  1682.09

1682.33  1687.65  1693.51  2376.30  2379.85  2380.71

3050.72  3054.93  3056.76  3057.71  3059.36  3059.37

3059.38  3059.43  3060.51  3061.90  3063.69  3064.56

3066.63  3068.78  3128.14  3128.62  3130.91  3132.97

3133.01  3138.46  3141.71  3142.46  3142.78  3144.04

3144.17  3144.66  3145.06  3145.97  3146.47  3148.76

3149.55  3150.67  3150.73  3152.15  3152.91  3153.06

3154.23  3158.64  3169.17  3169.72  3170.19  3170.28

3173.31  3207.56  3209.73  3211.36  3212.11  3216.08

3217.02  3217.59  3218.98  3223.47  3225.98  3226.21

3226.55  3228.49  3232.31  3232.63  3233.89  3234.03

3234.87  3236.64  3238.19  3238.69  3240.82  3242.54

3242.98  3250.22  3255.59  3256.01  3256.26  3268.56

3281.14  3302.94  3311.99  3312.52  3324.63  3336.52

===============================

TS(D)

===============================

-540.52     9.57    14.12    16.98    19.13    19.62

21.20    22.42    26.96    27.62    30.23    32.23

35.33    36.20    36.90    38.34    40.98    43.28

45.10    45.92    51.52    51.75    58.12    61.17

68.18    77.04    78.88    80.19    82.01    87.46

89.81    94.24    96.88    98.57   101.02   103.74

111.93   113.25   115.34   120.03   120.65   124.71

129.77   134.11   136.19   137.82   143.62   147.66

149.52   154.10   159.83   161.87   165.73   167.20

171.65   187.24   189.05   192.33   201.33   206.63

211.21   217.08   227.25   233.57   236.60   238.28

240.38   242.97   244.44   245.84   247.45   249.91

251.22   257.25   262.63   268.75   269.20   271.86

273.65   285.13   287.97   289.11   291.31   294.04

295.07   298.88   301.62   307.64   308.28   318.59

319.27   319.70   322.95   323.52   326.16   330.12

340.47   353.74   355.13   357.86   359.47   362.79

373.40   376.92   378.20   381.15   382.66   384.28

391.33   419.36   420.93   422.01   423.68   425.27

426.05   428.48   432.13   435.13   442.63   446.16

448.89   451.60   456.92   463.33   466.92   467.86

483.35   485.93   491.33   494.41   507.31   523.37

524.99   525.87   528.89   529.60   535.76   541.25

542.11   543.62   547.63   551.15   553.72   556.45

569.53   571.75   573.04   574.46   576.92   581.06

592.29   595.55   598.19   602.63   607.09   611.62

619.61   621.58   622.19   624.82   625.86   630.00

632.62   633.68   639.42   646.48   652.94   657.02

663.51   664.60   672.39   674.38   684.87   695.11

696.72   705.28   717.69   729.43   739.75   742.32

743.24   748.42   756.81   759.49   760.30   760.78

762.27   764.05   774.17   777.71   792.69   796.50

797.72   800.49   817.02   819.49   820.36   838.57

844.78   855.00   856.21   859.99   861.59   862.33

864.47   866.08   868.16   869.03   875.93   891.89

894.19   899.17   903.17   904.75   908.64   913.56

913.60   916.14   923.85   930.23   931.45   939.72

942.14   944.40   949.21   951.32   951.54   952.39

956.27   958.37   960.36   961.02   964.03   967.61

968.53   969.02   969.17   970.76   972.28   977.14

979.03   979.53   995.48   998.39   998.61   998.86

1000.48  1006.15  1010.40  1012.54  1014.07  1015.98

1017.07  1022.01  1024.23  1024.94  1025.82  1029.78

1049.63  1050.75  1054.44  1054.50  1054.67  1054.70

1056.13  1056.59  1056.84  1057.10  1058.61  1058.77

1059.94  1062.97  1063.37  1064.08  1065.65  1067.84

1069.74  1070.21  1082.81  1085.74  1098.31  1101.81

1107.07  1116.09  1119.64  1126.89  1134.95  1148.38

1155.06  1165.54  1172.75  1173.79  1175.15  1181.64

1185.27  1187.62  1195.05  1195.17  1196.50  1199.70

1203.01  1213.95  1217.15  1217.88  1228.18  1230.53

1234.17  1244.06  1246.24  1246.58  1248.92  1249.24

1250.15  1263.00  1266.13  1267.26  1267.32  1269.74

1275.98  1277.64  1281.58  1294.38  1296.13  1296.21

1308.43  1312.35  1314.94  1320.87  1336.43  1339.64

1342.76  1351.45  1354.46  1354.65  1355.66  1367.75

1370.82  1372.59  1378.82  1379.93  1382.05  1383.44

1390.11  1392.68  1398.48  1406.32  1407.82  1409.57

1409.90  1412.11  1412.70  1413.08  1418.19  1420.87

1421.55  1422.48  1426.83  1427.37  1430.59  1433.59

1436.75  1439.64  1439.81  1444.16  1444.67  1444.87

1447.70  1465.56  1466.32  1472.06  1473.82  1473.99

1487.09  1488.72  1488.82  1489.49  1490.25  1490.37

1490.61  1490.70  1490.89  1491.07  1492.02  1492.71

1492.85  1493.82  1494.69  1496.22  1496.30  1502.24

1504.88  1508.00  1508.06  1510.39  1510.72  1512.97

1515.66  1516.14  1516.89  1519.44  1519.64  1519.74

1524.56  1530.04  1531.78  1532.29  1532.89  1538.62

1540.91  1542.43  1545.66  1546.69  1553.88  1560.90

1564.85  1571.45  1591.19  1593.06  1594.32  1600.28

1604.01  1606.91  1635.34  1666.11  1666.19  1667.42

1670.33  1670.38  1675.28  1676.68  1677.94  1682.09

1682.33  1686.63  1691.85  2376.30  2379.85  2380.71

3050.72  3054.93  3056.76  3057.71  3059.36  3059.37

3059.38  3059.43  3060.51  3061.90  3063.69  3064.56

3066.63  3068.78  3128.14  3128.62  3130.91  3132.97

3133.01  3138.46  3141.71  3142.46  3142.78  3144.01

3144.15  3144.66  3145.06  3145.97  3146.47  3148.76

3149.55  3150.67  3150.73  3152.15  3152.91  3153.06

3154.23  3158.64  3169.17  3169.72  3170.19  3170.28

3173.31  3207.56  3209.73  3211.36  3212.11  3216.08

3217.02  3217.59  3218.98  3223.47  3225.98  3226.21

3226.55  3228.49  3232.31  3232.63  3233.89  3234.03

3234.87  3236.64  3238.19  3238.69  3240.82  3242.54

3242.98  3250.13  3255.59  3256.01  3256.25  3268.56

3281.14  3302.94  3311.99  3312.52  3324.63  3336.52

===============================

3

===============================

11.98    16.67    17.90    19.52    21.67    23.08

24.55    25.82    27.75    28.87    30.08    31.99

32.81    35.83    37.32    42.40    42.49    44.57

46.86    49.37    51.17    53.67    55.48    65.54

70.65    76.77    80.97    81.32    87.33    89.84

93.02    95.85    99.41   100.17   102.92   108.23

109.62   111.57   112.25   115.46   116.38   119.88

126.40   128.79   133.20   138.45   143.26   147.17

151.27   152.52   154.14   162.91   165.53   169.28

182.46   186.60   187.00   188.77   198.50   201.00

212.12   217.23   225.55   231.52   235.01   235.76

240.40   241.00   243.90   244.43   248.14   251.94

254.79   256.93   261.90   264.97   271.40   272.35

276.63   282.09   288.54   288.90   289.53   291.96

296.53   301.66   302.08   306.44   309.49   315.04

318.96   319.50   322.04   325.27   326.24   331.46

343.69   355.53   357.15   357.33   359.27   361.01

372.64   376.69   382.11   382.95   383.37   384.80

410.32   418.26   419.90   420.64   422.58   423.88

424.49   425.34   428.91   439.27   442.21   447.94

448.23   448.89   455.85   463.44   463.76   469.15

485.06   485.31   487.60   500.37   518.22   521.53

523.60   524.55   525.59   528.54   537.54   538.82

539.70   544.73   549.51   552.26   555.33   555.62

559.51   567.52   572.77   573.85   577.02   579.72

595.40   597.83   598.49   599.45   608.46   613.50

619.21   621.29   624.86   625.26   626.73   627.29

628.57   631.57   643.77   651.79   662.36   664.45

670.13   671.85   673.19   674.62   686.32   703.27

704.55   708.98   714.00   725.17   735.83   742.54

743.64   744.47   748.06   749.90   758.47   759.59

760.88   762.84   763.44   770.71   771.70   782.66

796.13   799.63   813.71   817.67   820.70   824.93

840.78   856.72   858.90   859.42   860.17   861.42

861.46   863.46   864.68   867.17   869.73   870.51

875.83   877.35   887.03   903.35   903.94   904.08

914.03   914.27   919.17   931.39   933.76   937.11

938.31   939.83   943.02   947.34   949.04   952.35

952.46   952.52   953.96   960.60   960.83   961.93

964.90   968.63   969.63   970.41   971.50   973.45

977.24   980.43   986.39   995.26   996.84   997.76

1000.18  1003.38  1005.84  1006.07  1006.70  1009.68

1014.98  1020.48  1023.54  1025.06  1025.77  1047.46

1051.27  1054.27  1054.35  1054.57  1055.11  1056.30

1056.86  1057.27  1057.53  1058.20  1058.51  1059.45

1062.86  1062.95  1065.25  1067.38  1069.49  1070.50

1087.05  1097.76  1102.72  1106.80  1112.08  1117.19

1119.52  1126.77  1134.60  1144.65  1167.11  1171.13

1173.42  1175.49  1176.43  1178.10  1182.64  1183.47

1190.03  1191.98  1194.11  1197.39  1200.95  1203.25

1210.74  1220.84  1229.09  1230.28  1234.30  1244.68

1246.47  1246.91  1248.36  1249.04  1251.63  1259.21

1266.23  1267.54  1269.45  1275.13  1275.93  1276.99

1283.64  1288.12  1292.39  1296.17  1296.76  1304.48

1312.61  1313.63  1333.76  1336.39  1338.73  1340.73

1342.90  1354.63  1355.93  1366.76  1367.69  1369.10

1371.11  1376.89  1381.94  1383.23  1383.70  1385.91

1395.59  1404.12  1408.95  1409.89  1410.29  1411.08

1412.42  1412.67  1412.71  1413.64  1416.82  1420.93

1421.71  1425.83  1426.98  1427.46  1437.95  1438.38

1441.65  1443.73  1444.49  1444.70  1445.85  1449.06

1459.30  1465.01  1466.74  1473.11  1473.40  1482.16

1485.72  1487.55  1489.40  1489.63  1490.56  1490.72

1490.96  1491.13  1491.19  1491.55  1492.21  1492.42

1493.06  1493.23  1495.57  1496.32  1496.70  1501.39

1504.68  1507.42  1508.21  1509.41  1516.02  1516.03

1518.23  1519.06  1519.83  1519.92  1519.99  1525.00

1528.64  1531.70  1531.93  1532.79  1538.16  1539.28

1540.84  1541.98  1545.99  1546.89  1551.00  1561.94

1564.44  1589.04  1591.92  1594.37  1597.96  1599.30

1606.22  1625.95  1636.04  1644.47  1664.50  1665.36

1667.29  1672.14  1674.62  1676.02  1681.30  1681.68

1683.64  1688.26  2370.75  2381.92  2382.24  3057.53

3058.01  3058.26  3058.34  3060.04  3060.34  3060.64

3060.71  3060.80  3064.63  3064.86  3065.74  3067.32

3070.61  3130.34  3131.42  3132.70  3136.71  3141.32

3141.34  3143.99  3144.12  3144.13  3145.36  3145.83

3146.05  3146.43  3149.06  3150.28  3150.94  3151.20

3151.67  3153.03  3153.52  3154.64  3155.67  3157.32

3160.51  3170.61  3170.65  3170.83  3172.20  3174.86

3205.63  3212.42  3215.29  3216.97  3217.43  3218.14

3219.43  3219.99  3225.41  3227.01  3227.35  3229.18

3232.47  3232.83  3234.03  3234.58  3237.76  3239.38

3239.81  3240.23  3243.22  3243.92  3245.74  3248.55

3249.52  3251.62  3258.11  3259.66  3272.30  3289.86

3300.86  3303.99  3310.53  3315.68  3323.99  3325.61