Use of 2D nanoplatelets to improve the sensitivity in hybrid photodetector for indirect X-ray imaging

Jehoon Lee, Kyunghan Yoo, Hailiang Liu, and Jungwon Kang*

*jkang@dankook.ac.kr

Department of Electronic and Electrical Engineering, Dankook University, Yongin-si 16890, Korea

Synthesis methods

Preparation of cadmium myristate (Cd(Myr)2)

Cadmium myristate was prepared according to follwed process. For the synthesis, 1 g (4 mmol) of sodium myristate and 0.615 g (2 mmol) of cadmium nitrate were dissolved in 50 mL of methanol, respectively. After sonicating sodium myristate solution for 20 min and cadmium nitrate solution was added into sodium myristate solution. When the two solutions are mixed, a white precipitate was formed, and the mixture was stirred at room temperature for 2-hours to sufficiently mixed. The resulting precipitate was filtered and washed 3 times with methanol and dried at 40℃ under vacuum overnight.

Preparation of selenium precursor (SeODE)

Selenium precursor was prepared according to the followed process. For the synthesis, 7.9 mg (0.1 mmol) of selenium (Se) powder was dispersed in 3 mL of 1-octadecene (ODE) and that solution was sonicated for 20 min. After that, 7 mL of ODE was loaded in the three-neck flask and that was heated to 180℃ under argon flow. At the 180℃, the Se powder dispersed ODE solution was injected in the three-neck flask and the mixture was heated at 220℃ for 30 min.