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Table captions
Table S1. The textural properties, including specific surface area, pore volume, and average pore diameter, were determined for CS, CS@UiO-66-NH₂, and CS@ UiO-66-NH₂@rGO.
	Sample
	Specific surface area
（m2·g-1）
	Pore volume
（cm3·g-1）
	Average pore
Diameter(nm)

	CS
	17.45
	0.132
	25.12

	UiO-66-NH₂
	803
	0.235
	1.03

	CS@UiO-66-NH₂
	165.89
	0.241
	3.12

	CS@UiO-66-NH₂@rGO
	298.76
	0.338
	3.00

	CS@UiO-66-NH₂@rGO +TC
	96.4
	0.21
	28.6

	CS@UiO-66-NH₂@rGO +NOR
	68.9
	0.17
	41.3
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Figure captions
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Fig. S1. FTIR spectra of CS@UiO-66-NH₂@rGO treated under pH=3 and pH=12.
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