Supplementary material

Table captions

Table S1. The textural properties, including specific surface area, pore volume, and average pore diameter, were determined for CS, CS@UiO-66-NH₂, and CS@ UiO-66-NH₂@rGO.

| Sample | Specific surface area （m2·g-1） | Pore volume （cm3·g-1） | Average pore Diameter(nm) |
| --- | --- | --- | --- |
| CS | 17.45 | 0.132 | 25.12 |
| UiO-66-NH₂ | 803 | 0.235 | 1.03 |
| CS@UiO-66-NH₂ | 165.89 | 0.241 | 3.12 |
| CS@UiO-66-NH₂@rGO | 298.76 | 0.338 | 3.00 |
| CS@UiO-66-NH₂@rGO +TC | 96.4 | 0.21 | 28.6 |
| CS@UiO-66-NH₂@rGO +NOR | 68.9 | 0.17 | 41.3 |

Figure captions

Fig. S1. FTIR spectra of CS@UiO-66-NH₂@rGO treated under pH=3 and pH=12.