Supporting Information for

Efficient H2O2 Synthesis from Seawater via Na,Pb-codoped SnSe under a Small Temperature Gradient

Yuyan Xu,1 Xinyue Zhang,1,2 Yangyang Wan,3* Bingchao Qin,4 Jun Pei,5 Hong Liu,1 Xiaoxue Song,1 Shutong Jiang,1 Yuqiao Zhang,1 Long Zhang,1 Yong Liu,2 Qian Yu,6 Li-Dong Zhao,4* Shun Li,1* and Jianming Zhang1*

1 School of Chemistry and Chemical Engineering, Jiangsu University, Zhenjiang, Jiangsu 212013 China

2 Foshan (Southern China) Institute for New Materials, Foshan 528231, China

3 Institute for Advanced Materials, School of Materials Science and Engineering, Jiangsu University, Zhenjiang, Jiangsu 212013 China

4 School of Materials Science and Engineering, Beihang University, Beijing 100191, China

5 Beijing Municipal Key Laboratory of New Energy Materials and Technologies, School of Materials Science and Engineering, University of Science and Technology Beijing, Beijing 100083, China

6 School of Life Sciences, Jiangsu University, Zhenjiang, Jiangsu 212013 China

*Corresponding author emails: yangyang.wan@ujs.edu.cn; zhaolidong@buaa.edu.cn; shun@ujs.edu.cn; zhangjm@ujs.edu.cn

Supplemental Figures

Supplementary Fig. 1. TEC H2O2 generation in 2 h under different T using SnSe (a), Na-SnSe (b) and Na,Pb-SnSe (c) nanocatalysts in O2-saturated DI water.

Supplementary Fig. 2. Thermoelectric properties as a function of temperature for SnSe, Na-SnSe and Na,Pb-SnSe crystals along the b axis: (a) electrical conductivity, (b) Seebeck coefficient, (c) power factor (PF), (d) total thermal conductivity, and (e) ZT values. The data were taken from Refs. S1-S3.

At low temperature range (300–400 K), Na-SnSe and Na,Pb-SnSe exhibited much higher electrical conductivity than pristine SnSe bulk crystal (Supplementary Fig. 2a), which are beneficial to supply charge carriers under a small temperature gradient. The Na,Pb-SnSe sample exhibited the highest power factor (PF) value (Supplementary Fig. 2c), calculated from Seebeck coefficient (Supplementary Fig. 2b). The thermal conductivity for both Na-SnSe and Na,Pb-SnSe is largely greater than that of SnSe (Supplementary Fig. 2d). The calculated ZT values of the three bulk samples along b axis are presented in Supplementary Fig. 2e.

Supplementary Fig. 3. TEC reactions conducted across varying artificial seawater concentration. n0 is the concentration of the suggested standard artificial seawater, and n is the concentration of diluted or concentrated artificial seawater.

Supplementary Fig. 4. Photograph of the continuous-flow TEC reactor and schematic of the commercial stainless-steel reaction column with the internal packing structure.

Supplementary Fig. 5. XRD patterns of powdered SnSe, Na-SnSe and Na,Pb-SnSe samples. Standard PDF card No. 48-1224 of orthorhombic Pnma phase of SnSe is also shown for comparison.

Supplementary Fig. 6. SEM images of exfoliated powdered nanocatalysts from bulk crystals: (a) SnSe, (b) Na-SnSe and (c) Na,Pb-SnSe. Corresponding TEM images of (d) SnSe, (e) Na-SnSe and (f) Na,Pb-SnSe.

Supplementary Fig. 7. (a, b) HRTEM images (inset of a shows SAED patterns) and (c-e) EDS mappings of exfoliated SnSe nanosheets from bulk crystal.

Supplementary Fig. 8. (a, b) HRTEM images (inset of a shows SAED patterns) and (c-f) EDS mappings of exfoliated Na-SnSe nanosheets from bulk crystal.

Supplementary Fig. 9. (a, b) HRTEM images (inset of a shows SAED patterns) and (c-g) EDS mappings of exfoliated Na,Pb-SnSe nanosheets from bulk crystal.

Supplementary Fig. 10. Specific surface area analysis of (a) SnSe, (b) Na-SnSe and (c) Na,Pb-SnSe nanosheets exfoliated from bulk crystals.

Supplementary Fig. 11. High-resolution XPS spectra of (a, b) SnSe, (c, d) Na-SnSe and (e-g) Na,Pb-SnSe nanosheets under different temperatures.

Supplementary Fig. 12. (a) Bandgap calculation and (b) schematic band structure of SnSe and Na,Pb-SnSe. The bandgap was achieved by converting reflectance data obtained by UV-Vis DRS to absorption data through the Kubelka-Munk equation: α/S = (1/2R)2/(2R), where R is the reflectance, and α and S are the absorption and scattering coefficients, respectively. Eg is estimated by the Tauc plots. The conversion from vacuum energy (EVB-vac) to the potential versus the normal hydrogen electrode (EVB-NHE) is achieved through the following relation: EVB-NHE = − EVB-vac − 4.5.

Supplementary Fig. 13. UPS spectra of (a, c) SnSe and (b, d) Na,Pb-SnSe under different temperatures. The photon energy hν (21.22 eV) corresponds to monochromatic ionizing radiation, whereas Ecutoff refers to the secondary-electron cutoff derived from the linear extrapolation in UPS spectra. The work function (φ) is calculated by the formula: φ = hν – Ecutoff. The valence band potential (EVB) was determined using the formula: EVB = EF – EVBE.1, 2 Here, Ef represents the Fermi level (Ef = –φ), and EVBE is the valence band edge energy derived from extrapolation of UPS spectrum onsets.

Supplementary Fig. 14. Mott-Schottky plots of (a) SnSe, (b) Na-SnSe and (c) Na,Pb-SnSe nanosheets-based electrodes under different ΔT.

Supplementary Fig. 15. EIS Nyquist plots of SnSe, Na-SnSe and Na,Pb-SnSe nanosheets-based electrodes without ΔT (a), under the same ΔT = 100 K, (b) and under different ΔT (c–e).

Supplementary Fig. 16. (a) Comparison of H2O2 evolution in DI water of different samples under different conditions. (b) Comparison of H2O2 evolution in artificial seawater over Na,Pb-SnSe nanosheets under different atmospheres.

Supplementary Fig. 17. Total ion chromatogram (a) and extracted Ion Spectra (b–d) for 18O2 labelled experiment.

Supplementary Fig. 18. LC-MS spectrum of 18O2 labeled experiments.

Supplementary Fig. 19. Total Ion Chromatogram (a) and extracted Ion Spectra (b–d) for H218O labelled experiment.

Supplementary Fig. 20. Mass spectrum of H218O labeled experiments.

Supplementary Fig. 21. Schematic illustration of the experimental setup for in situ Raman tests (upper) and photo-images of the home-designed measurement system (lower).

Supplementary Fig. 22. In situ Raman spectra of Na,Pb-SnSe dry powder catalyst at different temperatures in air.

Supplementary Fig. 23. Computational models and the most stable OOH adsorption configurations for SnSe, Na-SnSe, and Na,Pb-SnSe, respectively.

Supplementary Fig. 24. PDOS and COHP analysis of the Sn‒OOH interaction on Na-SnSe.

Supplementary Fig. 25. Differential charge-density plots of OOH adsorption on Na,Pb-SnSe; yellow and blue regions denote electron accumulation and depletion, respectively.

Supplementary Fig. 26. Bader charge analysis of Sn and O atoms for the O‒OOH bond on SnSe, Na-SnSe and Na,Pb-SnSe.

Table S1. Comparison of represented work of photocatalysis and piezocatalysis for H2O2 production.

| Catalysts | Catalytic conditions | H2O2 evolution rates (mmol·g−1·h−1) | Refs. |
| --- | --- | --- | --- |
| Co-N@G | Sunlight | 0.35 | Nat. Commun. 2023, 14, 2493 |
| ZnIn2S4 nanosheets | Visible-light | 1.7 | J. Am. Chem. Soc. 2023, 145, 27757 |
| COTh-PAFs | Visible-light | 3.9 | Angew. Chem. Int. Ed. 2024, 63, e202402095 |
| CN-PDA | Visible-light | 0.74 | Angew. Chem. Int. Ed. 2024, 63. e202319216 |
| DPT-MOF | Visible-light | 1.7 | J. Am. Chem. Soc. 2024, 146, 11319 |
| COF-S-OH | Visible-light | 10.2 | Angew. Chem. Int. Ed. 2025, 64, e202511024 |
| COF/MoS2 | Visible-light | 8.2 | Angew. Chem. Int. Ed. 2025, 64, e202505491 |
| COF-TPT-Azo | Visible-light | 1.5 | Angew. Chem. Int. Ed. 2024, 63, e202409250 |
| BTT-H3 COF | λ = 467 nm | 1.6 | Nat. Commun. 2025, 16, 503 |
| DBS-C/Z | Visible-light | 1.42 | Angew. Chem. Int. Ed. 2025, e202508226 |
| PBCPs | Visible-light | 2.6 | Angew. Chem. Int. Ed. 2025, 64, e202425054 |
| Si-CDs | Visible-light | 1.4 | Angew. Chem. Int. Ed. 2025, 64, e202509790 |
| TpAP | Visible-light | 2.3 | J. Am. Chem. Soc. 2025, 147, 16, 13618 |
| DT2TA-TAPB | Visible-light | 8.6 | Nat. Commun. 2025, 16, 5658 |
| Au/Cu-Zn3In2S6 | UV-vis light | 5.7 | Adv. Mater. 2025, 37, e11422 |
| O-Ru-ZIS | λ = 350-780 nm | 3.7 | Adv. Mater. 2025, 37, e09867 |
| CTN | Ultrasonication 100 W/40 kHz | 4.1 | Angew. Chem. Int. Ed. 2025, 64, e202419867 |
| CQDs-C3N5 | Ultrasonication 100 W/40 kHz | 5.0 | Angew. Chem. Int. Ed. 2025, 64, e202502390 |
| Sn0.9Se nanosheets | 40 ℃, pure water | 2.6 | Nat. Catal. 2025, 8, 465 |
| Na,Pb-SnSe | ΔT = 120 K seawater | 6.1 | This work |

Table S2. Comparison of H2O2 production activity from seawater with previously reported representative work.

| Catalysts | Catalytic conditions | H2O2 evolution rates in seawater (mmol·g−1·h−1) | H2O2 evolution rates in DI water (mmol·g−1·h−1) | Refs. |
| --- | --- | --- | --- | --- |
| PM-CDs | Visible light | 1.8 | 1.3 | Nat. Commun. 2021, 12, 483 |
| TD-COF | White LED light (400-700 nm) | 3.4 | 4.1 | Angew. Chem. Int. Ed. 2023, 62, e202309624 |
| TB-COF | White LED light (400-700 nm) | 4.1 | 5.2 | ACS Catal. 2024, 14, 4728 |
| 3D COFs | Visible light | 6.9 | 7.9 | Adv. Funct. Mater. 2024, 34, 2411077 |
| ECUT-COF | Xenon lamp light | 2.4 | 3.4 | Nano Lett. 2024, 24, 3819 |
| TBA-COF | Visible light | 8.9 | 3.9 | Adv. Funct. Mater. 35, 2025, 2421514 |
| UP-TP | Visible light | 3.8 | 2.1 | Adv. Funct. Mater. 35, 2025, 2414755 |
| BiOBr | Ultrasonication 110 W/37 kHz | 0.23 | 0.46 | Adv. Funct. Mater. 2024, 34, 2411464 |
| Bi2O2(OH)(NO3) | Ultrasonication 300 W/40 kHz | 0.20 | 0.97 | Adv. Mater. 2025, 37, 2505592 |
| Na,Pb-SnSe | ΔT = 120 ℃ | 6.1 | 0.39 | This work |

References:

(1) Su, B.; Zheng, M.; Lin, W.; Lu, X. F.; Luan, D.; Wang, S.; Lou, X. W. S-scheme Co9S8@Cd0.8Zn0.2S-DETA hierarchical nanocages bearing organic CO2 activators for photocatalytic syngas production. Adv. Energy Mater. 2023, 13 (15), 2203290. DOI: https://doi.org/10.1002/aenm.202203290.

(2) Braun, S.; Salaneck, W. R.; Fahlman, M. Energy-Level Alignment at Organic/Metal and Organic/Organic Interfaces. Adv. Mater. 2009, 21 (14-15), 1450-1472. DOI: https://doi.org/10.1002/adma.200802893.