Supplementary information for

Tuning siRNA packing order in lipid nanoparticles modulates oligonucleotide functional delivery

Supplementary Table S1: Formulation and imaging parameters for size-calibrated fluorescent LNPs. All formulations share Composition A (SM102/DSPC/cholesterol/

PEG₂₀₀₀-PE/PEG₂₀₀₀-DSPE-biotin/DPPE-ATTO488, 50:9.5:38.5:1:0.5:0.5 mol%) and encapsulate eGFP siRNA (sense-3′-Alexa 647N) at N/P = 3. Particle size was tuned by varying the microfluidic parameters and lipid concentration listed below. DLS size values are reported as mean ± s.d. (n = 3 independent preparations). DLS, dynamic light scattering; TFR, total flow rate; FRR, flow rate ratio; TIRF, total internal reflection fluorescence.

|  | LNP 1 | LNP 2 | LNP 3 | LNP 4 | LNP 5 | LNP 6 | LNP 7 |
| --- | --- | --- | --- | --- | --- | --- | --- |
| DLS size (nm) | 39 ± 2 | 54 ± 2 | 64 ± 3 | 76 ± 5 | 78 ± 2 | 99 ± 3 | 102 ± 2 |
| Microfluidics |  |  |  |  |  |  |  |
| Lipid conc. (mg mL−1) | 1 | 1 | 5 | 7 | 10 | 7 | 14 |
| TFR (µL min−1) | 666 | 100 | 100 | 100 | 100 | 100 | 100 |
| FRR | 3 | 3 | 3 | 3 | 3 | 1 | 1 |
| TIRF parameters |  |  |  |  |  |  |  |
| Laser emission | Laser power (%) / exposure time (ms) |  |  |  |  |  |  |
| λex = 488 nm | 8.5 / 1,000 | 8.5 / 750 | 8.5 / 300 | 8.5 / 300 | 8.5 / 250 | 8.5 / 200 | 8.5 / 100 |
| λex = 640 nm | 5 / 1,000 | 5 / 750 | 5 / 300 | 5 / 300 | 5 / 200 | 5 / 150 | 5 / 50 |

Supplementary Table S2: LNP formulations used to assess subpopulation coexistence across compositions and N/P ratios. Compositions A and B differ primary in the identity of the ionizable lipid (SM-102 and ALC-0315, respectively), with a minor shift in the ionizable-lipid-to-cholesterol molar ratio while all remaining components are matched. All formulations were prepared under identical microfluidic conditions (total lipid concentration 5 mg mL⁻¹, TFR 100, FRR 3). TIRF parameters were optimized per formulation to ensure comparable signal-to-noise conditions. DLS size values are reported as mean ± s.d. (n = 3).

|  |  | Comp. A NP1 |  | Comp. A NP3 |  | Comp. A NP6 |  | Comp. B NP3 |  | Comp. A NP3 50% siRNA |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| DLS size (nm) |  | 74 ± 1 |  | 71 ± 2 |  | 70 ± 5 |  | 65 ± 3 |  | 60±3 |  |
| Composition (mol%) |  |  |  |  |  |  |  |  |  |  |  |
| SM-102 |  | 50 |  | 50 |  | 50 |  | – |  | 50 |  |
| ALC-0315 |  | – |  | – |  | – |  | 46.3 |  | – |  |
| DSPC |  | 9.5 |  | 9.5 |  | 9.5 |  | 8.9 |  | 9.5 |  |
| Cholesterol |  | 38.5 |  | 38.5 |  | 38.5 |  | 42.7 |  | 38.5 |  |
| PEG2000-PE |  | 1 |  | 1 |  | 1 |  | – |  | 1 |  |
| ALC-0159 |  | – |  | – |  | – |  | 1.1 |  |  |  |
| PEG2000-DSPE-biotin |  | 0.5 |  | 0.5 |  | 0.5 |  | 0.5 |  | 0.5 |  |
| DPPE-ATTO488 |  | 0.5 |  | 0.5 |  | 0.5 |  | 0.5 |  | 0.5 |  |
| DPPE-ATTO655 |  | – |  | – |  | – |  | – |  | – |  |
| Cargo |  |  |  |  |  |  |  |  |  |  |  |
| eGFP siRNA |  | Sense-3′-Alexa 647N |  | Sense-3′-Alexa 647N |  | Sense-3′-Alexa 647N |  | Sense-3′-Alexa 647N |  | 1:1 labelled and unlabeled |  |
| N/P ratio |  | 1 |  | 3 |  | 6 |  | 3 |  | 3 |  |
| TIRF parameters |  |  |  |  |  |  |  |  |  |  |  |
| Laser emission |  | Laser power (%) / exposure time (ms) |  |  |  |  |  |  |  |  |  |
| λex = 488 nm |  | 10 / 200 |  | 10 / 100 |  | 10 / 75 |  | 10 / 40 |  | 10 / 80 |  |
| λex = 640 nm |  | 12 / 12 |  | 12 / 12 |  | 12 / 12 |  | 12 / 10 |  | 12 / 12 |  |

Supplementary Table S3: Composition and N/P ratio effect in live cell assays. Compositions A and B differ primarily in the identity of the ionizable lipid (SM-102 and ALC-0315, respectively), with a minor shift in the ionizable-lipid-to-cholesterol molar ratio while all remaining components are matched. All formulations were prepared under identical microfluidic conditions (total lipid concentration 5 mg mL⁻¹, TFR 100, FRR 3). DLS size values are reported as mean ± s.d. (n = 3).

|  | Comp. A NP1 | Comp. A NP3 | Comp. A NP6 | Comp. B NP3 |
| --- | --- | --- | --- | --- |
| DLS size (nm) | 84 ± 2 | 77 ± 1 | 63 ± 1 | 78 ± 2 |
| Composition (mol%) |  |  |  |  |
| SM-102 | 50 | 50 | 50 | – |
| ALC-0315 | – | – | – | 46.3 |
| DSPC | 9.5 | 9.5 | 9.5 | 8.9 |
| Cholesterol | 38.5 | 38.5 | 38.5 | 42.7 |
| PEG2000-PE | 1 | 1 | 1 | – |
| ALC-0159 | – | – | – | 1.1 |
| PEG2000-DSPE-biotin | 0.5 | 0.5 | 0.5 | 0.5 |
| DPPE-ATTO488 | – | – | – | – |
| DPPE-ATTO655 | 0.5 | 0.5 | 0.5 | 0.5 |
| Cargo |  |  |  |  |
| Silencer™ eGFP siRNA | All formulations |  |  |  |
| N/P ratio | 1 | 3 | 6 | 3 |

Supplementary Note 1: Size-dependent siRNA partitioning between formulations. Stratifying total siRNA content into five diameter intervals revealed a consistent depletion of Composition A relative to Composition B at smaller and mid-sized particles (0.42× at 0–75 nm; 0.58× at 75–100 nm; 0.72× at 100–180 nm; 0.63× at 180–320 nm), with inversion only in the largest bin (>320 nm; 3.15×). While bulk dosing based on input RNA concentration captures differences in mean loading, it fails to resolve this size-dependent cargo partitioning, which may have important implications for functional delivery, as discussed in the main text.

Supplementary Figure S1 | High-throughput single-particle imaging of lipid nanoparticles. Total internal reflection fluorescence (TIRF) montage of 4 replicates for a total of 14,400 fields of view (FOVs) acquired in the lipid fluorescence channel (ATTO488, cyan), representing more than 0.5 million individual LNPs. Progressive zoom-ins from the full dataset (left) through an intermediate grid of FOVs (middle) to a single representative FOV (right) illustrate the imaging scale. Dynamic contrast of the left and middle panels has been adjusted for visualization clarity. Each diffraction-limited spot corresponds to a single LNP. These data underpin the fluorescence–diameter calibration and single-particle heterogeneity analyses presented in the main text.

Supplementary Figure S2 | Bulk size characterization of LNP formulations by dynamic light scattering. a, Mode hydrodynamic diameters of the seven LNP preparations used for single-particle fluorescence calibration (Supplementary Table S1). Bars represent the mode diameter from number-weighted size distributions; error bars denote s.d. (n = 3–4 technical replicates). Bar shading progresses from light blue (preparation 1, smallest) to dark blue (preparation 7, largest). b–h, Number-weighted size distributions for preparations 1–7, respectively. Individual replicates are shown as dashed lines; the shaded envelope indicates ± 1 s.d. across replicates. Distributions are monomodal across all formulations, with mode diameters spanning approximately 40–110 nm. These bulk measurements provided the physical reference for converting fluorescence intensities into particle size.

Supplementary Figure S3: Exposure-time dependence of single-molecule Alexa 647 fluorescence intensity. a–f, Single-molecule intensity distributions of Alexa 647-biotin immobilized on PLL-PEG-biotin/NeutrAvidin-functionalized coverslips, imaged under 640 nm excitation at six exposure times (50, 100, 400, 500, 700 and 1,000 ms). Light blue histograms show the integrated fluorescence intensity of individual molecules; black curves are log-normal fits. Insets report the log-normal mode ± s.d., histogram mode, peak value and number of molecules analysed (N > 105,000 per condition; three independent experiments). g, Log–log plot of log-normal mode intensity versus exposure time. Blue circles indicate the mode; error bars denote s.d. across three independent experiments. The orange dashed line is a linear fit in natural-log space (ln y = 0.79 ln x + 6.45). h, Same data displayed on linear axes with the corresponding power-law fit (y = 632.4 x0.79), showing a sublinear increase in detected signal with exposure time. This calibration was used to correct exposure-dependent intensity deviations in downstream siRNA quantification.

Supplementary Figure S4: Control for fluorophore self-quenching in single-particle siRNA loading measurements. a–c, Two-dimensional kernel density estimate (KDE) contour plots of labelled siRNA copy number versus LNP radius for Composition A (N/P 3) formulated with 50% Alexa 647N-labelled and 50% unlabelled eGFP-targeting siRNA, shown for three independent technical replicates (approximately 100,000–200,000 particles per replicate). Dashed lines represent power-law fits (y = AxB) to the low-order subpopulation (blue), the high-order subpopulation (green) and the overall population (black). The joint size-loading distributions consistently resolve two distinct packing subpopulations across all replicates, demonstrating that the observed bimodality does not arise from fluorophore self-quenching but reflects intrinsic heterogeneity in siRNA packing within the LNP population.

Supplementary Figure S5: Replicate analysis of siRNA packing subpopulations for Composition A (N/P 3). a-d, Two-dimensional kernel density estimates of siRNA copy number versus LNP diameter for four independent technical replicates (approximately 100,000–200,000 particles per replicate). Power-law fits (y = AxB) are shown for the low-order subpopulation (blue), the high-order subpopulation (green) and the overall population (black dashed). All replicates consistently resolve two distinct loading subpopulations. e, Gaussian mixture model (GMM) analysis of replicate 1, shown as representative, across 18 diameter percentile bins. Top row: Scatter plots of siRNA copy number versus diameter (log scale), colored by local density (purple to yellow); white dashed lines mark the percentile bin whose siRNA copy-number data are shown in the corresponding histogram below. Middle row: log-transformed siRNA copy-number distributions within each bin (grey histograms) overlaid with individual Gaussian components (red curves) and the summed fit (black curves). Bottom row: Bayesian information criterion (BIC) as a function of the number of mixture components (1–4); the minimum indicates the preferred model.

Supplementary Figure S6: Cryo-TEM of siRNA-LNP morphologies across compositions and N/P ratios. Representative cryogenic transmission electron micrographs of siRNA-loaded LNP formulations. a, Comp B (N/P 3): Coexisting multilamellar and inverse-hexagonal phases are visible; the magenta box highlights an inverse-hexagonal particle and the red box a multilamellar particle with concentric bilayer order. Amorphous and bleb-like morphologies are also present. Scale bar, 50 nm. b, Comp. A (N/P 1): the population is dominated by multilamellar vesicles. The green box highlights concentric bilayers consistent with siRNA intercalated between lipid layers. Scale bar, 100 nm. c, Comp. A (N/P 3): a heterogeneous population comprising multilamellar, amorphous and bleb-like particles. Scale bar, 100 nm. d, Comp. A (N/P 6): predominantly amorphous, electron-lucent particles with occasional bleb-like surface lobules; the blue box highlights a representative low-order particle. Scale bar, 100 nm.

Supplementary Figure S7: Log-log scaling of siRNA copy number with LNP radius for Composition A (N/P 3). a-d, Two-dimensional scatter plot (log-log axes) of siRNA copy number versus LNP radius for technical replicates 1–4. Color scale (purple to yellow) indicates particle count per bin. Power-law fits are shown for the high-order subpopulation (green), the low-order subpopulation (blue) and the overall population (black dashed). a, Enlarged view of replicate 1. Green and blue circles and vertical bars denote the Gaussian mixture model component means ± s.d. within each radius bin; the legend denotes the power-law fits in the log space. Two distinct scaling regimes are resolved across all four replicates, consistent with the coexistence of high-order and low-order packing subpopulations.

Supplementary Figure S8: Stochastic merger model of siRNA-LNP scaling behavior. a, Schematic of the stochastic merger of spherical volumes (SMSV) model. Precursor vesicles, cargo-loaded (dark grey) and empty (light grey), coalesce into progressively larger LNPs. The fraction of initially loaded precursors determines the cargo-size scaling relationship (dashed line). b, Simulated cargo copies number (n cargo) versus LNP radius for seven fractions of initially empty precursors (0–99%, colored as indicated in the legend). Dashed lines show power-law fits (C = ArB) with exponents annotated in the upper left. Complete initial loading (0% empty, blue) yields near-cubic scaling (B ≈ 2.97), whereas increasing the empty fraction progressively reduces the exponent below 2.

Supplementary Figure S9: Replicate analysis of siRNA packing subpopulations for Composition B (N/P 3). a-d, Two-dimensional kernel density estimates of siRNA copy number versus LNP diameter for four independent technical replicates (approximately 100,000–200,000 particles per replicate). Power-law fits (y = AxB) are shown for the low-order subpopulation (blue), the high-order subpopulation (green) and the overall population (black dashed). All replicates consistently resolve two distinct loading subpopulations. e, Gaussian mixture model (GMM) analysis of replicate 1, shown as representative, across 18 diameter percentile bins. Top row: Scatter plots of siRNA copy number versus diameter (log scale), colored by local density (purple to yellow); white dashed lines mark the percentile bin whose siRNA copy-number data are shown in the corresponding histogram below. Middle row: log-transformed siRNA copy-number distributions within each bin (grey histograms) overlaid with individual Gaussian components (red curves) and the summed fit (black curves). Bottom row: Bayesian information criterion (BIC) as a function of the number of mixture components (1–4); the minimum indicates the preferred model.

Supplementary Figure S10: Time-lapse imaging of siRNA-mediated d2eGFP knockdown in live HEK293 cells. Representative spinning-disk confocal fluorescence images of HEK293-d2eGFP cells treated with siRNA-loaded LNPs. Columns correspond to treatment conditions (from left to right: untreated control, Composition A at N/P 1, 3 and 6, and Composition B at N/P 3). Rows show six time points sampled from a 24-hour imaging series acquired at 20-minute intervals (frames 1, 15, 29, 43, 57 and 72, corresponding to approximately 0, 5, 9, 14, 19 and 24 hours after treatment). The maximum-intensity z-plane for eGFP fluorescence (green) is displayed; brightness and contrast settings are identical across all panels. Scale bars, 50 μm.

Supplementary Figure S11: Normalized d2eGFP fluorescence trajectories during siRNA-mediated knockdown. Control-normalized mean eGFP fluorescence intensity over 24 hours (Δt = 20 min) for HEK293-d2eGFP cells treated with siRNA-loaded LNPs. Solid lines show mean trajectories for the untreated control (blue, n = 4 replicates), Composition A at N/P 1 (orange), N/P 3 (green) and N/P 6 (red), and Composition B at N/P 3 (purple) (n = 3 replicates each). Shaded envelopes indicate ± 1 s.d. across replicates. All trajectories are normalized to the pooled control at each time point and scaled to unity at t₀, isolating relative silencing dynamics from differences in starting fluorescence. The horizontal dashed grey line marks the control baseline (relative intensity = 1).

Supplementary Figure S12: Lattice light-sheet quantification of internalized LNP copy number. a, Representative three-dimensional lattice light-sheet microscopy (LLSM) volume rendering of Composition B (N/P 3) LNPs (magenta) immobilized in agarose, used for point spread function calibration and single-particle intensity extraction. Scale bar, 20 μm. b, Log-transformed integrated fluorescence intensity distributions of single LNPs from three technical replicates (histograms, dark to light red); dashed curves show Gaussian fits in log space used to derive calibration parameters. c, Volumetric LLSM rendering of d2eGFP-HEK293 cells (cyan) after 150 min incubation with Composition B (N/P 3) LNPs (magenta). Three-dimensional cell segmentation masks were derived from the eGFP signal. Scale bar, 20 μm. d, Distributions of total background-corrected LNP fluorescence intensity per cell for four biological replicates (dark to light blue), plotted on a logarithmic intensity axis. e, Comparison of single-particle intensity (pink, from agarose calibration) and per-cell internalized LNP intensity (blue, from live-cell experiments), both peak-normalized. The cellular distribution is shifted to higher values and broadened, consistent with internalization of multiple LNPs per cell. f, Internalized LNP copy-number distributions for Composition B (N/P 3, blue) and Composition A (N/P 3, green), obtained by dividing each cell's integrated LNP signal by the mean single-particle brightness. Dashed vertical lines indicate mean copy numbers (302±37 and 123±4, respectively). Composition B (N/P 3) shows higher uptake than Composition A (N/P 3) under identical conditions.

Supplementary Figure 13: DLS characterization of LNP formulations used in live-cell experiments. a, Mode hydrodynamic diameters of the four LNP formulations used for live-cell knockdown assays: Composition A at N/P 1, 3 and 6, and Composition B at N/P 3. Bars represent the mode diameter from number-weighted size distributions; error bars denote s.d. (n = 3–4 technical replicates). Bar shading scales with mode diameter from light pink (Composition A N/P 6, smallest) to dark red (Composition A N/P 1, largest). b–e, Number-weighted size distributions for Composition A at N/P 1 (b), N/P 3 (c) and N/P 6 (d), and Composition B at N/P 3 (e), respectively. Individual replicates are shown as dashed lines; the shaded envelope indicates ± 1 s.d. across replicates. All formulations display monomodal distributions with mode diameters spanning approximately 63–84 nm.

Supplementary Figure S14: Replicate analysis of siRNA packing subpopulations for Composition A (N/P 1). a-d, Two-dimensional kernel density estimates of siRNA copy number versus LNP diameter for four independent technical replicates (approximately 100,000–200,000 particles per replicate). Power-law fits (y = AxB) are shown for the low-order subpopulation (blue), the high-order subpopulation (green) and the overall population (black dashed). All replicates consistently resolve two distinct loading subpopulations. e, Gaussian mixture model (GMM) analysis of replicate 1, shown as representative, across 18 diameter percentile bins. Top row: Scatter plots of siRNA copy number versus diameter (log scale), colored by local density (purple to yellow); white dashed lines mark the percentile bin whose siRNA copy-number data are shown in the corresponding histogram below. Middle row: log-transformed siRNA copy-number distributions within each bin (grey histograms) overlaid with individual Gaussian components (red curves) and the summed fit (black curves). Bottom row: Bayesian information criterion (BIC) as a function of the number of mixture components (1–4); the minimum indicates the preferred model.

Supplementary Figure S15: Replicate analysis of siRNA packing subpopulations for Composition A (N/P 6). a-d, Two-dimensional kernel density estimates of siRNA copy number versus LNP diameter for four independent technical replicates (approximately 100,000–200,000 particles per replicate). Power-law fits (y = AxB) are shown for the low-order subpopulation (blue), the high-order subpopulation (green) and the overall population (black dashed). All replicates consistently resolve two distinct loading subpopulations. e, Gaussian mixture model (GMM) analysis of replicate 1, shown as representative, across 18 diameter percentile bins. Top row: Scatter plots of siRNA copy number versus diameter (log scale), colored by local density (purple to yellow); white dashed lines mark the percentile bin whose siRNA copy-number data are shown in the corresponding histogram below. Middle row: log-transformed siRNA copy-number distributions within each bin (grey histograms) overlaid with individual Gaussian components (red curves) and the summed fit (black curves). Bottom row: Bayesian information criterion (BIC) as a function of the number of mixture components (1–4); the minimum indicates the preferred model.