data_shelx

_audit_creation_method            'SHELXL-2016/6'

_shelx_SHELXL_version_number      '2016/6'

_chemical_name_systematic         ?

_chemical_name_common             ?

_chemical_melting_point           ?

_chemical_formula_moiety          ?

_chemical_formula_sum

'Al0.01 Ca0.01 Cr0.92 Fe1.31 Mg0.03 Mn0.02 Ni0.03 O4 Si0.08 Ti0.02 Zn0.01'

_chemical_formula_weight          193.12

loop_

_atom_type_symbol

_atom_type_description

_atom_type_scat_dispersion_real

_atom_type_scat_dispersion_imag

_atom_type_scat_source

'O'  'O'   0.0106   0.0060

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Mg'  'Mg'   0.0486   0.0363

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Al'  'Al'   0.0645   0.0514

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Si'  'Si'   0.0817   0.0704

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Ti'  'Ti'   0.2776   0.4457

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Cr'  'Cr'   0.3209   0.6236

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Mn'  'Mn'   0.3368   0.7283

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Fe'  'Fe'   0.3463   0.8444

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Ni'  'Ni'   0.3393   1.1124

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Zn'  'Zn'   0.2839   1.4301

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

'Ca'  'Ca'   0.2262   0.3064

'International Tables Vol C Tables 4.2.6.8 and 6.1.1.4'

_space_group_crystal_system       cubic

_space_group_IT_number            227

_space_group_name_H-M_alt         'F d -3 m'

_space_group_name_Hall            '-F 4vw 2vw 3'

_shelx_space_group_comment

;

The symmetry employed for this shelxl refinement is uniquely defined

by the following loop, which should always be used as a source of

symmetry information in preference to the above space-group names.

They are only intended as comments.

;

loop_

_space_group_symop_operation_xyz

'x, y, z'

'-x+1/4, -y+1/4, z'

'x, -y+1/4, -z+1/4'

'-x+1/4, y, -z+1/4'

'z, x, y'

'y, z, x'

'-z+1/4, -x+1/4, y'

'-y+1/4, z, -x+1/4'

'z, -x+1/4, -y+1/4'

'-y+1/4, -z+1/4, x'

'-z+1/4, x, -y+1/4'

'y, -z+1/4, -x+1/4'

'-y, -x, -z'

'y+1/4, x+1/4, -z'

'y+1/4, -x, z+1/4'

'-y, x+1/4, z+1/4'

'-x, -z, -y'

'-z, -y, -x'

'x+1/4, z+1/4, -y'

'-z, y+1/4, x+1/4'

'x+1/4, -z, y+1/4'

'z+1/4, y+1/4, -x'

'-x, z+1/4, y+1/4'

'z+1/4, -y, x+1/4'

'x, y+1/2, z+1/2'

'-x+1/4, -y+3/4, z+1/2'

'x, -y+3/4, -z+3/4'

'-x+1/4, y+1/2, -z+3/4'

'z, x+1/2, y+1/2'

'y, z+1/2, x+1/2'

'-z+1/4, -x+3/4, y+1/2'

'-y+1/4, z+1/2, -x+3/4'

'z, -x+3/4, -y+3/4'

'-y+1/4, -z+3/4, x+1/2'

'-z+1/4, x+1/2, -y+3/4'

'y, -z+3/4, -x+3/4'

'-y, -x+1/2, -z+1/2'

'y+1/4, x+3/4, -z+1/2'

'y+1/4, -x+1/2, z+3/4'

'-y, x+3/4, z+3/4'

'-x, -z+1/2, -y+1/2'

'-z, -y+1/2, -x+1/2'

'x+1/4, z+3/4, -y+1/2'

'-z, y+3/4, x+3/4'

'x+1/4, -z+1/2, y+3/4'

'z+1/4, y+3/4, -x+1/2'

'-x, z+3/4, y+3/4'

'z+1/4, -y+1/2, x+3/4'

'x+1/2, y, z+1/2'

'-x+3/4, -y+1/4, z+1/2'

'x+1/2, -y+1/4, -z+3/4'

'-x+3/4, y, -z+3/4'

'z+1/2, x, y+1/2'

'y+1/2, z, x+1/2'

'-z+3/4, -x+1/4, y+1/2'

'-y+3/4, z, -x+3/4'

'z+1/2, -x+1/4, -y+3/4'

'-y+3/4, -z+1/4, x+1/2'

'-z+3/4, x, -y+3/4'

'y+1/2, -z+1/4, -x+3/4'

'-y+1/2, -x, -z+1/2'

'y+3/4, x+1/4, -z+1/2'

'y+3/4, -x, z+3/4'

'-y+1/2, x+1/4, z+3/4'

'-x+1/2, -z, -y+1/2'

'-z+1/2, -y, -x+1/2'

'x+3/4, z+1/4, -y+1/2'

'-z+1/2, y+1/4, x+3/4'

'x+3/4, -z, y+3/4'

'z+3/4, y+1/4, -x+1/2'

'-x+1/2, z+1/4, y+3/4'

'z+3/4, -y, x+3/4'

'x+1/2, y+1/2, z'

'-x+3/4, -y+3/4, z'

'x+1/2, -y+3/4, -z+1/4'

'-x+3/4, y+1/2, -z+1/4'

'z+1/2, x+1/2, y'

'y+1/2, z+1/2, x'

'-z+3/4, -x+3/4, y'

'-y+3/4, z+1/2, -x+1/4'

'z+1/2, -x+3/4, -y+1/4'

'-y+3/4, -z+3/4, x'

'-z+3/4, x+1/2, -y+1/4'

'y+1/2, -z+3/4, -x+1/4'

'-y+1/2, -x+1/2, -z'

'y+3/4, x+3/4, -z'

'y+3/4, -x+1/2, z+1/4'

'-y+1/2, x+3/4, z+1/4'

'-x+1/2, -z+1/2, -y'

'-z+1/2, -y+1/2, -x'

'x+3/4, z+3/4, -y'

'-z+1/2, y+3/4, x+1/4'

'x+3/4, -z+1/2, y+1/4'

'z+3/4, y+3/4, -x'

'-x+1/2, z+3/4, y+1/4'

'z+3/4, -y+1/2, x+1/4'

'-x, -y, -z'

'x-1/4, y-1/4, -z'

'-x, y-1/4, z-1/4'

'x-1/4, -y, z-1/4'

'-z, -x, -y'

'-y, -z, -x'

'z-1/4, x-1/4, -y'

'y-1/4, -z, x-1/4'

'-z, x-1/4, y-1/4'

'y-1/4, z-1/4, -x'

'z-1/4, -x, y-1/4'

'-y, z-1/4, x-1/4'

'y, x, z'

'-y-1/4, -x-1/4, z'

'-y-1/4, x, -z-1/4'

'y, -x-1/4, -z-1/4'

'x, z, y'

'z, y, x'

'-x-1/4, -z-1/4, y'

'z, -y-1/4, -x-1/4'

'-x-1/4, z, -y-1/4'

'-z-1/4, -y-1/4, x'

'x, -z-1/4, -y-1/4'

'-z-1/4, y, -x-1/4'

'-x, -y+1/2, -z+1/2'

'x-1/4, y+1/4, -z+1/2'

'-x, y+1/4, z+1/4'

'x-1/4, -y+1/2, z+1/4'

'-z, -x+1/2, -y+1/2'

'-y, -z+1/2, -x+1/2'

'z-1/4, x+1/4, -y+1/2'

'y-1/4, -z+1/2, x+1/4'

'-z, x+1/4, y+1/4'

'y-1/4, z+1/4, -x+1/2'

'z-1/4, -x+1/2, y+1/4'

'-y, z+1/4, x+1/4'

'y, x+1/2, z+1/2'

'-y-1/4, -x+1/4, z+1/2'

'-y-1/4, x+1/2, -z+1/4'

'y, -x+1/4, -z+1/4'

'x, z+1/2, y+1/2'

'z, y+1/2, x+1/2'

'-x-1/4, -z+1/4, y+1/2'

'z, -y+1/4, -x+1/4'

'-x-1/4, z+1/2, -y+1/4'

'-z-1/4, -y+1/4, x+1/2'

'x, -z+1/4, -y+1/4'

'-z-1/4, y+1/2, -x+1/4'

'-x+1/2, -y, -z+1/2'

'x+1/4, y-1/4, -z+1/2'

'-x+1/2, y-1/4, z+1/4'

'x+1/4, -y, z+1/4'

'-z+1/2, -x, -y+1/2'

'-y+1/2, -z, -x+1/2'

'z+1/4, x-1/4, -y+1/2'

'y+1/4, -z, x+1/4'

'-z+1/2, x-1/4, y+1/4'

'y+1/4, z-1/4, -x+1/2'

'z+1/4, -x, y+1/4'

'-y+1/2, z-1/4, x+1/4'

'y+1/2, x, z+1/2'

'-y+1/4, -x-1/4, z+1/2'

'-y+1/4, x, -z+1/4'

'y+1/2, -x-1/4, -z+1/4'

'x+1/2, z, y+1/2'

'z+1/2, y, x+1/2'

'-x+1/4, -z-1/4, y+1/2'

'z+1/2, -y-1/4, -x+1/4'

'-x+1/4, z, -y+1/4'

'-z+1/4, -y-1/4, x+1/2'

'x+1/2, -z-1/4, -y+1/4'

'-z+1/4, y, -x+1/4'

'-x+1/2, -y+1/2, -z'

'x+1/4, y+1/4, -z'

'-x+1/2, y+1/4, z-1/4'

'x+1/4, -y+1/2, z-1/4'

'-z+1/2, -x+1/2, -y'

'-y+1/2, -z+1/2, -x'

'z+1/4, x+1/4, -y'

'y+1/4, -z+1/2, x-1/4'

'-z+1/2, x+1/4, y-1/4'

'y+1/4, z+1/4, -x'

'z+1/4, -x+1/2, y-1/4'

'-y+1/2, z+1/4, x-1/4'

'y+1/2, x+1/2, z'

'-y+1/4, -x+1/4, z'

'-y+1/4, x+1/2, -z-1/4'

'y+1/2, -x+1/4, -z-1/4'

'x+1/2, z+1/2, y'

'z+1/2, y+1/2, x'

'-x+1/4, -z+1/4, y'

'z+1/2, -y+1/4, -x-1/4'

'-x+1/4, z+1/2, -y-1/4'

'-z+1/4, -y+1/4, x'

'x+1/2, -z+1/4, -y-1/4'

'-z+1/4, y+1/2, -x-1/4'

_cell_length_a                    8.34222(6)

_cell_length_b                    8.34222(6)

_cell_length_c                    8.34222(6)

_cell_angle_alpha                 90

_cell_angle_beta                  90

_cell_angle_gamma                 90

_cell_volume                      580.556(13)

_cell_formula_units_Z             8

_cell_measurement_temperature     293(2)

_cell_measurement_reflns_used     8908

_cell_measurement_theta_min       4.2050

_cell_measurement_theta_max       64.7090

_exptl_crystal_description        block

_exptl_crystal_colour             black

_exptl_crystal_density_meas       ?

_exptl_crystal_density_method     ?

_exptl_crystal_density_diffrn     4.419

_exptl_crystal_F_000              736

_exptl_transmission_factor_min    ?

_exptl_transmission_factor_max    ?

_exptl_crystal_size_max           0.059

_exptl_crystal_size_mid           0.045

_exptl_crystal_size_min           0.041

_shelx_estimated_absorpt_T_min    ?

_shelx_estimated_absorpt_T_max    ?

_exptl_absorpt_coefficient_mu     10.188

_exptl_absorpt_correction_T_min   0.665

_exptl_absorpt_correction_T_max   0.782

_exptl_absorpt_correction_type            gaussian

_exptl_absorpt_process_details

;

CrysAlisPro 1.171.43.76a (Rigaku Oxford Diffraction, 2023)

Numerical absorption correction based on gaussian integration over

a multifaceted crystal model

Empirical absorption correction using spherical harmonics,

implemented in SCALE3 ABSPACK scaling algorithm.

;

_oxdiff_exptl_absorpt_empirical_full_min           0.827

_oxdiff_exptl_absorpt_empirical_full_max           1.297

_oxdiff_exptl_absorpt_empirical_details

;

Empirical correction (ABSPACK) includes:

- Absorption correction using spherical harmonics

- Frame scaling

;

_diffrn_ambient_temperature       293(2)

_diffrn_radiation_wavelength      0.71073

_diffrn_radiation_type            MoK\a

_diffrn_source 'micro-focus sealed X-ray tube'

_diffrn_source_type 'PhotonJet (Mo) X-ray Source'

_diffrn_measurement_device 'four-circle diffractometer'

_diffrn_measurement_device_type 'XtaLAB Synergy, Dualflex, HyPix'

_diffrn_detector 'Hybrid Pixel Array Detector'

_diffrn_detector_type HyPix

_diffrn_detector_area_resol_mean 10.0000

_diffrn_reflns_number             13568

_diffrn_reflns_av_unetI/netI      0.0068

_diffrn_reflns_av_R_equivalents   0.0318

_diffrn_reflns_limit_h_min        -21

_diffrn_reflns_limit_h_max        21

_diffrn_reflns_limit_k_min        -14

_diffrn_reflns_limit_k_max        21

_diffrn_reflns_limit_l_min        -20

_diffrn_reflns_limit_l_max        21

_diffrn_reflns_theta_min          4.231

_diffrn_reflns_theta_max          64.912

_diffrn_reflns_theta_full         25.242

_diffrn_measured_fraction_theta_max   1.000

_diffrn_measured_fraction_theta_full  1.000

_diffrn_reflns_Laue_measured_fraction_max    1.000

_diffrn_reflns_Laue_measured_fraction_full   1.000

_diffrn_reflns_point_group_measured_fraction_max   1.000

_diffrn_reflns_point_group_measured_fraction_full  1.000

_reflns_number_total              279

_reflns_number_gt                 269

_reflns_threshold_expression      'I > 2\s(I)'

_reflns_Friedel_coverage          0.000

_reflns_Friedel_fraction_max      .

_reflns_Friedel_fraction_full     .

_reflns_special_details

;

Reflections were merged by SHELXL according to the crystal

class for the calculation of statistics and refinement.

_reflns_Friedel_fraction is defined as the number of unique

Friedel pairs measured divided by the number that would be

possible theoretically, ignoring centric projections and

systematic absences.

;

_computing_data_collection     'CrysAlisPro system (CCD 40.84a 64-bit (release 31-07-2020))'

_computing_cell_refinement     'CrysAlisPro 1.171.43.76a (Rigaku OD, 2023)'

_computing_data_reduction      'CrysAlisPro 1.171.43.76a (Rigaku OD, 2023)'

_computing_structure_solution     ?

_computing_structure_refinement 'SHELXL-2016/6 (Sheldrick, 2016)'

_computing_molecular_graphics     ?

_computing_publication_material   ?

_refine_special_details           ?

_refine_ls_structure_factor_coef  Fsqd

_refine_ls_matrix_type            full

_refine_ls_weighting_scheme       calc

_refine_ls_weighting_details

'w=1/[\s^2^(Fo^2^)+(0.0327P)^2^+1.1448P] where P=(Fo^2^+2Fc^2^)/3'

_atom_sites_solution_primary      ?

_atom_sites_solution_secondary    ?

_atom_sites_solution_hydrogens    .

_refine_ls_hydrogen_treatment     undef

_refine_ls_extinction_method      'SHELXL-2016/6 (Sheldrick 2016)'

_refine_ls_extinction_coef        0.0032(7)

_refine_ls_extinction_expression

'Fc^*^=kFc[1+0.001xFc^2^\l^3^/sin(2\q)]^-1/4^'

_refine_ls_number_reflns          279

_refine_ls_number_parameters      10

_refine_ls_number_restraints      0

_refine_ls_R_factor_all           0.0218

_refine_ls_R_factor_gt            0.0214

_refine_ls_wR_factor_ref          0.0577

_refine_ls_wR_factor_gt           0.0576

_refine_ls_goodness_of_fit_ref    1.149

_refine_ls_restrained_S_all       1.149

_refine_ls_shift/su_max           0.000

_refine_ls_shift/su_mean          0.000

loop_

_atom_site_label

_atom_site_type_symbol

_atom_site_fract_x

_atom_site_fract_y

_atom_site_fract_z

_atom_site_U_iso_or_equiv

_atom_site_adp_type

_atom_site_occupancy

_atom_site_site_symmetry_order

_atom_site_calc_flag

_atom_site_refinement_flags_posn

_atom_site_refinement_flags_adp

_atom_site_refinement_flags_occupancy

_atom_site_disorder_assembly

_atom_site_disorder_group

Si1 Si 0.125000 0.125000 0.125000 0.00875(7) Uani 0.0797 24 d S T P . .

Zn1 Zn 0.125000 0.125000 0.125000 0.00875(7) Uani 0.0077 24 d S T P . .

Mg1 Mg 0.125000 0.125000 0.125000 0.00875(7) Uani 0.0336 24 d S T P . .

Mn1 Mn 0.125000 0.125000 0.125000 0.00875(7) Uani 0.0223 24 d S T P . .

Fe1 Fe 0.125000 0.125000 0.125000 0.00875(7) Uani 0.6519 24 d S T P . .

Cr2 Cr 0.500000 0.500000 0.500000 0.00535(6) Uani 0.4598 12 d S T P . .

Al2 Al 0.500000 0.500000 0.500000 0.00535(6) Uani 0.0059 12 d S T P . .

Ti2 Ti 0.500000 0.500000 0.500000 0.00535(6) Uani 0.0103 12 d S T P . .

Ni2 Ni 0.500000 0.500000 0.500000 0.00535(6) Uani 0.0173 12 d S T P . .

Ca2 Ca 0.500000 0.500000 0.500000 0.00535(6) Uani 0.0059 12 d S T P . .

Fe2 Fe 0.500000 0.500000 0.500000 0.00535(6) Uani 0.3259 12 d S T P . .

O O 0.26224(6) 0.26224(6) 0.26224(6) 0.00828(10) Uani 1 6 d S T P . .

loop_

_atom_site_aniso_label

_atom_site_aniso_U_11

_atom_site_aniso_U_22

_atom_site_aniso_U_33

_atom_site_aniso_U_23

_atom_site_aniso_U_13

_atom_site_aniso_U_12

Si1 0.00875(7) 0.00875(7) 0.00875(7) 0.000 0.000 0.000

Zn1 0.00875(7) 0.00875(7) 0.00875(7) 0.000 0.000 0.000

Mg1 0.00875(7) 0.00875(7) 0.00875(7) 0.000 0.000 0.000

Mn1 0.00875(7) 0.00875(7) 0.00875(7) 0.000 0.000 0.000

Fe1 0.00875(7) 0.00875(7) 0.00875(7) 0.000 0.000 0.000

Cr2 0.00535(6) 0.00535(6) 0.00535(6) -0.00018(2) -0.00018(2) -0.00018(2)

Al2 0.00535(6) 0.00535(6) 0.00535(6) -0.00018(2) -0.00018(2) -0.00018(2)

Ti2 0.00535(6) 0.00535(6) 0.00535(6) -0.00018(2) -0.00018(2) -0.00018(2)

Ni2 0.00535(6) 0.00535(6) 0.00535(6) -0.00018(2) -0.00018(2) -0.00018(2)

Ca2 0.00535(6) 0.00535(6) 0.00535(6) -0.00018(2) -0.00018(2) -0.00018(2)

Fe2 0.00535(6) 0.00535(6) 0.00535(6) -0.00018(2) -0.00018(2) -0.00018(2)

O 0.00828(10) 0.00828(10) 0.00828(10) -0.00050(10) -0.00050(10) -0.00050(10)

_geom_special_details

;

All esds (except the esd in the dihedral angle between two l.s. planes)

are estimated using the full covariance matrix.  The cell esds are taken

into account individually in the estimation of esds in distances, angles

and torsion angles; correlations between esds in cell parameters are only

used when they are defined by crystal symmetry.  An approximate (isotropic)

treatment of cell esds is used for estimating esds involving l.s. planes.

;

loop_

_geom_bond_atom_site_label_1

_geom_bond_atom_site_label_2

_geom_bond_distance

_geom_bond_site_symmetry_2

_geom_bond_publ_flag

Si1 O 1.9829(9) 4 ?

Si1 O 1.9829(9) 2 ?

Si1 O 1.9829(9) 3 ?

Si1 O 1.9830(9) . ?

Cr2 O 1.9887(5) 123_655 ?

Cr2 O 1.9887(5) 27 ?

Cr2 O 1.9887(5) 148_565 ?

Cr2 O 1.9887(5) 52 ?

Cr2 O 1.9887(5) 170_556 ?

Cr2 O 1.9887(5) 74 ?

Cr2 Cr2 2.949419(19) 3_566 ?

Cr2 Cr2 2.94942(2) 52 ?

Cr2 Cr2 2.949419(19) 4_656 ?

Cr2 Cr2 2.94942(2) 74 ?

Cr2 Cr2 2.949419(19) 2_665 ?

Cr2 Cr2 2.949419(19) 27 ?

loop_

_geom_angle_atom_site_label_1

_geom_angle_atom_site_label_2

_geom_angle_atom_site_label_3

_geom_angle

_geom_angle_site_symmetry_1

_geom_angle_site_symmetry_3

_geom_angle_publ_flag

O Si1 O 109.5 4 2 ?

O Si1 O 109.5 4 3 ?

O Si1 O 109.5 2 3 ?

O Si1 O 109.5 4 . ?

O Si1 O 109.5 2 . ?

O Si1 O 109.471(1) 3 . ?

O Cr2 O 180.0 123_655 27 ?

O Cr2 O 83.97(3) 123_655 148_565 ?

O Cr2 O 96.03(3) 27 148_565 ?

O Cr2 O 96.03(3) 123_655 52 ?

O Cr2 O 83.97(3) 27 52 ?

O Cr2 O 180.0 148_565 52 ?

O Cr2 O 83.97(3) 123_655 170_556 ?

O Cr2 O 96.03(3) 27 170_556 ?

O Cr2 O 83.97(3) 148_565 170_556 ?

O Cr2 O 96.03(3) 52 170_556 ?

O Cr2 O 96.03(3) 123_655 74 ?

O Cr2 O 83.97(3) 27 74 ?

O Cr2 O 96.03(3) 148_565 74 ?

O Cr2 O 83.97(3) 52 74 ?

O Cr2 O 180.0 170_556 74 ?

O Cr2 Cr2 85.84(2) 123_655 3_566 ?

O Cr2 Cr2 94.16(2) 27 3_566 ?

O Cr2 Cr2 42.138(15) 148_565 3_566 ?

O Cr2 Cr2 137.862(15) 52 3_566 ?

O Cr2 Cr2 42.138(15) 170_556 3_566 ?

O Cr2 Cr2 137.862(15) 74 3_566 ?

O Cr2 Cr2 137.862(15) 123_655 52 ?

O Cr2 Cr2 42.138(15) 27 52 ?

O Cr2 Cr2 94.16(2) 148_565 52 ?

O Cr2 Cr2 85.84(2) 52 52 ?

O Cr2 Cr2 137.862(15) 170_556 52 ?

O Cr2 Cr2 42.138(15) 74 52 ?

Cr2 Cr2 Cr2 120.0 3_566 52 ?

O Cr2 Cr2 42.138(15) 123_655 4_656 ?

O Cr2 Cr2 137.862(15) 27 4_656 ?

O Cr2 Cr2 85.84(2) 148_565 4_656 ?

O Cr2 Cr2 94.16(2) 52 4_656 ?

O Cr2 Cr2 42.138(15) 170_556 4_656 ?

O Cr2 Cr2 137.862(15) 74 4_656 ?

Cr2 Cr2 Cr2 60.0 3_566 4_656 ?

Cr2 Cr2 Cr2 180.0 52 4_656 ?

O Cr2 Cr2 137.862(15) 123_655 74 ?

O Cr2 Cr2 42.138(15) 27 74 ?

O Cr2 Cr2 137.862(15) 148_565 74 ?

O Cr2 Cr2 42.138(15) 52 74 ?

O Cr2 Cr2 94.16(2) 170_556 74 ?

O Cr2 Cr2 85.84(2) 74 74 ?

Cr2 Cr2 Cr2 120.0 3_566 74 ?

Cr2 Cr2 Cr2 60.0 52 74 ?

Cr2 Cr2 Cr2 120.0 4_656 74 ?

O Cr2 Cr2 42.138(15) 123_655 2_665 ?

O Cr2 Cr2 137.862(15) 27 2_665 ?

O Cr2 Cr2 42.138(15) 148_565 2_665 ?

O Cr2 Cr2 137.862(15) 52 2_665 ?

O Cr2 Cr2 85.84(2) 170_556 2_665 ?

O Cr2 Cr2 94.16(2) 74 2_665 ?

Cr2 Cr2 Cr2 60.0 3_566 2_665 ?

Cr2 Cr2 Cr2 120.0 52 2_665 ?

Cr2 Cr2 Cr2 60.0 4_656 2_665 ?

Cr2 Cr2 Cr2 180.0 74 2_665 ?

O Cr2 Cr2 94.16(2) 123_655 27 ?

O Cr2 Cr2 85.84(2) 27 27 ?

O Cr2 Cr2 137.862(15) 148_565 27 ?

O Cr2 Cr2 42.138(15) 52 27 ?

O Cr2 Cr2 137.862(15) 170_556 27 ?

O Cr2 Cr2 42.138(15) 74 27 ?

Cr2 Cr2 Cr2 180.0 3_566 27 ?

Cr2 Cr2 Cr2 60.0 52 27 ?

Cr2 Cr2 Cr2 120.0 4_656 27 ?

Cr2 Cr2 Cr2 60.0 74 27 ?

Cr2 Cr2 Cr2 120.0 2_665 27 ?

Si1 O Cr2 121.10(2) . 52 ?

Si1 O Cr2 121.10(2) . 74 ?

Cr2 O Cr2 95.73(3) 52 74 ?

Si1 O Cr2 121.10(2) . 27 ?

Cr2 O Cr2 95.73(3) 52 27 ?

Cr2 O Cr2 95.73(3) 74 27 ?

_refine_diff_density_max    1.446

_refine_diff_density_min   -1.234

_refine_diff_density_rms    0.160

_shelx_res_file

;

TITL saikai_2022_001 in Fd-3m

shelx.res

created by SHELXL-2016/6 at 11:23:42 on 04-Dec-2023

REM Fd-3m (#227 in standard setting)

CELL 0.71073   8.342217   8.342217   8.342217  90.0000  90.0000  90.0000

ZERR    8.00   0.000063   0.000063   0.000063   0.0000   0.0000   0.0000

LATT  4

SYMM  0.25000-X, 0.25000-Y,Z

SYMM X, 0.25000-Y, 0.25000-Z

SYMM  0.25000-X,Y, 0.25000-Z

SYMM Z,X,Y

SYMM Y,Z,X

SYMM  0.25000-Z, 0.25000-X,Y

SYMM  0.25000-Y,Z, 0.25000-X

SYMM Z, 0.25000-X, 0.25000-Y

SYMM  0.25000-Y, 0.25000-Z,X

SYMM  0.25000-Z,X, 0.25000-Y

SYMM Y, 0.25000-Z, 0.25000-X

SYMM -Y,-X,-Z

SYMM  0.25000+Y, 0.25000+X,-Z

SYMM  0.25000+Y,-X, 0.25000+Z

SYMM -Y, 0.25000+X, 0.25000+Z

SYMM -X,-Z,-Y

SYMM -Z,-Y,-X

SYMM  0.25000+X, 0.25000+Z,-Y

SYMM -Z, 0.25000+Y, 0.25000+X

SYMM  0.25000+X,-Z, 0.25000+Y

SYMM  0.25000+Z, 0.25000+Y,-X

SYMM -X, 0.25000+Z, 0.25000+Y

SYMM  0.25000+Z,-Y, 0.25000+X

SFAC O Mg Al Si Ti Cr Mn Fe Ni Zn Ca

UNIT 32.00 0.24 0.08 0.64 0.16 7.36 0.16 10.48 0.24 0.08 0.08

EADP SI1 ZN1 MG1 MN1 FE1

EADP CR2 AL2 TI2 NI2 CA2 FE2

EXYZ SI1 ZN1 MG1 MN1 FE1

EXYZ CR2 AL2 TI2 NI2 CA2 FE2

REM SUMP 1.30 0.001 0.65 2 0.65 3

REM SUMP 0.05558 0.00001 0.02779 2 0.02779 3

L.S.      20

LIST      3

FMAP      2

PLAN     25

ACTA

WGHT    0.032700    1.144800

EXTI    0.003235

FVAR       0.44925   0.98444   1.01607

SI1   4    0.125000    0.125000    0.125000    10.00332    0.00875    0.00875 =

0.00875    0.00000    0.00000    0.00000

ZN1  10    0.125000    0.125000    0.125000    10.00032    0.00875    0.00875 =

0.00875    0.00000    0.00000    0.00000

MG1   2    0.125000    0.125000    0.125000    10.00140    0.00875    0.00875 =

0.00875    0.00000    0.00000    0.00000

MN1   7    0.125000    0.125000    0.125000    10.00093    0.00875    0.00875 =

0.00875    0.00000    0.00000    0.00000

FE1   8    0.125000    0.125000    0.125000    10.02716    0.00875    0.00875 =

0.00875    0.00000    0.00000    0.00000

CR2   6    0.500000    0.500000    0.500000    10.03832    0.00535    0.00535 =

0.00535   -0.00018   -0.00018   -0.00018

AL2   3    0.500000    0.500000    0.500000    10.00049    0.00535    0.00535 =

0.00535   -0.00018   -0.00018   -0.00018

TI2   5    0.500000    0.500000    0.500000    10.00086    0.00535    0.00535 =

0.00535   -0.00018   -0.00018   -0.00018

NI2   9    0.500000    0.500000    0.500000    10.00144    0.00535    0.00535 =

0.00535   -0.00018   -0.00018   -0.00018

CA2  11    0.500000    0.500000    0.500000    10.00049    0.00535    0.00535 =

0.00535   -0.00018   -0.00018   -0.00018

FE2   8    0.500000    0.500000    0.500000    10.02716    0.00535    0.00535 =

0.00535   -0.00018   -0.00018   -0.00018

O     1    0.262237    0.262237    0.262237    10.16667    0.00828    0.00828 =

0.00828   -0.00050   -0.00050   -0.00050

HKLF      4

REM  saikai_2022_001 in Fd-3m

REM R1 =  0.0214 for     269 Fo > 4sig(Fo)  and  0.0218 for all     279 data

REM     10 parameters refined using      0 restraints

END

WGHT      0.0323      1.1558

REM Highest difference peak  1.446,  deepest hole -1.234,  1-sigma level  0.160

Q1    1   0.0000  0.0000  0.0000  10.08333  0.05    1.45

Q2    1   0.3750  0.3750  0.1156  10.25000  0.05    0.97

Q3    1   0.3750  0.3750  0.3356  10.25000  0.05    0.60

Q4    1   0.5372  0.4523  0.5372  10.50000  0.05    0.48

Q5    1   0.5000  0.4465  0.5535  10.50000  0.05    0.48

Q6    1   0.2095  0.2538  0.2095  10.50000  0.05    0.45

Q7    1   0.1814  0.2382  0.2382  10.50000  0.05    0.45

Q8    1   0.1250  0.1250  0.0566  10.25000  0.05    0.43

Q9    1   0.2270  0.2270  0.2270  10.16667  0.05    0.38

Q10   1   0.5396  0.5396  0.5396  10.16667  0.05    0.36

Q11   1   0.2483  0.3403  0.2483  10.50000  0.05    0.35

Q12   1   0.3750  0.3750  0.1776  10.25000  0.05    0.33

Q13   1   0.0922  0.0922  0.0922  10.16667  0.05    0.32

Q14   1   0.4973  0.5539  0.5539  10.50000  0.05    0.32

Q15   1   0.3633  0.1574  0.3318  11.00000  0.05    0.28

Q16   1   0.2053  0.2976  0.2352  11.00000  0.05    0.27

Q17   1   0.2195  0.3750  0.3750  10.25000  0.05    0.26

Q18   1   0.2500  0.2959  0.0459  10.50000  0.05    0.25

Q19   1   0.1154  0.3321  0.3321  10.50000  0.05    0.24

Q20   1   0.4886  0.4886  0.5826  10.50000  0.05    0.23

Q21   1   0.2140  0.2762  0.0360  10.50000  0.05    0.23

Q22   1   0.1667  0.3664  0.1667  10.50000  0.05    0.22

Q23   1   0.0676  0.0676  0.0676  10.16667  0.05    0.20

Q24   1   0.1250  0.1250 -0.0523  10.25000  0.05    0.19

Q25   1   0.2117  0.2981  0.2981  10.50000  0.05    0.18

;

_shelx_res_checksum   40575

_shelx_hkl_file

;

1   1  -1 1215.27 24.3282   4

-1   1  -1 1195.40 23.8652   2

1  -1   1 1204.64 23.6680   1

-1  -1  -1 1243.28 22.4254   2

-1  -1  -1 1218.16 23.6531   1

-1  -1   1 1200.44 24.1449  11

1  -1  -1 1187.30 24.0544  11

0  -2   0 0.37776 0.45944   2

0   0  -2 0.25253 0.89948   5

2   0   0 0.45857 1.13263  17

0   2  -2 3043.08 58.0946   5

0  -2   2 3063.15 58.0015   5

0  -2  -2 3212.80 58.1542   5

-2   0  -2 3129.85 58.2179   2

2   0  -2 3159.04 59.1195   4

0  -2   2 3121.01 57.4309   3

-2   0  -2 3204.61 59.0144   3

0   2   2 3023.98 57.9900   5

-2   2   0 3082.05 58.5932  17

-2  -2   0 3010.78 58.4986  17

2   0  -2 3107.01 60.2025  11

-2   2   2 1385.22 26.9492   4

2  -2   2 1359.48 28.4517   1

2   2  -2 1413.10 29.7726   4

2   2   2 1353.53 28.5137   1

-2   2   2 1368.74 29.3595  11

-2  -2   2 1373.25 29.3756  11

1  -3   1 7777.23 138.928   4

1  -3   1 7711.17 138.395   1

1  -1  -3 7766.87 141.192   5

-1  -1  -3 7697.14 141.118   1

-1  -1   3 7847.77 141.231   5

1  -1   3 7656.32 141.026   5

-1   1  -3 7726.17 140.843   2

1  -3   1 7766.66 140.093   2

1   3  -1 7785.69 139.156   2

-3  -1  -1 7861.56 140.109   3

1   1  -3 7621.28 138.522   3

1  -1   3 7903.44 140.318   3

1   3  -1 7775.88 138.383   5

1   3   1 7659.81 138.395   1

1  -3  -1 7698.60 138.384   5

3   1  -1 7644.58 138.142   3

3  -1   1 7707.07 141.759  17

1  -3   1 7453.39 138.521  17

-3  -1  -1 7702.77 141.666  17

1   3   1 7407.55 138.422  17

3  -1  -1 7602.01 142.236  11

-1   3   1 7429.91 138.779  11

-1  -3   1 7626.47 138.829  11

3   1   3 30.3595 2.38856   2

-1   3  -3 38.5411 2.88263   1

3   1  -3 33.6437 3.26376   4

-3   1  -3 30.2770 2.86113   3

1  -3   3 33.1794 2.59666   5

1   3  -3 34.2052 2.74401   5

-3  -3   1 34.2075 1.75900   3

-1  -3  -3 36.1458 2.81136   1

-1  -3   3 36.8545 3.27964   4

-3   1   3 29.7848 2.65661   4

1  -3  -3 37.8597 2.89501   5

1  -3   3 41.0023 2.82044   3

-3  -1  -3 34.8192 3.02728   3

1   3   3 33.9162 2.78144   5

-1  -3   3 36.9844 1.94358   3

-3   3   1 28.1834 2.81400  17

-3  -3   1 35.9666 3.09310  17

3  -3   1 37.9834 3.12953  17

3   3   1 30.6681 2.80499  17

3   3  -1 32.1187 3.01266  11

3  -3  -1 37.8049 3.27632  11

3  -3   3 2979.21 60.3793   1

3   3  -3 3012.58 62.3321   4

-3   3   3 3023.58 57.7981   4

3  -3  -3 3163.61 60.7928   5

3  -3   3 3040.15 60.5650   3

3   3  -3 3141.94 60.7668   5

3   3   3 3032.68 61.0284  17

3  -3   3 2995.51 60.8259  17

-3  -3   3 3048.46 61.7453  11

0   0  -4 13320.0 236.444   5

0  -4   0 13133.9 233.162   2

-4  -2   0 0.88565 1.57019  17

4   0   2 0.32130 1.40560  17

-2  -4   0 0.26703 0.84397  17

0  -2  -4 1.52651 1.20596   5

0   4  -2 0.42080 1.10261   2

-2   0  -4-0.21846 1.19570   2

-4  -2   0 0.74066 0.77645   3

0  -4  -2 0.48514 0.84275   1

0  -4   2 1.52270 0.74815   5

0   2  -4 3.33394 1.58659   5

-2   0  -4 0.28860 1.39304   1

4   0  -2-2.77015 1.43458   4

0   2  -4 0.49092 0.68432   3

0  -2   4-0.74195 1.31548   5

0  -4   2-0.22614 1.16698   4

2   0  -4 0.29037 1.37631   5

2   4   0 0.80694 0.54402   2

-4   0  -2-0.24290 1.10795   3

2   4   0 4.25294 1.25468  11

2  -4   0 0.58154 1.01010  11

4  -2   0 1.56987 1.59457  11

4   2   0-0.31434 1.64712  11

4   0  -2-0.35979 1.57394  11

2   4  -2 1632.08 33.5398   5

4  -2  -2 1695.39 33.4913   4

2   4   2 1670.03 33.5391   1

2  -4   2 1657.40 35.2431   2

4   2   2 1684.66 32.6937   2

2  -2   4 1663.20 35.1498   3

-2  -2  -4 1672.09 35.9008   1

2  -2  -4 1645.38 35.8788   5

-2  -2  -4 1672.22 33.2245   2

4  -2   2 1672.34 36.0713   1

2  -4   2 1647.78 33.5237   1

-2   2  -4 1743.49 35.9328   2

4   2  -2 1712.43 37.0665   4

-2   2  -4 1649.03 35.8396   1

2   2  -4 1654.46 36.0317   5

2   4  -2 1655.78 36.3826   4

-4  -2  -2 1684.38 35.0730   3

2   2  -4 1626.14 31.3187   3

2  -4  -2 1641.70 33.4550   5

-2   2  -4 1701.47 35.1743   3

4  -2   2 1620.18 36.4029  17

2   4   2 1626.35 33.6817  17

2  -4   2 1604.12 33.7712  17

4   2   2 1611.64 36.2958  17

-2  -2   4 1617.62 36.7106  11

-4  -2   2 1666.69 37.0787  11

4  -2  -2 1590.87 37.0570  11

-2   4   2 1639.21 34.3306  11

-2  -4   2 1691.07 34.3885  11

4   2  -2 1638.36 37.3159  11

-4   0  -4 24941.6 445.227   3

0  -4   4 24237.8 441.728   3

0  -4   4 23882.0 445.479   4

0  -4  -4 24081.5 443.311   1

-4   0   4 24578.3 445.409   4

0  -4   4 24560.6 443.066   5

0   4  -4 25546.8 445.046   2

0   4  -4 25616.2 443.582   1

-4  -4   0 23852.5 443.870  17

4   4   0 25033.3 444.805  11

4   2   4 22.5181 3.31774  17

4  -2   4 12.1643 2.74618  17

4   4   2 19.0110 2.76203  17

4  -4   2 22.2158 2.89307  17

4  -4   2 20.9415 2.74135   2

2  -4   4 16.6886 2.34913   5

4  -2   4 21.4653 2.79967   3

-2  -4   4 15.0626 2.86637   4

4  -2   4 19.3932 2.90962   1

4   2  -4 18.0745 3.03228   5

4  -2  -4 16.8612 2.99808   5

2   4  -4 15.6526 2.41648   5

4  -2   4 15.6829 2.65689   2

-4  -2  -4 16.9498 2.66085   3

-2   4  -4 14.3401 2.30495   1

4   2   4 17.6146 2.71234   1

2  -4  -4 15.3316 2.38149   5

2  -4   4 18.9446 2.38016   3

4  -4   2 16.9369 2.38575   1

-2  -4  -4 18.3848 2.54975   1

-4   2   4 14.4117 3.06471  11

-4  -2   4 10.3686 2.95543  11

4  -4  -2 24.0931 3.15894  11

4   4  -2 15.7836 2.84516  11

-2  -4   4 16.6496 2.75752  11

-4  -4   4 4462.12 89.5000  11

-4   4   4 4469.48 89.5462  11

4  -4   4 4380.69 87.5493   1

4   4  -4 4201.33 89.9070   4

4  -4   4 4624.41 88.7343   2

4   4  -4 4651.05 88.2200   5

4  -4   4 4531.76 88.0605   3

-4   4   4 4282.99 83.7860   4

4   4   4 4522.86 88.0360   1

4  -4  -4 4582.70 88.0109   5

4   4   4 4564.74 88.7552  17

4  -4   4 4434.82 88.3905  17

5  -1  -1 7085.47 130.893  11

1  -1  -5 6944.00 128.855   5

1   5  -1 7140.85 127.340   4

5   1  -1 6980.59 124.557   3

1   5  -1 7234.91 124.776   2

1   1  -5 6938.26 125.227   3

-1  -1  -5 7066.77 128.964   1

1  -5   1 7091.96 126.025   2

1   5  -1 6738.31 121.753   5

-1   1  -5 7253.87 126.912   3

1  -5  -1 6925.21 121.855   5

-5  -1  -1 7217.16 126.614   3

-1   1  -5 7204.99 127.908   2

1   5   1 6607.61 121.788   5

1  -5   1 6574.30 121.799   5

-1   5   1 6319.45 121.812  17

-1  -5   1 6674.49 122.121  17

5  -1   1 7143.35 130.041  17

3   5  -1 319.132 10.2110  11

-1  -5   3 332.082 10.1761  11

5  -3  -1 330.460 12.7351  11

-1   5   3 348.548 10.4674  11

-3  -1   5 330.146 13.1269  11

5   3  -1 358.931 13.0547  11

5  -1  -3 361.537 13.5733  11

3  -5  -1 331.339 10.1046  11

-5  -1   3 331.763 13.1481  11

3  -1  -5 353.311 12.6871   5

-1  -5  -3 370.669 9.94927   1

5   1  -3 352.016 12.3331   4

5  -3  -1 336.925 9.00051   4

1  -5   3 333.821 9.58511   5

5  -1  -3 360.786 11.5028   4

-5  -1  -3 334.597 11.5239   3

-1  -3   5 337.108 12.3884   4

3   5  -1 341.469 9.09041   2

1  -3   5 343.370 10.6609   3

1   5  -3 345.737 9.86101   5

-1   5  -3 345.248 9.76959   1

1  -3  -5 344.677 11.6546   5

1  -3   5 358.105 11.7579   5

-1  -3   5 352.431 11.7740   5

-3  -1  -5 332.808 12.2978   1

-5  -3  -1 348.244 10.5392   3

3   5   1 328.293 9.71205   1

1   5  -3 338.544 10.9899   2

-1  -3  -5 349.078 11.8612   1

-3  -1  -5 366.240 12.2015   3

-1   5  -3 350.694 11.5386   2

-1   3   5 353.365 11.8352   5

3   5  -1 422.362 13.4952   4

3  -5   1 323.374 11.1083   2

5  -1   3 361.120 12.8364   1

-3  -1  -5 348.111 10.7339   2

1   3  -5 349.281 11.7746   5

-3   1  -5 355.924 11.6895   2

1   3   5 350.926 11.6756   5

3  -5   1 308.266 9.51423   1

1   5   3 350.417 9.83235   5

1  -5   3 343.477 11.1311   4

-3   1   5 327.171 11.6153   4

1  -5  -3 345.533 9.77778   5

-1   3  -5 344.009 11.8423   1

5  -1   3 371.113 11.8376   2

-1   3  -5 344.327 11.9761   2

5   1  -3 330.696 8.53551   3

5  -1   3 327.570 12.6780  17

-5  -3   1 334.267 12.2511  17

-5   3  -1 357.789 12.2804  17

5   3   1 320.050 12.0891  17

-5  -3  -1 343.843 12.1430  17

-3  -5   1 346.318 10.2304  17

5  -3   1 343.155 12.4959  17

-5   3   1 351.620 12.6553  17

-3   5   1 326.588 10.1327  17

-5   3   3 3487.83 72.0730  11

5   3  -3 3370.91 72.1687  11

-5  -3   3 3509.70 72.0497  11

-3  -3   5 3496.85 72.1608  11

-3   3   5 3528.18 72.2577  11

-3  -5   3 3417.00 69.0984  11

5  -3  -3 3354.03 71.7569  11

5   3   3 3515.89 71.3975  17

3  -5   3 3374.25 68.6280  17

5  -3   3 3465.81 71.4128  17

3   5   3 3412.53 68.4454  17

5  -3   3 3575.73 70.5247   3

5   3   3 3478.06 70.5288   1

3   3  -5 3617.14 70.7538   5

3  -3  -5 3563.68 70.5800   5

-3   5   3 3293.50 63.4545   4

5  -3   3 3464.25 70.3824   1

3  -5   3 3319.99 67.9794   1

-5  -3  -3 3568.88 69.8348   3

3   3   5 3550.38 70.4163   5

-3  -3  -5 3509.35 70.5600   1

3  -3   5 3528.96 69.8664   3

-3   3  -5 3483.62 70.5239   1

3  -5   3 3602.22 69.8766   3

3   5  -3 3626.83 72.0995   4

3  -5  -3 3498.57 67.9980   5

-3   3  -5 3603.73 70.8193   2

5   3   3 3514.21 65.3495   2

5   3  -3 3585.86 72.3475   4

3   5  -3 3552.62 68.1563   5

-3  -3  -5 3560.68 66.1669   2

3  -3   5 3443.48 70.1045   5

-3  -3   5 3544.73 72.2682   4

3  -5   3 3515.01 70.0809   2

-5  -1  -5 628.838 18.7381  10

1   5  -5 614.755 17.9111   2

-5  -5  -1 628.911 16.1130   3

-5   1  -5 623.949 18.4831   3

5  -1  -5 626.851 19.2795   5

1  -5   5 633.242 18.4047   4

5  -1   5 627.105 17.7452   2

-1  -5   5 626.582 19.1601   4

5  -1   5 612.544 19.1898   1

-5  -1  -5 646.863 19.0136   6

-5  -5   1 622.926 13.8004   3

-5  -1  -5 614.226 18.5360   3

1   5   5 622.254 16.8801   5

1  -5   5 603.348 16.2226   3

-1   5  -5 626.100 18.3776   2

1  -5   5 620.908 16.7749   5

-1  -5  -5 624.838 17.0675   1

-1   5  -5 600.217 16.9032   1

-1  -5   5 597.334 14.3382   3

-5   5   1 608.956 18.0597  29

-5  -1   5 652.791 18.9257  25

-1   5  -5 588.596 17.4943  27

5  -5   1 608.858 17.7855  11

-1   5   5 598.313 17.5431  11

5   5   1 607.876 17.8267  11

-5  -1   5 643.303 20.8951  11

5   5  -1 600.062 18.0861  11

5  -5  -1 628.113 18.0882  11

-5   5  -1 638.608 17.9712  23

-5   5   1 603.508 17.5121  23

1   5   5 583.504 18.3516  19

-1   5   5 635.354 19.1089  19

5  -1   5 627.450 19.8183  17

-5   5   1 655.831 18.0011  17

5   5   1 596.172 18.8178  18

-5  -5   1 608.057 17.4985  17

-5  -3  -5 3502.34 71.0240  10

-5   3  -5 3412.35 70.8064  10

-5   5  -3 3504.35 70.5723   9

3  -5  -5 3416.15 69.1865   5

3  -5   5 3487.21 69.3456   5

5  -5   3 3400.08 69.0215   1

-5   3  -5 3394.59 70.5106   6

5  -3  -5 3557.59 71.6207   5

-3   5   5 3340.47 66.2913   4

5  -5   3 3481.38 70.8005   2

-5  -3  -5 3527.88 71.0986   3

5  -3   5 3411.79 70.9855   1

3   5  -5 3439.06 69.4959   5

-5  -3  -5 3370.46 70.7431   6

5  -3   5 3477.29 70.8541   3

3   5   5 3417.39 69.1930   5

3  -5   5 3318.51 69.2264   3

5   3  -5 3514.28 71.5314   5

5  -5   3 3415.73 70.4743   3

5  -3   5 3393.76 70.8089   2

5   3   5 3422.26 71.4047   1

5   5   3 3366.97 69.1761   1

-5   5   3 3458.63 70.4562  29

-5  -3   5 3384.47 70.4510  25

-5   3   5 3510.74 70.8514  25

-5   3   5 3515.27 73.4534  11

-5  -3   5 3335.80 72.8418  11

-3   5   5 3403.17 71.0538  11

5   3  -5 3340.99 71.3086  12

-3  -5   5 3348.24 70.6943  11

-5   5   3 3388.94 68.9035  23

-3   5  -5 3396.07 71.0476  22

-5   5  -3 3387.67 70.7320  22

-5   5  -3 3463.99 70.1053  23

-5   3  -5 3313.86 70.5920  22

-3   5  -5 3374.41 69.3827  23

5   5   3 3322.22 71.1719  19

-5   5  -3 3687.23 71.0927  20

3   5   5 3427.83 71.3735  19

5   5   3 3574.96 72.9847  18

5  -5   3 3429.82 70.5332  17

-5   5   3 3495.62 70.7996  17

-5  -5   3 3364.18 70.4215  17

5   5   3 3271.29 70.0536  17

5  -3   5 3258.13 71.4641  17

-5   3  -5 3455.81 69.6578  15

5   3   5 3563.02 72.6771  17

3   5  -5 3397.12 71.1153  16

-5   5  -5 3289.86 70.5841  10

5  -5   5 3409.25 71.2874   3

5  -5   5 3453.34 72.1506   2

-5   5  -5 3374.50 70.3001   6

5   5  -5 3453.49 71.2136   5

-5  -5  -5 3430.68 71.4709   3

5  -5  -5 3391.93 70.9192   5

-5  -5  -5 3398.41 70.5036   6

-5   5   5 3410.76 71.5513  29

-5  -5   5 3411.84 70.3137  25

-5   5   5 3490.21 70.8966  25

-5   5  -5 3451.01 70.9925  23

5   5   5 3542.64 73.0932  19

-5   5  -5 3453.46 71.9320  20

-5   5  -5 3509.45 72.1313  15

5  -5   5 3440.44 72.2682  17

5   5  -5 3415.79 72.4705  16

5   5   5 3477.37 72.2135  17

5   5  -5 3383.12 71.3426  12

-5  -5   5 3337.53 72.4463  11

-5   5   5 3482.30 73.1973  11

5  -5  -5 3335.95 70.7147  12

-6   0   0 0.44899 1.63807  17

0  -6   0 2.69730 1.08798   2

0   0   6-0.37746 1.41953   5

0   6   0 0.21757 1.08698   4

6   0   0-0.95470 1.89780  11

6  -2   0 1046.59 27.6491  11

6   0  -2 1043.62 28.4499  11

6   2   0 1065.28 27.6424  11

0  -6   2 982.992 20.0964  11

0   6   2 956.355 19.7758  11

0   2  -6 1024.27 23.3294   3

2  -6   0 1023.84 23.8374   2

0  -2   6 1023.66 25.6799   5

2   0  -6 1086.54 26.7332   5

-2   0  -6 1064.74 24.9299   2

6  -2   0 1030.53 25.0265   3

6   0  -2 1005.82 25.4872   4

2   6   0 978.719 19.5751   1

-2   0  -6 1086.17 25.5611   3

6   0   2 1029.54 24.9027   3

2  -6   0 1006.52 19.7516   1

0   2   6 1009.52 25.7866   5

-2   0  -6 1078.92 26.6590   1

2   0   6 1029.68 26.1996   5

-6   2   0 1026.59 27.1174  17

-6   0   2 1041.49 27.6246  17

-6  -2   0 1030.07 26.8493  17

6   0   2 1049.47 27.4693  17

6  -2  -2 1688.44 40.6575  11

6   2  -2 1697.38 40.8158  11

-6   2   2 1715.66 40.1724  17

2   6   2 1587.21 33.5023  17

-2  -6   2 1624.88 33.7673  17

6  -2   2 1702.82 39.9122  17

6   2   2 1683.50 39.7657  17

-6  -2   2 1678.97 39.9827  17

-2   6   2 1603.87 33.5846  17

2  -6   2 1637.40 33.6893  17

2  -6  -2 1671.93 33.1606   5

6   2  -2 1749.78 39.7726   4

-2  -2   6 1737.13 39.7218   4

2   2  -6 1673.37 33.7768   3

2  -2   6 1738.77 38.6290   5

6  -2  -2 1734.79 35.8443   4

2   2  -6 1635.93 38.9960   5

2   6  -2 1714.46 38.3095   4

2  -6   2 1694.60 36.9551   2

2   2   6 1681.75 38.4179   5

-6  -2  -2 1712.88 36.9453   3

-2   2  -6 1751.12 39.0249   1

6  -2   2 1621.36 37.5180   3

2  -2  -6 1693.21 38.7534   5

-2   2  -6 1719.78 38.1921   2

-2  -2  -6 1738.14 35.9795   2

2   6   2 1690.06 33.1916   5

-2  -2  -6 1741.73 38.9978   1

-2   2  -6 1745.40 37.3011   3

2  -6   2 1617.72 33.1328   5

2   6  -2 1681.94 33.2098   5

2   6  -2 1727.77 35.1919   2

-4   0  -6 1.32932 2.06073   6

6   0   4 2.69976 1.41050   2

-6  -4   0 0.41949 1.01227   3

6   0   4 1.48436 1.80511   1

0  -4  -6-0.78189 1.71004   1

0   6  -4 0.23600 1.09755   1

0  -4   6 0.74590 1.63133   5

-6   0  -4 0.46602 1.80331   6

0  -6   4-0.24331 1.01695   3

0   4   6 0.38069 1.62859   5

0   4  -6-0.39681 1.84544   1

4   0  -6 0.47601 2.21374   5

-6   0  -4-0.41241 1.40742   3

0  -6  -4 0.93671 1.15020   1

0   6  -4-0.36796 1.38374   2

0  -6   4 1.19188 1.73781   4

-4   0  -6-0.34008 1.38713   2

-4   0   6 0.43715 1.59483   4

0  -4   6-0.45658 1.86234   4

-6  -4   0-0.85409 1.78488  17

-6   4   0-0.43709 1.64369  17

6   0   4-0.52773 1.80097  17

6   4   0 0.46905 2.34320  18

0   6  -4 0.39416 1.56702  27

-6   0   4 0.44682 1.95443  25

0   4  -6-1.47093 1.86741  27

-4   0   6-0.44550 2.29853  25

4  -6   0 0.28318 1.34204  11

4   0  -6 0.47840 2.38990  12

-4   0   6-0.57174 1.88019  11

6   0  -4-1.13827 2.32144  11

4   6   0 0.29233 1.50827  11

-4   6   0 2.69634 1.98737  24

-6   4   0 2.33949 1.91512  23

-4   6   0 1.49343 1.95618  23

-4   6   0-0.38806 1.87288  22

-4   6   0-0.82700 1.80871  20

0   6   4 0.45749 1.91212  19

6   4   0 0.46800 2.17648  11

-4   0  -6 0.43870 2.00063  10

6  -4   0-1.40855 2.05373  11

-6   0   4 1.13983 2.43808  11

-6   0  -4 2.26573 1.89398  10

-6   4  -2 947.036 25.7081  10

-6   2  -4 980.682 26.4830  10

-4   2  -6 973.354 25.7256  10

-4   6  -2 970.995 25.3593   9

-4  -2  -6 942.970 25.9540  10

-6   4  -2 997.345 24.8689   9

-6  -2  -4 990.963 25.9550  10

-4   2  -6 965.069 26.0101   8

2   6  -4 1016.53 23.0699   5

-2  -4  -6 980.268 25.4749   1

-2  -4  -6 963.856 21.6968   2

6  -2   4 1044.44 26.0422   2

-4   2  -6 976.807 25.7274   3

-6   2  -4 973.263 26.0893   6

6  -2   4 1030.39 27.1083   1

6   2   4 957.043 26.5318   1

-6  -2  -4 1016.46 26.6276   6

2  -6  -4 1014.57 22.9536   5

-2   4  -6 972.206 25.4571   1

2   4   6 990.700 25.3969   5

2  -4   6 950.640 24.0665   3

2  -4   6 978.128 25.2130   5

4   2  -6 1066.08 27.1160   5

6  -4   2 965.099 25.4459   1

-4   2  -6 964.328 25.8141   6

-4  -2  -6 991.808 25.9774   6

-4  -2  -6 1009.63 26.3008   3

4  -2  -6 1018.78 26.7584   5

2  -4  -6 963.364 25.2674   5

6   4  -2 996.411 27.6442   4

2  -6   4 962.776 22.6388   5

6   4   2 939.938 20.1256   2

4   6  -2 947.227 26.7193   4

-2  -6   4 909.390 19.9567   3

-6  -4  -2 949.237 23.8522   3

-4   2   6 957.717 24.9037   4

4  -6   2 1004.89 25.3478   2

4  -6   2 946.387 22.7794   1

6  -4   2 1020.64 26.2873   2

-4  -2   6 882.764 26.3103   4

-6  -2  -4 1008.91 25.6298   3

-2   4  -6 999.046 26.1001   2

4   2  -6 947.835 19.1329   3

2  -6   4 958.790 24.2505   4

2   6  -4 971.789 24.2201   2

6   4   2 976.486 25.2741   1

6   2  -4 983.379 26.9709   4

6  -4   2 872.479 24.9333   3

4  -6   2 890.177 20.2931   4

2  -6   4 953.256 24.0503   3

-2  -4   6 1005.53 27.2998   4

6  -2   4 955.992 25.6034   3

2   4  -6 1016.65 25.6833   5

2   6  -4 996.328 25.4145  27

2   6  -4 969.096 25.8777  30

-4   6   2 934.325 25.4568  29

-6   4   2 964.340 24.9842  29

-6   2   4 984.303 26.0093  25

-6  -2   4 989.045 26.0028  25

-4   6   2 1005.18 24.7453  26

-4   2   6 975.054 25.9843  25

-4  -2   6 1011.95 26.1679  25

-2   6   4 918.632 23.9050  26

6   4  -2 978.048 27.1719  11

4   2  -6 928.629 26.1709  12

-6   2   4 1013.86 28.2158  11

-2   4   6 969.235 26.4610  11

-2  -6   4 951.163 23.7131  11

4  -2  -6 933.309 26.1631  12

6  -2  -4 937.552 27.4553  11

-4   2   6 966.210 27.8463  11

6  -4  -2 985.473 26.8277  11

-4  -2   6 922.680 27.5488  11

6   2  -4 999.006 28.2119  11

-2  -4   6 944.783 26.3601  11

-6  -2   4 937.879 27.6407  11

-6   4  -2 1040.34 25.4722  23

-2   4  -6 979.239 25.7056  22

-6   4   2 1014.47 25.3917  23

-6   2  -4 927.268 24.6856  22

-4   6   2 980.883 25.1404  22

-2   6  -4 915.408 24.9208  23

-2   6  -4 945.713 25.4005  22

-4   6  -2 987.233 25.3872  23

2   6   4 976.685 26.7844  19

-2   6   4 981.554 26.4076  19

-6   4  -2 993.763 25.5830  21

4   6   2 923.363 26.3914  19

2   4   6 980.401 25.5393  19

-6   4  -2 1015.81 25.0912  20

-4   2  -6 967.006 24.3694  15

-6  -4   2 953.411 26.2913  17

-6   4  -2 1006.11 25.2236  15

6   4   2 938.369 25.9816  17

6   4   2 1002.88 26.6590  18

6  -4   2 994.315 26.6072  17

6   2   4 990.718 27.5095  17

-6   4   2 1008.14 26.7080  17

-4   6  -2 987.784 24.6438  15

4  -6   2 932.336 23.3105  17

6  -2   4 914.362 26.7236  17

4   6   2 956.879 26.6612  18

-4  -6   2 947.026 23.5255  17

-6   2   4 949.332 24.9965  14

-4  -6   4 4.53429 2.13079  11

-4   4  -6 7.66798 2.60969  10

-4   6   4 4.63043 2.24253  11

-4   4  -6 5.73728 2.28077   8

-6  -4  -4 3.86877 2.25605  10

-4   6  -4 6.34584 2.63720   9

-6   4  -4 2.96389 2.38766  10

4  -4  -6 10.0485 2.85899   5

4   4  -6 21.8621 3.60226   5

4   6  -4 7.71956 2.31152   5

4   4   6 28.4736 3.88663   5

-6  -4  -4 4.68294 2.26787   3

6  -4   4 5.52995 2.38122   1

4  -4   6 6.27879 2.28125   5

4  -6   4 8.59781 2.08114   4

-6  -4  -4 6.42243 2.51386   6

4  -6  -4 7.46659 2.21449   5

-4   4   6 4.74727 1.85293   4

6   4   4 6.10777 2.42759   1

6  -4   4 6.08443 2.34178   3

4  -4   6 4.30762 2.11980   3

4  -6   4 5.12165 2.02697   3

4  -6   4 7.21486 2.33022   2

-6   4  -4 8.53270 2.72013   6

6   4  -4 8.05002 2.92290   4

-4  -4  -6 7.53840 2.86284   6

4   6  -4 7.83702 2.89115   4

-4   6   4 3.87993 2.34433  29

-4   4   6 7.05112 2.62421  29

-6   4   4 2.93751 2.20259  29

-6   4   4 33.0447 4.29259  25

-4  -4   6 12.3233 3.21400  25

-6  -4   4 31.5756 4.19715  25

-4   6   4 6.20755 2.31109  26

-4   4   6 7.67976 2.70501  25

6   4  -4 9.65533 3.37680  12

4  -4  -6 18.4284 3.78406  12

-4  -4   6 6.75556 2.81539  11

4   4  -6 21.5829 3.96341  12

6  -4  -4 5.38220 2.71769  12

-4   4   6 3.98448 2.70081  11

-6   4  -4 8.62452 2.57132  23

-4   4  -6 7.51677 2.14479  23

-6   4  -4 4.39507 2.40213  22

-4   6  -4 8.29095 2.91636  22

-4   6   4 7.54279 2.32060  23

-4   6  -4 3.66619 2.17582  23

-4   4  -6 4.72846 2.62788  22

6   4   4 10.4255 2.92627  19

-4   6  -4 7.55478 2.94428  20

4   6   4 2.81793 2.52162  19

-6   4  -4 6.52165 2.49729  20

-6   4  -4 5.45534 2.57085  21

4   4   6 6.10327 2.54934  19

-4   4  -6 9.95038 2.86102  15

4   6   4 10.3321 2.59173  17

6   4   4 14.6996 3.52105  17

4   6  -4 12.7188 3.42030  16

6   4  -4 3.92079 2.57837  16

6  -4   4 5.78552 2.75882  17

-6   4  -4 5.83111 2.49194  15

-4   6  -4 12.4100 3.13397  15

6   4   4 5.55238 3.24528  18

4  -6   4 9.64410 2.48919  17

4   6   4 6.07678 3.08868  18

-6   0  -6 914.329 27.1019   6

0   6  -6 900.350 23.8333   1

0  -6   6 945.856 23.6928   5

0  -6   6 883.104 21.7080   3

0  -6   6 911.289 25.9789   4

6   0  -6 927.243 26.8517   5

0  -6  -6 930.971 23.9410   1

-6  -6   0 894.422 21.0981   3

-6   0  -6 922.008 25.7699   3

6   0   6 953.619 27.3684   1

0   6  -6 942.010 25.5063   2

6   6   0 899.795 27.4657  18

6   0   6 927.245 27.6302  17

-6   0  -6 923.891 23.1994  15

-6   0   6 914.363 26.9828  25

-6   0   6 927.570 28.5476  11

6   0  -6 875.314 27.3132  12

0   6   6 898.869 23.5117  13

6  -6   0 926.178 24.9242  11

6   6   0 900.884 25.0165  11

-6   6   0 900.183 24.8467  22

0   6  -6 913.781 24.7133  22

-6   6   0 931.921 25.7023  23

0   6   6 907.296 27.0231  19

0  -6  -6 913.844 24.8777   7

-6   0  -6 917.245 27.1080  10

-6  -2  -6 1358.55 35.7108  10

-6   2  -6 1388.61 35.9940  10

-2   6  -6 1408.81 32.9400   8

-6   6  -2 1314.81 33.4370  10

-6   6  -2 1386.75 34.7043   9

-6   2  -6 1310.50 34.9105   8

-2  -6  -6 1305.67 32.2431   8

6  -6   2 1396.94 34.4833   3

6   2  -6 1428.43 35.9189   5

-6  -2  -6 1375.41 35.8754   6

-2   6  -6 1318.59 32.2977   1

2   6  -6 1337.75 32.3594   5

6  -2  -6 1384.23 35.3659   5

-2  -6  -6 1355.11 32.4252   1

6   2   6 1362.98 35.5487   1

-6   2  -6 1324.81 35.4481   6

-2  -6  -6 1311.56 26.9216   2

2  -6   6 1312.45 31.7355   3

2  -6   6 1349.95 33.5177   4

2  -6  -6 1447.35 32.6705   5

-6  -6  -2 1359.08 31.5970   3

2   6  -6 1385.20 33.6607   2

-2   6  -6 1421.66 34.7234   2

6  -2   6 1418.55 35.7199   1

2   6   6 1357.62 32.1465   5

6  -6   2 1340.05 34.0066   2

2  -6   6 1378.06 32.1247   5

6  -6   2 1316.33 31.8835   1

-6  -2  -6 1392.25 34.5670   3

6   6   2 1350.33 32.1429   1

-6   6   2 1344.31 34.9110  29

-2   6  -6 1317.57 33.3542  30

-2   6  -6 1369.81 34.4664  27

-6   6   2 1324.77 32.4557  24

-6   2   6 1357.72 35.5588  25

-6  -2   6 1365.10 35.5502  25

-2   6   6 1386.99 32.7650  26

-2  -6   6 1351.40 33.6683  11

6  -6  -2 1372.95 33.6238  11

6   6   2 1301.98 33.1646  11

6  -6   2 1390.29 33.7521  11

6   2  -6 1346.87 36.4994  12

6  -2  -6 1369.92 36.3407  12

-6  -2   6 1342.79 37.0029  11

-6   2   6 1436.53 37.6985  11

-2   6   6 1320.47 33.4567  11

6   6  -2 1305.45 33.7382  11

-6   6  -2 1354.17 31.9797  13

-6   6   2 1358.56 33.1472  22

-6   6   2 1341.29 33.7671  23

-2   6  -6 1360.58 34.0201  23

-2   6  -6 1308.10 34.6471  22

-6   6  -2 1329.14 34.3447  22

-6   6  -2 1419.08 35.1565  20

-6   2   6 1383.01 31.9776  21

-6   6  -2 1313.41 34.1658  21

2   6   6 1357.32 35.9383  19

6   2   6 1417.89 36.7336  17

-6  -6   2 1355.34 33.3351  17

-6   2  -6 1353.26 33.0832  15

-6   6  -2 1333.90 33.9821  15

-6   6   2 1433.99 33.8220  17

-2   6  -6 1351.29 33.9683  15

6   6   2 1394.39 36.7552  18

6  -2   6 1335.57 35.7990  17

-6   6  -2 1341.73 32.4377  14

-6   4  -6 335.592 14.1204   8

-4   6  -6 372.197 13.3200   8

-6  -4  -6 356.007 15.1723  10

-6   4  -6 333.678 14.6860  10

-6   6  -4 363.847 15.2020   9

-6   6  -4 327.065 13.5873  10

-6  -6  -4 332.525 12.6730  10

-4   6  -6 338.070 12.7595  10

6  -4   6 342.353 14.0467   3

6   6   4 334.174 13.1666   1

-6  -4  -6 331.362 13.9497   3

4  -6   6 352.153 13.2675   5

6  -6   4 338.287 14.0438   2

6  -6  -4 329.529 12.9922   5

6   6  -4 353.109 13.4036   5

-6  -6  -4 347.704 13.1463   6

-6   6  -4 339.358 12.9670   6

4  -6   6 330.692 13.1917   3

4   6   6 335.750 12.9425   5

6   4  -6 351.199 14.4701   5

4   6  -6 365.666 13.5600   5

6  -6   4 326.920 13.6499   3

6  -4  -6 364.096 14.6635   5

4  -6  -6 329.832 12.8411   5

-6  -4  -6 325.216 14.3561   6

-6   4  -6 306.959 13.9557   6

-4  -6  -6 360.109 13.4706   6

6  -6   4 323.983 12.8965   1

-6  -6  -4 334.746 13.1596   3

-4   6  -6 329.757 12.8768   6

4   6   6 344.779 12.4360  28

-6   4   6 337.969 13.4008  29

-6   6   4 346.130 14.7963  29

-4   6  -6 336.212 12.6747  30

-4   6   6 352.467 14.6995  29

4   6  -6 339.115 12.6824  28

-6   6   4 368.283 13.6834  25

-6  -4   6 343.301 14.6143  25

-4   6   6 342.572 12.4984  26

-4   6   6 350.798 13.4096  25

-4  -6   6 360.183 13.3221  25

-6   4   6 347.215 14.7695  25

-6  -6   4 319.327 12.7470  25

4  -6  -6 337.845 13.0346  12

4   6  -6 337.728 13.4620  12

-6   4   6 343.639 15.5268  11

6  -4  -6 322.349 14.7224  12

-4   6   6 324.164 14.0313  11

6   6  -4 338.189 13.6689  12

6  -6  -4 340.758 13.4713  12

6   4  -6 360.686 15.5699  12

-4  -6   6 326.877 13.9202  11

-6  -4   6 347.511 15.4045  11

-6   4  -6 337.273 12.9315  23

-6   4  -6 335.083 15.0859  22

-6   6  -4 356.144 15.3218  22

-6   6   4 341.088 13.5383  23

-4   6  -6 334.707 15.2197  22

-4   6  -6 332.045 13.8486  23

-6   6  -4 326.643 14.1053  23

-6   4  -6 341.517 12.8087  21

-6   4  -6 342.258 13.6880  20

4   6   6 361.190 15.7152  19

-6   6  -4 338.482 14.6467  20

6   6   4 323.951 15.0273  19

-6   6  -4 337.939 13.6912  21

6   4   6 366.102 13.9774  19

-4   6  -6 330.278 14.6877  20

4   6   6 338.386 13.4556  17

6   4   6 369.709 15.4989  17

6   6   4 363.506 16.5562  18

-6   4  -6 371.573 14.7918  15

-6   6  -4 336.268 12.2319  14

4  -6   6 364.961 14.3135  17

6   4  -6 335.072 13.9902  16

6   6  -4 358.994 15.3600  16

-6  -6   4 322.960 13.7106  17

4   6  -6 360.016 15.5660  16

6  -4   6 345.551 15.0209  17

6  -6   4 329.100 13.8156  17

6   6   4 335.621 13.7067  17

-6   6   4 346.229 14.0832  17

-6   6  -6 1048.40 29.9938  10

-6   6  -6 1074.90 28.5075   8

6   6   6 1129.72 29.6203   5

6  -6   6 1075.64 29.1929   5

-6   6  -6 1047.48 29.7306   6

-6  -6  -6 1118.52 30.3009   6

6  -6  -6 1079.44 29.3817   5

6   6  -6 1087.10 29.6474   5

-6   6   6 1060.19 31.2296  29

-6  -6   6 1069.30 29.7142  25

-6   6   6 1070.42 30.2337  25

-6   6   6 1074.73 26.9687  26

6   6  -6 1106.32 31.1021  12

6  -6  -6 1033.15 30.0247  12

-6  -6   6 1058.33 30.7327  11

-6   6   6 1116.75 31.5962  11

-6   6  -6 1084.83 30.6134  23

-6   6  -6 1052.41 28.0515  21

6   6   6 1098.22 32.5621  19

-6   6  -6 1124.99 31.9998  20

6   6  -6 1104.16 32.6036  16

-6   6  -6 1086.40 31.8554  15

6   6   6 1075.14 30.3658  17

6  -6   6 1055.40 30.8093  17

7  -1  -1 41.1510 5.01067  11

-7   1  -1 34.7560 4.29360  10

1   1  -7 30.5154 4.19514   8

-1   1  -7 33.6004 4.34359   8

-1  -1  -7 39.0156 4.48214   8

7  -1   1 45.7842 4.02910   3

1   1  -7 42.4450 3.48820   3

-1   1  -7 49.3849 4.12924   3

1  -1  -7 40.3439 4.61153   5

1   7  -1 39.6763 3.71387   4

-1   1  -7 48.3359 4.38553   2

1  -7   1 38.7860 3.39508   2

1  -1   7 58.4007 5.05884   5

-1  -1  -7 41.6301 4.47919   1

7   1   1 37.8739 3.58082   3

-1   7   1 38.9280 2.51872   4

-1  -1   7 43.9589 4.42681   5

7  -1  -1 35.6492 3.38177   3

1  -7  -1 39.5108 3.13796   2

-1  -1  -7 40.2385 4.64339   7

1  -1  -7 32.3886 4.20545   7

-1   7   1 40.3354 4.18728  28

1   7   1 33.0111 3.74932  26

-1   7  -1 35.9869 3.92870  26

-1   7   1 33.7301 3.74776  26

-1   7  -1 37.4186 4.25239  24

-1   7   1 33.6744 3.89655  24

-1   7  -1 42.1977 4.32532  22

-1   7  -1 32.2155 3.82876  23

-7  -1  -1 33.1663 4.02361  21

1   7   1 42.8028 4.57699  19

-1   7   1 35.3345 4.18911  22

-7   1   1 39.1318 4.39472  21

-7   1  -1 34.9065 4.13490  21

-7  -1   1 42.0721 4.76375  17

-7  -1  -1 41.0984 4.57530  17

-3   1  -7 1745.67 41.2464   7

1  -3  -7 1864.57 42.2010   7

-3  -1  -7 1716.16 42.1444   8

-3   7  -1 1835.67 40.8648   9

-1  -3  -7 1866.21 41.5469   8

-1  -3  -7 1867.43 42.6310   7

-7  -1  -3 1846.53 42.1678  10

-7   1  -3 1815.73 42.5201  10

-1   3  -7 1763.87 41.5973   8

-7   3  -1 1793.45 42.3429  10

-1   7  -3 1778.66 39.7219   9

7  -1  -3 1852.24 40.3837   4

3  -7  -1 1732.02 34.9602   5

1   3  -7 1840.99 37.2383   3

-7  -1  -3 1846.81 40.9731   3

7   1   3 1828.16 39.1710   2

-7  -3  -1 1847.08 38.6870   3

-7  -1  -3 1780.39 42.5133   6

-3   1   7 1788.96 41.5717   4

1   7  -3 1717.15 34.9440   1

-1   3  -7 1874.71 41.8784   2

1  -3  -7 1883.81 41.9141   5

1   3   7 1828.80 41.6228   5

-3   1  -7 1831.68 40.9104   3

-3  -1  -7 1747.74 41.2248   3

1  -7  -3 1781.50 35.1588   1

-1  -3   7 1828.95 42.9692   4

-1  -3   7 1878.26 41.8761   5

3  -1  -7 1878.41 42.8311   5

-3   1  -7 1811.73 40.8301   2

7  -1   3 1851.06 41.1383   3

1  -3   7 1830.96 41.4369   5

3   7  -1 1789.43 34.9894   5

-1  -3  -7 1829.04 41.9629   1

1   3  -7 1827.17 41.7925   5

3   1  -7 1757.17 36.6541   3

-1   3  -7 1858.76 42.1340   1

-3  -1  -7 1798.97 41.8944   6

-1   3   7 1810.54 41.7353   5

-3  -1   7 1793.28 42.5136   4

3   7  -1 1828.68 41.8446   4

7  -1   3 1920.92 43.6081   1

7  -3  -1 1785.89 37.3607   4

7  -1   3 1987.91 41.4855   2

7   1  -3 1901.61 42.3883   4

1   7  -3 1838.73 39.1592   2

7  -3   1 1780.06 40.7175   3

3  -7   1 1825.60 39.9584   2

-3  -1  -7 1843.42 42.4641   1

-3  -1  -7 1860.57 39.7553   2

3  -1   7 1910.61 42.5032   5

7   1  -3 1774.40 36.0151   3

-3   7  -1 1841.20 40.5987  30

-3   7   1 1823.62 41.0549  30

-1   7   3 1884.36 41.4853  30

1   7   3 1850.20 40.7541  30

-1   7   3 1785.86 40.0254  28

-3   7  -1 1810.88 40.8862  29

1   7   3 1842.25 40.4040  28

3   7   1 1792.38 41.2668  28

-1   7   3 1894.54 41.7810  29

1   7  -3 1747.33 40.2775  28

1   7  -3 1831.39 41.7808  30

-1   7  -3 1831.99 41.4721  30

3   7  -1 1793.47 40.6212  30

-1   7  -3 1780.81 40.3070  28

-1   7   3 1766.05 40.3570  26

-7  -1   3 1810.43 42.1112  25

-3  -1   7 1841.34 41.9646  25

1   7  -3 1861.15 40.9915  27

-3   7  -1 1810.56 41.4337  24

-7   3   1 1723.91 40.8559  25

-7  -3   1 1748.96 40.7448  25

-3   7   1 1767.29 40.9958  24

-3   7   1 1834.05 40.8729  26

-7   3  -1 1888.70 41.4420  14

-1   3  -7 1868.29 41.5707  12

-1  -7   3 1746.58 35.6896  11

7  -3  -1 1881.00 44.3618  11

-3  -1   7 1701.30 43.3848  11

7   3  -1 1814.11 43.8000  11

3   7   1 1792.30 35.8133  11

3  -1  -7 1819.69 42.6081  12

-3   7  -1 1836.68 40.6789  13

3  -7   1 1768.64 35.6848  11

-1   7  -3 1772.63 40.3967  13

7   3   1 1772.33 42.9773  11

7  -3   1 1761.81 43.3615  11

1   3  -7 1827.31 41.5297  12

-1   7   3 1750.75 40.5090  13

-1   7   3 1687.09 35.2979  11

7  -1  -3 1826.42 44.5774  11

-3   7   1 1796.36 39.9865  23

-3   7  -1 1837.25 40.9745  23

-1   7  -3 1750.87 40.9524  23

-1   7  -3 1751.09 40.8046  22

-3   7  -1 1871.74 41.8411  22

-7   3  -1 1879.79 41.1191  23

-7   3   1 1922.94 41.7680  23

-3   7  -1 1931.91 41.9709  20

-7   1   3 1857.40 40.5078  21

-1   7   3 1782.88 41.9206  19

-1   7  -3 1933.44 42.1197  20

3   7   1 1717.54 42.3402  19

-7   3   1 1877.83 42.1297  21

-7   1  -3 1842.38 41.4269  21

-7   1   3 1821.08 40.7680  14

-7   3  -1 1819.58 42.6088  17

1   7  -3 1860.73 41.8318  16

-7  -3  -1 1850.60 42.7041  17

3   7  -1 1777.31 41.8534  18

-7  -3   1 1832.08 43.0201  17

3   7   1 1798.49 42.2398  18

1   7   3 1650.82 34.9689  17

-7  -1   3 1766.62 43.6827  17

-7   3   1 1858.24 43.2153  17

7   3   1 1791.04 41.6176  18

7  -1   3 1837.04 43.7306  17

1  -7   3 1642.22 35.4302  17

-3  -3  -7 2.61980 2.43758   8

-3   7  -3 3.25534 2.36245   9

-7   3  -3 3.26526 2.67371  10

-7  -3  -3 7.62296 2.65125  10

-3   3  -7 5.08469 2.70490   8

-7   3  -3 6.92667 2.67372   9

7   3  -3 1.12079 2.16941   4

-3  -3   7 2.22460 2.15300   4

7  -3   3 3.10624 2.11262   1

-3  -3  -7 1.95844 1.89564   1

7   3   3 4.48093 2.13087   1

3  -7  -3 3.51411 1.44591   5

3   3   7 2.91199 2.12384   5

3   7  -3 2.01631 1.27765   5

-7  -3  -3 2.35164 1.75241   3

-7  -3  -3 3.07026 2.72213   6

-3   3  -7 2.34975 2.18650   2

3  -7   3 3.95668 1.51497   5

3   7  -3 3.20327 1.45613   2

3  -7   3 2.88453 2.25594   2

3  -3   7 4.76444 2.49710   5

3   3  -7 4.47397 2.39998   5

3  -3  -7 6.84127 2.56110   5

7  -3   3 2.45517 1.79255   2

-3  -3  -7 4.16575 1.60324   2

-7   3  -3 5.11725 2.83970   6

-3  -3  -7 5.26173 2.50703   6

-3   3  -7 2.45562 2.28492   6

-3   3  -7 1.99249 2.03278   1

-3   3   7 3.26264 2.00412   4

3   7  -3 3.54067 2.16477   4

3   7   3 7.84916 2.60880  28

3   7  -3 4.53612 2.34124  28

3   7  -3 5.39748 3.03598  30

-3   7  -3 6.90029 2.80977  30

-3   7   3 2.47498 2.16610  29

-3   7   3 4.21306 2.27419  26

-7  -3   3 4.84144 2.75834  25

-3  -3   7 3.32352 2.52583  25

-3   3   7 1.44525 2.19786  25

-7   3   3 12.8049 3.20849  25

3   7  -3 4.21886 2.34143  27

7   3  -3 4.90515 3.16411  11

7  -3  -3 2.98449 2.88145  11

-3   3   7 2.93867 2.57160  11

3   3  -7 11.2800 3.43705  12

-7   3   3 0.98765 2.38414  14

3  -3  -7 4.99703 2.88319  12

-3   7  -3 6.62131 2.56246  13

-3  -3   7 2.34070 2.66935  11

-7   3  -3 2.93794 2.13229  22

-7   3  -3 2.84797 1.99932  23

-3   7  -3 0.47615 2.81515  23

-3   7  -3 2.02948 2.40538  22

-3   7   3 6.70609 2.22731  23

-7   3  -3 3.86077 2.64173  21

3   7   3 4.69380 2.67642  19

-7   3   3 3.34391 2.42668  21

-3   7   3 2.98736 2.31640  22

-3   7  -3 4.64127 2.35260  20

-3   7   3 4.36360 2.69061  19

7  -3   3 1.68991 2.35525  17

3  -7   3 3.06708 1.43842  17

-7  -3   3 1.14582 2.39538  17

-7   3  -3 5.99605 2.47137  15

-3   7  -3 6.31071 2.56982  15

7   3   3 1.68418 2.40246  17

-3  -7   3 3.18760 1.53360  17

-7   3   3 5.77743 2.78903  17

-3   7   3 3.88751 1.51489  17

3   7  -3 3.76137 2.68508  16

3   7   3 4.23448 1.70128  17

7   3   3 6.46000 2.83111  18

-3   3  -7 0.43852 2.36705  15

-5   7  -1 2022.37 46.4154   9

-1  -5  -7 2007.04 44.5617   8

-7  -1  -5 2001.23 47.5833  10

-5  -1  -7 2022.12 47.6520  10

-7   5  -1 1885.55 46.3684  10

-5  -1  -7 1934.89 47.6581   8

-5   1  -7 1882.64 47.0853   8

-1   5  -7 1968.58 45.7997   8

-7   5  -1 1966.05 45.2695   9

1  -5  -7 2005.34 45.9036   7

-7   1  -5 1939.24 47.5784  10

5   7  -1 1898.48 38.2849   2

-1  -7   5 1918.60 40.0418   3

5   7   1 1926.85 41.4256   1

1  -7  -5 1971.84 41.6938   1

-7  -1  -5 1995.36 45.6680   3

1  -5   7 1948.67 46.0417   4

7   1  -5 1910.62 38.2558   3

5  -7   1 1984.92 44.8712   2

1   5  -7 1984.22 45.7435   2

1   7  -5 1948.30 41.7049   1

-1   5  -7 2091.16 45.4299   1

5  -1  -7 2068.52 47.5419   5

-1   7  -5 1932.60 41.5722   1

-5   1   7 1991.60 45.9841   4

5   7  -1 2050.49 47.6520   4

7  -1   5 2002.00 44.6732   2

-7  -1  -5 1954.89 47.7822   6

1  -7   5 1993.42 41.3927   5

1  -5   7 2006.27 44.6033   5

1  -7   5 1957.36 42.3439   3

1   5   7 1990.30 44.8222   5

-5  -7   1 1939.48 39.3240   3

1   7   5 1973.42 41.6227   5

-5  -1  -7 1973.75 47.4420   6

-1  -7  -5 1996.52 41.7186   1

7   1   5 1972.29 42.7930   2

7  -1   5 2131.14 48.4733   1

-5  -1  -7 2038.87 46.3040   3

-1  -5   7 2023.09 47.1712   4

-7   5  -1 1952.15 44.7756   6

-7  -5  -1 1889.92 44.4396   6

-1  -5  -7 2021.68 45.0636   1

1  -7   5 2061.85 45.1084   4

-5  -1   7 2042.19 47.2954   4

1   7  -5 2055.33 44.7446   2

-7  -5  -1 1974.39 41.6813   3

5  -7   1 1958.57 41.4662   1

-5   7   1 1978.17 46.8465  29

-5   7  -1 1941.19 44.2221  30

1   7   5 2019.36 45.2876  30

1   7   5 2035.80 43.6332  28

1   7  -5 1943.51 43.7114  28

-5   7   1 2081.88 45.5814  30

5   7  -1 1928.59 44.3042  30

-1   7  -5 1990.90 46.2931  30

-1  -5   7 1948.30 43.8968  25

-7   5   1 1961.49 43.3421  24

-1   7  -5 2036.97 46.6054  27

-7  -1   5 1978.86 47.3527  25

-1   5   7 1964.95 44.1287  25

1   7  -5 1994.56 43.5363  24

-5   7   1 2026.93 45.6240  24

1   7  -5 1946.63 46.1037  27

-1   7   5 2091.44 45.9210  26

-5  -1   7 1960.53 47.2464  25

-1   5  -7 2017.80 45.6560  27

-1  -5  -7 2055.81 44.4773  12

5  -1  -7 1968.92 48.1368  12

7  -5   1 2012.98 46.6950  11

5   7  -1 1874.98 42.7127  11

-7  -1   5 2038.72 49.2968  11

-1   7   5 1995.34 44.9506  13

5  -7  -1 1994.66 42.6903  11

-1   7   5 1947.66 42.7368  11

-1   5  -7 1994.46 44.7179  12

1  -5  -7 2045.28 44.5327  12

5  -7   1 1920.25 42.3906  11

7   5   1 1979.79 46.4096  11

7   5  -1 1981.31 46.9171  11

7  -5  -1 1976.58 46.6031  11

1   7   5 1974.69 43.7913  13

-1  -7   5 1970.84 42.7286  11

1   5  -7 2010.40 44.9054  12

5   7   1 1998.88 43.0848  11

-5   7  -1 1996.29 44.9183  13

-5  -1   7 1948.27 49.0562  11

7  -1  -5 2018.61 48.9457  12

-7   5   1 2031.34 46.1729  23

-1   7  -5 1815.05 45.5031  23

-5   7   1 1956.26 45.3337  23

-5   7   1 1938.32 45.4925  22

1   7  -5 2006.69 44.0908  22

-1   5  -7 1990.75 45.7842  22

1   5  -7 1982.62 43.7042  22

-5   7  -1 1955.62 45.8446  23

-5   7  -1 1955.00 46.1571  22

-1   5  -7 1909.50 44.3910  23

-1   7  -5 1987.85 45.7672  22

-7   5  -1 1971.97 44.4685  22

-7   5   1 1973.58 43.4671  22

1   5   7 1911.50 46.8070  19

-7   5   1 1958.97 46.8549  21

1   7   5 2000.98 48.1023  19

-7   5  -1 2003.72 46.7895  21

-7   1   5 2000.93 43.5012  21

-5   7  -1 2057.08 47.1211  20

-7   5   1 1996.46 46.2181  14

7  -1   5 2002.52 48.3683  17

-5   7  -1 1980.33 44.8950  15

-7  -5   1 1947.71 45.7305  17

-1   7  -5 1991.13 44.3938  15

-7   1  -5 2021.06 43.8507  15

-5   7   1 2000.27 41.9615  17

-7   5  -1 1980.44 45.3651  14

-5  -7   1 1918.31 41.7461  17

-7   5   1 1976.03 45.9334  17

-7  -1   5 2029.11 43.4767  14

5   7  -1 1872.35 47.6694  18

7   5   1 1979.72 47.8345  18

-5   1  -7 2007.66 44.0156  15

1   7  -5 1928.02 46.7353  16

-5   3  -7 49.2234 5.00810   7

-5   3  -7 55.7525 5.99101  10

-7  -3   5 44.4533 5.86565  11

-7  -5  -3 46.1285 4.77914  10

-3   5  -7 44.7117 5.22922   8

-5  -3   7 48.2080 6.03178  11

-7   5  -3 44.5065 5.61828  10

-7   5  -3 43.5718 5.18174   9

-5   3   7 50.4591 6.08882  11

-7  -3  -5 48.1694 5.64808  10

-7   3  -5 46.8660 5.75163  10

-5   7  -3 52.6109 5.81411   9

-5   3  -7 48.3498 5.62686   8

-3  -5  -7 45.9730 5.55794   8

7  -3   5 38.2774 5.04218   1

-3  -5   7 44.3852 5.90349   4

7  -5   3 50.2371 4.98999   1

7  -5   3 54.4530 5.43831   2

5  -7   3 52.9932 5.25608   3

7   5   3 44.9548 4.79339   1

5   3   7 46.4607 5.40542   5

5  -7   3 41.2438 4.62300   2

-5  -3  -7 51.8389 5.74864   6

-5   3  -7 50.4207 5.74692   6

7  -5   3 54.8863 5.36033   3

3   5   7 44.7845 4.71611   5

7   3  -5 53.1903 5.92311   4

3   7  -5 51.2555 4.33383   5

-7   5  -3 52.7038 5.32595   6

7   3  -5 45.8773 5.51844   5

-3  -5  -7 51.3461 5.11793   1

-7  -5  -3 57.2473 4.89602   3

7  -3  -5 61.4330 6.02038   5

-7   3  -5 62.3119 6.27547   6

5   7  -3 46.1378 3.75576   2

3   5  -7 50.6012 5.25541   5

7   3   5 58.3891 5.87517   1

-3   5  -7 49.8567 5.05563   1

5  -7  -3 46.3531 4.12312   5

-7  -5  -3 58.9022 5.70177   6

3   7   5 51.4129 4.31910   5

5   3  -7 40.4194 5.06174   5

3  -5   7 42.0601 4.75802   5

3  -5   7 51.7451 4.79725   3

5  -3   7 39.1494 5.01197   5

-3   5  -7 48.8261 5.44917   2

3  -7   5 60.2155 5.05939   3

3  -5  -7 45.0171 4.79003   5

7  -3   5 43.8184 5.07504   3

-3   7   5 44.7172 2.67618   4

-7  -3  -5 47.4798 4.92286   3

5   7  -3 43.2607 4.09855   5

3  -7   5 46.0060 4.08729   5

5   7   3 53.0932 4.34400   1

3  -7   5 45.2581 4.41717   4

7   5  -3 56.0087 6.10421   4

5  -3  -7 46.1417 5.26406   5

-3  -5  -7 45.0464 3.04038   2

5  -7   3 47.4912 3.04931   4

3  -7  -5 48.2093 4.16103   5

-5  -3  -7 48.5147 5.37540   3

-5   3   7 51.5214 4.78551   4

3   7  -5 43.0322 4.47185   2

-7  -3  -5 53.4377 5.98885   6

5  -7   3 49.7840 4.29010   1

7  -3   5 55.2128 5.59534   2

5   7  -3 44.6199 5.69354   4

-5   3   7 48.2217 4.90930  29

-7   3   5 47.8938 4.70539  29

-3   7  -5 43.6282 5.06984  30

3   7   5 42.0692 4.69298  28

-5   7  -3 49.0761 4.90840  30

-7   5   3 50.3094 5.52282  29

3   7  -5 43.2896 4.79567  28

-3   7   5 49.5530 5.65517  29

5   7  -3 52.2473 5.65636  30

-5   7   3 41.7687 5.53448  29

3   7   5 39.1672 4.60699  30

-3   7   5 37.9699 4.54262  26

-5   3   7 50.0259 5.93600  25

-7  -3   5 58.5946 6.03464  25

-5   7   3 46.5636 5.10993  26

-3  -5   7 48.7469 5.31904  25

-5  -3   7 42.2920 5.55451  25

-3   5   7 45.5794 4.24575  26

-3   5   7 45.7052 5.08814  25

-7  -5   3 51.2002 5.32300  25

-7   5   3 36.2792 4.82871  25

-7   3   5 45.3523 5.53489  25

3   7  -5 48.1751 5.55106  27

-7   5  -3 41.3339 4.76279  14

3   7   5 50.5461 4.78259  13

3   5  -7 38.9703 5.06462  12

-5   7  -3 49.1202 4.92903  13

7  -3  -5 50.4938 6.13749  12

-3  -7   5 45.4262 4.57359  11

3  -5  -7 48.6876 5.25220  12

7   5  -3 46.6926 5.56223  11

-3   5   7 52.6453 5.83252  11

-3   7   5 53.9114 4.97500  11

7  -5  -3 43.4912 5.33874  11

5   3  -7 36.2621 5.53896  12

7   3  -5 50.1829 6.45624  12

-3  -5   7 47.5682 5.71216  11

5  -3  -7 49.6685 6.07863  12

-5   7   3 36.7181 4.71515  23

-7   3  -5 55.9543 5.17363  23

-3   5  -7 41.9521 5.47080  22

-7   5  -3 49.9680 5.36591  23

-7   5  -3 50.5924 5.35433  22

-3   5  -7 40.8576 4.64247  23

-3   7  -5 53.8839 5.62576  23

-7   3  -5 52.0897 5.56673  22

-3   7  -5 54.1898 5.93546  22

-5   3  -7 40.9514 4.14731  23

5   3   7 50.6764 4.88096  19

-5   7   3 45.8944 5.52977  22

-7   3  -5 48.1572 5.23758  21

-7   3  -5 45.2355 4.56396  20

5   7   3 60.4530 6.76421  19

-7   5  -3 43.8773 5.31059  20

-5   3  -7 51.7725 5.06541  20

-7   3   5 38.8065 4.73230  21

-7   5   3 52.1535 5.94919  21

-7   5   3 42.4559 4.53248  22

-5   7  -3 53.3254 5.39725  21

-7   5  -3 48.7532 5.76037  21

3   5   7 43.5247 5.42417  19

3   7   5 60.1905 6.66865  19

7   3  -5 54.3618 5.12570  16

3   7  -5 54.0602 6.19699  16

-3   7  -5 42.1877 4.95699  15

-7   3  -5 53.3686 5.58006  15

7   3   5 57.4637 6.24794  17

5  -7   3 52.6440 4.64730  17

5   7   3 40.7708 5.86705  18

-3   5  -7 46.4566 5.44084  15

-7   5  -3 44.3300 5.26330  15

-5   7   3 43.3824 4.37502  17

7  -3   5 47.3763 5.77625  17

7  -5   3 47.4132 5.63244  17

-7   5   3 47.1352 5.42420  17

7   5   3 47.1310 5.26301  17

-5   7  -3 47.3098 5.18589  15

3   7   5 47.2933 4.37056  17

-5   3  -7 51.6745 5.45459  15

3  -7   5 46.1722 4.42297  17

-5  -7   3 53.5073 4.70754  17

7   5   3 47.2312 6.21778  18

-7  -5   3 50.5135 5.61022  17

-7   5  -5 122.560 7.95561   8

-5   7  -5 116.188 7.40305  10

-7  -5  -5 123.834 8.49684  10

-7   5  -5 119.481 8.86277  10

-5   5  -7 121.490 7.03233   7

-5   5  -7 138.882 9.00463   8

-5   5  -7 135.677 8.88745  10

5  -7  -5 137.606 7.61839   5

-7  -5  -5 134.598 9.00635   6

7   5  -5 125.885 8.55642   5

-7  -5  -5 117.414 7.97871   3

5   5  -7 118.458 8.27382   5

5   7  -5 116.004 7.29762   5

5  -5   7 123.372 8.24368   5

-5   7  -5 101.253 6.83129   6

-5  -5  -7 145.113 9.22873   6

7  -5  -5 121.941 8.27566   5

-7   5  -5 120.196 8.47973   6

-5   5  -7 126.828 8.80051   6

5   5   7 131.269 8.53726   5

5  -5  -7 113.430 7.98261   5

5  -7   5 135.995 7.65441   5

5   7   5 127.658 7.43577   5

-5   5   7 120.598 6.67795   4

7  -5   5 126.833 8.34781   1

7   5   5 132.160 8.71035   1

5   7   5 128.409 8.23239  28

-5   5   7 135.051 8.75008  29

-7   5   5 115.198 8.35146  29

5   7  -5 125.990 8.47309  28

-5   7   5 137.548 9.53603  29

-5   7  -5 130.658 7.90251  30

-5   7   5 115.076 7.36261  25

-5   7   5 123.227 7.76190  26

-7   5   5 115.437 8.44704  25

-5   5   7 138.850 9.17386  25

-7  -5   5 138.442 9.01670  25

-5  -5   7 128.811 8.90283  25

-5   5   7 132.880 9.52199  11

-5  -5   7 121.330 9.05077  11

7  -5  -5 116.677 8.87555  12

5  -5  -7 122.138 8.83048  12

5   7  -5 113.672 7.64651  12

-5   7  -5 122.619 7.38419  13

7   5  -5 120.860 9.25972  12

5   5  -7 122.517 9.17063  12

-5   5  -7 133.173 8.29072  23

-7   5  -5 118.981 8.22099  23

-7   5  -5 120.316 9.18811  22

-5   7   5 131.814 7.75862  23

-5   7  -5 129.338 9.66932  22

-5   7  -5 122.220 8.93262  23

-5   5  -7 124.360 9.73352  22

-7   5  -5 128.418 8.67557  20

5   7   5 110.749 9.43582  19

-5   7  -5 131.831 7.82340  21

5   5   7 120.780 8.77931  19

-5   7  -5 133.397 9.74974  20

-5   5  -7 137.183 9.14941  20

7   5   5 130.827 8.99634  19

-7   5  -5 137.827 8.81092  21

-5   5  -7 134.811 9.27891  15

7  -5   5 137.495 9.45952  17

5  -5   7 131.534 9.04427  17

7   5  -5 125.380 8.91813  16

5   7  -5 114.873 9.37663  16

5   5   7 136.641 9.10491  17

7   5   5 139.774 9.35368  17

5  -7   5 120.514 7.87659  17

-5   7  -5 125.736 8.92562  15

-7   5  -5 134.544 7.99270  14

5   7   5 140.688 8.16341  17

-7   5  -5 109.221 8.43151  15

-7   5   5 120.620 9.06475  17

7   5   5 140.881 10.4645  18

7  -7   1 1.96969 2.33391  11

7   7   1 3.05035 2.36455  11

-7  -1  -7 2.26594 2.92291  10

-7   7  -1 2.96686 2.75974  10

-7   1  -7-0.74494 2.88278   8

-7   7  -1 2.61318 2.52815   9

1  -7   7 2.21129 2.01707   4

-1  -7   7 2.48119 2.65379   4

-7  -1  -7 5.41575 3.38430   6

-1  -7  -7 1.65155 1.88315   1

1  -7  -7 0.51353 2.43393   7

1  -7   7-0.70259 1.63404   3

-7  -7  -1 2.43558 1.49565   3

1  -7   7 1.62811 1.78065   5

1  -7  -7 2.52769 1.84299   1

1   7  -7 2.15452 2.19722   2

1   7   7 0.83807 1.66619   5

1   7  -7 5.19850 2.40359   1

7  -7   1 1.97054 1.43813   1

-7   7  -1 1.25377 2.01721   6

7   7   1 5.31749 2.00928   1

-1   7  -7 0.42283 1.76752   1

-7   7   1 9.78776 3.28907  30

1   7  -7-1.13008 2.61672  28

-7   7  -1 2.19716 2.23172  30

-1   7  -7 3.95979 3.18527  27

-1   7   7 2.04101 2.03945  25

-7  -1   7 0.75242 3.14496  25

-1   7   7 1.73130 2.41225  26

1   7  -7 3.81394 2.25392  12

7  -1  -7 2.43726 3.31390  12

-1   7   7 1.54225 2.29724  13

-1  -7   7 0.49482 2.01854  11

1   7   7 1.27893 2.05769  13

7   7  -1 2.56027 2.24000  11

-1   7   7 1.49360 1.92677  11

7  -7  -1 1.47578 2.19824  11

-7   7  -1 3.15785 2.71562  13

-1   7  -7-0.60944 2.77941  22

-1   7  -7 0.62196 2.66089  23

-7   7   1 1.08574 2.26920  24

1   7  -7 0.48991 2.23436  22

-7   7   1 0.62151 2.59784  23

-7   7  -1 1.94126 2.63957  23

1   7   7 3.81897 3.61994  19

-7   7   1 1.10337 2.61474  22

-7   7  -1 0.68045 2.91109  21

-7   7  -1 0.60627 2.65208  22

-7  -7   1 1.79784 2.00851  17

-7   1  -7 0.48471 2.25442  15

7   7  -1 0.82865 3.46358  18

-7   7   1 3.67056 2.13403  17

7   7   1 3.21283 3.51346  18

-1   7  -7 1.76283 2.78500  15

-7  -1  -7 1.50601 1.88111  15

-7  -3  -7 668.356 24.1419  10

-3  -7  -7 674.747 21.5642   8

-7   3  -7 629.265 23.1513   8

-7   7  -3 673.523 23.7265   9

-7   7  -3 658.155 22.0289  10

-7   3  -7 680.644 24.7328  10

-7  -7  -3 682.091 20.0062   3

-3   7   7 637.480 17.4963   4

7  -7  -3 697.339 20.6201   5

3   7   7 659.532 20.1006   5

-7  -7  -3 666.031 20.1849   6

7   7   3 671.431 20.3108   1

3  -7   7 670.100 20.1436   5

3   7  -7 668.144 21.2485   2

3  -7   7 687.847 20.5425   3

-7   7  -3 641.944 20.0738   6

7   7  -3 681.843 20.5209   5

7  -7   3 642.466 19.8320   1

-7   3  -7 680.222 24.3217   6

3  -7   7 659.507 20.9918   4

-7  -3  -7 676.322 24.3963   6

3   7  -7 680.859 20.0066  28

-7   7   3 676.525 24.1106  29

-7   3   7 677.721 20.1403  29

-7   7   3 656.356 22.2410  30

-3   7   7 719.406 24.5321  29

-7   7  -3 649.800 19.3267  30

3   7   7 686.628 20.7846  30

3   7  -7 687.113 24.1209  27

-7  -3   7 692.884 24.4688  25

-7   7   3 657.100 20.4502  25

-3   7   7 678.989 20.7155  25

-3   7   7 645.917 20.4794  26

-7   3   7 672.656 24.3444  25

-3  -7   7 646.344 20.0056  25

-7  -7   3 638.479 20.0520  25

7  -7  -3 682.823 21.0629  12

3   7  -7 675.328 20.8378  12

-3  -7   7 709.643 22.0867  11

7  -7   3 695.102 21.6473  11

-3   7   7 680.686 21.8719  11

7   7   3 657.351 21.2757  11

7   7  -3 668.350 21.1961  12

-7   7  -3 682.772 20.3535  13

7   3  -7 657.721 25.0218  12

3  -7  -7 689.234 20.3638  12

7  -3  -7 647.489 24.3872  12

-3   7  -7 692.303 22.9480  23

-7   3  -7 679.190 19.7873  23

-7   7   3 663.982 22.2305  23

-3   7  -7 684.712 24.2158  22

-7   3  -7 662.023 24.0550  22

-7   7  -3 695.247 23.9480  22

-7   7   3 703.283 22.1610  22

-7   7   3 677.344 21.1825  24

-7   7  -3 734.124 24.4466  20

-3   7  -7 726.880 24.9173  20

7   7   3 650.310 24.1588  19

-7   3   7 670.917 20.9759  21

3   7   7 664.443 24.8288  19

-7   3  -7 676.092 20.0865  20

-7   7  -3 642.495 22.7675  21

-3   7  -7 671.990 23.1012  15

-7  -7   3 683.473 21.3059  17

-7   7   3 653.796 20.9716  17

3   7   7 675.421 20.5401  17

7   7   3 698.934 25.8962  18

-7   7  -3 626.156 20.4466  14

-7   3  -7 650.694 22.1943  15

-5   7  -7 944.285 26.4863   8

-7   7  -5 905.064 27.7982  10

-7   5  -7 892.286 27.9626   8

-5   7  -7 925.746 26.4281  10

-7   5  -7 931.970 29.8356  10

-5   7  -7 924.901 26.8953   6

5   7   7 883.017 25.7372   5

-7   7  -5 916.247 26.7296   6

-7  -7  -5 948.379 26.9189   6

7   7  -5 910.360 26.1938   5

-7  -5  -7 934.496 29.7024   6

-7   5  -7 894.122 29.0342   6

-5  -7  -7 963.413 27.4775   6

5   7  -7 906.621 26.2942   5

-7   5   7 923.684 27.9162  29

5   7  -7 976.837 26.7899  28

-5   7   7 929.031 29.8235  29

-7   7   5 893.359 29.6490  29

5   7   7 986.134 26.1678  28

-7  -7   5 960.121 27.1002  25

-7   7   5 921.537 27.2304  25

-5   7   7 906.515 25.4546  26

-7  -5   7 886.608 28.9627  25

-5   7   7 910.077 26.9956  25

-7   5   7 953.387 29.9477  25

-5  -7   7 889.769 26.4102  25

5   7  -7 936.909 27.7757  12

7  -7  -5 935.625 27.4817  12

7   7  -5 904.551 27.6002  12

5  -7  -7 929.476 27.0934  12

-5   7   7 913.142 27.7117  11

7   5  -7 898.746 30.1968  12

7  -5  -7 916.856 29.8776  12

-7   7  -5 909.151 30.5682  22

-5   7  -7 943.344 31.4064  22

-7   5  -7 893.165 26.7832  23

-7   5  -7 931.776 31.0805  22

-7   7  -5 923.553 29.2514  23

-5   7  -7 904.938 28.4927  23

-7   7  -5 935.543 30.1353  20

7   5   7 978.098 28.7704  19

-7   5  -7 894.118 25.9270  21

-7   7  -5 904.969 27.5119  21

7   7   5 934.184 30.9652  19

-7   5  -7 973.711 28.4634  20

-5   7  -7 943.059 30.5705  20

5   7   7 995.328 31.7239  19

-7   7  -5 891.665 24.8064  14

-7   5  -7 915.659 29.5397  15

-7   7   5 933.936 27.7616  17

5   7   7 917.579 26.8606  17

7   7   5 941.466 27.4165  17

-7   5  -7 936.695 25.1634  14

7   7  -5 886.022 30.1408  16

-7   7  -7 4.29760 3.20125  10

-7   7  -7 1.11878 2.39418   8

-7   7  -7 5.55760 3.35356   6

-7  -7  -7 7.60153 3.51002   6

-7   7   7 5.05009 4.06278  29

7   7  -7 3.90612 3.19840  28

7   7   7 3.63454 2.87175  28

-7   7   7 4.33940 3.29899  25

-7  -7   7 5.46721 3.47120  25

7   7  -7 5.32480 3.32813  12

7  -7  -7 1.44863 3.55831  12

-7   7  -7 6.09095 3.86705  23

7   7   7 1.81423 3.79210  19

-7   7  -7 5.91429 3.32675  21

-7   7  -7 5.05806 4.41749  20

-7   7  -7 2.69585 3.75658  15

-8   0   0 11592.2 228.771  10

0   0  -8 12460.6 229.816   8

8   0   0 12328.8 225.130   3

0   0   8 12275.4 229.011   5

0   0  -8 12245.4 229.778   1

0   0  -8 12304.2 226.078   3

0   8   0 12271.8 223.343   4

0   8   0 12070.5 227.772  30

0   8   0 11999.3 228.008  28

0   8   0 11703.9 226.712  26

0   0  -8 12283.2 229.543  12

0   8   0 12311.7 228.347  13

8   0   0 12192.1 231.812  11

0   8   0 12336.4 227.802  22

0   8   0 12202.2 227.544  24

0   8   0 11990.3 226.283  23

-8   0   0 12261.2 228.467  21

0   8   0 11974.8 228.019  19

0   8   0 12864.0 226.480  20

-8   0   0 12385.4 231.094  17

-8   0  -2 1.11656 2.49452  10

0  -2  -8 1.05264 2.44773   8

8  -2   0 0.64373 2.62572  11

0   8  -2-0.34431 1.63180   9

8   2   0 0.63260 2.51499  11

-2   0  -8-1.15928 2.47970   8

-8  -2   0 0.97000 2.54112  10

2   8   0 1.66253 1.81804   4

8   0  -2-0.92470 2.02239   4

2   0   8-0.52085 1.83987   5

-2   0  -8 0.54862 2.00154   1

0   2  -8 1.08331 2.31720   1

-2   0  -8 0.55712 2.15581   7

0  -2   8 1.51492 2.43712   5

2  -8   0 0.33203 1.17289   2

0  -8  -2 0.17215 0.80063   2

-2   0  -8-0.85108 1.69180   2

8  -2   0 0.40297 1.47018   3

0   2  -8 0.65489 1.26710   3

8   0  -2 0.28290 1.23746   3

0   2   8-1.02292 1.74545   5

-2   0  -8-0.44531 1.46441   3

8   0   2 0.40766 1.62071   3

-8   0  -2 2.39260 2.55888   6

0  -2  -8 1.14297 2.38860   7

2   0  -8 1.08983 2.04920   5

2   8   0 0.50599 2.11485  28

2   8   0 0.47139 1.87409  30

0   8   2-1.34580 2.04578  29

0   8   2 14.2156 3.46314  30

0   8   2 0.47504 2.25134  28

0   8  -2-0.48385 2.06989  28

-2   8   0-0.97059 2.54269  30

-2   8   0 0.45601 2.03754  29

-2   8   0 7.16450 2.72054  26

-8   0   2-0.55826 2.27710  25

0   8  -2 0.42580 1.86254  26

2   8   0 0.41709 1.70128  26

-2   0   8 1.57202 2.34138  25

0   8   2-0.46813 2.04767  26

0  -2  -8 0.53022 2.41798  12

-8   0   2-0.47427 2.11914  14

2   0  -8-0.57224 2.50305  12

-2   0  -8-0.55068 2.35582  12

8   0  -2 1.35799 2.76955  11

0   2  -8-1.07734 2.35622  12

0   8  -2-0.49585 2.43543  13

0   8  -2-1.35791 2.22320  24

-2   8   0 1.00461 2.29070  24

-2   8   0-0.43589 2.02717  23

0   8  -2 2.41403 2.45178  23

2   8   0 2.87870 2.37223  22

0   8   2 1.01884 2.12920  22

0   8  -2 0.92489 2.10891  20

2   8   0-0.56700 2.36985  19

0   8  -2-0.44102 1.97058  19

-2   8   0-0.51077 2.28224  22

0   8   2 1.09451 2.49567  19

-8   2   0 0.53522 2.62881  21

0   8  -2 0.92603 2.23461  22

-8   0   2 0.46324 2.35245  21

-8   0  -2 0.52409 2.90758  21

-2   8   0 2.82059 2.30896  20

-8   2   0 0.59424 2.42383  17

-8   0   2 3.13977 2.36146  17

0   8  -2 0.92113 2.18274  16

-8  -2   0 1.16720 2.38046  17

2   8   0-0.49230 2.05765  18

-2  -2  -8 688.809 22.2785   8

-8  -2  -2 669.026 21.3147  10

-2   2  -8 689.027 21.5175   7

-2  -2  -8 629.894 21.9604   7

2  -2  -8 691.273 22.2656   7

2  -2  -8 700.810 21.5050   8

-2   8  -2 656.905 20.1489   9

-2   2  -8 650.819 21.9839   8

8  -2  -2 698.873 19.4993   3

-2   2  -8 682.989 20.8515   2

2   2  -8 680.744 21.6585   5

-2   2  -8 671.161 21.7065   1

-2   2  -8 721.959 20.1635   3

2  -8   2 666.467 19.1978   2

-2  -2  -8 699.329 19.3571   2

-8   2  -2 675.256 22.3706   6

2  -2  -8 699.168 21.9241   5

-8  -2  -2 676.663 22.2629   6

2   2  -8 664.275 16.9943   3

2  -2   8 691.763 21.4458   5

2   2   8 652.245 21.1545   5

-2  -2  -8 710.716 21.3186   3

2   8  -2 684.939 20.5862   4

8  -2   2 653.798 20.1874   3

2  -8  -2 727.847 18.6013   2

8  -2  -2 699.930 19.0929   4

-2  -2  -8 676.628 21.7211   1

8   2  -2 673.844 21.9851   4

-2   8  -2 691.659 21.3111  30

2   8  -2 679.965 21.4571  30

2   8   2 699.139 21.3501  28

-2   8   2 690.075 21.3054  29

2   8   2 673.366 20.5482  30

2   8  -2 670.671 21.1976  28

2   8  -2 668.619 20.0326  27

-2  -2   8 659.996 21.2741  25

-2   8   2 652.923 20.5999  26

2   8   2 730.237 21.8151  26

-8  -2   2 672.473 21.7475  25

-8   2   2 661.828 21.6652  25

-2   8  -2 709.126 21.6844  24

2   8  -2 675.211 19.4305  26

-2   2   8 652.010 21.2136  25

2  -2  -8 691.217 22.2309  12

8   2  -2 683.231 23.5581  11

-2  -2  -8 672.781 21.6905  12

8  -2  -2 701.648 23.8064  11

2   2  -8 702.537 22.4299  12

-2   8   2 710.042 21.6015  13

-2   8  -2 649.575 20.5960  13

-2   2  -8 671.475 21.8224  12

2   8   2 694.160 21.0066  13

-2   8  -2 722.103 22.0701  22

2   8  -2 694.784 19.6517  22

-2   8  -2 671.044 21.0588  23

-2   8   2 666.544 19.2855  23

-2   8  -2 741.809 22.1836  20

-8   2   2 688.156 21.4322  21

-2   8   2 656.162 20.9767  19

2   8  -2 658.484 20.5778  18

-8  -2   2 697.923 23.0444  17

8   2   2 678.158 20.5941  18

-2   8  -2 670.425 18.6901  15

2   8   2 672.413 21.9101  18

-8   2   2 684.317 22.8186  17

-8   2   2 689.495 21.5172  14

-4   0  -8 2303.41 55.8012   8

-8   0  -4 2417.00 56.1833  10

-8  -4   0 2482.31 52.0668  10

0  -4  -8 2480.95 53.6536   8

0  -4  -8 2466.60 55.7782   7

0  -4  -8 2482.67 54.3065   1

4   0   8 2486.89 55.1450   5

8   0   4 2519.73 52.2072   2

8  -4   0 2366.53 52.8720   3

0  -8   4 2520.29 50.0260   3

8   0  -4 2378.34 48.0894   3

8   0  -4 2435.08 53.5515   4

0   4   8 2411.48 53.7086   5

-4   0   8 2453.29 54.6511   4

4   0  -8 2468.53 55.3717   5

4  -8   0 2329.68 46.2891   1

-8   0  -4 2360.97 56.3376   6

4   8   0 2257.37 45.8705   1

-4   0  -8 2460.72 53.8608   3

0  -4   8 2431.34 53.6387   5

-4   0  -8 2413.51 55.9360   6

0  -4   8 2313.51 54.7139   4

-4   0  -8 2414.49 55.0565   1

-4   0  -8 2469.03 52.3105   2

4  -8   0 2443.31 52.0929   2

8  -4   0 2383.58 47.9727   4

0   4  -8 2392.20 54.1182   1

8   0   4 2527.64 56.3628   1

4   8   0 2497.93 54.7423   4

4   8   0 2343.30 54.6830  28

-4   8   0 2324.66 54.3829  29

-4   8   0 2331.66 53.3986  30

0   4  -8 2470.72 53.5225  27

4   8   0 2386.04 53.1342  30

0   8   4 2446.23 54.4443  30

0   8  -4 2381.06 53.0770  28

0   8   4 2373.57 52.6646  28

-4   0   8 2465.01 55.9738  25

-8   0   4 2338.86 55.6719  25

0   8  -4 2412.47 54.5024  27

4   8   0 2444.19 52.3880  26

0   8   4 2396.54 54.3504  26

0   8  -4 2425.77 53.0530  24

0  -4  -8 2426.46 53.9410  12

0   8   4 2455.52 53.4366  13

8   0  -4 2415.57 57.5222  11

0  -8   4 2269.42 46.9338  11

-4   0   8 2360.37 56.9897  11

0   8   4 2187.73 46.2842  11

8  -4   0 2455.04 56.3150  11

0   4  -8 2426.77 54.3556  12

8   4   0 2297.67 55.2939  11

-4   8   0 2394.51 54.1109  13

4   0  -8 2398.81 56.4688  12

0   4  -8 2389.67 52.8563  22

0   8  -4 2330.13 53.0995  22

0   8  -4 2365.62 54.6757  23

-8   4   0 2411.21 50.5207  22

-4   8   0 2393.14 53.7547  23

-4   8   0 2522.41 55.5000  20

-8   4   0 2415.09 55.3919  21

-8   0   4 2370.28 51.9884  21

-8   0  -4 2456.77 51.0909  15

4   8   0 2359.11 55.8347  18

-8   0   4 2401.15 56.9738  17

-4   0  -8 2348.69 51.2308  15

-8   0   4 2371.77 52.8458  14

8   4   0 2407.21 56.0034  18

-8   4   0 2483.14 55.3088  17

0   8  -4 2416.98 51.0018  15

8   0   4 2395.85 56.4158  17

-8   4   0 2437.04 54.6940  14

0   8  -4 2490.09 54.8381  16

-8  -4   0 2482.36 55.0663  17

-2  -4  -8 20.0981 4.48449   8

2  -4  -8 10.7142 3.07790   8

-2   4  -8 13.1381 3.86266   8

4   8   2 18.2639 2.46817  11

8  -4   2 12.0756 3.58545  11

-4  -2  -8 17.4221 4.20023   8

8   4   2 20.4293 3.96338  11

4  -8   2 11.8679 2.13220  11

-8   4  -2 22.7985 4.57292  10

-8  -4  -2 17.3265 3.61089  10

-8  -2  -4 18.8636 4.12648  10

-4   2  -8 11.1198 3.87753   8

-8  -4   2 21.6386 3.77685  10

-8   4  -2 15.4862 3.46330   9

-2  -4   8 13.5607 3.74077   4

-4  -2   8 18.2887 4.05856   4

8   4  -2 16.0178 3.93112   4

-4   2  -8 22.4653 3.76627   3

2   8  -4 17.8175 2.14148   1

8  -4   2 18.5511 4.14010   1

-2   4  -8 15.6795 3.39352   1

2  -8  -4 16.1663 2.10221   1

4   8  -2 15.6094 2.11053   2

-8  -4  -2 16.6063 2.79107   3

-4  -2  -8 17.1326 2.79699   2

8   2   4 14.4219 3.64740   1

2   8  -4 14.0828 2.74099   2

-2   4  -8 22.8397 3.88493   2

8  -2   4 23.7749 4.42995   1

8  -2   4 16.4343 3.42278   2

-2  -4  -8 9.03543 3.04161   1

2   4   8 13.0192 3.43772   5

4  -8   2 15.9669 2.11725   5

2   4  -8 15.5986 3.44670   5

2  -4  -8 15.7565 3.43363   5

4  -8   2 12.8474 2.97377   2

4   8   2 21.1340 2.20838   5

-8  -2  -4 13.8917 3.25351   3

-4   2  -8 21.4123 4.38436   6

8   2   4 13.9091 2.49763   2

4  -2   8 17.9039 3.79592   5

4   2  -8 15.9345 1.72674   3

4   2   8 21.1403 3.87591   5

8   4   2 12.0534 3.03731   1

4   2  -8 16.9687 3.67053   5

4  -2  -8 15.1766 3.54371   5

8  -4   2 16.2783 3.51522   3

4  -8  -2 18.5264 2.11758   5

2  -4   8 16.4657 3.36444   5

-2  -4  -8 20.3021 2.75036   2

-4   2  -8 12.2420 3.77539   7

-4   2  -8 20.5140 4.04667   1

-4  -2  -8 15.5680 4.29812   6

2  -8   4 19.1136 2.09205   5

2   8   4 20.9095 2.16404   5

-4  -2  -8 19.0648 3.46777   1

8  -2   4 11.9848 3.02019   3

4   8  -2 21.7209 2.22880   5

-2  -8   4 12.1529 1.89802   3

-8  -4  -2 20.2922 4.24060   6

-8   4  -2 14.7624 4.04105   6

2  -8   4 13.4040 2.89934   3

2  -4  -8 13.0241 3.79109   7

-4   2  -8 26.9710 3.82271   2

-8  -2  -4 13.9279 3.88451   6

-8   2  -4 20.6550 4.26408   6

8   2  -4 16.4051 3.75221   4

-4   2   8 16.2004 3.67681   4

4   8  -2 14.2163 3.67921   4

4   8  -2 15.8816 3.81534  30

2   8  -4 23.4435 4.01454  28

2   8  -4 19.7814 4.55512  30

-4   8  -2 14.2717 3.64277  30

2   8   4 11.6149 3.33440  30

4   8   2 11.7986 3.13862  30

-4   8   2 16.1215 3.79826  30

4   8  -2 17.5485 3.93154  28

-2   8   4 12.4950 3.52927  30

-2   8  -4 13.6495 3.75210  30

4   8   2 18.8400 4.11060  28

2   8   4 21.9188 3.97186  28

-8   4   2 17.4638 4.05646  25

4   8  -2 13.9782 2.82746  26

2   8  -4 19.8506 4.21801  27

-2  -4   8 21.0994 4.06452  25

-2   4  -8 14.2868 3.26922  27

-8  -2   4 19.6136 4.44226  25

-8  -4   2 18.0761 4.06938  25

-4   8   2 14.4869 3.50718  26

-4   2   8 14.4250 4.01499  25

-4  -2   8 22.9635 4.53804  25

4   8  -2 14.3780 3.11761  27

-2   4   8 13.4450 3.71496  25

-2   8   4 18.6559 3.87999  26

-8   2   4 13.3757 3.86467  25

4  -2  -8 13.1836 3.86089  12

-2  -4   8 15.4476 3.79198  11

4   2  -8 12.0153 4.31505  12

8   4  -2 11.1347 4.01820  11

8  -4  -2 16.1917 4.26988  11

2   4  -8 13.2226 4.03830  12

8   2  -4 15.0479 4.44240  11

-8  -2   4 15.8484 3.37355  14

2  -4  -8 14.8700 3.80378  12

2   8   4 18.8021 3.64970  13

-2  -4  -8 13.4725 3.48797  12

-8   4  -2 16.8117 3.74592  14

-4   2   8 11.8907 3.83901  11

8  -2  -4 14.7527 4.01221  11

-8   4   2 15.0421 3.89157  14

-4  -2   8 17.4109 4.50117  11

-2   8   4 20.0223 4.06882  13

-4   8  -2 20.3245 3.76719  13

-8   2   4 16.2736 3.80712  14

-2   4   8 22.3802 4.09933  11

-2   4  -8 13.9061 3.87492  12

-8   4  -2 14.9120 3.23239  22

-2   8   4 12.0932 2.69903  23

-2   4  -8 22.6979 4.48245  22

2   8  -4 12.0501 3.01313  24

-4   8   2 20.3849 4.21449  24

2   4  -8 18.0323 3.19780  22

-4   8  -2 13.7513 3.88678  23

-4   8  -2 22.1954 4.45462  24

-2   4  -8 14.0092 2.81015  23

-4   8   2 18.2915 3.64167  23

-8   4  -2 19.4021 4.15238  23

-8   2  -4 15.6298 3.46322  22

-8   2  -4 22.0920 3.67810  23

-2   8  -4 17.5631 4.11197  22

-2   8   4 15.2202 3.97628  19

-2   8  -4 21.4076 4.38340  20

-8   4  -2 17.5204 4.20682  21

-8   4   2 16.6308 3.82163  21

-4   8   2 17.8156 4.20363  22

-8   2  -4 19.0207 3.97987  21

4   8   2 21.2498 4.62303  19

-4   8  -2 16.0056 3.86049  20

2   8   4 21.1550 4.77887  19

-8   2   4 19.4399 3.99742  21

2   8  -4 14.1170 3.11371  22

-8   2  -4 30.3485 4.33498  15

-4   2  -8 37.3149 4.55431  15

-2   8  -4 17.1052 3.61462  15

-8  -4   2 13.2979 3.75066  17

-4   8  -2 15.2494 3.27794  15

-8   2   4 27.8634 4.85002  17

4   8  -2 14.2081 4.04893  18

8   2   4 17.3697 3.79683  18

-8   4   2 14.7829 3.94354  17

4   8   2 22.5984 4.84695  18

8   4   2 15.4661 4.30724  18

-8  -2   4 16.9720 4.16404  17

8   2   4 30.8387 4.90050  17

-2   4  -8 16.8820 3.76149  15

2   8   4 15.0586 2.14815  17

2   8  -4 21.0896 4.04650  18

8  -2   4 17.8034 4.00010  17

-4  -8   2 14.7692 2.03819  17

-4   8   2 18.0154 2.24440  17

2  -8   4 14.7151 2.24326  17

-4   4  -8 7224.95 142.081   7

-8  -4  -4 7283.95 143.722  10

-4   4  -8 7431.96 145.926   8

-4  -4  -8 7297.83 146.482   8

-8   4  -4 7521.26 147.408  10

4   8  -4 7336.01 139.014   2

4  -8   4 7603.56 142.942   3

8  -4   4 7503.88 144.854   1

-8  -4  -4 7565.03 142.025   3

4   8  -4 7151.46 137.421   5

4  -4  -8 7584.93 144.369   5

4  -4   8 7355.09 143.597   5

4   4   8 7559.68 144.322   5

4   8   4 7110.87 137.199   5

-8   4  -4 7295.23 145.566   6

4   4  -8 7321.51 144.222   5

-8  -4  -4 7421.02 145.762   6

-4  -4  -8 7454.12 145.390   6

-4   4  -8 7351.12 145.366   6

-4   4   8 7266.29 140.760   4

8   4   4 7452.40 144.337   1

4   8  -4 7380.29 144.083  27

4   8   4 7458.70 143.955  28

4   8  -4 7058.94 145.338  30

-4   8   4 7595.77 146.815  29

4   8   4 7369.98 141.523  30

-4   8  -4 7381.43 143.588  30

4   8  -4 7349.14 144.511  28

-4   8   4 7296.26 143.460  26

-4  -4   8 7384.77 145.220  25

-4   4   8 7639.61 145.868  25

-8   4   4 7383.74 145.414  25

-8  -4   4 7182.06 144.689  25

-4  -4   8 7188.94 146.542  11

-4   4   8 7385.31 146.745  11

4   4  -8 7313.58 145.927  12

4  -4  -8 7195.03 145.362  12

-8   4  -4 7469.63 143.495  14

-4   8  -4 7233.97 141.895  13

-4   4  -8 7344.91 140.134  23

-4   8  -4 7452.70 146.686  22

-8   4  -4 7201.60 144.316  22

-4   4  -8 7445.54 147.090  22

-4   8   4 7425.23 140.814  23

-8   4  -4 7392.67 143.270  23

-4   8  -4 7265.35 141.151  21

-8   4  -4 7468.83 145.264  21

4   4   8 7204.52 142.883  19

8   4   4 7438.27 143.320  19

-8   4   4 7329.27 145.344  21

4   8   4 7419.81 148.796  19

-4   4  -8 7377.40 144.661  15

-8   4   4 7391.02 146.220  17

8   4   4 7685.08 147.472  18

4   8   4 7207.56 138.212  17

-8  -4   4 7532.34 140.333  14

-8   4  -4 7356.74 144.418  15

-4   8  -4 7413.07 143.892  15

-4   8   4 7188.77 138.263  17

8   4   4 7423.84 146.059  17

4   8  -4 7437.65 147.676  16

-8  -4   4 7230.15 145.683  17

8   4  -4 7317.88 142.627  16

8  -4   4 7353.49 145.895  17

-8   6   0 0.61756 2.70130   9

0  -6  -8 1.86029 2.16289   8

-6   0  -8-0.76234 2.94995  10

-8   6   0 0.70112 2.63659  10

-6   8   0-1.02273 2.23676  10

-8   0  -6 1.55215 2.91847  10

-8   0  -6-2.40693 3.58489   6

6   8   0-0.30657 1.31149   1

-6   0  -8-0.76637 3.42429   6

0   6  -8 2.05598 2.09653   1

0  -6  -8 5.77177 3.69933   7

0  -8  -6-0.93509 2.29642   7

0   8  -6-0.51475 1.69276   2

-8  -6   0 0.54621 2.44057   6

0  -6  -8-1.00173 2.04297   1

-8   6   0 1.66685 2.53380   6

0   8  -6 0.31484 1.37717   1

-6   8   0-1.65933 2.62132  30

0   8  -6-1.40021 3.37884  30

0   8   6 0.62416 2.78886  30

6   8   0-0.98066 2.19089  30

-8   6   0-0.79909 1.85814  30

0   6  -8-1.30168 3.14108  27

0   6   8-0.49329 2.29411  25

0  -6   8 0.48346 2.49438  25

-8   0   6 4.61035 3.96446  25

0   8   6-0.65933 2.68935  26

0   8  -6 0.68713 2.50683  27

-6   0   8-0.76413 3.19375  25

6   0  -8 2.45178 3.87319  12

0   8   6-0.52717 2.30590  13

8  -6   0-0.59713 2.61193  11

0   8   6 0.37238 1.51888  11

-8   6   0-0.63090 2.93409  14

8   6   0-0.60251 2.57751  11

0   6   8-0.41763 2.08629  13

0   6  -8-0.53068 2.78047  12

0  -6  -8 1.00417 2.24341  12

8   0  -6 4.24647 3.87306  12

-6   8   0 1.22233 3.05312  13

6   8   0 1.53608 1.67975  11

0   6  -8-1.12061 2.39698  22

-6   8   0 0.63562 2.45957  24

0   6  -8 1.75983 2.50950  23

-8   6   0 1.31036 2.92748  23

0   8  -6-0.68487 3.06013  23

0   8  -6-0.56479 2.57565  22

-6   8   0-2.55289 3.18830  23

-6   8   0 1.91261 3.07689  22

-8   0   6 0.40644 2.06398  21

0   8   6 0.79109 3.22676  19

-8   6   0-1.53800 2.14275  22

0   8  -6 0.52072 2.37465  15

8   6   0 2.43704 3.62972  18

-6   0  -8 0.89194 1.90785  15

-8   0  -6-3.06021 2.35892  15

-8   6  -2 371.668 15.8688   9

-6   8  -2 343.269 16.0397   9

-6   2  -8 359.162 16.9297   8

-2  -6  -8 338.948 14.6216   8

-8   6  -2 352.590 16.1541  10

2  -6  -8 338.427 14.8961   7

-6  -2  -8 351.309 17.3814   8

-6   8  -2 335.653 13.5031  10

-8  -2  -6 361.534 16.8938  10

-6   2  -8 334.704 16.3542  10

6   8  -2 347.309 9.96370   2

-8   6  -2 350.903 14.6953   6

2  -6   8 372.622 14.4325   5

2   6   8 350.227 14.1969   5

-8  -6  -2 365.468 12.6508   3

-8  -6  -2 341.239 14.3577   6

-8  -2  -6 364.802 17.4827   6

-8   2  -6 351.373 17.1435   6

2   8   6 347.823 11.9506   5

6   8  -2 365.504 12.2057   5

-6  -8  -2 376.421 12.9481   3

-6  -2  -8 365.690 17.0127   6

-6   2  -8 344.684 16.6850   6

2  -6   8 338.735 14.7715   4

6   8   2 362.834 12.2742   1

2   8  -6 336.723 11.9771   1

-2   6  -8 359.692 14.4186   1

-2  -6  -8 368.229 14.3801   1

8  -6   2 336.866 13.8391   1

8   6   2 354.369 14.2276   1

2  -8   6 346.995 13.9493   4

2  -8   6 355.711 13.2068   3

2   8  -6 370.761 14.2045   2

6   8   2 365.007 13.4985  30

2   8   6 354.446 13.8940  28

6   8  -2 362.643 13.7375  27

6   8  -2 348.112 14.8637  30

-2   8   6 355.589 16.6438  29

-6   8   2 359.266 16.6774  29

-8   6   2 349.598 13.9818  30

-2   8  -6 332.195 15.2998  30

-6   8  -2 370.084 14.5230  30

2   8   6 376.146 15.1155  30

2   8  -6 352.380 14.1875  28

-6   8   2 375.775 15.9017  30

6   8  -2 370.928 12.4130  26

-6   2   8 352.636 16.8361  25

-2   8   6 371.731 15.1846  26

-8  -2   6 359.375 16.8551  25

-2   6   8 376.697 14.1415  26

-2   6   8 384.977 15.0618  25

-6   8   2 366.481 15.3967  24

2   8  -6 367.896 13.4607  24

2   8  -6 376.102 16.5953  27

-8   2   6 339.689 16.6082  25

-2  -6   8 355.612 14.4358  25

-8   6   2 368.676 13.8448  24

-2   6  -8 351.996 15.4925  27

-6  -2   8 358.337 16.9411  25

-2  -6   8 352.910 15.2989  11

-2   6   8 343.913 15.0633  11

8  -6  -2 373.382 15.6425  11

8  -6   2 350.595 15.2833  11

-2   8   6 367.550 15.5655  13

-8   6  -2 342.951 13.3235  13

8   2  -6 359.379 17.7588  12

-2   8   6 339.167 12.9090  11

8   6  -2 359.644 15.7192  11

-6   8  -2 350.697 14.5328  13

8   6   2 333.945 15.0223  11

8  -2  -6 341.658 17.3379  12

6   2  -8 345.848 17.3043  12

2  -6  -8 365.524 14.7003  12

2   6  -8 390.908 15.5578  12

2   8   6 336.527 13.6066  13

6  -2  -8 327.063 16.5991  12

6   8   2 360.055 13.1072  11

-8   2  -6 366.274 13.1199  23

-6   8   2 369.445 15.5849  22

-2   6  -8 345.522 14.6808  23

-6   8  -2 347.994 16.1277  22

-8   6   2 363.757 15.9231  23

-6   8   2 356.707 15.2716  23

2   8  -6 369.379 13.9596  22

-8   2  -6 348.758 15.6438  22

-2   6  -8 364.263 16.3364  22

-2   8  -6 369.671 16.3690  22

-2   8  -6 353.874 15.8571  23

-6   8  -2 355.001 16.0216  23

2   6  -8 366.303 13.5416  22

-8   6  -2 358.813 15.2487  22

-8   6   2 390.497 14.4778  22

-6   8  -2 356.262 15.9261  21

-6   2  -8 355.643 12.7892  20

6   8   2 326.228 16.8783  19

-2   8  -6 371.436 17.2347  20

-8   6  -2 364.983 16.3616  21

-8   6   2 363.169 16.8551  21

2   8   6 335.826 17.1078  19

-8   2   6 362.447 14.3203  21

-6   8   2 344.370 12.2980  17

-8  -6   2 389.647 15.5939  17

8   6  -2 349.886 17.8779  18

6   8  -2 347.674 17.4240  18

-8   2  -6 339.880 14.5249  15

8   6   2 377.851 17.7350  18

-8   6  -2 340.370 14.8160  14

6   8   2 365.429 17.8494  18

-6   8  -2 369.000 15.6914  15

-6   2  -8 347.081 14.6824  15

-8  -2   6 363.020 13.4495  14

-8   6   2 347.939 14.8878  17

-2   8  -6 348.365 15.0439  15

2   8   6 352.508 12.1731  17

-6   4  -8 11.8071 4.31199  10

-8   4  -6 2.44297 3.48656  10

-8   6  -4 5.85026 3.77568  10

-8  -6  -4 8.78299 3.16421  10

-8   4  -6 5.28796 3.56947   8

-8  -4  -6 7.93525 4.05838  10

-4  -6  -8 10.0034 3.85811   8

-6   8  -4 8.70928 2.99644  10

-6   4  -8 3.69554 3.37358   8

-4   8   6 10.0022 2.88508  11

-6  -4  -8 7.04666 4.32866   8

-4   6  -8 6.94705 3.36173   8

-6   8  -4 6.99251 3.61609   9

-8  -4  -6 10.8745 4.48289   6

-8   4  -6 7.67436 3.77204   6

8  -6  -4 9.53403 3.39595   5

-6  -4  -8 12.9333 4.27975   6

-6   4  -8 11.9914 4.21615   6

4  -6  -8 7.10494 2.82338   5

-6   4  -8 1.58070 2.63601   7

6   8   4 6.60062 2.18763   5

4   8  -6 12.8118 2.85557   5

4   6  -8 3.98018 2.69847   5

4   8  -6 8.89336 2.89895   2

6   8  -4 11.8524 2.37667   2

4   8   6 12.7367 2.86337   5

6   8  -4 8.73700 2.46077   5

-8  -6  -4 7.14255 2.64556   3

8   6  -4 10.8209 3.28831   5

-6  -8  -4 10.6557 2.99954   3

-8  -6  -4 8.64288 3.47386   6

-8   6  -4 6.22171 3.05918   6

-4   8  -6 19.5589 4.32696  30

4   8   6 8.73613 3.23051  28

4   8   6 4.90108 2.93470  30

-6   4   8 9.66870 3.36171  29

-8   4   6 13.0239 3.63986  29

-4   6   8 6.23271 3.57585  29

-6   8  -4 13.3582 3.60217  30

-6   8   4 15.8132 4.73093  29

-6   8   4 6.57963 3.53116  30

4   8  -6 6.42515 3.01700  28

-4   8   6 9.35669 4.14918  29

-8   4   6 11.4709 4.00926  25

-6   4   8 6.09197 4.33970  25

-4   6   8 6.90168 2.54251  26

4   8  -6 7.33726 3.48021  27

-8  -4   6 9.63740 3.82753  25

-6  -4   8 12.6812 4.35874  25

-4  -6   8 7.23203 3.34656  25

-4   8   6 3.96884 2.92873  26

-8   6   4 4.44064 2.95369  25

-4   6   8 8.11327 3.60286  25

-8  -6   4 10.8863 3.78434  25

8   4  -6 8.45420 4.08264  12

8   6  -4 4.15713 3.57756  12

6  -4  -8 3.95743 3.61224  12

-8   6  -4 7.73714 3.26975  14

8  -6  -4 7.97868 4.02508  12

4  -6  -8 6.15353 3.02573  12

6   4  -8 8.18735 4.16011  12

-6   8  -4 7.89227 2.98763  13

8  -4  -6 8.14316 4.07048  12

4   6  -8 12.5370 4.08423  12

-8   4  -6 9.71920 3.51985  23

-6   8   4 4.55409 3.24555  23

-6   8  -4 6.63281 4.09115  23

-4   6  -8 10.5353 3.37922  23

-6   4  -8 5.00090 2.38622  23

-4   8  -6 12.0409 4.39515  22

-8   4  -6 10.6358 4.21715  22

-4   6  -8 9.84327 4.42836  22

-8   6  -4 8.87199 3.88980  23

-8   6  -4 8.75591 4.10487  22

-4   8  -6 7.19576 3.82950  23

4   8   6 8.01421 4.06332  19

-8   4  -6 4.17744 2.43263  20

-8   4  -6 15.3456 4.22916  21

8   4   6 8.27981 3.22678  19

-6   8  -4 10.1683 3.66234  21

-6   4  -8 5.58753 3.10316  20

-8   6  -4 6.13877 3.63026  20

-8   6  -4 10.1911 3.87243  21

-4   6  -8 6.61386 3.91080  20

-6   8  -4 7.92191 4.15306  20

6   4   8 10.1444 3.48056  19

6   8   4 8.71769 4.70609  19

-8   4   6 7.80016 3.45983  21

-8   6   4 4.71625 4.05801  21

8   6   4 5.15491 3.61979  19

4   6   8 8.27167 4.23023  19

6   8   4 2.81794 3.83399  18

4   8  -6 12.7275 4.38007  16

-6   8  -4 8.42760 3.89887  15

8   6  -4 10.6168 4.33279  16

-4   6  -8 8.71127 4.24192  15

-8   4  -6 12.9697 3.94018  15

-6   4  -8 4.13345 3.01672  15

4   6   8 11.6282 3.35682  17

8   6   4 7.91878 3.93398  18

-4   8  -6 4.85596 3.46840  15

4   8   6 12.5725 3.04055  17

-6   8   4 5.43651 2.15178  17

6   8  -4 8.37935 4.39260  16

-8   6  -4 6.55636 3.76125  15

-6  -6  -8 367.133 18.6023   8

-8   6  -6 389.278 17.9860  10

-8   6  -6 348.020 14.8382   8

-6   8  -6 344.716 14.4695  10

-6   6  -8 351.795 16.2670  10

-6   6  -8 346.374 16.0065   8

-8  -6  -6 344.784 16.2609   6

-8   6  -6 348.437 16.4803   6

-6   8  -6 328.003 13.8160   6

-6  -6  -8 356.428 16.7079   6

-6   6  -8 350.641 16.4941   6

-8   6   6 377.474 17.0909  29

6   6  -8 387.910 14.3680  28

-6   8  -6 357.090 14.5126  30

6   8   6 341.567 15.5058  28

-6   8   6 372.973 18.2354  29

6   8  -6 361.902 16.2235  28

-6   6   8 331.126 16.0823  29

-6  -6   8 352.469 16.5366  25

-8   6   6 379.268 17.3551  25

-6   8   6 341.424 14.3568  25

-6   6   8 347.763 16.5923  25

-8  -6   6 351.971 16.4258  25

-6   8   6 346.191 14.7874  26

8   6  -6 329.713 16.9452  12

6   6  -8 366.145 17.4896  12

8  -6  -6 364.135 17.2802  12

6   8  -6 339.885 14.6061  12

6  -6  -8 344.129 16.7642  12

-6   8  -6 354.735 17.2844  23

-6   6  -8 373.752 19.0205  22

-6   6  -8 361.375 15.7539  23

-6   8  -6 305.560 17.5321  22

-8   6  -6 344.498 17.9918  22

-8   6  -6 385.766 16.8122  23

-6   6  -8 382.265 17.3639  20

-8   6  -6 380.389 17.0031  20

6   6   8 377.281 17.5847  19

-6   8  -6 409.124 19.1333  20

6   8   6 380.623 19.1710  19

-6   8  -6 333.628 14.1530  21

-8   6   6 367.435 17.6169  21

-8   6  -6 366.172 16.0844  21

8   6   6 425.192 18.4600  19

-6   8  -6 373.331 17.7805  15

-6   6  -8 363.667 17.8308  15

6   8  -6 350.870 18.6381  16

-8   6  -6 366.352 17.9677  15

-8   6  -6 359.436 14.6098  14

8   6  -6 329.723 16.6035  16

-8   8   0 5110.56 107.858   9

-8   8   0 5006.94 106.096  10

0  -8  -8 4891.36 104.154   7

-8   0  -8 5252.49 111.390  10

-8   0  -8 4853.68 110.632   8

-8   8   0 4893.89 100.317   6

-8   0  -8 5163.43 111.330   6

-8   8   0 5123.15 102.981  30

0   8   8 4947.98 100.090  25

-8   8   0 4990.72 105.556  24

-8   0   8 5091.84 110.733  25

-8   8   0 5130.20 105.902  13

0   8   8 5068.08 102.824  13

8   0  -8 5082.65 112.216  12

0   8  -8 5104.27 105.192  22

-8   8   0 5137.49 105.751  22

0   8  -8 5006.79 107.433  23

-8   8   0 5106.08 107.515  23

-8   8   0 5006.36 109.285  21

0   8  -8 5044.07 105.610  15

-8   0  -8 5179.31 101.875  15

8   8   0 4993.35 111.655  18

-8   8  -2 26.0838 5.81822   9

-8  -2  -8 30.2146 6.23272  10

-8   2  -8 37.7019 6.96286  10

-8   2  -8 29.2855 5.92605   8

-8   8  -2 29.0496 5.54683  10

-8  -2  -8 30.1143 6.47206   6

-8   2  -8 22.0948 5.70302   6

2  -8  -8 30.7511 5.23889   7

-8   8  -2 26.1291 4.36866   6

2   8   8 31.0863 5.30986  30

-8   8   2 32.7265 5.44710  30

2   8  -8 28.8921 4.15153  28

-8   8  -2 25.3268 4.42337  30

-2   8   8 27.8036 4.88522  26

-8  -2   8 34.5855 6.51450  25

2   8  -8 34.9765 6.20037  27

-2   8   8 33.1358 4.69608  25

-8   2   8 38.6569 7.16293  25

8   8  -2 25.2537 4.56518  12

-8   8  -2 27.9703 5.14050  13

8  -2  -8 20.1640 6.05321  12

8   2  -8 32.0335 6.68543  12

2   8  -8 36.7698 4.80232  12

-2   8   8 26.8694 5.09390  13

-8   8   2 15.3996 4.48849  24

-8   8   2 36.8302 6.04349  23

2   8  -8 33.5311 5.07270  22

-2   8  -8 30.2112 5.88793  22

-8   2  -8 32.1962 6.22132  22

-2   8  -8 34.7431 6.03989  23

-8   8   2 31.0699 5.70437  22

2   8   8 35.4044 6.85179  19

-8   8  -2 37.6750 6.31918  21

-8   8   2 30.8339 6.45584  21

-8   8  -2 29.5670 5.57603  22

8   8   2 27.7691 5.75154  19

-8   2  -8 26.2929 5.35507  15

-2   8  -8 38.4334 6.13486  15

8   8   2 34.6813 7.16581  18

8   8  -2 35.2039 7.03633  18

-8   8  -4 1138.30 33.9619  10

-8   4  -8 1138.72 31.9337   7

-4  -8  -8 1215.58 34.5080   8

-8   4  -8 1127.71 37.5605  10

-8   8  -4 1267.99 38.2777   9

-8   4  -8 1191.33 36.6412   8

-8   8  -4 1155.99 31.7152   6

-8  -4  -8 1254.34 38.3961   6

-8   4  -8 1155.83 37.1766   6

-4   8   8 1205.93 37.3600  29

4   8  -8 1200.47 31.4990  28

4   8   8 1171.76 31.5669  30

-8   8   4 1210.78 35.9474  30

4   8  -8 1117.66 36.8885  27

-8   4   8 1259.36 32.7741  29

-8  -4   8 1213.89 37.7332  25

-4   8   8 1210.61 32.4031  25

-4   8   8 1183.66 32.3667  26

-8   4   8 1196.39 37.8547  25

8  -4  -8 1093.15 37.3413  12

8   4  -8 1131.19 38.0779  12

-8   8  -4 1176.49 31.2091  13

8   8  -4 1175.11 32.7748  12

4   8  -8 1189.66 32.5859  12

-8   4  -8 1181.65 31.4285  23

-8   4  -8 1146.97 37.5274  22

-8   8  -4 1147.86 37.0386  22

-8   8  -4 1207.44 36.9447  23

-4   8  -8 1183.88 35.6634  23

-4   8  -8 1184.38 38.1105  22

-4   8  -8 1260.38 38.7593  20

-8   4   8 1236.32 33.9053  21

4   8   8 1283.75 39.8906  19

8   8   4 1164.26 37.9097  19

-8   4  -8 1188.76 32.1831  20

-8   8  -4 1231.86 35.9990  21

-8   4  -8 1096.98 35.0426  15

8   8   4 1187.69 40.1042  18

-4   8  -8 1191.08 36.7230  15

8   8  -4 1178.96 37.7558  16

-8   6  -8 26.5152 6.08179  10

-8   8  -6 24.2350 5.62331  10

-6  -8  -8 23.1456 5.80031   8

-8   6  -8 18.9479 5.23149   8

-6   8  -8 22.2950 4.45973   8

-8   8  -6 24.4574 5.57009   6

-8  -6  -8 19.4563 5.30166   6

-8   6  -8 20.3665 5.36944   6

6   8  -8 18.1722 4.33006  28

-8   6   8 13.4190 4.73481  29

8   8   6 13.2765 4.79193  28

-6   8   8 25.8891 5.94245  29

8   8  -6 23.1134 5.44122  28

-8   8   6 26.1693 6.38491  29

-8   8   6 12.3372 4.11518  25

-8  -6   8 21.7176 5.72490  25

-6   8   8 21.7188 4.96545  25

-8   6   8 16.3877 5.32926  25

8   6  -8 15.5720 5.55529  12

8   8  -6 18.7173 4.92679  12

6   8  -8 17.8242 4.70313  12

8  -6  -8 14.9200 5.11583  12

-6   8  -8 28.0489 5.76060  23

-8   8  -6 26.8220 5.89141  23

-8   6  -8 20.5910 5.85888  22

-8   8  -6 27.5374 6.70240  22

-6   8  -8 18.6994 6.03031  22

-8   6  -8 14.2131 4.31464  23

6   8   8 27.4825 6.54865  19

8   6   8 20.4550 5.39347  19

-6   8  -8 23.9784 6.25767  20

-8   6  -8 14.9227 4.92431  20

-8   8  -6 21.9923 5.86145  20

-8   6   8 29.0546 5.82692  21

-8   8  -6 21.1778 4.78862  21

8   8   6 22.4139 6.03293  19

-8   6  -8 25.0807 5.97817  15

8   8  -6 25.5801 6.33981  16

-8   8  -8 2841.30 68.3493  10

-8  -8  -8 2878.50 67.2382   6

-8   8  -8 2843.46 67.9160   6

-8   8   8 2796.80 71.6077  29

8   8   8 2887.49 65.6962  28

8   8  -8 2965.59 67.1831  28

-8   8   8 2818.54 67.8989  25

-8  -8   8 2834.49 67.3751  25

8  -8  -8 2828.26 67.9260  12

8   8  -8 2945.65 69.2681  12

-8   8  -8 2900.38 70.1363  23

-8   8   8 2798.19 71.6828  21

-8   8  -8 3006.13 72.8623  20

8   8   8 3160.93 74.3920  19

-8   8  -8 2866.55 73.7228  15

1  -1  -9 337.726 15.4883   7

1   9  -1 337.546 11.7451   9

-1  -1  -9 343.328 15.6682   8

1  -1  -9 361.900 15.7539   8

1   1  -9 373.624 16.2719   8

-9  -1  -1 355.733 15.4093  10

-1  -1  -9 354.405 15.8652   7

-1   1  -9 361.182 15.5945   7

-9   1  -1 389.511 16.4327  10

-1   1  -9 331.239 15.5183   8

-1   9  -1 351.302 13.2327   9

-1  -1   9 331.359 14.5266   5

9  -1  -1 342.359 12.4158   3

1  -9  -1 337.662 11.0154   2

9  -1   1 360.641 13.3696   3

-1   1  -9 363.765 14.3067   2

1  -1   9 359.404 14.8624   5

-1  -1  -9 355.819 13.9243   3

9   1  -1 374.770 11.9321   3

-1  -1  -9 365.288 15.4588   1

1   9  -1 381.166 13.0056   4

1   1  -9 332.446 12.0182   3

1   9   1 347.836 12.2053   4

9  -1  -1 347.210 13.5228   4

-1   1  -9 358.337 13.1888   3

-1   1  -9 341.438 11.8820  27

-1   9   1 345.356 14.7888  30

1   9   1 328.823 14.6271  28

-1   9   1 358.899 14.3662  29

1   9   1 356.489 14.8510  30

1   9   1 355.695 13.3978  29

1   9  -1 364.567 15.1067  30

-1   9  -1 345.348 13.5104  29

1   9  -1 335.632 12.2380  29

-1   9   1 318.918 14.3755  28

-1   9  -1 335.968 14.5773  24

1   9  -1 333.263 13.7129  26

-1   9  -1 357.260 14.5593  26

1   9   1 343.450 14.2250  26

-1   9   1 358.365 15.0074  13

9  -1   1 347.160 16.2514  11

1   9  -1 361.802 15.2581  13

-1  -1  -9 370.581 16.0382  12

1  -1  -9 327.991 15.4231  12

9  -1  -1 344.392 16.3862  11

1   9   1 348.504 14.8010  13

-1   9   1 339.774 14.8006  22

-1   9  -1 345.919 14.3186  23

-1   9  -1 351.170 14.9575  22

1   9  -1 342.167 14.1429  22

-1   9   1 328.630 13.2074  23

1   9  -1 347.145 14.3494  23

1   9   1 339.390 14.3805  22

1   9   1 331.303 12.9604  23

-9  -1   1 388.900 15.4401  21

1   9  -1 354.189 13.6546  20

1   9  -1 326.705 14.8404  19

-1   9   1 383.013 15.3490  19

-1   9  -1 357.940 14.6122  20

-1   9   1 366.032 14.0575  20

-1   9  -1 332.812 13.7374  19

-9   1   1 361.012 15.2348  21

1   9   1 337.092 15.3358  19

-9   1  -1 399.737 16.2046  21

1   9   1 353.802 12.6354  20

1   9  -1 345.482 13.6902  18

-1   9  -1 334.010 13.3775  16

9   1   1 327.600 13.3140  18

1   9   1 346.639 14.4029  18

-9  -1   1 344.038 15.7174  17

-9  -1  -1 357.360 15.6541  17

-9   1   1 335.885 14.7654  14

-9  -3   1 2163.10 49.9769  10

-1   3  -9 2141.01 52.3986   8

-3   1  -9 2221.46 52.3589   7

1  -3  -9 2222.90 53.0527   7

-1   9  -3 2160.63 48.7503   9

-9   1  -3 2153.63 52.9787  10

-9  -3  -1 2081.95 50.0049  10

-9  -1  -3 2101.84 51.9344  10

-1  -3  -9 2166.46 53.0274   7

-1  -3  -9 2140.90 51.6057   8

-3  -1  -9 2200.98 53.3202   8

1  -3  -9 2157.80 50.8673   8

-9   3  -1 2147.86 47.2763   9

-3   9  -1 2010.89 49.4359   9

9  -3   1 2237.31 49.1777   3

-3  -1  -9 2171.28 47.8832   2

1   3  -9 2160.68 44.8890   3

9  -3  -1 2162.02 48.2364   3

-1   3  -9 2187.53 50.2272   2

9  -1  -3 2132.69 45.5870   3

3  -9   1 2188.11 47.6171   2

-1   3  -9 2118.63 50.7517   1

-3   1  -9 2191.28 49.0382   3

-1  -3  -9 2156.89 50.8130   1

9   1  -3 2138.95 43.5357   3

-9  -3  -1 2025.59 51.5741   6

-9   3  -1 2130.65 52.5345   6

-3  -1  -9 2233.28 50.1279   3

-9  -1  -3 2067.91 52.6857   6

3   1  -9 2141.92 44.5153   3

1  -3   9 2131.05 50.0687   5

9  -1   3 2179.68 49.0339   3

1   3  -9 2085.33 50.6259   1

-3   1   9 2124.03 50.0527   4

9  -1  -3 2189.55 48.4110   4

-3  -1   9 2101.33 50.9676   4

3   9  -1 2140.30 49.2423   4

9   1  -3 2207.61 50.5805   4

9  -1   3 2361.91 49.8761   2

9   1   3 2178.62 47.0768   2

9  -3  -1 2102.27 45.3963   4

-1   9   3 2056.05 42.0915   4

1  -9  -3 1999.61 43.3183   2

3  -9  -1 2374.35 47.7164   2

1   3   9 2127.84 50.1736   5

-3  -1  -9 2117.74 51.0350   1

3  -1  -9 2142.54 51.2135   5

-3   1  -9 2192.95 49.1690   2

3   9   1 2229.98 49.4252   4

-3   9   1 2143.84 51.0417  30

1   9   3 2126.63 50.2271  28

-1   3  -9 2090.18 47.8105  27

1   9   3 2107.66 50.5287  30

3   9   1 2235.43 51.8651  28

1   9  -3 2148.96 51.7833  30

-3   9  -1 2090.37 50.4971  30

3   9  -1 2138.19 50.7138  30

-1   9   3 2076.91 50.6080  29

3   9   1 2068.31 49.7242  30

1   9  -3 2128.13 50.6176  28

-3   9   1 2100.06 50.9123  29

3   9   1 2204.23 47.0428  29

-1   9  -3 2191.71 51.6750  30

-1   9   3 2140.92 51.3640  30

-3   9  -1 2233.00 51.9354  24

-3  -1   9 2148.56 51.9598  25

-3   9   1 2138.89 50.8457  26

3   9  -1 2117.41 47.5173  27

-1  -3   9 2058.76 50.3726  25

-9  -1   3 2180.87 52.6770  25

-1   9   3 2130.88 50.5350  26

1   9  -3 2103.65 50.0536  27

-1   9  -3 2128.40 50.4969  24

3   9   1 2145.70 49.8706  26

3   9  -1 2103.65 48.0775  26

1   9   3 2159.42 50.9595  26

1   9  -3 2139.57 48.5001  26

-1   3   9 2113.10 50.7633  25

1   9  -3 2150.46 49.3063  24

1   3  -9 2057.89 51.4441  12

1  -3  -9 2176.21 51.7198  12

-1  -3  -9 2157.49 51.5079  12

-3   9  -1 2143.57 50.7032  13

9   3  -1 2129.77 52.8970  11

3  -1  -9 2114.23 52.9127  12

-1   3  -9 2121.29 51.7202  12

-1   9   3 2198.92 50.9957  13

9  -3   1 2095.49 52.4518  11

9  -1  -3 2212.62 54.2659  11

9   3   1 2128.61 52.4962  11

9  -3  -1 2163.79 53.2450  11

1   9   3 2108.66 49.9598  13

-9   1  -3 2135.73 47.0034  22

1   9  -3 2119.84 51.1149  23

-3   9   1 2084.22 49.1255  23

-3   9  -1 2146.61 50.4802  23

-1   3  -9 2175.54 45.8340  23

3   9  -1 2131.77 47.8847  22

-1   9  -3 2112.56 51.0205  23

3   9   1 2007.13 47.2517  23

-1   9  -3 2218.58 51.2167  22

-1   9   3 2124.94 46.3866  23

-9   3  -1 2121.69 46.0265  22

1   9  -3 2177.24 49.4876  22

-3   9  -1 2236.59 52.2530  22

-1   9  -3 2225.07 51.8226  20

-9  -1   3 2125.91 49.0977  21

-3   9   1 2074.11 48.9629  19

-3   9  -1 2223.77 51.8577  20

1   9  -3 2160.65 50.4056  20

-3   9  -1 2083.62 46.8486  19

-1   9  -3 2077.45 47.5314  19

-9   3   1 2157.74 51.9189  21

-9   1   3 2126.68 50.0950  21

-1   9   3 2188.14 52.1877  19

3   9  -1 2223.55 47.3092  20

-9   3  -1 2147.61 51.3465  14

3   9  -1 2062.57 50.9791  18

-9   3   1 2183.38 52.3263  17

1   9  -3 2148.10 48.2225  18

9   1   3 2398.51 49.4132  18

-9   1   3 2170.33 50.7815  14

9  -1   3 2070.61 52.2072  17

3   9   1 2075.89 51.7382  18

-9  -1   3 2139.47 49.6679  14

-9   3   1 2146.32 51.6380  14

9   3   1 2028.94 50.4160  18

-1   9  -3 2173.02 46.6609  15

-1   9  -3 2102.84 49.5440  16

-9  -3   1 2146.38 51.8052  17

1   9  -3 2155.73 51.4921  16

-3   9  -1 2136.44 46.8242  15

-3   3  -9 156.478 9.98778   7

-3   9  -3 188.273 10.7174   9

-9  -3  -3 152.691 9.95192  10

-3  -3  -9 148.149 10.8882   7

-3   3  -9 161.428 11.0375   8

-3  -3  -9 171.211 11.1566   8

-3  -3  -9 152.393 7.77115   2

9   3   3 154.683 7.11567   2

-3   3   9 147.808 8.95083   4

-9  -3  -3 147.465 10.4129   6

-9   3  -3 158.046 10.9396   6

-3   9  -3 162.351 10.2916  30

3   9   3 185.527 10.7200  28

3   9  -3 161.454 10.3682  28

3   9   3 153.933 9.51293  30

3   9  -3 150.716 10.3174  30

-3   3   9 153.792 10.4759  25

3   9  -3 164.184 9.70795  27

-3  -3   9 166.774 10.7293  25

-3   3  -9 165.268 8.65392  27

-9  -3   3 167.044 10.7004  25

-3   9   3 153.253 9.88065  26

3   9  -3 153.874 8.43911  26

-9   3   3 165.617 10.8106  25

-3   9  -3 148.678 10.0814  24

3   9   3 155.852 9.73251  13

3  -3  -9 151.678 10.7012  12

3   3  -9 142.253 10.3205  12

-3   9  -3 162.996 9.93213  13

-3   9   3 159.989 10.3861  13

-9  -3   3 141.278 8.85422  14

-9   3  -3 180.494 10.6924  14

3   9  -3 133.495 8.09573  22

-3   9  -3 169.354 10.6081  23

-9   3  -3 149.905 8.85503  22

-9   3  -3 151.213 9.37132  23

-3   9   3 155.271 8.73141  23

-3   9  -3 157.124 10.4937  22

-3   3  -9 154.655 7.45470  23

-9   3   3 170.565 10.5724  21

3   9   3 170.418 11.5756  19

-3   9   3 155.204 10.0805  19

-9   3  -3 187.792 11.2688  21

-3   9  -3 182.932 11.2833  20

9   3  -3 156.233 8.43952  16

-9   3   3 159.957 10.5262  14

3   9  -3 132.796 9.58739  18

-3   3  -9 150.323 9.73686  15

9   3   3 166.290 10.4449  18

-3   9  -3 144.012 8.69691  15

-1  -5  -9 2182.29 54.3832   7

-9  -5   1 2141.77 48.4547  10

-9  -1  -5 2252.82 55.1713  10

-5   1  -9 2106.04 53.0457   7

-9  -5  -1 2095.66 48.8328  10

1  -5  -9 2115.48 53.3080   7

-9   5  -1 2134.63 50.8590   9

-9   1  -5 2215.04 55.6657  10

-1  -5  -9 2174.93 51.5485   8

1  -5  -9 2123.39 49.9573   8

-9   5  -1 2134.20 54.4379  10

-5  -1  -9 2118.87 55.0362   8

9  -1  -5 2146.93 45.4648   3

-1   5  -9 2160.44 50.9526   1

1   5  -9 2194.37 51.2703   1

-9  -5  -1 2103.79 52.1369   6

-9   5  -1 2143.36 52.6158   6

5   1  -9 2087.48 43.0497   3

-9  -1  -5 2208.23 55.9374   6

1  -9   5 2230.66 47.4000   3

1  -5  -9 2184.67 51.0003   1

-5  -1  -9 2147.99 54.6106   6

9   1   5 2151.90 47.4577   2

5  -9  -1 2088.45 48.4464   2

-1  -5  -9 2213.20 50.9877   1

-9   5   1 2185.81 46.9568  30

1   9  -5 2179.40 51.1784  28

5   9   1 2221.10 50.6640  30

5   9  -1 2059.16 51.1044  30

1   9   5 2161.87 52.2598  30

-1   9   5 2184.04 53.3903  30

1   5  -9 2220.92 52.8356  27

1   9   5 2162.93 50.5325  28

5   9   1 2198.18 53.6150  28

-5   9   1 2149.94 52.4719  30

-1   9  -5 2119.85 53.2797  30

-5   9  -1 2244.89 51.9372  30

-1  -5   9 2181.29 51.4415  25

5   9   1 2290.37 51.7623  26

1   9  -5 2196.31 50.2288  24

-9   5   1 2154.92 47.9260  24

-5  -1   9 2150.30 54.5144  25

1   9   5 2266.87 53.9683  26

-9  -1   5 2180.44 54.8939  25

-1   9   5 2062.32 51.6587  26

-5   9   1 2179.13 52.7926  24

-1   9  -5 2182.79 51.7898  24

5   9  -1 2225.85 48.1680  27

1   9  -5 2213.58 53.4267  27

5   9  -1 2156.38 48.5799  26

-1   5  -9 2183.79 51.4794  27

-1   5   9 2133.01 51.4005  25

1   5  -9 2231.29 52.8057  12

5  -1  -9 2189.95 55.6576  12

1  -5  -9 2210.15 51.8819  12

9   5   1 2070.67 52.2566  11

9   5  -1 2169.30 53.0077  11

1   9   5 2179.75 50.9755  13

9  -5   1 2179.87 53.1974  11

-5   9  -1 2113.32 51.7967  13

-1   9   5 2124.55 51.7671  13

9  -5  -1 2156.34 52.8971  11

-1  -5  -9 2238.93 51.9404  12

-5   9   1 2144.29 52.9755  13

-1   5  -9 2197.60 52.2896  12

-1   9  -5 2097.85 52.0755  22

-1   5  -9 2181.54 49.6256  23

-5   9   1 2226.25 52.0316  23

1   9  -5 2117.69 53.6987  23

-5   9   1 2187.18 53.2251  22

1   9  -5 2195.63 50.6132  22

1   5  -9 2139.67 49.4989  22

-5   9  -1 2208.61 53.0279  23

-9   5  -1 2164.17 49.3419  22

-9   1  -5 2179.05 50.7208  22

-9   5   1 2131.95 47.7592  22

-1   5  -9 2204.79 52.1993  22

-9  -1   5 2213.04 48.8618  21

-1   9   5 2107.45 54.6634  19

-9   5   1 2135.59 53.9240  21

-9   1   5 2222.40 50.3114  21

5   9   1 2187.24 56.1345  19

-5   9  -1 2282.54 54.6815  20

-1   9  -5 2300.69 55.0394  20

-1   9  -5 2104.14 47.5149  19

1   9   5 2197.55 55.7965  19

-9   1  -5 2157.65 49.6442  15

9   5  -1 2193.80 55.8762  18

5   9  -1 2194.84 55.3265  18

-9  -1   5 2152.91 50.0835  14

1   9  -5 2182.88 48.3429  15

-5   1  -9 2191.36 50.2391  15

-9   5  -1 2193.41 52.7187  14

9   5   1 2112.66 54.3180  18

-9   5   1 2191.16 53.6965  14

5   9   1 2153.95 55.1983  18

-9   1   5 2174.70 51.7239  14

-1   9  -5 2212.49 49.9598  15

1   9  -5 2150.37 49.1158  18

-5  -1  -9 2161.41 48.0179  15

1   9  -5 2110.12 53.5559  16

-5   3  -9 241.416 12.7778   7

-9  -3  -5 243.954 13.7587  10

-9   5  -3 224.197 12.1872   9

-5   3  -9 256.070 14.3232   8

-9  -5  -3 255.824 12.1780  10

-3  -5  -9 234.399 13.5330   8

-9   5  -3 220.877 13.5856  10

-5  -3  -9 222.407 14.0559   8

-9   3  -5 237.227 14.2765  10

-3   5  -9 267.765 14.1149   8

-9  -5  -3 239.164 10.6809   3

-9   5  -3 234.510 13.1843   6

-9  -5  -3 241.662 13.1816   6

-9  -3  -5 246.854 14.2896   6

-9   3  -5 244.530 14.3677   6

-3   5   9 236.202 11.0379   4

-5  -3  -9 251.023 14.1697   6

-5   3  -9 259.493 14.4680   6

3   9  -5 237.868 10.3822   2

-5   3   9 234.620 11.5245   4

-3   9   5 263.987 14.5376  29

-5   9  -3 228.987 12.2718  30

5   9  -3 234.260 13.2447  30

5   9   3 250.698 11.8431  30

5   9  -3 267.560 14.1407  28

3   9   5 230.571 12.3312  28

3   9  -5 223.895 13.6656  30

-3   9  -5 256.761 13.4308  30

3   9   5 220.077 11.7129  30

-5   9   3 242.746 14.1154  29

3   9  -5 254.075 13.0722  28

-5   3   9 263.191 11.6264  29

-5   9   3 242.681 13.6180  30

5   9   3 242.062 13.4288  28

-3   9   5 236.358 13.7736  30

-5   9  -3 243.219 13.8230  24

-5   3   9 241.558 14.2364  25

-5  -3   9 242.088 14.0716  25

-9   5   3 236.694 13.0666  25

-9  -5   3 232.648 12.8435  25

-9   3   5 243.650 14.1205  25

-5   9   3 244.043 12.9592  26

-9  -3   5 217.227 13.3999  25

3   9  -5 250.813 13.5553  27

5   9  -3 228.889 10.1128  26

5   9  -3 233.996 11.9028  27

-3   5   9 225.675 12.8059  25

-3   9   5 242.728 12.7919  26

-3  -5   9 248.588 13.1845  25

-9   5   3 230.888 9.95942  24

3   5  -9 244.178 13.5021  12

9   3  -5 237.890 14.8486  12

5  -3  -9 259.575 14.7385  12

-5   9  -3 241.613 12.3483  13

3   9   5 228.347 11.7441  13

9  -3  -5 254.278 15.3866  12

5   3  -9 243.394 14.5186  12

-3   9   5 224.542 13.0838  13

3  -5  -9 237.773 12.9155  12

3   9  -5 227.671 10.7406  22

-9   5  -3 237.368 12.8808  23

-9   3  -5 252.002 12.9533  22

-9   3  -5 230.196 11.4325  23

-3   9  -5 213.451 13.3238  22

-3   5  -9 236.042 11.2366  23

-5   3  -9 239.066 9.67835  23

-5   9   3 243.011 13.6062  22

-3   5  -9 244.279 13.9742  22

-5   9  -3 243.389 13.6089  23

-9   5  -3 239.723 12.4232  22

-9   5   3 236.200 10.2636  22

-5   9   3 246.017 12.2322  23

5   9   3 216.981 14.1908  19

-9   5   3 250.596 14.1034  21

-3   9  -5 251.160 14.3375  20

3   9   5 252.780 15.2207  19

-5   9  -3 238.846 13.9206  20

-9   5  -3 251.660 13.8792  21

-9   3   5 250.322 13.0124  21

-5   3  -9 247.749 11.6887  20

-3   9  -5 211.536 10.0275  21

-5   9  -3 234.902 12.3690  21

-9   3  -5 251.940 13.5436  21

-9   3  -5 247.454 12.7839  15

5   9  -3 228.866 14.1686  16

9   3  -5 242.287 11.0375  16

-9   5  -3 213.524 12.2968  14

-3   5  -9 253.214 13.5863  15

9   5  -3 229.763 12.2801  16

9   5   3 244.121 14.2074  18

-5   9  -3 244.417 12.5776  15

3   9  -5 220.767 10.0629  15

-9  -3   5 230.502 11.0381  14

-5   3  -9 243.936 12.8825  15

-3   9  -5 217.694 11.9794  15

3   9  -5 252.440 13.3911  18

5   9  -3 250.109 14.7145  18

-9   5  -5 362.957 18.2941  10

-9  -5  -5 331.048 15.8242  10

-9   5  -5 373.265 15.7427   8

-5   5  -9 350.081 14.7986   7

-5  -5  -9 357.639 18.3610   8

-5   5  -9 348.266 17.1612   8

-9  -5  -5 394.721 17.9709   6

-9   5  -5 364.080 17.5040   6

-5   9  -5 392.856 16.5251  30

5   9   5 362.190 16.5495  28

-5   9   5 385.520 18.5747  29

-5   5   9 369.395 16.1307  29

-5   9   5 365.546 18.0386  30

5   9  -5 379.809 17.3201  28

5   9   5 369.818 14.7420  30

5   9  -5 345.165 16.7390  27

-5   5   9 387.029 17.8073  25

-5   9   5 358.791 16.0825  26

-5  -5   9 410.757 18.0756  25

-9   5   5 371.141 17.6983  25

-9  -5   5 370.335 17.3895  25

5   5  -9 363.967 17.9279  12

-5   9   5 349.319 17.6733  13

9  -5  -5 369.551 18.1830  12

9   5  -5 363.493 18.1418  12

5  -5  -9 370.851 17.6279  12

-5   5  -9 378.820 18.9169  22

-5   9  -5 379.549 17.9544  23

-5   5  -9 372.253 14.7233  23

-9   5  -5 346.093 16.0665  23

-5   9  -5 392.886 18.9842  22

-9   5  -5 369.280 17.2985  22

-5   9   5 401.299 15.4086  23

9   5   5 378.894 16.6660  19

-9   5  -5 354.551 16.8691  21

-5   9  -5 344.385 14.6020  21

-9   5   5 378.243 17.9411  21

-5   5  -9 345.784 16.3056  20

5   9   5 422.495 20.4457  19

9   5  -5 342.086 15.7976  16

9   5   5 398.463 19.3478  18

-5   9  -5 370.925 17.2449  15

-9   5  -5 367.599 17.4574  15

5   9  -5 393.814 19.6973  16

-5   5  -9 370.273 17.4942  15

-9   5  -5 380.618 16.3043  14

5   9  -5 349.965 18.3309  18

-1  -7  -9 93.2451 7.77237   8

-9   1  -7 128.212 11.1926  10

-7   1  -9 120.134 10.7385   8

-9   7  -1 116.707 10.1494  10

-7   9  -1 128.646 10.2103   9

-9  -1  -7 128.393 11.4648  10

-1  -7  -9 120.681 10.0518   7

-7  -1  -9 119.015 10.9471   8

-7   9  -1 109.797 8.39153  10

-9   7  -1 118.465 9.85344   9

-1  -9  -7 122.648 9.24748   7

1  -7  -9 116.109 9.48483   7

-9  -1  -7 111.335 10.7337   6

-9  -7   1 118.511 9.03897   6

-9   7   1 117.484 9.19411   6

-9  -7  -1 102.988 8.31115   6

-9   7  -1 108.589 8.54443   6

-7  -1  -9 110.956 10.3887   6

-9   7   1 109.509 8.22019  30

-1   9   7 117.558 9.99084  30

-7   9   1 109.351 9.24605  30

1   9   7 119.366 9.52802  30

7   9  -1 106.952 8.50959  30

7   9   1 102.031 7.91026  30

-7   9  -1 118.181 8.96022  30

-1  -7   9 108.350 8.31332  25

-1   7  -9 124.930 10.0944  27

1   7  -9 105.406 9.69887  27

1   9  -7 123.918 10.2906  27

-9  -1   7 113.080 10.5288  25

1   9  -7 97.8917 7.93936  24

-7  -1   9 108.302 10.3325  25

7   9  -1 106.374 7.35262  26

-9   7   1 99.6502 8.11178  24

1   7   9 118.584 8.67757  25

-1   9   7 149.942 10.1998  26

-1   7   9 105.616 8.21041  25

-7   9   1 103.406 9.10160  24

1  -7   9 102.658 8.03203  25

-7   9  -1 122.124 10.1123  24

1   7  -9 128.148 9.26974  12

7  -1  -9 104.021 10.7072  12

-1   9   7 111.540 9.17365  13

-9   7  -1 94.7399 8.32409  13

9  -1  -7 118.494 11.6458  12

-7   9  -1 109.030 9.13863  13

1   9   7 110.721 8.59900  13

1  -7  -9 97.3927 8.02978  12

-1   7   9 116.279 8.46123  13

-7   9   1 123.342 10.0510  13

-1   9  -7 107.895 9.24925  22

-1   7  -9 105.094 8.94491  23

1   9  -7 107.716 10.2185  23

-1   9  -7 107.210 9.51075  23

-7   9   1 109.149 9.26328  22

-1   7  -9 121.382 9.73081  22

-9   7   1 100.567 9.09374  23

1   9  -7 107.725 8.45281  22

-9   7  -1 114.301 8.97395  22

-9   7  -1 113.414 10.0551  23

-7   9  -1 101.722 9.43368  22

-7   9  -1 102.470 9.30795  23

1   7  -9 104.445 8.22052  22

-7   9   1 110.958 9.35651  23

-9   7   1 106.121 8.34697  22

-9   1   7 116.274 8.12348  21

1   9   7 126.683 11.3046  19

-9   7   1 134.817 11.2208  21

-7   9  -1 105.199 9.81822  21

-9   7  -1 119.600 10.4413  21

-9  -1  -7 99.8409 7.29626  15

-9   1  -7 115.432 8.49885  15

-7  -1  -9 96.8566 7.15256  15

-7   1  -9 118.814 8.59688  15

-1   9  -7 109.872 8.94448  15

9   7  -1 122.912 11.5079  18

9   7   1 113.043 10.7063  18

-1   7  -9 100.844 9.30149  15

1   9  -7 124.117 8.91696  15

-7   3  -9 993.708 34.2758   8

-7   9  -3 1072.43 34.8705   9

-9   7  -3 1088.42 34.1606   9

-9   3  -7 1082.34 34.4610   8

-3  -7  -9 1038.52 31.6114   8

-9   7  -3 1079.70 33.8480  10

-9   3  -7 1100.36 36.4012  10

-7   3  -9 1017.78 34.8188  10

-7   3  -9 1077.09 32.0753   7

-9  -3  -7 1022.38 34.4481  10

-7  -3  -9 1057.47 36.8160   8

-7   9  -3 1066.94 29.6300  10

-9  -7  -3 1033.37 30.5182   6

-9   7  -3 1038.90 30.9243   6

-9  -3  -7 1041.60 35.4170   6

-9   3  -7 1056.19 35.5791   6

-7  -3  -9 1073.78 35.7931   6

-7   3  -9 1015.12 34.5391   6

3   9  -7 1054.25 30.3992  28

-7   9   3 1003.27 34.4429  29

3   9   7 1078.40 31.1467  30

3   7   9 1067.93 29.6312  30

-7   9   3 1101.76 33.9002  30

7   9   3 1092.67 34.1924  28

-9   7   3 1064.87 31.3411  30

7   9  -3 1050.88 30.2981  27

-3   9   7 1100.02 35.3691  29

3   9   7 1056.44 29.7813  28

7   9  -3 1063.44 34.2901  28

-7   9  -3 1007.90 29.7668  30

-3   9   7 1069.66 31.5828  26

-7  -3   9 1051.65 35.0156  25

-3   7   9 1036.41 28.8034  26

-9  -3   7 1089.57 35.3836  25

-7   3   9 1025.30 34.9212  25

-3   7   9 1037.91 30.8785  25

-9   3   7 1011.17 34.7735  25

3   9  -7 1077.58 34.6361  27

-3  -7   9 1084.79 30.9590  25

3   7  -9 1077.95 31.7863  12

9   7  -3 1071.00 32.3269  12

9   3  -7 1042.23 36.3527  12

7   3  -9 1105.13 36.7796  12

3   9   7 1066.41 29.2227  13

-9   7  -3 1047.30 28.4888  13

-7   9  -3 1015.51 30.3528  13

3  -7  -9 1096.21 31.1776  12

9  -3  -7 1044.86 35.9335  12

9  -7  -3 1023.89 31.3483  12

-7   9   3 1100.86 34.8845  13

-3   9   7 1077.13 33.5026  13

7  -3  -9 1045.00 35.5752  12

-7   9  -3 1023.75 34.3290  22

-7   9   3 1060.73 32.7365  22

-7   9   3 1045.66 32.2007  23

-9   7   3 1117.71 30.4770  22

-3   7  -9 1044.39 31.6406  23

-3   9  -7 1036.81 34.3904  22

-9   3  -7 1086.81 34.3322  22

-9   3  -7 1085.40 29.1507  23

-9   7  -3 1111.89 33.6936  22

-3   7  -9 1013.34 34.1086  22

-9   7  -3 1142.92 34.4630  23

-3   9  -7 1024.48 33.4246  23

9   7   3 1064.35 34.4510  19

-7   9  -3 1035.68 32.8780  21

-7   3  -9 1057.90 28.7291  20

-9   7   3 1092.78 35.7254  21

7   9   3 996.436 35.4797  19

3   9   7 1054.57 36.6892  19

-9   7  -3 1091.34 34.3542  21

-9   3   7 1076.61 30.9988  21

9   7  -3 1083.97 33.9828  16

9   7  -3 1045.86 37.3298  18

3   9  -7 1039.03 29.7735  15

7   9  -3 1022.54 34.9340  16

9   7   3 1086.78 36.6471  18

-9   3  -7 1020.85 31.8726  15

-7   3  -9 1049.52 32.3060  15

-3   9  -7 1078.23 33.2206  15

-9   7  -3 1032.60 31.3449  14

7   9   3 1035.35 36.5172  18

-7   9  -3 1103.03 33.7717  15

7   9  -3 1018.95 36.4466  18

-7   5  -9 1038.42 29.0326   7

-7   5  -9 1021.17 33.5194   8

-7   9  -5 1011.40 29.0606  10

-7   5  -9 999.199 33.5580  10

-9   5  -7 979.185 31.5692   8

-5  -9  -7 1020.13 31.5034   8

-5   7  -9 994.531 31.3181   8

-5  -7  -9 1065.15 34.2886   8

-9   7  -5 1031.21 33.6867  10

-9   5  -7 1078.17 35.7711  10

-7  -5  -9 998.464 36.3772   8

-9  -7  -5 997.231 31.0090   6

-9   7  -5 1063.61 31.9778   6

-9  -5  -7 1021.15 34.2001   6

-9   5  -7 966.072 33.6874   6

-7  -5  -9 1074.84 34.6916   6

-7   5  -9 1001.77 33.8637   6

7   9  -5 996.472 32.3428  27

7   9  -5 1055.83 33.5522  28

5   9  -7 1038.94 34.4043  27

7   9   5 1028.36 32.6234  28

-7   9   5 1022.35 35.2657  29

5   9   7 1003.60 30.2143  28

-7   9  -5 1046.34 29.3104  30

-7   9   5 966.864 33.5943  30

-5   7   9 1041.33 33.4961  29

5   9  -7 1047.25 31.3439  28

-5   9   7 1035.35 35.2524  29

-7   5   9 1035.10 30.8582  29

-9  -7   5 979.751 30.9736  25

-5   9   7 1033.69 30.7198  26

-7   5   9 999.082 34.0168  25

-9  -5   7 994.573 33.6655  25

-5  -7   9 1028.83 31.3744  25

-7  -5   9 1015.76 34.0793  25

-9   5   7 972.815 33.8443  25

-5   7   9 1017.99 31.8375  25

-9   7   5 953.167 31.4277  25

9   7  -5 989.158 32.3422  12

9  -7  -5 989.717 31.8705  12

5   7  -9 1007.26 32.2490  12

7   5  -9 1059.42 35.4615  12

7  -5  -9 1014.65 34.4815  12

5  -7  -9 1113.75 32.5986  12

9   5  -7 1012.46 35.2471  12

9  -5  -7 1014.91 34.8445  12

-7   9  -5 972.145 28.5822  13

-9   5  -7 1050.27 30.9697  23

-5   7  -9 1028.34 31.5701  23

-5   9  -7 1036.72 34.1048  23

-9   5  -7 1007.72 34.6839  22

-5   7  -9 1001.21 35.5616  22

-7   9  -5 1035.90 34.1789  23

-7   5  -9 976.951 28.7115  23

-9   7  -5 1117.77 35.4381  22

-5   9  -7 1033.48 36.0052  22

-9   7  -5 1036.36 33.4311  23

-9   5  -7 1065.40 30.9536  20

-9   5   7 1023.94 32.6552  21

9   7   5 1057.16 34.3444  19

-9   7   5 1048.43 35.3196  21

5   9   7 1126.15 37.8167  19

-7   9  -5 1116.65 36.2641  20

-7   9  -5 1034.63 31.1490  21

-7   5   9 1056.61 30.8873  21

-5   7  -9 1048.56 34.5393  20

-9   7  -5 999.167 32.4740  21

-5   9  -7 1111.71 36.6878  20

-7   5  -9 1100.29 32.0530  20

5   7   9 1081.75 35.2887  19

7   9   5 1038.25 36.4319  19

-9   5  -7 1071.70 31.8299  21

-9   7  -5 1018.12 29.9704  14

-7   9  -5 1030.33 34.1250  15

9   7  -5 994.671 33.4524  16

-9   5  -7 1019.22 33.6396  15

7   9  -5 1037.73 36.1772  16

7   9  -5 1060.91 37.3193  18

-7   5  -9 1083.91 34.5719  15

-5   9  -7 1086.12 34.6314  15

-9   7  -5 1005.43 34.2762  15

-5   7  -9 991.188 34.0352  15

-9   5  -7 1011.78 29.9443  14

-7  -7  -9 50.7041 8.72219   8

-7   7  -9 58.2489 7.30602   8

-9   7  -7 59.7324 8.13336  10

-7   9  -7 54.7828 6.92308  10

-9  -7  -7 60.0501 7.64055   6

-9   7  -7 69.8060 8.19754   6

7   9  -7 61.7884 7.66978  28

-7   9   7 52.6548 8.38178  29

-7   7   9 44.5381 7.57942  29

7   9   7 76.2960 7.83441  28

-7  -7   9 57.9929 7.81219  25

-9  -7   7 47.3871 7.35564  25

7   9  -7 55.8937 8.15842  27

-9   7   7 72.5842 8.71243  25

-7   7   9 62.4677 8.05247  25

7   7  -9 55.6462 7.86835  12

9   7  -7 58.1978 8.27796  12

9  -7  -7 41.9749 7.26941  12

7  -7  -9 50.3284 7.62644  12

-9   7  -7 52.9176 7.45865  23

-7   9  -7 57.4057 8.05486  23

-7   7  -9 62.7535 7.58369  23

-7   7  -9 55.9020 9.00644  22

-9   7  -7 83.4448 9.99736  22

-7   9  -7 53.3491 6.29996  21

7   9   7 81.6060 9.99990  19

-9   7   7 57.6878 8.37964  21

9   7   7 73.6994 8.86328  19

-9   7  -7 57.5018 7.12895  21

-9   7  -7 65.0722 8.19704  20

-7   9  -7 65.0617 8.90748  20

-7   7  -9 66.5789 8.53101  20

7   7   9 59.9916 8.25061  19

-7   7  -9 54.6608 8.58527  15

-9   7  -7 54.8192 8.33700  15

-9   9  -1 245.480 16.0869   9

-9   1  -9 259.196 17.2830   8

-9   9   1 253.289 15.4739  10

-9   9  -1 246.693 14.5429  10

1  -9  -9 232.381 13.4051   7

-1  -9  -9 255.554 14.8873   7

-9  -1  -9 293.440 18.4235  10

-9   9   1 258.637 16.3265   9

-9  -1  -9 259.286 17.7807   6

-9   9  -1 239.186 12.5135  30

-1   9   9 252.305 15.5450  30

1   9   9 290.413 15.5016  30

-9   9   1 260.102 14.0796  30

-9   9   1 245.449 14.4547  24

1   9  -9 268.588 12.9725  24

-9  -1   9 275.942 17.9395  25

-9   9  -1 294.612 16.2778  24

-1   9   9 265.532 14.6187  26

-9   9   1 249.510 15.1636  13

-9   9  -1 252.706 14.4803  13

-1   9   9 274.501 14.4233  13

1   9   9 274.623 13.2276  13

9  -1  -9 271.341 18.2888  12

-9   9   1 304.679 15.7468  22

-1   9  -9 243.762 15.3636  23

-9   9  -1 244.627 14.8056  22

1   9  -9 246.274 16.0038  23

-9   9  -1 265.480 16.2880  23

1   9  -9 281.172 14.2844  22

-9   9   1 277.330 16.2476  23

-1   9  -9 273.105 15.5491  22

-9   9  -1 278.729 17.2273  21

9   9   1 242.905 17.7012  18

-9   1  -9 242.018 13.2576  15

1   9  -9 262.496 15.0033  15

9   9  -1 303.298 19.3992  18

-1   9  -9 260.682 15.4936  15

-9   3  -9 1123.00 38.1621   8

-9   3  -9 1121.55 34.1052   7

-9   3  -9 1053.33 38.5665  10

-3  -9  -9 1138.82 37.0969   7

-9  -3  -9 1094.87 40.8742   8

-9   9  -3 1136.22 34.4587  10

-9   9  -3 1152.56 38.0699   9

-9  -3  -9 1128.26 39.3298   6

-9   3  -9 1064.73 38.3912   6

-9   9   3 1153.09 35.3614  30

3   9   9 1147.42 33.2655  30

9   9  -3 1050.43 31.4534  27

-3   9   9 1157.99 38.3802  29

-9   3   9 1107.00 39.0810  25

-9  -3   9 1073.71 38.2735  25

-9   9  -3 1075.60 37.0777  24

-3   9   9 1104.00 32.9798  26

3   9  -9 1103.44 37.9778  27

-3   9   9 1130.89 35.5103  13

-9   9  -3 1097.81 32.2253  13

9  -3  -9 1115.95 39.4517  12

9   3  -9 1113.26 40.1006  12

-3   9  -9 1092.91 35.7681  23

-9   3  -9 1152.31 38.7630  22

-9   9  -3 1154.80 37.6563  22

-3   9  -9 1121.67 37.8951  22

-9   9   3 1137.48 39.3769  21

-3   9  -9 1160.31 39.5443  20

9   9   3 1088.08 38.9674  19

-9   9  -3 1137.32 37.1762  21

-9   3  -9 1106.60 34.8877  15

3   9  -9 1114.71 34.0861  15

9   9  -3 1157.80 38.4632  16

-3   9  -9 1093.26 36.5284  15

9   9   3 1178.69 41.3540  18

-9   5  -9 1267.61 41.7177  10

-9   9  -5 1266.06 37.1221  10

-5  -9  -9 1251.50 37.7948   8

-9  -5  -9 1268.41 44.8545   8

-9   5  -9 1206.53 39.0812   8

-9  -5  -9 1246.39 41.0423   6

-9   5  -9 1161.36 40.2012   6

-5   9   9 1281.62 41.6107  29

9   9   5 1242.81 39.0215  28

9   9  -5 1267.74 39.9379  28

-9   5   9 1250.05 35.3489  29

5   9  -9 1277.42 33.7339  28

-9   9   5 1283.08 40.0995  30

5   9  -9 1172.94 40.5921  27

-9  -5   9 1243.63 40.8001  25

-5   9   9 1201.74 34.3455  26

-9   5   9 1190.54 40.4118  25

9  -5  -9 1265.94 42.1930  12

9   5  -9 1254.79 42.4112  12

-9   9  -5 1173.30 40.7557  22

-5   9  -9 1284.16 39.5835  23

-5   9  -9 1215.19 42.3751  22

-9   5  -9 1260.87 42.5807  22

-9   9  -5 1189.12 39.7108  23

-9   5  -9 1210.61 34.0342  23

-9   5   9 1265.91 36.8563  21

-5   9  -9 1300.38 42.5851  20

-9   5  -9 1310.01 35.7111  20

9   9   5 1244.47 41.8939  19

-9   9   5 1183.69 41.6074  21

-9   9  -5 1253.97 38.2861  21

5   9   9 1261.71 43.0983  19

-9   5  -9 1333.97 41.0663  15

-5   9  -9 1296.18 41.3197  15

9   9  -5 1238.76 41.6735  16

-9  -7  -9 92.7527 11.7661   8

-9   7  -9 105.294 9.80423   8

-9   9  -7 113.398 10.2554  10

-9   7  -9 95.9254 10.3494  10

-7  -9  -9 111.446 11.5912   8

-9   9  -7 82.6222 8.31347   6

-9  -7  -9 104.809 10.5642   6

-9   7  -9 107.482 10.9237   6

9   9   7 101.291 9.68877  28

-7   9   9 103.904 11.3297  29

7   9  -9 101.768 8.70070  28

7   9  -9 105.065 11.5323  27

-9   9   7 132.157 12.5743  30

9   9  -7 100.037 9.99246  28

-9   7   9 111.035 10.2535  29

9   7  -9 92.6907 8.43851  28

-9   9   7 82.2102 8.58630  25

-9  -7   9 114.325 10.9674  25

-7   9   9 86.3231 8.44513  25

-9   7   9 102.572 10.5885  25

9  -7  -9 117.248 11.2224  12

9   7  -9 98.6671 10.9054  12

7   9  -9 77.5255 8.56837  12

9   9  -7 82.6472 8.87468  12

-7   9  -9 85.8472 11.3752  22

-9   9  -7 98.6032 11.5513  22

-9   9  -7 100.307 10.3290  23

-9   7  -9 115.078 10.2359  23

-9   7  -9 102.173 11.8117  22

-7   9  -9 91.9881 9.89722  23

-9   9   7 113.284 12.0198  21

-9   7  -9 108.896 10.3245  20

-9   7   9 88.0787 9.96120  21

9   7   9 102.757 10.5163  19

9   9   7 115.722 11.6316  19

-7   9  -9 112.780 11.7756  20

7   9   9 112.021 11.9144  19

-9   9  -7 98.5860 9.35984  21

-9   7  -9 107.237 11.4399  15

-9  -9  -9 182.197 15.5775   8

9   9  -9 267.311 17.6925  27

9   9  -9 179.068 12.1581  28

-9   9   9 189.345 13.0695  25

9   9  -9 194.938 13.2845  12

-9   9  -9 222.303 14.9577  23

-9   9  -9 247.610 16.7808  20

-9   9   9 200.678 15.4029  21

9   9   9 242.377 16.6789  19

-9   9  -9 241.215 17.6255  15

0  10   0-0.43754 1.95500   9

-10   0   0-0.76552 3.34849  10

0   0 -10 0.78997 2.88201   8

0   0 -10-0.46551 1.64438   3

10   0   0 0.41245 1.59599   3

0  10   0 0.52527 2.29761  29

0  10   0 0.68689 3.06914  30

0  10   0-4.91463 2.79123  28

0  10   0 2.56735 2.80747  26

0  10   0-5.64613 2.94983  13

0   0 -10 3.91773 3.71341  12

0  10   0 1.14003 2.49331  23

0  10   0 3.19218 2.95164  20

0  10   0 0.68319 2.78667  19

0  10   0 1.33627 3.16645  22

-10   0   0-1.44790 3.30144  21

10   0   0 2.99419 2.45106  18

0  10  -2 479.210 16.6438   9

-10   2   0 503.777 15.6299   9

-2  10   0 446.667 17.4933   9

-10  -2   0 494.207 19.7441  10

-10   2   0 537.573 21.8672  10

-2   0 -10 478.876 20.5530   7

2  10   0 486.529 14.6277   9

-10   0  -2 472.323 20.2743  10

0  -2 -10 526.644 20.9448   8

-2   0 -10 495.914 21.1068   8

0  -2 -10 505.008 21.1549   7

-2   0 -10 493.894 17.6626   2

0   2 -10 487.848 15.7957   3

2 -10   0 504.930 15.6267   2

-10   0  -2 464.888 20.7926   6

10   0  -2 489.625 15.0683   3

10  -2   0 489.117 16.9119   3

-2   0 -10 515.803 17.8845   3

2   0 -10 505.270 15.9935   3

0  -2 -10 529.861 18.0877   3

2  10   0 516.261 16.9487   4

0  10   2 478.638 13.8312   4

10   0  -2 480.249 17.7881   4

0  10   2 490.300 19.5921  28

0  10   2 480.584 18.4724  29

2  10   0 486.012 19.3743  30

-2  10   0 465.798 18.4905  29

0  10  -2 470.073 19.5569  30

2  10   0 503.830 20.1571  28

0  10   2 500.182 19.8567  30

2  10   0 500.048 16.4978  29

0  10  -2 528.614 20.2933  28

2  10   0 487.391 18.5828  26

-10   0   2 462.166 20.1411  25

0  10  -2 517.192 19.0548  26

0  10  -2 523.519 19.5502  24

-2   0  10 494.176 20.3120  25

0   2 -10 489.182 20.5481  12

2   0 -10 500.411 20.9977  12

-2   0 -10 531.847 21.3021  12

0  10   2 477.397 19.5151  13

0  -2 -10 506.306 20.7257  12

-2  10   0 510.561 20.3320  22

0  10  -2 494.541 19.3965  23

-2  10   0 507.648 20.1319  24

2  10   0 523.470 18.5662  23

-2  10   0 519.147 19.0092  23

0  10   2 486.484 16.8159  23

0  10  -2 531.976 19.8425  22

0  10  -2 456.403 18.2518  19

0  10   2 515.820 20.7615  19

-10   0   2 495.697 19.3432  21

0  10  -2 510.567 19.2164  20

2  10   0 484.139 16.4403  20

-10   2   0 493.690 20.2911  21

-2  10   0 474.538 18.2022  19

-10   0  -2 526.522 20.9937  21

-2  10   0 498.853 19.0979  20

2  10   0 514.505 21.0643  19

0  10  -2 532.945 19.5136  16

-2  10   0 515.559 16.9521  16

0  10  -2 493.622 16.6992  18

2  10   0 473.981 18.9601  18

10   2   0 474.134 18.6729  18

-10   2   0 527.461 20.6318  14

-10   0   2 496.678 19.4548  14

-2  10  -2 946.612 28.5503   9

-10   2  -2 1032.73 33.0940  10

-10  -2  -2 1021.42 31.5181  10

-2  -2 -10 1047.86 33.3096   7

-2   2 -10 1052.02 32.1015   7

-10  -2   2 1021.20 30.9722  10

-2  -2 -10 1002.44 32.3353   8

-2   2 -10 1041.86 27.8349   3

-2  -2 -10 1054.40 27.6408   2

2   2 -10 977.503 24.2201   3

-10  -2  -2 974.403 32.2593   6

-10   2  -2 1006.01 32.8756   6

10   2   2 1049.47 26.3312   2

10  -2  -2 1003.68 26.6324   3

2  10   2 1084.36 27.4638   4

2  10   2 1029.62 28.7115  29

2  10  -2 982.292 31.0243  30

2  10   2 1012.22 31.1829  28

-2  10   2 951.526 30.9140  30

2  10  -2 976.451 31.0939  28

-2  10   2 1045.83 31.3688  29

2  10   2 980.297 30.2611  30

-2  10  -2 1023.74 31.1967  30

-2  -2  10 1008.47 31.5720  25

-2   2  10 961.316 31.2207  25

-10   2   2 933.401 31.1854  25

-2  10  -2 1043.07 31.6009  24

2  10   2 1018.27 30.4707  26

-10  -2   2 983.356 31.6909  25

-2   2 -10 1024.89 26.5116  27

-2  10   2 992.035 30.8674  26

2  10  -2 1047.58 29.1770  26

2  -2 -10 990.410 32.0009  12

2   2 -10 939.713 31.7162  12

-2  10  -2 994.348 30.7727  13

-10   2  -2 1000.37 31.5521  14

-2   2 -10 992.593 31.9577  12

2  10   2 987.493 30.5713  13

-10  -2   2 1013.96 30.1642  14

-2  10   2 1013.31 31.4359  13

-2  -2 -10 1005.01 31.9435  12

-2  10  -2 1031.36 31.6250  22

2  10   2 1025.38 27.0207  23

-2  10  -2 1045.67 31.2079  23

2  10  -2 983.283 30.3453  23

-2  10   2 1026.08 28.3418  23

-2  10   2 1060.67 32.1579  22

2  10  -2 1038.73 29.2203  22

-10   2  -2 1004.88 26.0606  22

2  10  -2 1037.65 29.0505  20

2  10   2 994.633 32.8654  19

-2  10  -2 983.266 27.4552  19

-2  10   2 1031.48 30.9039  19

-2  10  -2 1060.09 31.6950  20

-10   2   2 1092.56 32.0005  21

2  10  -2 1005.65 31.5838  19

2  10  -2 1033.44 29.9166  18

-2  10  -2 1011.81 28.1331  16

2  10  -2 1063.18 32.0699  16

-2  10  -2 1019.20 26.4506  15

10   2   2 1065.91 30.0113  18

-10   2   2 1053.19 31.7486  14

-4  10   0 2.16951 2.94973   9

-10   4   0 1.09017 2.22333   9

-4   0 -10 1.80607 3.68337   8

-10  -4   0 1.25916 2.87111  10

-10   0  -4-0.87486 3.47811  10

0  -4 -10-1.43558 3.20723   8

4  10   0-0.59403 2.59835   4

-4   0 -10-0.84611 4.00990   7

0  -4 -10 0.86174 3.33457   7

4 -10   0-1.46004 1.60045   2

4   0 -10-0.33394 1.46071   3

-10   4   0 5.85397 4.10750   6

-10   0  -4 1.84343 3.66438   6

10   0  -4-1.15263 2.03579   4

0  10   4 3.84852 3.43919  30

0  10   4 0.68037 2.84367  28

0  10   4-0.74806 3.05125  29

4  10   0 0.80281 2.64005  28

-4  10   0-0.73813 3.08511  30

4  10   0-2.79696 3.43440  30

0  10  -4 4.22608 2.87295  28

-4   0  10 0.85089 3.10427  25

0   4 -10 0.63536 2.45859  27

0  10   4-0.74529 3.18834  26

4  10   0 0.60008 2.50809  26

-10   0   4 0.87772 3.75488  25

-10   0   4-1.35390 3.02474  14

0   4 -10 1.56504 3.77660  12

0  10   4 1.41385 3.15867  13

4   0 -10-0.90936 3.89024  12

-4  10   0 1.52166 3.10335  13

0  -4 -10 1.50606 3.29384  12

0  10  -4 0.66034 2.82490  24

0   4 -10-3.15195 2.93172  22

-10   0  -4-0.98371 2.28745  22

-4  10   0-0.69890 2.98986  23

0  10  -4 0.78956 2.78905  23

0   4 -10-1.44656 2.48780  23

-10   4   0-0.79776 1.95914  22

0  10   4 1.76679 3.41836  19

0  10  -4-0.59203 2.64531  19

0  10  -4-0.77001 3.21834  20

0  10  -4-1.36117 3.22546  22

-10   4   0 1.65668 3.20532  21

-4  10   0-0.51092 2.18570  19

-10   0   4 0.62177 3.00078  21

10   4   0 0.81267 3.39665  18

-4   0 -10-0.55174 2.46529  15

4  10   0-0.83510 3.73138  18

0  10  -4 0.43831 2.22582  15

0  10  -4 1.47409 3.29325  16

-4   2 -10 232.976 14.9218   8

-10   4  -2 260.699 15.4725  10

-10   4  -2 259.734 12.5293   9

-4  10  -2 271.067 14.3485   9

-10  -4   2 300.647 13.9784  10

-10  -4  -2 257.627 13.3909  10

-10  -2  -4 253.951 14.7753  10

-4   2 -10 280.820 15.0568   7

-4  -2 -10 267.423 15.6157   8

-2  -4 -10 238.279 14.1700   8

-10   2  -4 243.686 15.0218  10

-2   4 -10 277.391 15.5521   8

-2  -4 -10 234.131 14.7049   7

10  -2  -4 267.763 10.9807   3

10   2   4 254.413 10.6320   2

-10   2  -4 258.062 15.4043   6

-10  -4  -2 275.416 14.9897   6

-10  -2  -4 243.208 15.1411   6

-4  -2 -10 271.948 11.5428   2

-10   4  -2 271.433 15.3157   6

4  10   2 265.884 13.6083  30

4  10   2 261.569 12.0501  29

-4  10  -2 276.338 14.4665  30

-2  10   4 273.312 15.0411  29

-2  10  -4 244.781 14.3067  30

2  10  -4 269.655 14.3127  28

4  10  -2 281.302 14.8062  30

4  10  -2 261.203 14.7986  28

-4  10   2 292.034 15.3833  30

-4  10   2 244.519 14.3981  29

2  10   4 266.500 14.0653  28

2  10   4 268.649 13.9689  30

2  10  -4 242.155 14.5261  30

-2  10   4 282.059 15.2594  30

4  10   2 234.501 14.0874  28

-4  -2  10 269.760 15.3210  25

-2  -4  10 257.920 14.1845  25

-10   2   4 261.514 15.3473  25

-10  -2   4 291.980 15.8634  25

2  10  -4 273.901 14.3526  27

4  10   2 281.220 14.2687  26

-2  10   4 262.746 14.3410  26

-2   4 -10 257.287 12.4707  27

-4   2  10 227.160 14.2152  25

-2  10  -4 271.420 14.4944  24

-4  10   2 269.771 14.4781  26

4  10  -2 274.077 12.4028  26

4  10  -2 281.317 13.0295  27

-4  10  -2 270.139 14.9644  24

-2   4  10 279.303 14.9226  25

2  -4 -10 265.593 14.4975  12

2   4 -10 270.309 15.0464  12

2  10   4 254.318 13.4873  13

-4  10  -2 270.473 14.2646  13

4  -2 -10 275.253 15.7646  12

4   2 -10 257.522 15.5595  12

-2  10   4 269.812 14.7229  13

2  10  -4 250.610 14.6910  23

2   4 -10 269.891 12.0994  22

-2  10   4 257.941 11.4109  23

-2  10  -4 283.587 15.0592  22

-4  10   2 264.615 14.8135  22

-2   4 -10 261.335 11.2621  23

2  10  -4 286.232 13.2402  22

-2  10  -4 271.414 14.9323  23

-4  10  -2 263.851 14.6066  23

-4  10  -2 275.298 15.3664  22

-10   2  -4 285.930 13.0481  22

4  10   2 272.944 11.7827  23

-4  10   2 265.212 13.2536  23

-2   4 -10 263.028 14.5659  22

-10   4  -2 278.849 12.4057  22

4  10   2 267.414 15.9955  19

-2  10  -4 270.133 15.2730  20

-4  10  -2 287.217 15.5424  20

-10   2   4 271.120 14.0570  21

4  10  -2 276.496 12.2899  20

-2  10   4 274.114 15.3273  19

-10   2  -4 293.408 15.6380  21

-10   4  -2 254.354 14.6831  21

-10   4   2 268.549 15.0840  21

-4  -2 -10 277.803 11.6248  15

-10  -2   4 259.719 13.0911  14

-2   4 -10 269.899 14.3796  15

2  10  -4 233.995 12.6177  18

-10   4  -2 274.366 14.7286  14

10   2   4 297.223 14.2482  18

4  10  -2 254.622 14.5738  18

-4  10  -2 251.834 12.3824  15

-2  10  -4 261.343 12.3576  15

-10   4   2 260.700 14.9216  14

-10   2   4 274.968 14.6140  14

10   4   2 265.136 14.5068  18

2  10  -4 268.982 10.5714  15

4  10   2 274.917 15.7082  18

2  10  -4 261.314 15.1507  16

-4   2 -10 269.102 13.5583  15

-4  10  -4 1.63169 3.49039   9

-4  -4 -10 0.91844 3.65156   8

-10   4  -4 2.90378 3.94825  10

-10  -4  -4-0.76341 3.26607  10

-4   4 -10-0.90630 3.50719   8

-4  -4 -10 5.98811 4.36562   7

-4   4 -10 2.11389 3.46109   7

-10  -4  -4 5.32967 3.88563   6

-10   4  -4 0.90899 3.51761   6

-4  10  -4 0.77531 3.24072  30

4  10  -4 1.64492 3.35495  28

4  10   4 6.28420 4.05304  28

4  10  -4 3.47609 3.63239  30

4  10   4 3.27897 3.16524  30

4  10  -4 1.45417 3.24899  27

-10  -4   4 6.78021 4.23408  25

4  10  -4 0.92249 2.06131  26

-10   4   4 6.99277 4.14274  25

-4  -4  10-0.84182 3.83919  25

-4   4  10 0.85749 3.40928  25

-4  10   4 7.73363 3.86360  26

-4  10  -4 6.92658 3.57393  13

-4  10   4-0.86490 3.25274  13

4  -4 -10 4.37638 4.14832  12

4   4 -10 4.54055 3.97237  12

-10   4  -4 0.76996 3.06129  14

-10  -4   4 0.58655 2.62111  14

-10   4  -4 2.03657 2.69914  22

-4  10  -4 0.86072 3.59768  23

-4  10  -4 1.73873 3.45647  24

-10   4  -4 2.09154 2.98277  23

-4   4 -10 2.12429 2.29280  23

-4  10   4-0.55927 2.74721  23

-4   4 -10 0.91125 3.11002  22

-4  10  -4 4.64055 3.69001  20

10   4   4 1.84857 3.07847  19

4  10   4 7.29408 4.55804  19

-10   4  -4 2.54665 4.16958  21

-4  10  -4 3.50227 2.76662  21

-10   4   4-0.83012 3.46979  21

-4  10  -4 8.12429 4.50969  22

-4   4 -10 0.78621 3.04256  15

10   4  -4 3.31671 2.85232  16

4  10  -4 2.51787 3.75031  18

10   4   4 4.20737 3.68091  18

-4  10  -4 2.70219 3.08097  15

-6   0 -10 132.151 11.1177   7

-10   0  -6 152.006 12.3772  10

-10   6   0 138.856 10.2860   9

0  -6 -10 139.389 9.81303   8

-10   6   0 133.218 11.3888  10

0  -6 -10 142.490 11.4072   7

-10  -6   0 100.910 9.19630   6

-10   6   0 138.024 10.8594   6

-10   0  -6 128.703 11.9064   6

-6   0 -10 138.156 11.6863   6

6  10   0 132.995 10.8324  28

0  10   6 134.170 10.7081  30

0  10   6 132.217 11.0708  29

0  10  -6 148.327 12.0152  30

6  10   0 139.229 9.98676  30

-6  10   0 135.965 10.6956  30

0  10  -6 145.180 10.0742  24

-6   0  10 141.229 12.0175  25

0   6 -10 141.586 10.9653  27

0  -6  10 119.164 9.61907  25

0  10   6 151.298 11.0499  26

6  10   0 139.601 9.40756  26

-10   6   0 153.002 9.77320  24

-10   0   6 127.536 11.2460  25

-6  10   0 141.228 11.1684  24

0   6  10 130.769 10.0622  25

6   0 -10 125.772 11.6518  12

0  10   6 129.431 9.84173  13

0  -6 -10 149.685 10.5052  12

10   0  -6 123.450 12.0859  12

-6  10   0 149.494 11.2834  13

0   6 -10 117.739 9.97584  12

-6  10   0 143.093 11.3091  22

0   6 -10 129.530 9.62300  23

-10   0  -6 135.039 9.83597  22

-6  10   0 148.420 11.0207  23

0   6 -10 132.396 9.75694  22

0  10  -6 129.672 10.1370  22

-10   6   0 134.655 9.09823  22

0  10  -6 121.807 11.0537  20

-10   0   6 128.581 8.92317  21

6  10   0 141.960 11.8843  18

10   6   0 125.031 11.4153  18

-6   0 -10 142.961 9.27476  15

-10   6   0 122.978 10.4314  14

0  10  -6 112.014 8.74910  15

-6   2 -10 863.998 31.8975   8

-10   6  -2 865.675 28.5178   9

-6   2 -10 898.538 30.0615   7

-10  -6  -2 866.351 25.8251  10

-10  -2  -6 913.174 32.0198  10

-2  -6 -10 859.962 28.5205   8

-6  -2 -10 838.998 32.0806   8

-2  -6 -10 851.997 31.0437   7

-10   6  -2 829.566 30.7316  10

-10  -6  -2 902.281 29.2462   6

-10   6  -2 804.572 28.4140   6

-10  -2  -6 821.797 31.6389   6

-10   2  -6 858.597 32.0884   6

-6  -2 -10 883.352 31.9184   6

-6   2 -10 847.923 31.4366   6

6  10   2 856.606 26.8989  30

-6  10  -2 908.219 28.7169  30

2  10   6 903.045 29.1198  30

6  10  -2 849.969 30.3765  28

6  10   2 838.675 30.1178  28

6  10  -2 847.821 28.8212  30

-2  10   6 930.500 31.3921  30

-6  10   2 930.779 30.7600  30

2  10  -6 816.593 27.6130  28

2  10   6 856.837 27.4591  28

2   6 -10 890.814 30.5160  27

-10   6   2 891.186 25.5124  30

-2  10  -6 939.250 31.1274  30

-2  10  -6 900.927 29.8915  24

2  10  -6 905.112 26.5018  24

-6  -2  10 846.038 31.4449  25

-2  -6  10 918.375 28.9244  25

-2   6 -10 880.821 28.8464  27

-6   2  10 900.425 31.9900  25

2  10   6 905.685 30.9981  26

6  10   2 942.452 29.4714  26

6  10  -2 863.349 26.0071  27

-10  -2   6 827.095 31.1769  25

-2  10   6 869.594 29.1363  26

-10   2   6 840.707 31.4572  25

6  10  -2 871.589 24.8055  26

-2   6  10 788.369 27.7084  25

-2   6  10 890.260 25.6102  26

-10   6   2 895.051 25.0947  24

2  10  -6 835.928 29.9904  27

2  -6 -10 920.086 29.1950  12

2   6 -10 873.477 29.3967  12

6  -2 -10 877.800 32.3707  12

-2  10   6 826.397 29.1962  13

10  -2  -6 898.068 33.4197  12

-6  10  -2 844.437 28.4976  13

6   2 -10 869.779 32.5034  12

-10   6  -2 873.660 25.3939  13

10   2  -6 852.669 32.9903  12

-6  10   2 901.217 30.8778  13

2  10   6 896.636 27.8152  13

2   6 -10 895.233 25.8321  22

-2   6 -10 890.203 27.0617  23

-6  10  -2 837.764 30.5199  22

-2  10  -6 898.037 30.5083  22

2  10  -6 860.789 31.1174  23

2  10  -6 884.075 26.8585  22

-6  10  -2 862.542 30.1329  23

-2   6 -10 884.620 30.2463  22

-10   6  -2 854.654 27.3854  22

-6  10   2 906.105 29.0474  23

-10   2  -6 881.161 28.7819  22

-6  10   2 885.106 30.1962  22

-10   6  -2 890.913 30.0417  23

-10   6   2 904.176 25.2888  22

-10   2   6 864.314 27.4019  21

6  10   2 911.487 33.3947  19

-2  10  -6 880.872 31.8513  20

-6   2 -10 912.436 24.7768  20

-10   6  -2 881.360 31.0140  21

2  10   6 872.075 32.9142  19

-10   6   2 835.182 30.9652  21

-6  10  -2 840.737 29.2284  21

10   6  -2 858.073 32.7713  18

-10   6  -2 862.960 29.3077  14

-10   2  -6 877.826 27.7929  15

6  10  -2 840.605 31.8269  18

10   6   2 853.498 31.3569  18

-2  10  -6 946.672 28.6202  15

-10  -2   6 848.611 26.3471  14

-6   2 -10 904.824 28.4538  15

2  10  -6 882.615 31.6959  16

2  10  -6 861.158 25.3301  15

2  10  -6 845.568 27.1026  18

-10   4  -6 401.573 18.4384   8

-10   6  -4 404.781 20.1529  10

-10   4  -6 356.591 19.8488  10

-10  -6  -4 360.015 16.1720  10

-4  -6 -10 365.049 18.5878   8

-6  -4 -10 389.071 20.8401   8

-10  -4  -6 384.421 18.9362  10

-6   4 -10 396.588 20.0058   8

-6   4 -10 386.861 17.4602   7

-4   6 -10 388.165 18.7721   8

-10  -6  -4 374.586 17.9730   6

-10   6  -4 396.917 18.7102   6

-10  -4  -6 416.877 20.4499   6

-10   4  -6 381.630 19.7080   6

4  10  -6 366.561 17.5113  28

-4  10   6 377.415 19.7638  30

6  10   4 387.004 18.8766  28

-4   6  10 418.928 18.7041  29

6  10   4 377.905 15.8812  30

-6  10   4 341.613 18.5607  30

-4  10   6 396.102 20.3175  29

4  10   6 394.645 16.7551  30

-6  10   4 360.143 19.6187  29

-6  10  -4 382.300 17.1897  30

-4  10  -6 404.247 18.5500  30

-6   4  10 353.694 15.5700  29

4  10   6 354.000 16.9242  28

6  10  -4 394.816 19.3962  28

-4   6  10 395.094 18.4157  25

-10   6   4 394.401 18.6369  25

-4  -6  10 402.806 18.6083  25

6  10  -4 385.315 17.4596  27

-6  -4  10 344.323 18.6352  25

-6   4  10 400.180 20.0201  25

4  10  -6 376.723 18.8471  27

-10  -6   4 332.928 17.0789  25

-4  10   6 373.515 17.6015  26

-6  10  -4 406.088 20.3911  24

-10   4   6 370.046 19.5942  25

-10  -4   6 360.732 19.0096  25

4  -6 -10 385.485 18.2062  12

4   6 -10 387.623 18.9300  12

10  -4  -6 380.297 20.3556  12

10   6  -4 381.643 19.1642  12

-6  10   4 361.179 19.0686  13

-10   4  -6 399.350 18.0389  14

6   4 -10 353.611 19.6786  12

-6  10  -4 389.422 17.0567  13

6  -4 -10 318.634 18.7692  12

10   4  -6 401.082 20.9972  12

-4  10   6 409.402 19.7943  13

10  -6  -4 388.776 18.9857  12

-10   4  -6 388.749 16.8134  23

-4  10  -6 382.276 19.3446  23

-6   4 -10 390.649 20.5722  22

-10   6  -4 352.075 17.7873  23

-4  10  -6 381.605 19.7376  22

-4   6 -10 390.310 20.2959  22

-10   4  -6 394.879 18.7451  22

-6  10   4 396.883 17.2184  23

-4   6 -10 379.483 16.1511  23

-10   6  -4 354.834 17.7299  22

-10   6  -4 394.671 19.2551  21

-4   6 -10 384.114 18.8797  20

-6   4 -10 373.514 16.4103  20

6  10   4 415.626 21.6150  19

-10   4   6 407.990 18.7115  21

-10   4  -6 391.540 18.6431  21

4  10   6 385.549 21.2910  19

-6  10  -4 374.742 17.1653  21

-4  10  -6 412.849 21.3160  20

-10   6   4 365.409 19.2989  21

10   6   4 364.181 17.9605  19

10   6  -4 401.099 18.1361  16

4  10  -6 350.805 14.1450  15

-10   4  -6 402.445 18.6871  15

-4  10  -6 378.797 18.0778  15

6  10  -4 380.463 20.4467  18

-6  10  -4 349.684 17.7893  15

4  10  -6 386.108 18.9400  18

-10   6  -4 370.059 17.3660  14

-6   4 -10 391.709 18.8864  15

-4   6 -10 397.040 19.4452  15

6  10  -4 375.327 20.3629  16

10   6   4 379.060 20.1566  18

4  10  -6 361.089 19.9967  16

-6   6 -10 751.927 28.4810   8

-6  -6 -10 826.555 31.6607   8

-10   6  -6 763.253 25.3289   8

-10   6  -6 779.371 30.5781  10

-10  -6  -6 836.558 29.6493   6

-10   6  -6 810.047 29.5731   6

6  10   6 793.240 27.8837  28

-6  10  -6 769.621 26.2662  30

6  10  -6 766.927 28.1868  28

-6   6  10 822.527 27.9638  29

-6  10   6 782.823 31.1732  29

-6  10   6 803.536 31.0028  30

-6   6  10 779.428 29.1427  25

-6  10   6 757.092 26.7585  26

-10   6   6 759.579 29.1314  25

-6  -6  10 790.279 28.9927  25

-10  -6   6 786.861 28.7749  25

6  10  -6 748.317 28.7513  27

-6  10   6 737.166 30.0820  13

10  -6  -6 797.143 29.7518  12

6  -6 -10 805.968 29.4027  12

6   6 -10 861.038 30.9775  12

10   6  -6 721.338 29.3449  12

-6  10  -6 802.768 31.9580  22

-10   6  -6 760.729 29.4133  22

-6   6 -10 765.892 25.0961  23

-6   6 -10 764.985 31.6772  22

-10   6  -6 800.470 28.0174  23

-6  10  -6 814.781 30.4425  23

6  10   6 791.032 32.3310  19

-6   6 -10 786.775 28.2702  20

-6  10  -6 796.330 24.7418  21

-10   6   6 828.313 30.4430  21

-6  10  -6 789.715 31.2915  20

10   6   6 854.490 28.5865  19

-10   6  -6 806.317 28.4764  21

6  10  -6 784.542 32.0991  16

-6  10  -6 784.041 29.5018  15

6  10  -6 759.338 31.0224  18

-10   6  -6 776.905 26.3701  14

-10   6  -6 770.393 29.6657  15

-6   6 -10 762.849 29.6012  15

10   6  -6 764.691 27.3901  16

-8  10   0 5.04326 3.77483  10

-10   0  -8 1.20406 4.25325   8

-10   0  -8 1.17926 4.81005  10

-10   8   0-0.94607 3.22859   9

-10   8   0 1.99966 3.86891  10

-8  10   0 1.03968 3.79303   9

-10   0  -8 6.08481 4.96386   6

0  -8 -10 0.88611 3.52281   7

-8   0 -10-1.19466 4.22004   6

-10  -8   0-0.67591 2.75698   6

-10   8   0 0.69514 2.53607   6

8  10   0 5.27107 3.96443  28

0  10   8 1.88232 3.93368  30

-8  10   0 0.78028 3.48646  30

-10   8   0-0.53162 2.86853  30

0   8  10-0.65478 2.73673  25

-8   0  10-1.15671 5.37943  25

8  10   0-2.39578 2.83855  26

0   8 -10-1.01920 3.47818  27

0  10   8 0.90583 3.40641  26

-10   0   8-1.17361 4.54138  25

8   0 -10 2.49825 4.83358  12

0  10   8 0.75685 2.84617  13

-8  10   0 0.91255 3.90387  13

10   0  -8 1.27855 5.59253  12

-10   8   0-0.81171 3.70168  13

0   8 -10-1.57966 3.45480  22

-8  10   0 0.93126 3.70232  24

-10   8   0-0.77840 3.01206  24

0  10  -8 2.08034 4.24275  23

0   8 -10 0.89050 3.34878  23

-8  10   0 1.93074 3.73556  23

-10   8   0 5.92350 4.50219  23

-8  10   0-2.15192 3.92539  21

-10   8   0-0.75643 3.23600  22

0  10  -8 0.81643 3.79695  22

-8  10   0 2.81472 4.44654  22

0  10  -8-2.34178 3.69942  15

-10   0  -8-2.45281 3.16378  15

10   8   0 2.49816 4.41227  18

0   8 -10-0.92625 3.37920  15

-8   0 -10 1.25335 2.68089  15

-8  10  -2 219.608 12.4100  10

-8  -2 -10 220.544 16.7196   8

-10   8  -2 219.024 14.9527   9

-8  10   2 246.591 14.1564  10

-10   2  -8 225.636 15.9501   8

-2 -10  -8 192.739 12.9872   7

-10  -2  -8 258.284 17.3474  10

-8  10  -2 214.696 15.2449   9

-2  -8 -10 213.502 12.5091   8

-2  -8 -10 260.132 15.9768   7

-10   8  -2 224.373 14.9487  10

-8   2 -10 233.790 14.8406   7

-8   2 -10 205.807 15.3959   8

-10  -8   2 217.209 12.9955   6

-10   8   2 212.768 12.9122   6

-10  -8  -2 215.122 12.5848   6

-10   8  -2 207.358 12.5069   6

-10  -2  -8 288.687 18.4969   6

-10   2  -8 220.326 16.4162   6

-8  -2 -10 224.247 16.4436   6

-8   2 -10 239.371 16.6556   6

2   8  10 230.791 13.3021  30

8  10   2 229.910 15.6135  28

-2  10   8 209.235 14.9444  30

8  10  -2 222.743 15.3839  28

2  10   8 230.898 14.0890  30

-10   8   2 247.904 13.3670  30

-8  10  -2 236.633 13.1733  30

-8  10   2 232.429 14.3571  30

-2  10   8 255.481 16.5621  29

-2  -8  10 230.304 12.5734  25

-2   8  10 225.615 12.9485  25

-10   8   2 225.234 12.7199  24

2  10   8 279.908 17.1035  26

-8  -2  10 215.754 15.7217  25

-10  -2   8 201.313 15.7088  25

-2   8  10 216.701 12.3820  26

-8   2  10 208.697 15.9388  25

2  10  -8 244.427 16.0075  27

-8  10  -2 263.303 16.5407  24

-10   2   8 222.867 16.2576  25

-2  10  -8 243.745 14.7550  24

-10   8  -2 243.413 14.7656  24

2  -8  10 222.627 12.4278  25

-2  10   8 221.947 13.7737  26

2   8  10 197.688 11.9855  25

-8  10   2 207.076 14.8317  13

10   2  -8 227.554 17.2930  12

-8  10  -2 227.699 13.6788  13

-2  10   8 208.404 13.9822  13

-2   8  10 233.974 13.3946  13

-10   8  -2 209.212 12.4606  13

2  10   8 243.311 12.9087  13

10  -2  -8 257.224 17.8094  12

8   2 -10 250.489 17.6770  12

8  -2 -10 231.261 17.0374  12

2   8 -10 245.410 13.4803  12

-8  10  -2 237.178 15.5106  22

2  10  -8 221.921 12.3074  22

2   8 -10 260.158 15.8182  23

-8  10   2 226.049 14.6336  23

2  10  -8 256.582 16.9894  23

-2   8 -10 222.508 14.9193  22

-2   8 -10 210.687 13.6602  23

-8   2 -10 221.211 15.8409  22

-10   2  -8 251.686 15.6201  22

-10   8  -2 230.935 14.2299  22

-2  10  -8 229.045 15.1614  22

-2  10  -8 238.756 15.6620  23

-10   8   2 255.220 13.4580  22

-8  10  -2 236.510 15.6366  23

-8  10   2 247.091 14.8921  22

-10   8   2 223.169 16.1580  21

8  10   2 228.009 17.0934  19

-8  10  -2 213.068 14.9233  21

-10   8  -2 214.524 15.2764  21

-2  10  -8 218.870 16.0629  20

10   8   2 254.257 16.9016  19

2  10   8 230.778 17.0609  19

8  10   2 211.578 16.5237  18

8  10  -2 209.721 16.5486  18

10   8   2 225.504 16.6556  18

2  10  -8 223.511 12.8184  15

-2  10  -8 225.566 14.1602  15

10   8  -2 193.743 15.8921  18

2  10  -8 231.809 13.2858  18

-8   2 -10 221.298 13.3281  15

-2   8 -10 217.068 14.8902  15

-10   2  -8 206.940 12.8623  15

-4  -8 -10 2.61803 3.81796   8

-8  -4 -10 5.28164 5.38634   8

-10   8  -4 4.85660 4.06046  10

-8  10  -4 2.53169 2.94449  10

-8   4 -10 6.52873 4.65558   8

-10   4  -8 12.0155 6.19979  10

-10   4  -8 2.98739 4.06246   8

-10  -8  -4 5.66927 3.42098   6

-10   8  -4 3.76885 3.50635   6

-10  -4  -8 1.14869 4.80167   6

-10   4  -8 4.62344 4.47334   6

-8   4 -10 4.47696 3.91020   7

-8  -4 -10 4.57123 4.99936   6

-8   4 -10 6.75457 4.92481   6

-4  -8 -10 9.20069 5.13938   7

-4  10   8 1.13516 4.51360  30

-4  10   8 4.56829 4.03500  29

-8  10  -4 5.72158 3.75850  30

8  10  -4 4.12275 4.70090  28

8  10   4 3.98795 4.16772  28

-4   8  10 7.20466 4.40372  29

4  10  -8 2.10853 3.07527  28

4  10   8 3.48007 3.41942  30

-8  10   4 5.04797 4.01448  30

-10   8   4 5.88736 4.40729  30

8  10  -4 4.63648 3.79622  27

-10   4   8 6.84864 5.20591  25

-8   4  10-1.12579 5.43381  25

-8  -4  10 1.10638 4.62488  25

-10  -4   8 2.22711 4.76436  25

4  10  -8 8.74590 4.45985  27

-4  10   8 5.62715 3.66675  26

-4   8  10 4.76083 3.07135  26

4   8 -10 3.35800 4.08434  27

-4   8  10 3.72415 3.46479  25

-4  -8  10 0.71068 3.43072  25

-8  10  -4 4.16381 3.10173  13

-10   4  -8 3.82680 3.19982  14

8   4 -10 4.88074 5.22047  12

10  -4  -8 3.59576 5.24332  12

4   8 -10 3.95031 3.94757  12

-4  10   8 2.02789 4.43578  13

10   4  -8 12.4049 5.87948  12

8  -4 -10 9.40894 5.47024  12

4  -8 -10 8.10555 4.03316  12

10   8  -4 4.86227 4.18179  12

10  -8  -4 1.51089 3.51414  12

-4   8 -10 3.36576 3.25691  23

-8  10  -4 10.0719 5.49715  24

-4  10  -8 7.17490 4.67491  23

-4   8 -10 6.80324 5.06695  22

-10   8  -4 5.03014 4.20550  23

-10   4  -8 4.31108 4.61130  22

-4  10  -8 6.79059 4.50010  22

-8  10  -4 9.01741 5.72451  22

-10   8   4 4.65663 4.86633  21

-8   4 -10 4.86458 3.18687  20

-4   8 -10 1.10717 4.03997  20

-10   8  -4 0.99336 4.05254  21

10   8   4 10.6337 5.57197  19

-10   4   8 6.30631 3.80521  21

-8  10  -4 3.59504 4.33827  21

8  10   4 6.18965 5.17464  19

4  10   8 2.56973 4.38546  19

-10   8  -4 7.03570 4.20163  22

10   8   4 6.32618 5.53482  18

-4  10  -8 2.94862 4.00975  15

8  10  -4 11.7522 6.07328  18

-8   4 -10 4.72894 3.85852  15

8  10  -4-1.17610 4.79778  16

4  10  -8 7.33317 3.79792  15

10   8  -4 4.11399 5.30701  18

-10   4  -8 3.73518 4.08524  15

10   8  -4 2.00587 3.98800  16

-6 -10  -8 89.9460 9.37343   8

-8  -6 -10 79.7167 10.8533   8

-10   6  -8 68.6342 8.40344   8

-8   6 -10 80.1068 9.57478   8

-6  -8 -10 75.6481 9.61497   8

-10   8  -6 48.8146 8.57996  10

-10   6  -8 63.1970 9.23367  10

-10  -8  -6 75.4196 8.22614   6

-10   8  -6 60.6912 8.13564   6

-10  -6  -8 65.8940 8.89630   6

-10   6  -8 90.8015 10.2598   6

-8  10   6 76.2268 9.88037  30

-6   8  10 82.0256 9.84131  29

8  10  -6 79.9804 9.23736  28

-8   6  10 67.4772 7.96043  29

-8  10   6 75.3809 10.3819  29

6  10   8 83.5170 8.17939  28

8  10   6 99.8122 10.3320  28

-10   8   6 76.9888 9.45078  30

6  10  -8 64.8034 7.71098  28

-6  10   8 81.5748 10.3508  29

-10  -6   8 69.7523 9.30279  25

8  10  -6 78.9560 9.12154  27

-10   6   8 74.2198 9.79466  25

-6  -8  10 66.7263 8.24192  25

-6   8  10 76.7773 9.00896  25

6  10  -8 92.4855 10.2194  27

-8   6  10 76.0629 10.1013  25

-8  -6  10 78.8216 9.83040  25

-6  10   8 59.7412 7.39824  26

6   8 -10 60.4287 9.26701  27

6  -8 -10 69.2178 8.57490  12

6   8 -10 75.7917 8.94249  12

10  -8  -6 69.1584 8.39751  12

-10   6  -8 58.3467 7.14391  14

8   6 -10 57.4964 9.12087  12

10   8  -6 75.8140 8.97451  12

10  -6  -8 62.8692 9.42453  12

10   6  -8 85.1470 10.7345  12

8  -6 -10 62.7807 9.35776  12

-6  10   8 72.5024 10.2620  13

-8  10   6 55.3019 8.99665  13

-10   8  -6 75.9111 10.3651  22

-6  10  -8 91.7813 10.3421  23

-8  10  -6 82.3726 10.0564  23

-10   6  -8 69.8633 10.0466  22

-10   6  -8 74.5594 8.36299  23

-6   8 -10 87.4328 8.99515  23

-10   8  -6 101.227 10.3477  23

-8   6 -10 77.4293 7.75714  23

-6  10  -8 77.2318 10.7301  22

-6   8 -10 69.1025 10.3945  22

-8  10  -6 64.7393 9.81050  20

6  10   8 86.7132 11.2781  19

-8   6  10 73.3717 8.21875  21

8  10   6 88.6498 10.8861  19

-8  10  -6 74.9333 8.41984  21

-6  10  -8 79.3161 10.4667  20

-8   6 -10 76.2586 8.52423  20

-10   8   6 80.2463 10.4787  21

-6   8 -10 114.071 11.3529  20

-10   6   8 87.0135 9.68607  21

-10   8  -6 61.4615 8.43252  21

10   8   6 81.2025 9.68250  19

10   8  -6 70.2988 9.32520  16

-10   8  -6 79.8915 10.2171  15

-8   6 -10 80.4395 9.98828  15

6  10  -8 72.3574 7.38569  15

-6  10  -8 91.0566 10.3159  15

-6   8 -10 95.1323 10.8457  15

8  10  -6 74.2358 10.6495  18

-10   6  -8 104.259 10.8171  15

-8  10  -6 82.4042 10.1237  15

8  10  -6 113.900 12.1016  16

-8 -10  -8 5.26058 4.70308   8

-8  -8 -10 10.0274 5.71771   8

-10   8  -8 11.1933 5.87139  10

-10  -8  -8 14.5296 5.17262   6

-10   8  -8 7.35165 4.19301   6

10   8  -8 6.70568 4.25880  28

10   8   8 6.20106 3.31886  28

8  10  -8 6.94411 4.19148  28

-8  10   8 10.1090 5.52899  30

-8   8  10 10.2105 4.75056  29

8  10   8 3.17026 3.68852  28

-8  10   8 6.10055 5.78403  29

-8  -8  10 7.91988 4.88401  25

8  10  -8 10.3663 5.04006  27

-10   8   8 9.37693 4.68636  25

-8   8  10 5.55109 4.22139  25

-10  -8   8 11.5831 5.14156  25

8  -8 -10 6.40403 4.25693  12

8   8 -10 9.77437 5.27591  12

10  -8  -8 15.4680 5.25039  12

10   8  -8 7.79922 4.79034  12

-8  10   8 9.20016 5.87420  13

-8   8 -10 11.0705 4.46391  23

-10   8  -8 12.9663 6.99777  22

-10   8  -8 7.65019 4.77914  23

-8  10  -8 5.46359 4.78167  23

-8   8 -10 6.87052 6.39195  22

10   8   8 3.00988 4.57743  19

-8   8  10 2.88786 4.12036  21

-8  10  -8 11.0418 5.48362  20

-8  10   8 3.64301 5.42765  21

-8   8 -10 2.08326 4.55830  20

-10   8   8 11.1230 5.27326  21

8  10   8 8.80795 5.85343  19

-8   8 -10 16.0336 6.26468  15

8  10  -8 4.33702 5.59583  18

-10   8  -8 9.89927 5.29539  15

0 -10 -10 317.754 16.8744   7

-10  10   0 347.374 18.4141  10

-10  10   0 322.261 19.4613   9

-10   0 -10 319.037 21.1171   8

-10   0 -10 359.745 22.3691   6

0  10  10 346.099 19.2954  30

-10  10   0 337.286 15.8973  30

0  10  10 323.162 17.8155  26

-10   0  10 314.408 20.6716  25

10  10   0 322.594 14.1540  26

0  10 -10 321.143 15.9903  24

-10  10   0 321.086 17.9520  24

10   0 -10 312.992 21.4263  12

-10  10   0 319.287 18.1289  13

0  10  10 359.329 16.6691  13

0  10 -10 346.849 19.8103  23

-10  10   0 317.488 19.3123  23

-10  10   0 322.719 18.0347  22

0  10 -10 348.762 17.9025  22

-10  10   0 338.226 20.7134  21

10  10   0 326.697 22.0029  18

-10   0 -10 315.472 15.2163  15

0  10 -10 324.845 18.0249  15

-10  10   2 663.425 29.2276   9

-2 -10 -10 680.371 27.5067   7

-10  10  -2 665.859 26.0887  10

-10  10   2 637.174 27.2423  10

-10  -2 -10 616.559 31.3900   8

-10  10  -2 685.794 29.4415   9

-10   2 -10 674.891 27.2190   7

-10   2 -10 730.275 31.6232   8

-10  -2 -10 710.037 32.4172   6

-10   2 -10 692.845 31.5128   6

-2  10  10 673.037 29.9155  29

-10  10   2 709.514 26.0882  30

2  10  10 681.808 26.3416  30

-2  10  10 727.256 30.0678  30

2  10 -10 671.754 29.8432  27

2  10  10 752.658 29.9500  26

-10   2  10 677.882 30.7910  25

-10  10  -2 638.351 27.8052  24

-2  10  10 708.840 26.2391  26

-2  10 -10 700.359 27.0918  24

-10  -2  10 633.621 29.9147  25

-2  10  10 665.010 26.0976  13

10   2 -10 668.141 32.1949  12

-10  10   2 721.929 29.3097  13

-10  10  -2 708.302 25.8061  13

10  -2 -10 719.293 32.6729  12

-2  10 -10 695.034 28.4806  23

2  10 -10 706.387 30.1069  23

-2  10 -10 700.141 28.6848  22

-10  10  -2 680.339 28.3028  22

-10  10   2 707.950 26.8468  22

-10  10  -2 763.826 30.6496  23

-10   2 -10 733.782 30.6796  22

10  10   2 654.592 30.6757  19

-10  10  -2 682.844 29.5138  21

-10   2 -10 707.292 26.1192  15

10  10  -2 674.380 29.5397  16

2  10 -10 693.824 26.7559  15

10  10  -2 685.131 32.5172  18

10  10   2 711.989 33.0685  18

-2  10 -10 700.637 28.5276  15

-10   4 -10 34.2200 7.85476   8

-10  10  -4 24.8555 5.97922  10

-10   4 -10 27.8378 7.94763  10

-10  -4 -10 29.0449 8.49909   8

-4 -10 -10 19.7054 6.87397   7

-10  -4 -10 28.5914 7.13361   6

-10   4 -10 22.1904 6.75751   6

10  10  -4 42.9410 7.94061  28

10  10   4 32.7369 7.37369  28

-4  10  10 47.2899 8.66298  30

-4  10  10 38.3949 8.08627  29

-10  10   4 31.9946 6.84665  30

10  10  -4 23.2039 5.35485  27

4  10 -10 35.4537 7.85229  27

-4  10  10 31.0485 5.73465  26

-10   4  10 25.7766 7.17178  25

-10  -4  10 26.5557 7.58341  25

-10   4 -10 35.2203 5.86745  14

10   4 -10 23.7030 7.54385  12

10  -4 -10 29.5785 8.15295  12

-4  10  10 25.9925 6.31459  13

-10  10   4 42.9055 8.15862  13

-10  10  -4 24.0346 7.53466  24

-10   4 -10 35.9935 8.05702  22

-10  10  -4 36.3913 7.88745  23

-4  10 -10 29.8530 7.37329  22

-4  10 -10 30.5300 6.87951  23

-10  10  -4 29.9424 6.91897  21

10  10   4 36.6228 7.93253  19

-4  10 -10 35.5647 8.34192  20

-10  10   4 32.1891 8.40469  21

-10  10  -4 34.2776 8.08646  22

4  10 -10 29.9142 6.01339  15

-4  10 -10 32.1826 7.28408  15

-10   4 -10 47.0042 7.59173  15

10  10  -4 41.1780 8.43081  16

-10   6 -10 587.533 25.0792   8

-10  10  -6 615.068 23.7896  10

-10  -6 -10 653.472 31.8301   8

-6 -10 -10 577.367 24.3705   8

-10  -6 -10 634.651 27.5782   6

-10   6 -10 638.053 28.1011   6

10  10  -6 643.088 27.0023  28

10  10   6 594.403 25.4720  28

10  10  -6 592.864 25.0962  27

-10  10   6 636.389 27.4180  30

-6  10  10 639.757 30.0056  30

-6  10  10 607.170 28.0969  29

6  10 -10 526.277 27.0247  27

-10   6  10 589.788 27.2729  25

-10  -6  10 586.168 26.9949  25

10   6 -10 581.765 27.9035  12

-6  10  10 645.377 28.4091  13

10  -6 -10 611.206 28.0136  12

-6  10 -10 615.873 26.2208  23

-6  10 -10 643.962 30.2223  22

-10  10  -6 568.401 27.9222  22

-10   6 -10 585.261 21.5522  23

-10   6 -10 540.438 27.8182  22

-10  10  -6 610.369 27.3004  23

-6  10 -10 659.142 29.6775  20

-10   6  10 612.442 23.9721  21

10  10   6 591.412 27.6654  19

-10  10  -6 587.095 24.3240  21

-10  10   6 636.538 29.8826  21

-6  10 -10 515.989 26.3507  15

-10   6 -10 599.905 27.3838  15

6  10 -10 578.457 22.9373  15

10  10  -6 556.583 29.9005  18

10  10  -6 615.699 28.0620  16

-8 -10 -10 206.192 14.9488   8

-10  -8 -10 158.381 15.3801   8

-10 -10  -8 160.418 14.4856   8

10  10  -8 172.116 14.0053  27

-8  10  10 181.031 14.8642  29

8  10 -10 140.974 14.0236  27

10  10  -8 194.086 13.4277  28

10  10   8 180.037 12.6334  28

-10  10   8 182.915 15.5393  30

-8  10  10 200.436 16.3708  30

-10   8  10 141.743 12.6016  25

-10  -8  10 153.138 12.7865  25

-10   8 -10 175.642 16.1964  22

-10  10  -8 177.631 15.9857  22

-10   8 -10 205.156 13.2080  23

-8  10 -10 189.654 13.8444  23

-10  10  -8 190.078 14.5374  23

-8  10 -10 210.174 17.3965  22

8  10 -10 181.924 16.9081  18

-10   8 -10 186.293 15.5918  15

10  10  -8 162.848 16.4341  18

-10   8  10 189.032 13.8952  21

-8  10  10 165.739 13.9275  21

-8  10 -10 205.334 15.7748  20

-10  10   8 154.905 14.4279  21

10  10   8 203.018 15.4429  19

10   8 -10 191.420 14.6625  12

10  -8 -10 154.040 12.9653  12

-8  10  10 194.733 15.9545  13

-10  10   8 233.919 17.7471  13

-10 -10 -10 482.555 23.9820   8

10  10 -10 503.162 24.6571  27

-10  10  10 467.564 24.5783  30

-10  10  10 495.456 26.4066  13

-10  10 -10 500.563 22.0756  23

-10  10 -10 545.973 27.5889  22

-10  10  10 479.676 22.9908  21

-10  10 -10 477.490 25.1848  15

10  10 -10 489.226 27.5125  18

1  11   1 766.205 22.0856   9

-11  -1  -1 745.665 27.7558  10

-1   1 -11 800.218 29.6217   8

-1  11   1 768.663 24.2123   9

1  11  -1 761.746 22.1288   9

-1  11  -1 746.522 23.9151   9

-11   1  -1 737.032 28.4731  10

-11   1   1 776.180 28.9909  10

-1   1 -11 767.989 28.5640   7

-1  -1 -11 793.358 29.1845   8

-11  -1   1 802.801 28.2956  10

-11  -1  -1 803.242 29.7085   6

11  -1  -1 769.965 22.3326   3

1   1 -11 776.627 21.9288   3

-1  11  -1 744.794 24.5952  29

1  11  -1 751.319 22.9817  29

1  11   1 777.493 24.7593  29

-1  11   1 757.267 25.9986  29

1  11  -1 819.471 28.3612  30

-1  11   1 784.438 27.9072  30

-1   1 -11 765.430 22.0470  27

1  11   1 774.525 27.7311  28

1  11   1 735.194 26.9522  30

-1  -1  11 761.028 27.9057  25

1  11  -1 817.278 26.6918  26

-1  11  -1 771.153 26.9651  26

1  11   1 793.517 27.0889  26

1  -1 -11 788.245 28.9229  12

1  11   1 752.411 27.3634  13

-1  11   1 770.480 27.7846  13

-11   1  -1 821.101 28.7185  14

-11  -1   1 815.193 27.8661  14

-1  -1 -11 865.156 29.8808  12

-1  11   1 781.067 25.0563  23

1  11  -1 795.118 26.5704  23

1  11  -1 796.426 26.8519  22

-1  11  -1 776.058 26.4346  23

-1  11  -1 821.769 28.0599  22

-1  11   1 888.131 29.1978  22

1  11   1 756.703 24.3409  23

1  11  -1 799.055 27.9286  19

-11   1   1 768.676 27.7056  21

1  11   1 834.206 29.1755  19

1  11  -1 863.181 25.7903  20

-1  11   1 791.377 27.2751  19

-11   1  -1 797.288 28.7846  21

-1  11  -1 841.482 26.9994  20

1  11   1 820.817 23.7862  20

-1  11  -1 782.395 25.9458  19

-1  11  -1 777.608 25.0180  16

1  11  -1 765.973 26.7390  16

11   1   1 822.405 25.3354  18

-11   1   1 807.876 28.2912  14

1  11  -1 795.779 25.2296  18

-1   3 -11 0.98180 4.20041   8

-11  -3   1 6.26124 3.77756  10

-11   3  -1 3.99851 2.69735   9

-11  -3  -1 1.61680 3.53636  10

-11   3   1 4.09633 4.28054  10

1  -3 -11 2.55081 4.10386   8

-11   3   1 10.4336 3.07377   9

-11   1  -3 0.98577 3.11492  10

-11  -1  -3 0.93388 3.80949  10

-1  -3 -11 1.79269 3.46881   8

-3  11  -1 4.40134 2.91673   9

-3  -1 -11 3.97361 4.62021   8

3  11   1 2.64734 2.46284   4

1  -3 -11 2.94491 4.38640   7

-1  -3 -11 3.99701 3.97292   7

3  -1 -11 6.22011 2.36334   3

-11  -3  -1 3.84408 4.29429   6

-11   3  -1 1.96437 3.90508   6

-11  -1  -3 4.06175 4.34428   6

-3   1 -11 1.85979 3.79323   7

-1  11  -3 0.88245 3.94326  30

3  11   1 3.12381 2.42177  29

3  11  -1 1.68566 3.43815  30

1  11  -3-1.70696 3.39345  28

-1  11   3 2.67063 3.44506  30

-1  11   3 1.65044 3.19362  29

1  11   3 5.15468 3.49023  29

1  11   3-1.67164 3.88740  30

1  11  -3 1.79739 3.93128  30

1  11   3-0.82617 3.10721  28

3  11   1 2.67966 3.90734  28

3  11   1 4.01043 3.80158  30

-3  11  -1 3.40021 3.79850  30

-3  11   1 4.35717 3.81206  30

-3  11   1 0.83324 3.04028  29

3  11  -1 25.2797 5.02428  26

-3  -1  11 4.64395 3.97363  25

1  11  -3 2.72900 3.04881  26

-1   3 -11 4.06423 3.04242  27

-11  -1   3 2.88721 4.20994  25

-3  11   1 0.85121 3.64177  26

-1  11   3 4.25912 3.38686  26

-1   3  11 0.87168 3.55581  25

-1  -3  11 2.57930 3.99877  25

3  11   1 2.24501 3.54688  26

3  -1 -11 0.99324 4.24932  12

-1  11   3-1.70105 3.72062  13

-11  -1   3 1.54021 3.58181  14

-11   1   3 9.12845 4.41363  14

-11   3   1 0.89395 3.55432  14

1  11   3 3.24265 3.62251  13

-3  11  -1 5.11518 4.46703  13

1  -3 -11 3.64320 4.31676  12

1   3 -11 13.0697 5.38531  12

-1   3 -11 3.69093 4.29157  12

-1  -3 -11 2.70215 3.94013  12

-11   1  -3 2.67357 2.26332  22

-1  11  -3 0.80260 3.73290  24

-3  11   1 2.11468 2.87558  23

-1  11   3 2.60608 2.64726  23

-3  11  -1 3.51732 4.01032  24

-1  11  -3 4.24930 4.10188  23

1  11  -3 5.08433 3.94120  23

3  11  -1 1.47399 3.08072  23

3  11   1 1.78460 2.87136  23

-3  11  -1 0.80056 3.18307  23

-3  11  -1 0.56782 2.69147  19

3  11  -1 1.94988 3.44423  19

1  11  -3 7.05511 3.98108  19

3  11   1 2.04343 3.95390  19

-3  11   1 1.80648 3.95117  22

1  11  -3 4.52424 3.36954  20

-1  11  -3 0.84722 3.18638  20

-1  11  -3 6.77023 3.41493  19

1  11   3 0.99058 3.61421  19

1  11  -3 5.06815 3.49461  22

-11   3   1 1.81135 4.13046  21

-3  11   1 4.91125 3.38644  19

3  11  -1 6.35239 3.01558  20

-3  11  -1 0.84089 3.59763  20

-1  11  -3-0.82162 3.35165  22

-11   3  -1 4.64014 4.23239  21

-11   1   3 11.0199 4.48367  21

-1  11   3 1.82175 3.32346  19

-3  11  -1 0.90072 3.67424  22

-3  11  -1 6.79671 2.87001  16

-1  11  -3 0.71459 2.76559  16

1  11  -3 4.23321 3.86127  16

-1  11  -3-0.44748 2.19837  15

3  11  -1 4.90664 3.57736  18

11   3  -1 5.93371 3.70814  18

3  11   1 0.88533 3.23027  18

-3  -1 -11 2.90941 2.60041  15

11   3   1 16.2626 4.79069  18

-3   1 -11 0.68778 2.73477  15

1  11  -3-0.58668 2.39350  18

-3   3 -11 538.333 24.0167   8

-3   3 -11 485.896 21.3399   7

-3  11  -3 497.230 20.6251   9

-11  -3   3 499.283 20.7237  10

-3  -3 -11 541.119 23.5092   8

-11  -3  -3 481.904 21.2710  10

-3  -3 -11 509.068 23.4485   7

-11  -3  -3 520.686 23.1399   6

-11   3  -3 480.702 22.6865   6

3  11  -3 508.242 22.2764  30

3  11  -3 502.940 22.1541  28

3  11   3 507.887 19.5052  29

-3  11  -3 454.929 20.8953  30

3  11   3 501.079 21.7237  28

-3  11   3 475.781 21.8541  29

3  11   3 499.599 20.7704  30

-3   3  11 461.146 21.7198  25

-3  -3  11 468.282 21.5359  25

3  11   3 507.359 21.3858  26

-3  11   3 500.193 21.6196  26

-3  11  -3 501.619 21.8574  24

3  11  -3 488.839 18.6802  26

3   3 -11 537.642 23.4749  12

-3  11  -3 484.482 20.9479  13

3  -3 -11 541.876 23.5544  12

-3  11   3 494.283 22.0384  13

3  11  -3 508.662 21.9009  23

-3  11  -3 518.932 22.1520  23

-3  11   3 459.998 18.1552  23

-3  11  -3 545.564 23.0958  22

-11   3  -3 444.911 17.1372  22

3  11  -3 530.721 19.3193  22

-3  11  -3 515.183 22.7649  20

3  11  -3 547.092 20.1146  20

-11   3   3 505.516 21.7607  21

-11   3  -3 517.478 22.8518  21

-3   3 -11 498.338 20.8880  15

-3  -3 -11 463.870 16.5214  15

3  11  -3 463.657 20.1439  18

11   3   3 543.992 21.4425  18

-11   3  -3 490.782 21.6856  14

3  11  -3 510.806 22.9469  16

-11  -3   3 485.318 19.8847  14

-11   3   3 488.371 21.8821  14

-3  11  -3 473.234 17.9365  15

-1  -5 -11 25.3271 5.82788   8

-5  11  -1 19.0273 5.30740   9

-11   5   1 27.3850 6.86164  10

-5  11   1 11.8752 4.80368   9

-11   5  -1 30.4289 5.47792   9

-11   5  -1 16.1129 5.81076  10

-5  -1 -11 27.4919 6.81491   8

-11  -5   1 28.6968 5.10915  10

-11  -5  -1 26.3981 5.20250  10

-11   1  -5 32.5929 7.42657  10

-11  -1  -5 30.2360 6.86962  10

-11   5   1 20.6379 4.87744   9

-5   1 -11 36.9578 7.10829   7

-1  -5 -11 28.0321 6.22303   7

1  -5 -11 25.8174 6.54373   7

-5  -1 -11 25.2031 6.50902   7

-11  -5  -1 26.0717 5.77455   6

-11   5  -1 27.7067 5.98806   6

-11  -1  -5 22.3243 6.28920   6

1  11   5 19.8384 5.13420  28

5  11   1 15.5602 5.33782  28

1  11   5 24.9009 5.51659  29

-5  11   1 29.2975 6.09305  30

-1  11  -5 16.5999 5.71741  30

-1  11   5 28.7023 5.93261  29

5  11  -1 32.6086 6.12659  30

1  11  -5 20.0393 5.18139  28

5  11   1 27.6292 5.59214  30

-1  11   5 11.5429 5.63265  30

1  11   5 26.5653 5.94915  30

-5  11  -1 15.6124 5.14326  30

1  11   5 26.2825 5.80077  26

5  11   1 14.9038 4.72675  26

1   5 -11 47.0120 6.94569  27

-11  -1   5 12.7768 5.24570  25

-1  11   5 24.2684 5.86889  26

5  11  -1 19.4515 4.56093  26

-1   5 -11 20.4252 4.74799  27

-5  -1  11 17.6498 5.69640  25

-1  -5  11 29.8613 5.99124  25

-1   5  11 24.1819 5.64025  25

-11   5  -1 25.8081 6.19127  14

-11  -1   5 30.1321 5.96431  14

1  -5 -11 27.0500 6.22937  12

-1  -5 -11 31.1889 6.13446  12

-1   5 -11 32.6864 6.48082  12

1  11   5 31.5452 6.18592  13

-5  11  -1 18.6939 5.75573  13

1   5 -11 21.2286 5.84678  12

-5  11   1 22.7441 5.61661  13

5  -1 -11 8.86589 5.55152  12

-11   1   5 21.8392 5.21221  14

-1  11   5 24.5145 5.66139  13

-11   5   1 19.6086 3.69840  24

1   5 -11 26.4270 4.94941  22

-5  11   1 21.1296 5.41176  23

-5  11  -1 34.2056 6.31954  23

5  11   1 18.5937 4.47003  23

-11  -1  -5 30.1112 4.99940  22

-1   5 -11 22.2972 5.06933  22

1  11  -5 21.6461 5.76079  23

-11   1  -5 21.3472 4.55049  22

1  11  -5 25.9332 5.31299  24

1   5 -11 18.4536 4.40096  23

-1  11  -5 19.8230 5.18087  24

-1   5 -11 28.2145 4.89985  23

-1  11  -5 27.0994 6.37872  23

1  11  -5 19.2166 4.92476  22

-1  11   5 24.5497 6.39701  19

-1  11  -5 17.2462 4.92873  22

1  11  -5 18.7397 4.99415  19

-5  11   1 17.2850 5.75792  22

-11   5  -1 17.8940 3.88443  22

1  11  -5 22.7864 5.89258  20

-1  11  -5 23.6405 6.23788  20

-11   5   1 29.2169 6.37950  21

-1  11  -5 21.9028 4.42986  19

-11   1   5 29.5538 5.57209  21

5  11  -1 19.2111 6.02394  19

-5  -1 -11 24.8438 4.52104  15

1  11  -5 24.9743 6.08359  16

-5   1 -11 39.0683 5.98719  15

1  11  -5 18.1386 4.15626  18

-1  11  -5 26.0234 4.59565  15

11   5  -1 25.2120 6.65079  18

11   5   1 29.2765 6.36965  18

5  11  -1 15.2896 5.43644  18

-1   5 -11 22.7325 5.93692  15

5  11   1 24.5557 6.61712  18

1  11  -5 24.3812 4.42188  15

-3   5 -11 689.502 27.5169   8

-11   5  -3 644.780 27.6157  10

-11  -5   3 652.872 22.8668  10

-3  -5 -11 616.313 27.4299   7

-11  -5  -3 663.698 24.1788  10

-5  -3 -11 649.315 27.9151   8

-5   3 -11 663.875 27.8851   8

-3  -5 -11 651.831 26.1909   8

-5  11  -3 656.561 26.1806   9

-11  -3  -5 643.393 26.3063  10

-5   3 -11 678.608 25.8845   7

-11  -5  -3 602.242 25.5813   6

-11   5  -3 627.059 26.2008   6

-11  -3  -5 706.698 28.3484   6

-11   3  -5 639.427 27.5990   6

5  11   3 654.250 22.2746  29

-11   5   3 685.117 21.3633  30

5  11   3 679.506 24.1030  30

-5   3  11 624.118 21.1635  29

5  11  -3 617.800 25.6422  30

5  11  -3 693.132 27.3958  28

-5  11  -3 692.330 25.7691  30

3  11  -5 627.900 26.7311  30

5  11   3 637.940 26.0310  28

-5  11   3 629.162 26.2747  30

3  11  -5 687.810 26.0923  28

3  11   5 691.074 25.4199  28

-3  11  -5 623.615 25.7602  30

-3  11   5 688.054 27.5487  30

3  11   5 667.647 24.6193  30

-11   3   5 621.526 26.7733  25

-3   5  11 647.922 25.8179  25

-5  -3  11 723.775 28.2004  25

-5   3  11 651.265 27.1436  25

5  11  -3 660.504 23.4590  27

-11  -3   5 612.922 26.4846  25

5  11   3 624.568 25.1028  26

-3  -5  11 661.076 26.0061  25

5  11  -3 620.312 20.8837  26

-5  11  -3 664.375 27.1662  24

-3  11   5 628.508 25.3103  26

-3  11  -5 673.204 26.5504  24

3  11  -5 709.423 26.5761  27

3  -5 -11 656.703 25.8581  12

5   3 -11 605.843 27.1904  12

-11  -5   3 678.276 23.4618  14

-11   3  -5 656.469 25.8288  14

-5  11  -3 643.617 24.7174  13

3   5 -11 667.159 26.6836  12

-3  11   5 664.951 26.5579  13

-5  11   3 625.466 26.3332  13

11   3  -5 700.319 29.3906  12

11  -3  -5 676.669 28.9222  12

5  -3 -11 659.800 27.6932  12

-3   5 -11 654.404 26.5945  22

-3  11  -5 630.631 26.3411  22

3  11  -5 683.940 27.5125  23

-5  11  -3 608.347 26.4750  22

-5   3 -11 639.900 27.1297  22

-3  11  -5 626.253 26.4292  23

-5  11  -3 641.673 26.3884  23

-5  11   3 608.231 23.0158  23

-11   3  -5 651.948 23.7340  22

3  11  -5 672.641 22.3631  22

-3   5 -11 664.851 21.0519  23

-11   5  -3 681.442 23.3959  22

-5   3 -11 651.750 22.3797  20

5  11  -3 651.712 22.0894  20

-5  11  -3 636.765 23.9935  21

5  11   3 628.223 28.5048  19

-5  11  -3 691.903 28.1809  20

3  11   5 638.662 28.6008  19

-3  11  -5 613.083 20.4643  21

-11   3   5 628.097 24.6965  21

-11   5  -3 652.335 26.7738  21

-11   5   3 660.875 26.9826  21

11   5   3 632.794 23.7708  19

-3  11  -5 682.593 28.3302  20

11   5  -3 652.424 22.8514  16

5  11  -3 643.796 26.6532  18

-5  11  -3 650.174 23.8254  15

11   5   3 688.238 27.0397  18

-11  -3   5 617.285 22.5431  14

-11   5  -3 657.911 25.4322  14

-3  11  -5 648.880 23.4438  15

3  11  -5 623.343 23.9351  18

-5   3 -11 706.003 25.7431  15

3  11  -5 714.633 28.5832  16

-3   5 -11 610.390 25.5115  15

-11   5  -5 668.716 24.0713   8

-11   5  -5 751.232 30.3356  10

-11  -5  -5 663.600 25.5859  10

-5   5 -11 670.156 27.9329   8

-5  -5 -11 684.416 28.6963   8

-5  -5 -11 631.537 29.2228   7

-11  -5  -5 695.129 27.8340   6

-11   5  -5 691.068 28.3653   6

-5  11  -5 662.130 25.6797  30

5  11   5 665.076 23.8358  30

5  11  -5 637.501 26.6096  28

5  11   5 749.903 27.4587  28

-5  11   5 718.279 29.6755  29

-5   5  11 629.506 23.8474  29

-5  11  -5 724.813 29.1432  24

-5   5  11 682.035 27.7354  25

-5  -5  11 716.020 28.0581  25

5  11   5 768.482 29.1361  26

5  11  -5 713.845 26.7047  27

-11   5   5 640.595 27.1803  25

-11  -5   5 680.196 27.2111  25

-5  11   5 647.338 25.8769  26

5  -5 -11 632.993 27.0892  12

5   5 -11 679.065 28.1012  12

-5  11   5 649.273 27.8001  13

11   5  -5 709.428 29.0704  12

11  -5  -5 692.635 28.6153  12

-5  11   5 676.615 23.1554  23

-5  11  -5 665.499 28.7976  22

-5   5 -11 679.056 29.2674  22

-5   5 -11 644.898 20.8134  23

-11   5  -5 682.279 25.9011  22

-5   5 -11 712.042 25.9132  20

-5  11  -5 747.688 30.1063  20

5  11   5 727.807 31.0826  19

-5  11  -5 642.774 22.7520  21

-11   5   5 710.475 28.1100  21

-11   5  -5 644.595 26.7156  21

5  11  -5 681.371 27.7125  18

-5  11  -5 637.911 25.3214  15

-11   5  -5 650.739 25.3661  14

-5   5 -11 677.507 27.3326  15

11   5  -5 676.474 23.5092  16

5  11  -5 728.128 30.5675  16

-7   1 -11 388.091 20.8266   7

-1  -7 -11 425.051 18.7293   8

-11   7   1 454.813 20.6252   9

-7   1 -11 427.486 22.9276   8

-11   1  -7 411.377 22.8552  10

-11   7  -1 429.815 22.0982  10

-1  -7 -11 441.833 21.9131   7

-11   7   1 442.388 22.7208  10

-7  -1 -11 403.719 22.6896   8

1  -7 -11 417.190 20.6494   7

-7  -1 -11 369.734 21.0876   7

-11   7  -1 431.727 20.1196   9

-11  -1  -7 428.553 23.0617  10

-11  -7   1 399.475 19.4338   6

-11   7   1 416.937 19.7927   6

-11  -7  -1 397.582 19.2879   6

-11   7  -1 436.394 19.8711   6

-11  -1  -7 417.185 23.2098   6

-7  -1 -11 457.130 23.7186   6

1  11   7 472.503 22.6237  29

7  11  -1 420.923 19.3183  30

7  11   1 437.876 22.0693  28

7  11   1 417.506 18.4296  30

1  11   7 436.656 20.6327  30

-7  11  -1 394.897 19.2426  30

-7  11   1 487.202 21.5825  30

-1  11   7 436.761 21.7967  30

-11   7  -1 440.947 19.2441  24

-1  -7  11 428.304 19.1133  25

-1   7  11 406.427 19.0545  25

1   7 -11 431.160 21.4451  27

-1  11   7 419.292 20.3846  26

-7  -1  11 441.352 23.1857  25

-1   7  11 446.282 18.3650  26

7  11   1 463.660 19.0334  26

7  11  -1 432.213 17.0734  26

-11  -1   7 480.376 24.3195  25

-11   7   1 416.511 17.4627  24

-7  11  -1 396.682 20.9165  24

-1  11  -7 406.917 19.3645  24

1  11  -7 412.214 18.0611  24

1  11   7 439.187 21.1965  26

-1   7 -11 430.100 20.7938  27

1  -7  11 413.613 18.9625  25

1   7  11 419.046 19.1604  25

7  -1 -11 441.782 23.7925  12

1  11   7 424.133 19.1086  13

-7  11  -1 445.652 20.9795  13

-7  11   1 404.264 21.0030  13

11  -1  -7 458.480 24.6163  12

-11   7  -1 462.172 18.6816  13

-1  11   7 437.392 20.3020  13

1  -7 -11 450.632 19.5597  12

1   7 -11 385.426 19.1805  12

-1   7 -11 447.029 20.3812  22

-1  11  -7 429.680 20.5245  22

1   7 -11 426.108 19.5496  23

-7  11  -1 456.515 22.3400  22

1  11  -7 437.879 19.1228  22

-11   1  -7 400.256 19.2245  22

-1   7 -11 460.402 19.4990  23

-11   7  -1 441.469 18.4000  22

-7  11  -1 444.442 21.6881  23

-7  11   1 442.976 20.9928  23

-11   7   1 424.307 17.0639  22

-7  11   1 428.006 21.1787  24

1   7 -11 408.331 18.1242  22

-7  11   1 439.557 21.5894  22

-1  11  -7 435.463 22.6268  20

1  11  -7 427.302 21.9006  20

7  11   1 405.797 23.6337  19

-11   7  -1 458.166 22.8597  21

1  11   7 423.928 23.5855  19

-11   1   7 449.488 18.2776  21

-11   7   1 455.970 23.2085  21

-7  11  -1 430.073 21.7224  21

11   7   1 424.112 22.7933  18

11   7  -1 446.386 23.8822  18

-7  -1 -11 418.292 16.6739  15

7  11  -1 392.896 22.1969  18

-7   1 -11 450.596 18.9495  15

-1  11  -7 436.093 18.8892  15

1  11  -7 458.833 18.1932  15

7  11   1 417.730 23.2884  18

-11   3  -7 1.25720 5.12808  10

-7  -3 -11 31.2374 8.72349   8

-11   7  -3 2.22303 4.30123  10

-11   3  -7-1.05157 4.06928   8

-7   3 -11 3.54009 5.69517   8

-11  -3  -7 3.38273 4.71296  10

-3  -7 -11 0.90782 4.14012   8

-11  -3  -7 2.43016 4.43307   6

-11   3  -7 1.23901 3.91478   6

-7   3 -11 4.56749 3.99589   7

-11  -7  -3 2.60927 3.72095   6

-11   7  -3-0.90106 3.58244   6

-3  -7 -11 1.17126 4.27321   7

-11   7   3 0.66657 2.91585  30

-3  11   7 3.40657 4.63180  30

3   7  11 0.65302 2.97819  30

7  11  -3 2.17022 4.08074  28

3  11   7 3.33970 3.73077  30

-7  11   3 12.5348 5.38950  30

7  11   3 4.23346 4.09556  28

-3   7  11 1.00694 4.40462  29

3  11  -7-0.82417 3.44488  28

3  11   7-0.76454 3.34436  28

-7  11  -3 3.27191 3.73041  30

-3  11   7 3.51128 5.00717  29

3  11  -7 1.07679 3.80384  27

-7   3  11 1.17099 5.00956  25

3   7 -11 1.09981 4.13603  27

3  11   7 2.17098 4.20052  26

7  11  -3 2.82444 3.15523  27

-3   7  11 2.59997 3.95239  25

-11  -3   7 2.34592 3.85744  25

-7  -3  11-3.45867 4.81876  25

7  11   3 0.91854 3.55454  26

-3  11   7 7.44184 4.15659  26

-3  -7  11 1.68430 3.68382  25

-11   3   7 4.76781 5.09926  25

11   7  -3-0.95390 3.89101  12

7  -3 -11 6.10392 5.89185  12

7   3 -11 8.78615 5.36967  12

-11   7  -3 0.91133 3.52662  14

11  -7  -3 0.91318 3.90673  12

-7  11  -3 0.84648 3.18341  13

-3  11   7 1.01908 4.05160  13

11   3  -7 1.30524 5.05083  12

3  -7 -11 8.55486 4.74627  12

3   7 -11 2.75957 3.93527  12

11  -3  -7 1.27953 5.21917  12

-3  11  -7 6.57193 4.79119  23

-3   7 -11 4.43968 3.57130  23

-3   7 -11 2.14741 4.26876  22

-3  11  -7-2.04175 4.36741  24

-7  11   3 1.74603 3.81882  23

-7   3 -11 1.20862 4.67698  22

3  11  -7 9.40891 5.36358  23

-11   7  -3 2.01589 4.00735  23

-7  11  -3 1.08909 3.84729  23

-11   3  -7 1.90005 4.06432  22

11   7   3-1.00270 3.98650  19

7  11   3 1.31719 4.49521  19

-7  11  -3-0.93126 3.98404  21

-11   7  -3 3.44427 4.57948  22

-3  11  -7 1.08798 4.09154  22

-11   3   7 0.81263 3.70603  21

-3  11  -7-1.22150 4.59363  20

3  11   7 3.96444 5.52338  19

-7  11  -3 1.14046 4.28889  22

-11   7  -3 5.40748 4.62674  21

-11   7   3 4.66789 4.38859  21

11   7  -3 2.69841 5.07386  18

3  11  -7 3.50367 2.76767  15

-11   3  -7 2.62045 4.06241  15

7  11  -3 3.73675 4.95207  18

-3  11  -7 0.87690 3.39339  15

11   7  -3-0.88728 3.79592  16

3  11  -7 0.82857 3.02303  18

11   7   3 10.8092 6.29276  18

-7   3 -11 1.80321 3.48899  15

7  11  -3 2.42991 4.14635  16

-7   5 -11 14.4795 6.01468   8

-7  -5 -11 14.4889 6.24695   8

-11   5  -7 15.0410 6.26613  10

-11   5  -7 15.0006 4.96687   8

-5  -7 -11 10.8017 5.49051   8

-11  -5  -7 16.3078 5.58278  10

-11   7  -5 11.4268 5.51998  10

-5  -7 -11 10.5796 6.15489   7

-11  -7  -5 13.8464 4.84239   6

-11   7  -5 8.66231 4.65126   6

-11  -5  -7 14.7901 5.19378   6

-11   5  -7 11.6331 5.20338   6

5  11   7 15.0307 4.88255  28

7  11  -5 12.7089 5.63748  28

5  11  -7 8.12490 4.36349  28

-5  11   7 11.2512 5.59095  29

-11   7   5 14.2083 4.82706  30

7  11   5 17.1703 6.04545  28

-5   7  11 18.3407 5.71076  29

-7  11  -5 14.6667 4.62296  30

-7   5  11 14.5247 4.35005  29

5  11   7 14.5700 4.39069  30

-7  11   5 15.0056 6.05247  30

-7  11   5 22.4290 6.72778  29

-11   5   7 13.8442 5.86348  25

7  11  -5 23.5506 5.42266  27

-5  -7  11 14.4891 4.89216  25

-5   7  11 17.7923 5.73440  25

-7  -5  11 13.2756 5.43900  25

-7   5  11 7.91075 4.94900  25

-5  11   7 8.03872 4.46841  26

-11  -5   7 19.8869 6.45672  25

5  11  -7 16.3022 6.27374  27

7   5 -11 12.1118 6.15521  12

-11   5  -7 8.33325 4.50285  14

-11   7  -5 11.7109 4.83116  14

7  -5 -11 16.2871 6.37086  12

-7  11   5 16.7905 5.79309  13

-5  11   7 16.1085 5.75294  13

11   5  -7 20.9194 7.10238  12

11  -5  -7 16.7451 6.07860  12

11   7  -5 13.2092 5.32911  12

11  -7  -5 5.79829 4.41349  12

5  -7 -11 7.51342 4.61908  12

5   7 -11 14.9493 5.60844  12

-5  11  -7 16.9341 5.73793  23

-5  11  -7 14.0990 6.16051  24

-11   5  -7 14.7871 5.62231  22

-5   7 -11 1.23539 4.65188  22

-5   7 -11 13.0388 4.38898  23

-11   7  -5 14.8203 5.48663  23

-11   7  -5 16.2870 5.65244  22

-7  11  -5 10.8930 5.74102  24

-7   5 -11 23.1312 7.03647  22

-7  11  -5 16.5199 5.17941  21

-7   5 -11 13.9565 4.42281  20

11   7   5 16.0827 5.66313  19

-11   7   5 15.1063 6.18452  21

-11   5   7 12.5672 5.07061  21

5  11   7 8.12890 5.39151  19

-5  11  -7 17.1614 6.02550  22

-5   7 -11 15.6286 5.86283  20

-11   7  -5 17.5570 6.03616  21

7  11   5 18.7152 6.68239  19

7  11  -5 9.04185 5.89540  16

11   7  -5 10.1694 6.49569  18

11   7  -5 14.5227 5.04133  16

-11   5  -7 10.3828 5.60748  15

5  11  -7 16.2858 5.77902  18

-5  11  -7 5.06904 4.44095  15

7  11  -5 14.0913 5.96239  18

-7   5 -11 15.8248 5.77825  15

-5   7 -11 19.1316 6.07713  15

-7  11  -5 18.7477 5.86078  15

-7   7 -11 186.733 13.8778   8

-11   7  -7 216.799 16.3334  10

-7  -7 -11 200.551 16.0617   8

-11  -7  -7 224.175 14.9626   6

-11   7  -7 187.376 14.3274   6

-7   7  11 188.190 13.7917  29

-7  11   7 183.198 15.5889  29

7  11   7 196.353 13.6024  28

-7  11   7 203.555 16.2217  30

7  11  -7 212.842 14.8481  28

-7   7  11 189.286 14.3662  25

-11  -7   7 187.775 13.9053  25

-11   7   7 188.236 14.5084  25

-7  -7  11 234.771 15.5329  25

7  11  -7 207.471 15.1072  27

-7  11  -7 178.821 15.6570  24

7  -7 -11 202.486 14.9198  12

7   7 -11 176.591 14.4370  12

11   7  -7 191.327 14.9305  12

11  -7  -7 225.092 15.4452  12

-7  11   7 211.541 16.1729  13

-7  11  -7 209.136 16.8615  22

-7  11  -7 215.992 16.0985  23

-7   7 -11 189.419 12.0292  23

-7   7 -11 206.791 17.2942  22

-11   7  -7 193.507 13.8761  23

-11   7  -7 248.413 17.0467  22

-11   7   7 200.300 14.8672  21

-7   7 -11 237.386 15.2462  20

7  11   7 175.544 15.5144  19

-7   7  11 189.213 12.7292  21

-7  11  -7 233.084 17.2928  20

-7  11  -7 205.507 15.3126  15

-11   7  -7 191.662 12.2317  14

-7   7 -11 213.856 15.9295  15

7  11  -7 182.992 15.8932  18

-9  11   1 589.546 27.3094   9

-11   9   1 552.239 25.4260   9

-1  -9 -11 572.724 25.4772   7

-9  11  -1 593.929 27.4705   9

-9  11  -1 566.487 22.1797  10

-11   9   1 529.804 25.5435  10

-11  -1  -9 598.230 28.9822  10

-11   1  -9 612.702 29.4281   8

-9  11   1 548.873 22.7333  10

-11   9  -1 569.994 25.6519  10

-11   9  -1 633.195 26.8993   9

-9  -1 -11 600.230 28.1044   7

-11  -1  -9 608.077 30.2789   8

-9   1 -11 563.653 28.2264   8

-11   1  -9 625.708 29.6932  10

-9   1 -11 597.625 26.7197   7

-11  -1  -9 563.966 28.8289   6

-9  -1 -11 553.229 28.6906   6

-1  11   9 595.284 27.7200  29

-1  11   9 589.609 26.9631  30

-9  11   1 589.796 24.4835  30

9  11   1 599.248 27.5970  28

1  11   9 590.415 25.5397  30

-9  11  -1 569.440 22.6894  30

1   9  11 626.277 25.2207  30

-11  -1   9 581.067 28.8153  25

1  11  -9 588.580 21.5924  24

-9  -1  11 550.829 28.1033  25

1  11   9 627.720 26.4464  26

1   9 -11 639.257 28.4303  27

1   9  11 596.951 25.3810  26

9  11   1 549.523 21.4608  26

-1  11   9 547.434 24.3878  26

-1   9  11 584.230 23.1565  26

-11   9  -1 549.173 24.0911  24

-1  11  -9 608.195 24.3266  24

-11   9   1 561.021 22.7562  24

-9  11  -1 640.296 27.3090  24

9  -1 -11 601.949 29.8845  12

1  11   9 617.322 23.1744  13

11  -1  -9 580.184 29.6429  12

-1  11   9 581.859 24.1968  13

-9  11  -1 600.107 25.2349  13

-9  11   1 642.785 27.1777  13

-11   9  -1 595.277 23.5840  13

-11   9   1 627.183 25.6969  13

-1   9  11 608.537 22.4397  13

1   9 -11 640.284 26.8263  23

1   9 -11 589.867 22.7479  22

-1   9 -11 599.792 25.1956  22

-1  11  -9 578.194 26.7960  23

1  11  -9 603.752 23.3266  22

-9   1 -11 607.671 28.0634  22

-11   9  -1 582.469 24.2507  22

-11   1  -9 559.793 25.4268  22

-1   9 -11 562.612 24.8053  23

-9  11  -1 598.347 26.6206  22

-9  11  -1 556.490 26.1342  23

-9  11   1 636.952 27.1200  23

-11   9  -1 566.342 26.3485  23

-11   9   1 577.083 22.9455  22

-9  11   1 570.027 25.3245  22

-1  11  -9 563.658 25.0550  22

1  11  -9 583.434 27.5787  23

11   9   1 636.545 29.4833  19

-9  11   1 566.809 27.7740  21

-11   9  -1 623.147 28.5890  21

-1  11  -9 613.091 29.0413  20

-9  11  -1 588.870 27.3704  21

9  11   1 586.283 29.8642  19

9  11   1 534.052 28.6727  18

11   9  -1 535.236 28.6734  18

-11   1  -9 574.994 22.3788  15

11   9   1 606.089 29.9160  18

-1  11  -9 587.786 24.5258  15

-9   1 -11 560.901 22.3822  15

1  11  -9 598.219 23.7589  15

-1   9 -11 603.918 26.5589  15

1   9 -11 597.861 25.7044  15

-9  -3 -11 31.4696 7.99755   8

-11  -3  -9 61.3664 10.5852   8

-11   9  -3 41.0774 7.65408  10

-9  11  -3 35.0454 7.93711   9

-11   3  -9 42.5609 8.32653   8

-11   9   3 28.4040 7.41616  10

-9  11   3 34.6152 6.91168  10

-9   3 -11 38.5971 8.07233   8

-11   3  -9 44.3085 9.13123  10

-11   9   3 32.9551 7.43183   9

-11   9  -3 41.6060 6.31092   6

-11  -3  -9 36.3715 8.17718   6

-11   3  -9 46.5047 8.20767   6

-11   3  -9 28.6809 6.15402   7

-3 -11  -9 39.1418 7.60247   7

-9   3 -11 37.5798 8.50718   6

-9   3 -11 35.3875 7.23793   7

-9  -3 -11 40.5313 9.24539   6

-3  -9 -11 29.5249 7.64578   7

3   9  11 39.8672 6.51896  30

9  11  -3 29.9746 7.36609  28

9  11   3 50.4607 8.45407  28

-3   9  11 54.6342 8.82574  29

-9  11  -3 40.7035 6.13699  30

-3  11   9 29.5237 8.38755  29

-3  11   9 55.2124 9.32178  30

3  11   9 27.6383 6.18863  30

-9  11   3 25.9483 6.52425  30

-11   9   3 40.3043 6.88996  30

9  11   3 43.3463 7.01905  26

-11   3   9 59.5947 9.37994  25

-11  -3   9 26.1405 7.75444  25

-3   9  11 35.8127 6.11253  25

3  11   9 49.6745 8.24242  26

-9   3  11 31.6207 7.99893  25

-9  -3  11 27.2583 7.42337  25

-3   9  11 32.2721 5.62833  26

-3  11   9 48.3005 7.21949  26

3  11  -9 48.7251 8.85175  27

3   9  11 30.5275 5.67635  25

9   3 -11 47.1181 8.76135  12

-11   3  -9 40.5822 7.20164  14

-9  11   3 44.5699 8.24875  13

11  -3  -9 35.0828 9.16477  12

11   3  -9 53.2838 9.76381  12

-9  11  -3 54.6105 7.57648  13

3   9 -11 32.4118 6.23009  12

-3  11   9 37.4974 7.26576  13

9  -3 -11 37.2670 8.74736  12

-3   9  11 25.6616 6.38987  13

-11   9   3 40.9263 7.78794  13

11   9  -3 40.4109 6.70360  12

3  11  -9 42.7845 8.63454  23

-3  11  -9 34.7209 7.85690  23

-3   9 -11 30.2373 6.30961  23

-3  11  -9 43.6733 7.74018  24

-11   9  -3 44.6152 7.96792  24

-9  11  -3 36.0730 8.01195  24

-3   9 -11 42.9009 8.42037  22

-9   3 -11 25.1962 7.18660  22

-11   9  -3 42.6784 8.63717  23

3   9 -11 33.7102 7.52645  23

-11   3  -9 44.1245 8.23062  22

-9  11  -3 39.3345 8.09006  23

-3   9 -11 40.0049 8.18181  20

-11   9  -3 34.2321 7.53923  22

11   9   3 27.3701 7.38392  19

9  11   3 39.7125 9.07969  19

-9  11  -3 37.3400 7.79692  22

-3  11  -9 57.7503 9.20854  22

-9  11   3 40.3007 8.86045  21

-9  11  -3 34.7659 7.57596  21

-11   9   3 54.4284 9.55712  21

-11   9  -3 42.3054 8.32905  21

11   9  -3 37.5264 7.56271  16

3  11  -9 38.5500 6.47945  15

9  11  -3 26.3265 7.80695  18

3   9 -11 35.5587 7.01009  15

-9   3 -11 33.3899 6.77281  15

9  11   3 55.7579 9.93382  18

11   9  -3 34.6559 9.24310  18

9  11  -3 38.5272 8.30930  16

11   9   3 43.1260 8.91751  18

-3  11  -9 36.4632 7.39041  15

-11   3  -9 32.7007 6.95502  15

3  11  -9 28.8860 6.18656  18

-3   9 -11 32.5366 7.14090  15

-9   5 -11 42.8314 8.28546   8

-11  -5  -9 51.3626 10.3661   8

-9  -5 -11 49.5474 10.1877   8

-11   5  -9 58.9511 8.57977   8

-11   9  -5 50.5346 8.39928  10

-5  -9 -11 42.4081 7.55388   8

-11   5  -9 43.9401 9.20414  10

-11   9  -5 35.6325 6.46291   6

-11  -5  -9 46.0340 8.37760   6

-11   5  -9 49.5096 9.22541   6

-5  -9 -11 38.6313 8.27970   7

-11   9   5 53.1105 8.48606  30

9  11  -5 40.0431 7.78055  28

-5  11   9 52.1741 9.64130  30

-9  11   5 47.4226 8.21119  30

5  11  -9 37.2749 6.18585  28

9  11   5 52.6114 8.28296  28

-5   9  11 50.2722 8.43478  29

-5  11   9 69.6167 10.6113  29

-11  -5   9 50.1729 8.61090  25

5   9 -11 46.6089 8.63438  27

-5   9  11 43.6250 6.73485  25

9  11  -5 43.7057 7.27552  27

5  11  -9 23.8185 7.54077  27

-11   5   9 50.4475 8.87220  25

-9  -5  11 48.5967 8.69187  25

-9   5  11 36.0455 8.52168  25

-5  11   9 41.0612 6.88343  26

9   5 -11 49.3069 9.21168  12

-11   5  -9 44.7025 6.63201  14

11  -5  -9 62.2923 10.6832  12

11   5  -9 50.9746 9.74445  12

11   9  -5 40.1531 6.68137  12

9  -5 -11 47.3367 9.07442  12

-5  11   9 46.1202 8.73307  13

5   9 -11 41.0719 7.10422  12

-5   9  11 54.7312 8.40755  13

-5   9 -11 43.4142 7.24315  23

-5  11  -9 45.5775 9.09377  24

-11   5  -9 37.0929 8.01473  22

-9  11  -5 41.4246 8.55212  24

-5  11  -9 45.9925 8.02726  23

-11   9  -5 60.1969 8.94767  23

-9  11  -5 46.2873 8.05180  23

-5   9 -11 52.6894 9.41783  22

5  11   9 48.8078 10.1737  19

-9  11   5 36.8575 8.57364  21

-11   5   9 40.7329 7.15955  21

-11   9   5 49.8942 9.31113  21

-11   9  -5 53.6995 9.07040  22

-5   9 -11 47.7035 8.68180  20

11   9   5 59.0308 9.11707  19

-5  11  -9 79.4733 10.6350  20

-9  11  -5 31.0694 7.69430  22

-9  11  -5 41.8576 7.58349  21

-5  11  -9 49.1480 9.18222  22

9  11   5 41.2331 8.90070  19

-11   9  -5 49.0153 8.45500  21

11   9  -5 37.8232 7.83506  16

9  11  -5 25.0624 7.65154  16

11   9  -5 54.8765 10.4419  18

-11   5  -9 47.3432 8.44022  15

-9   5 -11 61.2739 9.23647  15

5  11  -9 43.6942 6.56240  15

-5  11  -9 40.2555 8.02965  15

9  11  -5 47.3950 9.68065  18

5  11  -9 44.6595 8.12268  18

-9   7 -11 415.452 20.5196   8

-9 -11  -7 455.836 22.0581   8

-11  -7  -9 458.621 25.9891   8

-11   9  -7 418.297 21.1421  10

-7  -9 -11 421.666 25.0510   7

-11   7  -9 434.419 22.9586  10

-9  -7 -11 448.493 25.1999   8

-7  -9 -11 391.197 21.4267   8

-11   9  -7 399.876 18.8417   6

-11  -7  -9 421.112 21.3755   6

-11   7  -9 443.949 22.2987   6

11   7  -9 385.065 17.8594  28

11   9  -7 462.734 21.7814  28

11   9   7 432.978 20.5633  28

9  11   7 442.159 20.9411  28

9  11  -7 455.527 21.9055  28

-7  11   9 386.180 22.9570  29

7   9 -11 453.351 24.4340  27

-9  11   7 402.820 22.8405  30

-11   9   7 446.066 22.3391  30

-7   9  11 420.194 22.0544  29

7  11  -9 421.534 19.0024  28

-9   7  11 410.846 19.4475  29

-11   7   9 393.481 21.5923  25

-9  -7  11 391.711 21.1064  25

9  11  -7 402.620 21.3677  27

7  11  -9 455.040 23.7933  27

-11  -7   9 410.108 21.4640  25

-9   7  11 381.300 21.0865  25

-7   9  11 361.804 18.2691  25

9  -7 -11 438.700 22.3338  12

9   7 -11 441.485 23.1658  12

11  -7  -9 430.274 22.4198  12

11   7  -9 413.595 22.6377  12

11   9  -7 386.174 18.9436  12

-7  11   9 480.982 25.3457  13

-9  11   7 450.647 24.9189  13

7   9 -11 459.872 20.4328  12

-7   9 -11 432.951 20.1670  23

-11   9  -7 372.438 22.2575  22

-7  11  -9 440.272 24.9688  22

-11   9  -7 431.545 21.9279  23

-7  11  -9 434.005 22.5894  23

-9  11  -7 464.457 23.8337  23

-9   7 -11 409.488 17.6854  23

-9  11  -7 408.788 24.0532  22

-7   9 -11 378.419 23.6268  22

-11   7  -9 414.171 23.3844  22

-9   7 -11 467.242 20.7728  20

-9  11   7 440.452 24.2068  21

-11   9   7 451.252 23.7138  21

11   9   7 440.174 21.9207  19

-7   9  11 439.076 21.0003  21

9  11   7 432.693 24.0015  19

-11   7   9 410.683 20.7129  21

-7  11  -9 519.466 25.9297  20

-11   9  -7 405.849 19.8200  21

7  11   9 443.365 24.6528  19

-7   9 -11 474.551 23.4690  20

7  11  -9 454.986 24.8638  18

-11   7  -9 423.373 23.0694  15

-7  11  -9 428.249 23.2184  15

-9   7 -11 444.803 23.6119  15

-9  11  -7 451.082 23.8140  15

-7   9 -11 375.662 22.4894  15

9  11  -7 427.957 25.4590  18

-11  -9  -9 390.920 22.9090   8

-9 -11  -9 335.109 18.7578   8

-9  -9 -11 383.104 21.5698   8

-11   9   9 404.654 21.8987  30

11   9  -9 352.295 17.0921  28

-9  11   9 374.487 22.0299  30

9  11  -9 354.348 17.2468  28

11   9  -9 358.701 20.3813  27

9   9 -11 377.140 22.0289  27

9  11  -9 363.717 21.0165  27

-9   9  11 336.028 17.3349  25

-9  11  -9 382.826 23.0265  24

9   9 -11 334.132 17.6647  12

11   9  -9 345.418 17.8844  12

-9  11   9 400.584 23.3828  13

-11   9  -9 376.249 22.4519  22

-9  11  -9 352.911 20.0306  23

-9   9 -11 374.564 18.0870  23

-11   9  -9 365.045 18.9327  23

-9  11   9 348.308 20.8579  21

-9   9 -11 370.684 19.9352  20

-9   9  11 371.289 19.0534  21

-11   9   9 351.866 19.9839  21

9  11   9 371.042 21.2370  19

9  11  -9 410.902 24.4280  18

-9   9 -11 368.778 22.1728  15

11   9  -9 356.859 23.9962  18

-11  11  -1 5.13260 5.61286   9

-11  11   1 7.70006 5.73444   9

-11   1 -11 1.48642 5.75201   8

-11  11  -1 1.85549 3.78449  10

-11  11   1 1.00901 4.50872  10

-11  -1 -11 1.52726 5.91005   6

-1 -11 -11 3.80531 4.07006   7

-11   1 -11 2.29174 5.01241   7

1  11  11 2.10419 3.95677  30

-1  11  11 4.82726 5.16296  30

11  11   1 6.65978 6.19466  28

-1  11  11 1.35215 5.08507  29

-11  11   1 3.01435 3.43697  30

-11  -1  11 7.29723 7.16843  25

1  11  11 6.45742 4.70785  26

11  11   1 1.24544 2.89647  26

-1  11  11 4.88014 4.45129  26

-11  11   1 1.11664 4.19948  13

11  -1 -11 4.72251 6.09157  12

-1  11  11 5.73126 4.54261  13

-11  11  -1 1.92295 4.29634  13

-1  11 -11-2.35780 4.80885  23

-11  -1 -11 2.46102 4.89227  22

-11  11  -1 7.65676 5.08723  24

-11   1 -11 11.5924 5.75546  22

-11  11  -1 1.26113 5.01400  23

-1  11 -11 3.34903 4.04109  24

1  11 -11 1.24877 4.26191  23

11  11   1 6.09093 6.05399  19

-1  11 -11 5.08219 4.44630  22

1  11 -11 3.14941 3.51839  22

-11  11  -1-1.07319 4.03610  22

-1  11 -11 5.78758 6.04767  20

-11  11   1 2.92780 4.53899  22

-11  11  -1 3.99316 5.29198  21

11  11  -1 4.68576 4.93512  19

11  11  -1 1.29396 4.72097  16

-11   1 -11 1.54616 3.23156  15

11  11  -1 1.61008 6.23053  18

-1  11 -11 4.36685 4.77554  15

11  11   1-3.23914 5.52723  18

1  11 -11 4.02707 4.40400  15

-11  11   3 204.542 16.3738   9

-11  11  -3 184.925 13.1649  10

-11  11   3 207.667 15.6245  10

-11   3 -11 166.353 12.9651   7

-3 -11 -11 193.408 14.9361   7

-11  -3 -11 212.259 18.3004   8

-11   3 -11 195.215 16.3078   8

-11  -3 -11 198.861 17.1775   6

-11   3 -11 231.245 18.3785   6

11  11  -3 191.209 15.6209  28

11  11   3 197.128 15.7342  28

-11  11   3 193.136 13.3419  30

-3  11  11 210.863 16.7866  30

3  11  11 195.528 13.2657  30

-3  11  11 162.460 15.0190  29

-11  -3  11 202.839 16.9666  25

-3  11 -11 208.164 14.7689  24

11  11   3 208.863 13.3173  26

3  11  11 222.249 16.3242  26

-11   3  11 161.802 15.5146  25

-3  11  11 171.348 12.5262  26

3  11 -11 188.128 16.1732  27

-11  11  -3 175.766 14.7816  24

-11   3 -11 173.676 12.0638  14

-11  11  -3 176.554 12.3283  13

-3  11  11 141.929 12.5750  13

-11  11   3 174.517 15.0497  13

11  -3 -11 212.047 17.6531  12

11   3 -11 190.472 17.5359  12

-3  11 -11 170.970 14.5364  22

-11  11  -3 173.905 14.6431  22

3  11 -11 183.193 16.1584  23

-3  11 -11 187.419 14.6419  23

-11   3 -11 187.966 16.0626  22

11  11   3 212.019 17.3239  19

-3  11 -11 195.464 16.6573  20

-11  11   3 204.437 17.2937  21

-11  11  -3 179.810 15.0989  21

11  11  -3 184.214 15.5151  16

11  11   3 210.068 18.5327  18

-3  11 -11 198.456 15.4726  15

-11   3 -11 183.666 13.5719  15

3  11 -11 171.411 12.9602  15

-5 -11 -11 301.506 19.4001   7

-11  -5 -11 331.302 22.5555   8

-11  11   5 310.994 19.5976  10

-11   5 -11 302.583 18.8454   8

-11  11   5 295.118 19.8008   9

-11  -5 -11 327.503 20.7728   6

-11   5 -11 288.317 20.1435   6

11  11  -5 315.681 19.6632  28

11  11   5 320.872 19.1478  28

-5  11  11 360.711 22.4523  30

-5  11  11 292.654 19.7206  29

-11  11   5 317.338 18.4256  30

11  11  -5 304.639 16.0408  27

-11  -5  11 289.762 19.4424  25

-11   5  11 267.672 19.0525  25

-11  11  -5 278.409 19.0721  24

-5  11 -11 295.881 19.0352  24

5  11 -11 270.044 19.1305  27

11   5 -11 321.177 21.2380  12

11  -5 -11 311.293 20.6544  12

-5  11  11 310.541 18.6968  13

-11  11   5 297.351 20.0135  13

-5  11 -11 295.082 20.1709  22

-5  11 -11 292.588 18.0084  23

5  11 -11 304.505 20.8230  23

-11   5 -11 338.501 21.3702  22

-11  11  -5 345.088 20.4939  23

-11  11  -5 312.101 20.0206  22

-5  11 -11 324.973 21.0993  20

-11  11   5 318.621 21.2738  21

-11  11  -5 303.023 18.0790  21

11  11   5 303.872 19.9091  19

5  11 -11 242.025 16.6079  18

-5  11 -11 329.279 20.2037  15

11  11  -5 324.697 20.0021  16

5  11 -11 295.922 15.9592  15

-11   5 -11 313.205 19.0283  15

-11 -11  -7 1.14066 4.41391   8

-11  -7 -11 4.40011 5.67555   8

-7 -11 -11-1.29830 4.88235   7

11  11  -7 2.02082 4.32256  28

11  11   7 1.89066 3.55502  28

-7  11  11 2.45081 4.99834  29

-11  11   7 1.11229 4.75840  30

11  11  -7 0.95662 3.49008  27

-11  -7  11-1.05224 4.18334  25

7  11 -11-1.29821 4.88204  27

-11   7  11 4.38650 4.89999  25

11  -7 -11 5.40381 5.57616  12

11   7 -11-1.14883 4.80170  12

-7  11  11 1.20534 4.39746  13

-7  11 -11-0.97849 4.37212  23

-7  11 -11 1.29644 5.01670  24

-11  11  -7 3.99719 5.15585  24

-11   7 -11 1.35882 4.95737  22

-11  11  -7-1.14388 5.21651  23

-11  11  -7-0.76575 3.20060  21

-11  11  -7-1.30056 5.17055  22

-7  11  11 2.13208 4.45569  21

-7  11 -11 1.26764 4.47790  20

-7  11 -11-1.40349 5.86610  22

-11  11   7 3.91760 5.19166  21

11  11   7 5.76821 5.15474  19

-11   7 -11 2.41609 5.28418  15

7  11 -11 1.37705 3.26316  15

-7  11 -11 3.81512 4.92100  15

7  11 -11 2.46755 4.05733  18

11  11  -7-1.56142 6.20762  18

-11 -11  -9 30.5473 6.58581   8

-11  -9 -11 38.9085 8.23945   8

-9 -11 -11 41.5463 8.38806   7

-11  11   9 28.8851 7.18224  30

-9  11  11 27.9006 7.24072  30

-11   9  11 20.7306 6.90611  30

11  11  -9 25.7977 5.19027  28

11   9 -11 26.5478 7.15749  27

9  11 -11 40.0067 8.11778  27

11  11  -9 29.4015 7.05986  27

-11  11   9 24.6993 7.32581  13

-9  11  11 33.9930 7.60749  13

-9  11 -11 30.5233 6.53508  23

-11   9 -11 32.5219 8.14938  22

-11  11  -9 24.8263 6.35977  23

-9  11 -11 30.8898 7.62403  24

-9  11 -11 22.7453 7.43954  22

-11  11  -9 21.7100 7.00633  22

-11  11   9 20.8950 6.36328  21

-9  11  11 33.4339 6.87834  21

-11   9  11 27.2443 5.82224  21

11   9 -11 31.1961 8.58364  18

11  11  -9 24.6418 7.37776  18

9  11 -11 20.6554 6.67926  18

-11 -11 -11 82.0504 9.00806   8

-11 -11 -11 61.7634 10.1266   7

-11  11  11 59.8130 8.61922  30

11  11 -11 70.0989 8.89345  27

-11  11  11 91.3848 10.7035  13

-11  11 -11 75.2787 10.2719  24

-11  11 -11 73.2671 10.3620  22

-11  11  11 60.4766 8.03166  21

11  11 -11 83.1256 10.6158  18

0  12   0 1003.90 29.3137   9

0   0 -12 1085.52 37.5918   8

-12   0   0 1027.77 36.1426  10

-12   0   0 1071.63 38.0843   6

0  12   0 1035.15 35.1771  28

0   0 -12 1101.13 28.3899  27

0  12   0 1059.09 31.5695  29

0  12   0 1039.50 35.2345  30

0  12   0 1093.18 35.0254  26

0   0  12 1080.98 36.0473  25

0  12   0 1009.34 35.2948  13

-12   0   0 1101.78 36.2104  14

0   0 -12 1098.26 37.3115  12

0  12   0 1072.99 35.1533  22

0  12   0 1129.65 33.4476  23

0  12   0 1025.73 34.2997  19

0  12   0 1166.42 32.6969  20

0  12   0 1086.50 33.1920  16

-2   0 -12-1.11572 4.31735   8

0  12   2-4.73052 3.05085   9

0  12  -2 0.58370 2.60809   9

-12   0   2-1.04903 3.82713  10

-12   2   0-2.24397 4.57645  10

-12  -2   0-1.90423 3.97948  10

-12   0  -2 1.06928 4.25102  10

0  -2 -12 2.06953 4.62353   8

-2  12   0 1.45958 3.82367   9

-2   0 -12 1.08582 3.96136   7

0  -2 -12-2.23738 4.32885   7

-12  -2   0 2.25824 4.11933   6

-12   2   0 6.82947 4.75743   6

-12   0  -2 2.29867 4.56930   6

-2  12   0 0.82199 3.09112  29

2  12   0 0.95650 4.09188  30

2  12   0-2.01052 3.43059  28

0  12  -2-0.98874 4.32487  30

0  12   2 0.80977 3.21934  29

0  12   2 3.91107 4.27687  30

2  12   0 0.56249 2.51329  29

0  12  -2 0.84738 3.45635  26

0   2 -12 1.20301 2.26199  27

0  -2  12 3.92781 4.47803  25

2  12   0-0.85194 3.72649  26

0   2  12 2.97842 4.14955  25

-2   0  12 3.09846 4.51767  25

-12   2   0-2.01411 4.20911  14

0  -2 -12 5.29292 4.82750  12

-12   0   2-0.93655 3.52194  14

0  12   2 1.92674 3.40302  13

0   2 -12 2.14324 4.58437  12

2   0 -12 2.21617 4.84689  12

0  12   2-0.62576 3.02005  23

-2  12   0-0.81557 3.48898  23

2  12   0 2.23497 3.72167  23

0  12  -2-0.89352 3.64456  23

-12   0   2 1.82118 4.15258  21

2  12   0-1.05848 3.98047  19

-12   2   0-1.02343 4.17447  21

0  12   2-2.03460 4.14946  19

0  12  -2-0.88829 4.28705  22

0  12  -2 0.82712 3.37371  19

0  12  -2-1.63042 3.15451  20

2  12   0-0.56329 2.86047  20

-2  12   0-1.99080 4.53937  22

-2  12   0-0.77787 3.01003  19

0  12  -2 4.18151 3.81381  16

-2  12   0-1.81186 2.64176  16

12   2   0 0.78610 3.28559  18

2  12   0 0.84552 4.56233  18

-2  -2 -12 235.595 16.4464   7

-2  12  -2 245.199 13.5782   9

-12  -2   2 186.712 13.9560  10

-12  -2  -2 232.617 15.2506  10

-12   2  -2 225.434 16.1544  10

-12   2   2 203.517 15.2229  10

-2  -2 -12 243.023 16.1847   8

-12  -2  -2 183.796 14.6274   6

-12   2  -2 224.692 16.1912   6

-2  12   2 217.809 14.4185  29

-2  12  -2 209.321 14.4984  30

2  12  -2 251.740 15.7469  30

-2  12   2 229.064 15.0183  30

2  12   2 240.821 13.2944  29

2  12   2 234.316 15.1131  28

2  12  -2 248.372 15.6892  28

2  12   2 243.424 15.2207  30

-2  -2  12 228.136 15.4129  25

-2   2  12 225.522 15.3430  25

-2   2 -12 224.396 11.0116  27

2  12   2 209.144 13.8769  26

-2  12   2 219.801 14.8813  26

2  12  -2 233.163 13.6191  26

2  -2 -12 226.072 15.6329  12

2   2 -12 261.861 16.8003  12

-2  12  -2 216.362 14.6729  13

-2  12   2 212.330 14.9467  13

2  12  -2 249.260 14.1069  22

-2  12  -2 246.747 15.4515  24

2  12   2 213.240 11.6041  23

2  12  -2 220.703 14.2644  23

-2  12   2 213.516 12.4499  23

-2  12  -2 243.761 15.3802  22

-2  12  -2 229.295 14.6603  23

2  12  -2 244.719 15.4418  19

2  12  -2 234.460 13.2107  20

2  12   2 213.429 15.8083  19

-12   2  -2 215.341 15.2844  21

-2  12  -2 217.165 12.2806  19

-12   2   2 233.193 15.1657  21

-2  12   2 243.180 14.8805  19

-2  12  -2 240.768 15.0239  20

2  12  -2 208.164 13.0996  18

2  12  -2 266.509 16.2102  16

-2  12   2 220.565 11.7146  16

-12   2   2 223.318 14.9568  14

-2  12  -2 200.014 12.0345  16

12   2   2 239.166 13.8882  18

-12  -2   2 235.995 14.5011  14

-4  12   0 3584.47 83.6196   9

-12   4   0 3741.23 78.1258   9

0  -4 -12 3700.19 84.7986   8

-12  -4   0 3762.43 83.1257  10

0  -4 -12 3677.76 88.7613   7

-12   0  -4 3567.31 87.8017  10

-4   0 -12 3691.58 87.9083   7

-4   0 -12 3618.07 88.9440   8

-12  -4   0 3589.17 86.8975   6

-12   4   0 3530.31 86.9891   6

-12   0  -4 3568.05 89.1074   6

-4  12   0 3531.71 85.1754  30

0  12   4 3621.01 85.8038  30

4  12   0 3672.24 86.8723  28

0  12   4 3513.58 83.8915  29

4  12   0 3569.00 84.3159  30

0   4 -12 3670.96 81.1624  27

-4   0  12 3736.56 88.1567  25

-12   0   4 3527.94 87.4675  25

0  12   4 3497.12 84.9049  26

4  12   0 3661.94 81.9675  26

0  -4  12 3740.91 85.6250  25

0   4  12 3490.28 84.4564  25

4   0 -12 3604.63 88.9724  12

-4  12   0 3605.62 85.9421  13

0  12   4 3622.19 84.7393  13

0  -4 -12 3647.44 86.0195  12

0   4 -12 3679.21 86.7407  12

0  12  -4 3693.06 83.3895  24

-4  12   0 3579.86 83.3717  23

0   4 -12 3622.32 75.7090  23

0  12  -4 3621.71 85.9910  23

0   4 -12 3562.71 81.4210  22

0  12  -4 3647.09 83.4503  22

4  12   0 3655.35 80.8832  23

-4  12   0 3696.19 87.3043  22

4  12   0 3728.28 89.6397  19

0  12  -4 3776.52 85.8216  20

-12   4   0 3771.72 87.8957  21

0  12   4 3585.18 87.8748  19

-12   0   4 3527.96 81.9288  21

0  12  -4 3709.95 80.8495  19

-12   0   4 3488.91 83.0591  14

12   4   0 3484.15 84.2849  18

4  12   0 3616.47 85.9596  18

0  12  -4 3522.30 74.5372  15

0  12  -4 3538.59 83.7145  16

-4   0 -12 3556.50 79.8240  15

-12  -4   2 12.5617 4.39334  10

-2  -4 -12 21.8495 6.15397   8

-4   2 -12 9.52145 6.23980   8

-4  12  -2 9.23436 4.76956   9

-12   4   2 13.8598 4.02827   9

-12   2  -4 9.60633 5.14173  10

-12  -4  -2 13.5504 4.94851  10

-12  -2  -4 14.0921 5.32886  10

-4  -2 -12 21.1946 6.35739   8

-2  -4 -12 13.0853 6.51359   7

-4   2 -12 21.9040 6.66300   7

-12  -4  -2 15.3399 5.83143   6

-12   4  -2 13.5023 5.33717   6

-12  -2  -4 9.49713 5.08339   6

-12   2  -4 13.3513 5.86203   6

-4  12  -2 10.9825 5.46819  30

2  12   4 10.2618 4.34824  29

4  12   2 14.6159 4.19937  29

-4  12   2 11.6747 5.56519  29

4  12  -2 19.3413 5.57512  30

2  12   4 19.2275 5.75407  28

-2  12  -4 9.42098 4.87322  30

2  12  -4 13.0147 5.33157  30

4  12   2 9.05483 4.52885  30

2  12  -4 13.0856 4.86302  28

-2  12   4 13.6961 5.17937  29

4  12  -2 4.31473 4.51392  28

4  12   2 10.5561 4.81903  28

2  12   4 12.3988 5.07713  30

-4  12   2 10.6187 5.03735  30

-2  12   4 14.1138 5.15006  30

-2  -4  12 9.20310 5.36224  25

-2   4  12 9.32322 5.34932  25

2   4 -12 19.3985 5.33916  27

-4  -2  12 23.3366 6.41408  25

-4   2  12 16.8919 6.25154  25

-2   4 -12 6.77950 3.39401  27

-12  -2   4 9.04363 4.94971  25

4  12   2 8.06413 4.00970  26

-12   2   4 11.3883 5.59792  25

-2  12   4 11.2718 4.86141  26

4  12  -2 18.0855 4.67080  26

-4  12   2 11.1722 5.07865  26

4  -2 -12 17.6395 6.34924  12

4   2 -12 11.8886 5.84345  12

2  12   4 16.4979 5.08975  13

-12   2  -4 10.5686 5.19562  14

-12   2   4 17.0330 5.71122  14

-12   4   2 7.54733 4.72134  14

-12  -2   4 15.1406 4.91735  14

-12   4  -2 8.21251 4.87017  14

-4  12  -2 12.7201 5.50577  13

-2  12   4 16.4503 5.93492  13

-12  -4   2 11.2225 4.24586  14

2  -4 -12 9.45860 5.42686  12

2   4 -12 19.6527 6.06132  12

-2  12  -4 14.6038 5.46990  23

-2   4 -12 11.5737 5.13409  22

-4  12  -2 14.0211 5.00804  23

-2  12  -4 13.6264 5.54828  24

-4  12   2 15.0703 4.91152  23

-4  12  -2 12.6596 5.18636  24

-12   2  -4 12.3709 3.91780  22

2   4 -12 16.1969 3.90154  22

4  12  -2 14.7004 5.10209  23

2  12  -4 19.7591 6.15101  23

-4  12  -2 19.5576 6.03203  22

4  12  -2 9.28891 5.40448  19

2  12  -4 4.74507 4.15701  19

-12   4  -2 14.8392 3.78174  22

-2  12  -4 9.67285 5.28348  20

-4  12  -2 12.8154 5.42774  20

-2  12  -4 12.0724 5.03064  22

-12   4   2 12.8604 5.08386  21

-12   2   4 12.9156 5.25933  21

2  12  -4 10.5015 4.92527  20

-2  12   4 14.0493 5.49253  19

2  12  -4 13.0669 4.60245  22

12   4  -2 7.60877 4.96188  18

-4   2 -12 17.0650 5.28279  15

2  12  -4 8.61006 4.60953  16

-4  -2 -12 11.7434 3.51875  15

12   4   2 12.2019 5.06946  18

-2  12  -4 16.8530 4.04015  15

4  12  -2 12.4812 5.48054  16

-2   4 -12 6.77877 4.33265  15

2  12  -4 8.74398 3.46042  18

4  12  -2 15.7046 5.37595  18

-4   4 -12 854.054 33.7957   8

-4  -4 -12 867.681 34.7955   7

-4  -4 -12 820.786 32.9048   8

-12  -4   4 901.149 30.2305  10

-12  -4  -4 886.168 31.9521  10

-12   4  -4 907.665 35.3937  10

-12  -4  -4 876.731 33.5216   6

-12   4  -4 875.893 33.9292   6

4  12  -4 781.195 31.9312  30

-4   4  12 905.907 28.6821  29

4  12   4 898.058 29.2975  29

-4  12  -4 824.413 31.4213  30

4  12   4 861.433 30.0968  30

4  12  -4 845.785 32.4144  28

4  12   4 842.570 31.6817  28

-4   4  12 876.278 33.1201  25

-4  12  -4 882.259 33.1075  24

4  12   4 873.930 31.7087  26

-4  12   4 835.438 31.6791  26

-4  -4  12 926.651 33.6611  25

4  -4 -12 884.745 33.7034  12

4   4 -12 890.229 34.0003  12

-4  12   4 836.042 32.6621  13

4  12  -4 848.165 32.4280  23

-4   4 -12 806.219 32.2671  22

-4  12  -4 894.902 33.4256  23

-4  12   4 856.476 27.4476  23

-12   4  -4 847.966 27.8881  22

-4  12  -4 813.547 32.7444  22

4  12  -4 893.900 29.2898  20

-12   4   4 932.269 33.1610  21

-4  12  -4 913.496 34.3667  20

-4  12  -4 878.970 28.1051  21

4  12   4 823.889 35.0422  19

-12   4  -4 863.161 32.9359  21

4  12  -4 832.076 30.5761  18

-4  12  -4 810.968 28.0063  15

12   4   4 957.056 32.8148  18

-12   4  -4 915.003 32.6168  14

-4   4 -12 848.897 31.2246  15

-12  -4   4 887.023 29.0002  14

-6  12   0-1.08892 3.84652   9

0  -6 -12 4.31833 3.93861   8

-12   6   0-0.82288 3.09449   9

-12   6   0-2.49000 4.24874  10

-12   0  -6-2.51204 5.12316  10

-12   0  -6 2.64798 4.51830   6

-6   0 -12-3.51674 4.40829   7

0  -6 -12-1.14482 4.04398   7

-12  -6   0-2.06220 4.41103   6

-12   6   0 3.16600 4.19559   6

6  12   0 4.62029 4.21402  28

0  12  -6-1.16429 4.11277  30

6  12   0 0.92040 4.02596  30

0  12   6 2.17950 3.97570  29

-6  12   0-3.06696 4.27290  30

0  12   6-6.42891 4.58378  30

-12   0   6 1.26167 5.01590  25

0   6 -12 0.95986 3.81604  27

-6   0  12 3.70778 5.04120  25

0  12   6-1.05615 3.60428  26

6  12   0-0.77236 3.45104  26

0  -6  12 3.81033 4.16671  25

0   6  12 0.95736 4.36589  25

6   0 -12 1.32087 5.25126  12

-12   6   0 1.10048 3.88737  14

12   0  -6-1.40980 5.30164  12

0   6 -12 4.07378 4.15413  12

0  12   6 0.96355 3.93023  13

-6  12   0 5.38857 4.91473  13

0   6 -12 0.83601 3.04998  22

-12   0  -6 0.71743 3.20561  22

0  12  -6-0.87025 3.72290  24

0  12  -6 2.31123 4.71363  23

-6  12   0 1.11227 4.53682  24

-12   6   0 0.62824 2.97736  24

-6  12   0 1.00672 3.31060  23

6  12   0-0.78125 3.02310  23

0   6 -12-0.70372 3.14438  23

0  12  -6 0.91111 3.80808  22

-12   0   6-0.76481 3.41734  21

-6  12   0 2.26646 4.95688  22

0  12  -6-1.12671 4.35990  20

-12   6   0-1.18324 4.94547  21

0  12  -6-0.67399 3.01151  19

0  12  -6-0.62560 2.90944  15

12   6   0-2.40346 4.38422  18

-6   0 -12 3.61579 3.02252  15

6  12   0-1.24727 4.69040  18

-12   6   2 193.860 12.8186   9

-6  12  -2 182.683 14.2222   9

-12   6  -2 177.007 14.8186  10

-12   2  -6 202.766 16.0596  10

-12  -6  -2 180.814 11.8447  10

-12   6   2 214.222 16.3781  10

-12  -2  -6 164.753 14.1649  10

-2  -6 -12 176.332 15.0451   7

-6  -2 -12 168.678 15.0750   8

-6   2 -12 190.671 15.5915   8

-12   6  -2 167.337 12.1090   9

-6  -2 -12 198.391 15.7815   7

-6  12   2 197.298 14.6350   9

-6   2 -12 171.944 13.8829   7

-2  -6 -12 169.987 13.0645   8

-12  -6   2 184.630 14.0770   6

-12   6   2 169.741 13.9328   6

-12  -6  -2 196.640 14.1156   6

-12   6  -2 178.740 14.0238   6

-12  -2  -6 185.029 15.5035   6

-12   2  -6 160.090 14.9387   6

-2  12  -6 196.338 14.8565  30

6  12  -2 153.283 12.9255  30

2  12   6 226.918 15.0369  29

2   6 -12 176.090 13.8840  27

-6  12   2 180.954 14.1654  30

-2  12   6 174.854 14.4609  29

-6  12  -2 184.736 13.7726  30

6  12   2 186.822 14.6120  28

-2  12   6 176.239 14.5171  30

6  12   2 206.565 13.2939  30

2  12   6 202.480 14.0496  30

2  12  -6 179.437 13.3612  28

-12  -2   6 168.228 14.7830  25

-2  -6  12 152.726 12.7612  25

6  12   2 190.264 13.1272  26

-6   2  12 198.922 15.6682  25

-6  -2  12 179.097 14.8901  25

-2  12  -6 199.463 14.1004  24

-2  12   6 196.909 14.2272  26

6  12  -2 176.822 11.0718  26

-12   2   6 213.503 16.0386  25

-2   6  12 173.518 13.4718  25

2  12   6 179.835 14.1510  26

2  -6  12 185.005 13.5110  25

2   6  12 182.865 13.4105  25

6  -2 -12 182.852 15.5819  12

6   2 -12 180.611 15.5528  12

-12  -6   2 160.982 11.7690  14

-6  12  -2 199.646 14.1558  13

-2  12   6 168.068 13.3017  13

-6  12   2 207.536 15.4531  13

12   2  -6 209.469 17.0969  12

12  -2  -6 170.326 15.8062  12

2  12   6 159.390 12.3973  13

2  -6 -12 186.448 13.8420  12

2   6 -12 172.536 14.0195  12

-6  12   2 181.872 14.5423  22

-2  12  -6 186.901 14.6010  23

2  12  -6 195.597 15.3300  23

-2   6 -12 181.404 11.3135  23

-12   6  -2 168.108 11.3065  22

2  12  -6 178.098 12.1330  22

2   6 -12 201.265 12.8649  23

-2  12  -6 185.798 14.5660  22

-12  -2  -6 172.331 11.0553  22

-6  12  -2 220.882 15.1513  23

-2   6 -12 202.737 14.4107  22

-6  12   2 192.931 13.4779  23

-12   2  -6 188.027 12.3809  22

2  12  -6 189.033 14.0940  20

6  12   2 196.775 16.6533  19

-6  12  -2 195.659 13.9829  21

-2  12  -6 193.729 15.6194  20

-12   6   2 207.793 15.7804  21

-12   2   6 176.870 12.5921  21

-12   6  -2 167.957 14.5992  21

2  12   6 173.518 15.5861  19

6  12  -2 189.604 15.9309  19

2  12  -6 189.007 13.2620  19

-12   6  -2 186.824 14.1725  14

12   6  -2 170.378 11.7450  16

6  12  -2 192.442 15.5200  16

6  12  -2 173.788 14.9197  18

6  12   2 190.501 15.7315  18

12   6   2 175.535 14.3722  18

-2  12  -6 173.340 11.7262  15

2  12  -6 181.267 10.2072  15

-6   2 -12 200.315 13.4194  15

2  12  -6 157.998 11.1536  18

12   6  -2 185.451 15.8052  18

-2   6 -12 178.317 13.8475  15

-12  -4   6 12.2759 4.66614  10

-6   4 -12 7.42841 5.29894   8

-12   6  -4 13.9086 6.10453  10

-12   4  -6 11.5635 5.56099   8

-6  -4 -12 15.9325 6.29446   8

-12   4  -6 11.9523 6.63631  10

-4  -6 -12 8.91724 5.18644   8

-12  -4  -6 8.84009 5.33551  10

-12  -6  -4 13.2687 4.66543  10

-12  -4  -6 12.3425 5.74239   6

-12   4  -6 17.8118 6.14240   6

-4  -6 -12 9.37080 6.10704   7

-6  -4 -12 16.7400 6.85368   7

-12  -6  -4 13.9130 5.43727   6

-12   6  -4 12.1392 5.60649   6

-6  12   4 12.7972 6.17836  29

4  12  -6 5.06665 4.43544  28

-12   6   4 7.85957 3.73415  30

4  12   6 3.78664 4.40561  28

-4  12   6 7.42853 5.53443  30

6  12   4 8.54561 3.95421  29

-4   6  12 10.1619 4.76911  29

-4  12  -6 16.6712 5.78293  30

-6  12  -4 5.72252 4.52301  30

6  12  -4 12.5526 5.30957  28

6  12   4 10.0360 3.92376  30

6  12   4 7.69161 4.59547  28

4  12   6 11.0867 4.47130  30

-6  12   4 4.75574 5.31491  30

-6  -4  12 11.8181 6.28723  25

-4   6  12 3.14685 4.28166  25

6  12  -4 12.7602 4.84810  27

4   6 -12 4.58989 5.54035  27

-12   4   6 12.2104 5.34349  25

-12  -4   6 14.2116 6.57240  25

6  12   4 2.05136 3.86057  26

-6   4  12 10.8294 5.91224  25

-4  -6  12 7.20932 5.06114  25

4  12  -6 13.7520 5.79126  27

-4  12   6 5.15581 4.41430  26

12   4  -6 15.8282 7.51468  12

6  -4 -12 12.3445 6.16899  12

12  -4  -6 11.8033 6.44359  12

6   4 -12 14.0361 6.37651  12

-12   4  -6 8.02790 5.18000  14

-12   6  -4 10.8833 4.86228  14

12   6  -4 7.98675 5.30874  12

-4  12   6 10.4519 4.97078  13

-6  12   4 16.8698 6.59618  13

12  -6  -4 6.74367 5.80122  12

4  -6 -12 9.44561 4.88364  12

4   6 -12 17.8118 6.17828  12

-6  12  -4 7.25189 5.62336  24

-4   6 -12 5.93560 3.01862  23

-6  12  -4 17.5893 6.05226  23

-6   4 -12 3.85034 5.36679  22

-12   6  -4 7.73000 4.43439  22

-12   4  -6 7.20873 4.27360  22

4  12  -6 11.0576 5.82504  23

-4  12  -6 10.3611 5.84843  24

-4   6 -12 8.39328 5.24729  22

-6  12   4 7.27420 4.60654  23

-12   6   4 2.36466 4.94438  21

-4  12  -6 8.41666 5.26189  22

4  12  -6 4.91679 4.48741  20

12   6   4 13.0585 4.70030  19

4  12   6 11.2557 6.41832  19

-6  12  -4 7.43986 5.30710  22

-6  12  -4 5.03005 3.90225  21

-4   6 -12 7.12137 5.16880  20

-6   4 -12 16.7127 4.64207  20

-6  12  -4 11.5439 6.40970  20

-4  12  -6 16.7058 6.52782  20

-12   4   6 8.97277 5.22613  21

-12   6  -4 12.5618 5.70720  21

6  12   4 2.82640 4.99469  19

12   6  -4 21.1493 7.27638  18

12   6  -4 7.66781 3.63762  16

6  12  -4 13.2212 6.60679  16

-4   6 -12 11.2552 5.13536  15

4  12  -6 10.5230 5.30984  18

-4  12  -6 7.15503 4.54474  15

6  12  -4 2.39671 5.01132  18

12   6   4 12.8607 6.03440  18

-6   4 -12 5.13680 4.68795  15

-12  -6  -6 80.9645 9.35005  10

-6   6 -12 90.6494 10.9966   8

-6  -6 -12 102.951 12.0792   8

-12   6  -6 107.002 12.2453  10

-12  -6  -6 93.7378 10.9730   6

-6  -6 -12 81.2972 11.7876   7

-12   6  -6 104.038 11.3495   6

-6  12  -6 99.6099 10.4699  30

6  12  -6 91.4894 10.6066  28

-6   6  12 90.7563 9.40203  29

-6  12   6 117.712 13.3327  29

6  12   6 121.527 11.0102  28

-6  12   6 92.9663 11.6522  30

-6  12  -6 104.997 12.0199  24

6  12  -6 86.7021 10.3452  27

-6   6  12 97.6888 11.1018  25

6  12   6 95.3710 11.0189  26

-6  -6  12 61.4959 9.48201  25

6  -6 -12 96.0997 11.3548  12

6   6 -12 105.553 12.0439  12

-12   6  -6 64.0372 8.37635  14

-6  12   6 101.657 11.7600  13

12   6  -6 86.8885 11.2878  12

12  -6  -6 88.0987 11.0975  12

-6   6 -12 87.3468 11.6114  22

-12   6  -6 92.1714 10.1903  22

-12   6  -6 92.2216 10.9161  21

-6   6 -12 92.2184 9.95637  20

-6  12  -6 88.0971 11.8011  22

-12   6   6 112.477 11.6063  21

6  12   6 99.6364 12.8042  19

6  12  -6 110.625 13.1254  16

6  12  -6 82.9622 10.4145  18

-6   6 -12 78.2441 10.2342  15

-6  12  -6 72.2416 9.39941  15

-8  12   0 647.959 29.6702   9

-8   0 -12 686.377 30.1161   7

-12   8   0 706.763 28.2103   9

-12   8   0 701.889 30.5264  10

-12   0  -8 683.239 31.9972   8

-12   0  -8 755.760 32.9934  10

0  -8 -12 712.489 29.2134   7

-12  -8   0 733.252 26.8848   6

-12   8   0 661.023 26.0339   6

-12   0  -8 697.374 32.3995   6

-8  12   0 688.525 27.3487  30

0  12   8 673.486 29.7021  29

0  12   8 641.385 28.2985  30

8  12   0 673.979 29.9418  28

0  -8  12 681.841 25.5803  25

0   8  12 714.163 26.1650  25

0   8 -12 655.532 28.7636  27

-8   0  12 723.405 32.2025  25

-12   8   0 684.193 25.0010  24

0   8  12 696.859 26.0002  26

0  12   8 705.545 29.0085  26

8  12   0 689.162 24.1786  26

0  12  -8 681.730 25.8121  24

-12   0   8 709.637 32.1776  25

8   0 -12 689.819 32.4630  12

-8  12   0 739.073 29.8819  13

12   0  -8 679.021 33.0280  12

-12   8   0 681.423 25.9744  13

0  12   8 697.648 27.0741  13

-8  12   0 673.260 28.9838  24

0  12  -8 695.599 27.1787  22

0   8 -12 679.036 26.3339  23

-12   0  -8 650.586 26.3130  22

-12   8   0 684.032 24.2959  22

-8  12   0 692.366 29.0902  23

-8  12   0 642.548 28.7629  22

0   8 -12 611.497 25.1163  22

-8  12   0 662.934 29.9876  21

0  12  -8 738.129 31.4283  20

8  12   0 699.353 32.9150  19

-8   0 -12 666.592 24.1509  15

12   8   0 668.555 31.6173  18

8  12   0 684.357 32.2509  18

0  12  -8 655.470 24.6462  15

0   8 -12 716.469 29.7265  15

-12   8  -2 32.5086 6.86007   9

-8  -2 -12 37.0613 9.09247   8

-12   8   2 18.5831 6.13550   9

-12   2  -8 49.8685 8.98070   8

-8  12   2 45.5186 8.80575   9

-8  12  -2 29.0191 7.12228   9

-2  -8 -12 38.8626 6.94111   8

-12   8   2 48.5110 9.36134  10

-12   8  -2 30.3555 7.53805  10

-8   2 -12 50.6460 9.11114   8

-12  -2  -8 29.3554 7.81863  10

-12  -2  -8 30.9146 7.71621   6

-12   2  -8 57.3849 9.72478   6

-8  -2 -12 34.7736 8.14816   7

-2  -8 -12 42.6738 8.77934   7

-8   2 -12 40.4919 8.25552   7

-12  -8   2 35.9912 6.60470   6

-12   8   2 35.2707 6.90692   6

-12  -8  -2 40.1213 7.00955   6

-12   8  -2 30.7475 6.42068   6

-2  12   8 34.6244 7.67592  30

2   8  12 26.4132 6.10286  30

8  12   2 41.9285 8.05756  28

-2   8  12 39.1840 8.20112  29

2  12   8 34.7942 7.60825  29

-8  12  -2 34.2052 6.79992  30

2  12   8 37.1342 7.23577  30

-8  12   2 31.3632 7.40892  30

-8  -2  12 49.3662 9.44757  25

-2   8  12 29.4814 6.30946  25

-2  -8  12 41.9800 7.21177  25

-12   2   8 41.2731 9.15722  25

-2   8  12 46.0697 6.08780  26

2  12   8 32.1484 7.05364  26

-8   2  12 48.6795 9.33302  25

-12  -2   8 35.4510 8.08461  25

8  12   2 41.3166 6.59922  26

-2  12   8 38.3667 7.17128  26

2   8 -12 38.0379 7.77972  27

2  -8  12 37.8565 6.82566  25

2   8  12 39.8283 6.85569  25

8   2 -12 43.6570 9.21763  12

12  -8  -2 34.0059 6.76066  12

-12  -8   2 39.2429 6.40277  14

-8  12   2 35.1067 7.83329  13

2  12   8 30.7242 6.13921  13

2  -8 -12 41.6013 6.95524  12

-8  12  -2 33.1924 7.13453  13

2   8 -12 33.7894 6.58933  12

-2  12   8 31.8446 7.20817  13

-12   8  -2 30.2133 5.41115  13

12   2  -8 27.0023 8.45828  12

12  -2  -8 32.6849 8.37727  12

-2   8  12 25.9390 5.65089  13

8  -2 -12 39.7910 9.09535  12

12   8  -2 25.6927 6.58345  12

-2  12  -8 27.3398 7.54536  23

-2   8 -12 42.1856 6.73872  23

-8  12   2 37.5670 7.39983  23

-12  -2  -8 36.4659 6.93287  22

-2  12  -8 42.1442 7.86969  24

-8  12  -2 37.8557 8.05675  24

-8  12  -2 37.2737 8.15788  23

-12   8  -2 37.8398 7.34886  24

-2   8 -12 37.4650 7.52613  22

2   8 -12 43.1557 7.46374  23

-12   2  -8 34.3080 7.09784  22

-2  12  -8 28.3560 7.91147  20

8  12   2 43.5452 9.89630  19

-2  12  -8 22.4486 7.12117  22

2  12  -8 49.4038 8.89283  20

12   8   2 39.4757 8.40466  19

-12   8   2 37.2011 8.33195  21

-8  12   2 31.5538 7.36775  22

2  12  -8 36.4382 6.13738  22

-12   8  -2 40.3797 6.90547  22

-8  12  -2 38.4100 8.25173  22

-8  12  -2 29.2823 7.21863  21

-12   8  -2 37.8166 8.62718  21

2  12  -8 29.3474 6.10347  19

12   8   2 51.2623 8.95796  18

12   8  -2 41.5073 9.19215  18

12   8  -2 32.8138 6.99527  16

8  12  -2 44.1161 9.20006  18

2   8 -12 38.8153 7.46015  15

-2  12  -8 29.0850 6.34541  15

2  12  -8 37.3696 5.92159  15

8  12  -2 36.3356 8.07395  16

-8   2 -12 34.2161 6.80207  15

-12   8  -4 2368.93 63.8352  10

-12   4  -8 2332.99 67.1894  10

-4  -8 -12 2297.78 65.6161   7

-4 -12  -8 2271.36 58.9203   7

-8  12   4 2162.35 55.7236  10

-8   4 -12 2235.87 57.6131   7

-12   4  -8 2334.10 61.7601   8

-8  -4 -12 2206.88 67.1837   8

-4  -8 -12 2265.88 59.7921   8

-8   4 -12 2284.61 64.8395   8

-12  -8   4 2187.89 58.7574   6

-12   8   4 2213.52 58.9358   6

-12  -8  -4 2178.96 57.2475   6

-12   8  -4 2165.99 57.8477   6

-12  -4  -8 2295.55 65.4700   6

-12   4  -8 2333.70 66.1834   6

-8  12   4 2375.51 63.6298  30

-4  12   8 2171.68 64.5908  29

4  12   8 2192.50 56.5252  30

8  12  -4 2242.27 63.0569  28

8  12   4 2260.21 62.4208  28

-12   8   4 2301.76 55.8184  30

-4  12   8 2311.39 65.4881  30

-4   8  12 2360.45 62.2968  29

-8  12  -4 2186.21 55.9745  30

4  12  -8 2218.77 56.9737  28

8  12   4 2236.10 59.8932  26

-8  -4  12 2279.57 64.2784  25

-8   4  12 2134.19 63.2872  25

-4  -8  12 2193.36 56.9224  25

4  12   8 2387.66 64.1675  26

-12   4   8 2148.03 63.9248  25

-4  12   8 2192.94 59.2498  26

-12  -4   8 2208.37 64.0642  25

4  12  -8 2164.13 62.7478  27

4  -8  12 2378.29 58.5827  25

4   8  12 2193.64 57.0246  25

8  12  -4 2267.81 56.3167  27

-4   8  12 2187.06 57.6791  25

-4  12  -8 2266.53 63.0440  24

8  -4 -12 2258.43 65.4499  12

8   4 -12 2217.73 65.8121  12

-8  12  -4 2228.34 57.0374  13

12  -4  -8 2253.20 66.1775  12

12   4  -8 2118.53 65.1710  12

-4  12   8 2245.17 62.8390  13

12   8  -4 2228.14 58.9821  12

12  -8  -4 2108.13 57.1260  12

-4   8  12 2276.14 58.0975  13

4  -8 -12 2342.49 58.4735  12

4   8 -12 2258.68 58.9486  12

-12   8  -4 2372.27 60.5935  22

-4  12  -8 2290.63 64.7532  22

4  12  -8 2373.54 66.4206  23

-4  12  -8 2262.15 63.7114  23

-4   8 -12 2226.49 56.1510  23

-12   4  -8 2243.95 60.8853  22

-4   8 -12 2262.95 63.9799  22

-8  12  -4 2158.51 63.1701  23

-8  12  -4 2201.31 64.1009  22

12   8   4 2242.70 61.0279  19

-4   8 -12 2367.36 64.1679  20

-4  12  -8 2273.73 66.6558  20

-8  12  -4 2209.88 58.7992  21

-12   8   4 2229.52 64.6751  21

-12   4   8 2336.82 58.5520  21

8  12   4 2216.10 67.2088  19

-12   8  -4 2287.04 62.9695  21

4  12   8 2299.67 67.7864  19

-4  12  -8 2218.16 60.0204  15

8  12  -4 2140.33 65.3461  18

12   8  -4 2188.93 68.0630  18

12   8   4 2351.88 66.5532  18

-8   4 -12 2267.92 60.9114  15

4  12  -8 2096.81 57.7507  18

-12   4  -8 2196.14 58.2712  14

12   8  -4 2228.67 59.0687  16

8  12  -4 2307.42 66.0412  16

-8   6 -12 14.7326 6.21467   8

-8  -6 -12 18.7525 7.68197   8

-6  -8 -12 19.7706 6.96706   8

-12   6  -8 18.2288 5.25108   8

-12   8  -6 16.7060 5.87464  10

-12   6  -8 28.0277 8.17565  10

-12  -8  -6 26.3424 5.81320   6

-12   8  -6 23.2556 6.44645   6

-12  -6  -8 31.8392 7.38436   6

-12   6  -8 29.3614 7.32784   6

-8  -6 -12 28.7108 9.54808   7

-6  -8 -12 26.7441 8.25266   7

-12   8   6 22.3140 6.12808  30

6  12  -8 19.9907 5.38593  28

6  12   8 25.5814 5.89195  28

8  12   6 14.8370 5.22064  28

8  12  -6 18.0035 6.42159  28

-6   8  12 15.8252 5.70675  29

-6  12   8 18.0327 6.58612  29

-8  12   6 15.3871 6.73021  30

8  12  -6 14.1111 5.37534  27

6  12  -8 15.7131 6.05145  27

-12   6   8 23.0765 6.84039  25

8  12   6 27.4749 7.40031  26

-12  -6   8 23.2028 6.78713  25

-6   8  12 24.6538 6.48428  25

-6  -8  12 19.8881 5.60642  25

-8   6  12 19.0467 6.43581  25

-8  -6  12 20.8898 6.87151  25

8  -6 -12 25.4946 6.92652  12

8   6 -12 24.1034 7.14376  12

-12   6  -8 30.5161 5.89859  14

12   6  -8 27.8581 8.17641  12

12  -6  -8 25.7081 6.89451  12

12   8  -6 20.1665 6.04388  12

12  -8  -6 27.0343 6.31827  12

-6  12   8 22.1261 7.13377  13

-8  12   6 20.4510 7.97242  13

6  -8 -12 33.2623 6.72602  12

6   8 -12 23.1078 6.16003  12

-8   6 -12 21.4478 7.50230  22

-6  12  -8 18.4992 6.85380  23

-6  12  -8 38.4457 8.29911  24

-8  12  -6 21.7671 7.55820  24

-8  12  -6 16.3614 6.30003  23

-6   8 -12 20.7942 7.16361  22

-12   6  -8 22.3855 6.72271  22

-6   8 -12 27.6565 5.42597  23

-12   8  -6 23.4948 6.76019  21

-6   8 -12 20.3465 7.15395  20

12   8   6 22.2407 6.24921  19

-8   6 -12 21.0158 5.58031  20

8  12   6 28.8258 8.21914  19

6  12   8 26.3382 7.90555  19

-12   8  -6 30.8191 7.58972  22

-12   8   6 16.3247 6.69032  21

-12   6   8 33.9548 7.15827  21

-8  12  -6 19.4115 5.11145  21

-6  12  -8 30.5369 7.71109  22

8  12  -6 26.8477 7.84958  16

8  12  -6 26.8222 7.73572  18

-6  12  -8 14.9804 6.23074  15

6  12  -8 28.8192 7.59839  18

12   8  -6 21.0861 8.37821  18

-8   6 -12 22.7707 6.92478  15

-6   8 -12 35.7078 7.72577  15

-12   8  -8 485.803 24.1025  10

-8  -8 -12 443.986 24.3611   8

-8  -8 -12 474.716 27.5061   7

-12  -8  -8 467.085 21.4473   6

-12   8  -8 470.060 22.1523   6

8   8 -12 488.731 25.8452  27

12   8  -8 474.667 21.1132  28

12   8   8 517.995 21.1344  28

-8  12   8 481.429 25.5430  30

8  12  -8 448.200 21.3514  28

8  12   8 479.062 20.6968  28

-8   8  12 481.164 21.9253  29

-12   8   8 524.705 23.6821  30

-8  12  -8 492.228 26.1089  24

-8   8  12 467.922 22.0813  25

8  12  -8 486.206 24.0471  27

8  12   8 514.900 26.0767  26

-8  -8  12 437.415 21.0675  25

8  -8 -12 491.141 22.3729  12

8   8 -12 452.382 22.5325  12

12  -8  -8 482.034 21.9137  12

12   8  -8 434.951 21.8808  12

-8  12   8 487.267 26.3858  13

-12   8  -8 470.694 24.7119  22

-8  12  -8 511.988 25.0168  23

-8   8 -12 405.436 17.8585  23

-8  12  -8 477.338 26.2043  22

-8   8 -12 518.125 27.4632  22

8  12   8 512.004 26.4393  19

-8   8 -12 436.588 21.4802  20

-8  12   8 525.302 26.3011  21

-12   8   8 471.779 23.5048  21

-8  12  -8 450.018 23.9851  15

12   8  -8 512.011 28.9141  18

8  12  -8 446.373 25.0828  18

-8   8 -12 442.827 24.4572  15

-12  10   0-1.20316 5.02876   9

-10   0 -12 3.09593 5.98997   8

-12  10   0 2.29658 5.23659  10

-12   0 -10-7.64583 6.23730   8

-10  12   0 1.33726 4.72379   9

-12   0 -10-1.54626 5.46205   6

-10   0 -12 2.57398 4.83980   7

-10   0 -12 1.54698 5.27930   6

0  10  12 1.09510 4.79010  30

10  12   0 1.35306 5.37925  28

-10  12   0 1.68629 3.60695  30

0  12  10-1.17112 4.89484  30

-12   0  10 1.48601 4.88675  25

0  10  12-1.89674 4.57703  26

0  12  10 1.10486 4.15489  26

-10   0  12-1.46108 5.49446  25

10   0 -12 3.18156 5.80360  12

12   0 -10 1.61314 6.24217  12

0  12  10-0.85022 3.71896  13

-10  12   0 3.35108 4.44086  13

-12  10   0-1.94513 4.06494  13

0  12 -10 1.55987 3.48492  24

-10   0 -12-2.73062 5.97204  22

-12   0 -10 1.13049 4.49437  22

-12  10   0 0.92145 3.85130  24

-10  12   0 9.87110 5.95500  23

0  10 -12-3.27820 4.56720  23

0  12 -10 1.30792 4.62012  23

-12  10   0-0.88564 3.87389  22

10  12   0 1.59757 6.18192  19

0  10 -12 4.43275 4.12304  22

-10  12   0 3.42503 5.30954  22

0  12 -10 2.85869 3.91098  20

0  12 -10-0.93126 3.79850  22

-10  12   0 2.71397 4.95065  21

-12  10   0-1.39767 5.40838  21

12  10   0 1.47961 5.72548  19

0  10 -12 3.42882 4.66192  15

12  10   0 1.59250 4.81728  18

0  12 -10-0.94539 3.75850  15

-12  10   2 92.9937 11.0639   9

-10  12  -2 85.9182 11.2572   9

-12   2 -10 93.4627 11.8273   8

-10  -2 -12 92.1840 13.0317   8

-12  10   2 67.2435 10.0879  10

-10  12   2 83.4210 9.08067  10

-10  12   2 88.8689 11.5545   9

-12  10  -2 71.5849 9.95852  10

-10   2 -12 76.7663 10.9983   8

-10  -2 -12 59.8483 11.0825   7

-12  -2 -10 86.8041 11.8395   6

-12   2 -10 102.256 13.2190   6

-12   2 -10 83.6729 10.0360   7

-10   2 -12 70.1271 9.75933   7

-2 -10 -12 90.3202 10.5368   7

2  10  12 84.9054 9.54976  30

-2  10  12 106.636 12.2740  30

10  12   2 85.5149 11.4837  28

-2  12  10 106.364 12.0438  30

-2  10  12 100.881 12.3376  29

-2  12  10 84.0296 11.4774  29

-10  12   2 66.4168 9.03594  30

2  12  10 74.9388 9.71992  30

2  12  10 87.8449 11.3589  29

12  10   2 77.7104 7.97894  26

-12   2  10 65.8679 11.0319  25

-12  -2  10 94.2739 12.3604  25

2  10 -12 101.520 11.9380  27

2  12  10 100.627 11.1423  26

10  12   2 81.4464 8.64504  26

2  10  12 94.4534 10.5196  26

-2  10  12 80.0175 8.72069  26

-2  12  10 79.1749 9.45319  26

-10   2  12 103.997 12.7943  25

-10  -2  12 91.2290 11.8698  25

10  -2 -12 96.8724 13.1684  12

12  -2 -10 84.4222 12.9220  12

12   2 -10 96.7364 12.9446  12

-10  12  -2 77.5135 9.19587  13

-12  10  -2 82.6428 8.59613  13

-2  12  10 77.7001 9.73365  13

-2  10  12 81.9202 8.74563  13

-10  12   2 87.5883 11.3529  13

-12  10   2 71.1680 9.78298  13

10   2 -12 102.563 12.9607  12

2  10 -12 92.0621 11.3914  23

-2  12 -10 80.5230 10.7489  23

-2  10 -12 71.7018 9.55595  23

-12  -2 -10 86.0641 10.5019  22

-2  10 -12 84.4582 9.50072  24

-12  10  -2 92.7795 10.8929  24

-10  12  -2 82.1067 10.7692  24

-2  12 -10 69.0357 9.16568  24

-10   2 -12 84.4378 11.6506  22

-12  10  -2 86.5479 10.2094  22

-2  10 -12 61.5676 9.15071  22

-12   2 -10 88.1436 11.1290  22

2  12 -10 81.5819 11.3314  23

-10  12  -2 106.256 11.9463  23

12  10   2 107.735 12.6591  19

-2  12 -10 87.5818 10.4324  22

2  12 -10 103.664 12.4441  20

-2  10 -12 85.6354 11.5959  20

10  12   2 85.6986 11.8164  19

-10  12  -2 88.8056 11.2388  21

-2  12 -10 110.569 12.8856  20

-12  10   2 80.1392 11.6263  21

-12  10  -2 93.3763 11.7278  21

10  12  -2 98.0518 13.1999  19

-10  12  -2 84.4031 11.0356  22

12  10  -2 121.667 14.3116  18

12  10  -2 105.866 11.8496  16

10  12  -2 102.507 12.5573  16

-10   2 -12 82.5507 9.14133  15

-2  12 -10 95.1471 10.4690  15

2  10 -12 73.8935 9.68907  15

12  10   2 82.1035 12.3967  18

10  12   2 94.7924 13.5008  18

-2  10 -12 88.4030 10.9830  15

2  12 -10 76.1249 9.02465  15

-12  10   4 2.59801 5.29884  10

-12  -4 -10 1.64368 5.99687   8

-10  12   4 2.73034 4.98087   9

-10  -4 -12-1.61635 6.91498   8

-10  12   4 4.74448 4.32770  10

-12  10   4 1.22627 4.74552   9

-12   4 -10 1.19871 4.50821   8

-12  10  -4 4.08539 4.26926  10

-12   4 -10 2.90946 5.62950  10

-10   4 -12-1.30068 4.74561   8

-10  -4 -12 3.16718 6.45956   7

-12  -4 -10 8.33292 5.80504   6

-12   4 -10 1.42812 5.67795   6

-4 -10 -12 7.62300 5.67716   7

-4 -12 -10 4.16932 5.20740   7

-4  12  10 2.78080 4.91184  30

10  12  -4 10.0694 5.62430  28

12  10  -4 1.23443 4.90798  28

12  10   4 4.84055 5.05826  28

-4  10  12 4.03853 6.01528  30

10  12   4 2.44173 4.01527  28

-4  10  12-1.26853 4.90905  29

-4  12  10-1.38932 4.90804  29

-10  12   4 1.09019 5.07045  30

-12  10   4 9.28759 4.49071  30

-12   4  10-1.38026 5.63026  25

10  12   4 3.81422 4.43506  26

-12  -4  10 4.06315 5.24123  25

4  12 -10 6.69075 5.59328  27

4  12  10 7.47777 4.95514  26

-4  12  10 1.82092 3.98292  26

-10   4  12 2.75025 5.32148  25

-10  -4  12 1.34888 5.63810  25

-4  10  12 3.82479 4.53204  13

10  -4 -12 2.83497 5.63569  12

-12   4 -10-1.60363 3.27106  14

12  -4 -10 7.22661 5.10583  12

12   4 -10 1.47585 4.85371  12

-4  12  10-1.12639 4.47848  13

-10  12   4 5.29248 5.53046  13

-12  10   4 5.00271 4.70361  13

10   4 -12-1.47168 6.00313  12

-4  12 -10 7.22561 4.66039  23

-4  10 -12 5.07448 4.90938  22

-4  10 -12 4.79602 4.19610  23

-4  12 -10 4.63115 4.60330  24

-12  10  -4 5.93317 5.30246  24

-10  12  -4 3.90368 4.74760  24

-12   4 -10 9.91941 5.65480  22

-12  10  -4 11.0830 6.25376  23

4  10 -12 1.25620 4.58334  23

4  12 -10 4.17516 5.95405  23

-10   4 -12 2.85710 5.97110  22

-4  12 -10 5.19149 4.88108  22

-12  10  -4 1.12118 4.79675  22

-10  12  -4 6.47450 5.41252  22

-4  10 -12 2.73387 5.28979  20

12  10   4 1.26296 4.88747  19

-10  12   4 4.34949 5.76427  21

-10  12  -4 4.24796 4.43911  21

-12  10   4 4.23108 5.89506  21

10  12   4 7.39764 4.86580  19

-12  10  -4 7.11587 5.62095  21

4  10 -12 4.96765 4.34623  15

12  10  -4 4.56736 4.77283  16

10  12  -4 5.40278 6.40155  16

-4  12 -10 10.2492 5.78335  15

-10   4 -12 2.11385 3.97506  15

4  12 -10 4.44427 4.29021  18

12  10  -4 11.3196 6.75908  18

10  12  -4 4.65147 6.16443  18

-4  10 -12 1.26711 4.76539  15

4  12 -10 5.16399 3.36475  15

-10   6 -12 112.340 11.7353   8

-10  -6 -12 97.2974 13.3094   8

-12  10  -6 121.120 11.0358  10

-12  -6 -10 127.323 14.3365   8

-12   6 -10 107.839 10.9079   8

-10  -6 -12 118.260 14.3923   7

-6 -10 -12 102.575 12.9416   7

-12  -6 -10 119.502 12.4489   6

-12   6 -10 123.168 12.9967   6

-6 -12 -10 107.619 11.7103   7

-6  10  12 112.289 13.2951  30

12  10  -6 139.065 12.3176  28

12  10   6 103.489 10.8922  28

-6  10  12 109.517 12.2105  29

10  12   6 120.595 11.8148  28

-10  12   6 108.585 11.7922  30

-12  10   6 140.598 11.7741  30

-6  12  10 142.925 14.5143  30

12  10  -6 100.806 9.83808  27

10  12  -6 118.516 12.1753  28

-6  12  10 133.720 13.6463  29

-12  10  -6 132.101 13.4136  24

6  10 -12 130.877 13.4643  27

6  12 -10 125.522 13.0868  27

10  12  -6 93.9052 10.2215  27

10  12   6 112.691 11.3129  26

6  12  10 118.156 12.8602  26

-10   6  12 135.639 13.2715  25

-10  -6  12 117.861 12.3294  25

-10  12  -6 133.612 14.0192  24

-12  -6  10 127.749 12.6057  25

-12   6  10 105.283 11.6194  25

10  -6 -12 131.818 13.3067  12

10   6 -12 112.173 12.6638  12

12   6 -10 91.9138 11.8182  12

12  -6 -10 75.0087 10.7141  12

-6  12  10 107.014 12.4555  13

-6  10  12 129.901 12.5203  13

-12  10   6 144.248 13.8769  13

-12   6 -10 110.625 12.4936  22

-6  12 -10 122.391 14.0999  22

-6  10 -12 109.910 13.1192  22

-6  10 -12 78.5363 9.29353  23

-6  12 -10 117.914 11.8482  23

-6  12 -10 93.5979 11.9258  24

-10  12  -6 135.304 13.5009  23

-10   6 -12 129.619 13.5279  22

-12  10  -6 125.789 12.5296  23

6  10 -12 106.325 12.2295  23

-12  10  -6 129.985 13.1456  22

-10  12  -6 96.6222 12.4665  22

-6  12 -10 127.993 13.8739  20

12  10   6 114.098 11.9699  19

10  12   6 104.556 12.5493  19

-12  10   6 128.629 13.4030  21

-10  12  -6 115.688 10.4050  21

-12  10  -6 122.630 11.8310  21

-6  10 -12 102.263 11.9930  20

-10  12   6 102.401 13.0793  21

-6  12 -10 101.577 11.3752  15

6  10 -12 103.658 10.4112  15

6  12 -10 103.810 11.5165  18

10  12  -6 117.449 14.0586  18

-10   6 -12 130.640 12.6813  15

-12 -10  -8 10.0340 5.72401   8

-12  -8 -10 20.9555 6.62452   8

-10  -8 -12 15.6761 7.25079   8

-8 -10 -12 10.7199 4.70847   8

-8 -12 -10 20.2833 6.62303   7

-10  -8 -12 18.4478 8.17873   7

-8 -10 -12 8.37656 5.97650   7

10  12   8 8.82731 4.14620  28

-12  10   8 15.3425 5.75493  30

-8  12  10 5.34042 5.45019  30

12  10  -8 12.8569 4.94916  28

-12   8  10 15.0930 5.65275  30

12  10   8 15.8792 4.91632  28

10  12  -8 13.2433 5.09761  28

-10  12   8 11.9579 5.87741  30

-8  10  12 14.4956 5.67039  29

8  12 -10 10.7470 5.45001  27

10   8 -12 10.0933 5.52306  27

8  10 -12 23.0567 6.71493  27

-10   8  12 16.7440 5.43702  25

-10  -8  12 13.2337 5.21949  25

10  12   8 16.6280 6.50339  26

10  12  -8 9.08293 4.96177  27

12  10  -8 9.79240 4.97762  27

10  -8 -12 8.07806 4.33740  12

10   8 -12 11.7257 5.35182  12

12   8 -10 14.5303 6.06103  12

12  -8 -10 12.4020 4.71633  12

-8  12  10 11.4242 5.90741  13

-10  12   8 10.8325 6.42098  13

-8  10  12 6.96091 5.70248  13

-12   8 -10 11.3565 6.41157  22

-8  10 -12 12.4127 6.41791  22

-8  12 -10 14.4999 6.13430  24

-8  12 -10 14.6374 5.13995  23

-8  10 -12 15.2206 4.91302  23

-10  12  -8 11.1683 5.39454  23

-12  10  -8 10.3402 5.77943  24

-8  12 -10 13.8096 6.78631  22

-12  10  -8 18.5135 6.37173  22

10  12   8 11.8598 6.02663  19

-10  12  -8 17.3696 6.67834  22

-8  12  10 12.6937 5.76898  21

-8  10  12 12.7163 4.83370  21

-10  12   8 16.4468 6.63225  21

-8  10 -12 16.0130 6.31388  20

-12  10   8 15.0436 6.06704  21

-12   8  10 3.51782 4.17375  21

-8  12 -10 14.6862 6.01512  15

8  10 -12 3.91019 5.82799  18

8  12 -10 11.1956 6.21817  18

8  10 -12 14.9756 4.88211  15

-10   8 -12 12.2185 6.20865  15

10  12  -8 15.7544 6.91569  18

-8  10 -12 11.4327 6.75930  15

-12 -10 -10 18.5307 5.97454   8

-10 -10 -12 21.1758 5.96360   8

-10 -12 -10 18.5822 6.70773   7

-10 -10 -12 30.2970 7.88541   7

-12  10  10 15.8994 5.52314  30

-10  10  12 8.10599 5.49823  30

-10  12  10 18.1949 6.05704  30

12  10 -10 14.7399 5.31285  27

10  10 -12 22.5052 6.41806  27

10  12 -10 21.1485 5.74588  27

10  12  10 14.6233 5.53507  26

-10  12  10 21.5736 6.19280  13

-10  10  12 19.1167 5.98975  13

-12  10  10 27.8970 7.51046  13

-10  12 -10 26.9487 7.16158  24

-10  12 -10 27.2751 6.12061  23

-12  10 -10 28.0887 7.70476  22

-10  12  10 12.0498 5.50528  21

-12  10  10 13.9897 5.24005  21

-10  10 -12 13.9071 6.08131  15

10  12 -10 20.9272 6.55533  18

10  10 -12 19.2106 7.48689  18

12  10 -10 22.3954 7.77267  18

-12   0 -12 1489.20 47.8881   7

-12  12   0 1488.31 48.7514   9

-12  12   0 1426.57 41.9698  10

-12   0 -12 1572.90 53.4516   8

-12   0 -12 1380.50 51.4244   6

0  12  12 1411.94 48.6910  29

12  12   0 1558.94 50.2999  28

0  12  12 1456.01 45.9530  30

0  12  12 1474.88 44.5516  26

-12   0  12 1494.76 51.3232  25

12   0 -12 1541.33 53.7956  12

-12  12   0 1453.28 44.1782  13

-12  12   0 1379.53 43.4538  22

0  12 -12 1470.53 41.7650  22

0  12 -12 1504.50 47.6426  23

-12   0 -12 1477.14 47.7099  22

0  12 -12 1570.49 51.7948  20

-12  12   0 1485.53 49.7093  21

12  12   0 1484.73 52.0662  19

12  12   0 1513.89 49.5549  16

12  12   0 1572.15 54.2304  18

0  12 -12 1498.06 45.0575  15

-12  12   2 55.6263 9.09218   9

-12  12   2 29.8004 6.67385  10

-12   2 -12 45.3762 9.61923   8

-12  -2 -12 64.4687 10.7049   6

-12   2 -12 36.7249 9.69684   6

-12   2 -12 38.8933 7.67604   7

-12  -2 -12 33.5613 8.86647   7

-2  12  12 47.6146 9.17175  30

2  12  12 44.9214 7.58991  30

-2  12  12 47.5436 9.30007  29

12  12   2 39.4640 8.43021  28

-12   2  12 40.7164 8.92690  25

-12  -2  12 57.4062 9.73489  25

2  12  12 50.2192 8.24332  26

-2  12  12 41.0518 7.27132  26

-12   2 -12 35.5103 6.62408  14

12   2 -12 50.3246 10.5656  12

-12  12  -2 39.3929 7.00500  13

-12  12   2 34.3377 7.91531  13

12  -2 -12 47.9910 10.3052  12

-2  12 -12 28.6900 6.15214  24

-2  12 -12 57.2317 8.77530  23

-12  -2 -12 31.5496 7.57127  22

-12  12  -2 48.7873 8.49257  24

-12   2 -12 34.5427 8.28317  22

2  12 -12 46.3657 9.52195  23

12  12  -2 36.1497 9.42849  19

-12  12  -2 42.9519 8.28457  22

2  12 -12 38.3118 9.27108  20

12  12   2 26.5083 7.97984  19

-2  12 -12 39.6113 7.93110  22

-12  12  -2 42.7116 9.19510  21

12  12  -2 43.0581 8.44055  16

12  12  -2 41.5673 9.13540  18

-2  12 -12 45.2839 8.45976  15

2  12 -12 44.2157 7.54997  15

-4 -12 -12 349.483 19.6172   7

-12  12   4 310.605 18.4435  10

-12  -4 -12 406.982 24.5338   7

-12  -4 -12 432.835 26.0528   8

-12  12   4 423.608 23.1287   9

-12   4 -12 421.722 22.7494   8

12  12  -4 395.419 21.8102  28

12  12   4 404.015 21.7852  28

-4  12  12 360.916 22.1429  29

-12  12   4 359.154 18.2356  30

-4  12  12 432.414 23.7025  30

12  12   4 389.671 17.8438  26

4  12  12 366.723 20.8178  26

-12   4  12 350.839 22.0165  25

-12  -4  12 403.136 22.8237  25

-12  12  -4 355.395 20.9520  24

-4  12 -12 336.752 19.1602  24

12   4 -12 360.990 23.1981  12

-4  12  12 358.600 19.0188  13

-12  12   4 367.091 21.4769  13

12  -4 -12 370.966 23.1775  12

4  12 -12 403.942 22.7537  23

-4  12 -12 389.756 20.4646  23

-12  12  -4 340.887 20.4912  22

-4  12 -12 364.053 21.0454  22

-12   4 -12 422.775 23.1023  22

-4  12 -12 415.562 24.1687  20

12  12   4 364.778 22.2677  19

-12  12   4 428.870 24.2597  21

-12  12  -4 352.000 19.9969  21

-4  12 -12 418.611 22.0573  15

4  12 -12 370.222 17.7243  15

12  12  -4 339.827 20.5778  16

-12  12   6 28.0096 7.04449   9

-12   6 -12 38.1864 6.78351   8

-12  -6 -12 27.5537 7.73037   8

-12  12   6 30.0834 6.92510  10

-6 -12 -12 24.7423 6.81799   7

-6  12  12 31.7256 8.28232  30

12  12  -6 44.7221 7.72436  28

12  12   6 35.5042 6.92924  28

-12  12   6 31.5321 6.59459  30

-6  12  12 23.9878 7.10894  29

6  12 -12 26.3141 7.85276  27

-12  -6  12 37.2911 7.57079  25

12  12   6 30.2351 6.14602  26

6  12  12 26.6365 6.70115  26

-12   6  12 28.1923 7.36400  25

12  -6 -12 25.9860 6.93264  12

12   6 -12 29.3983 7.60216  12

-6  12  12 24.4638 6.72471  13

-12  12   6 36.4994 8.45190  13

-12   6 -12 40.0888 8.25628  22

-6  12 -12 44.6493 7.21661  23

-6  12 -12 26.6266 7.10271  24

-12  12  -6 31.2512 7.76968  24

-12  12  -6 27.1525 7.24222  23

6  12 -12 23.7610 7.14250  23

-12  12  -6 22.4658 5.54993  21

-12  12  -6 17.3342 6.51853  22

-6  12 -12 50.3611 9.27296  22

-6  12  12 22.2363 6.25731  21

12  12   6 30.3250 7.11663  19

-6  12 -12 40.2352 8.97212  20

-12  12   6 26.9953 7.24662  21

-6  12 -12 28.0568 7.40582  15

6  12 -12 25.2639 5.78456  18

12  12  -6 33.8727 8.82382  18

6  12 -12 28.5547 5.17089  15

-12 -12  -8 963.084 32.1444   8

-12  -8 -12 1045.22 37.8092   8

-12  -8 -12 1077.80 40.0954   7

-8 -12 -12 1084.92 36.2994   7

-12  12   8 894.384 32.6235  10

-12  12   8 990.546 35.7454   9

-12  12   8 1025.37 33.4086  30

12  12  -8 919.293 30.2674  28

-12   8  12 1035.59 35.0004  30

12   8 -12 989.674 35.5363  27

12  12  -8 960.930 30.9676  27

-8  12 -12 1036.97 36.1655  24

12  12   8 1074.37 34.4235  26

8  12  12 1037.30 36.0460  26

8  12 -12 975.877 35.8218  27

-12  12  -8 987.545 36.2006  24

12   8 -12 963.045 31.8608  12

-8  12  12 1003.58 34.9491  13

-12   8 -12 1116.38 38.0307  22

8  12 -12 1039.84 36.8897  23

-8  12 -12 1001.14 37.2435  22

-8  12 -12 958.292 30.7598  23

-12  12  -8 934.849 35.3306  22

-8  12  12 985.342 32.1053  21

-12  12   8 1021.82 35.8020  21

12  12   8 1017.11 32.9038  19

12  12  -8 1035.44 39.0814  18

8  12 -12 931.980 33.2950  18

-8  12 -12 1028.63 36.2647  15

12   8 -12 950.689 38.5053  18

-12  12  10 13.7415 4.87686   9

-12  12  10 8.01798 4.01135  10

-12 -10 -12 14.2265 5.06759   8

-12 -12 -10 6.09158 4.54160   7

-12 -10 -12 14.4632 6.00713   7

-10 -12 -12 5.69986 4.25024   7

-12  10  12 8.54514 4.34481  30

-12  12  10 15.9770 4.89245  30

-10  12  12 21.1385 6.07542  30

10  12 -12 13.2818 5.04809  27

12  12 -10 15.3140 4.75484  27

12  10 -12 15.7275 4.91735  27

12  12  10 9.29775 3.93696  26

-10  12  12 11.0641 4.76202  13

-12  12  10 21.0385 5.92571  13

-12  10  12 15.4669 5.22061  13

-12  10 -12 6.08333 4.62877  24

-10  12 -12 22.6516 5.96227  24

10  12 -12 17.7484 5.32486  23

-12  12 -10 9.69920 4.85020  22

-12  10 -12 13.9401 5.88960  22

10  12 -12 14.4006 4.15442  20

-10  12 -12 13.3752 5.14436  22

-12  12  10 12.2381 4.30593  21

12  10 -12 7.73908 4.94474  18

10  12 -12 9.18040 4.74155  18

12  12 -10 15.0375 5.88197  18

-12  12  12 176.188 10.8609  30

-12  12 -12 176.357 11.7448  24

12  12  12 166.631 10.5250  26

-12  12  12 159.132 11.1279  13

12  12 -12 160.544 11.1220  23

-12  12 -12 170.046 11.5375  22

12  12 -12 150.758 11.0058  18

-12 -12 -12 187.976 12.2286   7

-12  12  12 186.381 11.3800   9

1  13   1 1170.15 31.3092   9

-1  -1 -13 1209.06 41.9653   8

-1  13  -1 1215.32 34.5258   9

-1   1 -13 1121.74 41.3565   8

-13   1   1 1165.24 41.2444  10

-13  -1   1 1124.07 39.3952  10

-13  -1  -1 1136.19 39.9073  10

-13   1  -1 1230.76 42.1617  10

-1  13   1 1203.23 34.5471   9

-13  -1  -1 1167.96 41.9971   6

1  13  -1 1122.98 39.5413  30

1   1 -13 1142.87 32.6760  27

1  13   1 1161.33 34.7933  29

-1  13   1 1171.09 40.1684  30

-1  13   1 1212.33 37.3401  29

1  13   1 1127.20 39.1092  30

1  13   1 1188.87 40.2319  28

-1  -1  13 1166.70 40.3329  25

1  13   1 1175.61 38.9659  26

1  13  -1 1189.72 38.1316  26

-13  -1  -1 1209.39 40.6563  14

-1  13   1 1174.01 40.1291  13

-1  -1 -13 1165.57 41.0312  12

1  -1 -13 1129.40 40.9718  12

1  13  -1 1159.43 37.2112  23

1  13   1 1184.38 35.0017  23

-1  13  -1 1174.44 37.7677  23

-1  13   1 1181.93 35.9094  23

-1  13  -1 1199.29 39.8795  22

1  13  -1 1223.09 35.5194  20

1  13   1 1154.91 39.9392  19

-1  13  -1 1174.74 36.6184  19

-1  13   1 1220.98 38.8226  19

-13   1   1 1219.74 40.3382  21

1  13  -1 1135.83 38.5585  19

-1  13  -1 1226.93 37.5114  20

1  13  -1 1189.85 38.3839  16

-1  13   1 1237.35 35.3915  16

-13   1   1 1207.10 40.1998  14

-13  -1   1 1217.58 40.0150  14

-13   1  -1 1181.34 40.6107  14

-1  13  -1 1156.69 35.3215  16

13   1  -1 1147.89 35.2703  18

-3  13   1 154.713 12.2184   9

-3   1 -13 162.181 14.3450   8

-13  -3  -1 177.564 13.9094  10

-1  -3 -13 165.427 13.9372   8

-3  13  -1 144.460 11.5283   9

-13   3   1 167.227 14.8442  10

-13  -1   3 139.370 13.0642  10

-13   3  -1 178.918 15.1547  10

-13  -3   1 166.073 13.1722  10

-13   1   3 142.368 13.6115  10

-13   1  -3 144.845 13.6726  10

-13  -1  -3 163.301 14.2348  10

-3   1 -13 183.987 14.9150   7

-1  -3 -13 157.162 14.7704   7

-3  -1 -13 155.516 14.2944   8

1  13   3 170.560 10.0772   9

-13  -3   1 173.048 15.0951   6

-13   3   1 150.397 14.0231   6

-13  -3  -1 145.083 13.7080   6

-13   3  -1 170.381 14.7694   6

-13  -1  -3 177.437 15.2012   6

3  13  -1 144.477 12.8660  30

1  13   3 171.751 13.9597  30

3  13   1 199.772 14.7375  30

1   3 -13 154.345 11.4501  27

1  13   3 157.366 12.2139  29

-1  13   3 179.220 13.6279  29

3  13   1 164.316 10.4555  29

1  13  -3 164.656 14.0085  30

3  13   1 159.048 13.5364  28

-3  13  -1 153.217 13.1945  30

-1  13   3 169.162 13.9180  30

-1  -3  13 150.130 13.3548  25

-1   3  13 147.419 13.2684  25

-3  -1  13 174.100 14.4978  25

-1   3 -13 162.183 10.7262  27

3  13   1 148.812 12.3019  26

-1  13   3 157.155 13.4781  26

3  13  -1 169.798 12.7158  26

1  -3  13 149.837 12.9294  25

1   3  13 175.893 14.0206  25

3  -1 -13 175.976 14.6827  12

-13  -3   1 169.279 13.3603  14

1  13   3 159.608 13.1343  13

-3  13  -1 148.395 13.4633  13

-1  13   3 142.194 12.7542  13

1  -3 -13 139.232 13.0278  12

1   3 -13 179.063 14.7287  12

-1  13  -3 161.941 13.0851  23

-3  13   1 158.209 13.8819  22

3  13  -1 176.259 12.8144  23

1  13  -3 188.841 13.8169  23

3  13   1 164.186 11.3302  23

-1   3 -13 152.506 12.4479  22

1   3 -13 135.083 10.7529  22

-3  13  -1 165.764 13.1284  23

-3  13   1 174.715 12.3931  23

-1  13   3 169.332 10.6217  23

-1  13  -3 170.470 13.5287  22

-3  13  -1 187.828 14.7082  22

1  13  -3 159.473 12.5159  22

-13   3  -1 150.855 13.7688  21

3  13  -1 168.490 14.3785  19

1  13  -3 152.382 12.5076  19

3  13   1 165.111 14.5534  19

-1  13  -3 175.476 13.4598  20

-1  13  -3 160.098 11.4427  19

1  13   3 151.976 13.7156  19

-13   3   1 167.757 14.2705  21

-13   1   3 172.648 13.3926  21

1  13  -3 163.327 12.6175  20

-1  13   3 182.988 14.5280  19

-3  13  -1 163.883 11.1307  19

-3  13   1 160.575 12.3207  19

3  13  -1 169.121 14.0219  16

-3   1 -13 164.305 12.2318  15

-3  -1 -13 161.323 11.1507  15

13   3   1 143.925 12.0989  18

13   3  -1 171.933 13.2004  18

-13   1   3 171.695 13.7034  14

3  13  -1 159.389 12.9389  18

1  13  -3 166.462 10.8397  18

-13   3   1 191.674 14.8113  14

-13  -1   3 154.259 12.6371  14

-1  13  -3 176.253 12.7315  16

1  13  -3 161.415 13.4368  16

-3   3 -13 917.378 36.8135   8

-13   3   3 919.488 37.4203  10

-13  -3   3 954.048 33.2926  10

-13  -3  -3 978.008 35.1614  10

-3  -3 -13 927.835 37.3316   7

-3  -3 -13 896.166 35.6493   8

-13  -3  -3 937.557 36.5672   6

-13   3  -3 884.742 35.9032   6

3  13   3 959.730 30.7532  29

3  13  -3 907.152 35.0673  30

3  13   3 937.382 33.5196  30

3  13  -3 999.144 36.1822  28

-3  13   3 891.852 34.6170  29

3  13   3 937.932 34.7110  28

-3  13  -3 921.197 34.9428  30

-3  -3  13 860.411 34.7889  25

-3   3  13 1046.15 37.3156  25

-3  13  -3 939.452 34.9830  24

-3  13   3 942.409 35.1553  26

3  13   3 920.612 33.9406  26

3  -3 -13 945.188 36.5086  12

3   3 -13 910.800 36.1586  12

-3  13   3 894.234 35.1448  13

-3  13  -3 881.831 34.5070  22

-3  13  -3 958.232 35.3458  23

3  13  -3 925.625 33.9822  23

-3   3 -13 917.820 34.4492  22

-3  13   3 919.509 29.6078  23

3  13  -3 992.476 31.3215  20

3  13   3 930.775 37.4175  19

-13   3   3 941.219 34.7996  21

-3  13  -3 995.185 35.9642  20

3  13  -3 880.699 34.3567  19

-3   3 -13 975.710 33.8807  15

-3  -3 -13 939.877 27.7864  15

13   3  -3 907.637 34.3580  18

-13  -3   3 980.995 33.0494  14

3  13  -3 880.687 31.2044  18

-13   3  -3 911.751 34.6909  14

13   3   3 1106.90 34.8629  18

-13   3   3 889.263 34.5778  14

3  13  -3 959.873 36.0810  16

-5  13   1 214.993 15.5930   9

-1  -5 -13 216.584 16.7481   7

-13  -5   1 217.883 13.8360  10

-13   5   1 214.581 12.5463   9

-5  13  -1 210.965 15.0585   9

-1  -5 -13 213.857 15.1632   8

-13   5  -1 208.518 12.7205   9

-13  -5  -1 228.543 14.4934  10

-13   1  -5 217.130 16.9297  10

-13  -1  -5 195.710 16.1169  10

-5   1 -13 255.282 17.5871   7

-5  -1 -13 206.728 16.4069   7

-13   5  -1 241.042 17.9560  10

-5  -1 -13 185.884 16.4527   8

-13  -5   1 236.458 16.8147   6

-13   5   1 215.438 16.7041   6

-13  -5  -1 215.697 16.0043   6

-13   5  -1 217.893 16.3391   6

-13  -1  -5 251.320 18.2946   6

-5  13  -1 198.585 15.1415  30

-1  13  -5 222.072 17.0265  30

5  13  -1 244.069 16.3130  30

5  13   1 217.390 14.8425  30

-1  13   5 209.728 15.5243  29

-1  13   5 225.045 16.7003  30

5  13   1 198.574 15.7481  28

1  13   5 216.681 15.0852  29

-5  13   1 208.996 15.7551  30

1  13   5 206.563 15.3796  30

-1  -5  13 194.043 14.8723  25

-1   5  13 243.493 16.6798  25

-5  -1  13 209.734 16.7923  25

1   5 -13 205.880 14.0878  27

1  13   5 199.781 15.2121  26

5  13   1 255.329 15.4934  26

-1  13   5 203.625 15.5131  26

5  13  -1 228.349 13.9213  26

-1   5 -13 208.794 13.6108  27

-13  -1   5 176.516 15.4278  25

-13   5  -1 202.342 11.8321  24

1  -5  13 239.428 15.9654  25

1   5  13 192.597 14.6898  25

-1  13   5 224.012 15.7824  13

5  -1 -13 199.552 16.8899  12

-13  -5   1 210.245 14.5413  14

1  13   5 220.445 15.3567  13

-5  13  -1 220.307 15.7341  13

-5  13   1 203.279 15.7405  13

13  -1  -5 231.152 18.5361  12

1  -5 -13 201.971 15.4610  12

1   5 -13 213.686 16.2344  12

-1  13  -5 219.434 15.1761  24

5  13  -1 202.971 13.6902  23

1   5 -13 207.094 11.9282  23

5  13   1 217.247 12.8094  23

1  13  -5 190.983 15.6432  23

-1  13  -5 225.812 16.3189  23

-1  13  -5 214.458 15.1854  22

-1   5 -13 198.249 14.1955  22

-5  13  -1 224.495 15.5476  23

1   5 -13 206.121 12.9082  22

-5  13   1 191.606 13.9833  23

1  13  -5 216.201 14.3055  22

-13   1  -5 187.309 11.3156  22

-5  13  -1 211.969 16.5841  22

1  13  -5 209.001 14.0022  19

1  13  -5 232.806 15.7904  20

-1  13  -5 252.616 17.4151  20

-13   5   1 208.496 16.1843  21

-13   1   5 185.632 13.5344  21

1  13   5 215.425 17.2234  19

-1  13   5 226.663 17.1094  19

5  13  -1 218.654 17.2122  19

5  13  -1 218.590 16.6942  16

-1   5 -13 240.680 16.4558  15

-13   5  -1 177.705 14.6148  14

13   5  -1 203.382 15.6123  18

5  13  -1 225.447 16.3215  18

5  13   1 215.741 16.7596  18

-1  13  -5 203.021 11.3903  15

13   5   1 222.265 15.6906  18

-13  -1   5 211.875 14.4467  14

-5  -1 -13 209.387 12.7034  15

-5   1 -13 218.324 13.9157  15

-13   5   3 898.130 29.0560   9

-5   3 -13 886.993 36.1747   8

-13  -3   5 879.719 32.3678  10

-13  -5  -3 947.848 32.5495  10

-13  -5   3 934.529 30.5186  10

-13   5  -3 912.550 36.7775  10

-13  -3  -5 959.470 35.5387  10

-3  -5 -13 895.953 36.7277   7

-5  -3 -13 880.073 36.4846   8

-3  -5 -13 832.873 33.5261   8

-13  -5  -3 986.883 36.1742   6

-13   5  -3 928.406 35.8392   6

-13  -3  -5 881.324 36.0454   6

-13   3  -5 912.583 36.9585   6

-5  13   3 916.443 35.3559  30

3  13   5 889.521 31.6899  29

-3  13  -5 879.442 34.2751  30

5  13   3 893.280 28.1619  29

-5  13  -3 950.560 34.5976  30

5  13   3 895.255 31.5406  30

3  13   5 887.677 32.3946  30

-3  13   5 911.628 36.0446  29

-3  13   5 862.143 35.4104  30

-5  13   3 870.642 35.5196  29

5  13  -3 933.228 35.0901  30

5  13  -3 951.893 35.9563  28

5  13   3 898.594 34.8338  28

3   5 -13 936.201 34.0056  27

3  13  -5 936.240 34.5502  28

3  13   5 893.676 33.1887  28

-5  13  -3 918.909 35.7197  24

-3  -5  13 984.124 35.6603  25

-3   5  13 869.927 34.2103  25

-5  -3  13 934.305 36.0619  25

-5   3  13 961.739 36.7777  25

-3  13  -5 874.374 33.8798  24

5  13   3 871.472 32.4278  26

-3  13   5 880.694 34.0770  26

5  13  -3 830.846 27.6361  26

5  -3 -13 943.887 37.1476  12

5   3 -13 880.837 36.2738  12

-3  13   5 976.402 35.9756  13

-5  13   3 851.339 34.8798  13

13   3  -5 856.531 36.5073  12

13  -3  -5 923.716 38.1072  12

3  -5 -13 923.946 34.7397  12

3   5 -13 911.637 35.3414  12

3  13  -5 872.871 29.0979  22

-5  13  -3 892.340 35.5350  22

-13   5  -3 882.235 27.8890  22

5  13  -3 913.247 33.8740  23

-3  13  -5 921.795 35.3869  22

-5   3 -13 840.785 34.9115  22

-3  13  -5 841.602 34.3761  23

-5  13  -3 892.827 34.7795  23

-3   5 -13 902.280 34.5090  22

3  13  -5 844.408 34.4122  23

-5  13   3 907.060 30.4741  23

-13   3  -5 849.351 28.2847  22

3  13  -5 1007.87 33.3418  20

-5   3 -13 872.046 28.2032  20

-13   3   5 930.103 33.5684  21

5  13   3 863.512 37.4195  19

-5  13  -3 883.763 30.9429  21

-13   5   3 890.929 35.1706  21

-13   5  -3 884.594 35.0107  21

-3  13  -5 942.919 36.4949  20

5  13  -3 918.128 36.8636  19

3  13  -5 876.425 33.2249  19

-13  -3   5 897.089 30.5454  14

13   5  -3 845.733 35.3944  18

-13   5  -3 899.821 34.0598  14

3  13  -5 856.227 29.9867  18

5  13  -3 895.670 34.0332  18

-13   3  -5 920.633 34.7060  14

-3  13  -5 906.803 29.3424  15

-13  -5   3 882.034 30.4932  14

-5   3 -13 928.558 33.1011  15

3  13  -5 892.396 35.9095  16

-3   5 -13 971.419 35.2182  15

13   5   3 862.436 33.0383  18

-5   5 -13 911.104 36.9603   8

-5  -5 -13 955.197 39.5606   7

-13   5  -5 1040.22 39.9466  10

-13  -5  -5 980.520 34.8151  10

-13   5  -5 973.836 31.8915   8

-5  -5 -13 1008.69 38.5749   8

-13  -5  -5 978.561 37.2541   6

-13   5  -5 938.009 37.1921   6

5  13   5 991.320 32.7605  30

-5   5  13 968.680 31.3250  29

-5  13  -5 1005.19 35.6254  30

5  13   5 967.630 32.2251  29

5  13  -5 963.370 36.1677  28

5  13   5 1014.59 36.0132  28

-5  -5  13 1021.51 37.5234  25

-5   5  13 1008.86 37.4759  25

-5  13  -5 952.160 37.1339  24

5  13   5 976.058 35.7538  26

5  -5 -13 1031.71 37.8347  12

5   5 -13 996.593 38.0079  12

13   5  -5 963.358 37.8213  12

13  -5  -5 990.451 38.0789  12

-5  13   5 1034.27 38.5306  13

-13   5  -5 898.471 31.2298  22

5  13  -5 937.406 36.7738  23

-5  13  -5 954.458 37.5283  23

-5  13  -5 999.559 38.5431  22

-5   5 -13 976.389 38.0721  22

-5   5 -13 1005.61 33.1648  20

5  13  -5 1023.13 32.9000  20

5  13   5 917.713 39.5344  19

-5  13  -5 891.748 29.3925  21

-13   5   5 979.559 36.3440  21

5  13  -5 943.392 37.3456  19

-5  13  -5 1138.79 41.1202  20

13   5  -5 1014.38 40.4190  18

5  13  -5 952.069 34.9098  18

-5  13  -5 1027.27 33.6365  15

-13   5  -5 1001.61 35.3479  14

-5   5 -13 965.367 36.0332  15

-7  13   1 722.748 31.0173   9

-13   7   1 734.648 27.5338   9

-7  13  -1 729.108 31.1679   9

-1  -7 -13 684.364 26.9597   8

-13   7  -1 682.727 26.8634   9

-13   7   1 733.054 32.5738  10

-1  -7 -13 673.815 30.3884   7

-7  -1 -13 691.425 31.6028   7

-13   1  -7 696.549 32.7104  10

-13  -1  -7 754.500 33.0615  10

-13   7  -1 741.222 32.3597  10

-7  -1 -13 713.749 33.7449   8

-7   1 -13 628.680 31.2563   8

-7   1 -13 685.975 30.4631   7

-13   1  -7 640.960 30.6721   8

-13  -7   1 683.300 28.4283   6

-13   7   1 717.404 29.2046   6

-13  -7  -1 730.152 29.0310   6

-13   7  -1 736.016 29.2747   6

-13  -1  -7 733.208 33.3558   6

1  13   7 702.022 30.1113  29

-1  13   7 683.401 30.6162  29

-7  13  -1 712.140 28.8960  30

-7  13   1 743.788 30.4322  30

7  13   1 745.439 32.0183  28

1  13   7 714.075 29.4787  30

-1  13   7 704.609 30.6531  30

7  13   1 713.209 27.1550  30

1  -7  13 747.023 28.8505  25

1   7  13 757.787 28.9273  25

-1  -7  13 728.184 28.6218  25

-1   7  13 700.662 28.3154  25

1   7 -13 685.261 29.5500  27

-1  13  -7 731.058 28.4713  24

-7  -1  13 717.047 32.3157  25

1  13   7 683.236 29.7662  26

7  13   1 630.468 25.6006  26

-1  13   7 698.215 29.7558  26

-13   7  -1 669.655 24.7904  24

-13  -1   7 705.986 32.6066  25

7  13  -1 686.945 24.5919  26

7  -1 -13 663.779 32.1910  12

1  13   7 730.124 28.4188  13

-7  13  -1 683.840 29.5545  13

-1  13   7 706.866 29.3146  13

-7  13   1 773.533 31.8284  13

13  -1  -7 753.495 35.0843  12

-13   7  -1 716.961 24.8178  13

-7  13   1 766.061 31.6592  22

-7  13  -1 667.400 30.1887  24

7  13  -1 706.699 27.1686  23

1   7 -13 701.207 25.8552  23

-1   7 -13 690.747 24.5835  23

-1  13  -7 593.168 29.3645  23

-1  13  -7 707.900 29.0101  22

-13   7  -1 740.158 24.1898  22

-13  -1  -7 686.357 24.8851  22

1  13  -7 663.405 26.3963  22

-13   1  -7 662.397 25.3582  22

-7  13  -1 733.946 30.3715  23

-7  13   1 702.978 28.7524  23

-1   7 -13 731.450 28.2073  22

-7  13  -1 693.886 30.8345  22

1   7 -13 743.649 25.7329  22

1  13  -7 714.922 32.0651  23

1  13  -7 639.629 24.4170  19

7  13   1 713.814 33.8325  19

-13   7   1 683.308 31.2343  21

1  13  -7 722.899 31.0526  20

-1  13  -7 696.963 31.3632  20

-7  13  -1 689.977 29.6510  21

13   7  -1 675.236 26.1307  16

7  13  -1 716.216 32.4348  16

1   7 -13 732.596 30.6695  15

13   7  -1 642.497 31.0799  18

13   7   1 736.871 31.9269  18

7  13  -1 704.519 32.0367  18

7  13   1 738.063 33.5407  18

-1  13  -7 697.262 24.9339  15

1  13  -7 650.071 22.6058  15

-7   1 -13 670.817 25.8925  15

-3  -7 -13 108.357 11.1334   8

-13   7   3 101.093 10.2988   9

-7   3 -13 107.208 12.7474   8

-13   3  -7 77.6480 10.5395   8

-13   7   3 96.8637 12.6227  10

-13   7  -3 84.5914 11.4817  10

-7  -3 -13 76.8162 11.6170   8

-13  -3  -7 88.7824 11.1078  10

-7  13   3 117.622 12.5100   9

-3  -7 -13 96.9153 12.2290   7

-13   7   3 109.627 11.7202   6

-13  -7  -3 96.2362 10.6387   6

-13   7  -3 110.193 11.4070   6

-13  -3  -7 112.895 12.7883   6

-13   3  -7 132.348 14.1393   6

-13  -7   3 89.0511 10.4903   6

-7   3 -13 94.6958 10.9713   7

3  13   7 107.058 11.3150  29

7  13   3 110.142 11.8736  28

-3   7  13 92.0782 10.7289  29

-7  13  -3 85.1332 10.0129  30

3  13   7 79.5355 9.78579  30

-7  13   3 95.9408 11.5100  30

-3  13   7 108.741 12.3906  30

7  13   3 90.3996 9.23169  30

7  13  -3 110.476 12.1804  28

-3  -7  13 86.3616 10.3675  25

-3   7  13 94.2930 10.2972  25

3   7 -13 116.055 11.9303  27

-7  -3  13 86.2060 11.5826  25

-7   3  13 99.9518 12.2247  25

-13   3   7 106.437 12.4675  25

3  13   7 82.2565 10.5444  26

7  13   3 81.0129 9.84276  26

-13   7  -3 94.7144 10.1413  24

3  -7  13 97.9669 10.6917  25

-3  13   7 81.4122 10.4898  26

-13  -3   7 88.3762 11.7548  25

3   7  13 119.162 11.5539  25

7  -3 -13 65.0642 10.9246  12

7   3 -13 122.358 13.7179  12

13   7  -3 105.335 11.5344  12

-13   3  -7 79.7403 10.1258  14

-7  13  -3 86.2912 10.5236  13

3  -7 -13 84.8825 10.0892  12

3   7 -13 91.0133 10.9864  12

13   3  -7 101.681 13.2601  12

13  -3  -7 89.9697 12.8677  12

-3  13   7 116.078 11.9463  13

13  -7  -3 84.0080 11.0349  12

-3  13  -7 81.3680 10.2534  24

-3   7 -13 92.3502 11.0360  22

3   7 -13 96.1263 10.1050  23

-7   3 -13 109.066 12.6386  22

-7  13  -3 80.5853 10.9046  23

-13  -3  -7 96.7907 8.56472  22

-3   7 -13 92.3258 8.33657  23

-13   3  -7 94.0845 10.1389  22

-7  13   3 104.241 10.3668  23

3  13  -7 75.4563 11.0528  23

7  13  -3 71.9781 10.9861  19

-3   7 -13 119.128 12.5310  20

3  13  -7 123.126 12.4883  20

-3  13  -7 116.485 12.7600  20

3  13   7 109.268 13.4229  19

-13   3   7 91.6847 10.0104  21

-3  13  -7 84.1005 10.9505  22

-7  13  -3 93.4203 10.6132  21

7  13   3 99.6231 13.0441  19

-13   7  -3 79.0202 8.92469  22

-13   7   3 94.7386 11.7946  21

3  13  -7 97.7240 10.3097  19

-13   7  -3 88.8364 11.4494  21

13   7   3 116.044 11.2299  19

13   7  -3 70.7085 8.50900  16

13   7  -3 134.739 14.2903  18

13   7   3 113.731 12.4217  18

-3  13  -7 105.181 9.95148  15

7  13  -3 82.4416 11.4229  18

7  13  -3 92.5498 12.2987  16

-7   3 -13 111.498 11.0891  15

-3   7 -13 113.952 12.0969  15

3  13  -7 80.7548 8.82803  18

-7   5 -13 76.4026 11.1956   8

-7  -5 -13 106.903 13.1172   8

-13   5  -7 97.1548 10.3638   8

-13   7  -5 91.1111 11.9567  10

-13   5  -7 86.3606 12.3498  10

-5  -7 -13 96.2316 11.3033   8

-13  -7  -5 77.0505 9.92938   6

-13   7  -5 90.1727 10.9014   6

-13  -5  -7 95.8150 11.8007   6

-13   5  -7 104.525 12.4481   6

-7  -5 -13 96.6552 13.2640   7

-5  -7 -13 99.0243 12.7917   7

-13   7   5 75.5121 8.16631  30

5  13   7 111.925 11.4169  29

7  13   5 92.2766 8.90638  29

-5   7  13 113.879 11.0308  29

-7  13   5 116.872 13.0544  30

5  13   7 82.3986 9.58805  28

5  13   7 91.7939 9.15567  30

-7  13  -5 104.098 10.3473  30

7  13  -5 96.9454 11.8069  28

5  13  -7 91.4953 10.7234  28

-5  13   7 101.466 12.4695  29

7  13   5 83.1165 10.5987  28

-5  13  -7 112.775 12.5593  24

5   7 -13 101.352 11.7823  27

-5   7  13 77.8074 10.6912  25

-5  -7  13 94.7545 10.4664  25

-7   5  13 96.9816 11.8638  25

-7  -5  13 75.1809 11.3122  25

7  13   5 68.3460 9.61207  26

7  -5 -13 86.6162 11.5309  12

7   5 -13 81.9952 11.8680  12

-13   7  -5 76.5457 9.55865  14

-13   5  -7 89.2287 10.1566  14

-5  13   7 96.6226 12.0169  13

-7  13   5 82.8510 11.3997  13

13   5  -7 58.6476 10.6771  12

13  -5  -7 70.5113 11.3140  12

5  -7 -13 84.6092 10.2644  12

5   7 -13 73.3256 10.2580  12

13   7  -5 95.4920 11.4636  12

13  -7  -5 90.8353 10.9532  12

-5   7 -13 85.7420 11.5100  22

-7  13  -5 82.4565 11.0753  24

-7   5 -13 93.3499 12.1829  22

5  13  -7 83.3303 11.5319  23

-13   5  -7 113.065 11.0507  22

-7  13  -5 81.4485 8.88615  21

-7   5 -13 101.858 9.51544  20

-7  13  -5 110.145 12.6599  22

-5   7 -13 82.4583 10.1226  20

5  13   7 92.3159 12.4974  19

7  13   5 101.561 12.9632  19

5  13  -7 78.4445 9.72092  20

-13   7  -5 118.473 12.7218  21

-13   7  -5 78.0945 9.36171  22

-5  13  -7 121.085 13.4395  20

-5  13  -7 92.2956 11.8536  22

-13   7   5 96.9783 11.7487  21

-13   5   7 95.8465 10.8917  21

7  13  -5 88.7241 12.3358  16

-5  13  -7 84.5953 10.2251  15

13   7  -5 101.304 13.7142  18

7  13  -5 85.1580 11.3869  18

-7   5 -13 84.9186 10.7832  15

-5   7 -13 97.6117 11.5002  15

5  13  -7 114.216 11.5014  18

-7  -7 -13 536.818 29.4002   7

-13   7  -7 555.945 27.3049  10

-7  -7 -13 522.773 26.5031   8

-13  -7  -7 491.763 23.8314   6

-13   7  -7 523.913 25.0284   6

7  13   7 478.393 21.9364  29

-7   7  13 484.354 21.6282  29

-7  13   7 534.415 27.1854  30

-7  13   7 514.943 27.1786  29

-13   7   7 493.864 21.6125  30

7  13  -7 545.437 24.4421  28

7  13   7 556.788 23.8166  28

7  13  -7 531.373 24.6018  27

7  13   7 514.174 25.4502  26

-7   7  13 511.842 24.3868  25

-7  -7  13 480.438 23.4746  25

-7  13  -7 567.930 28.4055  24

7  -7 -13 540.086 24.9413  12

7   7 -13 523.058 25.2497  12

13  -7  -7 474.682 23.8008  12

13   7  -7 471.748 24.1325  12

-7  13   7 511.226 26.9471  13

-13   7  -7 519.629 24.3766  22

7  13  -7 520.400 27.0834  23

-7  13  -7 537.507 26.6918  23

-7   7 -13 521.855 27.6329  22

-7  13  -7 491.199 26.7356  22

7  13  -7 498.430 22.0487  20

-7   7 -13 516.710 22.6443  20

-13   7   7 496.308 24.5737  21

7  13   7 482.096 27.1950  19

7  13  -7 446.835 24.4716  18

-7  13  -7 507.674 24.4906  15

-7   7 -13 532.932 26.4813  15

-13   7  -7 445.920 20.4608  14

13   7  -7 578.293 30.5817  18

-9  13   1 780.457 33.3619   9

-13   1  -9 748.832 34.0363   8

-13   9   1 770.494 30.4766   9

-13   9  -1 716.550 31.5902  10

-9  13  -1 801.345 33.9742   9

-13   9  -1 810.979 31.2496   9

-13   9   1 823.575 34.0724  10

-13  -1  -9 749.828 35.2159   8

-9  -1 -13 762.559 33.8499   7

-13   1  -9 725.834 34.2330  10

-13  -1  -9 793.206 35.2675  10

-9   1 -13 750.644 31.7199   7

-9   1 -13 782.358 35.1129   8

-1  -9 -13 755.991 31.4223   7

-13   9   1 690.673 26.3201   6

-13   9  -1 709.876 26.5887   6

-13  -1  -9 808.260 36.0665   6

-1   9  13 778.965 32.9395  29

-9  13  -1 768.171 28.6152  30

9  13   1 733.571 32.7336  28

-9  13   1 758.186 29.9553  30

1  13   9 770.498 30.9727  30

-1  13   9 756.621 32.4972  30

1   9  13 750.297 28.7744  30

-1   9  13 803.089 31.5838  30

1  13   9 772.926 32.8680  29

1   9  13 759.286 26.5622  25

-1  13  -9 726.119 28.0603  24

1   9 -13 766.506 32.6105  27

-9  -1  13 696.180 33.2010  25

1   9  13 759.251 28.4943  26

-1   9  13 744.732 26.2597  26

1  13   9 797.216 32.0915  26

9  13   1 711.891 26.0075  26

-1  13   9 796.020 31.6857  26

-1   9  13 735.128 26.5971  25

-13  -1   9 729.020 33.8181  25

-13   9  -1 752.548 27.8881  24

9  -1 -13 733.773 34.9485  12

1  13   9 799.590 28.5394  13

-1  13   9 735.905 29.2962  13

13  -1  -9 784.085 36.2225  12

-9  13  -1 718.823 29.9602  13

-9  13   1 807.538 32.8355  13

-13   9  -1 784.615 27.0377  13

-13   9   1 783.014 29.7430  13

13   9  -1 719.111 27.3249  12

-9  13   1 768.843 31.9996  22

1   9 -13 746.185 29.0592  23

-1  13  -9 759.679 29.9879  22

-1  13  -9 737.814 32.8654  23

-1   9 -13 711.103 27.5836  23

-9   1 -13 711.384 33.2782  22

1  13  -9 767.111 27.5116  22

-13  -1  -9 749.454 28.5664  22

-13   1  -9 698.231 28.5175  22

-9  13  -1 760.003 32.3485  23

-13   9  -1 751.944 26.8461  22

-9  13   1 791.349 31.9121  23

-9  13  -1 773.054 33.0077  22

-1   9 -13 757.374 29.1745  22

9  13   1 792.350 36.4095  19

1  13  -9 808.137 34.0046  20

-1  13  -9 816.841 34.9564  20

-9  13   1 791.410 33.9512  21

-9  13  -1 835.492 33.5620  21

-13   9   1 698.164 33.0631  21

-13   9  -1 729.477 33.0865  21

13   9   1 751.932 32.9433  19

9  13  -1 760.865 36.2142  19

13   9  -1 711.448 29.3750  16

9  13  -1 744.837 33.9087  16

13   9  -1 779.004 35.6639  18

13   9   1 807.418 35.8809  18

9  13  -1 766.648 35.4890  18

9  13   1 834.584 36.8414  18

-9   1 -13 775.743 27.2091  15

-1  13  -9 753.707 27.8064  15

1  13  -9 768.558 26.6155  15

-1   9 -13 721.925 31.3328  15

1   9 -13 748.325 31.3791  15

-9  13   3 157.499 14.8402   9

-13   9   3 140.394 12.7067   9

-9   3 -13 115.971 11.5541   7

-3  -9 -13 136.101 13.8397   7

-13   9   3 146.528 14.8692  10

-13   9  -3 136.126 13.3021  10

-13   3  -9 162.969 16.0259  10

-13   3  -9 132.458 13.8886   8

-9  -3 -13 125.942 14.7460   8

-9   3 -13 136.243 14.2343   8

-9  -3 -13 122.262 14.4958   7

-13   3  -9 98.8375 12.9310   6

-13   9   3 91.2090 9.60621   6

-13   9  -3 112.039 10.2390   6

-13  -3  -9 158.305 15.2071   6

3  13   9 125.988 13.2089  29

-9  13  -3 120.109 10.5126  30

-3   9  13 129.811 12.9746  29

9  13  -3 159.007 14.7204  28

9  13   3 141.109 13.5925  28

3  13   9 127.115 11.4637  30

-9  13   3 130.857 12.5404  30

-3  13   9 135.723 14.2094  30

-3  13   9 121.838 13.3623  29

3   9  13 104.523 9.74684  25

-13  -3   9 119.223 13.5107  25

-3   9  13 112.835 10.4861  25

-9   3  13 126.592 13.6628  25

9  13   3 122.983 11.3240  26

3  13   9 137.241 13.4785  26

-13   9  -3 132.069 12.3468  24

-3  13   9 130.378 11.9186  26

-3  13  -9 125.057 12.2094  24

-13   3   9 125.173 13.5646  25

-9  -3  13 123.050 13.6179  25

-9  13  -3 123.768 13.2863  24

3   9 -13 154.614 14.4189  27

13   3  -9 141.455 14.6071  12

9   3 -13 113.673 13.9050  12

9  -3 -13 126.201 13.9206  12

-3  13   9 115.992 12.1916  13

-9  13   3 155.915 14.3293  13

-13   9   3 120.404 12.1738  13

13  -3  -9 133.156 14.5419  12

-9  13  -3 119.494 11.3834  13

13   9  -3 96.7199 10.1802  12

-3  13  -9 139.499 14.1721  23

-13   9  -3 106.698 10.4622  22

-13  -3  -9 137.707 11.2931  22

-3   9 -13 115.158 10.3810  23

3   9 -13 119.852 11.8824  23

-9  13  -3 137.312 13.3926  22

-9  13  -3 144.474 13.9698  23

-13   3  -9 124.233 12.2059  22

-3  13  -9 112.675 12.7190  22

-3   9 -13 139.265 13.3684  22

13   9   3 114.083 12.2990  19

3  13  -9 130.412 13.6091  20

-3   9 -13 123.154 13.7018  20

9  13   3 131.503 14.7615  19

-13   9   3 133.249 13.8005  21

-3  13  -9 138.776 14.6088  20

-13   9  -3 143.444 14.1465  21

-9  13  -3 101.207 11.2569  21

3  13  -9 116.069 10.7787  19

3   9 -13 132.803 12.4481  15

13   9  -3 101.069 11.0432  16

9  13  -3 111.512 13.6064  16

9  13  -3 131.582 14.5712  18

13   9   3 177.138 15.9705  18

-9   3 -13 114.656 11.0975  15

-3  13  -9 106.666 11.0961  15

3  13  -9 110.454 9.02265  15

13   9  -3 147.221 15.4671  18

-13   3  -9 141.143 12.3276  14

-9   5 -13 137.458 13.8991   8

-13   9  -5 181.875 14.8979  10

-13  -5  -9 137.008 16.2242   8

-5  -9 -13 179.403 16.0020   7

-13   9   5 153.380 15.4753  10

-13   5  -9 188.542 16.5885  10

-9  -5 -13 173.705 16.6390   8

-13   5  -9 150.008 13.0056   8

-5 -13  -9 157.636 12.7616   7

-9  13   5 164.461 15.1855   9

-5  -9 -13 161.583 12.9723   8

-13   9   5 184.517 14.3907   9

-13   9   5 147.405 12.1830   6

-13   9  -5 165.591 12.1852   6

-13  -5  -9 193.545 15.8744   6

-13   5  -9 180.416 15.6352   6

5  13   9 149.935 13.5411  29

-5  13   9 153.959 14.9473  29

-5   9  13 192.045 15.1307  29

-9  13   5 176.331 14.8845  30

13   9  -5 166.002 11.7157  27

-13   9   5 155.260 11.7209  30

9  13   5 174.641 14.7424  28

-5  13   9 192.986 16.2275  30

9  13  -5 167.060 14.2019  28

-13   9  -5 179.877 14.5817  24

-9   5  13 159.516 14.7375  25

-5   9  13 161.413 11.9516  25

9  13   5 142.748 12.5236  26

-9  -5  13 171.620 15.4036  25

-13   5   9 158.767 15.0473  25

-13  -5   9 184.797 15.2649  25

5  13   9 150.947 13.8451  26

-5  13  -9 206.786 16.2730  24

5   9  13 127.678 10.9519  25

9  -5 -13 152.974 15.0034  12

9   5 -13 181.781 16.2300  12

13  -5  -9 176.611 15.9011  12

13   9  -5 152.755 12.1292  12

-5   9  13 149.911 12.6909  13

-13   9   5 165.739 14.6669  13

-5  13   9 187.112 15.2956  13

5   9 -13 139.982 11.6833  12

13   5  -9 161.081 15.4575  12

-13   9  -5 156.140 13.2282  22

5   9 -13 191.254 15.0313  23

5  13  -9 161.544 15.5505  23

-9  13  -5 158.402 14.9261  22

-5   9 -13 170.604 11.8444  23

-5  13  -9 215.685 16.9505  22

-5  13  -9 196.760 16.0641  23

-13   5  -9 178.127 14.5145  22

-5   9 -13 171.862 15.1083  22

5  13  -9 219.184 16.1177  20

-5   9 -13 209.186 16.2367  20

-9  13   5 199.898 17.0220  21

-13   9   5 170.672 15.3975  21

-9  13  -5 159.890 12.3774  21

-13   5   9 154.217 12.4936  21

-13   9  -5 153.299 13.8017  21

13   9   5 183.183 13.6547  19

9  13   5 178.731 16.4755  19

5   9 -13 162.716 13.2974  15

5  13  -9 157.573 12.9199  18

-5  13  -9 159.974 13.5464  15

-9   5 -13 159.859 13.6856  15

-13   5  -9 181.918 12.5425  14

13   9  -5 161.824 16.6988  18

9  13  -5 151.638 15.3327  18

9  13  -5 167.811 15.7668  16

-7  -9 -13 406.134 24.7491   7

-13  -7  -9 459.394 26.1538   8

-13   9  -7 424.834 21.7246  10

-13   7  -9 417.190 23.1275  10

-9  -7 -13 429.172 24.6519   8

-9  -7 -13 433.872 26.0458   7

-7 -13  -9 410.172 21.1710   7

-7  -9 -13 450.609 22.4299   8

-13   9  -7 431.379 19.3932   6

-13  -7  -9 426.458 21.7698   6

-13   7  -9 406.196 21.6305   6

13   7  -9 433.061 18.5503  28

13   9  -7 444.704 21.1917  28

13   9   7 447.813 20.7639  28

7  13   9 409.396 21.0440  29

9  13   7 416.701 18.2379  29

9   7 -13 452.880 24.4326  27

-9  13   7 423.307 23.1622  30

-13   9   7 419.934 19.9444  30

-7  13   9 393.187 23.5653  29

-13   7   9 389.043 19.9776  30

9  13  -7 410.476 20.8592  28

-7   9  13 446.649 21.6468  29

9  13   7 430.561 20.8441  28

13   9  -7 435.867 20.6385  27

7  13  -9 436.226 19.1308  28

9  13  -7 419.655 20.7628  27

7  13  -9 411.221 22.2424  27

-9   7  13 367.343 20.8159  25

9  13   7 429.441 22.2659  26

7   9 -13 476.319 25.3201  27

-7   9  13 386.315 18.5989  25

-9  -7  13 421.679 21.5086  25

-7  13  -9 437.771 24.1212  24

-9  13  -7 454.858 25.0769  24

9  -7 -13 429.898 21.9558  12

9   7 -13 410.666 22.0964  12

13   9  -7 374.276 18.6458  12

13  -7  -9 395.865 21.2991  12

13   7  -9 434.999 22.3447  12

-7  13   9 447.748 24.1930  13

-9  13   7 457.246 25.3419  13

-7   9  13 434.550 21.7154  13

7   9 -13 409.346 19.1915  12

-13   7  -9 406.479 21.9974  22

-13   9  -7 412.679 21.9440  22

-7  13  -9 457.454 25.5238  22

-7  13  -9 420.844 22.6017  23

-9  13  -7 432.855 23.3315  23

7  13  -9 420.285 24.0968  23

-9   7 -13 421.577 24.5875  22

-7   9 -13 468.450 25.5063  22

7  13  -9 438.212 21.6850  20

-7  13  -9 464.123 25.2535  20

-13   9   7 394.080 22.0833  21

-13   7   9 489.173 21.7595  21

9  13   7 416.686 24.1881  19

-7   9 -13 450.392 22.2048  20

-9  13   7 428.965 24.4102  21

9  13  -7 394.590 23.4910  18

13   9  -7 441.362 26.5802  18

7  13  -9 421.958 22.2772  18

-7  13  -9 443.284 22.9288  15

13   7  -9 415.591 26.1596  18

-9   7 -13 387.788 22.0861  15

-7   9 -13 430.894 23.8203  15

-9  -9 -13 543.119 28.0321   7

-13  -9  -9 518.036 26.2265   8

-9  -9 -13 537.492 24.6376   8

9  13   9 503.762 21.3551  29

13   9  -9 508.530 23.0920  27

-9  13   9 540.847 26.0310  30

-13   9   9 522.030 22.6298  30

-9   9  13 580.638 27.0550  30

9  13  -9 552.419 24.2354  27

9  13   9 537.349 24.8302  26

9   9 -13 515.754 25.5409  27

-9  13  -9 513.449 25.9366  24

-9  13   9 500.720 25.8729  13

-9   9  13 546.784 25.0628  13

-9   9 -13 537.500 26.6281  22

-13   9  -9 511.001 24.4354  22

-9  13  -9 517.053 24.1594  23

9  13  -9 524.929 26.1919  23

-9  13   9 495.466 24.6774  21

-13   9   9 517.887 23.3504  21

13   9  -9 507.047 28.3044  18

9  13  -9 473.401 24.7646  18

-9   9 -13 492.614 24.9331  15

-11  13   1 43.2542 8.84854   9

-13  11   1 47.9854 8.37962   9

-11  13  -1 63.3372 10.1740   9

-13   1 -11 48.2026 10.3574   8

-13  -1 -11 59.9685 10.6140   8

-13  11   1 47.9048 8.41388  10

-13  11  -1 56.8584 8.73203  10

-11   1 -13 55.8444 10.2473   8

-13  -1 -11 47.0413 9.60307   7

-13  -1 -11 50.4640 9.80322   6

-13   1 -11 49.7031 8.54577   7

-11  -1 -13 47.1219 9.63134   7

-11   1 -13 48.8637 8.71651   7

-1  11  13 57.3471 9.33984  30

13  11   1 64.1505 9.86723  28

11  13   1 50.2594 9.31334  28

1  11  13 83.1708 10.8772  29

-1  11  13 77.6557 10.4710  29

-1  13  11 71.3847 10.4380  29

-11  13   1 51.6492 7.37271  30

1  13  11 46.2167 8.34371  30

-1  13  11 43.7877 8.77988  30

1  11  13 46.2335 7.50665  30

-11  -1  13 49.4924 9.88585  25

-13  -1  11 36.6755 8.91942  25

1  11  13 38.8718 7.14573  26

1  13  11 56.2259 8.92622  26

-1  11  13 54.3084 7.43585  26

-1  13  11 45.1852 8.01022  26

11  -1 -13 40.7958 9.31667  12

13  -1 -11 70.0551 11.9193  12

-13   1 -11 53.7175 8.62925  14

-13  11  -1 40.2240 6.82235  13

-1  13  11 44.8711 7.24410  13

-11  13  -1 48.5287 8.32596  13

-11  13   1 44.6242 8.71380  13

-13  11   1 52.3259 8.45802  13

-1  13 -11 63.6364 9.95738  23

-1  11 -13 35.6067 7.35950  23

-13  11  -1 38.5699 7.23293  24

-11  13  -1 67.2088 9.78563  23

-11   1 -13 50.8977 9.34671  22

-13  -1 -11 55.7632 8.62857  22

-11  -1 -13 53.1196 9.26668  22

-13   1 -11 41.2187 7.98484  22

1  11 -13 42.9398 8.08220  23

1  13 -11 63.0200 9.98619  23

-1  13 -11 41.8239 6.95996  24

13  11  -1 41.9680 9.89762  19

-1  11 -13 44.0424 7.49068  22

11  13  -1 46.5378 9.85819  19

13  11   1 47.0639 9.42163  19

-11  13  -1 56.1904 9.79561  22

-1  13 -11 60.3814 8.34004  22

-13  11  -1 50.8814 7.76668  22

1  11 -13 45.1105 8.84812  20

11  13   1 45.6282 10.1857  19

1  13 -11 57.8857 10.1779  20

-1  13 -11 52.6255 9.46912  20

-11  13   1 64.1201 10.2880  21

-11  13  -1 41.1487 8.42224  21

-13  11  -1 39.2731 9.11956  21

13  11  -1 52.0446 9.44647  16

11  13  -1 50.9568 9.27278  16

13  11  -1 60.9084 10.9756  18

13  11   1 70.4079 11.6179  18

1  13 -11 41.6691 7.37041  15

11  13   1 45.7231 10.3566  18

-1  11 -13 48.4910 8.66467  15

1  11 -13 53.7611 8.42547  15

-1  13 -11 43.0283 7.50361  15

-11  13   3 382.910 22.7628   9

-13  11   3 383.392 21.4002   9

-3 -11 -13 424.957 21.9702   7

-13  11  -3 377.605 19.3425  10

-11   3 -13 370.865 18.6491   7

-13  11   3 379.407 21.4428  10

-11  -3 -13 389.523 25.5192   8

-13   3 -11 380.585 22.5937   8

-11  -3 -13 374.097 23.7712   7

-11   3 -13 399.913 23.5786   8

-13  -3 -11 417.948 24.4264   6

-13   3 -11 365.274 23.2936   6

13  11  -3 419.167 22.8429  28

13  11   3 424.598 23.0205  28

3  13  11 415.335 22.9223  29

-3  11  13 404.447 22.9963  29

-11  13   3 378.561 19.3990  30

11  13  -3 425.633 23.4120  28

-3  13  11 382.837 23.1138  29

3  13  11 356.579 17.9243  30

-3  13  11 423.118 23.6789  30

-3  11  13 437.549 23.6358  30

11  13   3 383.995 22.2748  28

-13  11  -3 412.419 21.1057  24

11  13   3 392.486 17.9375  26

-11  -3  13 417.498 23.8592  25

-3  11 -13 389.196 19.1824  24

13  11   3 398.492 16.7006  26

3  11  13 424.854 21.3234  26

3  13  11 394.507 21.6048  26

-3  13 -11 426.048 20.7387  24

-11   3  13 409.682 23.9162  25

-3  13  11 400.226 19.6568  26

-13   3  11 367.034 22.8415  25

-13  -3  11 390.340 23.4526  25

-11  13  -3 399.070 22.2090  24

11  -3 -13 447.675 25.5987  12

11   3 -13 421.498 25.1854  12

13  -3 -11 432.034 25.4135  12

-3  13  11 391.623 19.9208  13

-11  13   3 406.087 22.4469  13

-13  11   3 416.516 21.9532  13

13   3 -11 349.040 23.3372  12

-3  11 -13 392.840 21.2142  22

-13  -3 -11 398.699 19.8889  22

-3  13 -11 386.917 21.5065  22

3  11 -13 352.855 20.8338  23

3  13 -11 402.985 23.4644  23

-3  13 -11 441.584 23.0946  23

-3  11 -13 392.327 19.9119  23

-11   3 -13 452.479 24.9027  22

-13  11  -3 410.737 20.7276  22

-11  13  -3 362.900 21.3875  22

-13   3 -11 400.587 21.6516  22

-11  13  -3 455.992 23.9211  23

3  13 -11 430.970 23.7137  20

13  11   3 394.478 22.9840  19

-3  11 -13 452.951 25.2175  20

11  13   3 403.527 24.5613  19

-13  11   3 409.027 24.2437  21

-11  13  -3 373.491 20.7669  21

-13  11  -3 367.476 21.4841  21

11  13  -3 410.943 25.4814  19

13  11  -3 422.586 25.9822  18

-11   3 -13 410.227 19.6542  15

11  13  -3 362.872 23.6575  18

-3  13 -11 436.290 21.4548  15

-13   3 -11 390.189 18.5995  14

-3  11 -13 396.377 22.2115  15

3  13 -11 376.113 17.5499  15

3  11 -13 364.871 19.4959  15

13  11  -3 392.439 21.2102  16

11  13  -3 386.283 22.8387  16

-11  13   5 307.496 20.0514   9

-13  11   5 363.925 20.5579   9

-11   5 -13 323.810 19.3763   8

-13  11  -5 294.018 16.2780  10

-13  -5 -11 342.926 22.9680   8

-5 -13 -11 354.239 18.5452   7

-11  -5 -13 354.818 22.9527   8

-13  11   5 320.538 20.2513  10

-11  -5 -13 324.980 22.2840   7

-13   5 -11 298.475 17.6600   8

-5 -11 -13 308.124 19.3102   7

-13  -5 -11 333.350 20.5221   6

-13   5 -11 357.241 21.4204   6

13  11  -5 363.050 20.1394  28

5  13  11 361.952 20.6453  29

13  11   5 323.801 18.8861  28

-5  11  13 311.213 19.7035  29

-11  13   5 304.799 17.9783  30

11  13  -5 343.898 20.1424  28

11  13   5 371.157 19.9254  28

-5  13  11 352.385 21.5433  29

-5  13  11 350.843 21.9320  30

-5  11  13 344.392 21.2271  30

5  11 -13 326.772 20.5021  27

-5  11 -13 331.800 18.5937  24

13  11   5 326.311 16.5357  26

5  11  13 336.183 19.5907  26

5  13  11 350.164 20.2211  26

11  13   5 321.875 17.2035  26

-11   5  13 280.714 19.0683  25

-11  -5  13 308.789 19.7561  25

-13   5  11 333.796 20.6018  25

-13  -5  11 293.073 19.3115  25

-5  13 -11 307.345 18.5870  24

-13  11  -5 336.778 19.5512  24

-11  13  -5 332.765 20.4890  24

11  -5 -13 341.983 21.0412  12

11   5 -13 329.819 21.2656  12

13  -5 -11 337.244 20.9030  12

-5  13  11 331.412 19.0828  13

-5  11  13 322.761 17.4663  13

-11  13   5 331.164 20.7661  13

-13  11   5 339.316 20.3995  13

13   5 -11 293.754 20.0845  12

-5  11 -13 320.301 20.0670  22

-5  13 -11 364.302 21.3743  22

-5  13 -11 377.904 20.1961  23

5  13 -11 340.492 20.9913  23

-13  -5 -11 291.557 16.3441  22

-13  11  -5 285.762 17.8109  22

-11  13  -5 318.884 20.1659  22

-5  11 -13 333.231 17.0254  23

5  11 -13 337.749 20.0092  23

-11  13  -5 323.578 20.0456  23

-11   5 -13 333.440 21.4419  22

-13   5 -11 330.161 19.8584  22

5  13 -11 370.018 21.1787  20

13  11   5 322.549 18.9347  19

11  13   5 341.665 21.4332  19

-11  13   5 365.987 22.1749  21

-13  11   5 313.245 20.6780  21

-5  13 -11 357.520 22.0904  20

-11  13  -5 304.131 16.9139  21

-5  11 -13 320.273 20.4607  20

5  13 -11 300.049 16.7614  19

-13  11  -5 309.302 18.1360  21

13  11  -5 325.026 22.5156  18

5  11 -13 295.484 16.9557  18

11  13  -5 332.535 22.1227  18

-11   5 -13 316.707 18.4931  15

-5  13 -11 340.985 19.4051  15

-5  11 -13 341.013 20.5911  15

11  13  -5 330.161 20.4587  16

5  11 -13 321.782 16.9711  15

-13  11   7 44.1478 8.01994   9

-13  -7 -11 43.4125 9.12896   8

-13  11   7 39.4211 7.79834  10

-11  13   7 35.4101 6.35014  10

-13 -11  -7 52.3507 8.65854   8

-11  13   7 53.0106 8.62076   9

-11  -7 -13 59.6430 10.1366   8

-11  -7 -13 67.7683 11.2656   7

-7 -13 -11 35.6921 7.00707   7

-7 -11 -13 56.4165 9.19519   7

11  13   7 32.8792 6.25246  28

-7  13  11 44.7394 8.21839  29

-7  11  13 41.4581 8.38142  30

-13   7  11 42.9915 7.71478  30

13  11  -7 53.4081 7.82952  28

13  11   7 40.8453 6.80633  28

7  13  11 45.2339 7.88699  29

-11  13   7 51.7509 8.10873  30

-13  11   7 44.0601 6.81859  30

-7  11  13 40.4166 7.53094  29

11  13  -7 59.2474 8.22817  28

7  13  11 51.5280 8.58658  26

11   7 -13 41.2536 8.50382  27

7  11 -13 48.4573 8.52588  27

13  11  -7 48.5144 6.71941  27

13  11   7 59.3169 7.89418  26

7  11  13 74.0684 9.78352  26

11  13   7 48.2547 7.56663  26

-11  -7  13 38.1332 6.72886  25

-11   7  13 47.2569 7.81112  25

11  -7 -13 41.5487 7.64981  12

11   7 -13 49.4788 8.12243  12

13  -7 -11 44.3463 7.74008  12

13   7 -11 36.9697 7.39223  12

-7  13  11 53.3819 8.64349  13

-7  11  13 38.2424 7.02324  13

-13  11   7 62.7775 9.44294  13

-7  11 -13 45.9163 7.83011  24

-13  11  -7 56.7204 9.05656  24

-7  13 -11 52.3578 9.08669  24

-7  13 -11 35.2846 6.89685  23

-7  11 -13 43.6115 6.49843  23

-13   7 -11 47.0058 8.81865  22

-11   7 -13 41.8980 8.93188  22

-11  13  -7 45.4066 8.17175  23

-11  13  -7 37.4974 8.29584  24

7  11 -13 43.3794 8.43364  23

-7  11 -13 51.7163 8.51792  22

-11  13  -7 61.9355 9.75048  22

-13  11  -7 42.1065 8.07389  22

11  13   7 46.1494 8.56647  19

7  13 -11 46.5017 7.70194  20

-7  13  11 49.8805 8.72476  21

-7  11 -13 47.4732 7.97608  20

-11  13   7 49.0993 8.85279  21

-7  13 -11 50.0292 9.28041  20

-7  13 -11 39.8104 8.37778  22

-13  11   7 48.1355 8.65814  21

-11   7 -13 43.6543 7.99045  15

7  11 -13 44.6642 6.43627  15

7  11 -13 42.3115 7.55269  18

7  13 -11 37.2649 7.03234  18

11  13  -7 48.1632 9.16751  18

-7  13 -11 50.0941 8.58286  15

-11  13   9 28.3114 6.71414   9

-13 -11  -9 41.3993 7.42830   8

-11  13   9 21.3242 5.04780  10

-13  11   9 28.0693 6.48552  10

-13  -9 -11 37.4027 7.44060   8

-13  11   9 32.6275 6.60585   9

-11  -9 -13 36.8166 7.56738   8

-11  -9 -13 18.5040 6.95464   7

-9 -13 -11 34.9371 6.45384   7

-9 -11 -13 26.1881 6.84209   7

-13   9  11 19.8611 5.25430  30

-9  11  13 36.9128 7.29450  30

-11   9  13 25.2060 6.25791  30

9  13  11 34.3657 6.06624  29

-11  13   9 23.2144 6.06991  30

-13  11   9 25.6534 5.22074  30

-9  13  11 25.7395 6.65405  30

11  13   9 29.5915 6.24968  26

13   9 -11 20.0146 5.52779  27

11   9 -13 28.7308 7.38686  27

13  11  -9 20.0551 5.31594  27

9  11 -13 35.3646 7.24302  27

13  11   9 32.4512 6.54576  26

9  11  13 31.0306 7.32548  26

-9  13  11 30.6555 6.99322  13

-11  13   9 36.4250 7.74978  13

-9  11  13 35.1389 6.81895  13

-11   9  13 31.9381 7.01092  13

-13   9  11 34.7007 7.28600  13

-9  11 -13 23.9293 6.52560  24

-9  13 -11 41.4723 7.95537  24

-9  13 -11 26.8353 5.61783  23

-13  11  -9 27.2899 6.65225  24

-11  13  -9 30.6653 6.56640  23

11  13  -9 24.7016 6.66333  23

9  11 -13 25.5537 6.86988  23

-11   9 -13 30.3404 7.26527  22

-9  13 -11 40.3202 7.99477  22

-13  11  -9 29.3263 7.03903  22

9  13 -11 35.7663 6.15916  20

-11  13  -9 18.3561 6.24959  22

-9  11 -13 29.2087 6.96821  22

-9  13  11 29.3273 6.41184  21

-11  13   9 29.2861 6.50216  21

-13  11   9 37.4323 6.80302  21

-13   9 -11 19.1550 5.83800  22

-9  11 -13 42.1041 7.93329  15

11   9 -13 27.5897 7.67563  18

9  11 -13 34.4279 7.83802  18

9  13 -11 24.1061 6.40490  18

11  13  -9 23.4367 6.99714  18

11   9 -13 29.3443 4.98892  15

13  11  -9 41.3666 8.64696  18

-11 -13 -11 231.898 13.5769   7

-11 -11 -13 223.691 14.5023   7

-13  11  11 186.031 12.8585  10

-13 -11 -11 226.542 12.8076   8

-13 -11 -11 197.605 14.4716   7

-11  13  11 217.295 13.5089   9

-13  11  11 223.255 12.9045   9

-11  13  11 245.305 13.8763  30

-13  11  11 216.874 12.3067  30

-11  11  13 230.013 13.9852  30

11  11 -13 195.077 12.8020  27

-11  11 -13 220.472 14.0483  24

13  11 -11 212.301 12.4321  27

-11  13 -11 210.105 13.8717  24

13  11  11 233.664 13.2644  26

11  13  11 212.380 12.7999  26

-13  11 -11 234.496 14.4673  24

-11  13  11 240.760 14.2999  13

-11  11  13 218.299 13.4084  13

-13  11  11 204.572 13.7382  13

11  11 -13 247.427 14.4668  23

-13  11 -11 233.235 14.1073  22

-11  13 -11 208.208 13.8626  22

-11  13  11 220.970 12.3347  21

11  13 -11 194.039 13.5502  19

11  13 -11 192.435 13.1823  18

11  11 -13 212.680 13.8554  18

13  11 -11 227.441 15.0042  18

-13  13   1 90.8148 10.9000   9

-13  -1 -13 120.296 13.6718   8

-13   1 -13 96.9886 12.3467   8

-13   1 -13 82.8390 9.68274   7

-13  -1 -13 102.512 11.5238   7

-1  13  13 115.568 12.3156  29

1  13  13 104.038 11.7156  29

1  13  13 92.8460 9.33029  30

-1  13  13 117.245 11.3154  30

13  13   1 66.1084 10.3025  28

-13  -1  13 81.4255 11.2274  25

1  13  13 110.531 10.5522  26

-1  13  13 91.1346 9.17490  26

13  -1 -13 69.7618 11.5837  12

-13   1 -13 76.5797 8.39121  14

-13  13   1 96.0919 10.0210  13

-13  13  -1 83.5691 8.69819  13

1  13 -13 85.3983 10.3409  23

-13   1 -13 95.1475 10.7004  22

-1  13 -13 75.4422 9.45292  23

-13  -1 -13 108.627 10.9419  22

1  13 -13 104.041 12.0901  20

13  13  -1 111.262 12.7262  19

-1  13 -13 90.4007 11.7440  20

13  13   1 76.0086 11.0670  19

-13  13   1 90.5839 11.9812  21

-13  13  -1 91.4787 11.2355  21

13  13   1 126.049 12.7530  16

13  13  -1 82.5314 10.4775  16

-1  13 -13 83.8946 9.51387  15

13  13  -1 86.1260 11.9457  18

1  13 -13 95.0786 9.35996  15

-13  -3 -13 383.269 21.9368   7

-13  13   3 361.735 20.6134   9

-13  -3 -13 363.589 22.8162   8

-13   3 -13 380.892 20.9367   8

13  13  -3 372.861 20.7836  28

13  13   3 421.527 21.7421  28

-3  13  13 387.970 21.8206  29

-3  13  13 330.030 19.6478  30

3  13  13 387.927 19.6993  26

-13   3  13 345.766 20.9225  25

-13  -3  13 309.024 19.9369  25

13  -3 -13 393.176 22.6785  12

13   3 -13 345.502 21.2735  12

-13  13   3 356.764 19.4151  13

-3  13 -13 371.663 18.8327  22

3  13 -13 358.077 20.2786  23

-13  -3 -13 345.201 18.4471  22

-3  13 -13 359.495 18.4591  23

-13   3 -13 351.847 19.8833  22

-13  13  -3 348.657 18.5876  22

3  13 -13 398.304 22.2040  20

-3  13 -13 383.443 22.4585  20

13  13   3 366.720 21.2113  19

-13  13   3 342.488 21.0691  21

-13  13  -3 381.156 19.8575  21

13  13  -3 387.107 23.1068  19

-3  13 -13 340.292 18.6207  15

3  13 -13 368.972 16.6552  15

13  13  -3 379.581 20.3332  16

-13   5 -13 374.557 18.5688   8

-13  13   5 411.147 21.2306   9

-13  -5 -13 412.245 23.4153   8

-13  -5 -13 469.446 24.3824   7

5  13  13 423.289 21.4583  29

13  13  -5 414.851 20.3432  28

13  13   5 396.729 19.7338  28

-5  13  13 399.046 21.1723  29

-5  13  13 416.741 21.8892  30

-13  13  -5 405.451 20.3797  24

5  13  13 412.780 20.0907  26

-5  13 -13 430.454 19.4646  24

13  13   5 364.988 15.8442  26

-13   5  13 365.439 20.2600  25

-13  -5  13 402.849 20.5768  25

13  -5 -13 391.738 20.9585  12

13   5 -13 397.908 21.2786  12

-5  13  13 402.936 18.0859  13

-13  13   5 433.436 21.4997  13

-5  13 -13 376.064 19.9288  22

5  13 -13 414.818 21.1716  23

-13  -5 -13 380.225 18.2015  22

-5  13 -13 407.841 18.4496  23

-13  13  -5 380.097 19.5446  22

-13   5 -13 415.626 21.1474  22

5  13 -13 436.993 21.8995  20

-5  13 -13 422.968 22.2946  20

-5  13  13 403.159 18.5926  21

13  13   5 422.002 20.9564  19

-13  13   5 416.781 21.9482  21

-13  13  -5 366.179 17.6834  21

13  13  -5 454.778 24.3699  19

-5  13 -13 410.162 20.4725  15

-13  13   7 54.4845 7.93034   9

-13  -7 -13 41.9918 8.24440   8

-7 -13 -13 37.9695 6.35450   7

13  13  -7 35.0150 5.75324  28

13  13   7 52.7002 6.58881  28

-13   7  13 36.1090 6.62179  30

7  13  13 53.1751 7.69748  29

-13  13   7 33.9843 5.50717  30

-7  13  13 41.1071 7.47070  30

13   7 -13 28.9402 6.63039  27

7  13  13 32.6170 6.56725  26

13  13   7 39.7910 5.88585  26

13   7 -13 37.1459 6.25983  12

-7  13  13 35.5486 6.32148  13

-13  13   7 38.4203 7.05047  13

13  -7 -13 26.9878 5.57606  12

-13  -7 -13 33.5171 5.51402  22

-7  13 -13 31.9935 6.22826  24

-13  13  -7 39.8367 6.94975  24

-7  13 -13 30.7337 5.64324  23

-13   7 -13 36.2766 6.88957  22

7  13 -13 50.3459 7.77905  23

-7  13 -13 52.4626 8.00386  22

-13  13  -7 41.6242 7.10681  22

7  13 -13 43.3966 7.28705  20

-13  13   7 46.4662 7.31247  21

13  13   7 32.9267 5.70346  19

13  13  -7 34.1659 7.30278  18

-7  13 -13 49.2710 7.47437  15

-9 -13 -13 73.6404 7.76304   7

-13  13   9 58.4483 7.28398   9

-13  -9 -13 66.4293 7.83136   8

-13 -13  -9 71.4025 8.53293   7

-13  -9 -13 73.3306 9.12221   7

-9  13  13 90.7676 9.13075  30

-13   9  13 72.0766 7.59749  30

9  13  13 63.0298 7.13059  29

13   9 -13 66.4751 7.42652  27

9  13  13 89.6313 8.43790  26

13  13   9 70.5269 6.81378  26

-9  13  13 83.7527 8.17215  13

-13   9  13 72.6544 8.24674  13

-9  13 -13 64.2585 7.81214  24

-13  13  -9 70.5715 8.18424  24

13  13  -9 57.7496 7.70642  23

9  13 -13 63.5385 7.84159  23

9  13 -13 73.5242 7.24866  20

-13   9 -13 68.1972 8.24842  22

-9  13 -13 72.6341 8.50533  22

-13  13  -9 66.8943 7.86162  22

13  13  -9 93.0143 9.71821  19

-13  13   9 71.3563 7.64102  21

13  13  -9 83.8419 9.29038  18

13   9 -13 68.2182 9.10851  18

0  14   0-0.65803 2.54631   9

-14   0   0 2.59295 4.72990  10

-14   0   0-1.43576 5.39926   6

0  14   0-1.25003 5.58540  30

0   0  14 1.27378 4.92897  25

0  14   0-2.29285 4.31118  26

-14   0   0 3.71151 4.91851  14

0   0 -14-1.36440 4.97768  12

0  14   0-0.93270 3.40276  23

0  14   0 1.11070 3.79041  19

0  14   0-0.94079 3.74020  16

0  14   2 112.253 9.34977   9

-2  14   0 115.949 10.3294   9

-14   2   0 113.188 12.8856  10

-14  -2   0 108.787 11.4187  10

-2   0 -14 101.771 12.7298   8

-14   0   2 91.9508 11.6684  10

-14   0  -2 96.9345 11.9561  10

-14  -2   0 117.106 13.7504   6

-14   2   0 103.527 12.4841   6

-14   0  -2 103.514 12.7872   6

2  14   0 104.051 12.0193  30

0  14   2 106.376 12.1211  30

0  14   2 96.7969 10.3322  29

0  14  -2 120.204 12.7837  30

2  14   0 115.267 12.3729  28

-2   0  14 121.208 13.2994  25

0   2 -14 101.514 8.77388  27

2  14   0 117.826 11.5276  26

0  -2  14 103.280 11.7562  25

0   2  14 98.2897 11.9106  25

-14   2   0 88.8830 11.3285  14

2   0 -14 85.1378 11.5430  12

0  -2 -14 112.215 12.7457  12

0   2 -14 116.226 13.0083  12

0  14  -2 108.259 11.8595  22

2  14   0 108.416 10.2358  23

0  14  -2 94.7794 10.6855  23

-2  14   0 123.128 11.2896  23

0  14   2 90.4791 8.80684  23

-14   2   0 106.326 12.1220  21

2  14   0 112.564 12.3274  19

0  14  -2 114.227 11.0638  20

0  14  -2 100.256 10.5876  19

-2  14   0 107.530 12.0025  22

-2  14   0 102.807 10.3337  19

0  14   2 92.9562 11.2374  19

-14   0  -2 125.129 12.7048  14

2  14   0 115.717 11.9494  16

0  14   2 126.989 10.8949  16

-2   0 -14 136.037 11.2891  15

0  14  -2 95.1251 10.4656  16

14   2   0 95.4443 10.2027  18

-14   0   2 106.107 11.4869  14

-2  14   0 115.523 9.71661  16

-14  -2   0 110.446 11.9446  14

-2  14   2 661.349 25.7002   9

-2  -2 -14 640.208 30.3765   8

-14   2   2 658.629 31.4615  10

-14  -2   2 687.712 29.1839  10

-14   2  -2 627.384 30.6481  10

-14  -2  -2 669.796 29.4818  10

-2  -2 -14 670.161 31.5143   7

-14   2   2 652.708 31.4339   6

-14  -2  -2 654.415 31.1663   6

-14   2  -2 594.639 29.8907   6

2  14  -2 658.717 29.7200  30

-2  14  -2 623.026 29.1657  30

2  14   2 668.005 29.1346  30

-2  14   2 667.103 30.0038  30

2  14   2 649.597 24.8584  29

-2  14   2 673.411 28.4632  29

2   2 -14 675.698 24.7210  27

2  14   2 639.154 29.4802  28

-2  -2  14 645.187 29.9654  25

-2   2  14 686.203 30.6344  25

2  14   2 706.495 29.4184  26

-2  14   2 670.015 29.9216  26

-2  14   2 711.890 31.0119  13

2  -2 -14 702.594 31.7470  12

2   2 -14 634.165 30.4927  12

2  14  -2 667.524 27.7090  23

2   2 -14 646.466 23.9371  22

-2  14  -2 657.585 28.6421  23

-2  14   2 670.647 25.0813  23

-2  14  -2 716.316 30.1683  22

2  14  -2 659.640 28.8595  19

2  14  -2 723.371 25.8353  20

2  14   2 618.818 30.1112  19

-2  14  -2 742.111 29.6203  20

-2  14  -2 602.742 23.6498  19

-14   2   2 637.580 28.9505  21

-2  14   2 691.927 28.6824  19

-2   2 -14 672.093 27.6315  15

-2  -2 -14 658.029 24.2641  15

-14   2   2 651.883 29.2650  14

-14  -2   2 703.953 28.8519  14

14   2  -2 629.409 26.1853  18

2  14  -2 708.085 29.8803  16

-4   0 -14-4.31999 5.41518   8

-4  14   0 1.05290 3.18500   9

-14   0   4 3.97007 5.12083  10

0  14   4 0.70753 2.66071   9

-14  -4   0-2.07846 4.13157  10

-14   0  -4-1.38622 5.21294  10

-4   0 -14-1.35665 5.39352   7

-14  -4   0-1.34018 4.73407   6

-14   4   0-1.36749 4.66677   6

-14   0  -4 1.47956 5.39783   6

4  14   0 2.62027 4.30839  28

4  14   0 2.36144 4.69408  30

-4  14   0-1.26802 4.32731  30

0  14   4 2.20421 4.38153  29

0  14   4-1.25490 5.11858  30

-4   0  14 1.37585 5.32397  25

0   4 -14 3.33093 3.56242  27

0  14   4 1.25318 4.84928  26

4  14   0 1.00681 3.43589  26

0  -4  14 1.23035 4.89140  25

0   4  14-1.24513 5.56347  25

-14   0   4-1.12447 4.22864  14

-14  -4   0 3.47526 4.09203  14

0  14   4-2.40098 4.64539  13

-4  14   0 2.56304 4.21429  13

4   0 -14-1.45586 4.78761  12

0  14  -4-1.22290 4.86178  23

-4  14   0-1.06572 4.34694  23

0   4 -14-0.92999 3.79332  22

4  14   0 0.85979 3.67816  23

-4  14   0 3.95748 4.96076  22

0  14  -4 2.13707 4.77442  22

0  14  -4 5.52180 4.50456  20

4  14   0 1.42590 5.36216  19

0  14  -4-0.85239 2.90892  19

0  14   4 1.37553 4.52344  19

-14   4   0 1.32542 5.40624  21

-4   0 -14 0.86597 3.44277  15

4  14   0 1.29842 4.58658  16

14   4   0-2.11312 3.33820  18

-4  -2 -14 158.995 15.2843   8

-4  14   2 154.895 13.3037   9

-2  -4 -14 169.811 14.9060   8

-4  14  -2 140.771 12.6097   9

-14   4   2 185.666 16.8054  10

-14  -2   4 195.086 15.2009  10

-14   2  -4 168.333 15.6110  10

-2  -4 -14 178.657 16.1581   7

-14   2   4 171.633 15.7021  10

-14  -2  -4 203.778 16.3349  10

-14  -4   2 187.032 13.7977  10

-14  -4  -2 178.818 14.2896  10

-2  14   4 149.772 12.0395   9

-14  -4   2 161.567 15.1281   6

-14   4   2 160.528 15.1998   6

-14  -4  -2 193.693 15.8405   6

-14   4  -2 142.327 14.1082   6

-14  -2  -4 182.139 16.4756   6

-14   2  -4 179.366 16.2018   6

2  14  -4 158.408 14.7351  30

4  14  -2 172.669 14.5969  30

-2  14  -4 166.734 14.4956  30

4  14   2 166.529 13.8884  30

-4  14  -2 179.003 15.0401  30

2  14   4 157.917 12.9108  29

2  14   4 149.399 13.7314  30

-4  14   2 173.811 15.0916  30

-2  14   4 155.416 14.6738  30

-2  14   4 167.467 14.6050  29

2   4 -14 174.183 13.1061  27

4  14   2 181.626 11.3546  29

4  14   2 171.638 14.7574  28

-2  -4  14 153.223 14.1321  25

-2   4  14 179.043 15.4563  25

-4  -2  14 174.927 15.7350  25

-4   2  14 160.377 14.8315  25

4  14   2 150.450 13.0570  26

-2  14   4 199.248 16.0259  26

4  14  -2 143.614 11.7670  26

2  -4  14 175.567 14.6653  25

2   4  14 170.554 14.7428  25

4  -2 -14 165.253 15.5002  12

4   2 -14 167.282 15.5728  12

-2  14   4 179.829 15.2239  13

2  -4 -14 167.497 14.7007  12

2   4 -14 183.104 15.5648  12

2  14  -4 159.632 12.6143  22

4  14  -2 195.564 14.5038  23

2  14  -4 163.800 14.4000  23

-2  14  -4 191.398 15.7225  23

-2   4 -14 179.316 14.5640  22

-4  14  -2 160.208 14.1145  23

-4  14   2 175.839 12.9798  23

-2  14  -4 170.261 14.5286  22

-4  14  -2 172.826 15.3526  22

4  14  -2 163.935 14.9755  19

2  14  -4 156.031 13.4847  19

2  14  -4 172.697 13.1997  20

4  14   2 161.785 15.5662  19

2  14   4 164.831 15.7098  19

-14   4   2 197.476 16.0319  21

-14   2   4 151.282 13.4659  21

14   2  -4 142.190 13.1011  18

-2  14  -4 182.777 15.7318  20

4  14  -2 188.084 15.9750  16

-2   4 -14 201.185 15.2959  15

-14  -2   4 165.565 13.2042  14

14   4  -2 168.326 14.3391  18

14   4   2 189.858 14.3822  18

4  14  -2 186.312 14.3912  18

-14   4  -2 197.939 15.8125  14

-14   2  -4 162.977 14.6611  14

-14  -4   2 145.800 12.5272  14

-4  -2 -14 144.783 10.6376  15

-4   2 -14 145.189 12.4052  15

2  14  -4 192.670 15.6977  16

-4  -4 -14-1.36329 5.27535   8

-4  14   4 2.19589 4.24858   9

-14   4   4 6.12854 6.84589  10

-14  -4   4 0.97499 4.35646  10

-14  -4  -4-1.16802 4.64359  10

-4  -4 -14-1.50159 5.47819   7

-14  -4  -4-1.36497 5.42658   6

-14   4  -4 1.40512 4.25048   6

4  14  -4-1.26872 4.00851  28

4  14   4-1.21443 4.14442  28

-4   4  14 2.27691 3.17222  29

-4  14  -4-1.22760 4.61647  30

4  14   4 1.05766 4.72584  30

4  14   4 3.34379 3.96176  29

-4  14   4-1.35202 4.77592  29

-4  -4  14-2.61511 5.19833  25

-4   4  14 1.32380 4.97823  25

4   4 -14 1.09857 4.48095  27

4  14   4-1.16951 4.26670  26

-14  -4   4-1.83836 3.84184  14

-14   4  -4-1.23370 4.63940  14

14   4  -4-4.30539 5.99830  12

14  -4  -4-1.46896 5.99172  12

-4  14   4 1.32487 5.26717  13

4  -4 -14 4.01293 6.22091  12

4   4 -14-1.38245 5.19877  12

-4  14  -4 6.39347 5.71347  24

-4  14  -4-2.57933 4.70505  23

-4  14   4 5.11390 3.46229  23

-4   4 -14 1.30052 5.03247  22

4  14  -4 1.21447 4.43072  23

-4  14  -4-1.31659 5.63234  22

4  14  -4 2.56337 5.35697  19

-4   4 -14 0.87556 3.99287  20

4  14  -4 1.68687 3.76865  20

-4  14  -4 2.32467 3.31498  21

-4  14  -4 1.35033 5.07799  20

-14   4   4 2.44391 5.22750  21

-4   4 -14-1.14844 4.56577  15

4  14  -4 1.39588 5.69365  16

14   4  -4-1.31845 5.24165  18

4  14  -4 0.99931 4.64744  18

-6  14   0 223.759 16.7596   9

-14   6   0 219.991 13.6406   9

-14   0  -6 245.868 19.0706  10

-6   0 -14 225.381 17.6559   7

-14   6   0 231.840 18.4667  10

-6   0 -14 254.503 19.5659   8

-14  -6   0 220.643 16.7003   6

-14   6   0 209.684 16.6283   6

-14   0  -6 248.005 19.4296   6

6  14   0 241.890 16.3822  30

0  14   6 227.343 16.7422  29

0  14   6 232.136 17.0561  30

6  14   0 213.834 17.3428  28

-6  14   0 237.370 17.2208  30

0  -6  14 285.695 18.1081  25

0   6  14 248.035 17.0901  25

-6   0  14 221.462 17.8295  25

0  14   6 242.780 17.5639  26

6  14   0 243.338 15.0397  26

0   6 -14 202.335 14.7568  27

6   0 -14 239.273 18.8519  12

0  14   6 234.873 16.7889  13

-6  14   0 226.251 17.3211  13

14   0  -6 231.729 19.1971  12

-14   6   0 229.999 13.7924  13

6  14   0 236.816 14.1897  23

0  14  -6 221.723 17.4144  23

-6  14   0 234.542 16.4151  23

0  14  -6 219.417 15.4604  22

0   6 -14 226.412 14.5291  22

6  14   0 244.653 19.5565  19

0  14  -6 229.813 17.2124  20

-14   6   0 250.417 18.3110  21

0   6 -14 234.649 17.5413  15

6  14   0 210.668 17.5620  16

14   6   0 216.564 16.8824  18

6  14   0 242.965 18.1316  18

-6   0 -14 219.844 13.6031  15

-6   2 -14 612.594 30.6116   8

-6  14   2 612.442 28.1901   9

-14   6   2 588.976 23.1639   9

-2  -6 -14 591.842 26.7974   8

-6  14  -2 572.187 27.4114   9

-14  -2   6 593.798 27.2545  10

-14   6   2 554.270 29.5696  10

-2  -6 -14 562.025 29.3702   7

-14   6  -2 605.015 30.0348  10

-6   2 -14 591.117 27.7956   7

-14   2  -6 578.565 29.9599  10

-14  -6  -2 608.740 24.1825  10

-14  -2  -6 600.070 29.3882  10

-6  -2 -14 591.882 30.0470   7

-6  -2 -14 587.024 30.4645   8

-14  -6   2 556.200 26.9708   6

-14   6   2 566.663 27.3989   6

-14  -6  -2 582.925 27.3345   6

-14   6  -2 633.489 28.6250   6

-14  -2  -6 569.596 29.9354   6

-14   2  -6 495.537 28.2920   6

-6  14   2 573.771 27.9382  30

-2  14  -6 539.979 27.3872  30

6  14   2 592.355 25.2772  30

2  14   6 590.077 26.4309  29

-6  14  -2 642.231 28.0732  30

-2  14   6 632.004 29.3909  29

2  14   6 626.338 27.5486  30

-2  14   6 615.411 29.4936  30

6  14   2 597.276 28.9185  28

2   6  14 561.482 26.4272  25

-14   6  -2 577.159 22.3735  24

-2  -6  14 580.272 27.1513  25

-2   6  14 581.357 26.8533  25

2   6 -14 641.107 27.4720  27

-6  -2  14 562.080 29.1309  25

-6   2  14 549.480 28.7057  25

2  14   6 656.075 29.3713  26

6  14   2 601.603 25.9711  26

-2  14   6 609.835 28.5282  26

6  14  -2 598.244 22.6800  26

2  -6  14 609.801 27.2504  25

6  -2 -14 670.701 31.9085  12

6   2 -14 585.358 30.2679  12

-6  14  -2 563.041 26.7881  13

-2  14   6 607.187 28.2206  13

-6  14   2 537.602 27.6398  13

14   2  -6 578.816 30.8209  12

14  -2  -6 619.444 31.7289  12

2  -6 -14 593.272 27.1252  12

2   6 -14 613.151 28.1992  12

-2  14  -6 648.235 27.8015  24

6  14  -2 570.663 25.4387  23

2   6 -14 592.152 22.3694  23

2  14  -6 542.841 27.7960  23

-6   2 -14 615.323 30.2938  22

-2  14  -6 625.597 29.4611  23

-2  14  -6 628.324 28.1408  22

-6  14  -2 663.916 29.4682  23

-2   6 -14 649.450 27.5851  22

-6  14   2 646.048 26.1897  23

-14   2  -6 620.045 22.3637  22

2  14  -6 577.888 23.6466  22

6  14  -2 662.943 31.7357  19

2  14  -6 578.814 24.8946  19

2  14  -6 693.028 28.4364  20

-2  14  -6 639.316 30.1275  20

-6  14  -2 590.322 26.2266  21

-14   6   2 543.030 28.2339  21

-14   6  -2 532.753 27.9809  21

-14   2   6 642.670 26.2525  21

14   6   2 578.031 24.4623  19

6  14  -2 566.928 27.9518  18

14   6  -2 593.202 29.1689  18

-14  -6   2 604.704 24.9144  14

-14   2  -6 654.518 29.3384  14

14   6   2 584.375 27.1646  18

-2  14  -6 574.125 21.9351  15

-6   2 -14 628.982 25.8621  15

-14   6  -2 622.098 28.1902  14

-2   6 -14 598.287 28.3996  15

-4  -6 -14 31.1479 7.81246   8

-6  14   4 37.4507 7.99156   9

-14   4  -6 39.4337 7.84708   8

-14   6   4 32.8441 6.06615   9

-6   4 -14 39.6499 9.05978   8

-14   6   4 37.1590 9.38540  10

-14  -4   6 40.8023 7.16067  10

-14   6  -4 34.7127 8.86868  10

-14   4  -6 31.6460 9.34029  10

-14  -4  -6 45.8138 9.05360  10

-14  -6  -4 34.8478 6.84330  10

-6  -4 -14 41.5219 9.29093   8

-14  -6  -4 28.3821 7.31750   6

-14   6  -4 24.1839 7.63508   6

-14  -4  -6 30.7277 7.66578   6

-14   4  -6 30.2964 8.44571   6

-6  -4 -14 39.2581 9.62558   7

-4  -6 -14 31.8624 9.30152   7

-14  -6   4 29.2365 7.79933   6

-14   6   4 30.3575 7.82366   6

6  14  -4 43.9224 8.59768  28

6  14   4 40.9831 8.34422  28

4  14  -6 26.5750 7.09354  28

-4  14  -6 39.5972 8.49740  30

-6  14  -4 29.0255 7.22352  30

-4   6  14 27.1881 6.42558  29

6  14   4 36.3757 6.59997  30

4  14   6 36.6624 7.42060  29

6  14   4 27.1757 5.39819  29

4  14   6 50.2157 7.95287  30

-6  14   4 38.8434 8.21595  30

-4  14   6 45.7882 8.78726  30

4   6 -14 31.8911 7.52743  27

-4  -6  14 30.9592 7.54701  25

-4   6  14 26.4646 7.21835  25

-6   4  14 28.5303 7.85873  25

-6  -4  14 24.0808 7.92935  25

6  14   4 33.6118 7.24943  26

4  -6  14 28.5608 7.46418  25

4   6  14 40.1505 8.25922  25

-4  14   6 43.4644 8.18752  26

14   4  -6 23.3224 7.88705  12

14  -4  -6 29.6060 8.55903  12

14   6  -4 25.6361 8.20455  12

14  -6  -4 33.4781 7.98663  12

-14   6  -4 31.2036 7.55026  14

-14   4  -6 37.1925 8.23206  14

-4  14   6 33.1073 7.84958  13

-6  14   4 45.2568 9.21029  13

4  -6 -14 36.0372 7.92224  12

4   6 -14 24.0913 7.69344  12

6  -4 -14 38.9252 8.98480  12

6   4 -14 35.9646 9.10924  12

-4   6 -14 31.0379 7.84598  22

-4  14  -6 25.6402 7.50964  23

-14   4  -6 28.5333 5.94606  22

-6  14  -4 29.0726 7.35478  23

-4  14  -6 48.4672 8.95462  24

-6  14   4 32.6052 7.01307  23

-6  14  -4 40.6332 9.09671  24

-6   4 -14 32.9216 8.77717  22

4   6 -14 33.5784 6.61229  23

6  14  -4 30.3165 7.60510  23

4  14  -6 42.8877 9.00175  23

-14   6  -4 30.2816 8.25319  21

-6  14  -4 30.5521 8.51686  22

6  14  -4 33.2804 8.77371  19

4  14  -6 21.2868 7.09710  19

-14   6  -4 28.6593 5.91037  22

6  14   4 36.8372 9.25732  19

-4  14  -6 50.4906 9.32690  22

4  14   6 47.6856 10.4707  19

-4   6 -14 26.3330 7.52609  20

4  14  -6 32.1899 7.18962  20

-4  14  -6 41.1879 8.89998  20

-6  14  -4 26.6874 6.05947  21

-14   6   4 35.2944 8.53451  21

-14   4   6 33.2189 7.64723  21

-4  14  -6 31.4049 6.12369  15

14   6  -4 31.1968 9.30738  18

4  14  -6 19.0918 5.83380  18

6  14  -4 41.3878 8.61985  18

-6   4 -14 27.1610 7.02513  15

-4   6 -14 41.6689 8.08287  15

-14   6  -6 562.834 28.9440  10

-6  -6 -14 566.810 30.2700   7

-6  -6 -14 522.547 26.9909   8

-14   6   6 531.541 22.1719   9

-14  -6  -6 516.740 25.9635   6

-14   6  -6 560.796 27.2934   6

6   6 -14 587.848 27.7217  27

6  14   6 512.225 22.0210  29

-6   6  14 542.973 21.9948  29

-6  14   6 556.144 27.8152  30

-6  14   6 537.805 28.3641  29

6  14  -6 568.895 26.3003  28

6  14   6 526.758 24.7414  28

-6  14  -6 581.092 28.2704  24

-6   6  14 507.081 25.4159  25

-6  -6  14 600.337 27.0876  25

6  14   6 489.478 24.8890  26

6  -6 -14 598.613 27.4572  12

6   6 -14 532.785 26.7736  12

-6  14   6 598.091 28.8971  13

14   6  -6 552.515 26.9049  12

14  -6  -6 519.289 26.2025  12

-14   6  -6 509.718 22.6178  22

6  14  -6 546.496 27.2751  23

-6  14  -6 553.369 28.2350  22

-6   6 -14 554.339 28.1389  22

6  14  -6 561.496 22.9033  20

-6   6 -14 592.839 23.7607  20

-14   6   6 555.451 26.3445  21

6  14   6 518.623 28.9842  19

6  14  -6 546.781 27.5722  19

14   6  -6 600.365 30.6375  18

6  14  -6 508.964 24.9245  18

-6   6 -14 527.576 26.2618  15

-14   6  -6 533.752 24.2702  14

-14   8   0-0.98204 3.58275   9

-14   8   0 2.80794 5.43277  10

-14   0  -8 6.00274 6.12113   8

-14   0  -8-3.00203 4.93610  10

-14   0  -8 3.13487 5.34910   6

-8   0 -14 1.35815 5.10740   7

-14  -8   0-1.00329 3.54404   6

-14   8   0 2.03698 4.04913   6

0  14   8 2.63426 4.49490  29

-8  14   0 1.12011 4.68162  30

8  14   0-2.79158 5.24894  28

0  14   8-1.23776 4.51568  30

0  -8  14-1.95679 4.37167  25

0   8  14 0.96425 4.03020  25

-8   0  14 4.42603 6.31148  25

0   8  14-1.50671 3.43555  26

-14   0   8 3.01228 6.58804  25

0  14   8 1.25367 4.98409  26

8  14   0-0.76943 3.13842  26

8   0 -14-1.58211 5.94961  12

0  14   8 1.05911 4.31998  13

-8  14   0 2.50478 4.42396  13

14   0  -8-4.94100 6.88382  12

-14   8   0 0.81216 3.22882  13

-14   0  -8 0.77771 3.61684  22

-8  14   0 6.03014 5.27532  23

0   8 -14-1.72330 3.51457  22

0   8 -14-0.78552 3.36043  23

0  14  -8 0.98643 4.49847  22

-8  14   0 2.66203 5.94724  22

0  14  -8 2.73566 5.14380  20

-8  14   0 1.31214 4.63505  21

14   8   0 2.55960 4.52079  19

0   8 -14-1.29041 4.85267  15

14   8   0-1.90215 3.87932  16

8  14   0 2.97129 6.05978  16

0  14  -8 2.73245 3.17692  15

-8   0 -14 0.73504 2.99816  15

14   8   0 1.45109 5.29398  18

8  14   0-3.04814 5.38366  18

-14   2  -8 86.2275 11.6639   8

-8   2 -14 64.3378 10.9796   8

-14   8   2 60.5291 8.52773   9

-14  -2  -8 64.5135 11.9171   8

-14   8   2 70.9099 11.3375  10

-14   8  -2 68.0812 10.8184  10

-14   2  -8 73.4632 11.8200  10

-8  -2 -14 54.4752 10.6023   8

-14  -2  -8 71.3438 12.0551  10

-14   8  -2 72.0940 9.28852   6

-14  -2  -8 78.6567 11.9253   6

-14   2  -8 52.7065 10.4553   6

-8  -2 -14 87.1745 12.0857   7

-8   2 -14 60.1039 9.56467   7

-2  -8 -14 80.6620 11.3648   7

-14  -8   2 64.9878 9.00747   6

-14   8   2 53.4872 8.57526   6

-14  -8  -2 53.5571 8.17476   6

2   8  14 81.0144 8.76534  30

-2   8  14 56.1408 9.31781  29

2  14   8 75.8263 10.7048  29

-8  14  -2 67.5066 9.49383  30

8  14   2 85.1807 11.4292  28

-2  14   8 71.0963 10.9260  29

-8  14   2 61.1893 9.97783  30

2  14   8 76.6115 10.0997  30

-2  14   8 56.5011 9.49667  30

2  -8  14 61.4253 8.69871  25

2   8  14 61.1146 8.47995  25

-2  -8  14 66.2018 9.21048  25

-2   8  14 49.3541 8.22088  25

2   8 -14 57.9501 9.88638  27

-8   2  14 75.7506 11.5656  25

-8  -2  14 68.9622 10.9473  25

2   8  14 69.9895 9.02174  26

-14   2   8 73.7131 10.9861  25

-14  -2   8 68.7096 11.1371  25

2  14   8 71.9334 10.1675  26

8  14   2 77.2978 9.15321  26

-2  14   8 71.3688 10.1190  26

8  -2 -14 67.2233 11.2087  12

8   2 -14 78.3425 12.2657  12

14   8  -2 62.7255 9.07081  12

14  -8  -2 57.7569 8.89315  12

-14   2  -8 77.7359 10.4707  14

-8  14  -2 53.0136 9.50087  13

-2  14   8 69.1961 10.4366  13

-8  14   2 63.8675 10.5746  13

14   2  -8 68.6165 11.8814  12

14  -2  -8 77.1266 12.0525  12

-14   8   2 67.0298 9.19747  13

-2   8 -14 54.5112 6.99289  23

-14   8  -2 67.0965 8.32123  24

-8  14  -2 66.7602 9.86633  23

-8   2 -14 64.5378 11.0133  22

-8  14   2 60.6177 9.07004  23

-14   2  -8 60.1914 8.19617  22

8  14  -2 75.7677 9.33338  23

-2  14  -8 63.7763 9.26978  24

2   8 -14 57.9787 7.81448  23

2  14  -8 65.9622 11.0731  23

-2   8 -14 75.4118 9.74754  22

14   8   2 58.6512 8.98530  19

-2  14  -8 71.5863 10.0517  22

-8  14  -2 97.0511 12.3342  22

-2   8 -14 81.4375 11.2868  20

2  14  -8 61.9446 10.2499  20

-2  14  -8 73.9186 10.9869  20

-8  14   2 70.7654 11.5327  21

8  14   2 70.3480 11.5207  19

-8  14  -2 69.9425 10.2062  21

-14   8   2 61.2325 10.3748  21

-14   8  -2 59.5607 9.85522  21

14   8  -2 59.8707 8.46488  16

8  14  -2 82.9853 12.0697  16

-2  14  -8 63.5786 7.77837  15

2   8 -14 64.9064 10.3750  15

-8   2 -14 63.5030 8.51242  15

14   8  -2 72.6659 11.5287  18

8  14  -2 42.2514 9.83451  18

14   8   2 42.9543 9.52914  18

-14   8   4 3.88136 4.59871   9

-4  -8 -14 4.15318 4.82878   8

-8   4 -14 4.14354 5.49107   8

-14   4  -8 1.06645 4.34997   8

-14   8   4-2.97200 5.58820  10

-14   8  -4-6.58881 4.80758  10

-8  -4 -14-4.68550 6.37056   8

-14   4  -8 1.49862 5.95795  10

-14  -8  -4 2.92159 4.25983   6

-14   8  -4 2.01748 3.90344   6

-14  -4  -8 2.79355 4.93403   6

-14   4  -8 1.44830 4.94256   6

-4  -8 -14 1.43992 5.41493   7

-14  -8   4-2.04814 4.57579   6

-14   8   4 4.14973 4.23161   6

-8  14  -4 3.54827 4.04537  30

4  14   8 1.11700 4.55614  29

-4   8  14 1.07803 4.71549  29

4  14   8 0.89252 3.64053  30

-8  14   4 2.52814 4.75363  30

-4  14   8-1.40566 5.58839  30

8  14  -4-2.58604 4.41265  28

8  14   4 3.73987 5.21044  28

4   8 -14 3.93479 5.48200  27

-4   8  14-1.93393 3.84433  25

-4  -8  14 3.77326 3.94274  25

-8   4  14 1.37669 4.86308  25

-8  -4  14 2.70515 5.78630  25

4  14   8 3.77624 4.73361  26

8  14   4 6.16423 4.19057  26

-4  14   8 6.63848 4.94371  26

4  -8  14 0.97938 4.28394  25

4   8  14 1.87525 4.36061  25

8  -4 -14-4.24360 6.18736  12

8   4 -14-1.47014 5.36351  12

-14   4  -8 2.06015 3.75803  14

4  -8 -14 2.87356 4.27992  12

14   4  -8 1.45947 6.24360  12

4   8 -14-2.03701 4.15440  12

-4  14   8 1.26389 4.89074  13

14  -4  -8 1.47080 5.84736  12

14   8  -4 2.05709 4.69054  12

14  -8  -4 0.97522 4.62182  12

-4  14  -8 2.69436 6.01950  23

-14   8  -4 2.99937 4.46730  24

-8  14  -4 2.64487 5.39409  23

-14   4  -8 0.93335 3.40517  22

-4  14  -8 1.21898 4.71696  24

-8   4 -14 1.48465 6.05576  22

8  14  -4-2.36907 4.58368  23

-4   8 -14 1.24549 4.81956  22

4   8 -14 4.86655 4.52656  23

4  14  -8 2.79206 5.55011  23

-14   8  -4 1.28694 5.37897  21

8  14  -4-1.55628 5.85248  19

8  14   4 1.59269 6.16307  19

4  14  -8 5.14053 4.39825  19

-14   8  -4 1.66515 4.08935  22

-4  14  -8 1.30875 5.33826  22

4  14  -8-1.14479 4.42990  20

-4   8 -14-1.19839 5.00883  20

-4  14  -8 2.92444 5.49878  20

-8  14  -4 2.75834 3.65541  21

-14   8   4 2.71644 5.25576  21

-14   4   8-0.91660 3.73876  21

8  14  -4 1.46486 4.81724  16

-4  14  -8 0.93473 3.61706  15

-8   4 -14-1.08397 5.04121  15

14   8  -4-1.56890 5.15938  18

8  14  -4 2.76058 5.19068  18

4   8 -14 4.74383 4.83742  15

-4   8 -14 1.31673 5.23482  15

-14   8   6 92.3471 10.3279   9

-8  -6 -14 132.702 14.8205   7

-14   8  -6 131.945 13.0331  10

-14   6  -8 146.650 14.6912  10

-14   8   6 120.695 14.2304  10

-8  -6 -14 113.472 13.6245   8

-6  -8 -14 146.240 13.3631   8

-14   6  -8 103.146 12.4575   6

-6  -8 -14 119.861 14.1758   7

-14  -8   6 122.425 11.6628   6

-14   8   6 122.479 11.6132   6

-14  -8  -6 122.415 11.1032   6

-14   8  -6 107.797 11.2386   6

-14  -6  -8 124.211 12.7087   6

6  14   8 140.885 12.0928  29

-6   8  14 131.558 11.4232  29

8   6 -14 167.204 14.9297  27

-8  14   6 143.792 13.8331  30

-6  14   8 129.356 14.1373  29

-14   6   8 105.551 10.0374  30

8  14  -6 136.733 12.8147  28

8  14   6 106.938 11.2714  28

6   8 -14 113.255 12.5620  27

-8  14  -6 157.510 14.7151  24

-6   8  14 108.941 11.0153  25

-6  -8  14 147.264 12.0897  25

-8   6  14 122.467 12.7923  25

-8  -6  14 129.338 12.7671  25

8  14   6 128.539 12.1184  26

-6  14  -8 122.231 13.5985  24

-14   8  -6 149.597 12.9342  24

6  -8  14 116.232 10.9157  25

6   8  14 113.425 10.8997  25

8  -6 -14 133.770 13.2830  12

8   6 -14 137.789 13.8676  12

14  -6  -8 117.486 12.8201  12

14   6  -8 154.197 14.0653  12

14  -8  -6 110.739 10.8949  12

-6  14   8 154.301 14.7501  13

-8  14   6 126.922 13.7309  13

-6   8  14 121.451 11.1440  13

14   8  -6 113.405 11.6519  12

6  -8 -14 129.770 11.7483  12

6   8 -14 113.231 11.6268  12

-14   6  -8 100.509 10.6355  22

6   8 -14 132.748 12.3131  23

8  14  -6 144.637 13.7923  23

6  14  -8 115.521 12.7124  23

-14   8  -6 127.893 11.4634  22

-6  14  -8 125.748 13.3768  22

-6  14  -8 128.516 13.4951  23

-8   6 -14 157.453 15.3843  22

-6   8 -14 134.106 13.9062  22

6  14  -8 137.181 11.8786  20

-6   8 -14 124.579 11.8403  20

-14   8   6 138.413 13.4019  21

-14   6   8 113.724 11.1564  21

-8  14   6 91.4626 12.2184  21

6  14   8 122.989 14.4518  19

8  14   6 109.344 13.6351  19

8  14  -6 146.247 14.7779  19

6  14  -8 108.385 12.1342  19

14   6  -8 140.494 15.2930  18

14   8  -6 133.654 14.6792  18

6  14  -8 119.885 11.8663  18

8  14  -6 127.544 13.1653  18

-6  14  -8 115.958 11.8599  15

-8   6 -14 134.275 12.8117  15

-6   8 -14 132.167 13.4747  15

-14   6  -8 110.474 10.4633  14

-8  -8 -14 2.30104 4.57429   8

-14   8   8 3.56971 3.54830   9

-14  -8  -8-1.42265 5.35020   8

-8 -14  -8 0.87263 4.13592   7

-14   8  -8 2.24655 4.69512  10

-14  -8  -8 1.73343 3.87298   6

-14   8  -8 0.91759 3.64834   6

-8  -8 -14 1.46886 5.68408   7

-14   8   8 5.15160 3.85625  30

14   8  -8 0.79781 3.56513  28

8  14   8 3.78572 3.38345  29

8  14  -8 0.85016 3.71903  28

-8  14   8-1.26287 4.88704  30

-8   8  14 3.54527 4.50115  25

-8  -8  14 5.10409 4.17854  25

8  14   8 3.37298 3.97192  26

14  -8  -8 5.97974 4.12308  12

14   8  -8 12.9102 5.11627  12

-8  14   8 2.59524 4.73433  13

8   8 -14 4.65947 4.49780  12

-8   8  14 1.98913 4.15721  13

-8  14  -8 1.17537 4.79449  23

-8   8 -14 2.66701 5.43945  22

8  14  -8 5.09394 6.14630  23

-8  14  -8 5.14454 4.97705  24

-14   8  -8 4.92858 4.21717  22

8  14   8 6.70598 5.04389  19

-8  14  -8-1.31991 5.24771  22

-8  14   8 3.89351 5.02232  21

-8   8 -14 2.30175 3.89655  20

-14   8   8 6.03369 5.10694  21

8  14  -8-2.57442 5.25062  19

-8   8 -14 2.38871 5.22449  15

14   8  -8 6.12396 7.25591  18

8  14  -8 5.63642 5.63168  18

-10  14   0 6.81328 6.09036   9

-14  10   0 11.8803 5.21448   9

-14   0 -10 10.4195 6.22306   8

-14  10   0 3.60451 5.14207  10

-14   0 -10 6.61597 5.41784   7

-10   0 -14 7.80099 7.11652   8

-14   0 -10 6.15666 5.95770   6

-10   0 -14 10.1957 6.04175   7

0  10  14 14.0727 5.87221  30

0  10  14 9.22386 6.24657  29

10  14   0 12.3970 6.02690  28

-10  14   0 3.50353 3.83399  30

0  14  10 10.7022 5.97923  29

0  14  10 5.81586 5.51448  30

-14   0  10 4.42964 6.59911  25

0  10  14 8.78513 3.78780  26

0  14  10 9.28553 5.39994  26

-10   0  14 7.26089 5.92507  25

10   0 -14 10.9588 6.38735  12

14   0 -10 6.41930 6.54753  12

-10  14   0 2.27282 4.52028  13

-14  10   0 9.77120 4.75762  13

0  14 -10 4.05133 5.08050  23

-14   0 -10 8.97506 4.63292  22

0  10 -14 6.27146 4.24850  23

-10   0 -14 15.7077 6.51368  22

-10  14   0 2.42719 5.53633  23

14  10   0 6.81981 5.27996  19

0  14 -10 11.2135 4.97783  22

0  10 -14 10.0833 6.57063  20

10  14   0 4.82578 6.05095  19

0  14 -10 12.6122 6.26321  20

-10  14   0 1.31123 5.35035  21

14  10   0 13.8719 5.67677  16

10  14   0 18.7645 7.09106  16

0  14 -10 14.5417 4.57976  15

14  10   0 12.3061 7.29165  18

10  14   0 11.0163 6.88534  18

0  10 -14 5.96315 5.44075  15

-10  14   2 507.529 26.1937   9

-14  10   2 473.646 23.1825   9

-10   2 -14 469.594 22.8999   7

-14  10  -2 527.669 24.8165  10

-10  -2 -14 482.905 26.8225   7

-14  -2 -10 489.962 27.8458   8

-14   2 -10 539.664 27.0075   8

-14  10   2 504.880 25.4654  10

-10  -2 -14 498.264 28.5574   8

-10   2 -14 444.958 25.8695   8

-14  -2 -10 480.456 26.9362   6

-14   2 -10 520.389 28.0207   6

14  10  -2 458.538 24.6301  28

14  10   2 527.926 26.2014  28

-2  10  14 522.758 25.6724  29

2  14  10 518.337 25.6885  29

-10  14   2 499.966 22.8453  30

2  14  10 467.136 22.0684  30

10  14   2 510.005 26.4549  28

-2  14  10 513.758 25.9862  30

-2  10  14 522.682 24.9364  30

-14  10  -2 465.113 21.1918  24

2  10  14 487.498 22.1576  26

-10   2  14 491.563 26.5519  25

-10  -2  14 492.896 26.5209  25

2  14  10 474.171 24.1453  26

10  14   2 479.115 19.9763  26

-2  14  10 486.979 23.4108  26

-14   2  10 479.512 26.4807  25

-14  -2  10 506.066 27.0369  25

10  -2 -14 476.678 27.1780  12

10   2 -14 435.258 26.2868  12

14  -2 -10 467.068 27.3879  12

14   2 -10 450.493 26.8518  12

-10  14  -2 489.060 22.5061  13

-2  14  10 485.939 22.6268  13

-10  14   2 495.662 25.0888  13

-14  10   2 496.887 22.8442  13

-2  10 -14 460.046 22.1508  22

-2  14 -10 530.569 22.8564  24

10  14  -2 497.137 22.1629  23

2  10 -14 507.527 22.9826  23

2  14 -10 448.452 25.3135  23

-2  14 -10 488.279 23.2609  22

-2  14 -10 495.653 25.7979  23

-2  10 -14 453.537 20.2619  23

-10   2 -14 534.260 27.8274  22

-14  -2 -10 446.634 20.2609  22

-10  14  -2 494.568 25.3126  23

-14   2 -10 468.554 21.9061  22

-14  10  -2 495.217 20.4620  22

-10  14  -2 501.077 25.3347  22

14  10   2 475.459 24.6673  19

-2  10 -14 536.251 27.1314  20

2  14 -10 527.953 26.6321  20

-2  14 -10 526.310 27.3437  20

-10  14   2 457.039 25.4967  21

-10  14  -2 461.928 23.7226  21

-14  10   2 491.474 26.4947  21

-14  10  -2 517.306 26.3978  21

10  14   2 520.411 28.6264  19

14  10  -2 487.928 26.6907  19

10  14  -2 466.072 27.7237  19

10  14  -2 484.102 26.1971  16

14  10  -2 425.975 26.2357  18

10  14  -2 463.774 26.8149  18

-10   2 -14 483.061 20.8194  15

14  10   2 516.501 27.6091  18

-2  14 -10 447.634 20.8288  15

-2  10 -14 529.052 25.8177  15

2  10 -14 474.023 23.7217  15

-14   2 -10 529.730 23.7855  14

14  10  -2 472.636 22.5821  16

-10  14   4 167.606 14.9855   9

-10   4 -14 173.219 15.3867   8

-14  10   4 172.390 13.7289   9

-10  -4 -14 210.993 17.7585   7

-14  10  -4 169.976 13.7698  10

-14  10   4 151.167 14.5169  10

-14  -4 -10 214.107 18.0609   8

-4 -10 -14 157.680 14.5143   7

-14   4 -10 189.032 14.2543   8

-10  -4 -14 189.134 16.8538   8

-14  -4 -10 190.080 15.8494   6

-14   4 -10 156.084 15.4024   6

14  10  -4 165.957 14.3440  28

14  10   4 157.427 13.5531  28

4  14  10 176.169 14.6007  29

-4  10  14 178.748 14.8882  29

-4  14  10 179.790 16.0570  29

-4  14  10 176.881 15.4022  30

10  14  -4 164.523 14.6833  28

10  14   4 222.031 16.2586  28

-4  10  14 136.657 13.7049  30

-10  14   4 174.155 14.0291  30

-14  10  -4 178.122 13.6002  24

-10  14  -4 150.723 14.5441  24

4  10 -14 173.114 15.1177  27

14  10   4 156.683 10.8004  26

4  10  14 204.821 14.8670  26

-4  14 -10 189.961 14.4755  24

4  14  10 182.043 14.7354  26

10  14   4 153.797 11.9913  26

-10   4  14 148.912 14.7702  25

-10  -4  14 157.793 14.9329  25

-14   4  10 145.735 14.5708  25

-14  -4  10 160.976 14.7779  25

-4  10 -14 144.792 12.3416  24

10  -4 -14 169.022 15.5369  12

10   4 -14 172.676 15.9051  12

14   4 -10 183.583 16.4379  12

-4  14  10 175.307 14.0381  13

-10  14   4 188.548 15.4593  13

-14  10   4 132.256 12.9836  13

14  -4 -10 139.682 14.4074  12

-4  10 -14 168.432 14.0967  22

10  14  -4 170.586 14.0094  23

4  10 -14 146.578 12.7985  23

-4  14 -10 163.428 14.5084  22

-4  14 -10 195.852 15.7638  23

-14  10  -4 161.813 12.4022  22

-4  10 -14 139.054 10.3929  23

-10  14  -4 180.389 15.6511  22

-10  14  -4 139.523 14.2550  23

-14   4 -10 170.265 13.3016  22

4  14 -10 208.814 15.9700  20

-4  10 -14 161.759 15.3146  20

14  10   4 179.570 13.8973  19

-4  14 -10 152.153 15.3260  20

10  14   4 141.654 14.9740  19

-10  14   4 166.175 15.5652  21

-14  10   4 167.177 14.9316  21

-10  14  -4 161.279 12.6320  21

-14  10  -4 153.358 13.9877  21

14  10  -4 131.923 15.4180  18

10  14  -4 140.241 14.7723  18

-10   4 -14 176.463 13.5306  15

-4  14 -10 166.024 13.1392  15

-14   4 -10 153.434 11.9843  14

14  10  -4 179.744 13.1758  16

10  14  -4 184.326 15.6559  16

4  10 -14 156.095 12.9150  15

-10  14   6 451.275 23.6000   9

-6 -10 -14 443.303 23.9785   7

-14  10   6 455.188 21.5544   9

-14  10  -6 415.103 20.3677  10

-14  -6 -10 422.765 25.1342   8

-14  10   6 428.781 23.5855  10

-10  -6 -14 465.525 25.5754   8

-14  -6 -10 440.524 22.2765   6

-14   6 -10 462.901 23.2174   6

6  14  10 447.428 21.5815  29

14  10  -6 458.979 21.6071  28

14  10   6 457.500 21.1445  28

-10  14   6 463.087 22.7092  30

-6  10  14 427.577 21.0192  29

-6  14  10 483.848 25.1968  30

-6  14  10 438.487 24.2954  29

-6  10  14 430.688 23.4731  30

-14   6  10 384.596 18.6945  30

10  14  -6 417.094 21.4613  28

10  14   6 408.070 20.4610  28

6  14  10 459.176 23.0393  26

10  14   6 444.420 20.7586  26

-14  10  -6 415.481 21.5792  24

-10   6  14 424.694 22.1642  25

-10  -6  14 389.580 21.2010  25

-6  14 -10 428.356 22.5507  24

10  -6 -14 414.408 21.8727  12

10   6 -14 454.174 23.2186  12

14  -6 -10 443.609 22.6299  12

14   6 -10 478.859 23.3421  12

-6  14  10 487.239 23.6310  13

-6  10  14 464.729 20.3171  13

-14  10   6 449.668 23.1024  13

-14   6 -10 439.978 21.4237  22

-6  10 -14 442.414 23.2858  22

10  14  -6 464.973 23.4040  23

6  10 -14 453.266 21.9831  23

-6  14 -10 427.189 23.4465  22

-14  10  -6 414.993 20.4187  22

-10  14  -6 426.598 23.5547  22

-6  14 -10 457.846 22.7826  23

-10  14  -6 457.462 23.3909  23

6  14 -10 477.928 22.3487  20

-6  10 -14 442.233 22.1421  20

-6  14 -10 475.328 25.2565  20

-10  14   6 470.886 24.9344  21

-14  10   6 459.882 23.4099  21

10  14   6 501.684 25.6711  19

14   6 -10 443.345 25.7514  18

10  14  -6 422.143 24.7578  19

6  14 -10 379.271 20.1065  19

6  10 -14 423.996 21.0580  18

14  10  -6 445.311 25.7984  18

10  14  -6 444.786 24.5068  18

-6  14 -10 398.405 20.8109  15

-10   6 -14 449.098 22.0516  15

6  10 -14 384.139 19.3371  15

-10  14   8 11.1455 5.18568   9

-14  10   8 13.1736 4.87482   9

-14 -10  -8 12.4011 5.63400   8

-14  -8 -10 15.9540 6.23399   8

-14  10   8 5.74156 4.91486  10

-10  -8 -14 8.56609 5.52666   8

-10  -8 -14 5.26960 5.37573   7

-8 -10 -14 16.7079 6.15929   7

-14   8  10 7.98383 3.86305  30

-8  10  14 10.3190 5.53563  30

14  10  -8 9.03497 3.58909  28

8  14  10 12.4224 4.59179  29

10  14  -8 12.9661 4.26062  28

-10  14   8 10.1276 5.22754  30

-8  14  10 14.9579 5.93849  30

14   8 -10 2.71916 3.70025  27

10   8 -14 9.97940 5.15904  27

14  10  -8 9.29027 3.85915  27

8  10 -14 11.2566 5.13570  27

-10   8  14 10.5402 4.17967  25

10  14   8 8.34308 4.39601  26

14   8 -10 7.00623 4.20334  12

-8  14  10 19.6676 6.38298  13

-10  14   8 8.18605 4.77248  13

-8  10  14 12.9644 4.73228  13

-14  10   8 11.1500 5.93182  13

10   8 -14 6.27637 4.41368  12

-10   8  14 10.6476 4.83800  13

-14  10  -8 7.18917 4.77881  24

-8  14 -10 2.20778 4.27436  24

-10  14  -8 11.4508 5.42900  24

-8  14 -10 5.66067 4.39033  23

-10  14  -8 9.99599 4.91207  23

-8  10 -14 1.16544 4.87351  22

10  14  -8 8.83934 5.70282  23

8  10 -14 8.77837 4.95551  23

8  14 -10 4.59342 4.91504  23

10  14  -8 11.0601 5.93290  19

8  14 -10 3.99182 4.27200  19

-14  10  -8 6.30887 4.50500  22

-8  14 -10 15.1783 6.30188  22

10  14   8 5.41451 5.03855  19

8  14 -10 12.5917 4.43259  20

-8  14  10 15.6842 5.39697  21

-10  14   8 10.1287 5.13455  21

-14   8 -10 11.2510 5.34258  22

-14  10   8 9.44094 4.79674  21

-10   8 -14 1.02935 4.40621  15

-8  10 -14 6.61280 5.02845  15

8  10 -14 6.03007 4.49323  18

14   8 -10 6.77022 5.92475  18

14  10  -8 12.1163 5.76131  18

8  14 -10 6.99102 4.58120  18

10  14  -8 11.1199 6.08721  18

8  10 -14 6.80869 3.51627  15

-14  10  10 320.141 15.5711   9

-10 -14 -10 270.761 14.6943   7

-14  10  10 316.654 17.9252  10

-10 -10 -14 326.636 18.5560   7

-14 -10 -10 320.876 17.4459   8

-10  14  10 323.366 17.4059   9

-10  14  10 343.854 17.5106  30

-14  10  10 281.294 13.7210  30

-10  10  14 343.779 17.8489  30

-10  14 -10 328.839 18.1067  24

14  10 -10 312.047 15.0417  27

10  10 -14 342.783 17.9484  27

-14  10 -10 310.770 17.0494  24

10  14  10 364.237 17.3598  26

-10  10 -14 349.434 18.1856  24

-10  14  10 320.721 17.6570  13

-10  10  14 334.935 16.7262  13

-10  10 -14 339.783 18.4741  22

10  10 -14 322.888 16.7299  23

10  14 -10 369.027 18.7476  23

-14  10 -10 321.010 16.5180  22

-10  14 -10 308.181 15.5373  23

-10  14  10 323.962 16.8978  21

10  14 -10 306.512 17.2905  19

10  10 -14 309.922 17.4303  18

10  14 -10 315.349 16.6956  18

-14   0 -12-1.35637 4.94842   8

-14  12   0-2.40575 3.58316  10

-12   0 -14 2.80681 5.72434   8

-14   0 -12-0.95197 4.16407   7

-14   0 -12-2.79468 4.76864   6

-12   0 -14 1.04763 4.16500   7

14  12   0-1.21499 5.54077  28

12  14   0 3.73296 4.53965  28

0  12  14 1.21573 4.70439  29

0  14  12 1.93919 3.95491  30

0  12  14 2.66376 4.12944  30

-12   0  14 9.27156 5.66623  25

-14   0  12 1.32518 4.83463  25

0  12  14 0.77119 3.22330  26

0  14  12 2.86721 3.48682  26

12   0 -14-1.42233 5.94481  12

-14   0 -12 2.75247 3.92503  14

14   0 -12 1.44078 5.25638  12

-12  14   0 1.79085 4.61991  13

-14  12   0-0.72523 3.24051  13

0  14 -12 1.13594 4.39565  23

0  12 -14-0.89781 3.17150  23

-14   0 -12 0.89857 3.66521  22

-12   0 -14 5.86923 5.56316  22

14  12   0 5.16496 4.99657  19

0  14 -12 2.59780 5.02621  20

12  14   0 1.41397 4.82539  19

-12  14   0 1.19390 4.86983  21

-14  12   0-2.48634 4.81056  21

14  12   0 2.11314 4.20054  16

12  14   0 1.24980 5.92311  16

0  14 -12 2.24766 3.48440  15

14  12   0 4.33015 5.26587  18

0  12 -14-0.96269 3.92675  15

-12   2 -14 74.7272 10.7614   8

-12  14   2 55.3618 9.10922   9

-14  12   2 66.3228 9.31572   9

-14  -2 -12 53.8623 10.3926   8

-14  12   2 48.8794 7.36635  10

-14   2 -12 66.7242 9.95314   8

-14  -2 -12 64.0190 9.77888   7

-12  -2 -14 58.4541 9.86255   7

14  12  -2 61.8399 9.14964  28

14  12   2 66.4717 9.62696  28

2  12  14 49.0722 8.65603  29

2  14  12 63.1711 9.04827  29

12  14  -2 58.6311 9.25231  28

12  14   2 57.0729 9.13059  28

-2  12  14 50.8809 8.89270  29

-2  14  12 50.7742 8.95214  29

2  14  12 60.3853 7.64164  30

-2  14  12 62.0290 9.09358  30

-2  12  14 59.6415 8.80606  30

-12   2  14 54.0787 10.0856  25

-12  -2  14 69.7640 10.7149  25

-14   2  12 51.3937 9.35729  25

-14  -2  12 50.6712 9.51225  25

2  12  14 57.1704 8.00531  26

2  14  12 55.4579 8.28886  26

-2  14  12 42.2925 6.88330  26

12  -2 -14 54.1028 10.0740  12

12   2 -14 61.8124 10.1521  12

-14   2 -12 58.4814 7.31505  14

14   2 -12 62.0516 10.3450  12

-12  14   2 63.2333 9.21826  13

-14  12   2 60.2112 8.46081  13

14  -2 -12 53.8113 9.72013  12

2  14 -12 65.9281 9.60721  23

2  12 -14 61.9766 8.62567  23

-12   2 -14 61.0069 9.68968  22

-2  14 -12 55.5776 9.20146  23

-2  12 -14 38.7829 7.02680  23

-12  -2 -14 60.7328 9.12158  22

-14   2 -12 53.6375 8.29529  22

-14  -2 -12 49.1351 7.23654  22

12  14  -2 63.3549 7.55143  23

14  12  -2 54.9439 9.28419  19

-14  12  -2 48.4461 7.18966  22

-2  12 -14 63.3253 7.90272  22

-2  14 -12 52.4424 7.93348  22

-12  14  -2 65.8859 9.07108  22

2  12 -14 66.7498 10.6509  20

2  14 -12 72.2323 10.6423  20

-2  12 -14 58.0521 10.1730  20

-2  14 -12 70.5326 10.7703  20

14  12   2 64.5485 9.86349  19

12  14  -2 45.4250 8.84034  19

-12  14   2 53.7824 9.80013  21

12  14   2 48.3929 9.39297  19

-12  14  -2 65.9097 9.45303  21

-14  12  -2 62.2628 9.29132  21

14  12  -2 57.1145 8.81339  16

12  14  -2 58.3890 9.59143  16

12  14   2 53.9795 9.56538  16

-2  14 -12 66.1287 8.49439  15

2  14 -12 44.2183 6.25434  15

-2  12 -14 63.4478 8.66560  15

14  12  -2 71.2238 10.9950  18

2  12 -14 61.3821 8.33285  15

14  12   2 72.5340 9.82799  16

-14   4 -12 3.68914 4.45118   8

-12   4 -14 2.07386 3.78305   8

-12  14   4 1.14389 4.66583   9

-14  12   4 3.01149 3.88443   9

-14  -4 -12 6.84204 6.24042   8

-14  12   4 1.73960 3.27099  10

-12  -4 -14 1.36039 5.81975   8

-14  -4 -12 4.91709 5.93274   7

-12  -4 -14-5.13197 6.08044   7

-4  12  14 1.10510 4.39347  30

14  12  -4 1.04012 4.13516  28

14  12   4 4.06840 3.71070  28

4  14  12-1.06418 4.00194  29

12  14  -4 2.12400 4.33181  28

-12  14   4 0.69841 2.77666  30

12  14   4 4.12863 4.51482  28

-4  12  14-2.16960 5.04505  29

-4  14  12 5.90199 4.16970  29

-4  14  12 2.29561 4.91031  30

-12   4  14 9.17119 5.72698  25

-12  -4  14-1.12400 4.46861  25

4  12  14 4.52936 3.87534  26

-14   4  12 2.27773 5.29650  25

4  14  12-4.00592 4.08497  26

-14  -4  12-2.23009 4.43301  25

12  14   4 1.20113 2.68352  26

12  -4 -14 1.17799 4.16121  12

12   4 -14-1.20433 4.91236  12

14  -4 -12 1.18899 4.84978  12

14   4 -12 1.18988 4.47465  12

-4  14  12 0.78824 3.59469  13

-12  14   4 7.50950 5.17752  13

-14  12   4 1.96118 4.28927  13

-4  14 -12-0.95505 4.08571  23

-4  12 -14 0.68530 3.12524  23

-12  -4 -14 4.95596 4.95163  22

-14   4 -12-0.94395 3.33448  22

-4  12 -14-2.20759 3.73689  24

-4  14 -12-0.81038 3.98035  24

-14  12  -4 0.89187 4.22685  24

-12   4 -14 1.16241 5.30102  22

-14  -4 -12 3.53274 3.34855  22

12  14  -4 4.40853 3.85673  23

4  12 -14 1.92928 4.12676  23

4  14 -12 1.12705 4.23837  23

-14  12  -4 0.93745 4.10055  21

14  12  -4 1.32407 5.12361  19

12  14  -4 1.37354 4.68744  19

-4  12 -14-0.94696 4.05111  22

-4  14 -12 0.96816 3.94906  22

14  12   4 6.83594 4.62820  19

-14  12  -4 0.79599 3.84167  22

-12  14  -4 1.01164 4.02193  22

12  14   4-2.40367 5.25700  19

4  12 -14-1.19396 4.74675  20

4  14 -12 1.10037 6.10478  20

-4  12 -14-3.47767 5.28648  20

-12  14   4-1.21581 4.95921  21

-14  12   4 2.38859 4.21878  21

-12  14  -4-0.81701 4.01289  21

12  14  -4 1.09528 4.46757  16

-4  14 -12 6.17788 4.48180  15

-4  12 -14 3.11549 4.12869  15

14  12  -4 1.35757 5.25323  18

12  14  -4 5.26829 5.50488  18

4  12 -14 2.18463 2.97034  15

-14 -12  -6 19.6654 5.59945   8

-12  14   6 28.9164 6.66892   9

-14  12   6 18.0888 5.29277   9

-14  -6 -12 32.5892 7.71349   8

-14  12   6 14.0152 4.94228  10

-12  -6 -14 31.5202 8.32289   8

-14  -6 -12 29.9267 7.33183   7

-6 -12 -14 14.5955 4.90185   7

-6  14  12 12.4652 5.45300  29

-6  12  14 28.7540 6.52453  30

-14   6  12 19.6147 5.18599  30

12  14  -6 16.8556 5.28053  28

12  14   6 17.3533 4.78405  28

6  12  14 25.2942 6.33539  29

14  12  -6 20.7923 5.26629  28

6  14  12 13.5227 4.73547  29

14  12   6 14.8796 4.80336  28

-12  14   6 19.9211 4.95343  30

-6  14  12 30.4580 6.95312  30

-6  12  14 16.3039 5.23576  29

12   6 -14 16.1990 5.84992  27

-12   6  14 15.2942 5.13543  25

-12  -6  14 19.3033 5.43816  25

6  12  14 19.4454 5.47804  26

14  12   6 15.2794 3.91138  26

6  14  12 13.2023 5.24263  26

12  14   6 18.4525 4.66808  26

14  -6 -12 16.0442 5.34164  12

14   6 -12 22.1642 5.78438  12

-6  14  12 18.9037 5.25825  13

-6  12  14 24.8735 5.24955  13

-12  14   6 10.4656 5.65715  13

-14  12   6 26.5315 6.47169  13

12  -6 -14 19.4577 5.59896  12

12   6 -14 20.3326 6.20353  12

-12  -6 -14 25.2159 5.74679  22

-6  12 -14 16.1970 5.12856  24

-6  14 -12 15.2104 4.63021  23

-6  14 -12 17.2670 5.35129  24

-14  12  -6 25.0113 5.65458  24

-12  14  -6 23.9969 6.39255  24

-12   6 -14 20.4315 6.44027  22

12  14  -6 26.5957 6.37914  23

-14   6 -12 17.0407 5.18458  22

6  12 -14 20.1366 5.48464  23

6  14 -12 21.8363 6.51059  23

-6  12 -14 16.7000 5.53344  22

-6  14 -12 18.8874 5.74415  22

-12  14  -6 24.2402 6.32451  22

6  12 -14 14.4778 5.59021  20

6  14 -12 14.4530 5.28620  20

12  14   6 15.7863 5.84169  19

-6  14  12 21.3106 5.72317  21

-6  12 -14 20.1665 5.61843  20

-6  14 -12 21.7369 7.01750  20

-12  14   6 27.1630 6.35433  21

-14  12   6 9.31413 5.09426  21

14  12  -6 14.8713 6.20012  19

-14  12  -6 20.6502 5.18424  22

-6  14 -12 20.0750 5.63922  15

-6  12 -14 16.8878 5.59544  15

14   6 -12 23.7774 7.22674  18

12  14  -6 17.5329 6.22541  18

6  12 -14 23.0085 4.42567  15

-12  14   8 2.60980 3.45882   9

-14  12   8 1.50672 3.57065   9

-14 -12  -8 3.47932 3.23654   8

-14  12   8-0.70920 3.36140  10

-14  -8 -12 7.56695 4.48293   8

-12  -8 -14 9.65780 4.66952   8

-12  -8 -14 5.23276 4.67642   7

-8 -12 -14 1.57309 3.72791   7

-8  12  14 1.85095 4.04839  30

-14   8  12 4.88719 3.15222  30

-12   8  14-0.80787 3.53400  30

8  12  14-0.81299 3.55642  29

8  14  12 4.70405 3.30096  29

-12  14   8 6.54860 3.32580  30

14   8 -12-0.78337 3.03165  27

12   8 -14 4.32816 4.02600  27

8  12  14 6.33653 3.75407  26

14  12   8 4.62242 2.88683  26

8  14  12 2.45146 3.24900  26

12  14   8 3.87319 3.17094  26

-8  14  12 8.50536 4.73100  13

-8  12  14-0.65787 2.93984  13

-14  12   8 0.89022 3.44507  13

-12   8  14 9.03541 4.30391  13

-14   8  12 0.90749 3.70182  13

-8  12 -14 2.35509 3.72072  24

-14  12  -8 0.81767 3.41784  24

-8  14 -12 0.81886 3.25579  24

-12  14  -8-4.43476 4.12516  24

-8  14 -12 0.60734 3.27746  23

-12   8 -14 0.92796 4.05928  22

12  14  -8 5.92520 4.08543  23

8  12 -14 7.21768 3.93921  23

8  14 -12 0.89765 3.56899  23

12  14  -8 4.08431 4.05966  19

-12  14  -8 0.85843 3.32208  22

-14   8 -12 2.35930 3.36465  22

-8  12 -14 2.70611 3.49079  22

-8  14 -12 5.44025 4.05161  22

-14  12  -8 1.45242 3.31207  22

8  12 -14 4.79925 3.79107  20

8  14 -12 2.54553 3.07165  20

-8  14  12 2.67910 2.99303  21

-12  14   8 4.31401 4.08928  21

-14  12   8 5.50822 3.99622  21

12   8 -14 3.10047 4.52084  18

14   8 -12 2.12779 3.75839  18

12  14  -8 3.78048 4.13432  18

12   8 -14 3.78364 2.36314  15

-10  14  12 43.4940 6.22456   9

-12  14  10 54.6607 6.63685   9

-14 -12 -10 39.3103 6.51137   7

-14 -10 -12 53.9607 7.39651   7

-12 -10 -14 63.4667 7.68494   7

-12  10  14 58.7468 6.80023  30

-10  14  12 52.0438 6.50166  30

-10  12  14 48.5023 6.82363  30

12  10 -14 53.2735 6.54885  27

14  10  12 44.3628 6.05789  26

12  10  14 43.9061 6.09849  26

10  12  14 48.4146 6.18475  26

12  14  10 41.4986 5.34157  26

-10  14  12 36.8172 5.62065  13

-12  14  10 59.3161 7.02036  13

-12  10  14 52.6920 6.50469  13

-14  10  12 48.8360 6.69975  13

-12  10 -14 45.4783 6.44194  24

-14  10 -12 56.8249 7.06333  24

-10  12 -14 51.2146 6.48048  24

-14  12 -10 43.7380 6.10627  24

-10  14 -12 49.0701 6.45941  24

14  12 -10 58.6311 7.14282  23

12  10 -14 51.0730 6.13957  23

12  14 -10 46.3965 6.49545  23

10  12 -14 45.1885 6.14246  23

12  14 -10 38.9661 6.05848  19

-12  10 -14 45.0312 6.76792  22

-10  12 -14 40.3903 6.36915  22

-10  14 -12 50.0732 6.89760  22

-12  14 -10 49.0146 6.56964  22

14  12 -10 63.6196 7.89338  19

12  10 -14 57.7106 7.19969  18

14  10 -12 49.8913 7.38167  18

14  12 -10 56.8357 7.46442  18

-14   0 -14 128.468 10.0043   7

-14   0 -14 124.173 12.1697   8

0  14  14 153.221 12.4573  29

0  14  14 139.374 10.1091  30

14  14   0 131.112 11.8870  28

0  14  14 115.876 9.07829  26

-14   0  14 96.8779 10.9021  25

14   0 -14 135.578 12.9227  12

0  14 -14 117.549 10.1821  23

-14   0 -14 124.350 10.2247  22

14  14   0 130.683 12.0474  19

0  14 -14 154.455 12.9692  20

-14  14   0 128.060 11.6987  21

0  14 -14 126.736 9.48336  15

14  14   0 126.449 11.2004  16

-14   2 -14 325.682 17.9118   8

-14  -2 -14 361.499 20.2701   8

-14  -2 -14 327.849 17.2061   7

-2  14  14 362.074 18.9389  29

-2  14  14 344.850 16.8988  30

14  14  -2 368.511 18.5964  28

14  14   2 326.395 17.8075  28

2  14  14 352.299 16.1875  26

-14   2  14 328.684 18.5785  25

-14  -2  14 330.343 18.4015  25

14  -2 -14 318.742 18.8033  12

14   2 -14 323.663 18.9564  12

-14  -2 -14 305.747 14.8990  14

-14  14   2 353.725 16.2694  13

2  14 -14 301.955 15.9918  23

-2  14 -14 334.341 15.7510  23

-14  -2 -14 327.353 15.5312  22

-14   2 -14 303.469 16.1189  22

14  14  -2 330.979 19.1041  19

2  14 -14 319.053 18.2473  20

14  14   2 380.168 19.0514  19

-14  14   2 334.298 18.2888  21

-14  14  -2 366.850 17.6900  21

14  14   2 347.956 17.9497  16

14  14  -2 324.400 19.2854  18

-2  14 -14 358.960 16.1315  15

2  14 -14 327.370 13.8895  15

14  14  -2 338.283 17.3303  16

-14  14   4 6.49851 3.92046   9

-14   4 -14 1.33963 3.05468   8

-14  -4 -14 2.06939 4.22047   8

-14  -4 -14 0.90418 3.95506   7

4  14  14-1.67470 3.49989  29

14  14  -4 1.58114 3.22473  28

-4  14  14 2.48743 3.70485  30

14  14   4 3.06102 2.87787  28

-4  14  14-0.86584 4.02681  29

4  14  14-2.12557 3.35795  26

14  -4 -14 2.63958 4.01252  12

14   4 -14-0.88146 3.68426  12

-14  14   4 5.11580 3.82920  13

4  14 -14 6.10323 3.47918  23

-4  14 -14 1.10378 2.75712  23

-14   4 -14 1.50885 3.15329  22

-14  -4 -14 0.56606 2.73203  22

14  14  -4 1.73302 2.47139  23

-4  14 -14 1.28899 3.16562  22

14  14  -4 5.14575 4.78628  19

4  14 -14 0.86786 3.16627  20

-4  14 -14 4.56073 4.55677  20

14  14   4 0.77653 3.24568  19

-14  14   4-1.83852 4.02102  21

14  14   4 3.36766 3.99011  16

-4  14 -14 0.69102 2.81869  15

-14  14   6 299.426 14.5893   9

-14  -6 -14 285.871 15.8846   7

-14  -6 -14 303.540 16.2958   8

6  14  14 275.491 14.1074  29

-6  14  14 284.435 15.0796  30

14   6 -14 276.590 14.3848  27

14  14  -6 247.017 12.6434  28

6  14  14 274.331 13.7047  26

14   6 -14 251.012 13.2182  12

-14  14   6 298.539 14.7979  13

-14   6 -14 275.833 14.1257  22

14  14  -6 250.344 12.8807  23

6  14 -14 274.302 14.1484  23

-6  14 -14 261.016 13.8533  22

14  14  -6 266.254 15.9766  19

6  14 -14 276.530 14.3270  20

-14  14   6 266.841 14.6413  21

14  14   6 267.378 14.4490  16

-6  14 -14 289.880 14.0709  15

14  14  -6 273.041 15.7504  18

14   6 -14 262.651 15.8343  18

-1  15   1 4.67520 3.95729   9

-15   1   1 5.77365 6.31390  10

-15  -1   1-1.31089 4.78279  10

-15   1  -1 8.71732 6.21565  10

-15  -1  -1 6.70178 5.32901  10

-15  -1   1 6.19656 6.31900   6

-15  -1  -1 3.06181 5.58542   6

1  15  -1 2.72389 5.69267  30

-1  15  -1 8.21162 6.24153  30

1  15   1 8.05518 6.47955  30

-1  15   1 1.37093 5.59214  30

-1  -1  15 1.39447 5.08768  25

1   1 -15 3.19048 3.24083  27

1  -1  15 1.36926 5.58533  25

1  15   1 6.20003 4.93008  26

-15   1   1 1.32764 4.53107  14

-15   1  -1 2.73254 4.98482  14

-15  -1  -1 4.03799 5.35143  14

-15  -1   1 2.53293 4.62073  14

1  -1 -15 1.47538 5.70934  12

1  15  -1 1.04551 4.04605  23

1  15   1 5.09828 3.46632  23

-1  15  -1 4.39475 4.90945  23

-1  15   1 2.75105 3.64611  23

-1  15  -1 2.95414 4.40024  19

1  15  -1 4.75588 4.72719  19

-1  15   1 2.29926 4.57081  19

1  15   1 3.94771 5.23180  19

-1  15  -1-0.88350 3.86492  16

-1  15   1 2.44452 3.93296  16

1  15  -1 6.68042 5.07779  16

1  15   1 1.05690 3.97489  16

-1   1 -15 2.11269 4.19997  15

-1  15   3 239.946 14.3320   9

-3  15   1 280.235 16.7292   9

-3  -1 -15 308.301 21.2227   8

-3   1 -15 264.354 20.7673   8

-3  15  -1 257.575 16.2821   9

-15   1   3 267.111 19.7597  10

-15   3   1 308.796 21.8587  10

-15   3  -1 274.301 20.5610  10

-15  -1   3 261.402 18.4845  10

-15  -3   1 261.199 17.4430  10

-15  -3  -1 304.550 18.9618  10

-15  -1  -3 275.936 19.6715  10

-15   1  -3 250.260 19.5361  10

-15  -3   1 245.779 19.0607   6

-15   3   1 236.319 18.7533   6

-15  -3  -1 265.658 19.9655   6

-15   3  -1 287.023 20.4865   6

-15  -1  -3 267.858 20.6501   6

1  15  -3 245.435 19.0351  30

3  15  -1 253.513 18.5269  30

3  15   1 276.290 18.8615  30

-3  15  -1 261.533 19.0228  30

1  15   3 265.243 18.8809  30

-1  15   3 276.167 19.5025  30

3   1 -15 243.817 14.2535  27

1  15   3 252.717 16.1538  29

-1  15   3 265.763 17.3812  29

3  15   1 246.440 18.3966  28

1  -3  15 255.570 18.6951  25

1   3  15 266.587 18.9559  25

-1  -3  15 284.558 19.5346  25

-1   3  15 272.169 19.4414  25

-3  -1  15 269.602 20.0946  25

1   3 -15 262.661 14.8442  27

3  15   1 289.298 18.2270  26

-1  15   3 291.644 19.5220  26

3  15  -1 277.293 17.3048  26

-15  -3  -1 273.535 18.9636  14

-15  -1  -3 289.489 19.8304  14

-1  15   3 276.712 19.6595  13

1  -3 -15 280.962 19.7908  12

1   3 -15 268.623 19.7827  12

3  -1 -15 273.237 20.3179  12

-3  15  -1 267.292 19.7443  22

3  15  -1 283.840 16.9153  23

1  15  -3 269.997 18.1370  23

3  15   1 276.686 14.9682  23

-1  15  -3 239.745 17.5902  23

-1   3 -15 257.932 17.3031  22

1   3 -15 260.330 15.5410  22

-3  15  -1 245.942 17.2438  23

-3  15   1 262.647 16.3472  23

-1  15  -3 297.224 19.4254  22

3  15  -1 274.126 19.2867  19

1  15  -3 260.237 16.7786  19

1  15  -3 268.402 16.4725  20

3  15   1 259.669 19.6269  19

-1  15  -3 271.687 17.7395  20

-1  15  -3 266.622 15.1748  19

1  15   3 282.904 19.9500  19

-15   3   1 270.117 19.3324  21

-1  15   3 280.879 19.2021  19

3  15  -1 257.968 18.6551  16

-1  15   3 268.292 14.6396  16

3  15   1 271.764 18.6915  16

-1   3 -15 241.175 17.1134  15

1  15   3 260.228 16.3237  16

-15  -1   3 247.149 17.3297  14

15   1  -3 252.512 15.7895  18

15   3  -1 248.070 16.3497  18

-15  -3   1 237.066 17.1520  14

-15   1   3 267.657 18.4355  14

1  15  -3 304.549 19.0763  16

-3   1 -15 264.596 16.4525  15

-3  -1 -15 244.482 14.7960  15

-15   3   1 301.221 19.9212  14

-3  15   3-0.99583 4.06187   9

-3  -3 -15 1.42139 5.94087   8

-15   3   3-1.55023 4.89795  10

-15  -3   3 2.23587 4.67253  10

-15   3  -3 3.07930 6.73461  10

-15  -3  -3 1.25651 5.12518  10

-3  -3 -15 6.11131 6.23184   7

-15  -3   3 4.54663 4.98387   6

-15   3   3-6.11428 6.23486   6

-15  -3  -3-1.47360 5.70221   6

-15   3  -3 1.50164 4.74441   6

3  15  -3 4.07458 5.94090  30

-3  15  -3 2.67983 5.98699  30

3  15   3-1.21682 5.20550  30

3  15   3-2.44661 4.46294  29

-3  -3  15 1.39103 4.39494  25

-3   3  15 2.81620 5.29523  25

3   3 -15 0.94961 3.96901  27

3  -3  15 1.31600 5.23191  25

3  15   3 3.70277 4.90692  26

3   3  15 2.70991 5.52672  25

-15  -3   3 2.15922 4.51236  14

-15   3  -3-1.35256 5.23383  14

-3  15   3 1.37629 5.17561  13

3  -3 -15-1.43739 4.90531  12

3   3 -15-2.93650 6.56044  12

-3  15  -3 1.27444 4.79258  23

-3  15   3 4.68229 3.69841  23

-3   3 -15-3.79750 4.76023  22

3  15  -3-1.16799 4.26114  23

-15   3   3-1.28140 5.35574  21

-3  15  -3-5.30490 5.80106  22

3  15   3-1.54012 4.65884  19

3  15  -3 1.25259 4.56980  19

3  15  -3 1.61597 3.29569  20

3  15  -3 4.03299 5.61879  16

-3   3 -15-1.13966 3.88925  15

15   3  -3 1.11257 4.18389  18

-5  -1 -15 322.196 22.3164   8

-5  15   1 296.164 18.4832   9

-5  15  -1 280.848 18.2584   9

-15  -1   5 321.027 20.1514  10

-15  -5   1 277.728 16.6743  10

-15  -5  -1 288.863 17.1296  10

-15   1  -5 343.538 22.3624  10

-15  -1  -5 298.436 20.6172  10

-5  -1 -15 332.512 21.8601   7

-15   1   5 315.120 21.2839  10

-1  15   5 315.131 16.2850   9

-15  -5   1 301.479 20.0042   6

-15   5   1 312.467 20.5949   6

-15  -5  -1 297.232 20.0198   6

-15   5  -1 327.962 21.1305   6

-15  -1  -5 315.315 22.2638   6

1  15  -5 283.336 20.2562  30

-1  15  -5 351.901 21.7066  30

5  15  -1 320.463 20.1200  30

5  15   1 283.269 18.3110  30

-5  15  -1 288.072 19.5480  30

-5  15   1 313.251 20.8165  30

1  15   5 356.111 21.2996  30

1  15   5 328.850 19.2244  29

-1  15   5 326.607 21.0961  30

-1  15   5 293.811 19.2319  29

5  15   1 265.932 19.5898  28

1  -5  15 298.930 19.5999  25

1   5  15 327.889 20.2478  25

-1  -5  15 344.628 21.1254  25

-1   5  15 316.831 20.2304  25

-5  -1  15 341.268 22.0933  25

1   5 -15 281.121 16.9019  27

1  15   5 303.775 19.8422  26

5  15   1 314.461 18.4966  26

-1  15   5 298.525 20.2760  26

5  15  -1 261.866 16.1479  26

5  -1 -15 314.162 22.0845  12

-15  -5  -1 314.341 19.6200  14

-1  15   5 287.582 19.5516  13

-5  15   1 296.225 20.4438  13

15  -1  -5 296.835 22.4118  12

-5  15  -1 303.149 20.8883  22

1  15  -5 311.268 17.7900  22

5  15  -1 290.413 16.9863  23

1  15  -5 336.422 21.2326  23

-1  15  -5 342.795 21.2858  23

-5  15  -1 310.891 19.4567  23

-1   5 -15 304.534 17.9758  22

-5  15   1 324.295 18.5763  23

-1  15  -5 297.368 18.6744  22

5  15  -1 308.553 21.7208  19

1  15  -5 302.152 18.6619  20

1  15  -5 292.154 16.9686  19

5  15   1 276.445 21.1211  19

-1  15  -5 294.428 19.5460  20

-15   5   1 284.089 20.6799  21

-15   5  -1 298.475 20.7633  21

1  15   5 367.755 23.5242  19

5  15  -1 322.929 21.4682  16

5  15   1 300.590 20.7125  16

-15  -5   1 276.210 17.9336  14

1   5 -15 328.581 20.6535  15

15   1  -5 244.714 16.8638  18

15   5  -1 335.830 19.5390  18

-15   1  -5 322.984 20.8918  14

15   5   1 321.951 18.9576  18

-5  -1 -15 296.383 15.3801  15

-5   1 -15 318.719 17.5690  15

-15   5  -1 319.454 20.9641  14

-1   5 -15 299.509 19.7988  15

-5  -3 -15 1.50139 6.12523   8

-15   3  -5 6.62833 4.93762   8

-3  15   5 4.02682 4.68343   9

-5  15   3 11.6510 5.31463   9

-3  -5 -15 10.3441 5.77875   8

-5   3 -15 1.50093 6.27451   8

-15   3   5 1.56917 4.95930  10

-15  -3   5 9.79366 5.34616  10

-15   5  -3 18.2645 7.34668  10

-15  -5  -3 10.5217 4.70289  10

-15  -3  -5 6.54526 5.34087  10

-15  -3  -5 5.93951 5.90455   6

-15   3  -5 9.12504 6.93661   6

-3  -5 -15 4.60396 6.41542   7

-15  -5   3 9.56614 6.47775   6

-15   5   3 4.23686 5.90408   6

-15  -5  -3 1.34283 5.19760   6

-15   5  -3 5.53549 5.50308   6

5  15  -3 5.42118 5.09812  28

5  15   3 6.58215 5.37096  28

-3   5  15 7.10731 4.51317  29

-3  15  -5 9.16018 5.20390  30

-5  15  -3 5.03559 5.62633  30

5  15   3 5.29202 4.63120  30

3  15   5 6.88141 5.01817  30

3  15   5 9.66105 4.98605  29

-5  15   3 17.9823 7.02547  30

-3  15   5 11.2323 6.65517  30

-3  15   5 12.2299 6.32085  29

-3  -5  15 5.20206 5.56491  25

-3   5  15 11.7742 5.84676  25

3   5 -15 8.73039 5.54315  27

-5  -3  15 8.47615 6.31337  25

-5   3  15 15.7395 7.26720  25

5  15   3 9.22099 5.46392  26

3  -5  15 6.18522 6.77071  25

3   5  15 3.78527 4.88399  25

-3  15   5 9.19065 5.35677  26

15   3  -5 6.17402 6.75258  12

15  -3  -5 7.88164 7.47160  12

-15   5  -3 5.15317 5.12320  14

-15  -5   3 6.59909 4.46948  14

-15   3  -5 11.6686 5.79436  14

15   5  -3 15.5026 7.38508  12

15  -5  -3 18.7583 7.78688  12

-3  15   5 4.05235 5.37158  13

-5  15   3-1.39632 5.55255  13

3  -5 -15 20.8128 7.31460  12

3   5 -15 4.08914 4.48405  12

5  -3 -15 4.39121 5.66536  12

5   3 -15 9.04180 6.87336  12

-3  15  -5 4.05995 4.62000  23

-5  15  -3 2.60355 5.44228  23

-15   5  -3 4.98193 3.49776  24

-5  15   3 9.52737 5.05971  23

-5   3 -15 12.6796 7.03905  22

-3   5 -15 6.15109 5.49821  22

5  15  -3 3.38976 5.45460  23

3  15  -5 10.3861 5.92176  23

-15   3   5 6.91631 5.56460  21

-3  15  -5 6.50077 6.16295  22

-5  15  -3 2.79511 5.70179  22

-3   5 -15 5.10680 4.65934  20

5  15  -3 11.3155 6.32114  19

3  15  -5 3.36310 4.45846  19

3  15  -5 4.83406 4.58358  20

-5  15  -3 7.42933 4.64085  21

-3  15  -5 6.79591 6.19952  20

-15   5   3 4.03087 4.90342  21

-3   5 -15 6.24842 4.70108  15

5  15  -3 10.1809 6.22311  16

15   3  -5 5.05911 5.16033  18

15   5  -3 9.09424 5.68407  18

5  15  -3 10.0643 5.10109  18

15   5   3 5.45148 4.97362  18

-5   3 -15 13.1546 5.74486  15

-5  15   5 6.95036 5.28616   9

-15   5   5 14.2964 6.79822  10

-15   5  -5 10.5281 7.76225  10

-5  -5 -15 9.69533 5.92832   8

-15  -5  -5 8.82377 5.03360  10

-15  -5  -5 22.7244 7.41853   6

-15   5  -5 5.52456 5.63680   6

-5  -5 -15 18.9847 8.03628   7

5  15   5 5.89796 5.27416  28

-5  15  -5 14.1707 6.28318  30

5  15   5 10.4729 5.35642  30

5  15   5 13.4990 4.69752  29

5  15  -5 14.9463 6.22511  28

5   5 -15 8.28986 5.51096  27

-5   5  15 11.7538 6.63480  25

-5  -5  15 11.6455 6.67879  25

5  15   5 12.1231 5.74865  26

15   5  -5 9.67581 5.64136  12

15  -5  -5 4.22704 6.92323  12

-15   5  -5 14.2192 5.72196  14

-5  15   5 20.7635 7.14445  13

5  -5 -15 11.8774 7.12361  12

5   5 -15 19.2605 7.42584  12

-5  15  -5 5.39385 5.50359  23

-5  15  -5 14.7818 6.93590  24

5  15  -5 10.1571 6.02020  23

-5   5 -15 16.4158 6.60499  22

5  15   5 3.22722 6.41797  19

-5  15  -5 16.5395 6.41284  22

5  15  -5 5.19730 4.43831  19

-5   5 -15 11.6193 4.48244  20

-15   5   5 7.33137 5.68586  21

15   5  -5 8.53087 5.94574  18

5  15  -5 15.0286 5.85438  18

-5   5 -15 12.0665 6.22858  15

-7  -1 -15 3.16325 6.12029   8

-15   1  -7 2.75190 5.32443   8

-7  15   1-1.29101 5.76857   9

-7  15  -1 2.58804 5.00741   9

-15   7   1 3.26542 3.79672   9

-15   1   7 1.45001 5.91451  10

-15  -1   7 1.27421 5.06585  10

-15   7   1 2.97920 5.43455  10

-15   7  -1 1.45798 6.23729  10

-15   1  -7 4.56588 5.55261  10

-15  -1  -7 1.45753 5.14870  10

-15  -1  -7 1.55966 4.92785   6

-7  -1 -15 2.90110 5.91672   7

-7   1 -15-1.30670 5.05647   7

-15  -7   1 2.29351 4.79311   6

-15   7   1 1.18339 4.18036   6

-15  -7  -1 4.57270 5.10803   6

-15   7  -1 5.88338 4.91816   6

7  15   1-1.38872 5.22245  28

7  15   1 5.74767 4.54004  30

-7  15  -1 1.18496 4.45622  30

-7  15   1 1.25548 5.24752  30

1  15   7 3.62594 4.40958  29

1  15   7 3.63247 5.41029  30

-1  15   7 1.31871 5.76828  29

-1  15   7 1.32444 5.12511  30

1  -7  15-2.24045 5.10870  25

1   7  15 7.68191 5.29645  25

-1  -7  15 2.24097 4.79350  25

-1   7  15 5.54133 4.95205  25

1   7 -15 6.60770 4.37839  27

-7  -1  15-1.47181 5.02285  25

1  15   7 2.60828 5.45090  26

7  15   1 6.46204 4.45542  26

-1  15   7 10.3529 5.53625  26

7  15  -1-0.74353 2.71280  26

-15  -7   1-0.95364 3.98597  14

-15   1  -7 2.62644 4.63896  14

-15  -7  -1 1.12339 4.58229  14

-7  15  -1 10.0574 5.84678  13

-1  15   7-1.19486 4.62372  13

-7  15   1-1.33908 5.32377  13

-15   7   1 0.83449 3.31776  13

15  -1  -7-1.63942 6.68708  12

7  -1 -15 3.11176 6.80569  12

-1  15  -7-1.38957 5.06964  23

-7   1 -15-1.50093 5.64443  22

-7  15  -1 2.46680 4.20928  23

-7  15   1 2.21212 4.28010  23

-1   7 -15 1.92325 4.01936  22

7  15  -1 0.87923 3.58643  23

1  15  -7 5.53831 5.35782  23

15   7   1 4.13155 4.21315  19

-1  15  -7-4.42232 5.23971  22

1  15  -7 2.72466 4.22393  22

7  15  -1 1.58789 5.01702  19

1  15  -7 1.24136 4.52893  20

-1  15  -7 3.99687 4.86065  20

-7  15   1-1.35152 4.93080  21

-7  15  -1 2.39199 5.34404  21

-15   7   1 2.85996 5.68512  21

-1   7 -15 1.32533 5.26910  15

7  15   1 1.46834 5.18689  16

15   7  -1 6.77747 6.05670  18

-7   1 -15 2.58041 3.84340  15

15   7   1 7.61624 6.54932  18

7  15  -1 1.38170 4.71537  18

-3  -7 -15 173.266 16.4473   7

-7  -3 -15 135.416 14.9462   7

-7  15   3 166.980 14.6009   9

-7   3 -15 202.135 17.1782   8

-15   7   3 159.130 11.7941   9

-3  -7 -15 191.683 14.6615   8

-15  -3   7 145.579 12.9027  10

-15   7   3 169.662 16.4094  10

-15   7  -3 173.447 15.6468  10

-15  -3  -7 160.133 14.9673  10

-15   3  -7 171.828 14.6481   8

-7  -3 -15 193.100 17.6166   8

-15  -7   3 159.283 13.8298   6

-15   7   3 131.294 13.4596   6

-15  -7  -3 168.608 14.1991   6

-15   7  -3 134.385 13.0671   6

-15  -3  -7 178.126 16.4916   6

-15   3  -7 153.253 15.5719   6

7  15   3 165.361 11.9620  30

-3   7  15 148.901 12.8202  29

-7  15  -3 182.571 14.2565  30

3  15   7 169.645 13.7965  29

3  15   7 163.328 13.4197  30

-7  15   3 174.958 15.1624  30

-3  15   7 183.004 15.9692  30

-3  15   7 156.227 14.9337  29

7  15  -3 210.412 16.7683  28

7  15   3 166.881 15.1573  28

3  -7  15 155.944 13.6869  25

3   7  15 156.997 13.6272  25

3   7 -15 161.691 14.2218  27

-3  -7  15 159.749 13.7657  25

-3   7  15 115.906 12.3981  25

-7   3  15 153.638 15.2751  25

-7  -3  15 192.074 16.7086  25

-15   7  -3 149.374 11.4061  24

3  15   7 178.232 15.1432  26

7  15   3 159.423 13.4754  26

-3  15   7 146.401 13.8863  26

7  -3 -15 177.326 16.2244  12

7   3 -15 154.232 15.6074  12

15   7  -3 120.035 12.8677  12

-3  15   7 155.720 14.2919  13

15   3  -7 164.137 16.3443  12

15  -3  -7 148.566 15.7105  12

15  -7  -3 150.676 13.8629  12

7  15  -3 162.930 13.4217  23

3   7 -15 140.236 10.6363  23

3  15  -7 143.334 14.6787  23

-3  15  -7 170.697 15.1142  23

-7   3 -15 173.458 16.0697  22

-3  15  -7 146.464 13.9341  22

-7  15  -3 148.283 14.3595  23

-7  15   3 154.632 12.4209  23

-3   7 -15 148.543 13.5098  22

7  15  -3 145.644 15.7796  19

-3   7 -15 165.695 14.0972  20

3  15  -7 137.394 11.9242  19

3  15  -7 149.088 13.2343  20

-3  15  -7 184.879 16.3964  20

-7  15   3 141.915 15.1646  21

7  15   3 201.076 18.0861  19

-7  15  -3 142.878 12.3428  21

-15   7  -3 145.006 14.8667  21

-15   7   3 123.562 13.6563  21

3   7 -15 178.005 15.1982  15

-15   3  -7 143.954 13.4472  14

15   7  -3 142.816 15.0290  18

-3  15  -7 136.421 11.0239  15

7  15  -3 159.667 14.7909  18

-7   3 -15 137.419 12.6480  15

-3   7 -15 167.732 14.9002  15

-7  15   5 233.285 16.9373   9

-15   7   5 228.354 13.8305   9

-5  -7 -15 213.909 16.1899   8

-15   5   7 213.708 18.4521  10

-15   7   5 242.719 19.5511  10

-15   7  -5 263.323 18.7373  10

-15   5  -7 243.327 19.0298  10

-5  -7 -15 211.004 18.3805   7

-7  -5 -15 239.175 19.6472   7

-7  -5 -15 255.930 18.8973   8

-15  -7   5 208.577 15.7998   6

-15   7   5 216.957 16.2626   6

-15  -7  -5 235.678 16.2234   6

-15   7  -5 221.129 16.2270   6

-15  -5  -7 248.851 17.9622   6

-15   5  -7 235.150 18.0143   6

-7  15  -5 222.794 14.8156  30

5  15   7 218.420 14.4179  29

-5   7  15 196.245 13.4901  29

-7  15   5 239.250 17.7249  30

7   5 -15 267.676 18.0224  27

7  15  -5 212.754 16.6720  28

7  15   5 195.120 15.2836  28

-15   7  -5 213.446 14.3687  24

5   7 -15 253.720 17.5333  27

-5   7  15 236.385 16.4773  25

-5  -7  15 234.314 16.4164  25

-7   5  15 220.088 17.1842  25

-7  -5  15 215.922 17.0084  25

7  15   5 214.441 15.4988  26

5  -7  15 207.658 15.3562  25

5   7  15 250.680 16.5701  25

7  -5 -15 215.800 17.3780  12

7   5 -15 234.798 18.4370  12

-5  15   7 235.053 18.0438  13

15   5  -7 220.474 17.4569  12

15  -5  -7 280.022 19.3085  12

-7  15   5 247.590 18.5041  13

15   7  -5 221.164 16.1425  12

15  -7  -5 255.837 17.0197  12

5  -7 -15 240.004 16.3441  12

5   7 -15 207.974 16.4040  12

-15   5  -7 200.204 13.0006  22

-7  15  -5 255.388 18.4014  24

5   7 -15 232.431 14.2571  23

7  15  -5 240.650 17.2869  23

5  15  -7 241.070 17.6884  23

-5  15  -7 252.055 17.6969  24

-5  15  -7 245.682 17.9889  22

-7  15  -5 256.378 18.1978  23

-7  15  -5 259.903 18.7529  22

-7   5 -15 246.006 18.7441  22

-5   7 -15 253.583 18.1519  22

5  15  -7 202.790 15.9428  19

-5   7 -15 211.581 14.8439  20

5  15  -7 254.690 15.6881  20

-5  15  -7 280.853 19.9802  20

7  15   5 260.077 20.2657  19

-15   7   5 213.210 16.9378  21

-15   5   7 220.716 15.6379  21

5  15   7 207.686 18.1938  19

7  15  -5 225.511 17.8742  19

-15   5  -7 228.594 15.8277  14

15   5  -7 228.894 19.0771  18

15   7  -5 226.869 18.7625  18

5  15  -7 184.114 13.8587  18

7  15  -5 233.718 17.0205  18

-7   5 -15 246.859 17.1137  15

-5   7 -15 244.986 17.7506  15

7  15  -5 236.541 18.6467  16

-7  -7 -15 6.00231 5.25099   8

-7  15   7-1.17504 3.86414   9

-15   7   7 2.93491 3.47734   9

-15   7   7-1.45979 4.98175  10

-15   7  -7-1.25980 5.00849  10

-15  -7  -7 3.06415 4.26901   6

-15   7  -7-1.06384 3.63053   6

-7  -7 -15-1.49216 5.77405   7

-15  -7   7 1.08368 4.84214   6

-15   7   7-2.19886 4.25434   6

7  15   7 0.69955 3.25339  29

-7  15   7 1.27874 4.66522  30

7   7 -15 3.67506 5.35841  27

7  15   7-1.12292 3.96667  26

7  -7  15-0.94364 4.30335  25

7   7  15 1.92182 4.38209  25

-7   7  15 2.03751 4.73789  25

-7  -7  15 1.99682 4.36718  25

15  -7  -7-1.03207 4.41519  12

15   7  -7-2.12032 4.63728  12

-7  15   7 3.92613 4.77455  13

7  -7 -15 2.02756 4.71477  12

7   7 -15 5.38116 5.00520  12

-7   7  15 0.84958 4.10029  13

-7  15  -7 2.55715 5.34396  24

-7   7 -15 1.31279 5.86581  22

7   7 -15 2.56821 3.40343  23

7  15  -7-1.24183 4.38669  23

7  15  -7 2.48451 4.53210  19

-15   7  -7 0.78448 3.57751  22

-7  15  -7 1.31866 5.24248  22

7  15   7 2.89390 5.59910  19

-7   7 -15 3.58431 2.99625  20

-15   7   7 1.04259 5.12081  21

15   7  -7 2.96541 5.73745  18

-7   7 -15 2.34076 5.00687  15

7  15  -7-3.03456 4.51969  18

-9  -1 -15 9.35371 7.11582   8

-9   1 -15 17.9843 7.61666   8

-15  -1  -9 13.4221 6.24063   8

-15   9   1 16.6047 5.32991   9

-15   1  -9 26.9133 7.86464   8

-15  -1   9 16.6075 6.22268  10

-15   9   1 17.2198 6.51303  10

-15   9  -1 11.4820 6.16463  10

-15   1  -9 11.7773 6.72040  10

-15  -1  -9 22.3830 7.94165   6

-15   1  -9 18.5864 5.82899   7

-9  -1 -15 19.0881 7.67174   7

-9   1 -15 10.6589 5.92418   7

1   9  15 20.7534 5.41557  30

-1   9  15 17.4401 5.62227  30

-1   9  15 16.7935 5.79716  29

-9  15  -1 17.7953 5.47821  30

-9  15   1 16.7508 5.89400  30

1  15   9 18.6073 6.70039  29

-1  15   9 15.8010 6.90571  29

1  15   9 11.0166 5.51183  30

-1  15   9 19.8935 6.00830  30

9  15   1 29.6520 7.58399  28

1   9  15 16.4458 4.97288  26

-9  -1  15 18.4657 7.77913  25

1  15   9 13.4015 5.56421  26

9  15   1 15.0628 4.44740  26

-1  15   9 23.5490 6.96638  26

9  -1 -15 18.2376 7.20910  12

-15   1  -9 15.1519 6.89599  14

-15  -9  -1 14.9994 5.34826  14

-1  15   9 16.0868 5.87961  13

-9  15  -1 20.0621 6.51618  13

15  -1  -9 29.7144 8.91301  12

-9  15   1 17.1937 6.72764  13

-15   9   1 8.13673 4.46308  13

1   9 -15 22.3168 5.30779  23

-1   9 -15 15.4133 4.76031  22

-9  15  -1 22.9284 6.61085  23

-9  15   1 15.5181 5.98865  23

-15   1  -9 20.6189 5.03225  22

15   9  -1 10.1913 5.70021  19

15   9   1 23.7511 7.22726  19

-1  15  -9 18.5064 5.76531  22

-9  15  -1 12.8909 6.96235  22

-1   9 -15 20.2225 7.87926  20

1  15  -9 23.0986 7.02905  20

-1  15  -9 16.1376 6.61215  20

-9  15   1 22.4168 6.91557  21

-9  15  -1 17.7100 6.28639  21

9  15   1 28.4834 8.54385  19

-15   9   1 26.4925 7.74162  21

-15   9  -1 26.0464 8.01170  21

1   9 -15 19.4236 5.97031  15

15   9  -1 17.6943 5.27727  16

15   9   1 12.8502 5.36903  16

-1  15  -9 12.5683 3.92173  15

9  15   1 23.1009 8.12326  16

15   9  -1 17.2690 7.43106  18

15   9   1 16.5172 6.76735  18

9  15  -1 14.4812 6.34151  18

9  15  -1 21.6073 7.55342  16

-1   9 -15 13.8326 5.50885  15

-9   3 -15 257.878 19.2940   8

-15   9   3 262.911 15.8413   9

-15  -3   9 233.114 15.3967  10

-15   9   3 275.033 19.6098  10

-15   9  -3 271.134 18.3229  10

-15   3  -9 266.060 17.6055   8

-9  -3 -15 299.130 20.8636   7

-9  -3 -15 284.386 21.0782   8

-15  -3  -9 264.674 19.3153   6

-15   3  -9 271.626 19.7203   6

-9  15  -3 250.771 14.6528  30

-3   9  15 268.109 17.4056  29

3  15   9 311.520 18.4798  29

3  15   9 214.304 14.5785  30

-9  15   3 262.470 17.4141  30

-3  15   9 262.712 18.8200  30

-3   9  15 275.172 18.0343  30

9  15  -3 243.952 17.9322  28

9  15   3 261.447 18.1964  28

3   9 -15 253.139 17.9642  27

3   9  15 307.569 16.6777  26

-9   3  15 287.632 19.6884  25

-9  -3  15 226.863 17.9139  25

3  15   9 280.184 18.2012  26

9  15   3 243.946 14.7972  26

-3  15   9 263.993 16.8220  26

-15   9  -3 221.699 13.9383  24

9  -3 -15 262.891 19.5229  12

9   3 -15 257.802 19.7886  12

15  -3  -9 259.478 19.8212  12

15   3  -9 254.574 19.2162  12

-3  15   9 260.693 17.2555  13

-9  15   3 293.449 19.3059  13

-15   9   3 257.446 16.2126  13

-3   9 -15 285.493 17.1580  22

9  15  -3 282.983 17.0036  23

3   9 -15 249.675 14.7039  23

3  15  -9 262.257 18.9153  23

-3  15  -9 283.712 19.1901  23

-3  15  -9 267.711 17.9271  22

-9  15  -3 286.224 19.1887  23

-9  15  -3 257.909 18.6338  22

-15   3  -9 267.464 14.8254  22

9  15  -3 298.080 20.9563  19

-3   9 -15 285.211 18.9483  20

15   9   3 258.457 15.8526  19

3  15  -9 297.139 18.5888  20

9  15   3 238.089 19.6155  19

-9  15   3 254.585 18.8164  21

-9  15  -3 245.540 15.7537  21

-15   9   3 238.576 18.1522  21

-3  15  -9 295.310 20.0459  20

-15   9  -3 270.864 18.7772  21

-15   3  -9 256.545 16.1048  14

15   9  -3 255.174 19.5259  18

-3  15  -9 232.296 14.3249  15

9  15  -3 247.696 18.4555  18

-9   3 -15 252.037 15.5078  15

3   9 -15 283.485 18.1285  15

9  15  -3 257.309 19.1451  16

-15   9   5 221.323 14.0051   9

-15   9   5 266.377 18.6611  10

-15   9  -5 188.786 14.7839  10

-15  -5  -9 177.994 16.8815   8

-15   5  -9 214.764 17.1571  10

-9  -5 -15 211.222 17.3667   8

-5  -9 -15 181.930 16.0233   7

-15  -5  -9 220.257 16.4744   6

-15   5  -9 247.903 17.5548   6

15   9  -5 231.706 15.9023  28

15   9   5 244.803 15.7313  28

5  15   9 231.853 15.1970  29

9   5 -15 215.170 16.1628  27

-5   9  15 207.267 14.4726  29

-9  15   5 243.178 16.4245  30

-5  15   9 221.009 16.9671  30

-5  15   9 221.941 17.1427  29

-5   9  15 223.884 16.3408  30

9  15  -5 197.167 15.3630  28

9  15   5 232.719 15.8605  28

-5  15  -9 263.787 17.0979  24

5   9 -15 236.151 16.9205  27

-9   5  15 228.423 16.8397  25

-9  -5  15 219.025 16.1040  25

5  15   9 228.948 16.4711  26

9  15   5 212.298 14.2783  26

-15   9  -5 204.081 13.9757  24

9  -5 -15 204.333 15.7185  12

9   5 -15 232.400 17.2823  12

15  -5  -9 250.195 17.9633  12

15   5  -9 237.431 17.4192  12

-5  15   9 199.232 15.6045  13

-15   9   5 209.899 15.4199  13

-5   9 -15 218.329 15.9556  22

-15   5  -9 195.961 13.4110  22

9  15  -5 244.699 16.1890  23

5   9 -15 221.007 14.1161  23

5  15  -9 220.368 17.2239  23

-5  15  -9 256.714 17.5810  22

-15   9  -5 215.556 12.9496  22

-5  15  -9 206.928 15.8954  23

-9  15  -5 235.620 16.7300  23

-9   5 -15 214.342 17.2283  22

-9  15  -5 227.872 17.0224  22

5  15  -9 210.024 14.1748  19

5  15  -9 192.732 14.3325  20

-5   9 -15 213.013 15.0805  20

-5  15  -9 227.463 17.6207  20

-9  15   5 189.512 16.1269  21

9  15   5 232.175 18.0464  19

-15   9   5 220.661 16.7694  21

9  15  -5 229.963 18.0342  19

5   9 -15 237.773 15.9172  15

15   5  -9 235.022 18.5239  18

15   9  -5 226.853 18.0202  18

9  15  -5 178.224 15.4724  18

-9   5 -15 210.931 14.7637  15

-5   9 -15 231.812 17.1388  15

-15   5  -9 205.147 13.1813  14

-9  -7 -15 17.0525 6.23098   8

-15  -9  -7 12.6165 6.61953   8

-15  -7  -9 17.2939 6.31427   8

-15   9   7 19.2061 5.20816   9

-7  -9 -15 21.7787 5.92809   8

-15   9   7 17.3312 6.68887  10

-15   9  -7 20.8232 6.29446  10

-15  -7  -9 21.5449 5.74199   6

-15   7  -9 18.8319 5.57658   6

-9  -7 -15 25.8925 7.86874   7

-7  -9 -15 22.6310 7.52763   7

-7   9  15 11.5390 6.05585  30

15   9  -7 17.8688 4.92626  28

15   9   7 26.0511 5.55779  28

7  15   9 16.3966 4.77112  29

9  15  -7 18.8034 5.52324  28

-9  15   7 22.5827 6.21298  30

9  15   7 22.6195 5.42905  28

-9   7  15 20.6987 5.98574  25

-9  -7  15 27.2111 6.21115  25

7   9 -15 25.1087 7.22032  27

9  15   7 19.7187 5.75560  26

15  -7  -9 17.9196 5.73097  12

15   7  -9 12.9863 5.36212  12

-7  15   9 14.6781 6.10236  13

-9  15   7 31.2573 7.19863  13

-7   9  15 19.3119 4.75498  13

9  -7 -15 18.4071 5.49187  12

9   7 -15 19.7659 5.76935  12

-15   9   7 23.7935 6.62630  13

-9   7  15 14.8988 4.87469  13

-9   7 -15 19.6548 6.73147  22

-7   9 -15 32.3217 7.30264  22

-15   9  -7 17.6692 5.30837  24

-7  15  -9 20.3160 6.40459  23

-7  15  -9 26.6756 6.50052  24

-9  15  -7 31.6162 7.40756  24

-9  15  -7 25.0592 6.82157  23

7   9 -15 22.0497 5.58863  23

9  15  -7 27.2788 6.83168  23

7  15  -9 24.3525 6.69839  23

9  15  -7 18.4202 6.14457  19

-15   7  -9 17.3985 5.00947  22

7  15  -9 14.5119 5.15698  19

-15   9  -7 19.4090 4.92212  22

-7  15  -9 20.0671 6.64589  22

9  15   7 12.4192 5.78625  19

-7  15   9 27.9884 6.90198  21

-9  15   7 14.5720 6.07635  21

-7   9 -15 18.1958 4.90201  20

-15   9   7 18.8146 5.93275  21

-15   7   9 17.7006 4.95541  21

-9   7 -15 32.5543 6.82732  15

-7   9 -15 17.8556 6.11702  15

7   9 -15 12.0074 4.70649  15

15   7  -9 25.7533 7.82651  18

15   9  -7 16.3237 6.45626  18

7  15  -9 20.0308 5.26987  18

9  15  -7 15.7784 5.76695  18

-9  -9 -15 15.4031 4.82116   8

-15   9   9 13.8849 3.91095   9

-15  -9  -9 12.6372 4.99624   8

-15   9   9 8.55796 5.43725  10

-9  -9 -15 16.6952 5.92375   7

-9  15   9 11.4184 5.06573  30

15   9  -9 17.7798 4.16753  27

9  15   9 16.4662 5.00448  26

-9  15   9 13.1192 5.60351  13

-9   9  15 14.6111 4.52507  13

-15   9   9 10.7913 4.90623  13

-15   9  -9 13.0568 4.89946  24

-9  15  -9 9.97589 5.15216  24

-9  15  -9 14.0098 5.11886  23

9   9 -15 7.54324 3.95896  23

9  15  -9 8.83703 4.48370  23

-9   9 -15 8.34822 4.66840  22

9  15  -9 16.9076 5.21631  19

-15   9  -9 12.6492 4.30574  22

-9  15  -9 18.5433 5.94699  22

-9  15   9 9.74285 4.70776  21

-15   9   9 17.0850 4.67009  21

-9   9 -15 16.9211 5.29040  15

9   9 -15 7.66791 3.87277  15

9   9 -15 18.1483 5.58307  18

15   9  -9 19.9260 6.23786  18

9  15  -9 11.8258 4.43861  18

-11  15   1 130.700 13.0261   9

-15  -1  11 123.168 12.0025  10

-15  11   1 116.826 11.7095  10

-15  11  -1 123.259 11.5683  10

-11  -1 -15 150.866 13.7285   7

-11   1 -15 151.674 12.7247   7

-15  -1 -11 166.751 15.0354   8

-15   1 -11 163.182 14.5331   8

-15  -1 -11 160.563 12.9250   7

-11   1 -15 156.571 14.7132   8

-15  -1 -11 182.277 16.1850   6

15  11   1 180.871 14.8115  28

1  11  15 141.488 13.4333  29

-1  11  15 150.125 13.2829  29

1  15  11 150.747 13.6571  29

1  15  11 148.492 11.7678  30

-1  15  11 140.071 12.7615  30

-1  11  15 149.371 12.0019  30

11  15   1 139.087 13.3872  28

1  11  15 121.185 9.95879  26

1  15  11 162.141 13.2624  26

-11  -1  15 149.273 14.3345  25

-1  15  11 140.042 11.9441  26

11  -1 -15 142.795 14.3931  12

-15  -1 -11 142.761 12.5961  14

15  -1 -11 144.661 14.5755  12

-11  15   1 143.922 12.4390  13

-15  11   1 128.439 10.2647  13

1  15 -11 165.375 14.2503  23

1  11 -15 131.613 10.4968  23

-1  15 -11 149.024 13.5446  23

-11  -1 -15 153.035 13.8908  22

-1  11 -15 126.159 9.90224  23

-11   1 -15 177.760 14.9273  22

-1  15 -11 143.287 10.8448  22

-15   1 -11 141.343 10.8898  22

15  11   1 113.706 12.0126  19

11  15  -1 147.238 14.8273  19

-1  11 -15 172.212 15.1618  20

1  15 -11 131.372 13.3876  20

11  15   1 167.289 15.3095  19

-1  15 -11 157.893 14.2080  20

-11  15   1 110.522 12.1895  21

-11  15  -1 140.239 12.7209  21

-15  11  -1 146.693 13.7999  21

15  11  -1 166.701 14.6064  19

15  11   1 155.825 12.5607  16

11  15   1 177.782 15.4638  16

15  11  -1 124.639 13.4033  18

-1  15 -11 133.787 10.0512  15

-1  11 -15 141.244 12.6066  15

1  11 -15 152.105 12.5123  15

-15   1 -11 127.812 11.3615  14

15  11  -1 125.831 11.1832  16

11  15  -1 139.747 13.6772  16

-11   3 -15 3.51917 4.66361   8

-11  15   3 1.16944 5.00284   9

-15  11   3-1.78498 4.07007   9

-15  11   3 1.00301 3.65926  10

-15  11  -3 4.10648 4.03391  10

-15   3 -11-1.97028 4.49258   8

-11  -3 -15 1.37906 4.87142   8

-15  -3 -11 1.13253 4.13179   7

-15  -3 -11-1.22278 4.98757   6

-15   3 -11 1.26495 5.15959   6

-11  -3 -15 2.51651 4.86892   7

11  15  -3 3.36687 4.57769  28

-3  11  15-2.05764 4.69176  30

11  15   3-1.09970 4.70447  28

15  11  -3-1.07531 3.92300  28

15  11   3 1.06686 4.12828  28

3  11  15 1.15630 4.94664  29

3  15  11-1.05932 4.42757  29

-11  15   3-0.77830 3.68857  30

-3  11  15-1.04750 5.14492  29

-3  15  11-1.13136 4.37787  30

-3  15  11 1.20346 4.65689  29

-11   3  15-1.19813 5.57207  25

-11  -3  15 1.17718 4.92018  25

3  11  15 3.19092 3.56442  26

3  15  11 1.03714 4.12328  26

11  -3 -15 4.99247 5.33942  12

11   3 -15-1.28203 5.09686  12

-15   3 -11 0.68747 2.94099  14

15  -3 -11 1.27216 5.31712  12

15   3 -11-2.51833 5.62619  12

-3  15  11 0.81264 3.92197  13

-11  15   3-2.15231 5.10016  13

-15  11   3 1.72797 3.43487  13

-3  15 -11 1.08787 4.32495  23

-11   3 -15 2.45196 4.87402  22

-11  -3 -15-3.36527 4.34072  22

-11  15  -3-2.20880 5.13618  23

-15   3 -11-0.76799 3.43154  22

11  15  -3 0.78051 3.41406  23

3  11 -15-0.80285 3.35562  23

3  15 -11 5.79205 5.17601  23

-15  11  -3-1.06570 4.55903  21

15  11   3 1.82385 4.07466  19

15  11  -3-3.75240 4.97270  19

-3  11 -15 2.56204 3.73556  22

11  15   3 2.61673 4.77327  19

-3  15 -11 0.91213 3.90206  22

-11  15  -3-2.13568 4.13209  22

3  11 -15-1.24044 4.52547  20

3  15 -11 1.09271 4.22833  20

-3  11 -15 1.15970 4.23091  20

-3  15 -11 6.19478 5.41934  20

-11  15  -3 5.17013 4.64955  21

-15  11   3 2.40921 5.15328  21

11  15  -3 1.18954 4.72914  16

-3  15 -11-2.20364 3.73016  15

15  11   3 5.59238 4.57796  16

11  15   3-1.24333 4.39197  16

-3  11 -15 1.07506 4.38505  15

15  11  -3 2.69257 4.75565  18

11  15  -3-1.28604 4.97643  18

3  11 -15-2.64709 3.68795  15

-11  -5 -15 6.12455 5.91416   8

-15  -5 -11 3.51206 4.89604   7

-11  15   5 10.7705 5.01193   9

-15  11   5 3.28470 3.82286   9

-15  -5 -11 12.7524 6.58175   8

-15  11   5 6.74372 4.73492  10

-11  -5 -15 14.9867 6.44585   7

-5  11  15 10.4945 5.50119  30

11  15  -5 14.0955 5.07339  28

11  15   5 9.82016 4.31198  28

15  11  -5 12.7627 4.48084  28

15  11   5 9.62931 4.51979  28

5  15  11 8.11393 4.35444  29

-11  15   5 11.1555 4.36391  30

-5  11  15 6.21416 4.51135  29

-5  15  11 11.1252 5.56034  30

-5  15  11 19.0307 6.53996  29

-11   5  15 19.1484 5.66888  25

-11  -5  15 5.94308 4.69742  25

5  11  15 8.27411 3.99695  26

5  15  11 12.8454 5.10098  26

11  15   5 4.01777 3.11894  26

15  -5 -11 16.4572 5.93575  12

15   5 -11 10.2588 4.95408  12

-5  15  11 10.3531 4.65850  13

-11  15   5 14.9935 5.44126  13

-15  11   5 10.1175 4.59803  13

11  -5 -15 12.1306 5.37886  12

11   5 -15 18.8817 5.82219  12

-15   5 -11 8.38075 4.50668  22

-5  15 -11 13.4555 5.18885  23

-5  11 -15 10.1618 4.34455  24

-15  11  -5 8.64112 4.05666  24

-5  15 -11 11.9704 4.74670  24

-11   5 -15 9.15685 5.11721  22

11  15  -5 6.99535 4.14764  23

5  11 -15 11.2339 4.45506  23

-5  11 -15 11.2703 4.61614  22

11  15  -5 8.84748 6.31640  19

-5  15 -11 6.85627 4.64510  22

-15  11  -5 14.1236 4.22580  22

-11  15  -5 1.03316 4.80793  22

5  15 -11 11.8404 4.62837  20

-5  11 -15 13.4616 5.68615  20

-11  15   5 12.6122 6.00979  21

-15  11   5 8.57005 5.52974  21

15  11  -5 12.2043 6.68090  19

11  15   5 9.21356 5.56097  19

5  11 -15 8.07451 3.96453  15

-11   5 -15 5.49236 3.92342  15

-5  15 -11 9.97523 4.26050  15

15   5 -11 7.45455 5.66848  18

15  11  -5 8.90374 5.44413  18

11  15  -5 14.9714 6.03639  18

-11  -7 -15 69.3117 8.99046   8

-15  11   7 70.9827 7.65099   9

-11  15   7 70.2251 8.74898   9

-15 -11  -7 60.1795 8.35939   8

-15  -7 -11 91.2791 10.2951   8

-15  11   7 73.2604 8.79961  10

-15  -7 -11 57.5962 8.77896   7

-11  -7 -15 71.2692 9.70907   7

-7 -11 -15 52.5346 8.24854   7

-7  11  15 52.0513 8.23986  30

15  11  -7 67.7769 7.18293  28

7  15  11 67.6964 7.68065  29

11  15  -7 66.4220 7.41677  28

-11  15   7 53.8251 7.21797  30

15   7 -11 71.7473 8.37858  27

-7  11 -15 81.8423 8.52077  24

15  11   7 61.8261 6.18469  26

11  15   7 77.4309 7.73036  26

-11   7  15 62.6058 7.35617  25

-11  -7  15 61.5089 7.36666  25

7  11  15 68.1664 7.97611  26

7  15  11 58.6284 8.06984  26

15  -7 -11 77.0500 8.00502  12

15   7 -11 68.9737 7.76241  12

-7  15  11 55.1840 7.97820  13

-15  11   7 62.0511 8.13253  13

11   7 -15 56.9974 7.54002  12

-11   7  15 54.4513 7.50589  13

11  -7 -15 76.5460 7.95880  12

-15  11  -7 61.4964 7.89798  24

-7  15 -11 66.8251 8.32348  24

-7  15 -11 80.4728 8.48568  23

-11  15  -7 77.4688 8.81407  23

11  15  -7 77.8331 8.76846  23

7  11 -15 69.2263 7.83777  23

-7  11 -15 87.3886 9.56689  22

-15   7 -11 63.6640 7.61705  22

11  15  -7 79.0404 9.61945  19

-7  15 -11 63.8834 8.98434  22

-15  11  -7 56.4212 6.82211  22

-11  15  -7 71.1711 8.99678  22

11  15   7 72.9319 9.33872  19

7  15 -11 65.5867 7.39884  20

-7  15  11 62.6916 8.33597  21

-11  15   7 65.4005 9.02662  21

-15  11   7 81.0197 9.08302  21

15   7 -11 57.8697 8.87101  18

15  11  -7 82.0038 10.2126  18

11  15  -7 66.4739 8.65689  18

7  11 -15 78.2452 7.14723  15

-11  15   9 180.998 11.7907   9

-11  -9 -15 147.452 11.7918   7

-15   9  11 162.496 11.8702  10

-15  11   9 145.293 10.7721  10

-15 -11  -9 161.107 10.8067   8

-15  -9 -11 162.154 11.6198   8

-15  -9 -11 170.152 12.6424   7

-9 -11 -15 177.855 11.8837   7

-9  15  11 160.295 11.0921   9

-11  15   9 137.962 10.1134  30

-9  15  11 175.965 11.5702  30

-11   9  15 155.771 11.4416  30

15   9 -11 152.217 9.83978  27

11   9 -15 152.668 11.0300  27

-15   9 -11 163.981 11.1829  24

-15  11  -9 148.168 10.6371  24

9  11  15 149.008 10.3704  26

-9  11 -15 140.743 10.2451  24

9  15  11 165.414 10.7808  26

11  15   9 152.410 9.91092  26

-11   9 -15 182.107 11.8979  24

-9  15  11 148.100 10.9731  13

-11  15   9 151.033 11.2447  13

-15  11   9 156.787 11.1682  13

-11   9  15 161.557 10.3423  13

-11  15  -9 155.179 11.3367  24

-9  11 -15 146.425 11.1382  22

11   9 -15 134.400 9.36651  23

11  15  -9 164.735 11.2297  23

9  11 -15 143.978 9.91741  23

9  15 -11 150.568 10.9877  23

-9  15 -11 147.637 11.4792  22

-9  15 -11 150.239 11.0422  24

-11  15  -9 149.407 11.4002  22

-9  15 -11 129.672 9.29720  23

-9  15  11 133.556 9.85725  21

-11  15   9 142.781 10.5948  21

11  15  -9 155.115 11.5292  19

11   9 -15 157.457 11.6260  18

15   9 -11 123.794 11.1869  18

11  15  -9 152.536 10.6411  18

-13   1 -15 205.420 14.9242   8

-13  -1 -15 162.971 12.2902   7

-15  -1  13 145.726 11.0176  10

-15  -1 -13 170.458 11.6996   7

-15  -1 -13 185.670 14.5641   8

-15   1 -13 179.754 13.4536   8

-13  -1 -15 182.353 14.1907   8

1  13  15 190.972 13.8978  29

-1  13  15 171.513 13.1035  29

15  13   1 194.437 13.4742  28

-1  15  13 164.227 13.0437  29

-1  15  13 178.565 11.9951  30

-1  13  15 198.465 11.9893  30

13  15   1 201.882 14.1238  28

1  15  13 184.417 11.9633  26

-1  15  13 181.925 11.1749  26

-13  -1  15 170.212 13.5222  25

13  -1 -15 202.758 15.1391  12

15  -1 -13 187.384 14.5650  12

-13  15   1 175.148 11.5264  13

1  15 -13 183.821 13.1645  23

1  13 -15 181.737 11.2837  23

-1  15 -13 196.321 12.9864  23

-1  13 -15 165.225 10.5163  23

-13  -1 -15 199.451 12.8804  22

-13   1 -15 170.374 12.6474  22

-15  -1 -13 155.903 9.90220  22

-15   1 -13 163.901 10.5125  22

15  13  -1 201.205 14.1861  19

1  13 -15 223.672 14.9747  20

13  15  -1 202.255 14.8710  19

-1  13 -15 188.905 14.3488  20

1  15 -13 215.714 14.7392  20

15  13   1 186.942 13.4984  19

-1  15 -13 187.687 14.0251  20

13  15   1 194.993 14.4483  19

-13  15   1 168.757 13.1098  21

-13  15  -1 205.110 13.4570  21

-15  13   1 170.352 13.3940  21

-15  13  -1 186.762 13.4344  21

-15  -1 -13 180.231 11.4179  14

-1  15 -13 171.943 10.3164  15

-1  13 -15 170.295 11.5135  15

1  13 -15 172.914 11.1124  15

15  13  -1 165.662 11.6592  16

13  15  -1 202.395 13.9084  16

15  13   1 183.827 12.2613  16

13  15   1 201.315 14.1674  16

-13  -3 -15 25.8214 6.66838   8

-15   3 -13 24.6451 5.54928   8

-13   3 -15 17.6870 5.16982   8

-13  15   3 25.9471 5.84258   9

-15  -3 -13 19.3759 5.71341   7

-13  -3 -15 26.2420 6.29923   7

13  15  -3 31.1209 6.41890  28

13  15   3 22.0974 5.60523  28

15  13  -3 29.8687 5.99306  28

15  13   3 33.6521 6.43334  28

3  15  13 25.8580 5.68417  29

-3  15  13 17.4544 5.04567  30

-3  13  15 27.0209 5.85677  29

-3  13  15 17.1885 4.90296  30

-3  15  13 20.5827 6.22609  29

-13   3  15 28.8853 6.42968  25

-13  -3  15 30.1694 6.47222  25

3  13  15 24.9422 5.00109  26

3  15  13 25.7061 5.40180  26

13   3 -15 26.1959 6.01610  12

15  -3 -13 29.2835 6.37147  12

15   3 -13 27.1149 6.32125  12

-15  -3 -13 22.7906 4.94490  14

-13  15   3 22.5926 5.15682  13

-15  13   3 21.3303 4.62314  13

13  -3 -15 27.9333 6.46913  12

3  15 -13 22.0583 5.43249  23

3  13 -15 23.3807 4.89192  23

-3  15 -13 28.3190 5.39641  23

-13  -3 -15 28.7921 5.56806  22

-13   3 -15 35.1201 6.40843  22

-15   3 -13 18.4547 4.36325  22

-15  13  -3 24.3132 5.68748  21

-3  15 -13 15.7119 4.18192  22

15  13  -3 28.2566 6.45638  19

15  13   3 26.4129 5.30322  19

3  13 -15 18.1399 5.85615  20

13  15  -3 27.8311 6.70609  19

13  15   3 26.2733 6.53099  19

3  15 -13 24.0018 5.97252  20

-3  13 -15 23.3630 5.66907  20

-15  13   3 18.9702 5.48717  21

-13  15  -3 20.7031 4.89062  21

-3  15 -13 19.5341 4.33908  15

15  13   3 27.8210 5.86966  16

13  15   3 33.3331 6.82126  16

-3  13 -15 25.7377 5.66666  15

3  13 -15 13.8544 3.87989  15

15  13  -3 15.0740 5.65665  18

-13  -5 -15 20.4353 6.05733   8

-13  15   5 16.6592 4.96903   9

-15  13   5 13.4054 3.97276   9

-15  -5 -13 12.4049 5.08326   8

-15  -5 -13 12.8742 4.83450   7

-13  -5 -15 19.7133 5.61059   7

13  15  -5 11.5904 4.08822  28

13  15   5 17.9872 4.54796  28

5  13  15 15.6860 4.69997  29

5  15  13 15.0784 4.40292  29

15  13  -5 21.7080 4.88070  28

15  13   5 20.5232 4.68885  28

-5  15  13 20.2405 5.33298  30

-5  13  15 17.1784 4.94285  30

-5  13  15 15.7768 4.63428  29

-13   5  15 17.4673 4.79579  25

5  13  15 20.9003 4.59437  26

-13  -5  15 16.3985 4.65325  25

5  15  13 13.5998 4.19054  26

15  -5 -13 17.0065 4.87201  12

15   5 -13 8.89857 4.12451  12

-13  15   5 18.8425 4.96580  13

-15  13   5 14.2324 4.59365  13

13  -5 -15 13.9050 4.63383  12

13   5 -15 17.9280 4.87442  12

5  15 -13 18.5721 4.94927  23

5  13 -15 15.7764 4.08046  23

-5  15 -13 21.6376 5.15210  23

-13  -5 -15 17.6308 4.34074  22

-15   5 -13 18.1307 4.52144  22

15  13  -5 13.2198 4.07514  23

-13   5 -15 17.3654 4.61915  22

13  15  -5 15.0715 4.00242  23

15  13  -5 17.0427 5.40094  19

-5  13 -15 15.4945 4.33701  22

-5  15 -13 17.2677 4.66208  22

-13  15  -5 18.9510 5.02364  22

13  15   5 17.3595 4.67816  19

5  13 -15 16.3709 4.90440  20

5  15 -13 14.3732 4.69017  20

-5  15  13 20.3430 4.40948  21

-5  13 -15 23.1501 5.59410  20

-13  15   5 20.4755 5.28570  21

-15  13   5 22.3769 5.61360  21

-5  13 -15 13.0855 4.20377  15

15  13   5 23.3807 5.13752  16

13  15   5 16.7697 4.78494  16

15   5 -13 12.2412 4.71319  18

15  13  -5 9.68515 5.08297  18

13  15  -5 20.1666 5.97788  18

-13  15   7 164.693 10.7110   9

-15  -7 -13 178.180 12.0690   7

-15  -7 -13 141.292 10.8375   8

7  13  15 138.404 9.58176  29

15   7 -13 174.831 10.5303  27

-7  15  13 176.996 11.1621  30

-7  13  15 171.492 11.0209  30

13   7 -15 150.494 10.2547  27

7  13  15 137.612 9.22461  26

7  15  13 190.317 10.9890  26

-13  15   7 156.250 10.6552  13

-15  13   7 150.307 10.2211  13

-13   7  15 174.179 10.4324  13

-15   7  13 182.446 11.4197  13

13  15  -7 163.796 11.6286  19

-13  15   7 163.058 10.8673  21

15  13  -7 184.858 12.2584  19

13  15   7 165.479 11.0407  16

13   7 -15 158.243 11.5855  18

15   7 -13 145.212 11.2395  18

-7  13 -15 152.998 10.3003  15

-13   7 -15 150.026 10.5714  22

7  15 -13 167.550 10.7597  23

15  -1 -15 5.65082 3.34908  12

-16   0   0 1729.19 56.1975  10

-16   0   0 1782.88 58.3855   6

0  16   0 1755.04 56.4369  30

0   0  16 1683.60 55.3487  25

0  16   0 1702.82 48.8703  23

0  16   0 1667.52 51.0468  19

-16   0   0 1640.59 54.2338  14

0  16   0 1698.70 48.2716  16

-16   0   2 1.40928 5.14145  10

-16   2   0-1.54264 5.80118  10

-16  -2   0-2.55264 5.20597  10

-16   0  -2-1.45350 4.77987  10

-16   0   2-1.61921 5.52579   6

-16  -2   0-1.55907 5.50731   6

-16   2   0-1.56509 5.34110   6

-16   0  -2-1.59191 5.62330   6

0  16  -2-2.86240 5.38211  30

2  16   0 1.38771 5.51698  30

0  16   2-1.41542 5.77335  30

0  -2  16 5.68689 5.94226  25

0   2  16-1.44711 5.90262  25

-2   0  16-1.47791 5.71888  25

2   0  16 2.89894 5.45081  25

0  16   2 4.01188 5.72091  26

-16   0   2 1.30680 5.05675  14

-16   2   0-1.41245 5.46559  14

-16  -2   0 1.31419 5.22471  14

-16   0  -2-2.83867 4.66750  14

2   0 -16 3.10840 6.49597  12

2  16   0-1.81853 3.97725  23

0  16  -2-2.31464 4.22223  23

-2  16   0-1.03985 4.34619  23

0   2 -16-0.99179 3.94297  22

0  16   2-1.31542 5.09012  19

2  16   0-4.02142 5.18707  19

0  16  -2 5.95384 4.78909  19

2  16   0-3.52057 5.35167  16

0  16   2 1.75354 4.07756  16

-2   0 -16 0.97653 3.44953  15

0   2 -16-1.16921 4.39690  15

-16   2   2 114.933 13.4307  10

-2  16   2 84.9916 9.07286   9

-16  -2   2 90.3963 11.4093  10

-16   2  -2 89.7834 12.4941  10

-16  -2  -2 92.2111 11.6988  10

-16  -2   2 88.2442 12.2177   6

-16   2   2 85.2544 12.2405   6

-16  -2  -2 110.048 13.8733   6

-16   2  -2 99.8484 13.3704   6

2  16  -2 128.357 13.0931  30

-2  16  -2 100.894 12.9320  30

2  16   2 98.9709 12.2444  30

-2  16   2 81.8306 11.5289  30

-2  -2  16 96.7486 12.7355  25

-2   2  16 84.9067 11.9023  25

2   2 -16 78.9381 8.36467  27

2  16   2 102.797 12.0819  26

2  -2  16 77.2311 11.2815  25

2   2  16 89.0473 12.0432  25

-16  -2   2 91.9493 11.1525  14

-16  -2  -2 79.4539 11.0554  14

2  -2 -16 102.449 12.9914  12

2   2 -16 102.098 13.1378  12

-16   2   2 93.7201 12.0344  14

2  16  -2 86.9999 10.5627  23

-2  16  -2 98.6919 11.3108  23

-2   2 -16 96.1453 11.5576  22

-2  16   2 89.7266 9.09161  23

2  16  -2 93.8153 11.3565  19

2  16   2 114.760 13.2815  19

2  16  -2 77.3920 10.8097  16

2  16   2 64.3644 9.68446  16

-2   2 -16 91.2350 11.0018  15

-2  -2 -16 87.2571 9.08718  15

-4   0 -16 429.073 25.9976   8

-4  16   0 446.884 21.9369   9

-16   0   4 415.624 24.3454  10

-16   4   0 422.930 25.9147  10

-16  -4   0 411.856 21.2975  10

-16   0  -4 451.211 25.6974  10

-16   0   4 431.185 26.2231   6

-16  -4   0 397.744 23.9232   6

-16   4   0 419.973 24.9249   6

-16   0  -4 416.252 25.7206   6

4  16   0 403.920 23.1105  30

-4  16   0 393.896 23.6159  30

0  16   4 394.245 23.5086  30

4   0 -16 394.287 17.9640  27

0  16   4 378.781 20.7148  29

4  16   0 395.434 23.6994  28

0  -4  16 380.777 23.0468  25

0   4  16 430.545 24.5196  25

-4   0  16 352.738 23.0594  25

0  16   4 417.257 24.0379  26

4  16   0 397.897 20.8505  26

4   0  16 395.495 24.3063  25

16   0  -4 411.738 26.1816  12

4   0 -16 418.567 25.6867  12

4  16   0 403.737 18.9372  23

0  16  -4 427.147 23.4647  23

0   4 -16 396.623 19.7322  22

-4  16   0 451.957 22.3068  23

4  16   0 364.801 23.4308  19

0  16  -4 407.025 21.5621  20

4  16   0 433.794 23.9336  16

0  16   4 362.516 18.1819  16

0   4 -16 445.767 23.9297  15

16   4   0 417.548 20.6572  18

-16  -4   0 424.623 22.9342  14

-4   0 -16 433.436 20.1253  15

-2  16   4 11.8894 4.38419   9

-4  16   2 5.23094 4.57860   9

-4  -2 -16 13.6265 6.47882   8

-16   2   4 3.04664 5.55950  10

-16   4   2 15.7280 7.45539  10

-16  -2   4 7.16923 4.62607  10

-16  -4   2 15.1965 5.62257  10

-16   2  -4 15.4654 7.59749  10

-16  -4  -2 10.1274 5.43284  10

-16  -2  -4 8.10777 5.91262  10

-16  -2   4 7.96266 6.81446   6

-16   2   4 9.56378 7.27055   6

-16  -4   2 2.88506 4.92512   6

-16   4   2 5.89583 5.86180   6

-16  -4  -2 4.28780 5.21650   6

-16   4  -2 10.2390 5.96811   6

-16  -2  -4 10.7855 5.96409   6

-16   2  -4 7.78884 6.51260   6

-2  16   4 15.9063 6.50890  29

-2   4  16 2.51219 3.82175  29

2  16  -4 9.87832 6.17453  30

4  16  -2 14.6914 6.44754  30

-2  16  -4 9.66588 5.63429  30

4  16   2 10.8044 5.89829  30

-4  16  -2 1.36064 5.55192  30

2  16   4 6.34127 5.54952  30

-4  16   2 5.66191 5.77552  30

-2  16   4 14.1357 5.62178  30

2  16   4 1.84883 3.95746  29

-2  -4  16 10.9036 6.46107  25

-2   4  16 5.51762 5.33981  25

4   2 -16 6.22959 3.97926  27

-4  -2  16 7.25713 5.61840  25

-4   2  16 7.33945 6.28138  25

2   4 -16 8.03034 4.45989  27

4  -2  16 4.18462 5.54750  25

4   2  16 4.28711 5.05018  25

2  16   4 13.0525 6.41267  26

4  16   2 4.67194 4.52209  26

2  -4  16 13.1089 7.46817  25

2   4  16 10.7887 6.39302  25

-16  -2   4 5.42321 4.94860  14

-16   4  -2 1.37471 5.01754  14

-16  -4   2 10.8441 5.14148  14

-16   2  -4 16.5078 6.87385  14

16   2  -4 4.81840 7.32604  12

16  -2  -4 3.24496 7.54708  12

-16  -4  -2 23.9193 7.76202  14

-16  -2  -4 14.2439 6.23224  14

-2  16   4 10.9671 6.37729  13

-4  16   2 11.3229 6.70939  13

2  -4 -16 12.4177 6.16677  12

2   4 -16 11.4257 6.77032  12

4  -2 -16 12.1316 7.18835  12

4   2 -16 7.69565 5.25464  12

2  16  -4 11.1291 5.96983  23

-2  16  -4 3.91488 5.71002  23

-4  16  -2 8.62775 5.50925  23

-4  16   2 14.2722 5.21158  23

-4   2 -16 14.8957 6.87828  22

-2   4 -16 10.2560 5.40272  22

4  16  -2 7.21587 4.70335  23

-16   4   2 13.7006 6.61391  21

2  16  -4 9.30154 4.62033  19

-2  16  -4 6.32413 5.76998  22

-4  16  -2 6.97481 5.69187  22

4  16   2 6.18339 5.81517  19

-4  16  -2 13.9043 5.65893  21

2  16  -4 7.38345 4.37656  20

4  16  -2 8.16852 5.55510  19

2  16   4 10.7536 6.86580  19

4  16  -2 4.11526 6.00209  16

-2   4 -16 10.9662 6.18940  15

4  16   2 1.27873 5.21797  16

2  16   4 9.30516 5.73796  16

16   2  -4 8.06951 4.69345  18

16   4  -2 13.7854 5.72380  18

-4   2 -16 16.7356 6.03548  15

-4  16   4 1357.01 42.8891   9

-4  -4 -16 1474.64 49.7657   8

-16   4   4 1349.84 50.0724  10

-16  -4   4 1361.93 41.7217  10

-16  -4  -4 1491.98 46.1234  10

-16  -4   4 1403.55 48.9173   6

-16   4   4 1411.41 49.4160   6

-16  -4  -4 1458.71 49.2106   6

-16   4  -4 1367.21 48.5794   6

-4  16  -4 1409.73 47.2008  30

4  16   4 1439.12 44.8289  30

4  16   4 1359.14 38.6038  29

4   4 -16 1435.61 43.5987  27

-4  -4  16 1386.72 47.6574  25

-4   4  16 1453.37 48.7166  25

4  16   4 1386.23 45.9584  26

4  -4  16 1368.64 46.5898  25

4   4  16 1396.25 47.3472  25

-16  -4  -4 1410.59 48.2770  14

-4  16   4 1447.23 48.9680  13

16   4  -4 1377.48 48.9298  12

16  -4  -4 1383.54 49.3624  12

4  -4 -16 1480.97 49.2163  12

4   4 -16 1423.99 48.8546  12

4  16  -4 1401.64 45.4365  23

-4  16  -4 1440.62 47.6673  23

-4   4 -16 1496.63 48.0534  22

-4  16  -4 1384.35 47.7798  22

-4   4 -16 1411.02 39.5625  20

4  16  -4 1360.19 45.3987  19

4  16   4 1406.20 50.6158  19

-16   4   4 1395.57 46.3866  21

-16   4  -4 1363.25 46.5554  14

16   4  -4 1327.13 44.6361  18

-4   4 -16 1445.07 45.8024  15

-16  -4   4 1322.81 41.0131  14

-6   0 -16 3.09743 5.99287   8

-6  16   0-1.18803 4.59716   9

-16   0   6 1.34372 5.05313  10

-16   6   0-1.50405 5.65605  10

-16   0  -6 1.46713 5.18250  10

-16   0  -6 1.56090 5.69458   6

-16  -6   0-3.69562 5.02468   6

-16   6   0 1.28131 4.67458   6

6  16   0 3.28482 4.35305  30

6  16   0 4.16169 4.73412  28

-6  16   0 1.29096 5.39570  30

0  16   6-1.29399 5.27806  30

0  16   6 1.17315 4.41169  29

0  -6  16 1.20694 4.53876  25

0   6  16-2.40809 4.91116  25

-6   0  16 1.46530 5.17606  25

0  16   6 1.32013 4.50512  26

6  16   0 0.89313 3.35864  26

16   0  -6-3.23639 6.08530  12

-16  -6   0 2.16764 3.56415  14

-16   0  -6-4.09672 5.57002  14

6   0 -16 4.65773 6.17244  12

0  16  -6-1.34047 5.60266  23

-6   0 -16-1.45533 5.14085  22

-6  16   0 1.11417 4.54458  23

-16   6   0 2.84204 6.34940  21

0  16  -6-3.07818 4.18518  22

-6  16   0 2.46828 5.51438  21

0  16  -6 1.18407 4.31979  20

6  16   0 4.61219 6.42572  19

6  16   0-1.41841 5.17473  16

0   6 -16 1.30174 5.44078  15

16   6   0-1.12491 5.02632  18

-6   0 -16 0.76663 3.35334  15

-2  16   6 67.1320 8.25931   9

-16   2  -6 54.4717 9.42594   8

-6  -2 -16 69.1240 11.1813   8

-6  16   2 50.4935 9.28680   9

-6   2 -16 42.0904 10.7716   8

-16   2   6 86.0965 11.8605  10

-16  -2   6 70.4006 10.0019  10

-16   6   2 82.0306 12.6005  10

-16   6  -2 76.9848 11.3575  10

-16   2  -6 53.0065 10.3102  10

-16  -2  -6 89.4408 11.6533  10

-16  -2  -6 76.7307 11.2926   6

-16   2  -6 74.8510 11.4638   6

-6  -2 -16 58.3197 10.6289   7

-16  -6   2 59.0789 9.26254   6

-16   6   2 51.3048 9.43116   6

-16  -6  -2 67.3924 9.74855   6

-16   6  -2 53.3260 9.75874   6

-2   6  16 65.6593 9.01155  29

6  16   2 65.8202 8.94646  30

-6  16  -2 74.2670 10.7147  30

6  16   2 74.7502 11.0190  28

2  16   6 66.2957 10.0195  30

-6  16   2 54.2958 9.95523  30

-2  16   6 71.8060 10.6221  30

2  16   6 85.8480 10.3568  29

-2  16   6 66.5605 10.1104  29

2  -6  16 62.5437 9.99141  25

2   6  16 65.0541 9.89733  25

-2  -6  16 74.6994 10.7740  25

-2   6  16 61.3415 9.57180  25

2   6 -16 67.6181 9.00038  27

-6   2  16 79.0797 11.5663  25

-6  -2  16 65.4112 10.6799  25

2  16   6 67.4606 10.4483  26

6  16   2 68.8494 9.39819  26

-2  16   6 55.6235 9.65570  26

-16  -6   2 54.4739 7.67854  14

-16   2  -6 79.7501 11.1908  14

-16  -6  -2 64.3754 9.47237  14

16   6  -2 83.0034 11.5883  12

16  -6  -2 70.5176 11.1832  12

-2  16   6 70.3084 10.6860  13

6  -2 -16 79.0980 11.9238  12

6   2 -16 56.4069 10.1897  12

-16   6   2 62.1979 8.23225  13

16   2  -6 66.8956 11.4990  12

16  -2  -6 64.6362 12.4239  12

2  16  -6 57.6262 9.70099  23

-2  16  -6 70.0488 10.2724  23

-6  16  -2 75.0832 10.7140  23

-6  16   2 72.5443 9.28845  23

-2   6 -16 82.4834 10.3226  22

-6   2 -16 64.7844 10.8905  22

6  16  -2 72.0750 9.06440  23

-16   6   2 98.9880 11.8871  21

-2  16  -6 63.9733 9.85386  22

-6  16  -2 60.0284 10.8668  22

-2   6 -16 60.5054 8.88149  20

2  16  -6 48.6713 8.47563  20

6  16  -2 59.6547 10.6804  19

-6  16  -2 44.7428 7.79198  21

-2  16  -6 68.2756 9.82932  20

-2   6 -16 57.4715 10.0881  15

6  16  -2 63.0737 10.4429  16

6  16   2 50.7610 9.76239  16

16   2  -6 69.5350 9.88059  18

2   6 -16 75.0263 11.0662  15

16   6  -2 75.4344 10.9352  18

16   6   2 77.7919 9.80052  18

-6   2 -16 63.5979 8.77865  15

-4  16   6 5.94762 4.69905   9

-6  -4 -16 4.30364 5.85230   8

-6  16   4 3.41734 4.40915   9

-16   4  -6 7.71630 4.35513   8

-4  -6 -16 15.5392 5.76984   8

-16   4   6 4.57803 6.37902  10

-16   6  -4 11.4069 6.88230  10

-16  -4  -6 3.50596 4.39604  10

-16  -6  -4 3.58486 4.36079   6

-16   6  -4 8.65916 5.04678   6

-16  -4  -6 4.08919 5.27553   6

-16   4  -6 2.80630 5.27766   6

-4  -6 -16 1.49492 5.45489   7

-16  -6   4 4.86399 4.96104   6

-16   6   4 6.31166 5.14999   6

6  16   4 10.8180 6.00562  28

-6  16  -4 12.0933 5.49315  30

6  16   4 14.4454 4.52030  30

4  16   6 4.81676 4.30574  30

-4   6  16 3.89134 3.88934  29

-6  16   4-1.32905 5.81437  30

4  16   6 5.99268 4.27802  29

-4  16   6 8.17507 6.08888  30

6  16  -4 10.0212 5.23664  28

6   4 -16 8.66734 5.67747  27

4   6 -16 8.77292 4.79788  27

-4   6  16 4.69638 4.90841  25

-4  -6  16 15.2171 6.31699  25

-6   4  16 3.99209 5.42879  25

-6  -4  16 2.63095 5.23088  25

4  16   6 4.92974 4.49750  26

6  16   4 1.09925 4.80942  26

4  -6  16 10.1425 5.99428  25

4   6  16 3.41855 5.09268  25

16   6  -4 9.93192 5.43145  12

16  -6  -4-2.52373 5.63925  12

-16   4  -6 9.24077 5.57573  14

-4  16   6 6.56738 5.35856  13

-6  16   4 6.80825 5.27006  13

4  -6 -16 7.00548 5.53445  12

4   6 -16 11.0596 5.93160  12

6  -4 -16 6.75617 5.37301  12

6   4 -16 1.40320 5.12035  12

16   4  -6 4.20488 4.95226  12

16  -4  -6 11.4535 7.15291  12

-4  16  -6 3.98873 5.68888  23

-6  16  -4 1.27471 5.06886  23

-4   6 -16 10.7934 6.65422  22

-6   4 -16 8.26112 5.61702  22

6  16  -4 7.71951 4.82488  23

4  16  -6 5.03226 4.44527  23

-4  16  -6 10.2506 6.29429  22

-6  16  -4 10.8556 6.66565  22

-4   6 -16 1.79375 3.92445  20

6  16  -4 9.37712 5.59996  19

4  16  -6 8.20472 5.03842  19

4  16  -6 8.43889 4.21705  20

6  16   4 7.81706 6.83936  19

-16   6   4 3.76859 4.99526  21

6  16  -4 8.51317 5.49140  16

16   4  -6 1.27312 4.78879  18

16   6  -4 5.22540 4.91373  18

-6   4 -16 5.33894 4.56919  15

-4   6 -16 1.21950 4.45032  15

-6  16   6 80.7352 9.63477   9

-6  -6 -16 63.6013 9.85271   8

-16   6  -6 66.7050 10.5970  10

-16  -6  -6 65.3070 10.0196   6

-16   6  -6 54.8850 9.10657   6

-6  -6 -16 54.6042 10.7422   7

-16  -6   6 60.7830 9.42189   6

-16   6   6 51.4342 9.06569   6

-6  16   6 82.2178 10.9860  30

6   6 -16 65.0064 9.43566  27

-6   6  16 52.1713 9.06794  25

-6  -6  16 55.0462 8.93848  25

6  16   6 64.9694 9.37487  26

6  -6  16 84.2898 10.1066  25

6   6  16 69.9379 9.58437  25

-6  16   6 58.3779 9.96255  13

16   6  -6 69.6329 9.99249  12

16  -6  -6 60.8727 9.67421  12

6  -6 -16 51.2171 8.98109  12

6   6 -16 65.5513 10.1901  12

-16   6  -6 66.1597 8.13850  24

-6  16  -6 74.7938 10.1035  23

-6   6 -16 62.0265 9.65542  22

6  16  -6 74.9327 10.3036  23

-16   6   6 59.4842 9.30945  21

6  16   6 81.6816 11.8614  19

-6  16  -6 61.8041 9.88899  22

6  16  -6 55.5410 9.44678  19

16   6  -6 53.4839 9.74417  18

-6   6 -16 70.6927 9.55674  15

6  16  -6 47.0889 7.49215  18

-8  16   0 1299.74 42.8177   9

-16   0   8 1196.56 41.7498  10

-16   8   0 1201.98 43.0379  10

-16   0  -8 1208.09 43.9901  10

-16   0  -8 1164.60 42.4297   8

-16  -8   0 1137.75 37.0117   6

-16   8   0 1248.85 38.3054   6

-16   0  -8 1238.66 45.2594   6

0   8  16 1255.75 41.2337  29

-8  16   0 1202.87 39.6195  30

0  16   8 1114.97 39.9472  30

0  16   8 1141.08 40.5203  29

0   8  16 1141.23 35.8747  30

8  16   0 1065.62 41.2765  28

0  -8  16 1217.28 37.8104  25

0   8  16 1138.91 36.4817  25

-8   0  16 1085.57 41.8424  25

0  16   8 1176.58 41.3370  26

8  16   0 1143.70 33.2770  26

8   0 -16 1249.56 45.5940  12

-8  16   0 1188.09 41.2594  13

16   0  -8 1138.92 44.4772  12

16   8   0 1093.85 37.0524  12

16  -8   0 1234.27 39.2603  12

0  16  -8 1191.69 42.5805  23

-8   0 -16 1125.66 42.9144  22

-8  16   0 1157.52 39.1811  23

0  16  -8 1196.52 36.6109  22

0  16  -8 1175.76 41.0960  20

-8  16   0 1158.67 40.5234  21

16   8   0 1163.02 38.4090  19

16   8   0 1151.49 40.8715  18

-16   0  -8 1154.67 41.2652  14

-16  -8   0 1158.25 36.4468  14

-8  -2 -16 17.9960 8.10327   8

-2  16   8 21.7940 5.32969   9

-16  -2  -8 33.4189 8.28709   8

-8  16   2 24.2539 6.74148   9

-8   2 -16 36.8015 8.57405   8

-16   2  -8 21.6254 6.89920   8

-16   2   8 27.5657 8.15808  10

-16  -2   8 24.4613 6.78109  10

-16   8   2 19.1051 7.58301  10

-16   8  -2 33.6311 8.35313  10

-16   2  -8 24.3306 7.39660  10

-16  -8  -2 13.6411 5.19747   6

-16   8  -2 31.6559 6.25485   6

-16  -2  -8 26.8375 8.45873   6

-16   2  -8 27.3471 7.55334   6

-8  -2 -16 20.9611 8.07217   7

-16  -8   2 27.5421 6.16803   6

-16   8   2 29.9896 6.29576   6

-2   8  16 30.7013 7.18223  30

8  16   2 21.4549 6.72548  28

-8  16  -2 20.2229 5.90743  30

-2   8  16 20.2353 6.20508  29

-8  16   2 21.6229 6.49625  30

2  16   8 23.4557 6.18464  30

2  16   8 20.4207 6.36723  29

-2  16   8 8.82693 5.65056  30

-2  16   8 25.2839 7.12062  29

2  -8  16 28.5106 6.82805  25

2   8  16 23.7895 6.13507  25

-2   8  16 21.2858 5.67856  25

-2  -8  16 31.7353 6.57796  25

-8   2  16 39.6452 8.91467  25

-8  -2  16 13.5135 6.65108  25

2  16   8 43.9081 7.79868  26

8  16   2 23.1270 5.60322  26

-2  16   8 24.2592 6.92226  26

16   8  -2 20.8278 6.24124  12

16  -8  -2 26.8323 6.55461  12

-16   2  -8 24.6300 6.55220  14

-16  -8  -2 22.6891 6.39401  14

-16  -2  -8 32.1883 7.53144  14

-2  16   8 28.6028 7.03662  13

-8  16   2 18.8893 6.71079  13

16   2  -8 24.7996 8.10457  12

16  -2  -8 22.1740 7.75707  12

-16   8   2 25.3648 5.97693  13

8  -2 -16 26.9621 8.09406  12

8   2 -16 20.4158 7.29746  12

2  16  -8 33.5624 8.25255  23

-2  16  -8 19.5031 7.41812  23

-8  16  -2 17.6923 6.37868  23

-8   2 -16 34.0136 8.77734  22

-2   8 -16 16.4447 5.41704  22

8  16  -2 31.2686 6.38255  23

-16   8  -2 24.9811 7.50108  21

8  16   2 34.8557 8.75228  19

-2  16  -8 20.9368 6.69719  22

-8  16  -2 35.1287 8.81087  22

-2   8 -16 19.7087 6.61725  20

8  16  -2 33.5567 8.53132  19

2  16  -8 28.1779 7.00258  20

-8  16   2 15.6283 7.04036  21

-2  16  -8 36.9965 8.32049  20

-8  16  -2 21.7757 6.26917  21

-16   8   2 11.9244 6.17664  21

2   8 -16 17.9457 6.28290  15

8  16   2 24.5492 7.57855  16

-8   2 -16 20.8541 5.49112  15

16   2  -8 27.2531 7.42142  18

16   8  -2 36.3496 8.12867  18

-2   8 -16 26.1219 7.00671  15

-8  -4 -16 334.942 21.5706   8

-8  16   4 285.764 18.2323   9

-16   4   8 300.339 20.8106  10

-16   8   4 308.718 20.5504  10

-16   8  -4 326.677 19.8795  10

-16   4  -8 265.487 19.2772  10

-16   4  -8 264.543 15.5326   8

-4  16   8 299.920 17.0367   9

-16  -8   4 289.948 16.4254   6

-16   8   4 269.519 16.1344   6

-16  -8  -4 296.367 16.1846   6

-16   8  -4 256.464 15.8531   6

-16  -4  -8 276.735 18.7698   6

-16   4  -8 328.609 20.5338   6

4  16   8 296.577 15.8326  30

-4   8  16 298.837 16.3021  29

4  16   8 276.456 16.3252  29

-8  16   4 325.139 19.2833  30

-4  16   8 288.223 19.1263  30

-4  16   8 286.393 19.4527  29

8   4 -16 308.393 18.2903  27

8  16  -4 302.813 18.6436  28

8  16   4 289.706 18.2472  28

4   8  16 266.625 15.6553  25

-16   8  -4 254.907 13.9122  24

4   8 -16 305.603 18.6954  27

-4   8  16 233.450 15.0196  25

4   8  16 302.122 16.1784  26

-8   4  16 289.225 19.4484  25

-8  -4  16 319.411 19.8659  25

4  16   8 296.060 18.5788  26

8  16   4 304.799 16.8706  26

16  -4  -8 280.189 19.4170  12

16   4  -8 292.853 19.6763  12

-4  16   8 295.889 18.9240  13

16   8  -4 223.429 14.9072  12

-16   8   4 296.840 16.9729  13

8  -4 -16 283.706 18.8829  12

8   4 -16 311.606 20.5234  12

8  16  -4 319.179 17.6951  23

4  16  -8 287.118 18.9655  23

-8   4 -16 298.502 19.8668  22

-8  16  -4 293.621 18.6315  23

-4  16  -8 298.507 18.9909  22

-4   8 -16 268.557 17.2557  22

8  16  -4 293.228 19.6981  19

-4   8 -16 286.771 17.0560  20

4  16  -8 249.757 15.7571  20

-4  16  -8 327.487 20.4494  20

8  16   4 324.537 21.4801  19

-16   8   4 298.386 18.9433  21

4   8 -16 294.752 18.0414  15

16   4  -8 342.606 20.8014  18

-16   4  -8 268.398 16.1957  14

16   8  -4 289.532 19.6770  18

8  16  -4 290.957 18.5838  18

-8   4 -16 281.331 16.6497  15

-4   8 -16 289.592 18.7780  15

8  16  -4 294.871 19.7991  16

-6  16   8 18.4830 5.47904   9

-8  -6 -16 22.2737 6.33394   8

-16  -6  -8 19.1376 6.94934   8

-8  16   6 9.58339 5.05692   9

-6  -8 -16 22.3625 5.94834   8

-16   8   6 20.3267 6.76419  10

-16   8  -6 16.1997 6.00042  10

-16   6  -8 22.4638 6.74210  10

-16   8  -6 20.0465 5.23302   6

-16  -6  -8 23.0984 6.22092   6

-16   6  -8 19.8824 6.04509   6

-8  -6 -16 21.8096 6.92969   7

-6  -8 -16 21.7634 7.20508   7

-16  -6   8 18.0099 5.80662   6

-16   6   8 17.0540 5.84195   6

-16   8   6 9.65446 3.96496   6

16   8  -6 18.8282 5.49522  28

16   8   6 20.5286 5.12607  28

6  16   8 10.3704 4.19533  29

-8  16   6 17.5764 6.34511  30

8   6 -16 22.2965 6.43172  27

6   8 -16 20.5531 7.12206  27

6  16   8 15.9863 5.92161  26

8  16   6 16.8974 5.75276  26

8  -6  16 21.1949 5.70973  25

8   6  16 8.42064 4.44608  25

-6   8  16 19.9856 5.16217  25

-8   6  16 20.0625 5.93827  25

-8  -6  16 20.8123 6.00471  25

6   8  16 25.2745 5.47589  25

16  -6  -8 18.5671 6.45803  12

16   6  -8 18.5347 6.44679  12

16   8  -6 10.4373 4.46609  12

-6  16   8 14.7907 5.59765  13

-8  16   6 12.0139 5.70294  13

8  -6 -16 17.8757 5.73781  12

8   6 -16 20.9827 5.98457  12

-16   8   6 14.8665 6.07262  13

-8   6  16 24.6725 5.26336  13

-16   8  -6 21.3007 5.24852  24

-8  16  -6 22.3793 6.54293  23

-8   6 -16 14.6458 6.00337  22

-6   8 -16 22.1397 6.06660  22

6   8 -16 20.0804 4.51111  23

8  16  -6 25.8464 6.80745  23

6  16  -8 16.9167 5.73630  23

-6  16  -8 19.5996 6.40452  22

-8  16  -6 20.1829 6.94115  22

8  16  -6 14.1390 6.27465  19

6  16  -8 17.7852 5.13993  19

-6   8 -16 17.0058 4.67165  20

-8  16   6 27.2453 7.23981  21

8  16   6 19.8360 6.72326  19

-16   8   6 26.3007 6.59683  21

-8   6 -16 22.3634 5.95786  15

6   8 -16 28.2523 5.96947  15

16   6  -8 21.6572 7.44710  18

-6   8 -16 15.3248 5.47799  15

16   8  -6 16.8242 6.47333  18

8  16  -6 21.7190 6.09878  18

-8  16   8 797.204 28.8736   9

-8  -8 -16 793.458 28.0366   8

-16   8   8 788.273 31.2774  10

-16  -8  -8 788.675 31.5126   8

-8  -8 -16 811.560 32.2161   7

16   8  -8 718.277 23.6583  28

-8  16   8 796.536 29.8101  30

-8   8  16 818.625 30.4172  30

16   8  -8 777.705 24.5427  27

-16   8  -8 782.374 26.7110  24

8   8 -16 811.225 29.9207  27

8  16   8 795.185 28.5656  26

-8   8  16 697.535 24.3749  25

16   8  -8 741.788 25.0841  12

-8  16   8 807.225 30.7756  13

-16   8   8 828.634 29.6112  13

8   8 -16 715.161 24.9872  12

-8   8 -16 796.675 30.3022  22

8   8 -16 723.254 24.0914  23

8  16  -8 817.190 29.6385  23

-8  16  -8 828.543 29.9598  23

-8  16  -8 771.864 30.1199  22

8  16  -8 740.284 27.9981  19

-8  16   8 797.814 30.6762  21

-16   8   8 779.270 26.3336  21

8   8 -16 815.855 27.2753  15

16   8  -8 785.506 31.4860  18

8  16  -8 678.423 24.8118  18

-8   8 -16 794.895 29.0042  15

-16   0 -10 1.20173 4.38426   8

-16   0  10 1.05362 4.18880  10

-16  10   0-3.13121 4.66364  10

-16   0 -10 1.31194 4.31433   6

-16   0 -10 3.85080 3.78276   7

0  10  16-2.22662 3.94724  30

16  10   0-1.13042 4.61089  28

10  16   0-1.18293 4.57747  28

0  10  16 1.06905 4.36056  29

-10  16   0 2.90488 3.74690  30

0  16  10-0.98089 4.29054  30

0  16  10 1.11665 4.77700  29

0  16  10-1.02011 4.26366  26

-10   0  16 1.24781 4.10346  25

-16   0 -10 4.00395 4.37845  14

16   0 -10 1.34819 5.06995  12

10   0 -16 2.66622 5.95660  12

-10   0 -16 3.74521 5.46067  22

16  10   0 1.98867 4.05580  19

0  10 -16 2.40055 5.01671  20

0  16 -10 2.26727 5.27214  20

-10  16   0 4.27508 3.89918  21

10  16   0-2.72843 5.13021  19

10  16   0 6.25635 5.35291  16

16  10   0-1.21736 4.71068  18

0  10 -16 1.05301 3.59357  15

-10  -2 -16 62.0416 10.3963   8

-2  16  10 45.0451 6.45210   9

-10   2 -16 34.6714 8.56436   8

-16  -2 -10 37.3424 9.13255   8

-16   2  10 46.0610 8.45140  10

-16  -2  10 47.0986 7.38925  10

-16   2 -10 46.5401 8.24102   8

-16  10   2 31.0517 7.15490  10

-16  10  -2 42.8490 7.83525  10

-16  -2 -10 45.8970 7.95699   7

-16  -2 -10 35.9826 8.35474   6

-16   2 -10 46.9030 8.76582   6

-10  -2 -16 51.1798 8.98775   7

-2  10  16 51.4711 7.81118  30

16  10  -2 40.0276 7.81064  28

16  10   2 49.6913 8.16421  28

10  16  -2 46.5824 8.58277  28

10  16   2 33.5931 7.68480  28

2  10  16 46.3083 8.33138  29

-10  16   2 51.6870 7.41337  30

-2  10  16 54.0949 8.35762  29

2  16  10 40.9351 6.79694  30

2  16  10 40.8389 7.72070  29

-2  16  10 61.8570 9.47602  30

-2  16  10 50.6127 8.43143  29

-10   2  16 27.7891 7.91057  25

-10  -2  16 40.5623 8.03611  25

2  16  10 36.5856 7.42842  26

-2  16  10 48.1871 7.60213  26

-16   2 -10 57.1124 7.89298  14

-16 -10  -2 37.6054 6.31202  14

-16  -2 -10 23.5565 6.74318  14

16  -2 -10 52.7498 9.27455  12

16   2 -10 59.7921 9.53140  12

-10  16   2 45.2089 8.17622  13

-16  10   2 50.3996 6.56434  13

10  -2 -16 56.6541 9.43326  12

10   2 -16 42.6056 8.69036  12

-2  16 -10 47.6269 8.37704  23

-10  -2 -16 39.1504 8.35011  22

-10  16  -2 65.4719 9.01939  23

-16  10  -2 52.0448 8.97268  21

16  10  -2 57.2688 9.13133  19

-2  10 -16 47.6303 7.01199  22

10  16   2 47.8760 9.03123  19

-2  16 -10 43.7121 7.14184  22

-2  10 -16 56.2134 8.80072  20

2  16 -10 50.5531 8.07970  20

-2  16 -10 40.8450 8.55283  20

-10  16   2 51.9777 8.91312  21

-10  16  -2 38.0338 7.03247  21

-16  10   2 46.2755 8.49041  21

10  16  -2 47.5196 8.64552  16

10  16   2 46.6564 8.56613  16

16  10  -2 47.5248 8.87206  18

-2  10 -16 42.0485 7.78450  15

2  10 -16 41.1651 7.98594  15

-10  -4 -16 14.8680 6.39284   8

-4  16  10 7.87127 4.36733   9

-16  10   4 6.86214 3.42861   9

-16   4  10 1.20376 5.15003  10

-16  10   4 1.04678 4.47855  10

-16  10  -4 5.15937 3.59457  10

-16  -4 -10 11.8407 5.64018   6

-16   4 -10 6.70137 4.77845   6

-10  -4 -16 8.57654 6.12102   7

-4  10  16 6.84118 4.80060  30

16  10  -4 4.75797 4.51026  28

16  10   4-1.85685 4.14885  28

10  16  -4 0.99581 3.63350  28

10  16   4 5.74898 4.09947  28

-10  16   4 6.75700 4.00336  30

4  16  10 0.87351 3.65146  29

-4  10  16 5.85588 3.89101  29

-4  16  10 2.20209 4.60236  30

-10   4  16 3.19455 4.65819  25

-10  -4  16 3.14532 4.78165  25

10   4 -16 0.96361 4.39480  27

4  10  16 3.51901 3.01148  26

4  16  10 1.00682 4.00319  26

10  16   4 1.31296 2.80910  26

-16   4 -10 5.07821 3.32645  14

16  -4 -10 4.45215 4.86896  12

16   4 -10 5.48233 4.69106  12

-4  16  10 3.50576 4.07649  13

-10  16   4-1.06647 4.45785  13

-16  10   4 0.79888 3.92431  13

10  -4 -16-2.16845 4.31089  12

10   4 -16 4.50347 4.92507  12

-10  -4 -16 4.31008 4.71361  22

-4  16 -10 8.33917 5.03120  23

-10  16  -4 4.12816 5.32510  23

10  16  -4 3.12611 3.63513  23

4  10 -16 3.07115 2.96505  23

4  16 -10 1.08209 4.83540  23

-4  10 -16 4.26087 3.80819  22

-4  16 -10 0.92599 3.87080  22

-10  16  -4 4.23665 4.53149  22

10  16  -4 2.48234 4.08207  19

-4  10 -16 2.79990 3.90134  20

4  16 -10 3.50163 4.30013  20

10  16   4 4.91329 5.25510  19

-4  16 -10 11.4706 5.53628  20

16  10  -4 9.00458 5.13336  19

-16  10   4 1.07790 4.91596  21

4  10 -16 1.72525 3.60598  15

-10   4 -16 6.46486 3.46730  15

16  10   4 0.73897 3.30244  16

16   4 -10 1.15112 3.92885  18

16  10  -4 6.09215 5.21278  18

10  16  -4 6.49791 5.13290  18

-16 -10  -6 27.5645 6.79350   8

-10  -6 -16 32.4408 6.93373   8

-6  16  10 26.6042 5.52058   9

-16  10   6 17.8083 4.07614   9

-16  -6 -10 26.0806 7.02872   8

-16   6  10 13.3115 5.74075  10

-16  10   6 16.2466 5.59915  10

-16  10  -6 28.0408 5.36806  10

-16  -6  10 23.4009 5.49487   6

-16   6  10 21.4549 5.60766   6

10  16  -6 25.2557 5.60209  28

-6  10  16 29.4721 6.78711  30

16  10  -6 22.9515 4.93630  28

16  10   6 25.1215 4.99096  28

6  16  10 18.5711 4.58897  29

-10  16   6 33.1675 6.10070  30

-6  16  10 23.2610 5.85098  30

-10   6  16 21.2540 5.34324  25

-10  -6  16 24.9342 5.65262  25

10   6 -16 30.9117 6.05336  27

6  10  16 30.3633 5.65133  26

6  16  10 21.8182 5.70192  26

10  -6  16 21.5709 5.27710  25

10  16   6 30.1604 5.17478  26

10   6  16 20.4943 5.42550  25

16  -6 -10 25.4623 5.47211  12

16   6 -10 28.8971 5.99370  12

-6  16  10 33.7923 6.38710  13

-16  10   6 27.1346 5.87439  13

10  -6 -16 27.8755 5.96269  12

10   6 -16 26.1476 5.87586  12

-10   6  16 21.4895 5.27088  13

-10   6 -16 34.4735 7.33217  22

-6  10 -16 21.6486 4.95643  24

-6  16 -10 26.9332 6.25203  23

-16  10  -6 28.3270 5.20511  24

10  16  -6 35.1762 6.25846  23

6  10 -16 25.1107 4.89776  23

6  16 -10 27.1831 6.40076  23

-6  10 -16 23.8851 5.83540  22

-6  16 -10 22.2911 6.24110  22

-10  16  -6 26.3062 7.50107  22

10  16   6 22.1379 6.09741  19

10  16  -6 25.4827 6.36603  19

-6  16  10 31.7367 6.75235  21

-6  10 -16 30.3885 5.35271  20

-10  16   6 29.9033 7.05206  21

-16  10   6 19.4993 5.61853  21

6  10 -16 27.2948 5.47215  15

-10   6 -16 24.9992 5.75675  15

-6  10 -16 29.4775 6.50546  15

16   6 -10 30.3882 7.35459  18

16  10  -6 30.2822 7.66804  18

10  16  -6 18.8392 5.68638  18

-8  16  10 6.58017 3.77482   9

-10  -8 -16 3.47702 3.23712   8

-16 -10  -8 9.82891 4.22829   8

-16  -8 -10 12.4962 4.88661   8

-16   8  10 8.11212 5.20123  10

-16  10   8 9.63209 4.20789  10

-10  -8 -16 5.59280 4.16732   7

-8 -10 -16 7.50668 4.37233   7

-8  10  16 4.93907 3.68080  30

-10  16   8 5.67159 3.48492  30

-8  16  10 8.97840 4.07991  30

16   8 -10 6.63217 2.94263  27

8  10  16 6.63045 3.36998  26

8  16  10 8.17801 3.65427  26

10  16   8 5.12914 2.80794  26

-8  16  10 5.41027 3.92741  13

-10  16   8 5.05860 4.07139  13

-16  10   8 8.25426 4.33082  13

-10   8  16 12.0789 3.68250  13

-16   8  10 9.58506 4.18737  13

-8  10 -16 3.96936 3.62304  24

-16   8 -10 7.30976 3.48455  24

-16  10  -8 10.2660 3.44247  24

-8  16 -10 13.4220 4.41933  23

-10  16  -8 4.44444 3.64095  23

-10   8 -16 4.32720 3.53282  22

10  16  -8 12.6161 4.11959  23

8  16 -10 9.61750 4.26464  23

-16  10   8 6.76881 3.59641  21

-8  10 -16 7.28356 4.04529  22

-8  16 -10 10.6872 4.91881  22

10  16  -8 6.37248 4.36135  19

-8  16  10 13.1288 4.67440  21

-10  16   8 17.3457 5.16663  21

8  10 -16 10.2264 3.20588  15

-10   8 -16 4.23481 3.58693  15

-8  10 -16 11.8435 4.66914  15

10   8 -16 9.90178 4.45459  18

10   8 -16 16.7092 3.71424  15

16   8 -10 9.26979 4.93187  18

16  10  -8 7.52077 4.37431  18

10  16  -8 5.14720 3.21723  18

-12   0 -16 163.112 13.7201   8

-16   0  12 182.696 12.5366  10

-16   0 -12 207.858 14.3605   8

16  12   0 177.509 13.0100  28

0  12  16 174.284 12.8689  29

0  16  12 194.705 12.2480  30

0  16  12 198.936 13.6437  29

12  16   0 178.225 13.3252  28

0  16  12 180.536 11.9126  26

-12   0  16 202.573 14.3999  25

12   0 -16 210.395 15.0748  12

16   0 -12 202.603 14.8208  12

0  16 -12 221.436 14.1517  23

-12   0 -16 196.935 13.5837  22

16  12   0 191.443 12.9565  19

0  12 -16 198.237 14.3086  20

0  16 -12 198.154 13.8423  20

12  16   0 204.075 14.7948  19

-12  16   0 177.581 12.9027  21

-16  12   0 197.217 14.0898  21

-16   0 -12 211.202 12.0804  14

0  12 -16 187.771 12.0473  15

12  16   0 229.717 14.9028  16

-16   2 -12 43.0891 7.05775   8

-12   2 -16 24.4637 6.27043   8

-16   2  12 23.2679 5.91011  10

-16  -2 -12 34.7504 7.53459   8

-16  12   2 25.7528 4.96797  10

-16  -2 -12 22.1335 5.15535   7

-12  -2 -16 25.7944 5.89277   7

12  16  -2 29.4385 6.27246  28

12  16   2 29.1686 6.47149  28

16  12  -2 26.0440 5.73468  28

16  12   2 31.9604 6.17640  28

2  12  16 40.9470 6.81366  29

-2  12  16 36.7201 6.25328  29

2  16  12 34.9103 6.70191  29

-2  16  12 32.9814 6.50177  30

-2  12  16 34.1919 5.74130  30

-12   2  16 34.3659 7.40718  25

-12  -2  16 26.3787 6.09932  25

2  16  12 39.4075 6.55742  26

16  -2 -12 44.2236 7.79682  12

16   2 -12 26.8727 6.37682  12

-16  -2 -12 23.6775 5.29786  14

-12  16   2 33.4155 6.04340  13

12  -2 -16 36.0086 7.37448  12

12   2 -16 24.3001 6.14890  12

2  16 -12 30.7664 6.63292  23

-2  16 -12 28.1351 6.15478  23

-12   2 -16 24.6240 5.90599  22

-12  -2 -16 26.1981 5.84382  22

-16  12  -2 27.1524 6.30987  21

16  12   2 30.9765 5.39082  19

12  16   2 32.3393 6.73161  19

16  12  -2 26.4463 6.19156  19

-2  12 -16 36.0629 7.07643  20

2  16 -12 30.0005 6.22820  20

-2  16 -12 40.7535 7.25197  20

12  16  -2 44.6421 7.46559  19

-12  16   2 19.1616 5.54617  21

-12  16  -2 31.3607 5.78058  21

-16  12   2 30.1978 6.74350  21

12  16  -2 31.4587 6.44911  16

16  12   2 39.2646 5.68461  16

12  16   2 37.2543 6.54165  16

-2  12 -16 20.4914 5.35771  15

16  12  -2 27.0731 6.66943  18

2  12 -16 27.2323 5.23861  15

-12  -4 -16 642.071 26.1445   8

-16  -4 -12 670.433 24.6523   7

-12  16   4 655.198 24.8865   9

-16   4  12 639.763 25.4136  10

-12  -4 -16 628.613 25.2741   7

-4  16  12 598.978 20.9956   9

4  12  16 657.841 24.5216  29

4  16  12 649.819 23.3910  29

16  12  -4 592.450 22.7773  28

16  12   4 674.803 23.7004  28

-4  16  12 664.586 24.7852  30

-4  12  16 616.039 22.7596  29

-4  12  16 664.311 23.8802  30

-4  16  12 643.652 24.9181  29

12  16  -4 613.684 23.2403  28

12  16   4 639.477 23.2825  28

12   4 -16 644.473 23.7700  27

4  12  16 644.057 21.1957  26

4  16  12 664.869 23.9469  26

-12   4  16 631.941 24.3958  25

-12  -4  16 593.592 23.5687  25

12  -4 -16 644.355 24.6011  12

12   4 -16 619.571 24.3742  12

16  -4 -12 673.023 25.1635  12

16   4 -12 593.537 23.9402  12

-16  -4 -12 645.494 23.7245  14

-12  16   4 645.851 23.9939  13

-16  12   4 667.619 21.9216  13

-4  12 -16 652.858 21.7770  22

4  16 -12 664.681 24.7427  23

-12  -4 -16 638.694 23.4894  22

-4  16 -12 676.311 23.6896  23

-4  16 -12 653.856 22.4505  22

-12   4 -16 663.114 25.1480  22

4  12 -16 649.253 25.4436  20

4  16 -12 659.735 23.5199  20

-4  12 -16 633.338 23.8043  20

-16  12   4 664.312 25.2346  21

12  16   4 712.176 26.2600  19

16  12  -4 624.459 25.3551  19

16  12   4 613.051 21.7441  16

12  16   4 663.226 25.4472  16

16   4 -12 618.181 25.1389  18

16  12  -4 659.713 26.2686  18

-4  12 -16 604.846 23.3383  15

4  12 -16 609.611 20.4767  15

-12  -6 -16 20.5555 5.29916   8

-6  16  12 22.9118 4.41527   9

-12  16   6 20.4954 4.70511   9

-16   6  12 25.2751 5.57529  10

-16  -6 -12 23.2018 5.46064   8

-16  -6 -12 13.0414 4.43834   7

-12  -6 -16 23.6593 5.47863   7

-12   6  16 19.7000 4.76605  30

-6  16  12 12.5275 4.15722  30

-6  12  16 22.3805 5.03435  30

16   6 -12 15.7962 4.19744  27

6  16  12 17.2533 4.33571  26

-12  16   6 24.1701 5.31816  13

16  12  -6 16.2622 4.93112  19

-6  16 -12 18.9414 4.69075  22

-12  16  -6 16.6205 4.63050  22

6  12 -16 21.8972 5.12491  20

12  16  -6 16.3548 4.95906  19

-12  16   6 17.2774 4.75902  21

-16  12   6 16.9733 4.80868  21

-6  12 -16 20.0256 4.59782  15

12  16   6 19.0221 4.76990  16

16   6 -12 25.7861 5.65563  18

16  12  -6 20.3048 5.35696  18

6  16 -12 20.5587 5.14344  23

-12   6 -16 20.1915 4.97729  22

16   0 -14-0.70615 2.73249  12

14   0 -16 0.71115 2.97233  12

-17  -1   1 147.586 14.2571  10

-17  -1  -1 144.524 14.2382  10

-17   1   1 110.574 13.6372  10

-17   1  -1 112.161 13.4966  10

-17  -1   1 144.969 15.5607   6

-17  -1  -1 122.074 13.9318   6

-1  17  -1 132.325 14.2305  30

1  17  -1 111.170 13.1751  30

1  17   1 127.232 13.9593  30

-1  17   1 107.475 13.2448  30

1  -1  17 141.107 14.5451  25

-1  -1  17 123.175 13.7121  25

-17  -1  -1 95.2685 12.0340  14

-1   1 -17 115.991 11.9487  22

1  17  -1 118.652 11.4098  23

-1  17  -1 110.260 11.3734  23

-1  17   1 103.398 10.1955  23

1  17  -1 117.705 12.1739  19

1  17   1 137.747 13.4151  19

-1   1 -17 136.853 12.5184  15

-1  -1 -17 101.187 10.1850  15

1   1 -17 111.935 11.9676  15

-17  -1   1 137.562 13.6919  14

-17   1  -1 122.872 13.6470  14

1  17  -1 124.731 11.9886  16

-17   1   1 130.545 13.9215  14

1  17   1 128.213 11.5610  16

-17   1   3 531.489 28.1139  10

-17  -1   3 520.299 26.0551  10

-17   3   1 530.238 28.7293  10

-17   3  -1 542.217 29.0871  10

-17  -3   1 532.499 24.6899  10

-17   1  -3 516.136 28.0647  10

-17  -3  -1 593.760 26.3323  10

-17  -1  -3 500.177 26.4764  10

-17  -1   3 577.385 29.9368   6

-17  -3   1 530.116 28.0289   6

-17   3   1 518.021 27.9710   6

-17  -3  -1 509.610 27.7957   6

-17   3  -1 517.164 28.0555   6

-17  -1  -3 551.078 29.2960   6

1  17  -3 511.330 27.5617  30

3  17  -1 572.606 27.9114  30

3  17   1 554.872 27.1921  30

-3  17  -1 611.113 29.1696  30

1  17   3 539.587 27.2949  30

-1  17   3 534.228 27.7945  30

3  -1  17 551.279 28.5302  25

1  -3  17 531.384 27.2460  25

1   3  17 586.184 29.0627  25

-1  -3  17 579.235 28.5521  25

-1   3  17 543.087 28.2931  25

-3  -1  17 508.255 27.3897  25

1  17   3 498.873 25.9662  26

3  17   1 539.046 25.4184  26

17  -1  -3 527.210 29.1200  12

3  -1 -17 556.459 29.0252  12

-3   1 -17 569.330 26.9340  22

3  17  -1 542.639 23.0712  23

1  17  -3 511.057 24.8843  23

-1  17  -3 543.153 26.0698  23

-1   3 -17 551.191 24.0939  22

-3  17  -1 547.622 25.1293  23

-3  17   1 545.325 22.9542  23

3  17  -1 605.337 27.7799  19

3  17   1 606.615 28.9741  19

1  17  -3 477.278 22.0834  19

1  17   3 544.100 27.8033  19

1   3 -17 543.500 26.1596  15

-17  -3  -1 537.626 26.7221  14

-17  -1  -3 536.595 27.6435  14

-17  -3   1 522.664 25.3148  14

-17  -1   3 517.455 25.2253  14

-3  -1 -17 511.437 21.4016  15

-3   1 -17 531.920 23.4212  15

3  17  -1 514.840 25.4648  16

-1   3 -17 589.257 26.5986  15

3  17   1 524.900 25.2698  16

1  17   3 495.118 21.9000  16

-3  17   3 94.4391 9.64680   9

-17   3   3 114.083 13.6073  10

-17  -3   3 118.919 11.6948  10

-17  -3  -3 110.698 11.9070  10

-17   3  -3 102.446 13.3058  10

-17  -3   3 99.5981 12.5225   6

-17   3   3 75.3768 11.8929   6

-17  -3  -3 109.504 13.2027   6

-17   3  -3 100.833 12.8452   6

3  17   3 113.595 11.8873  30

-3  17  -3 111.199 12.5947  30

-3  17   3 111.541 12.9100  30

3   3  17 129.509 14.1308  25

-3   3  17 112.437 12.6023  25

3   3 -17 99.9485 9.39323  27

-3  -3  17 102.389 12.6462  25

3  17   3 103.308 11.9911  26

3  -3  17 100.328 12.2375  25

-17   3  -3 94.7694 11.9438  14

17   3  -3 96.8145 12.4750  12

17  -3  -3 113.844 14.4369  12

3  -3 -17 108.242 12.7590  12

3   3 -17 112.344 13.2630  12

3  17  -3 93.8994 11.2458  23

-3  17  -3 109.391 12.0493  23

-3   3 -17 108.814 12.1507  22

3  17  -3 101.999 11.4523  19

3  17   3 93.4524 12.4850  19

3  17   3 84.2906 10.6392  16

-17  -3  -3 105.662 12.5739  14

-17  -3   3 97.7877 10.6543  14

-3   3 -17 94.2789 11.0688  15

-5  17   1 500.077 23.3010   9

-17   1   5 553.929 28.0059  10

-17  -1   5 496.060 24.9875  10

-17   1  -5 555.439 26.1838   8

-17   1  -5 559.108 28.7337  10

-17  -1  -5 542.898 27.2956  10

-17  -1   5 501.054 28.0843   6

-17  -5   1 491.115 25.4861   6

-17   5   1 492.278 25.8735   6

-17  -5  -1 458.551 24.8189   6

-17   5  -1 549.096 27.0852   6

-17  -1  -5 581.676 29.5782   6

5   1 -17 488.214 20.4726  27

-1   5  17 516.579 22.0841  29

5  17   1 516.767 24.5188  30

-5  17  -1 541.138 26.7105  30

-5  17   1 568.035 27.5561  30

1  17   5 530.470 25.9832  30

-1  17   5 507.043 26.5067  30

1  17   5 475.910 22.1632  29

-1  17   5 531.533 24.5351  29

1  -5  17 548.788 26.3072  25

1   5  17 513.175 25.6230  25

-1  -5  17 543.657 26.5911  25

-1   5  17 537.351 26.2299  25

-5  -1  17 504.810 27.1202  25

5  17   1 519.420 23.2497  26

-1  17   5 501.568 25.8069  26

5  -1  17 481.814 26.5754  25

17  -1  -5 504.696 28.1474  12

5  -1 -17 528.763 28.0207  12

5  17  -1 518.230 21.3496  23

1  17  -5 496.028 25.1536  23

-5   1 -17 534.264 27.0032  22

-1  17  -5 482.420 25.2525  23

-5  17  -1 557.893 25.3043  23

-5  17   1 497.048 22.3907  23

-1   5 -17 529.470 22.5689  22

5  17  -1 453.302 25.2193  19

-5  17   1 478.040 24.7502  21

-5  17  -1 517.411 23.7404  21

1  17  -5 517.998 23.0828  20

5  17   1 500.173 27.4808  19

5  17   1 492.632 25.5861  16

1   5 -17 519.035 25.9539  15

-17   1  -5 488.076 25.7679  14

17   5  -1 513.223 23.1384  18

-17  -5  -1 506.180 24.7913  14

-5   1 -17 546.657 22.2771  15

-17  -5   1 449.418 22.5090  14

-1   5 -17 521.932 25.6405  15

5  17  -1 489.016 25.7134  16

-3  17   5 80.9253 8.75295   9

-17   3  -5 91.0156 9.98998   8

-5  17   3 77.2775 9.77793   9

-17  -3  -5 100.656 11.0533  10

-17  -5  -3 102.745 10.4461  10

-17   3   5 96.6949 12.0969  10

-17   5   3 104.177 13.0031  10

-17  -3   5 83.9366 9.86062  10

-17   3  -5 97.1481 12.3666  10

-17  -5  -3 100.947 11.7552   6

-17   5  -3 82.5256 10.9586   6

-17  -3  -5 91.2622 11.4612   6

-17   3  -5 83.0368 11.5907   6

-17  -3   5 108.393 12.7115   6

-17   3   5 84.7330 12.2507   6

-17  -5   3 97.8507 11.8867   6

-17   5   3 83.0304 11.0243   6

3  17   5 87.0491 8.81499  29

-5  17  -3 93.0009 11.2560  30

5  17   3 86.6470 10.0931  30

3  17   5 90.0657 10.5616  30

-5  17   3 90.4508 11.3278  30

-3  17   5 95.5528 11.9656  30

3  -5  17 76.9424 10.7508  25

3   5  17 87.3911 10.9795  25

3   5 -17 96.4367 9.69298  27

5   3 -17 80.4794 9.26902  27

-3  -5  17 92.1284 12.2152  25

-3   5  17 90.4917 11.5386  25

-5   3  17 85.3973 11.9057  25

-5  -3  17 85.5328 11.1786  25

5  17   3 104.445 11.1963  26

5  -3  17 74.2571 10.7564  25

5   3  17 106.253 12.4199  25

3  17   5 90.5300 10.8475  26

17  -3  -5 88.0653 12.1009  12

17   5  -3 78.5285 11.4355  12

17  -5  -3 87.9238 12.0717  12

-17  -5   3 79.9090 8.83337  14

-17   3  -5 94.0210 11.5219  14

-17  -5  -3 94.5189 11.5275  14

-17  -3  -5 95.1256 11.7906  14

-5  17   3 96.8342 11.9601  13

5  -3 -17 93.9901 12.1498  12

5   3 -17 85.6270 11.7717  12

17   3  -5 89.9637 11.9005  12

3  17  -5 70.6898 9.87323  23

-3  17  -5 77.6217 10.8289  23

5  17  -3 100.474 10.2853  23

-5   3 -17 107.862 12.2743  22

-5  17  -3 103.878 11.7041  23

-3   5 -17 111.400 11.7498  22

5  17   3 110.456 13.3245  19

3  17  -5 75.2166 9.01272  19

-3  17  -5 68.6150 10.5933  22

-3   5 -17 76.1901 8.44888  20

3  17   5 106.195 13.2077  19

5  17  -3 97.1897 12.1373  19

5  17  -3 78.4180 11.3574  16

3   5 -17 107.643 12.0174  15

5  17   3 103.125 11.5005  16

3  17   5 90.2391 10.2966  16

17   5  -3 98.9334 10.5028  18

17   3  -5 81.0905 10.0885  18

-5   3 -17 71.5507 9.03554  15

-3   5 -17 97.4310 11.3232  15

-5  17   5 115.586 10.5726   9

-17   5   5 121.166 13.4794  10

-17   5  -5 145.942 14.4370  10

-17   5  -5 95.8343 11.5907   6

-17  -5   5 113.522 12.2045   6

-17   5   5 101.339 11.8563   6

-17  -5  -5 106.058 11.6707   6

5  17   5 99.7739 9.94715  30

5  -5  17 130.317 12.5693  25

-5  -5  17 109.324 12.2423  25

5   5 -17 94.3206 10.0889  27

5  17   5 101.552 11.0627  26

-5   5  17 81.2713 10.9533  25

5   5  17 96.5968 11.3247  25

-17  -5  -5 117.174 12.3054  14

-5  17   5 76.9650 11.0699  13

5  -5 -17 93.9398 11.0435  12

5   5 -17 94.6805 11.9619  12

17   5  -5 85.2701 11.2604  12

17  -5  -5 104.147 12.2643  12

-5  17  -5 98.3394 11.3570  23

5  17  -5 108.392 11.2436  23

-5   5 -17 121.664 12.7123  22

-5  17  -5 105.879 12.0764  22

5  17  -5 91.5588 10.5981  19

5  17   5 115.476 11.6659  16

17   5  -5 92.1921 11.1626  18

-5   5 -17 98.2273 10.5141  15

-17   5  -5 120.190 11.8872  14

-17  -1  -7 73.7792 11.0296   8

-17   1  -7 76.7859 10.2314   8

-7  17   1 76.7489 9.75236   9

-7  -1 -17 97.1029 12.4282   8

-17   1   7 73.4822 10.1849  10

-17  -1   7 80.3209 10.1922  10

-17   7   1 92.2334 11.5794  10

-17   7  -1 81.3287 11.2394  10

-17   1  -7 97.4148 11.9755  10

-17  -1  -7 78.9784 10.5419  10

-17   7  -1 66.7908 9.32693   6

-17  -1  -7 81.7684 11.1007   6

-17  -7   1 69.3140 9.17458   6

-17   7   1 82.3957 9.94288   6

-17  -7  -1 64.1895 9.06128   6

7  17   1 56.9421 9.40596  28

-1   7  17 61.4132 8.37751  30

-1   7  17 69.3092 9.13405  29

-7  17  -1 80.6873 10.4252  30

-7  17   1 80.1280 10.3800  30

1  17   7 69.7049 10.1701  30

-1  17   7 91.7018 11.4707  30

1  17   7 91.2470 10.0403  29

-1  17   7 86.0235 10.1973  29

1  -7  17 77.7174 9.87912  25

1   7  17 79.1882 9.70118  25

7   1 -17 69.3421 8.58991  27

-1  -7  17 95.9315 10.5272  25

-1   7  17 74.6725 9.45594  25

-7  -1  17 70.7523 10.9039  25

1  17   7 85.4535 10.8536  26

7  17   1 66.9741 8.02697  26

-1  17   7 56.0323 9.19477  26

17   7  -1 67.8208 9.51554  12

17  -7  -1 88.5939 10.9189  12

-17   1  -7 78.0348 10.4940  14

-17  -7  -1 71.7482 8.78416  14

-17  -1  -7 84.7732 11.0037  14

17  -1  -7 87.2216 12.2376  12

7  -1 -17 81.7346 11.0240  12

1  17  -7 76.3065 10.6803  23

-1  17  -7 78.5607 10.6466  23

-7  -1 -17 69.5206 10.2895  22

-7  17  -1 77.8289 9.68561  23

-7  17   1 68.5339 8.64450  23

-7   1 -17 72.3314 10.7343  22

7  17  -1 78.8106 11.2340  19

-17   7   1 65.3062 10.0681  21

7  17   1 83.2339 12.1443  19

-1   7 -17 70.1617 9.88340  20

-7  17   1 82.6605 10.7027  21

1  17  -7 83.5030 9.81474  20

-7  17  -1 72.2231 9.29922  21

-1  17  -7 73.5816 10.1038  20

1   7 -17 69.6962 10.0809  15

7  17  -1 71.1517 10.4399  16

7  17   1 82.5169 10.6333  16

17   7  -1 84.5636 10.0310  18

-17  -7   1 73.0742 8.17742  14

17   7   1 68.3304 9.13561  18

-1   7 -17 57.9763 9.37927  15

-3  17   7 383.741 17.4612   9

-7  -3 -17 419.259 23.8587   8

-7  17   3 380.571 20.1820   9

-17   3   7 337.077 21.5075  10

-17   7   3 394.783 23.0241  10

-17   7  -3 363.922 21.4540  10

-17  -3  -7 372.382 22.5863   8

-17   3  -7 378.803 18.5509   8

-17  -3   7 346.300 21.7236   6

-17   3   7 373.945 22.9058   6

-17  -7   3 345.098 18.6758   6

-17   7   3 348.242 19.0342   6

-17  -7  -3 422.019 20.2472   6

-17   7  -3 350.454 19.2104   6

-17  -3  -7 386.241 22.1914   6

-17   3  -7 401.137 22.6006   6

-7  17  -3 380.431 19.3557  30

-3   7  17 364.024 17.1989  29

3  17   7 379.303 19.0041  30

7   3 -17 350.414 18.4376  27

-7  17   3 368.432 20.9331  30

-3  17   7 388.903 21.8101  30

3  17   7 334.912 17.3882  29

3  -7  17 409.250 19.8056  25

3   7  17 378.055 19.3090  25

-3   7  17 339.399 18.5550  25

-3  -7  17 390.157 19.7507  25

-7   3  17 373.621 21.7713  25

-7  -3  17 380.522 21.8623  25

7  17   3 357.876 18.1566  26

7  -3  17 416.427 22.6759  25

7   3  17 387.819 21.9611  25

17   3  -7 350.884 21.6464  12

17  -3  -7 412.927 23.4739  12

17   7  -3 328.756 18.9491  12

17  -7  -3 376.620 20.1539  12

-17   7   3 387.601 17.4929  13

7  -3 -17 377.366 21.9429  12

7   3 -17 392.508 22.7064  12

7  17  -3 354.852 17.6673  23

3  17  -7 358.350 20.5400  23

-3  17  -7 390.466 21.7173  23

-7   3 -17 396.290 22.3463  22

-7  17  -3 340.464 19.8457  23

-3   7 -17 375.216 19.1032  22

-3  17  -7 398.437 20.8872  22

-3   7 -17 348.894 18.2406  20

7  17  -3 422.613 22.9835  19

3  17  -7 369.640 17.8699  20

-7  17   3 373.595 21.7409  21

-7  17  -3 333.564 16.5692  21

-17   7   3 391.893 21.5888  21

7  17   3 421.033 22.4137  16

3  17   7 359.708 17.9691  16

17   3  -7 398.411 20.4856  18

-17   3  -7 351.291 19.6546  14

17   7  -3 374.886 20.5114  18

-7   3 -17 402.901 18.5678  15

-17  -7  -3 369.989 20.0595  14

-3   7 -17 373.481 20.8365  15

7  17  -3 389.255 22.0334  16

-5  17   7 308.359 16.4338   9

-7  17   5 337.837 18.0927   9

-7  -5 -17 348.362 20.3777   8

-17   5   7 312.601 20.0315  10

-17   7   5 333.962 20.4524  10

-17   7  -5 285.320 18.4621  10

-17   5  -7 325.716 19.9245  10

-17  -5   7 300.277 18.4420   6

-17   5   7 292.892 18.5342   6

-17  -7   5 278.228 16.3311   6

-17   7   5 314.324 17.3167   6

-17  -7  -5 305.001 16.6397   6

-17   7  -5 305.588 16.9431   6

-17  -5  -7 320.464 18.6266   6

-17   5  -7 309.491 18.6079   6

-7  17   5 328.726 19.0973  30

-5  17   7 336.973 20.1054  30

5  -7  17 334.330 17.1409  25

5   7  17 316.994 16.8508  25

7   5 -17 293.483 17.0457  27

5   7 -17 296.968 17.2703  27

-5   7  17 312.637 16.9441  25

-5  -7  17 305.307 16.7682  25

-7   5  17 331.320 18.7557  25

-7  -5  17 293.874 17.9779  25

5  17   7 305.748 18.3888  26

7  17   5 309.694 17.0519  26

-17   5  -7 283.374 14.1616  24

7  -5  17 265.236 16.9515  25

7   5  17 295.645 17.5939  25

-17  -7  -5 318.393 18.6038  14

-17  -5  -7 327.009 19.3671  14

-5  17   7 330.136 19.5374  13

17   5  -7 266.739 17.6231  12

17  -5  -7 272.023 17.7598  12

-7  17   5 315.180 19.2634  13

17   7  -5 281.631 16.5146  12

17  -7  -5 294.052 17.0369  12

-17   7   5 316.958 16.8142  13

7  -5 -17 273.895 17.3242  12

7   5 -17 317.171 18.9150  12

7  17  -5 326.780 17.8350  23

5  17  -7 299.117 17.9096  23

-5  17  -7 317.795 19.0646  23

-7  17  -5 311.528 18.4548  23

-7   5 -17 291.134 18.6172  22

-5   7 -17 335.950 18.7803  22

-5  17  -7 316.174 18.6679  22

-7  17  -5 340.024 19.8146  22

7  17  -5 276.639 18.0158  19

5  17  -7 271.691 15.4181  19

-17   7   5 336.162 18.5070  21

7  17   5 290.230 19.5367  19

5   7 -17 299.568 17.9041  15

7  17   5 342.044 19.1693  16

17   5  -7 308.579 18.5247  18

17   7  -5 337.834 19.5978  18

-7   5 -17 337.069 17.5726  15

-5   7 -17 327.159 18.5162  15

-17  -7  -7 74.9936 10.1939   8

-7  17   7 59.9572 7.58119   9

-17   7  -7 67.5323 8.98907  10

-17  -7  -7 69.1642 7.98069   6

-17   7  -7 59.9039 7.74761   6

-17  -7   7 54.7237 7.48148   6

-17   7   7 49.5426 7.13908   6

17   7  -7 57.4226 6.91721  28

17   7   7 57.6410 6.67135  28

-7  17   7 55.2723 8.31674  30

-7  -7  17 51.4878 7.24795  25

7   7 -17 55.0044 7.83285  27

7  17   7 57.9994 7.96442  26

7  -7  17 48.0260 6.73540  25

7   7  17 39.1995 6.35738  25

-7   7  17 71.0977 8.37110  25

-17  -7  -7 73.9012 9.12431  14

17  -7  -7 60.5551 7.79408  12

17   7  -7 51.3999 7.34802  12

-7  17   7 74.0716 9.39575  13

-17   7   7 84.0252 9.15497  13

-17   7  -7 51.1873 6.20814  24

-7   7 -17 65.6454 8.67086  22

7  17  -7 57.5657 8.14895  23

-7  17  -7 77.6691 9.33434  22

-7  17   7 65.4710 9.49937  21

7  17  -7 62.1366 7.95963  19

-7   7 -17 85.5737 9.19979  15

7   7 -17 57.8658 7.90876  15

17   7  -7 55.8971 8.82710  18

-17   9   1 96.3236 10.6781  10

-9  -1 -17 90.6468 11.6124   8

-17  -1  -9 70.7572 10.2418   8

-9   1 -17 70.4185 10.7221   8

-17   1  -9 77.5680 9.74315   8

-17   1   9 60.9426 9.34768  10

-17  -1   9 71.2166 9.18025  10

-17   9  -1 93.0098 10.7907  10

-17  -1  -9 87.3292 11.0960   6

-17  -1  -9 77.9559 8.56705   7

17   9   1 93.6747 10.3896  28

-1   9  17 57.9428 7.21713  30

1   9  17 95.6259 10.3692  29

-1   9  17 90.2912 9.48501  29

1  17   9 92.3120 9.55715  30

-9  17  -1 83.6836 8.66533  30

-9  17   1 74.6510 8.77157  30

9  17   1 79.8542 9.92580  28

-1  17   9 87.6714 9.87035  30

1  17   9 75.8021 9.25279  29

-1  17   9 87.3442 10.1479  29

1  17   9 83.1546 9.71368  26

-1  17   9 75.4978 9.65144  26

-9  -1  17 77.1595 10.0628  25

-17   1  -9 76.4768 9.26829  14

-17  -1  -9 60.0549 8.72284  14

17  -1  -9 77.2390 10.8702  12

9  -1 -17 90.5430 10.6794  12

-9  17  -1 79.4843 9.20014  23

1  17  -9 85.3848 9.83190  23

-9   1 -17 79.9482 10.6445  22

9  17  -1 82.6718 10.8085  19

-17   9   1 98.9002 11.0132  21

17   9  -1 72.8777 8.75431  19

1   9 -17 67.0911 9.77503  20

-1   9 -17 72.2076 9.74115  20

1  17  -9 69.1595 9.21105  20

-1  17  -9 80.9612 10.1165  20

-9  17   1 73.1363 9.68323  21

-9  17  -1 82.5369 9.34161  21

-17  -9  -1 90.1229 8.43391  14

17   1  -9 78.2236 8.78291  18

17   9  -1 71.3168 9.37955  18

1   9 -17 78.7534 9.80285  15

-3  17   9 286.417 14.0291   9

-9  -3 -17 320.353 19.8410   8

-9  17   3 307.717 17.5892   9

-17   3   9 294.530 18.5847  10

-17   9   3 329.268 18.8121  10

-17   9  -3 326.816 17.8744  10

-17  -3  -9 319.495 19.8177   8

-17   3  -9 283.919 15.1360   8

-17  -3  -9 317.323 18.7528   6

-17   3  -9 301.896 18.6690   6

17   9  -3 307.820 17.3796  28

17   9   3 322.128 17.5139  28

3   9  17 350.426 18.7435  29

-9  17   3 308.553 16.6731  30

-3   9  17 307.028 15.6209  29

-3  17   9 309.066 18.2175  30

3  17   9 296.892 16.1685  29

9   3 -17 293.519 16.1171  27

-3   9  17 292.776 16.3449  30

-3  17   9 305.233 17.9042  29

9  17  -3 286.468 17.4055  28

9  17   3 323.303 17.9612  28

-9   3  17 305.633 18.1800  25

-9  -3  17 284.064 17.8254  25

3  17   9 300.768 17.6097  26

9  17   3 302.061 14.2387  26

-17  -3  -9 316.479 17.9571  14

17  -3  -9 284.439 18.1719  12

17   3  -9 279.369 18.0570  12

-9  17   3 332.635 18.8283  13

-17   9   3 298.825 14.3104  13

9  -3 -17 291.993 18.0741  12

9   3 -17 298.284 18.8876  12

-3   9 -17 319.798 15.7241  22

3  17  -9 331.615 18.5410  23

-9   3 -17 316.430 19.1389  22

-9  17  -3 299.044 17.2660  23

-3  17  -9 281.397 16.1314  22

-3   9 -17 323.866 17.0437  20

9  17  -3 277.904 18.5239  19

3  17  -9 298.114 16.1114  20

-9  17   3 305.215 18.3939  21

9  17   3 329.022 19.9269  19

-17   9   3 294.183 17.9484  21

17   9  -3 304.456 17.3965  19

9  17   3 316.186 18.6706  16

-17  -9  -3 296.533 15.9177  14

-17   3  -9 277.199 15.2462  14

17   3  -9 289.404 17.1922  18

17   9  -3 290.768 17.9782  18

-9   3 -17 281.944 14.1181  15

-3   9 -17 320.381 18.0466  15

3   9 -17 299.437 16.9847  15

-5  17   9 320.243 15.4704   9

-9  -5 -17 391.316 20.2995   8

-9  17   5 324.659 17.2338   9

-17   5   9 327.840 19.0049  10

-17   9   5 335.660 18.5732  10

-17   9  -5 311.087 16.7437  10

-17  -5   9 327.489 17.9120   6

-17   5   9 308.903 17.4187   6

-17  -5  -9 319.508 17.1487   6

-17   5  -9 330.145 17.5708   6

17   9  -5 337.410 16.6594  28

17   9   5 338.371 16.4685  28

-9  17   5 325.053 16.7805  30

-5  17   9 301.524 17.5554  30

5  17   9 286.073 14.1768  29

-5   9  17 366.174 18.0687  30

9   5 -17 357.551 17.3206  27

5   9  17 317.197 14.3216  26

-9   5  17 300.301 16.8657  25

-9  -5  17 345.815 17.8495  25

9  17   5 306.192 15.0138  26

9  -5  17 355.956 17.6915  25

9   5  17 291.112 16.0039  25

-17  -9  -5 300.384 16.3679  14

17  -5  -9 334.831 17.7170  12

17   5  -9 298.011 16.8243  12

-5  17   9 326.144 17.2752  13

-17   9   5 307.374 15.3876  13

9  -5 -17 372.603 18.2915  12

9   5 -17 318.194 17.5082  12

-5   9 -17 308.155 16.2554  22

9  17  -5 325.839 16.0276  23

5  17  -9 361.637 18.5784  23

-5  17  -9 326.832 17.6402  23

-9  17  -5 339.814 17.7796  23

-9   5 -17 348.406 19.0173  22

-5  17  -9 333.299 17.6210  22

9  17  -5 327.227 18.5125  19

-5   9 -17 275.444 14.0633  20

-17   9   5 324.128 17.4398  21

9  17   5 328.693 19.2612  19

17   9  -5 316.505 17.5789  19

9  17   5 352.691 18.6749  16

17   5  -9 360.402 18.8017  18

17   9  -5 337.879 18.8525  18

-9   5 -17 305.112 15.1665  15

-5   9 -17 353.915 18.3685  15

5   9 -17 319.204 16.4444  15

-7  17   9 31.2328 5.54320   9

-17  -9  -7 51.9576 7.82175   8

-9  17   7 39.0146 6.19366   9

-17  -7  -9 48.0738 7.76543   8

-9  -7 -17 33.2771 6.06823   8

-17   9   7 45.3213 7.09297  10

-9  -7 -17 27.5322 6.57032   7

-7   9  17 34.6788 6.61180  30

-9   7  17 43.3732 6.79076  30

-9  17   7 40.1948 6.54474  30

9   7 -17 39.7277 6.30022  27

7   9  17 45.0569 5.78472  26

7  17   9 29.5388 5.65039  26

9  17   7 31.4635 5.18082  26

-7   9 -17 31.9278 5.17512  24

-17   7  -9 33.9919 5.06131  24

-7  17  -9 33.4139 6.33351  23

-9   7 -17 39.5852 6.78361  22

9  17  -7 36.7880 6.05421  23

7  17  -9 36.2224 6.21298  23

-7   9 -17 43.6606 6.74052  22

-7  17  -9 27.7240 6.12284  22

9  17  -7 32.7989 6.02048  19

-7  17   9 37.2167 6.84488  21

-9  17   7 30.4235 6.27699  21

-17  -9  -7 33.0809 6.15219  14

-17  -7  -9 37.7350 6.74330  14

-7  17   9 38.8053 6.53384  13

-9  17   7 37.6511 6.74580  13

-17   9   7 33.3667 5.62810  13

-17   7   9 41.5986 6.43084  13

7   9 -17 37.4128 5.60448  15

-9   7 -17 41.8834 6.13467  15

-7   9 -17 49.0204 6.76456  15

9  17   7 36.2942 6.50505  16

9   7 -17 36.7607 5.74062  15

17   7  -9 38.7374 7.07665  18

17   9  -7 46.2301 7.51540  18

-17  -9  -9 58.4616 6.60575  14

-9  17   9 49.0428 6.32831  13

-9   9  17 53.3016 6.48614  30

-11   1 -17 233.274 15.3165   8

-17   1  11 188.795 12.8715  10

-17  11   1 201.202 12.4369  10

-17  11  -1 229.113 12.5789  10

-17  -1 -11 214.479 14.4593   8

-17   1 -11 229.005 13.7247   8

1  11  17 245.838 14.3144  29

17  11   1 241.049 14.2195  28

1  17  11 216.106 12.0376  30

-1  11  17 208.995 13.2401  29

-1  17  11 216.135 13.1290  30

1  17  11 221.498 13.6247  29

-1  17  11 225.691 14.1221  29

11  17   1 230.404 14.4227  28

-11  -1  17 232.371 14.6887  25

1  17  11 238.411 13.6007  26

17  -1 -11 230.680 15.4669  12

11  -1 -17 219.012 14.8311  12

1  17 -11 236.770 14.5216  23

-1  17 -11 214.535 13.9517  23

-11  -1 -17 234.251 14.4669  22

-11   1 -17 204.632 13.9951  22

17  11  -1 219.664 13.0354  19

1  11 -17 239.993 14.7954  20

-1  11 -17 246.448 14.9583  20

1  17 -11 235.009 14.0615  20

-1  17 -11 243.623 14.5898  20

11  17   1 233.364 15.4938  19

-11  17   1 217.779 13.9408  21

-11  17  -1 218.538 12.9603  21

17   1 -11 208.321 12.7708  18

-17  -1 -11 202.516 12.5293  14

-17   1 -11 201.421 11.6825  14

-1  11 -17 233.442 13.6925  15

1  11 -17 212.499 12.9057  15

11  17  -1 220.325 14.4913  16

11  17   1 233.094 14.8754  16

-11  -3 -17 44.9985 7.65205   8

-17   3  11 43.3334 7.51362  10

-17  -3 -11 56.7577 7.77028   8

-17  11   3 51.8805 6.72040  10

-17  -3 -11 40.1730 6.15585   7

17  11  -3 50.4783 6.91524  28

17  11   3 50.3134 6.69155  28

3  11  17 30.9157 6.14136  29

-3  17  11 42.7234 6.65897  30

-3  11  17 40.7309 5.85919  29

11  17  -3 51.9907 7.04917  28

3  17  11 40.2816 6.02295  29

11  17   3 43.1185 6.48201  28

-3  11  17 49.7924 6.31741  30

-11   3  17 43.3992 6.85255  25

11   3 -17 45.9499 6.36484  27

-11  -3  17 34.4737 6.65706  25

3  17  11 41.9271 6.56015  26

17  -3 -11 30.1779 6.14070  12

17   3 -11 40.9657 6.91833  12

-17  -3 -11 58.5574 7.25986  14

11  -3 -17 61.5126 7.90786  12

11   3 -17 40.2387 6.90695  12

-3  17 -11 39.8851 6.38718  23

-11  -3 -17 44.3842 6.70999  22

-11   3 -17 46.2067 7.41474  22

-17  11   3 45.4736 6.95591  21

11  17   3 48.1145 7.68128  19

17  11  -3 39.7420 6.56002  19

-3  17 -11 41.8003 5.82542  22

-3  11 -17 40.3280 6.34758  20

3  17 -11 40.8384 6.06368  20

-11  17   3 40.2482 6.75555  21

11  17  -3 55.0429 7.97089  19

11  17   3 53.2079 7.28931  16

-3  11 -17 37.1604 5.91640  15

17   3 -11 39.7320 6.59677  18

17  11  -3 43.4802 7.14933  18

3  11 -17 42.5299 6.09408  15

-17 -11  -5 24.9508 5.26482   8

-11  -5 -17 26.8133 5.86389   8

-17   5  11 26.5804 5.51926  10

-17  -5 -11 29.6872 5.80988   8

-17  -5 -11 21.1822 4.97067   7

17  11  -5 29.2363 4.96984  28

5  11  17 29.1891 5.79204  29

-5  17  11 22.9598 5.16774  30

-5  11  17 26.4329 5.17278  30

11   5 -17 32.8352 5.40408  27

5  17  11 28.6500 5.00126  26

17  -5 -11 31.1132 5.50429  12

17   5 -11 18.1003 4.74206  12

-17  -5 -11 26.7649 5.12233  14

-11  17   5 30.1396 5.33970  13

11  -5 -17 32.5440 5.25442  12

11   5 -17 34.5707 5.90969  12

-5  17 -11 29.0033 5.33216  23

-11  -5 -17 29.4023 5.42306  22

-17  11   5 31.3456 5.59631  21

11  17   5 31.2809 5.90197  19

17  11  -5 15.7552 4.76596  19

5  11 -17 27.7767 5.47296  20

-5  17  11 23.5270 4.83133  21

11  17  -5 24.1488 5.36722  19

17   5 -11 42.6603 6.53008  18

17  11  -5 34.5854 6.43562  18

-18   0   0 4.44597 5.40675   6

0  18   0 2.71690 5.10856  30

0   0  18 4.16791 5.80680  25

-18   0   0 3.81629 5.68402  14

0  18   0-1.58477 3.75538  23

0   0 -18 0.86610 3.35152  22

0   0 -18 3.74657 4.27146  15

-18   0   0-1.29592 4.72793  10

-18   0   2 79.2403 10.6646  10

-18   2   0 111.999 12.8418  10

-18  -2   0 87.1835 10.7792  10

-18   0  -2 78.3304 11.0627  10

-18   0   2 76.7487 11.5041   6

-18  -2   0 66.9815 10.6480   6

-18   2   0 77.2282 11.1523   6

-18   0  -2 62.8865 10.2502   6

0  18  -2 64.3968 10.7547  30

2  18   0 73.1193 10.9984  30

0  18   2 90.5434 11.6841  30

2   0  18 73.2321 11.6310  25

0  -2  18 66.3333 10.4284  25

0   2  18 73.3432 10.8149  25

-2   0  18 82.3693 11.3516  25

-18   2   0 74.1893 10.8365  14

-18  -2   0 80.7271 10.6968  14

-18   0  -2 63.3360 10.5013  14

18   0  -2 76.6430 11.8595  12

0  18  -2 66.2990 9.04093  23

-2  18   0 74.6673 8.89538  23

-2   0 -18 105.849 11.1598  22

2  18   0 76.3702 10.5850  19

-2   0 -18 76.4047 8.67026  15

2  18   0 66.5758 9.19356  16

0   2 -18 91.1207 10.4229  15

0  -2 -18 76.2232 8.04371  15

2   0 -18 88.9304 10.1178  15

-18   2   2 483.096 25.5462  10

-18  -2   2 458.696 22.5509  10

-18   2  -2 465.156 25.4837  10

-18  -2  -2 429.110 22.5261  10

-18  -2   2 476.437 26.0634   6

-18   2   2 415.109 24.2901   6

-18  -2  -2 480.176 26.3025   6

-18   2  -2 437.374 25.1347   6

2  18  -2 412.979 23.9628  30

-2  18  -2 399.715 23.1981  30

2  18   2 456.623 24.1056  30

-2  18   2 468.738 24.9677  30

2  -2  18 439.507 23.9733  25

2   2  18 430.780 24.3469  25

-2  -2  18 446.069 24.5699  25

-2   2  18 440.039 24.4567  25

18   2  -2 502.338 27.2054  12

18  -2  -2 388.648 24.3992  12

2  18  -2 472.642 21.0915  23

-2   2 -18 481.984 22.2845  22

-2  18  -2 445.643 21.6602  23

2  18  -2 410.447 20.6564  19

2  18   2 459.960 24.1040  19

2   2 -18 453.399 22.6870  15

2  -2 -18 400.222 19.3166  15

-18  -2   2 466.698 22.6129  14

-2   2 -18 431.453 20.9938  15

-18  -2  -2 433.055 23.5690  14

2  18   2 442.264 20.3464  16

-18   0   4 2.37366 4.59252  10

-18   4   0 1.38796 5.21950  10

-18  -4   0 0.86071 3.51074  10

-18   0  -4-2.56182 5.60285  10

-18   0  -4-1.40500 4.62036   6

-18   0   4 4.29908 5.22806   6

-18  -4   0 3.77052 4.43969   6

-18   4   0 1.28718 4.69597   6

4  18   0 1.12585 4.23383  30

-4  18   0-1.25943 5.00698  30

0  18   4 1.21718 4.00269  30

0  -4  18-1.18974 6.04173  25

0   4  18-1.22582 4.74340  25

-4   0  18-2.64313 5.25402  25

4   0  18 1.34229 5.33644  25

18   0  -4 1.44804 5.75684  12

-18  -4   0 1.04880 4.16963  14

4   0 -18 4.15830 5.92970  12

0  18  -4-1.07220 4.48138  23

-4   0 -18-1.18569 4.18835  22

-4  18   0-1.74078 3.46033  23

-4  18   0 0.99159 4.14447  21

4  18   0 1.21102 5.06158  19

4  18   0 1.07577 3.53768  16

0   4 -18-1.10028 3.75486  15

-4   0 -18 0.70488 3.63680  15

-18   2  -4 40.1088 7.20533   8

-18   2   4 36.4898 8.51014  10

-18   4   2 32.8118 8.66043  10

-18  -2   4 32.2560 6.75813  10

-18   4  -2 34.1081 8.99375  10

-18   2  -4 34.9863 8.78576  10

-18  -4  -2 25.1138 6.20604  10

-18  -2  -4 32.6661 7.64339  10

-18  -2  -4 33.6156 8.60622   6

-18   2  -4 52.7799 9.58039   6

-18  -2   4 41.1795 8.78473   6

-18   2   4 30.2511 8.52768   6

-18  -4   2 47.3487 8.60155   6

-18   4   2 31.8639 8.16006   6

-18  -4  -2 29.6459 7.06203   6

-18   4  -2 37.9914 8.35118   6

4  18   2 34.0741 7.19792  30

-4  18  -2 31.3178 8.17019  30

2  18   4 37.6084 7.83826  30

-4  18   2 42.6595 8.50859  30

-2  18   4 35.0875 7.43198  30

2  -4  18 32.4297 7.71442  25

2   4  18 44.3477 9.10107  25

-2  -4  18 49.5867 8.76923  25

-2   4  18 39.8653 8.41317  25

-4   2  18 29.5785 7.97846  25

-4  -2  18 35.4283 8.42350  25

2  18   4 46.3795 8.21172  26

4  -2  18 40.5572 8.74850  25

4   2  18 31.0320 8.10774  25

18   2  -4 50.2183 9.95549  12

18  -2  -4 27.7678 8.61001  12

18   4  -2 26.3738 7.91026  12

-18  -4   2 33.5519 6.54069  14

18  -4  -2 35.4984 8.75108  12

-18   2  -4 48.1811 9.14598  14

-18  -4  -2 33.9407 7.53674  14

-18  -2  -4 36.8398 8.02158  14

4  18  -2 35.7233 6.50456  23

2  18  -4 30.4335 7.13292  23

-2  18  -4 29.4508 7.53558  23

-2   4 -18 39.0986 6.99837  22

-4  18  -2 30.3143 6.79976  23

-4   2 -18 28.2692 7.46190  22

4  18   2 30.8882 7.63160  19

-2   4 -18 27.6862 5.50087  20

4  18  -2 22.6472 6.69882  19

-4  18  -2 35.9167 6.01044  21

4  18   2 30.1792 6.89294  16

2  18   4 28.9751 5.86075  16

2   4 -18 29.1001 7.02475  15

-4   2 -18 35.2639 6.63793  15

-2   4 -18 37.3811 7.77583  15

-4  18   4 0.73597 3.42272   9

-18   4   4 1.30847 4.62208  10

-18  -4  -4-4.47312 3.82718  10

-18  -4  -4-1.17207 4.78075   6

-18   4  -4 1.20320 4.65587   6

-18  -4   4-1.19357 4.74515   6

-18   4   4 1.21403 4.42911   6

4  18   4 2.70792 3.77269  30

4  -4  18-2.20302 4.60389  25

4   4  18 1.13420 4.00647  25

4   4 -18-1.38516 3.34254  27

-4   4  18 4.58797 4.79399  25

-4  -4  18 1.12621 3.84336  25

4  18   4-1.01966 4.74207  26

-18  -4  -4-1.14470 3.90644  14

18   4  -4 2.45586 5.59978  12

18  -4  -4 1.23286 5.15289  12

4  18  -4-0.91606 3.82879  23

-4   4 -18-2.04156 4.65509  22

-4  18  -4-1.06358 4.44535  23

4  18  -4 0.88684 3.61734  19

4  18   4-1.29873 5.16324  19

4  18   4-0.90393 3.77809  16

4   4 -18 1.08770 4.09035  15

-4   4 -18 2.81383 4.27733  15

-18   0  -6 11.7143 5.49887   8

-18   0   6 8.48658 4.74505  10

-18   6   0 13.8286 6.07124  10

-18   0  -6 9.60484 5.36904  10

-18   0  -6 6.46610 5.14603   6

-18   0   6 25.3213 7.09099   6

-18  -6   0 12.9057 5.04611   6

-18   6   0 18.6993 6.28884   6

0   6  18 7.05034 4.11029  29

-6  18   0 9.68323 5.00852  30

0  18   6 8.67204 5.50914  30

0  -6  18 12.6868 5.11789  25

0   6  18 11.7829 5.45196  25

-6   0  18 15.8883 6.30956  25

6   0  18 16.4542 6.53402  25

-18  -6   0 11.0690 5.03767  14

-18   0  -6 12.4146 5.45129  14

18   6   0 16.0180 6.00793  12

18  -6   0 10.0289 6.18602  12

6   0 -18 10.3279 6.66441  12

18   0  -6 25.1318 7.63320  12

0  18  -6 19.4492 6.46607  23

-6  18   0 15.3046 5.03055  23

-6   0 -18 19.1864 6.74564  22

0   6 -18 18.6508 5.58168  20

6  18   0 14.5810 6.07405  19

-6  18   0 14.1470 5.37643  21

0   6 -18 6.46274 4.50732  15

6  18   0 5.55089 5.45721  16

-18   2   6 407.672 22.2938  10

-18  -2   6 388.944 18.5591  10

-18   6  -2 391.369 21.8418  10

-18  -2  -6 392.283 22.0041   8

-18   2  -6 380.414 22.1078  10

-18  -2  -6 442.310 21.6801  10

-18   2  -6 373.018 18.4749   8

-18  -2   6 359.695 21.7665   6

-18   2   6 370.498 22.0461   6

-18  -6   2 403.025 20.2083   6

-18   6   2 378.196 20.1196   6

-18  -6  -2 400.231 20.0028   6

-18   6  -2 407.883 20.6264   6

-18  -2  -6 422.139 22.7821   6

-18   2  -6 377.628 21.8877   6

-6  18  -2 366.777 19.7819  30

2  18   6 355.937 19.0057  30

-6  18   2 359.150 20.3179  30

-2  18   6 395.920 21.5267  30

2  -6  18 426.655 20.4723  25

2   6  18 389.051 19.8018  25

6   2 -18 368.987 16.5036  27

-2   6  18 370.996 19.4720  25

-2  -6  18 412.180 20.1592  25

-6   2  18 401.277 22.0463  25

-6  -2  18 406.948 21.9568  25

6  -2  18 442.078 23.1742  25

6   2  18 384.746 21.7262  25

18   2  -6 410.930 23.0622  12

18  -2  -6 359.412 21.8047  12

18   6  -2 358.922 19.8883  12

18  -6  -2 397.379 21.0342  12

6  -2 -18 414.296 22.7134  12

6   2 -18 414.331 22.7381  12

-6  -2 -18 374.777 21.2152  22

2  18  -6 422.481 21.1091  23

-2  18  -6 421.072 21.7149  23

-6   2 -18 429.293 22.3804  22

-6  18  -2 403.827 20.1489  23

-2   6 -18 376.902 17.5756  22

-2   6 -18 368.022 17.6278  20

-6  18   2 416.403 21.1271  21

6  18  -2 412.105 21.6571  19

-6  18  -2 355.061 16.9128  21

6  18   2 405.138 22.4326  19

-18   2  -6 416.531 21.1735  14

-18  -6  -2 394.942 19.9044  14

18   6  -2 394.423 18.5806  18

-6   2 -18 362.850 17.0518  15

-2   6 -18 376.767 19.9509  15

-18  -6   2 358.128 16.4425  14

6  18  -2 373.902 20.8261  16

2   6 -18 390.904 20.7640  15

6  18   2 381.249 20.2354  16

-4  18   6 75.4316 7.64006   9

-6  18   4 99.2880 9.57171   9

-18  -4  -6 114.648 12.1228   8

-18   4   6 86.4949 10.8534  10

-18   6  -4 78.3761 10.4647  10

-18  -4  -6 67.7000 9.17023   6

-18   4  -6 87.0744 10.3744   6

-18  -4   6 94.1568 10.7636   6

-18  -6  -4 101.949 10.0854   6

-18   6  -4 101.010 10.3300   6

-18   4   6 70.6314 9.81866   6

-18  -6   4 60.1385 8.27066   6

-18   6   4 85.6453 9.92995   6

4  18   6 80.7394 8.15098  30

-6  18   4 66.9207 9.60666  30

-4  18   6 91.1931 10.4223  30

4  -6  18 81.2588 9.31251  25

4   6  18 70.5018 8.74510  25

6   4 -18 71.3615 8.10537  27

-4  -6  18 97.9786 9.91446  25

4  18   6 91.7486 10.1678  26

-4   6  18 77.5398 9.31186  25

-6   4  18 87.2442 10.1333  25

-6  -4  18 94.0626 10.8150  25

6  18   4 65.8012 8.27558  26

6  -4  18 88.6471 10.3778  25

6   4  18 90.5047 10.5967  25

-18   4  -6 79.7064 9.30947  14

-18  -4  -6 94.5755 10.7498  14

-18   6   4 72.8781 7.46709  13

6   4 -18 82.1561 10.7226  12

18   4  -6 81.1349 10.9627  12

18  -4  -6 83.9317 10.4264  12

18   6  -4 87.4375 9.91763  12

18  -6  -4 93.4667 10.3086  12

6  -4 -18 92.1741 10.8247  12

6  18  -4 76.7246 8.63615  23

4  18  -6 80.2300 9.34926  23

-4  18  -6 76.6772 9.79593  23

-6   4 -18 86.9445 10.2629  22

-6  18  -4 89.5306 10.1008  23

-4   6 -18 95.3559 9.82715  22

6  18  -4 82.6794 9.60911  19

-6  18   4 114.144 11.3331  21

-18  -6  -4 92.9555 10.1514  14

6  18   4 73.5476 9.08998  16

4  18   6 78.1723 8.57761  16

18   4  -6 78.2078 8.73298  18

18   6  -4 79.2336 9.21195  18

-6   4 -18 90.4276 9.29782  15

-4   6 -18 83.8305 9.56463  15

-6  18   6 330.216 15.9506   9

-18  -6  -6 380.435 20.5451   8

-18   6  -6 320.973 18.0591  10

-18  -6   6 344.000 17.1993   6

-18   6   6 285.101 16.3262   6

-18  -6  -6 364.385 17.3287   6

-18   6  -6 377.715 17.9054   6

-6  18   6 345.935 18.5016  30

6  -6  18 332.510 16.3929  25

6   6  18 297.744 15.9880  25

6   6 -18 316.593 15.8924  27

-6   6  18 303.462 16.4737  25

-6  -6  18 333.258 16.9654  25

6  18   6 332.431 16.9679  26

18  -6  -6 298.625 16.6226  12

18   6  -6 320.269 16.8190  12

-18   6   6 353.013 16.1448  13

6  18  -6 346.156 17.3069  23

-6  18  -6 358.868 18.4251  23

-6   6 -18 370.720 18.4578  22

6  18  -6 339.822 16.2168  19

6  18   6 345.805 17.1162  16

6   6 -18 340.242 17.4326  15

18   6  -6 341.444 17.4028  18

-6   6 -18 318.868 16.3750  15

-18  -6  -6 356.298 18.4038  14

-18   0  -8 0.92701 3.68541   8

-18   0   8-0.87350 3.90297  10

-18   8   0 1.02854 3.98001  10

-18   0  -8 1.12197 4.57638   6

-18   0   8-2.31906 4.48688   6

0  18   8-2.48388 3.20386  29

-8  18   0-1.58584 3.82679  30

0   8  18 1.51831 3.09651  29

0  18   8-0.89561 3.74331  30

8   0 -18 0.56439 2.72386  27

-8   0  18 2.13120 4.45379  25

8   0  18 1.11546 4.54985  25

-18   0  -8-1.85382 3.87413  14

18   0  -8 1.13956 4.87499  12

8   0 -18 1.13397 4.96012  12

0  18  -8-1.97538 3.82194  23

-8   0 -18-2.17427 4.43429  22

0   8 -18 2.67846 4.07156  20

8  18   0-1.11964 4.45127  19

-8  18   0 0.82753 3.92187  21

8  18   0 2.05991 4.40611  16

-18  -2  -8 47.4991 8.24498   8

-18   2   8 32.6856 6.86200  10

-18   2  -8 48.6171 6.69274   8

-18   8   2 37.0536 7.60609  10

-18   8  -2 46.9177 7.80851  10

-18  -2  -8 45.5425 7.94297   6

-18   2  -8 31.0867 7.48407   6

-18  -2   8 30.7617 7.40195   6

-18   2   8 36.2916 7.47696   6

-2   8  18 36.4131 5.95959  30

2   8  18 60.3952 7.91416  29

-8  18  -2 38.0912 6.18776  30

-8  18   2 25.9999 5.77399  30

2  18   8 56.3865 7.45109  30

-2   8  18 47.0001 6.17691  29

-2  18   8 64.3423 8.52554  30

2  18   8 44.1811 6.40878  29

8   2 -18 54.1156 6.66479  27

-8   2  18 35.8356 7.45048  25

8  -2  18 38.1915 7.53283  25

8   2  18 47.4949 8.24425  25

-8  -2  18 40.3744 7.62894  25

2  18   8 54.1682 8.11618  26

-18   2  -8 34.7652 6.45035  14

-18  -8  -2 38.6908 6.27947  14

-18  -2  -8 39.1631 6.84607  14

18  -2  -8 53.0416 8.80770  12

18   2  -8 33.4719 7.72846  12

8  -2 -18 54.9793 8.32970  12

8   2 -18 46.8268 8.34423  12

-8   2 -18 40.0083 7.53786  22

2  18  -8 41.8955 7.35648  23

-2  18  -8 43.6864 7.65419  23

-8  -2 -18 35.7763 7.47217  22

-8  18  -2 49.3529 7.27814  23

8  18  -2 49.3017 8.48329  19

2   8 -18 40.2647 7.40627  20

-2   8 -18 58.6630 7.13564  20

-8  18   2 43.1135 7.29270  21

-8  18  -2 34.0898 5.60327  21

8  18  -2 33.7715 7.26932  16

8  18   2 34.4433 7.16406  16

18   8  -2 50.9041 7.29972  18

-2   8 -18 57.1696 8.18910  15

-4  18   8 0.53417 2.33653   9

-18  -4  -8 1.03962 4.64521   8

-8  18   4-0.77734 3.61512   9

-18   4   8-0.99782 4.45846  10

-18   8   4 2.90841 4.59455  10

-18   8  -4-1.74884 3.56667  10

-18  -4  -8 2.66699 4.21316   6

-18   4  -8 0.91695 3.54819   6

-18  -4   8 0.92690 3.78071   6

-18   4   8 1.85339 3.38084   6

18   8  -4 2.36558 3.29574  28

18   8   4 0.76934 3.43757  28

-4   8  18 0.76005 3.46607  30

-8  18   4-0.81966 3.08237  30

-4  18   8 0.93978 3.73619  30

8   4 -18 1.36261 2.91462  27

8  -4  18 0.87944 3.76224  25

8  18   4-0.60399 2.91498  26

8   4  18-3.40747 3.80632  25

-8   4  18-3.53476 4.34036  25

-8  -4  18 5.21539 4.19509  25

-18  -8  -4-3.05149 3.40867  14

18  -4  -8-1.84083 4.19739  12

18   4  -8-0.91343 3.72579  12

8  -4 -18-0.88286 3.94480  12

8   4 -18 2.77398 3.86473  12

8  18  -4-0.59552 2.48905  23

4  18  -8 3.46004 4.09949  23

-8  -4 -18-0.96226 3.51060  22

-4  18  -8 1.79903 3.66903  23

-8  18  -4 0.84967 3.63485  23

-8   4 -18 0.95656 3.70147  22

-4   8 -18-0.67193 2.80840  22

18   8  -4-0.74253 3.02872  19

8  18  -4 2.71668 4.12966  19

8  18   4-7.40081 4.62458  19

-8  18   4-3.76559 3.93468  21

4   8 -18-0.82343 3.75510  15

8  18   4-0.89115 3.63490  16

4  18   8 0.56282 3.07995  16

-8   4 -18 1.19302 2.77416  15

18   4  -8-0.75444 3.07726  18

-4   8 -18 1.71991 3.41884  15

18   8  -4 0.84794 3.09352  18

-18  -8  -6 1.81318 3.88206   8

-6  18   8 12.5761 3.83503   9

-8  18   6 12.6794 4.30718   9

-18  -6  -8 15.7723 5.08002   8

-18   6   8 8.01858 4.14697  10

-18   8   6 5.13044 3.90310  10

-18   8  -6 13.7087 4.56237  10

-18  -6  -8 10.6410 3.61467   6

-18   6  -8 15.1772 4.17319   6

-18  -6   8 6.52769 3.26537   6

-18   6   8 6.47971 3.64706   6

-6   8  18 12.5427 4.36435  30

18   8  -6 12.5243 3.92375  28

-8  18   6 8.20674 4.08629  30

8   6  18 9.05244 3.69627  25

-8   6  18 3.79061 3.46144  25

8   6 -18 11.6278 3.95601  27

6  18   8 6.57479 3.65338  26

8  18   6 9.70167 3.75469  26

8  -6  18 7.85093 3.61590  25

8  18  -6 7.49452 3.51549  23

6  18  -8 8.82242 3.91363  23

-8  18  -6 16.8851 4.85280  23

-8   6 -18 14.5774 4.84657  22

-6   8 -18 16.7069 4.83829  22

8  18  -6 6.14346 3.63420  19

-6  18  -8 7.67861 4.43258  22

-6  18   8 5.08503 3.86862  21

18   8  -6 13.0331 4.23198  19

-18  -8  -6 9.43791 3.92102  14

-18  -6  -8 10.3840 4.05981  14

18  -6  -8 11.1110 4.04662  12

18   6  -8 2.59512 3.40345  12

-18   6   8 9.11501 3.85213  13

6   8 -18 9.43195 3.93817  15

8  18   6 9.00707 4.11102  16

6  18   8 14.2116 4.18292  16

-8   6 -18 13.4417 4.06045  15

-6   8 -18 10.9004 3.81123  15

8   6 -18 8.93787 3.86924  15

18   6  -8 11.8634 4.38594  18

18   8  -6 19.5389 5.04332  18

-18  -8  -8 0.61212 2.49679  14

-8   8  18-0.62214 2.40741  30

-18   0  10 88.9177 7.96537  10

-18  10   0 87.5060 8.52936  10

-18   0 -10 97.4584 8.84990   8

-18   0 -10 85.4341 9.38615   6

-18   0  10 73.8687 9.20765   6

0  18  10 75.7414 8.14113  29

18  10   0 101.313 9.18097  28

0  10  18 79.8871 7.92036  29

0  18  10 93.2164 8.30159  30

-10   0  18 89.5297 9.43897  25

10   0  18 97.9183 9.66526  25

18   0 -10 99.2328 10.0754  12

10   0 -18 84.7978 9.43947  12

0  10 -18 96.4823 8.98388  20

-10  18   0 81.1679 8.10094  21

-18   0 -10 77.0950 7.77683  14

0  10 -18 101.560 8.97843  15

-18   2  10 270.035 14.6742  10

-18  10   2 307.487 15.1579  10

-18  -2 -10 249.104 14.7324   8

-18  -2  10 266.547 15.6404   6

-18   2  10 284.132 16.0302   6

-18  -2 -10 315.958 16.2493   6

-18   2 -10 270.094 15.3721   6

18  10  -2 306.879 15.0645  28

18  10   2 314.958 15.1069  28

2  10  18 309.487 14.9362  29

-2  18  10 283.585 14.7114  30

2  18  10 293.365 13.9165  29

10   2 -18 284.922 13.1782  27

-10   2  18 282.343 15.4096  25

-10  -2  18 279.810 15.1415  25

2  18  10 277.878 14.3602  26

10  -2  18 314.676 16.5525  25

10   2  18 267.061 15.1801  25

18  -2 -10 286.837 15.9639  12

18   2 -10 265.430 15.3626  12

10  -2 -18 303.434 16.2902  12

10   2 -18 314.641 16.6268  12

2  18 -10 277.351 14.8717  23

-10  -2 -18 298.886 15.7257  22

2  10 -18 291.925 15.5517  20

-2  10 -18 270.281 13.9507  20

10  18  -2 297.573 16.3433  19

-10  18   2 287.666 15.1865  21

10  18   2 317.492 16.9441  19

-18  -2 -10 275.064 14.1310  14

2  10 -18 276.172 14.1405  15

-18  -4 -10 4.76953 3.76778   8

-18   4  10 0.74590 3.11813  10

-18  -4  10 2.07928 2.89745   6

18  10  -4 1.79794 2.99450  28

4  10  18 5.23876 3.68224  29

-4  18  10 4.95632 3.35611  30

-10   4  18 6.62763 3.62738  25

4  18  10 1.32488 3.08134  26

10   4  18 0.63583 2.95760  25

18  -4 -10 4.72532 3.42850  12

18   4 -10 4.04304 3.36674  12

-18  -4 -10 2.69140 3.06898  14

10  -4 -18 3.95985 3.35198  12

10   4 -18 5.47721 3.74714  12

4  18 -10 2.75486 3.07787  23

-4  18 -10 5.41646 3.38281  23

-10  -4 -18 2.84859 3.55808  22

-10   4 -18 2.99199 3.27235  22

10  18  -4 4.47391 3.78700  19

-4  18  10 4.32248 3.53889  21

10  18   4 3.97740 3.48001  19

-10  18   4 4.31702 3.53442  21

10  18   4 0.71961 2.86149  16

-4  10 -18 4.74790 3.15494  15

4  10 -18 2.80732 2.80545  15

-19  -1   1 112.973 12.1946   6

-19  -1  -1 133.022 13.2237   6

1  19  -1 120.726 12.6108  30

-1  19  -1 110.658 11.8900  30

1  19   1 127.907 13.2321  30

-1  19   1 121.141 12.3054  30

1  -1  19 120.297 12.9184  25

-1  -1  19 124.073 12.8096  25

19  -1  -1 121.980 13.1209  12

-1  -1 -19 123.900 10.6959  22

-1   1 -19 141.772 10.8424  22

-1  19  -1 118.064 10.0687  23

-19  -1  -1 123.169 11.9828  14

-19   1  -1 104.814 11.4018  14

-1  -1 -19 111.960 9.10212  15

-1   1 -19 131.923 10.7663  15

1   1 -19 104.556 10.1808  15

1  -1 -19 134.395 10.5332  15

-19   1   1 145.130 13.3208  10

-19  -1   1 112.904 11.4573  10

-19   1  -1 150.177 13.7309  10

-19  -1  -1 127.655 12.1550  10

-19   1  -3 0.81820 3.50037   8

-19   1   3 2.19629 4.90682  10

-19   3   1 1.20155 5.02209  10

-19  -1   3 0.94296 4.12471  10

-19   3  -1-2.41817 4.12629  10

-19  -3   1-0.78702 3.58919  10

-19   1  -3 10.3854 5.36662  10

-19  -3  -1-0.82914 3.29648  10

-19  -1  -3 1.03221 3.64631  10

-19  -1  -3 1.22730 4.47763   6

-19  -1   3-1.24393 5.44120   6

-19  -3   1-1.16256 4.49872   6

-19   3   1 7.05218 5.02826   6

-19  -3  -1 8.10057 5.68393   6

-19   3  -1-1.17139 5.12390   6

3  19   1 1.01073 4.22456  30

-3  19  -1 3.37110 4.80726  30

1  19   3 1.05450 4.40752  30

-1  19   3 3.35992 4.33391  30

3  -1  19 5.94339 5.42085  25

1  -3  19 1.09246 4.45613  25

1   3  19 2.26026 4.83476  25

-1  -3  19 1.09017 4.55658  25

-1   3  19-1.12606 4.81734  25

-3  -1  19-3.46500 4.71120  25

19  -1  -3-1.26636 5.41754  12

-19  -3   1 3.61509 3.95332  14

-19  -3  -1 4.97249 4.53535  14

-19  -1  -3 2.18127 3.72206  14

19   3  -1 2.48947 5.32502  12

19  -3  -1 2.42810 5.53656  12

1  19  -3 4.88675 3.93085  23

-1  19  -3 0.86021 3.50882  23

-3  19  -1 3.80389 3.60563  23

-3  -1 -19 4.77566 4.44209  22

-3   1 -19 2.72876 3.97875  22

3  19   1 8.07188 4.31651  19

-3  19   1 0.87682 4.07790  21

3  19  -1 0.88644 3.43026  19

3  19   1 3.05391 3.26627  16

1   3 -19-0.94020 4.37265  15

3   1 -19-0.90166 3.76871  15

3  -1 -19 3.95764 3.14694  15

-3   1 -19 4.18347 3.24278  15

-1   3 -19 2.66751 3.62695  15

-19   3  -3 105.942 12.0016  10

-19  -3  -3 103.718 9.82133  10

-19   3   3 95.1911 11.2582  10

-19  -3   3 114.632 11.8635   6

-19  -3  -3 102.843 11.0970   6

-19   3  -3 100.862 11.3808   6

-19   3   3 89.5504 11.0825   6

3  19   3 88.6958 9.82132  30

-3  19   3 108.598 11.3238  30

3  -3  19 111.630 11.2164  25

3   3  19 120.161 11.8145  25

-3   3  19 104.302 11.2774  25

-3  -3  19 103.548 11.1420  25

19   3  -3 119.125 12.4101  12

19  -3  -3 135.458 13.0701  12

-3  -3 -19 96.4944 10.0687  22

3  19  -3 84.5848 8.42203  23

-3  19  -3 91.3326 9.56135  23

-3   3 -19 95.6300 9.57160  22

3  19  -3 82.2538 8.25726  19

3   3 -19 96.9492 10.1655  15

3  -3 -19 100.788 8.43091  15

-19  -3  -3 94.5291 10.4727  14

-3   3 -19 114.593 9.86922  15

3  19   3 82.0301 8.21484  16

-19  -1  -5 5.66387 4.03884   8

-19   1  -5 6.08784 3.86494   8

-19   1   5 3.92112 4.55941  10

-19  -1   5 8.24260 4.18625  10

-19   5   1 3.36350 5.41137  10

-19   1  -5 8.57244 4.88709  10

-19  -1  -5 0.96977 3.85598  10

-19  -5  -1 1.86384 3.18099   6

-19   5  -1-0.96877 4.23803   6

-19  -1  -5 4.49118 4.09678   6

-19  -1   5 1.14525 5.11760   6

-19  -5   1 8.39459 4.66001   6

-19   5   1 6.76338 3.94155   6

-5  19  -1 5.76603 4.72055  30

-5  19   1 4.98984 4.73006  30

1  19   5 4.61579 4.29378  30

-1  19   5 2.01317 3.31080  30

5  -1  19 10.0037 5.55310  25

1  -5  19 5.35311 4.67500  25

1   5  19-1.83690 4.10434  25

-1   5  19 9.21588 4.97319  25

-1  -5  19 0.89813 4.25698  25

-5  -1  19 4.23906 4.42990  25

19   5  -1 1.99398 4.16754  12

19  -5  -1 4.02870 4.50073  12

-19  -5   1 3.56717 3.62354  14

-19   1  -5 2.96080 3.92421  14

-19  -5  -1 4.14081 3.77727  14

19   5   1 1.00929 4.51016  12

19  -5   1 6.14155 5.19839  12

19  -1  -5 3.44080 4.90698  12

1  19  -5 4.31507 3.43163  23

-1  19  -5 0.89133 3.54419  23

-5  19  -1 1.47278 3.07852  23

-5  -1 -19 0.99688 4.54658  22

-5   1 -19 0.96632 3.94204  22

5  19  -1 8.41517 4.82461  19

-1   5 -19 6.08923 3.23905  20

5  19   1 8.17979 5.19271  19

-5  19   1 3.32046 3.38657  21

-5  19  -1 0.63291 3.21469  21

1   5 -19 3.70027 3.67828  15

5  19   1 5.91873 4.00771  16

-1   5 -19 8.96626 4.40438  15

-19   3   5 107.892 11.1116  10

-19   5   3 115.161 11.7206  10

-19  -3  -5 124.425 11.7515   8

-19   3  -5 113.841 11.5498  10

-19  -3   5 127.359 11.9602   6

-19   3   5 112.414 11.1284   6

-19  -5   3 104.530 10.2626   6

-19   5   3 115.409 10.9656   6

-19  -5  -3 119.613 10.7870   6

-19   5  -3 122.743 11.1555   6

-19  -3  -5 123.201 11.6730   6

-19   3  -5 105.792 10.9818   6

3  19   5 110.314 9.89699  30

-5  19   3 121.362 11.2389  30

-3  19   5 119.435 11.3864  30

5  -3  19 143.811 12.0546  25

5   3  19 116.323 11.4238  25

3  -5  19 113.944 10.4823  25

3   5  19 128.351 10.9035  25

-3   5  19 117.417 10.9253  25

-3  -5  19 112.287 10.8098  25

-5   3  19 117.234 11.3248  25

-5  -3  19 144.962 12.3568  25

19   3  -5 146.253 12.4172  12

19  -3  -5 142.625 12.5744  12

19   5  -3 127.933 11.5235  12

19  -5  -3 129.112 11.8465  12

-5  -3 -19 118.844 10.9239  22

3  19  -5 101.167 9.79666  23

-3  19  -5 121.241 10.9930  23

-5  19  -3 112.151 10.1901  23

-5   3 -19 135.940 11.5881  22

-3   5 -19 129.263 9.65424  22

-5  19   3 120.908 11.0294  21

5  19  -3 115.304 10.0164  19

5  19   3 124.009 11.8279  19

5   3 -19 107.817 10.2199  15

-5   3 -19 100.896 8.76815  15

-3   5 -19 99.4604 9.80677  15

-19  -5  -3 129.997 10.7922  14

3   5 -19 128.934 10.9561  15

5  19   3 98.1989 9.10864  16

-19  -3  -5 109.333 10.7752  14

-19  -5   5 90.2179 9.21928   6

-19   5   5 108.505 9.78136   6

-19  -5  -5 85.7341 8.81703   6

-19   5  -5 101.573 9.53078   6

5   5 -19 103.435 9.37700  15

-19  -5  -5 97.0965 9.32090  14

-5   5 -19 93.4716 8.56089  15

5  19   5 91.7042 8.27645  16

5  -5  19 112.918 9.81275  25

5   5  19 87.7907 9.00015  25

-5   5  19 95.4152 9.48475  25

-5  -5  19 98.0543 9.40108  25

19   5  -5 89.5520 9.18526  12

19  -5  -5 119.207 10.4941  12

5  19  -5 95.2061 8.73665  23

-5  19  -5 111.347 10.1292  23

-5   5 -19 99.2007 9.19555  22

-5  19   5 69.2107 8.65236  21

-19   5   5 99.3532 10.2740  10

-19  -5  -5 100.074 10.5081   8

-19   5  -5 103.589 10.2711  10

-19   1   7 90.6297 9.03868  10

-19  -1   7 91.0073 8.29468  10

-19   7   1 79.4675 9.17341  10

-19   7  -1 89.9470 9.68586  10

-19   1  -7 108.166 10.3728  10

-19  -1  -7 95.8011 9.48146   8

-19   1  -7 89.4118 8.28955   8

-19  -1   7 110.675 10.8282   6

-19   7   1 96.3785 8.37588   6

-19   7  -1 91.8879 8.36885   6

-19  -1  -7 103.163 10.6076   6

-7  19  -1 88.7883 8.63657  30

1   7  19 91.4099 8.02438  29

-7  19   1 95.8195 9.15744  30

1  19   7 96.2207 8.90382  30

-1  19   7 92.6989 9.47322  30

1   7  19 83.1118 7.99666  25

-1   7  19 82.9507 8.05724  25

-7  -1  19 74.9732 9.46793  25

7  -1  19 91.8083 9.97628  25

19  -1  -7 108.342 10.8457  12

19   7  -1 89.6788 8.42511  12

19   7   1 91.1150 8.37782  12

7  -1 -19 79.7328 9.49894  12

1  19  -7 88.6217 8.83469  23

-7  -1 -19 109.516 10.2409  22

-1  19  -7 81.9415 9.11430  23

-7   1 -19 105.043 10.3151  22

-7  19  -1 102.854 8.94998  23

1   7 -19 94.6551 9.13357  20

-1   7 -19 87.1876 7.96257  20

-7  19   1 93.9513 9.01983  21

7  19  -1 84.5176 9.74137  19

7  19   1 95.3752 9.99453  19

-19   1  -7 116.879 9.93360  14

-19  -7  -1 88.6555 7.77866  14

-19  -1  -7 107.164 9.75269  14

-1   7 -19 79.5012 8.71315  15

1   7 -19 95.9308 9.35338  15

7  19   1 106.353 10.0074  16

-19  -3  -7 0.87935 3.84644   8

-19   3   7-1.72556 4.01253  10

-19   7   3 1.79703 3.84387  10

-19   7  -3-1.69257 3.93582  10

-19   3  -7-0.90713 3.60645  10

-19  -3  -7 3.38633 3.18367   6

-19   3  -7-0.86154 3.42519   6

-19  -3   7 3.48551 3.89353   6

-19   3   7-2.61704 3.97824   6

-3   7  19 2.35577 2.79120  30

3   7  19 3.89644 3.24423  29

-7  19   3 2.29210 4.12266  30

-3  19   7 2.53823 3.36372  30

-7   3  19 0.82977 3.93252  25

-7  -3  19 3.24363 3.77129  25

7  -3  19 2.56337 3.73755  25

7   3  19 5.81030 4.21515  25

-19  -7  -3-1.33045 2.78045  14

19  -3  -7 3.46671 3.79100  12

19   3  -7 1.74646 3.98226  12

3  19  -7-0.74490 3.32840  23

-3  19  -7 0.79184 3.46364  23

-7   3 -19-0.82948 3.54855  22

-7  -3 -19 3.48105 3.96873  22

-7  19  -3 0.71169 2.90297  23

7  19   3-1.86134 4.07092  19

3   7 -19 5.41064 4.45873  20

7  19  -3 3.81326 3.33599  19

-7  19   3 1.58024 3.60326  21

7  19   3-0.74374 3.32323  16

-3   7 -19 0.75611 3.16030  15

7   3 -19 2.28316 2.86204  15

-19  -7  -5 2.55203 3.72240   8

-19  -5  -7 6.69038 3.96477   8

-19   5   7 11.3047 4.35826  10

-19   7   5 3.99742 3.92814  10

-19   7  -5 5.07251 3.43582  10

-5   7  19 6.76965 3.22612  30

19   7  -5 10.8284 3.37028  28

-7  19   5 4.91394 3.84297  30

-5  19   7 5.33821 3.61563  30

5  19   7 4.64658 3.08882  26

-19  -7  -5 4.55213 3.35680  14

-19  -5  -7 6.51684 3.73735  14

19  -5  -7 9.89536 3.61158  12

19   5  -7 3.95083 3.45156  12

5  19  -7 4.43616 3.16759  23

-7   5 -19 7.02965 3.73995  22

-7  -5 -19 3.83887 3.70688  22

-5  19  -7 4.96716 3.36453  23

-7  19  -5 6.15057 3.29984  23

-7  19   5 3.02027 3.23182  21

5   7 -19 8.65203 3.48859  15

7  19   5 10.5960 3.89872  16

-5   7 -19 2.55992 3.03479  15

-19  -1   9 83.5462 8.55238   6

-19  -1  -9 103.191 9.34065   6

19   9   1 93.8829 8.27868  28

-1  19   9 106.714 8.65109  30

9  -1  19 84.5005 8.95395  25

-9  -1  19 89.3630 8.66286  25

19  -1  -9 92.8258 8.99683  12

9  -1 -19 98.1846 9.16031  12

1  19  -9 102.688 8.71801  23

-1  19  -9 97.8950 8.52679  23

-9  -1 -19 92.4309 9.01121  22

-9   1 -19 90.0891 8.64751  22

9  19  -1 93.7536 8.79657  19

9  19   1 87.9797 8.94764  19

-19  -1  -9 89.8971 8.02863  14

1   9 -19 94.3143 8.14117  15

9  19   1 92.5130 8.59461  16

-3   9 -19 9.76541 3.47888  15

9   3 -19 5.76180 2.88135  15

-20   0   0 152.422 12.9944   6

0  20   0 133.357 11.7526  30

0   0  20 152.278 13.0753  25

20   0   0 170.576 14.0440  12

-20   0   0 177.529 12.8319  10

0   0 -20 153.838 9.93830  15

-20   0  -2-2.05562 4.08618   6

-20   0   2-1.03643 4.22750   6

-20  -2   0-0.99889 3.86529   6

-20   2   0 1.00196 3.87717   6

0  20   2 0.91880 3.65282  30

2   0  20 5.06908 4.71491  25

0  -2  20-0.94881 3.77212  25

0   2  20-3.89676 3.97363  25

-2   0  20 0.98253 3.69485  25

20   0  -2 2.14323 4.47895  12

-20   0  -2 1.81211 3.87610  14

20   2   0 1.07421 4.38159  12

20  -2   0-1.04024 4.24302  12

0  20  -2 1.67322 2.69180  23

-2   0 -20-2.52145 2.75730  22

2   0 -20-0.64507 3.11325  15

0   2 -20 2.77552 3.16435  15

-20   0  -2-0.67566 2.89047   8

-20   0   2-1.67064 3.57350  10

-20   2   0-0.96336 4.12125  10

-20  -2   0-4.23416 3.58365  10

-20   0  -2-0.88044 3.50029  10

-20   2   2 22.1803 5.73982  10

-20  -2   2 34.9992 5.56901  10

-20   2  -2 27.5859 6.27723  10

-20  -2  -2 34.4068 6.04926  10

-20  -2  -2 32.8898 6.73880   6

-20   2  -2 32.0649 6.59234   6

-20  -2   2 34.1875 6.80416   6

-20   2   2 43.0926 7.38379   6

2  20   2 31.3995 6.32620  30

-2  20   2 27.7958 6.11528  30

2  -2  20 41.2613 7.42479  25

2   2  20 24.8781 6.60873  25

-2   2  20 29.1034 6.37088  25

-2  -2  20 27.4228 5.91747  25

20   2  -2 31.7733 7.13778  12

20  -2  -2 30.9045 6.38539  12

-20  -2  -2 22.0524 5.38399  14

-2  20  -2 31.3688 5.17498  23

-2  -2 -20 21.2474 4.52035  22

-2  20   2 23.6636 5.29778  21

2   2 -20 27.6153 5.64747  15

-2   2 -20 25.0728 4.82529  15

-20   0   4 586.498 24.6656   6

-20  -4   0 603.416 23.5579   6

-20   4   0 578.808 23.3910   6

-20   0  -4 594.678 24.6681   6

-4  20   0 594.542 23.7061  30

0  20   4 551.618 22.7977  30

4   0  20 635.193 25.3575  25

0   4  20 590.183 23.2093  25

0  -4  20 627.743 23.3797  25

-4   0  20 582.421 23.8462  25

20   0  -4 582.153 24.7674  12

20   4   0 602.755 24.0438  12

20  -4   0 552.652 23.1666  12

-4   0 -20 633.361 22.6148  22

0  20  -4 576.038 21.0561  23

4   0 -20 603.256 21.2817  15

-20  -4   0 542.120 20.8781  14

0   4 -20 575.616 21.8085  15

-20   0   4 560.747 21.9148  10

-20   4   0 573.853 24.4023  10

-20   0  -4 628.495 23.8697  10

-20   0  -4 554.526 20.7215   8

-20  -2  -4 7.67916 3.77229   8

-20   2   4 0.83064 3.38872  10

-20   4   2 5.41039 4.35244  10

-20   4  -2-2.71305 3.50007  10

-20   2  -4 4.40493 4.01812  10

-20  -2  -4 3.39092 3.27371  10

-20  -4  -2 7.14467 3.76283   6

-20   4  -2 4.88661 3.93118   6

-20  -2  -4 1.76546 3.94476   6

-20   2  -4 3.55041 4.36007   6

-20  -2   4 2.68633 3.56054   6

-20   2   4 2.69201 3.92561   6

-20  -4   2 3.20649 3.65626   6

-20   4   2 7.33969 3.56779   6

2  20   4 4.24307 3.41362  30

-4  20   2 1.68118 3.42930  30

-2  20   4 5.89079 3.76074  30

4  -2  20 8.80345 4.61297  25

4   2  20 4.42342 4.19324  25

2  -4  20 0.76371 3.68638  25

2   4  20 3.14522 3.92861  25

-2   4  20 0.78279 3.57041  25

-2  -4  20 3.01627 3.22655  25

-4   2  20 5.13957 4.13462  25

-4  -2  20 3.34308 4.44530  25

-20  -4  -2 5.06466 3.36549  14

-20  -2  -4 5.65531 3.37735  14

20   4   2 6.92471 4.60386  12

20  -4   2 10.2472 4.80158  12

20   2  -4 6.46350 4.37650  12

20  -2  -4 8.12394 4.58433  12

20   4  -2 3.38612 3.62203  12

20  -4  -2 4.16064 3.56043  12

2  20  -4-0.57830 2.63806  23

-2  -4 -20 3.22314 2.99866  22

-4   2 -20 4.56699 2.85455  22

-2  20  -4 1.30500 2.97635  23

-4  20  -2 5.18228 3.36341  23

-4  -2 -20 5.16558 3.80791  22

-4  20   2 4.61840 3.12750  21

2   4 -20 8.76385 3.82703  15

4   2 -20 1.40927 2.65062  15

4  -2 -20 5.62773 2.91481  15

-2   4 -20 0.65379 2.79768  15

-20  -4   4 109.672 9.67104   6

-20   4   4 134.934 10.3560   6

-20  -4  -4 148.922 10.6375   6

-20   4  -4 128.357 9.99544   6

-20  -4  -4 136.422 9.98991  14

-4   4 -20 113.184 8.49265  15

4   4 -20 117.569 9.44380  15

4  -4  20 122.895 9.69838  25

4   4  20 118.444 9.76832  25

-4   4  20 137.049 10.5308  25

-4  -4  20 125.485 9.77595  25

20   4  -4 121.816 10.0850  12

20  -4  -4 129.453 10.2446  12

-4  -4 -20 93.8148 8.84014  22

-4  20  -4 121.528 9.20927  23

-4  20   4 136.201 10.2309  21

-20   4   4 144.688 11.1600  10

-20  -4  -4 160.383 11.5970   8

-20   4  -4 138.019 11.0116  10

-20   6   0-0.78862 3.52372  10

-20   0  -6 0.80554 3.20253   6

-20   0   6-0.81953 3.17124   6

-6  20   0-0.64524 2.76032  30

0  20   6 0.66695 2.72042  30

6   0  20 2.48907 4.07512  25

-6   0  20 0.76910 3.43650  25

-20   0  -6 0.69901 2.85119  14

20   0  -6 0.81930 3.34183  12

0  20  -6-1.25550 2.97505  23

-6   0 -20 0.70597 3.02013  22

6  20   0-0.69243 2.82435  19

6   0 -20 0.58969 2.52268  15

0   6 -20-0.66529 2.78067  15

-20  -2  -6 27.6660 5.34296   6

-20   2  -6 27.1294 5.29615   6

-20  -2   6 18.3469 5.09329   6

-20   2   6 20.6538 5.19124   6

-6  20   2 29.7630 5.47871  30

-2  20   6 24.1042 5.14944  30

6  -2  20 26.9110 5.79811  25

6   2  20 28.5800 5.50381  25

-6   2  20 14.5667 4.62149  25

-6  -2  20 29.8705 5.32614  25

-2  20  -6 18.7264 4.46635  23

-6   2 -20 26.0242 4.98244  22

-6  -2 -20 22.5125 4.98794  22

-20   2   6 23.7901 5.05397  10

-20   6  -2 20.2818 5.00543  10

-20   2  -6 21.2118 5.04770  10

20   2  -6 28.6205 5.83291  12

20  -2  -6 16.6731 4.75739  12

6   2 -20 25.0216 4.75780  15

-2   6 -20 23.5115 4.63821  15

2   6 -20 32.2091 5.27758  15

-20  -4  -6 2.47319 2.76304  14

-4  20   6 1.98429 2.76489  30

4   6 -20 1.76995 2.79643  15

6   4 -20 4.08291 2.86518  15

1  -1  21 240.386 13.6903  25

-1  -1  21 214.207 13.1320  25

21  -1  -1 236.230 14.0386  12

21  -1   1 187.879 12.8408  12

-21  -1   1 249.972 13.8070   6

-21  -1  -1 226.776 13.4472   6

-1  21   1 238.465 13.3101  30

21  -1   3 45.6646 6.74519  12

21  -1  -3 49.6386 6.58527  12

-1  21   3 50.1086 6.31521  30

0   0   0    0.00    0.00   0

TITL saikai_2022_003 in Fd-3m

REM Fd-3m (#227 in standard setting)

CELL 0.71073   8.342217   8.342217   8.342217  90.0000  90.0000  90.0000

ZERR    8.00   0.000063   0.000063   0.000063   0.0000   0.0000   0.0000

LATT  4

SYMM -x+3/4,-y+1/4, z+1/2

SYMM -x+1/4, y+1/2,-z+3/4

SYMM  x+1/2,-y+3/4,-z+1/4

SYMM  z, x, y

SYMM  z+1/2,-x+3/4,-y+1/4

SYMM -z+3/4,-x+1/4, y+1/2

SYMM -z+1/4, x+1/2,-y+3/4

SYMM  y, z, x

SYMM -y+1/4, z+1/2,-x+3/4

SYMM  y+1/2,-z+3/4,-x+1/4

SYMM -y+3/4,-z+1/4, x+1/2

SYMM  y+3/4, x+1/4,-z+1/2

SYMM -y,-x,-z

SYMM  y+1/4,-x+1/2, z+3/4

SYMM -y+1/2, x+3/4, z+1/4

SYMM  x+3/4, z+1/4,-y+1/2

SYMM -x+1/2, z+3/4, y+1/4

SYMM -x,-z,-y

SYMM  x+1/4,-z+1/2, y+3/4

SYMM  z+3/4, y+1/4,-x+1/2

SYMM  z+1/4,-y+1/2, x+3/4

SYMM -z+1/2, y+3/4, x+1/4

SYMM -z,-y,-x

SFAC O Mg Al Si Ca Ti Cr Mn Fe Ni Zn

UNIT 32.00 0.24 0.08 0.64 0.08 0.16 7.36 0.16 10.48 0.24 0.08

SIZE 0.04 0.04 0.06

TREF

HKLF 4

END

;

_shelx_hkl_checksum   93217