Supporting Information for

Construction of 3D Cell Spheroids Based on Chemically Modified Hyaluronic Acid Biomimetic Hydrogel for 1-Nitropyrene Toxicity Evaluation

Guojie Zhao1| Conghui Liu2| Yanlei Ge2,4,5,6,7| Xuemin Yao8| Hongjiao Wu2| Yishuang Cui8| Weinan Yao2| Junqing Gan2,7| *Guogui Sun2,3,4,5,6,7

1 School of Public Health, North China University of Science and Technology, Tangshan, Hebei Province, 063210, China

2 Affiliated Hospital of North China University of Science and Technology, Tangshan, Hebei Province, 063000, China

3 Department of Hebei Key Laboratory of Medical-Industrial Integration Precision Medicine, Tangshan, Hebei Province, 063000, China

4 Hebei Province biological cell function development and precision detection technology Innovation Center, Tangshan, Hebei Province, 063000, China

5 Department of Tangshan Key Laboratory of Medical-Industrial Integration Precision Medicine, Tangshan, Hebei Province, 063000, China

6 Tangshan Biological Cell Function Development and Detection Innovation Technology Center, Tangshan, Hebei Province, 063000, China

7 Sun Guogui Innovation Studio, Tangshan, Hebei Province, 063000, China

8 Department of Oncology Radiation Physics Technology Section, Affiliated Hospital of North China University of Science and Technology, Tangshan, Hebei Province, 063000, China

*Corresponding author: guogui_sun2021@sina.com

Text

1. Synthesis of HA-based hydrogel precursor

HMDA-Cytosine: A solution containing NaHSO₃ (5.2 g, 50.0 mmol) and HMDA (20 mL, 150.0 mmol) in 50 mL solvent (pH 7.1) was mixed with 3% (w/v) cytosine solution (2.0 g, 18.0 mmol), followed by the addition of hydroquinone (0.16 g, 1.5 mmol) as a radical scavenger. The mixture was stirred and reacted at 100 °C for 10 h, and most of the water in the reaction mixture was then removed by rotary evaporation. The residue was transferred into ethanol, and the crude product was collected by filtration and precipitation. Afterwards, the precipitate was washed with ethanol and purified by silica gel column chromatography using methanol/dichloromethane (1:1, v/v) as the eluent. The final product was obtained by rotary evaporation and vacuum drying.

HA-HMDA-Cytosine: Dissolve HA (200.0 mg, 0.5 mmol) in 80 mL of deionized (DI) water. Subsequently, EDC (480.0 mg, 2.5 mmol) and NHS (2.5 mmol, 287.5 mg) were added into the HA solution. The mixture was continuously stirred for 2 h to activate the carboxyl groups (–COOH) of HA, followed by the addition of cytosine-HMDA (2.1 g, 10.0 mmol). After adjusting the pH to 4.7, the reaction was stirred at room temperature for another 24 h. The reaction mixture was dialyzed (MWCO: 10 kDa) against dilute hydrochloric acid (pH 3–5) to remove unreacted cytosine-HMDA, EDC, and NHS, and then thoroughly dialyzed against deionized water. The final product was obtained by freeze-drying.

HA-SH-HMDA-Cytosine: Dissolve HA‑HMDA‑Cytosine (200.0 mg, 0.5 mmol) in 80 mL of deionized (DI) water. EDC (480.0 mg, 2.5 mmol) and NHS (287.5 mg, 2.5 mmol) were then added to the HA‑HMDA‑Cytosine solution. The mixture was stirred continuously for 2 h to activate the carboxyl groups (–COOH) of HA‑HMDA‑Cytosine, followed by the addition of cysteamine hydrochloride (114 mg, 1.0 mmol). The pH was adjusted to 4–5, and the reaction proceeded at room temperature for 24 h under dark conditions. The reaction mixture was dialyzed (MWCO: 10 kDa) against dilute hydrochloric acid (pH 3–5) to remove unreacted cytosine‑HMDA, EDC, and NHS, and then extensively dialyzed against DI water. The final product was obtained by freeze‑drying.

HA-SH: Its synthetic route was identical to that of HA-SH-HMDA-Cytosine, with HA-HMDA-Cytosine simply replaced by native HA. The final product was obtained by freeze-drying.

Figures

Supplementary Figure 1 Synthetic route of HA hydrogel precursors. (A) Synthetic route of thiolated hyaluronic acid. (B) Cytosine functional modification of HA: the hydrophobic linker cytosine-HMDA was first synthesized; then HA-HMDA-Cytosine intermediate was prepared using HA as the raw material, and the final product HA-SH-HMDA-Cytosine was obtained via thiolation modification.

Supplementary Figure 2 ¹H NMR spectrum of cytosine-HMDA. ¹H NMR (600 MHz, D₂O, δ): 7.36 (d, 1H, –N–CH=C–), 5.87 (m, 1H, –C=CH–C–), 3.38 (t, 2H, –N–CH₂–C–), 3.05 (t, 2H, –C–CH₂–NH₂), 1.79–1.70 (m, 2H, –C–CH₂–C–), 1.68–1.58 (m, 2H, –C–CH₂–C–), 1.54–1.40 (m, 4H, –C–CH₂–CH₂–C–).

Supplementary Figure 3 1H NMR spectra of (A) Cytosine-HMDA, (B) HA-HMDA-Cytosine, (C) HA-SH-HMDA-Cytosine, (D) HA-SH. All 1H NMR spectra were acquired on a nuclear magnetic resonance (NMR) spectrometer. 1H NMR spectra were detailed below:

HA (A)

1H NMR (600 MHz, D2O, d): 4.6-3.3 (protons of HA), 2.00-1.80 (-COCH3).

HA-HMDA-Cytosine (B)

1H NMR (600 MHz, D2O, d): 4.6-3.2 (protons of HA), 2.92-2.85 (-CH2-NH-CO-), 2.37-2.46 (-NH-CH2-C-), 2.07-1.96 (-COCH3), 1.70-1.60 (-C-CH2-C-), 1.55-1.45 (-C-CH2-C-), 1.45-1.25 (-C-CH2-CH2-C-).

HA-SH-HMDA-Cytosine (C)

1H NMR (600 MHz, D₂O, δ): 4.6–3.2 (protons of HA sugar backbone), 2.95–2.85 (-CH₂-NH-CO- and -CH₂-SH), 2.70–2.60 (-CH₂-CH₂-SH), 2.45–2.35 (-NH-CH₂-C-), 2.07–1.96 (-COCH₃), 1.70–1.60 (-C-CH₂-C-), 1.55–1.45 (-C-CH₂-C-), 1.45–1.25 (-C-CH₂-CH₂-C-).

HA-SH (D)

1H NMR (600 MHz, D₂O, δ): 4.6–3.3 (protons of HA sugar backbone), 2.95–2.85 (-CH₂-NH-CO-), 2.70–2.60 (-CH₂-CH₂-SH), 2.07–1.96 (-COCH₃).

Supplementary Figure 4 Oscillatory rheological characterization of hydrogels. Frequency sweep results of Hybrid gels (A) and Covalent gels (B) with three different stiffnesses at 37 °C. The measurements were performed at a strain of 5% over a frequency range of 0.01–10 Hz. Data are presented as mean ± standard deviation (shaded regions), with samples independently prepared in triplicate (n=3).

Supplementary Figure 5 Deformation of HA-based hydrogel under heavy compression.

Supplementary Figure 6 Dose-dependent toxic effects of 1-NP on BEAS-2B 3D spheroids and 2D monolayer cells. (A) Representative bright-field microscopic images of BEAS-2B 3D spheroids treated with different concentrations of 1-NP for 48 h (Scale bar: 100 μm). (B, C) Cell viability curves of 1-NP against 3D spheroids (B) and 2D monolayer cells (C) determined by the CCK-8 assay. Data are presented as mean±SD (n=4).

Supplementary Figure 7 1-NP exposure induces oxidative stress, cell membrane damage, and altered expression of injury‑related genes in BEAS-2B 3D spheroids. (A) Relative levels of MDA content in spheroids after treatment with different concentrations of 1-NP. (B) Relative expression levels of cell injury marker genes (REPS2, H3C12, PRKAA2, MK167) and membrane protection‑related genes (CLDN18, CDHR4) detected by qPCR. (C) Relative levels of LDH release in cell supernatant after treatment with different concentrations of 1-NP. Data are presented as mean±SD (n=4). Statistical analysis was performed using one‑way ANOVA followed by Dunnett’s post‑hoc test. ns, no significant difference, **P<0.01, ***P<0.001, ****P<0.0001 vs the ctrl group.

Supplementary Figure 8 Effects of 1-NP exposure on the expression of tight junction‑related genes in BEAS-2B 3D spheroids. The relative expression levels of tight junction‑related genes (ZO-1, Occludin, Claudin1) after treatment with different concentrations of 1-NP were determined by qPCR. Data are presented as mean±SD (n=4). Statistical analysis was performed using one‑way ANOVA followed by Dunnett’s post‑hoc test. **P<0.01, ***P<0.001, ****P<0.0001 vs the ctrl group.

Tables

Supplementary table 1. Information on primers for quantitative RT-PCR

| Gene | primers | Sequence（5’— 3’） |
| --- | --- | --- |
| ZO-1 | Forward | TTGTCTTCAAAAACTCCCAC |
|  | Reverse | GACTCACAGGAATAGCTTTAG |
| Occludin | Forward | GGACTGGATCAGGGAATATC |
|  | Reverse | ATTCTTTATCCAAACGGGAG |
| Claudin1 | Forward | TCTTTATTGGCTGGGCAGGG |
|  | Reverse | TAAGAGCGGGGTACACGGTA |
| REPS2 | Forward | AGCACCTTATGAAGCTAGGCA |
|  | Reverse | GTCGGGGTAACTGCTGTTATC |
| H3C12 | Forward | GCTGCTCATCCGCAAACTG |
|  | Reverse | GCGTGAATAGCACAGAGGTTG |
| PRKAA2 | Forward | GTGAAGATCGGACACTACGTG |
|  | Reverse | CTGCCACTTTATGGCCTGTTA |
| MK167 | Forward | CACACCAACAAGCTCCAAGC |
|  | Reverse | CTGGTTTGGGTGTGTGCATG |
| CLDN18 | Forward | ACATGCTGGTGACTAACTTCTG |
|  | Reverse | AAATGTGTACCTGGTCTGAACAG |
| CDHR4 | Forward | CCAGGCTCAAAAGGTCTTCCA |
|  | Reverse | CAGGATTTCATAGCGCAGGTC |
| GAPDH | Forward | GTCAAGGCTGAGAACGGGAA |
|  | Reverse | AAATGAGCCCCAGCCTTCTC |

Supplementary table 2. Antibody information used in western blotting

| Antibodies | Dilution Ratio | Catalog Number | Distributor |
| --- | --- | --- | --- |
| ZO-1 tight junction protein Rabbit pAb | 1:1000 | 511417 | Zen-Bioscience |
| Occludin Rabbit mAb | 1:5000 | R381549 | Zen-Bioscience |
| Claudin 1 Rabbit pAb | 1:1000 | 343203 | Zen-Bioscience |
| GAPDH pAb | 1:10000 | AF7021 | Affinity Biosciences |
| Goat Anti-Rabbit IgG H&L(HPR) | 1:10000 | 511203 | Zen-Bioscience |