Supplementary information

Hyper Triplet-Triplet Fusion Blue Fluorescent Organic Light-Emitting Diode

1Chia-Hsun Chen, 2Pei-Hsi Lee, 2Hung-Yi Lin, 3Bo-Yen Lin, 1Man-kit Leung, 3Tien-Lung Chiu*

and 2Jiun-Haw Lee*

1Department of Chemistry, National Taiwan University, Taipei, Taiwan

2Graduate Institute of Photonics and Optoelectronics, and Department of Electrical Engineering,
National Taiwan University, Taipei, Taiwan

3Department of Electrical Engineering, Yuan Ze University, Taoyuan, Taiwan

Table of Contents

Figure S1 	PLQY values of (a) DMPPP, (b) DMPPP: Alq3 and (c) DMPPP: DPaNIF (5%) in solid state thin film.

Figure S2 	Kinetic model of upconversion electron-only device (EOD) and hole-only device (HOD).

Figure S3 	(a) PL spectra at 400−500 nm (ADN emission), (c) TrPL signal probed at 440 nm and (e) PL spectra at 600−680 nm (PtOEP emission) of TTF-upconversion electron-only device (EOD) and those for (b) (d) (e) hole-only device (HOD) under 532 nm photoexcitation and driving voltages (current).

Figure S4 	(a) Absorption of Alq3 and PL spectrum of DMPPP and ADN. (b) PL spectrum and (c) time-resolved photoluminescence (TrPL) of ADN, DMPPP, DMPPP: Alq3 (5%) and ADN: Alq3 layer (5%) by 355 nm laser excitation. The blue and green components of mixing layer were recorded at 420 nm and 520 nm by monochromator in front of PMT.

Figure S5 	(a) Current density (J)−Luminance (L) −voltage (V) characteristics, (b) CE−L, (c) PE−L, (d) EQE−L, (e) normalized EL spectra at J = 2.5 mA/cm2 and (f) CIE coordinates of selectively dopant devices.

Figure S6 	PLQY values of (a) ADN, (b) ADN: Alq3 and (c) ADN: DPaNIF (3%) in solid state thin film.

Figure S7 	(a) J−V−L, (b) CE−L, (c) PE−L, (d) CIE coordinate and (e) normalized EL spectra at 4.5 V of TTF-OLED in Figure 3.

Figure S8 	Low temperature fluorescence (LTFL) and phosphorescence (LTPh) spectra of DPaNIF in toluene at 77 K.

Figure S9 	PLQY values of (a) NPAN, (b) NPAN: DPaNIF (3%) in solid state thin film.

c

b

a

Figure S1 PLQY values of (a) DMPPP, (b) DMPPP: Alq3 and (c) DMPPP: DPaNIF (5%) in solid state thin film.

Figure S2 Kinetic model of upconversion electron-only device (EOD) and hole-only device (HOD).

c

b

a

f

e

d

Figure S3 (a) PL spectra at 400−500 nm (ADN emission), (c) TrPL signal probed at 440 nm and (e) PL spectra at 600−680 nm (PtOEP emission) of TTF-upconversion electron-only device (EOD) and those for (b) (d) (e) hole-only device (HOD) under 532 nm photoexcitation and driving voltages.

c

b

a

Figure S4 (a) Absorption of Alq3 and PL spectrum of DMPPP and ADN. (b) PL spectrum and (c) time-resolved photoluminescence (TrPL) of ADN, DMPPP, DMPPP: Alq3 (5%) and ADN: Alq3 layer (5%) by 355 nm laser excitation. The blue and green components of mixing layer were recorded at 420 nm and 520 nm by monochromator in front of PMT.

f

e

d

c

a

b

Figure S5. (a) Current density (J)−Luminance (L) −voltage (V) characteristics, (b) CE−L, (c) PE−L, (d) EQE−L, (e) normalized EL spectra at J = 2.5 mA/cm2 and (f) CIE coordinates of selectively dopant devices.

b

a

c

Figure S6 PLQY values of (a) ADN, (b) ADN: Alq3 and (c) ADN: DPaNIF (3%) in solid state thin film.

e

d

b

c

a

Figure S7 (a) J−V−L, (b) CE−L, (c) PE−L, (d) CIE coordinate and (e) normalized EL spectra at 4.5 V of TTF-OLED in Figure 3.

Figure S8 Low temperature fluorescence (LTFL) and phosphorescence (LTPh) spectra of DPaNIF in toluene at 77 K.

a

b

Figure S9 PLQY values of (a) NPAN, (b) NPAN: DPaNIF (3%) in solid state thin film.

Table S1. Material and device performances TTF OLEDs.

| Device | Driving voltage (V) | Max. EQE(%) | Delay Ratio | Ref |
| --- | --- | --- | --- | --- |
| HE-DEML | 2.95 | 15.4 | 0.32 | This work |
| HE-Reference | 2.95 | 10.1 | 0.10 | This work |
| BD3 (□) | 3.7 | 12/5.3/4.2 | 0.15 | Adv. Funct. Mater. 24, 2064–2071 (2014) |
| MBAn-(4)-F:BBPA (■) | 3.6 | 10.27 | 0 | iScience 9, 532–541 (2018) |
| DMPPP: TSTA (○) | 3.8 | 10.2 | 0.15 | Chem. Commun. 50, 6869–6871 (2014) |
| PIAnCN () | 3.0 | 9.44 | 0.3 | Adv. Funct. Mater. 28, 1705813 (2018) |
| 3CzAnBzt (∆) | 3.0 | 10.06 | 0.25 | J. Mater. Chem. C 7, 1014–1021(2019) |
| 2PPIAn (◊) | 3.0 | 8.9 | 0.25 | ACS Appl. Mater. Interfaces 12, 15422−15429 (2020) |