Supplementary Information for

Decoupling Na⁺ Solvation and Interfacial Chemistry via Dual-Anion Synergy Enables Wide-Temperature Sodium-Ion Batteries

Danning Yu1,3, Qiao Zhang2,3, Xingxing Yin2, Li Liu1, Min Zhou1, Mingjiong Zhou1*, Jun Wang2*, and Xing Xin1*

1 School of Material Science and Chemical Engineering, Ningbo University, Ningbo 315211, P. R. China

2 Department of Materials Science & Engineering, School of Innovation and Entrepreneurship, Southern University of Science and Technology, Shenzhen 518055, P. R. China

3 These authors contributed equally to this work.

*Corresponding authors.

E-mail addresses: zhoumingjiong@nbu.edu.cn (M. J. Zhou); xinxing@nbu.edu.cn (X. Xin); wangj9@sustech.edu.cn (J. Wang).

Supplementary Fig. 1. Cycling performance of Na||NMLTO cells with different electrolytes volume ratios at 1C.

Supplementary Fig. 2. LSV curves of Na||SS cells.

Supplementary Fig. 3. FTIR spectra of different electrolytes.

Supplementary Fig. 4. Tafel plots of Na||Na cells.

Supplementary Fig. 5. Nyquist plots of Na||Na cells.

Supplementary Fig. 6. Nyquist plots of Na||Na symmetric cells with the (a) Baseline, (b) NaDFOB-NaBr, (c) NaDFOB, and (d) NaBr electrolytes measured at various temperatures. (e) Equivalent circuit model used for fitting the EIS spectra.

Supplementary Fig. 7. Photographs of different electrolytes at −40 °C: (a) Baseline, (b) NaDFOB-NaBr, (c) NaDFOB, and (d) NaBr.

Supplementary Fig. 8. Temperature-dependent ionic conductivities of the electrolytes.

Supplementary Fig. 9. Na+ diffusion coefficients (DNa+) in the cathode calculated from GITT plots during charge and discharge: (a) Baseline, (b) NaDFOB-NaBr, (c) NaDFOB, and (d) NaBr.

Supplementary Fig. 10. CE of Na plating/stripping measured in Na||Cu cells via the Aurbach method for (a) Baseline, (b) NaDFOB, and (c) NaBr.

Supplementary Fig. 11. Voltage curves of Na||Na symmetric cells cycled at 0.5 mA cm−2 and 0.5 mAh cm−2.

Supplementary Fig. 12. Rate capabilities of Na||Na symmetric cells with varying current densities from 0.1 to 2 mA cm−2 and back to 0.1 mA cm−2.

Supplementary Fig. 13. Representative solvation structure snapshots of different electrolytes obtained from MD simulations.

Supplementary Fig. 14. CV curves of Na||NMLTO cells with different electrolytes.

Supplementary Fig. 15. Cycling performance of Na||NMLTO cells with different electrolytes at 1 C.

Supplementary Fig. 16. Initial charge/discharge curves of Na||NMLTO cells at 1 C.

Supplementary Fig. 17. Statistical comparison of the capacity retention after 500 cycles for Na||NMLTO cells with different electrolytes at 1 C (presented as mean ± standard deviation).

Supplementary Fig. 18. Statistical comparison of the capacity retention after 500 cycles for Na||NMLTO cells with different electrolytes at 5 C (presented as mean ± standard deviation).

Supplementary Fig. 19. Statistical comparison of the capacity retention after 500 cycles for Na||NMLTO cells with different electrolytes at 5 C and 60 °C (presented as mean ± standard deviation).

Supplementary Fig. 20. Rate capability of Na||NMLTO cell with NaDFOB-NaBr electrolyte at 60 ℃.

Supplementary Fig. 21. Initial charge/discharge curves of Na||NMLTO cells at 0.1 C and −30 ℃.

Supplementary Fig. 22. Cycling performance of Na||NVP cells with different electrolytes at 1 C.

Supplementary Fig. 23. Cycling performance of HC||NMLTO cell with NaDFOB-NaBr electrolyte at 2 C.

Supplementary Fig. 24. SEM image of pristine Na metal surface.

Supplementary Fig. 25. SEM images of Na metal surface after cycling with different electrolytes: (a) Baseline, (b) NaDFOB-NaBr, (c) NaDFOB, and (d) NaBr.

Supplementary Fig. 26. Survey XPS spectra of the cycled Na metal surface.

Supplementary Fig. 27. Normalized XPS fitting results of the C 1s peak.

Supplementary Fig. 28. Normalized XPS fitting results of the O 1s peak.

Supplementary Fig. 29. Normalized XPS fitting results of the F 1s peak.

Supplementary Fig. 30. Normalized XPS fitting results of the P 2p peak.

Supplementary Fig. 31. Quantitative comparison of SEI chemical components derived from the deconvolution of XPS Na 1s spectra for the four electrolytes.

Supplementary Fig. 32. 3D reconstruction of selected secondary-ion fragments on the cycled HC anode in the NaDFOB-NaBr electrolyte (TOF-SIMS).

Supplementary Fig. 33. TOF-SIMS depth profiles of the cycled HC anode in the Baseline electrolyte.

Supplementary Fig. 34. 3D reconstruction of selected secondary-ion fragments on the cycled HC anode in the Baseline electrolyte (TOF-SIMS).

Supplementary Fig. 35. TOF-SIMS depth profiles of the cycled HC anode in the NaBr electrolyte.

Supplementary Fig. 36. 3D reconstruction of selected secondary-ion fragments on the cycled HC anode in the NaBr electrolyte (TOF-SIMS).

Supplementary Fig. 37. Ex situ XRD patterns of NMLTO cathode surface at different states of charge/discharge (SOC).

Supplementary Fig. 38. Survey XPS spectra of cycled NMLTO cathode surface.

Supplementary Table 1. Compositions of the four electrolytes.

| Electrolyte | NaClO4 | EC | DMC | FEC | TMP | NaDFOB | NaBr |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Baseline | 1 M | 1 | 1 | 5 vol% | - | - | - |
| TMP-based (i) | - | - | - | - | 1 | 0.1 M | - |
| TMP-based (ii) | - | - | - | - | 1 | - | 0.01 M |
| TMP-based (iii) | - | - | - | - | 1 | 0.1 M | 0.01 M |

Supplementary Table 2. Physicochemical properties of the solvents used in the Baseline, NaDFOB-NaBr, NaDFOB, and NaBr electrolytes.

| Solvent structure | Melting Point Tm (°C) | Boiling Point Tb (°C) | Viscosity η (cP) | Dielectric Constant ε (25 °C) | Density ρ (g cm−3) | Donor Number DN (kcal mol−1) |
| --- | --- | --- | --- | --- | --- | --- |
| EC | 36 | 248 | 1.90 (40 °C) | 89.8 | 1.321 | 16.4 |
| DMC | 4 | 90 | 0.59 | 3.1 | 1.069 | 17.2 |
| FEC | 18 | 212 | - | 7.0 | 1.454 | 9.1 |
| TMP | −46 | 197 | 1.1 | 20.6 | 1.215 | 23 |

Supplementary Table 3. Fitted parameters from the EIS spectra of Na||Na symmetric cells at various temperatures.

| Electrolyte | Temperaure (°C) | Rb (Ω) | RSEI (Ω) | Rct (Ω) |
| --- | --- | --- | --- | --- |
| Baseline | 20 | 1.931 | 575.2 | 1246 |
|  | 0 | 3.108 | 3474 | 4799 |
|  | −10 | 4.58 | 8246 | 71210 |
|  | −20 | 6.421 | 45880 | 252200 |
| NaDFOB-NaBr | 20 | 2.162 | 4936 | 1799 |
|  | 0 | 3.037 | 7164 | 2729 |
|  | −10 | 2.948 | 6880 | 5487 |
|  | −20 | 3.618 | 51070 | 15110 |
| NaDFOB | 20 | 9.084 | 4516 | 1735 |
|  | 0 | 2.971 | 5770 | 8410 |
|  | −10 | 3.299 | 5972 | 27410 |
|  | −20 | 3.787 | 24910 | 85130 |
| NaBr | 20 | 5.038 | 1733 | 4241 |
|  | 0 | 2.682 | 3700 | 8705 |
|  | −10 | 3.282 | 31810 | 18160 |
|  | −20 | 3.71 | 38800 | 59800 |

Supplementary Table 4. Coordination numbers of Na+ with solvent molecules and anions in different electrolytes derived from MD simulations.

|  | Baseline | NaDFOB-NaBr | NaDFOB | NaBr |
| --- | --- | --- | --- | --- |
| ClO4− | 0.63472 | 0.49635 | 0.50011 | 0.58452 |
| DMC | 0.21733 | 0.19705 | 0.169 | 0.18689 |
| EC | 1.6655 | 1.27741 | 1.22297 | 1.37047 |
| FEC | 0.00594 | 0.00773 | 0.00382 | 0.00499 |
| TMP | - | 0.91413 | 0.91106 | 0.87793 |
| DFOB− | - | 0.03656 | 0.02526 | - |
| Br− | - | 0.02246 | - | 0.02514 |