A novel Ni-doped γ-Al2O3 catalyst for low-temperature CO2 methanation aided by frustrated Lewis pairs and spinel interlayers

Hubdar Ali Maitlo, Ki-Hyun Kim *

Department of Civil and Environmental Engineering, Hanyang University, 222 Wangsimni-ro, Seongdong-Gu, Seoul, 04763, Republic of Korea

*Corresponding Author: kkim61@hanyang.ac.kr

Supplementary Information (SI)

Table S1. The physicochemical properties of the prepared catalysts.

| Order | Catalysts | BETSA | Pv | Pd | Crystallite size (Dn = nm) |  | Element contents (wt.%) |  |  | Crystallographic structures |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | (m2 g-1) | (cm3 g-1) | (nm) | γ-Al2O3(440) | Ni0(111) | Al | O | Ni | d-pacing (nm) | Lattice fringe (hkl) |
| 1 | Al2O3 | 116.1 | 0.19 | 4.66 | 5.9 | 0 | 49.86 | 50.14 | - | 0.14 | γ-Al2O3(440) |
| 2 | A0N20 | 101.4 | 0.15 | 3.98 | 5.2 | 3.0 | 39.96 | 38.96 | 21.07 | 0.14 | γ-Al2O3(440) |
|  |  |  |  |  |  |  |  |  |  | 0.201 | Ni0(111) |
| 3 | A50N20 | 104.8 | 0.15 | 4.41 | 4.9 | 2.6 | 39.11 | 38.34 | 22.56 | 0.14 | γ-Al2O3(440) |
|  |  |  |  |  |  |  |  |  |  | 0.176 | Ni0(200) |
|  |  |  |  |  |  |  |  |  |  | 0.207 | Ni0(111) |

Table S2. XPS-derived surface chemical states of prepared catalysts.

| S. No | Sample | OV/(OL + OV) | OH*/(OL + OH*) | Ni0/(Ni0 + Ni2+) |
| --- | --- | --- | --- | --- |
|  |  | (%) | (%) | (%) |
| 1 | A0N20 | 82.2 | 56.4 | 2.4 |
| 2 | A50N20 | 90.2 | 86.5 | 2.5 |