Supporting material

A Pre-Enrichment-Free Colorimetric Biosensor Based on Immunomagnetic Separation and G-Quadruplex DNAzyme Signal Amplification for Ultrasensitive Detection of Vibrio parahaemolyticus in Seafood

Figure S1. Structural analysis diagram.(a)ssDNA. (b) Hairpin. (c) Hybrid duplex formed by ssDNA and Hairpin.

| Name | Sequence |
| --- | --- |
| Apt | 5'-SH-TCTAAAAATGGGCAAAGAAACAGTGACTCGTTGAGATACT-3' |
| ssDNA | 5'-AAAAAAAAAAAAAAATTGGGAAACATCGACTC-3' |
| CatG4 | 5'-TGGGTAGGGCGGGTTGGGAAA-3' |
| Hairpin | 5'-TGGGTAGGGCGGGTTGGGAAATTGGAGTGTGAGTCGATGTTTCCCAA-3' |

Table. S1 The DNA sequences used in this work.

Figure S2. Particle size distribution diagram: (a) Fe@Ag; (b) Fe@Ag - apt; (c) AuNPs; (d) AuNPs - IgY.

Figure S3. EDS map of element distribution of Fe3O4@Ag NPs.

Figure S4. Zeta potential measurements of Fe3O4@Ag NPs and Fe3O4@Ag NPs-apt.

Figure S5. Characterization results of Ultraviolet absorption spectrum.(a)AuNPs. (b) AuNPs-IgY.

Figure S6. TEM image of Fe3O4@Ag NPs-apt, AuNPs-IgY and V. parahaemolyticus

Figure S7. Photos of the plate count of V. parahemolyticus with different dosages of Fe3O4@Ag NPs-apt. (From left to right, they are positive control, 10 μL, 20 μL, 30 μL, 40 μL, 50 μL).

Figure S8. Photographs of the plate count of V. parahemolyticus with different enrichment time. (From left to right, they are positive control, 15 min, 30 min, 45 min, 60 min, 75 min).

Figure S9. Photographs of the plate count of capturing different concentrations of V. parahemolyticus.(From left to right, they are positive control, 1.0×108 CFU/mL、 1.0×107 CFU/mL、1.0×106 CFU/mL、1.0×105 CFU/mL、1.0×104 CFU/mL).

Figure S10. Optimization of pH for AuNPs solution.

Table S2. The comparison of the proposed method for the determination of V. parahaemolyticus with reported ones.

| No. | Methods | Samples | LOD | Detection range | References |
| --- | --- | --- | --- | --- | --- |
| 1 | Label-free colorimetric method | Shrimp | 6.1× 102 CFU/mL | - | (Chen et al., 2021) |
| 2 | Colorimetric immunoassay | Marine | 15 CFU/mL | 20 - 104 CFU/ml | (Liu et al., 2018) |
| 3 | Multichromatic colorimetric detection method | Pure culture | 1.12 CFU/mL | 0 - 104 CFU/ml | (Qiao et al., 2024) |
| 4 | One-step label-free colorimetric strategy | Shrimp | 103 CFU/mL | - | (Wang et al., 2023) |
| 5 | LF-NMR/colorimetric dual-mode homogeneous immunosensor | East Sea seawater and fish | 100 CFU/mL | 103 - 108 CFU/mL | (Zhang et al., 2024) |
| 6 | Colorimetric aptasensor | Water | 10 CFU/mL | 10 - 106 CFU/mL | (Wu et al., 2015) |
| 7 | Colorimetric-integrated PCR | Pure culture | 2.9×104 CFU/mL | 2.2×105 - 3.4 ×105 CFU/mL | (Cheng et al., 2016) |
| 8 | Colorimetric immunoassay | Pure culture | 10 CFU/mL | 10 - 106 CFU/mL | (Fu et al., 2018) |
| 9 | G-quadruplex-induced colorimetric method | Pure culture /Oyster | 3.02 CFU/mL /54.95 CFU/mL | 10 - 107 CFU/mL | This study |

References

Chen X, Wang L, He F, Chen G, Bai L, He K, Zhang F, Xu X (2021). Label-Free Colorimetric Method for Detection of Vibrio parahaemolyticus by Trimming the G-Quadruplex DNAzyme with CRISPR/Cas12a. Anal Chem [J], 93: 14300-14306.https://doi.org/10.1021/acs.analchem.1c03468

Liu P, Han L, Wang F, Li X, Petrenko V A, Liu A (2018b). Sensitive colorimetric immunoassay of Vibrio parahaemolyticus based on specific nonapeptide probe screening from a phage display library conjugated with MnO(2) nanosheets with peroxidase-like activity. Nanoscale [J], 10: 2825-2833.https://doi.org/10.1039/c7nr06633c

Qiao W, Wang L, Yang K, Liu Y, Liu Q, Yin F (2024). A multichromatic colorimetric detection method for Vibrio parahaemolyticus based on Fe(3)O(4)-Zn-Mn nanoenzyme and dual substrates. Microbiol Spectr [J], 12: e0318923.https://doi.org/10.1128/spectrum.03189-23

Wang P, Yu G, Wei J, Liao X, Zhang Y, Ren Y, Zhang C, Wang Y, Zhang D, Wang J, Wang Y (2023). A single thiolated-phage displayed nanobody-based biosensor for label-free detection of foodborne pathogen. J Hazard Mater [J], 443: 130157.https://doi.org/10.1016/j.jhazmat.2022.130157

Zhang D, Chen L, Lin H, Hao T, Wu Y, Xie J, Shi X, Jiang X, Guo Z (2024). Well plate-based LF-NMR/colorimetric dual-mode homogeneous immunosensor for Vibrio parahaemolyticus detection. Food Chem [J], 436: 137757.https://doi.org/10.1016/j.foodchem.2023.137757

Wu S, Wang Y, Duan N, Ma H, Wang Z (2015). Colorimetric Aptasensor Based on Enzyme for the Detection of Vibrio parahemolyticus. J Agric Food Chem [J], 63: 7849-7854.https://doi.org/10.1021/acs.jafc.5b03224

Cheng K, Pan D, Teng J, Yao L, Ye Y, Xue F, Xia F, Chen W (2016). Colorimetric Integrated PCR Protocol for Rapid Detection of Vibrio parahaemolyticus. Sensors (Basel) [J], 16.https://doi.org/10.3390/s16101600

Fu K, Zheng Y, Li J, Liu Y, Pang B, Song X, Xu K, Wang J, Zhao C (2018). Colorimetric Immunoassay for Rapid Detection of Vibrio parahemolyticus Based on Mn(2+) Mediates the Assembly of Gold Nanoparticles. J Agric Food Chem [J], 66: 9516-9521.https://doi.org/10.1021/acs.jafc.8b02494