## Slide 1
Green-Synthesized Orange Peel-CeO₂ Nanoparticles (OP-CeO₂-Nps) for Ciprofloxacin Photodegradation and Antibacterial Activity
01. Green Synthesis
Orange Peel Powder
Extract + Ce(NO₃)₃·6H₂O
60°C Water Bath → 120°C Drying → 300°C Calcination
OP-CeO₂-Nps Irregular Porous (Biogenic)
CeO₂-Nps Spherical (Direct Calcination)
02. Characterization
XRD / Raman Confirmed cubic fluorite crystal phase with high crystallinity
XPS Analysis Mixed valence (Ce³⁺/Ce⁴⁺) enhances redox reactions
Band Structure Eg = 3.14 eV, ECB = -0.50 eV Suitable for photocatalysis
03. Photocatalytic Degradation
Ciprofloxacin (CIP) Initial Conc. 20 mg/L Visible Light Irradiation
Degradation Efficiency 95.46%(within 120 min)
Active Species Ranking ·O₂⁻ > h⁺ > ·OH
04. Antibacterial Activity
Tested Strains:E. coli, S. aureus, B. subtilis
SignificantInhibition Zonesobserved for all pathogens
Conclusion: OP-CeO₂-Nps is a green, efficient, and bifunctional photocatalyst for sustainable antibiotic wastewater treatment.(Highly effective for CIP removal + Broad-spectrum antibacterial properties)