Supporting Information

Mechanistic Insight into CdS/TiO2 Heterojunctions for Efficient Photocatalytic Degradation of Diesel Oil Contaminants

Chi Huey Ng,1,2* Muhammad Alifaiman Matusin,1 Siow Hwa Teo,3# Fui San Lee,3 Zhenhua Xu,4 Putao Zhang,5 Yoshito Ando,6 Collin G. Joseph,3  Jidon Janaun,1 Rosalam Hj Sarbatly1,2

1Faculty of Engineering, Universiti Malaysia Sabah, Jalan UMS, Kota Kinabalu, 88400, Sabah, Malaysia.

2Membrane and Nanomaterials Technology Research Laboratory, Faculty of Engineering, Universiti Malaysia Sabah, Jalan UMS, Kota Kinabalu, 88400, Sabah, Malaysia.

3Sonophotochemistry Research Group, Faculty of Science and Technology, Universiti Malaysia Sabah, Kota Kinabalu, 88400, Sabah, Malaysia.

4School of Materials Science and Engineering, Ningbo Tech University, Ningbo 315100, China.

5Henan Key Laboratory of Quantum Materials and Quantum Energy, Henan University, Kaifeng, 475004, Henan, China.

6Department of Biological Functions and Engineering, Graduate School of Life Science and Systems Engineering, Kyushu Institute of Technology, 2-4 Hibikino Wakamatsu-ku, Fukuoka, Kitakyushu, 808-0196, Japan.

Corresponding authors:

*CH Ng: chihueyng@ums.edu.my

#SH Teo: tony@ums.edu.my

Figure S1. (a) EIS and (b) Mott-Schottky of Ti3C1 and Ti600, and (c) XRD profile of Ti3C1 before and after photodegradtion of diesel.

Table S1. Diesel composition in freshwater before and after 6h photodegradation extracted from GC-analysis.

| Parameter | Before | After | Observation |
| --- | --- | --- | --- |
| Diethyl Phthalate | 9.37% | 0.31% | 97.19% degraded |
| Siloxanes (Octasiloxane, Cyclooctasiloxane, etc.) | Present | Completely removed | Successful degradation |
| Heavy Hydrocarbons (C10-C19 alkanes) | Present | Reduced or transformed | Breakdown of diesel components |
| New Simpler Hydrocarbons (Decane, Heptane, Tetradecane, Nonadecane, etc.) | Not present | Formed | Indicates degradation of heavier hydrocarbons |
| Oxidation Products (Hexadecanoic acid methyl ester, 8-Octadecenoic acid methyl ester) | Not present | Present | Partial oxidation occurred |
| Total Hydrocarbons & Siloxanes | 11.67% | 0.31% | 97.74% degraded |